# Method

1.    Weigh crucible

2.    Add sample (about half full) and weigh

3.    Dry crucible + sample in oven (preferably 105 oC overnight)

4.    Cool crucible & reweigh

5.    Place crucible onto the furnace tray and put tray into furnace at 550 oC - leave for at least 4 hours

6.    Extract furnace tray when cool and reweigh crucible + ash

7.  Place crucible onto the furnace tray and put tray into furnace at 950 oC - leave for at least 4 hours

8. Extract furnace tray when cool and reweigh crucible + ash