
Float glass slumped over refractory plaster moulds


	oC/hr
	Temperature oC
	Soak Time
	Bungs

	75
	600
	2hrs
	Open

	50
	700
	-
	Closed

	AFAP
	820
	40 mins
	Closed

	AFAP
	560
	40 mins
	Closed

	20
	520
	-
	Closed

	40
	480
	-
	Closed

	100
	100
	-
	Closed
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Float glass slumped over fibre paper and whiting (aka chalk)

	oC/hr
	Temperature oC
	Soak Time
	Bungs

	75
	520
	15
	Closed

	150
	820
	30 mins
	Closed

	AFAP
	560
	30 mins
	Closed

	20
	520
	-
	Closed

	40
	480
	-
	Closed

	100
	100
	-
	Closed



