# ABAQUS Finite Element Analysis (FEA) Simulations on the Effectiveness of Various Constructions of Steel Armour

# Zoe Cummins

Contents

Table of Figures	2

Table of Tables	3

Abstract	4

Introduction	4

FEA Theory	4

Governing FEA Equations	4

ABAQUS	4

Johnson Cook and Damage Formulas	4

Control Measures	5

Assumptions	5

Methodology	5

Stress-Strain of 1040	6

Metallurgy	7

Results	7

Penetration Resistance at 500m/s	7

Penetration Resistance at 300m/s	9

Final Velocity of Projectile	10

Momentum	11

Kinetic Energy	11

Evaluation	12

Conclusions	13

Future Work	13

Appendices	15

Appendix 1 – Material Data	15

References	16

# Table of Figures

Figure 1, The Stress-Strain Graph of 1040	6

Figure 2, The Elastic Region of 1040	6

Figure 3, Copper Projectile at 500m/s General Trend (1 of 3)	7

Figure 4, Copper Projectile at 500m/s General Trend (2 of 3)	8

Figure 5, Copper Projectile at 500m/s General Trend (3 of 3)	8

Figure 6, The Last 125 Data Points of the Copper Projectile at 500m/s with the Lowest Final Velocities	9

Figure 7, Copper Projectile at 300m/s General Trend	9

Figure 8, The Last 125 Data Points of the Copper Projectile at 300m/s	10

Figure 9, Momentum of the Projectile at 500m/s	11

Figure 10, Kinetic Energy of the Projectile at 500m/s	11

Figure 11, Cost of Steel in US $	13

Figure 12, Finding the Equation of the Graph for 1040Alt4340	14

# Table of Tables

Table 1, Laminated Layers in Order and their names referenced in this report	5

Table 2, Metallurgy of Carbon Steels and their Morphology	7

Table 3, Final Velocity	10

Table 4, Raw Material Data	15

# Abstract

Using the Finite Element Analysis (FEA) simulation software ABAQUS, multiple configurations of steel laminated armour are simulated to investigate the penetrative resistance of the armour against a monolithic copper projectile. It was found that lamination produces a stronger restive effect and that the order of the lamination layers can increase or decrease the resistance to ballistic impact.

# Introduction

Armoured steel is used to provide protection to military and non-military vehicles. High strength steels are often considered as they have a high strength and high energy absorbing capabilities [1].

This paper investigates the penetration resistance of different configurations of steel laminated armour upon ballistic impact of a monolithic projectile in a high-speed impact test and a lower velocity impact test.

The report includes simulation and testing of multiple laminated steel armours in different configurations and conclusions drawn on the success of the design.

## FEA Theory

Finite Element Analysis (FEA) is a technique used in simulation software that approximates solutions of field problems that is within the area of interest that represents a real-life problem [2]. Forces at nodes are calculated, the more nodes that are calculated, the more detailed the simulation. However, the more calculations that need to be done the more time is needed for the simulation to run and it becomes resource heavy in terms of the (Computer Processing Unit) CPU and GPU (Graphics Processing Unit), and time to complete. The simulations were conducted manually, which is interactive processing. Batch processing reduces the human resources required but was not utilised as it requires a script that wasn’t provided for the simulations to run.

### Governing FEA Equations

Primarily FEA uses Matrices to solve linear or nonlinear algebraic equations

KU={F}

“…where u and f are the displacements and externally applied forces at the nodal points. The formation of the K matrix is dependent on the type of problem being attacked” [3].

## ABAQUS

ABAQUS is a nonlinear FEA simulation software created by Dassault systems with the aim to reduce the number of physical experiments by simulating outcomes that can be analysed.

### Johnson Cook and Damage Formulas

The Johnson-Cooks model is a type of Mises plasticity model that considers the hardening law and rate dependence. It has five constants: A, B, C n and m which are characteristics of the material [4]. It is suitable model for most metals [5] [6] and can be used for deformations with a strain rate of 103 s−1 and above [4].

The Johnson-Cooks failure model is only suitable for high strain deformation of metals [5]. It has five constants: d1, d2, d3, d4 and d5.

Combined these models provide a good basis for the ABAQUS computer simulations.

## Control Measures

The control measures are outlined as below

- A basic simulation where all parts were created and meshed

- Copper parameters – See Appendix 1 Material Data

- Layer thickness

- Initial velocity of 500m/s

- Total simulation time of 1.7E-04

### Assumptions

Due to the lack of readily available data, some assumptions were made

- Reference strain rate of 1000 (s-1)

- Transition temperature of 1200 (°C)

- The layers of lamination are of even thickness

# Methodology

Copper monolithic are readily available and are fired at a velocity of 457m/s [7]. Therefore, I will be testing these projectiles at 500m/s and at a lower velocity of 300m/s. The copper projectile’s displacement at failure is set to 1E-05.

Three different types of steel alloys from the American Iron and Steel Institute (AISI) will be tested: AISI 1045, AISI 4140 and AISI 4340 in a variety of configurations. The simulation has 5 layers to the lamination as described in the table below

| Laminated Layers Order and their Names |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Name | Layer | Material |  | Name | Layer | Material |  | Name | Layer | Material |
| 1045 | 1 | 1040 |  | 1045Alt4140 | 1 | 1040 |  | 4140Alt4340 | 1 | 4140 |
|  | 2 | 1040 |  |  | 2 | 4140 |  |  | 2 | 4340 |
|  | 3 | 1040 |  |  | 3 | 1040 |  |  | 3 | 4140 |
|  | 4 | 1040 |  |  | 4 | 4140 |  |  | 4 | 4340 |
|  | 5 | 1040 |  |  | 5 | 1040 |  |  | 5 | 4140 |
| 4140 | 1 | 4140 |  | 1045Alt4340 | 1 | 1040 |  | 4340Alt1045 | 1 | 4340 |
|  | 2 | 4140 |  |  | 2 | 4340 |  |  | 2 | 1040 |
|  | 3 | 4140 |  |  | 3 | 1040 |  |  | 3 | 4340 |
|  | 4 | 4140 |  |  | 4 | 4340 |  |  | 4 | 1040 |
|  | 5 | 4140 |  |  | 5 | 1040 |  |  | 5 | 4340 |
| 4340 | 1 | 4340 |  | 4140Alt1045 | 1 | 4140 |  | 4340Alt4140 | 1 | 4340 |
|  | 2 | 4340 |  |  | 2 | 1040 |  |  | 2 | 4140 |
|  | 3 | 4340 |  |  | 3 | 4140 |  |  | 3 | 4340 |
|  | 4 | 4340 |  |  | 4 | 1040 |  |  | 4 | 4140 |
|  | 5 | 4340 |  |  | 5 | 4140 |  |  | 5 | 4340 |

Table 1, Laminated Layers in Order and their names referenced in this report

The investigations look at whether lamination improves the effectiveness of steel armour.

It will also look at if lamination order matters.

### Stress-Strain of 1040

The graph shows the Elastic Region. The Yield Strength is approximately 1E8 and the ultimate strength is shown to be approximately 1.5E8. Fracture is assumed to be beyond the time frame that was tested.

Figure 1, The Stress-Strain Graph of 1040

Figure 2, The Elastic Region of 1040

Figure 2 shows the elastic region of 1040. From here it is calculated that Youngs Modulus to be 2E11. R2 is the statical measure that shows the proportional variance of 0.8289.

### Metallurgy

The table outlines the differences between the three steel alloy types that are being tested.

| Metallurgy of Carbon Steels |  |  |  |
| --- | --- | --- | --- |
| Element | Content (%) |  |  |
|  | AISI 1040 [8] | AISI 4140 [9] | AISI 4340 [10] |
| Iron, Fe | Remainder | Remainder | 95.195 - 96.33 |
| Carbon, C | 0.43-0.50 | 0.380 - 0.430 | 0.370 - 0.430 |
| Manganese, Mn | 0.60-0.90 | 0.75 - 1.0 | 0.600 - 0.800 |
| Sulfur, S | <0.05 | 0.040 | 0.0400 |
| Phosphorous, P | <0.04 | 0.035 | 0.0350 |
| Chromium, Cr | - | 0.80 - 1.10 | 0.700 - 0.900 |
| Silicone, Si | - | 0.15 - 0.30 | 0.150 - 0.300 |
| Molybdenum, Mo | - | 0.15 - 0.25 | 0.200 - 0.300 |
| Nickle, Ni | - | - | 1.65 - 2.00 |

Table 2, Metallurgy of Carbon Steels and their Morphology

# Results

## Penetration Resistance at 500m/s

Figure 3, Copper Projectile at 500m/s General Trend (1 of 3)

Figure 4, Copper Projectile at 500m/s General Trend (2 of 3)

Figure 5, Copper Projectile at 500m/s General Trend (3 of 3)

To increase the resolution of the graph, the last 125 data points were taken and replotted.

Figure 6, The Last 125 Data Points of the Copper Projectile at 500m/s with the Lowest Final Velocities

## Penetration Resistance at 300m/s

1040Alt4140, 1040Alt4340 and 4340Alt1040 had the lowest final velocities at 500m/s. Therefore, only these 3 armour plates were tested at 300m/s.

Figure 7, Copper Projectile at 300m/s General Trend

To increase the resolution of the graph, the last 125 data points were taken and replotted.

Figure 8, The Last 125 Data Points of the Copper Projectile at 300m/s

## Final Velocity of Projectile

The final velocity data point of the projectile as it passes through the armour as well as the average velocity from the last 125 data points is recorded in the table below.

| Final Velocity of Projectile |  |  |
| --- | --- | --- |
| Material Name | Final Recorded Velocity (m/s) | Average Final Velocity (m/s) |
| 1040 | 132.136 | 131.136 |
| 1040Alt4140 | 131.626 | 136.757 |
| 1040Alt4340 | 128.015 | 129.722 |
| 4140 | 180.456 | 199.725 |
| 4140Alt1040 | 137.237 | 155.952 |
| 4140Alt4340 | 173.840 | 189.032 |
| 4340 | 135.004 | 145.831 |
| 4340Alt1040 | 128.330 | 133.123 |
| 4340Alt4140 | 141.036 | 151.042 |

Table 3, Final Velocity

1040Alt4340 has the lowest average final velocity.

## Momentum

The initial momentum for the projectile travelling at 500m/s is 40kgm/s. The table below outlines the theoretical final momentum of the projectile as it passes through the material.

| Momentum of the Projectile at 500m/s |  |  |
| --- | --- | --- |
| Material Name | Mass (kg) | Momentum (kgm/s) |
| 1040 | 0.08 | 10.49088 |
| 1040Alt4140 | 0.08 | 10.94056 |
| 1040Alt4340 | 0.08 | 10.37776 |
| 4140 | 0.08 | 15.978 |
| 4140Alt1040 | 0.08 | 12.47616 |
| 4140Alt4340 | 0.08 | 15.12256 |
| 4340 | 0.08 | 11.66648 |
| 4340Alt1040 | 0.08 | 10.64984 |
| 4340Alt4140 | 0.08 | 12.08336 |

Figure 9, Momentum of the Projectile at 500m/s

## Kinetic Energy

The initial kinetic energy of the projectile travelling at 500m/s is 10000J.

| Kinetic Energy of the Projectile at 500m/s |  |  |
| --- | --- | --- |
| Material Name | Mass (kg) | Kinetic Energy (J) |
| 1040 | 0.08 | 687.866 |
| 1040Alt4140 | 0.08 | 748.0991 |
| 1040Alt4340 | 0.08 | 673.1119 |
| 4140 | 0.08 | 1595.603 |
| 4140Alt1040 | 0.08 | 972.8411 |
| 4140Alt4340 | 0.08 | 1429.324 |
| 4340 | 0.08 | 850.6672. |
| 4340Alt1040 | 0.08 | 708.8693. |
| 4340Alt4140 | 0.08 | 912.5474. |

Figure 10, Kinetic Energy of the Projectile at 500m/s

# Evaluation

The governing FEA equations as mentioned are nonlinear.  Nonlinear relates both material and geometric nonlinearity whereas in linear analysis the stress remains in the linear elastic range of the material. This means that the nonlinear is more representative of real-life problems where upon ballistic impact, the armour reaches the plastic stage and deformation stages.

The velocity was measured from centrally, at the trailing edge of the projectile. For simplicity, the displacement at failure for the copper projectile was set at 1E-05. The contact algorithm was at default where the outer nodes of the projectile were to meet the armour. No contact algorithm was set for the inner nodes. As a result, figures 3, 4 and 5 show a lot of noise. This occurs because as outer nodes meet the armour, they are compressed until they become small enough to be deleted by the algorithm. The nodes behind subsequently expand to fill the gap. This is shown in the fluctuations in the graph, where it suggests that the projectile gains velocity. All the steel armour tested in this setup, did not prevent penetration of the bullet at 500m/s or 300 m/s.

As the armour did not prevent the penetration of the projectile and due to the fluctuations in figures 3,4 and 5, further analysis will look at the penetrative resistance. Results from the average final velocities will only be considered.

The results show that that the solid steel armour 1040 performed the best with the average final velocity of 131.136 m/s, followed by 4340 at 145.831m/s and then 4140 at 199.725 m/s. This would suggest that the material with the best penetrative resistance would be the combination for 1040 and 4340, and the average final velocity would fall between 131.136m/s and 145.831m/s.

1040Alt4340 did perform the best with an average final velocity of 129.722m/s. The laminated plating that contains 1040 seems to have increased the penetrative resistance compared to the other combinations. Unexpectedly, when 1040 was laminated with 4340 in the 1040Alt4340 configuration, it produced a lower average final velocity than when the two materials were tested independently. This suggests that lamination can produce a stronger penetrative resistance.

1040Alt4340 and 4340Alt1040 have slightly different configurations, where 1040Alt4340 first layer is 1040 and has 3 layers of 1040 and 2 layers of 4340. 4340Alt1040 starts with 4340 and has 3 layers of 4340 and 2 layers of 1040, both could be considered to have a 60/40 split. 1040Alt4340 has an average final velocity of 129.722 m/s whereas 4340Alt1040 has an average final velocity of 133.124 m/s, which is higher than its component parts. This suggests that lamination order does matter in terms of penetration resistance.

Similarly, 4140Alt4340 had an average final velocity 189.032m/s whereas 4340Alt4140 had an average final velocity of 151.042m/s. The order of the lamination has drastically changed the resistive penetrative resistance by 37.99m/s. This supports the idea that lamination order does matter in terms of penetration resistance.

4340 and 4140 are very similar in their makeup with similar quantities of additional elements, however the only real difference between the two is that 4340 contains Nickel at 1.65-2.00%. Nickel is ductile and malleable [11], the addition of the nickel has decreased the penetrative resistance of the alloy.

The mesh was set at coarse rather than fine. However more elements do not mean more accurate results. A mesh convergence should have been conducted prior to the core of the study to establish the number of elements required to run the simulations accurately and reliably.

Figure 2 shows a stress-strain graph of the solid armour plate of 1040. The Young Modulus was calculated to be 2E11, which is the figure that was inputted as shown in Appendix 1. This was to assess the reliability of the software. The simulation was deemed to be reliable in comparison to real world data.

The plate is 22.5x10-3 meters thick, with layers of 4.85 x10-3, 3.90 x10-3, 4.607 x10-3, 4.268 x10-3 and 4.875x10-3 thick, opposed to equal thickness layers throughout the armour laminated plating as was provided. To what extend that the results would be affected is unclear.

Cost of the armour plating should also be considered for real-life capabilities.

| Cost of Steel [12] |  |
| --- | --- |
| Material | US $/kg |
| AISI 1040 | 0.90-0.95 |
| AISI 4140 | 1.50-2.60 |
| AISI 4340 | 2.55 |

Figure 11, Cost of Steel in US $

AISI 1040 is the cheapest per kilo.

Several assumptions were made for the materials as the data was not readily available. These assumptions include reference strain rate, transition temperatures and the figures provided with the ABAQUS setup. To what extent the results are affected is unclear.

The validity of the sources used for the parameters of the materials need to be considered. There is a wide range of sources for some of the materials as there is not a centralised data for all the parameters required to run the simulation.  For example, the Johnson Cook damage formulas were not readily available for a wide range of materials, especially upon ballistic impact. Whereas: density, melting temperatures and Young Modulus are dependent on the metallurgy of the steel which will be different from supplier to supplier.

Above all, the validity of the simulations cannot truly be stated until testing of ballistic impact is undertaken for the materials to gauge the reliability of the sources.

# Conclusions

The two main conclusions drawn

- Lamination order does matter

- Lamination can provide a greater penetration resistance than its component parts

## Future Work

- Explore the assumptions made for real values, like the transition temperatures reference strain rate for materials used

- Investigate why composite armours are used in armour laminate by investigating the differences in performance between composite armour types and steel armour types

- Compare at which point the projectile has a velocity of 0m/s, to the predictions stated below.

The results can be interpolated that the depth of the plate where the velocity 0m/s is 0.0450358m.

The steel armour tested did not prevent the penetration of the armour, however we can predict the depth of the armour that would be required by finding the gradient of the velocity-time graph.

Figure 12, Finding the Equation of the Graph for 1040Alt4340

The equation of the graph is y=-3E06 + 540.43. Where y=0, x= 1.8014333E-4.

Where u=500m/s, v=0m/s and t = 1.8014333E-4s.

s=u+v2t

s=displacement m,  u=initial velocityms,  v=final velocityms,  t=time(s)

The displacement, or the depth of the steel armour can be calculated to be 0.0450358m.

# Appendices

## Appendix 1 – Material Data

| Material Data Used in ABAQUS |  |  |  |  |
| --- | --- | --- | --- | --- |
| Parameters | Materials |  |  |  |
|  | AISI 1045 | AISI 4140 | AISI 4340 | Copper |
| Density (g/cm3) | 7870 [13] | 7850 [12] | 7850 [12] | 8770 [14] |
| Youngs Modulus (N/m2) | 2e11 [15] | 2e11 [15] | 2e11 [15] | - |
| Poisson Ratio | 0.27 [13] | 0.27 [9] | 0.3 [10] | - |
| A (Pa) | 50103000 [16] | 59500000 [17] | 79200000 [18] | - |
| B (Pa) | 17609100 [16] | 58000000 [17] | 51000000 [18] | - |
| n | 0.5176 [16] | 0.133 [17] | 0.26 [18] | - |
| m | 0.5655 [16] | 1.03 [17] | 1.03 [18] | - |
| Melting Temperature (°C) | 1520 [13] | 1416 [9] | 1416 [19] | 1085 [14] |
| Reference Strain Rate (s-1) | 1000* | 1000* | 1000* | 1000 [14] |
| d1 | 0.025 [16] | 1.5 [17] | 0.05 [20] | 0.54 [14] |
| d2 | 16.93 [16] | 3.44 [17] | 3.44 [20] | 4.89 [14] |
| d3 | -14.8 [16] | -2.12 [17] | -2.12 [20] | -3.03 [14] |
| d4 | 0.0214 [16] | 0.002 [17] | 0.002 [20] | 0.014 [14] |
| d5 | 0 [16] | 0.1 [17] | 0.61 [20] | 1.12 [14] |
| Transition Temperature (°C) | 1200* | 1200* | 1200* | 800 [14] |
| Shear Stress | - | - | - | 43e9 [14] |
| c0 | - | - | - | 3933 [14] |
| S | - | - | - | 1.489 [14] |
| Gammer0 | - | - | - | 2.02 [14] |

Table 4, Raw Material Data

*Assumed values

# References

| [1] | K. S. K. V. R. K. A. S. T. B. B. P.K. Jena, “Studies on the role of microstructure on performance of a,” Engineering failure Analysis, vol. 15, pp. 1088-1096, 2008. |
| --- | --- |
| [2] | U. o. V. -E. a. C. Science, “Introduction to Finite Element Analysis (FEA) or Finite Element Method (FEM),” University of Victoria -Engineering and Computer Science , Victoria. |
| [3] | D. Roylance, “Finite Element Analysis,” Department of Materials Science and Engineering Massachusetts Institute of Technology, Cambridge, 2001. |
| [4] | J. J. Michał GRĄZKA, Identification of Johnson-Cook Equation Constants, Warszawa: Polish Academy of Sciences • Institute of Fundamental Technological Research (IPPT PAN) National Engineering School of Metz (ENIM), 12. |
| [5] | “Johnson-Cook plasticity,” ABAQUS, [Online]. Available: https://abaqus-docs.mit.edu/2017/English/SIMACAEMATRefMap/simamat-c-johnsoncook.htm. [Accessed 18 03 22]. |
| [6] | W. H. C. Gordon R. Johnson, “Fracture characteristics of three metals subjected to various strains, strain rates, temperatures and pressures,” Elsevier BV, Netherlands, 1985. |
| [7] | Virtus Precision Ltd, “Virtus Precision Products,” Virtus Precision Ltd, [Online]. Available: https://www.virtusprecision.co.uk/products/. [Accessed 28 03 22]. |
| [8] | “AISI 1045 Carbon Steel (UNS G10450),” 13 06 13. [Online]. Available: https://www.azom.com/article.aspx?ArticleID=9153. [Accessed 20 03 22]. |
| [9] | “AISI 4140 Alloy Steel (UNS G41400),” 13 09 12. [Online]. Available: https://www.theenzone.com/_rc/_valves/AISI-4140-Alloy-Steel-(UNS-G41400).pdf. [Accessed 18 03 22]. |
| [10] | “AISI 4340 Alloy Steel (UNS G43400),” 13 09 12. [Online]. Available: https://www.azom.com/article.aspx?ArticleID=6772. [Accessed 18 03 22]. |
| [11] | A. M. Helmenstine, “Nickel Element Facts and Properties,” ThoughtsCo., 19 07 19. [Online]. Available: https://www.thoughtco.com/nickel-facts-606565. [Accessed 28 03 22]. |
| [12] | D. G. R. William D. Callister Jr, Materials Science and Engineering, Hoboken: John Wiley & Sons (Asia) Pte Ltd, 2015. |
| [13] | H.-E. S. J.-H. K. Tsung-Pin Hung, “Temperature Modeling of AISI 1045 Steel during Surface Hardening Processes,” Materials, pp. 1814-1835, 2018. |
| [14] | K. Donne, Interviewee, Given Values. [Interview]. 18 03 22. |
| [15] | “What Is Young's Modulus Of Steel?,” Steel On Call, 13 05 20. [Online]. Available: https://steeloncall.com/what-is-young-s-modulus-of-steel#:~:text=Young's%20modulus%20of%20steel%20at,underneath%20as%20far%20as%20possible.. [Accessed 18 03 22]. |
| [16] | D. W. J. Mohanraj Murugesan, “Johnson Cook Material and Failure Model Parameters Estimation of AISI-1045 Medium Carbon Steel for Metal Forming Applications,” Materials, pp. 608-626, 2019. |
| [17] | K. R. a. S. Kumar, “Numerical simulation of two tool turning process,” in The 4th International Conference on Engineering, Applied Sciences and Technology (ICEAST 2018) “Exploring Innovative Solutions for Smart Society”, 2018. |
| [18] | D. O. ,. A. O. ,. H. W. Gbadebo Owolabi, “Occurrence of Dynamic Shear Bands in AISI 4340 Steel under Impact Loads,” World Journal of Mechanics, pp. 139-145, 2013. |
| [19] | “Supply Range of AISI 4340 Alloy Steel,” [Online]. Available: https://www.otaisteel.com/products/quenched-and-tempered-alloy-steels/4340-steel/. [Accessed 18 03 22]. |
| [20] | P.-H. C. A. H. e. a. Pedro Franco Navarro, “Shear localization in 4340 steel with different microstructure using thick wall cylinder method,” in AIP Conference Proceedings 1979, 070022 (2018), 1979. |
| [21] | S. H. I. J. M. K. M. F. A. M. L. A. Sohail Akram, “Numerical and experimental investigation of Johnson–Cook material models for aluminum (Al 6061-T6) alloy using orthogonal machining approach,” Advances in Mechanical Engineering, vol. 10, no. 9, pp. 1-14, 2018. |