Opaque Binder and Pigment Colour
Opaque binders give a pastel, often chalky, appearance when printed and work well on darker grounds.  They can be used with or without concentrated pigment colour.  Pigment binders are one of the simplest methods of screen printing and are usually used as a final process when combining with other printing methods. They are easily fixed by heat, reasonably light and colourfast and can be used across a wide range of fabrics and substrates to give interesting surface effects. The main disadvantages of pigment printing are a stiffer handle and a relatively poor resistance to rubbing.
You are strongly advised and encouraged to keep thorough notes for any colour combinations and recipes you develop over your course of study, alongside a small fabric swatch, to help you establish your own colour reference library.
Additional Note: Opaque Binder can be mixed with up to 40% of Bricoprint Binder SF20E (for example 60gms Opaque Binder and 40gms Bricoprint Binder SF20E) to reduce the opacity of the Opaque Binder. 
Recipe:
1. 1 - 5% grams of concentrated pigment colour.
2. 95 - 99% grams Opaque Binder.
Method:
1. Gather your concentrated pigment colour, Opaque Binder, mixing pot, and a spatula.
2. Measure out your concentrated pigment colour - remember that 1 gram of pigment will create a paler depth of shade compared to 5 grams.
3. Make up to 100 grams using Opaque Binder, stirring thoroughly. 
4. ALTERNATIVELY
5. Measure out 100gms of Opaque Binder
6. Add in up to 5gms of concentrated pigment colour, stirring until the colour is thoroughly mixed with the binder.
7. Print and dry.
8. Press at 150*C for 20 seconds on the heat transfer press to fix.
 ALTERNATIVELY - for larger work
9. Bake at 150*C for 5 mins in the baker to fix.
Wash:
1. Rinse in cold water.
2. Dry and press.


