Bricoprint Binder SF20E and Pigment Colour
Bricoprint binder is translucent which makes it more suitable for printing on lighter coloured grounds, because of the translucent nature of the binder it can also be used to overprint layers whilst building colours.  For example, a red overprinted with a yellow could create an orange.  Pigment binders are one of the simplest methods of screen printing and are usually used as a final process when combining with other printing methods. They are easily fixed by heat, reasonably light and colourfast and can be used across a wide range of fabrics and substrates to give interesting surface effects. The main disadvantages of pigment printing are a stiffer handle and a relatively poor resistance to rubbing.
You are strongly advised and encouraged to keep thorough notes for any colour combinations and recipes you develop over your course of study, alongside a small fabric swatch, to help you establish your own colour reference library.
Recipe:
1. 1 - 5% grams of concentrated pigment colour.
2. Make up to 100 grams with Bricoprint Binder SF20E.
Method:
1. Gather your concentrated pigment colour, Bricoprint Binder SF20E, mixing pot, and a spatula.
2. Measure out your concentrated pigment colour - remember that 1 gram of pigment will create a paler depth of shade compared to 5 grams
3. Make up to 100 grams using pre-bought Bricoprint Binder SF2OE, stirring thoroughly.
4. ALTERNATIVELY
5. Measure out 100gms of Bricoprint Binder SF20E.
6. Add in up to 5gms of concentrated pigment colour, stirring until the colour is thoroughly mixed with the binder.
7. Print and dry.
8. Press at 150*C for 20 seconds on the heat transfer press to fix.
 ALTERNATIVELY - for larger work
9. Bake at 150*C for 5 mins in the baker to fix.
Wash:
1. Rinse in cold water.
2. Dry and press.

