University of Wales Trinity Saint David

School of Engineering

Manufacturing Design & Technology

Design for Manufacture and Assembly

ACMA 5002

Kelly Jenkins

2510063

June 2026

Word Count: 5226

# Abstract

This report presents the design, analysis, and optimisation of an injection mould for a mobile phone housing intended for high-volume consumer electronics production. The study integrates key engineering methodologies including computer-aided design (CAD), polymer flow simulation, finite element analysis (FEA), cost modelling, and sustainability assessment to develop a robust, manufacturable, and cost-effective solution. The design process addresses the challenges associated with injection moulding complex, thin-walled geometries, such as warpage, sink marks, weld lines, and air traps, while ensuring high surface finish and dimensional accuracy.

An iterative design approach was adopted, beginning with a baseline geometry which was progressively refined through simulation and validation. Optimisation of wall thickness, gate placement, and cooling behaviour significantly improved flow uniformity and reduced defect formation. The final design demonstrated high fill confidence, controlled shrinkage (~1.2-1.5%), and acceptable warpage (~2 mm), confirming suitability for mass production. Material selection using Granta analysis identified PC-ABS as the optimal choice, balancing strength, impact resistance, surface quality, and sustainability potential.

Finite Element Analysis validated the structural integrity of the component, highlighting stress concentration in snap-fit regions while confirming overall functional performance. Thermal analysis further emphasised the influence of cooling on deformation and residual stress. Cost analysis demonstrated the economic viability of large-scale production, with considerations for tooling, labour, and outsourcing strategies.

Sustainability was incorporated through material recyclability, energy-efficient design, and waste reduction strategies. Overall, the project demonstrates a successful integration of design for manufacture principles, simulation driven optimisation, and engineering analysis to deliver a viable injection moulding solution for high-volume production, with clear opportunities identified for further refinement in cooling efficiency and structural durability.

Contents

Abstract	2

Figures List.	5

Tables List.	7

1	Introduction	i

2	Literature Review	ii

3	Customer Requirements	v

3.1	Client’s design criteria	v

3.2	Performance Attributes	v

3.3	QFD Application	vi

3.4	FMEA	ix

4	Design and Development	xi

4.1	CAD design for phone case and Technical drawing.	xi

4.2	Material Selection.	xiv

4.3	Rationale for material selection choice.	xxi

5	Simulation and Validation	xxii

5.1	Simulation of phone case.	xxii

5.1.1	Filling Analysis	xxii

5.1.2	Thermal Analysis	xxiv

5.1.3	Defect Analysis	xxvi

5.1.4	Structural results	xxviii

5.2	Finite Element Analysis	xxx

5.2.1	Static stress analysis	xxx

5.2.2	Thermal stress analysis	xxxi

5.2.3	Non-linear static stress analysis	xxxi

5.3	Validation of the robustness	xxxi

5.4	Dimensional accuracy	xxxii

6	Engineering Calculations	xxxiii

7	Cost Calculation Analysis	xxxvii

7.1	Material Costs.	xxxvii

7.2	Manufacturing Costs	xxxvii

7.3	Break even analysis	xli

8	Sustainability Considerations	xlii

8.1	Material Recyclability	xlii

8.2	Energy Efficiency	xliii

8.3	Waste Reduction	xliii

9	Discussion and Recommendations	xliv

9.1	Comparison with Customer Requirements	xliv

9.2	Design Trade-Offs	xlv

9.3	Recommendations and Future Work	xlvi

10	Conclusion	xlvii

11	Appendices	xlviii

11.1	Initial simulation analysis	xlviii

11.2	Second simulation analysis	lxii

11.3	Final simulation Analysis	lxxviii

11.4	Static stress full report	xcii

11.5	Thermal stress full report	civ

civ

11.6	Non-Linear static stress	cxiii

12	References	cxx

# Figures List.

Figure 1- Injection moulding machine (Conrad, 2023)	iii

Figure 2- QFD for phone case	vii

Figure 3- FMEA for phone case	ix

Figure 4- Kano Model (University of Cambridge, 2016)	xi

Figure 5- Left view (AutoDesk, 2024)	xii

Figure 6- Top view (AutoDesk, 2024)	xii

Figure 7- Back View (AutoDesk, 2024)	xiii

Figure 8- Front View (AutoDesk, 2024)	xiii

Figure 9- Right View (AutoDesk, 2024)	xiv

Figure 10- Bottom View (AutoDesk, 2024)	xiv

Figure 11- Technical Drawing of phone case. (AutoDesk, 2024)	xv

Figure 12- Input parameters for material selection on Granta	xvi

Figure 13- Tensile strength vs density (ANSYS, 2025a)	xvi

Figure 14- Hardness vs density (ANSYS, 2025a)	xvii

Figure 15- Young's modulus vs price (ANSYS, 2025a)	xvii

Figure 16- price vs tensile strength (ANSYS, 2025a)	xviii

Figure 17- Polymer extrusion vs polymer moulding energy (ANSYS, 2025a)	xviii

Figure 18- Young's modulus vs density (ANSYS, 2025a)	xix

Figure 19- elongation vs young's modulus	xix

Figure 20- density vs price (ANSYS, 2025a)	xx

Figure 21- price vs thermal expansion coefficient (ANSYS, 2025a)	xx

Figure 22- Maximum service temperature vs price (ANSYS, 2025a)	xxi

Figure 23- young's modulus vs tensile strength (ANSYS, 2025a)	xxi

Figure 24- S-N graph for polycarbonate (Juracka, Bujdos and Lehner, 2025)	xxii

Figure 25- Fill confidence simulation image (AutoDesk, 2024)	xxiii

Figure 26- Fill time simulation image (AutoDesk, 2024)	xxiv

Figure 27- Injection pressure simulation (AutoDesk, 2024)	xxv

Figure 28- Flow front temperature simulation (AutoDesk, 2024)	xxv

Figure 29- Average temperature at end of fill simulation (AutoDesk, 2024)	xxvi

Figure 30- Solidified plastic at ejection simulation (AutoDesk, 2024)	xxvi

Figure 31- Time to ejection temperature (AutoDesk, 2024)	xxvii

Figure 32- Weld lines simulation (AutoDesk, 2024)	xxvii

Figure 33- Air Traps simulation (AutoDesk, 2024)	xxviii

Figure 34- Sink marks simulation (AutoDesk, 2024)	xxix

Figure 35- Warpage simulation (AutoDesk, 2024)	xxix

Figure 36- Deflection simulation (AutoDesk, 2024)	xxx

Figure 37- Volumetric shrinkage simulation (AutoDesk, 2024)	xxx

Figure 38- Von Mises stress (AutoDesk, 2024)	xxxi

Figure 39- Average salaries of production workers and machine operators (Reshoring Institute, 2022)	xlii

Figure 40- Break-even point graph (Schmidt, 2023)	xliii

Figure 41- Plastic recycling categories (Everich, 2020)	xliv

Figure 42- Category 7 recycling details (Hall, 2023)	xliv

# Tables List.

Table 1- Table of key components in a cost model (Thom, 2025)	iv

Table 2- customer needs vs engineering metrics	v

Table 3- Table showing key performance attributes.	v

Table 4- UK vs Asia outsourcing costings (Li, 2024) (admin, 2024) (Mulan, 2026) (Hu, 2025)	xliii

# Introduction

The purpose of this technical report is to design, analyse, and optimise an injection mould for a mobile phone housing intended for high-volume production. The objective is to develop a manufacturable, cost-effective, and sustainable solution that satisfies stringent performance, quality, and industrial production requirements.

The study applies integrated product development methodologies, including CAD modelling, polymer flow simulation, finite element analysis (FEA), cost modelling, and sustainability assessment, to validate design performance and manufacturability.

Mobile phone housings require lightweight, thin-walled structures incorporating complex features such as snap-fits, mounting bosses, and tight tolerances. While injection moulding enables efficient high-volume production, it introduces challenges including warpage from uneven cooling, sink marks in thicker regions, weld lines at flow convergence zones, and air traps in enclosed geometries.

The primary engineering challenge is therefore to optimise geometry and process parameters to minimise defect formation while maintaining structural performance, dimensional accuracy, and production efficiency. This report addresses these challenges through simulation-driven design and validation.

# Literature Review

Design For Manufacture (DFM) is a design philosophy aimed at simplifying manufacturing processes, reducing cost, and improving product quality. Key DFM principles for injection moulding would include uniform wall thickness to prevent warpage and sink marks, draft angles to facilitate ejection, filleted corners to reduce stress concentration, minimised undercuts to avoid complex tooling and having features sized to standard tooling capabilities. From the article from design for manufacturing (DFM) to manufacturing for design (MFD) via hybrid manufacturing and smart factory: A review and perspective of paradigm shift the author describes DFM as the main paradigm for the last three decades and “is defined by the limitations of available manufacturing processes” (Chu et al., 2016) DFM is a critical tool to use while designing as “70% of part cost is determined during the early design stage” (Molcho, Cristal and Shpitalni, 2014)

Design for Assembly (DFA) focuses on how easily parts can be assembled. It encourages the use of fewer parts, easy alignment, and modular designs that reduce the time and effort required for assembly. (Willson and Willson, 2025) In mobile phone housings this could include snap-fit features replace screws and adhesives, symmetry to help reduce assembly orientation errors, self-locating features support automated assembly and integrated mounting bosses reduce secondary components. The combination of DFM and DFA significantly improves assembly throughput and reduces labour costs.

Injection Moulding is a widely used manufacturing process for plastics, it can produce large quantities with high consistency. “Injection moulding works by forcing molten plastic into a metal mould, where it cools into shape and is then ejected. Before production starts, the mould is CNC-machined from aluminium or steel, then polished or textured depending on the surface finish you need. Once installed, production follows a repeatable four-step cycle: Clamping: The two mould halves are clamped together under high pressure. Injection: Molten plastic pellets are injected into the closed mould cavity through a nozzle. Cooling: The plastic cools and solidifies inside the mould. Cooling time directly affects cycle time and part quality. Ejection: Ejector pins push the finished part out, the mould closes, and the cycle repeats. Cycle times range from seconds to a couple of minutes, depending on part size, wall thickness, and material.” (ProtoLabs, 2023)

Figure 1- Injection moulding machine (Conrad, 2023)

Finite Elemental Analysis (FEA) validates structural integrity under mechanical and thermal loads. FEA “is the process of predicting an object’s behaviour based on calculations made with the finite element method (FEM). While FEM is a mathematical technique, FEA is the interpretation of the results FEM provides. FEA gives engineers insights into complex systems and structures, helping them make more informed design decisions.”  (ANSYS, 2025)

Quality Function Deployment (QFD) translates customer requirements into engineering specifications. “QFD is a powerful tool to support product definition and aims to link customer requirements to technical or engineering characteristics. The tool provides a conceptual map for communication across functions and provides a focus for design priorities.” (IfM, 2016)

Failure modes and effects analysis (FMEA) evaluates risk and prioritises defect mitigation. FMEA “… is a systematic, step-by-step approach to identify and prioritize possible failures in a design, manufacturing or assembly process, product, or service. It is a common risk analysis tool. The goal of this proactive tool is to mitigate or eliminate potential failures.” (ASQ, 2019)

Design of Experiments (DOE) optimises design variables statistically. DOE allows for the systematic exploration and optimisation of the factors influencing processes. “By testing and analysing multiple variables, our DOE approach uncovers critical insights, enhancing process control, product consistency, and operational efficiency.” (EnerTherm-Engineering, 2024)

In terms of sustainability, manufacturing has a large energy consumption and carbon footprint associated with its practices. In order to address this problem, the concept of sustainable manufacturing is being implemented by many companies along with this “…material selection plays a very important role in the sustainability of plastics. Some materials are more energy intensive to produce than others. Also, what happens to the material at the end of its use-life is very important to consider. Nowadays, for any particular application, a vast selection of materials is available. Hence, the careful selection of materials is crucial to achieve a process that is environmentally, socially and economically benign.” (Vassallo, Rochman and Refalo, 2020)

Another significant part of the project is cost modelling. “A comprehensive cost model is built from several core components, including cost drivers, cost elements, input parameters, and calculation logic; additionally, context-specific adjustments are vital for accurate prediction. These components collectively provide flexibility and support robust decision-making, with each element playing a distinct and necessary role in the model’s overall function.” (Thom, 2025)

Table 1- Table of key components in a cost model (Thom, 2025)

# Customer Requirements

## Client’s design criteria

The client’s design criteria has four defined points manufacturability, defect mitigation, material/ cost efficiency and sustainability. Manufacturability is defined as the design must be suitable for high volume production. Defect Mitigation states that the mould design must minimise defects such as warping, air pockets and stress concentrations. Material and cost efficiency, the client wants the design to balance material performance with cost effectiveness and demonstrate clear cost analysis. For sustainability the client wants recyclable materials and energy-efficient processes to be prioritised. Table 2 below shows the customer needs against possible engineering metrics to achieve these.

Table 2- customer needs vs engineering metrics

## Performance Attributes

Table 3 below shows the performance attributes for this part. These have been compiled using the client design criteria along with general expectations for the suitability of the mobile phone housing.

Table 3- Table showing key performance attributes.

## QFD Application

The Quality Function Deployment (QFD) presented in figure 2 below translates key customer requirements (the what) for a mobile phone housing into measurable engineering characteristics (the how) to guide the injection mould design. The matrix integrates performance, manufacturability, cost, and sustainability considerations, ensuring that the final design aligns with both user expectations and production efficiency.

Quality characteristics that were included in the QFD were wall thickness uniformity, normal wall thickness (mm), material density, impact strength, gate type, gate location, cooling channel efficiency, cycle time, snap-fit geometry robustness and recycled material content. These reflected a balance between the functional performance (strength, durability), aesthetic quality (surface finish), manufacturing efficiency (cost, defects) and the sustainability targets of the product.

These were placed against demand qualities such as lightweight housing, high impact resistance, minimal warpage, high surface finish, accurate internal mounting, fast assemble via snap fits, low defect rate, low unit cost, recyclable material and low environmental impact. While these parameters will directly control the injection moulding behaviour, structural performance and production cost and efficiency of the product.

Figure 2- QFD for phone case

The QFD relationship matrix identifies the primary design drivers governing the performance and manufacturability of the mobile phone case. The strongest relationships are associated with wall thickness uniformity, cooling channel efficiency, and gate design (location and type), as these directly influence critical customer requirements such as minimal warpage, high surface quality, and reduced defect rates. Wall thickness uniformity is essential for controlling shrinkage and maintaining dimensional accuracy, while cooling efficiency ensures uniform thermal distribution, reducing both warpage and cycle time. Gate design plays a key role in material flow behaviour, affecting the formation of defects such as weld lines and air traps. Collectively, these parameters form the foundation of an effective injection moulding process and require careful optimisation.

Based on their influence, the design requirements can be categorised into critical, major, and secondary factors. Critical factors include cooling efficiency, wall thickness uniformity, gate location, and cycle time, as these have the greatest impact on both product quality and production efficiency. Major factors include nominal wall thickness, snap-fit robustness, impact strength, and gate type, which are essential for mechanical performance but involve trade-offs. For example, increasing wall thickness improves strength but also increases cooling time and warpage risk, while snap-fit features must balance flexibility and durability. These aspects require iterative optimisation and structural validation using FEA.

Secondary factors include material density and recycled content, which mainly influence sustainability and weight rather than manufacturability. While important, their impact on defects and process performance is comparatively lower and constrained by mechanical requirements.

The QFD also highlights key engineering trade-offs. Increasing wall thickness improves strength but extends cycle time, while enhanced cooling systems reduce defects but increase tooling complexity and cost. Additionally, higher recycled material content may reduce environmental impact but can compromise mechanical performance.

Overall, the QFD demonstrates that successful design depends primarily on controlling thermal and flow-related parameters, with cooling design, wall thickness consistency, and gate configuration emerging as the most critical drivers. Prioritising these factors through simulation and optimisation enables a balanced outcome in terms of performance, cost, and sustainability for high-volume production.

## FMEA

The Failure Mode and Effects Analysis (FMEA) conducted for the injection moulding process of the mobile phone case below in figure 3 provides a systematic evaluation of potential process risks, their causes, and their impact on product quality and manufacturability. The analysis identifies key failure modes across different stages of the process, including material flow, cooling, moulding, and assembly, and quantifies their risk using Severity, Occurrence, and Detection ratings to generate a Risk Priority Number. This structured approach ensures that the most critical risks are identified and prioritised for corrective action.

Figure 3- FMEA for phone case

The FMEA identifies warpage, snap-fit failure, and sink marks as the highest-risk failure modes, driven primarily by non-uniform cooling, geometric inconsistencies, and material accumulation. These risks were mitigated through design optimisation, including improved cooling, wall thickness control, and refined gate placement, resulting in significantly reduced RPN values and improved process robustness.

Overall, the FMEA demonstrates that key risks are strongly linked to thermal behaviour, geometric consistency, and material flow characteristics. Addressing these through targeted design and process improvements enables high-quality, defect-free production, supporting high-volume manufacturing. The analysis complements the QFD, providing a cohesive framework for design optimisation, risk reduction, and process efficiency. Utilising all the findings from these will assist in value attract and quality, ensuring we keep loyal customers are per Kano’s Model which visualises product characteristics and stimulating debate within the design team, seen below in figure 4.

Figure 4- Kano Model (University of Cambridge, 2016)

# Design and Development

## CAD design for phone case and Technical drawing.

A wall thickness range of 2.1 mm to 2.5 mm is recommended, as it improves flow behaviour, reduces defect formation, enhances packing efficiency, and minimises warpage, resulting in a more robust and manufacturable design. The CAD design has 2.1mm wall thickness, fillets and edge radii were incorporated to reduce stress concentrations, improve material flow during injection moulding, and enhance both structural durability and dimensional stability of the component.

Figure 5- Left view (AutoDesk, 2024)

Figure 6- Top view (AutoDesk, 2024)

Figure 7- Back View (AutoDesk, 2024)

Figure 8- Front View (AutoDesk, 2024)

Figure 9- Right View (AutoDesk, 2024)

Figure 10- Bottom View (AutoDesk, 2024)

Figure 11- Technical Drawing of phone case. (AutoDesk, 2024)

## Material Selection.

Based on the material selection analysis, PC-ABS was identified as the optimal material, providing a balanced combination of mechanical performance, manufacturability, and sustainability. The material offers high impact resistance, ensuring durability under service conditions, while maintaining sufficient stiffness for thin-walled structures.

PC-ABS also provides good dimensional stability, reducing susceptibility to shrinkage-induced warpage during cooling, and exhibits favourable processing characteristics, enabling consistent flow and surface quality in injection moulding. In addition, the potential for recycled content supports environmental objectives without significantly compromising performance.

Overall, PC-ABS meets the functional, aesthetic, and manufacturing requirements of high-volume consumer electronics production more effectively than alternative materials.

Figure 12- Input parameters for material selection on Granta

Figure 13- Tensile strength vs density (ANSYS, 2025a)

Figure 14- Hardness vs density (ANSYS, 2025a)

Figure 15- Young's modulus vs price (ANSYS, 2025a)

Figure 16- price vs tensile strength (ANSYS, 2025a)

Figure 17- Polymer extrusion vs polymer moulding energy (ANSYS, 2025a)

Figure 18- Young's modulus vs density (ANSYS, 2025a)

Figure 19- elongation vs young's modulus

Figure 20- density vs price (ANSYS, 2025a)

Figure 21- price vs thermal expansion coefficient (ANSYS, 2025a)

Figure 22- Maximum service temperature vs price (ANSYS, 2025a)

Figure 23- young's modulus vs tensile strength (ANSYS, 2025a)

Figure 24- S-N graph for polycarbonate (Juracka, Bujdos and Lehner, 2025)

## Rationale for material selection choice.

Based on this assessment, a PC-ABS blend was selected as the most suitable material for the mobile phone housing. This material offers a combination of high impact resistance, ensuring durability under drop conditions, and an excellent surface finish, meeting aesthetic requirements for consumer electronics. In addition, PC-ABS exhibits good dimensional stability, reducing the risk of warpage during cooling, and supports the incorporation of recycled content (up to approximately 30%), contributing to sustainability targets. Its widespread use in consumer electronics further validates its suitability for high-volume injection moulding applications.

# Simulation and Validation

## Simulation of phone case.

Initial simulation results (appendices 11.1 and 11.2) identified limitations in flow uniformity, temperature distribution, and defect formation, primarily due to suboptimal gate placement and non-uniform wall thickness. These factors resulted in increased shrinkage variation, warpage, and a higher risk of weld lines and air traps.

Targeted design modifications, including optimised gate positioning, improved wall thickness consistency, and enhanced consideration of thermal behaviour, resulted in significantly improved performance. The final simulation (appendices 11.3) demonstrates uniform flow distribution, reduced defect concentration, and improved thermal consistency, confirming that the iterative design process effectively enhanced manufacturability, structural stability, and overall product quality.

### Filling Analysis

Figure 25- Fill confidence simulation image (AutoDesk, 2024)

The fill confidence results show a high level of confidence across the majority of the component, with only minor low-confidence areas in thinner or complex regions. This represents a clear improvement compared to the initial simulations, where larger low-confidence zones were present. The improved prediction confirms that the component is now highly manufacturable, with a low risk of defects during production.

Figure 26- Fill time simulation image (AutoDesk, 2024)

The filling results indicate a uniform and continuous flow front progression throughout the component, demonstrating that the revised gate placement has successfully balanced material distribution. There are no evidence of incomplete filling or hesitation zones, confirming that the melt is able to reach all regions efficiently. This improved flow behaviour reduces the likelihood of short shots and ensures consistent part formation, validating the gate design strategy.

Figure 27- Injection pressure simulation (AutoDesk, 2024)

The injection pressure distribution remains within acceptable limits, indicating that the melt flow is not restricted by the geometry. Pressure is evenly distributed from the gate through to the extremities of the part, confirming that the design supports efficient filling without excessive machine load. This aligns well with the calculated pressure (~200 MPa), demonstrating consistency between analytical and simulation results.

### Thermal Analysis

Figure 28- Flow front temperature simulation (AutoDesk, 2024)

Figure 29- Average temperature at end of fill simulation (AutoDesk, 2024)

The temperature results show a relatively uniform melt temperature throughout the filling process, with only slight cooling at the flow front edges. This improved thermal consistency reduces the formation of premature solidification, which was more evident in earlier simulations. The controlled temperature profile minimises defects such as weld lines and ensures better surface finish quality.

Figure 30- Solidified plastic at ejection simulation (AutoDesk, 2024)

Figure 31- Time to ejection temperature (AutoDesk, 2024)

The simulation predicts a cooling time of approximately 38- 40 seconds, confirming that cooling remains the dominant phase of the cycle. The thermal distribution indicates more uniform heat dissipation compared to earlier simulations, although minor hot spots are still present near thicker regions. While the cooling performance is acceptable, it highlights an opportunity for further optimisation to reduce cycle time and improve production efficiency.

### Defect Analysis

Figure 32- Weld lines simulation (AutoDesk, 2024)

Weld lines are present but are fewer and more controlled than in previous simulations. They occur primarily in areas where multiple flow fronts meet, which is expected in multi-directional filling. The reduced number and improved distribution of weld lines suggest enhanced flow uniformity and reduced risk to structural integrity.

Figure 33- Air Traps simulation (AutoDesk, 2024)

Air trap formation is limited to small, predictable regions at the end of flow paths. These are significantly reduced compared to earlier simulations and are located in areas where venting can be easily incorporated into the mould design. This indicates improved flow front convergence and reduced entrapment of gases.

Figure 34- Sink marks simulation (AutoDesk, 2024)

The sink mark analysis shows minor surface depressions in thicker sections of the design. While these are still present, their severity is lower than in earlier simulations, indicating improved packing and cooling balance. These defects are cosmetic and can be further reduced through minor geometry optimisation, such as ribbing or thickness reduction.

### Structural results

Figure 35- Warpage simulation (AutoDesk, 2024)

Figure 36- Deflection simulation (AutoDesk, 2024)

The warpage results indicate a maximum deformation of approximately 2 mm, with deflection concentrated in unsupported or thinner regions. This represents a reduction in deformation compared to earlier iterations, demonstrating that improved flow and cooling balance have positively impacted structural stability. Although still within acceptable limits, these areas remain critical for further design refinement.

Figure 37- Volumetric shrinkage simulation (AutoDesk, 2024)

The shrinkage results show values in the range of approximately 1.2-1.5%, with higher shrinkage occurring in thicker sections of the component. Compared to earlier simulations, the shrinkage distribution is now more consistent across the part, reducing the risk of dimensional inaccuracies. This confirms that the design adjustments have improved packing efficiency and material behaviour during cooling.

## Finite Element Analysis

### Static stress analysis

Figure 38- Von Mises stress (AutoDesk, 2024)

As seen in appendices 11.4 the static stress analysis indicates that the component experiences localised stress concentrations at snap-fit features, sharp geometric transitions, and thin wall sections. Peak stress levels approach the material yield strength (54.4 MPa), highlighting these regions as critical with respect to structural integrity.

The stress distribution demonstrates typical polymer behaviour, with low stress in uniform regions and elevated stress at discontinuities, confirming the influence of geometric features on load transfer. Corresponding displacement results indicate that, while global deformation remains within acceptable limits, localised regions are highly stressed and susceptible to yielding.

These results correlate with analytical predictions, confirming that while the structure is globally robust, the snap-fit regions represent the primary structural limitation due to stress concentration.

### Thermal stress analysis

As can be seen in appendices 11.5 the thermal stress analysis demonstrates that non-uniform cooling generates residual stresses, particularly in thicker regions and at geometric discontinuities where heat dissipation is uneven. These residual stresses contribute directly to the warpage observed in the moulding simulation (~2 mm).

The results highlight the strong coupling between thermal behaviour and mechanical response, where residual stresses amplify deformation and reduce dimensional accuracy.

This confirms that effective thermal management, particularly through uniform wall thickness and optimised cooling design, is critical for achieving both structural stability and manufacturing quality.

### Non-linear static stress analysis

As seen in appendices 11.6 The nonlinear static analysis provides a more accurate representation of snap-fit behaviour by incorporating large deformation effects. Results show significant elastic deformation in the snap-fit regions, allowing stress redistribution compared to the linear model.

Despite this redistribution, stress levels remain high relative to the material yield strength, indicating a risk of plastic deformation or fatigue failure under repeated loading cycles.

This confirms that the design successfully achieves functional flexibility but highlights a critical trade-off between deformation capability and long-term durability, with the snap-fit geometry representing the primary constraint on performance.

## Validation of the robustness

The robustness of the component is validated through the integration of simulation, analytical calculations, and FEA. Injection moulding simulations confirm stable filling behaviour, controlled shrinkage (~1.2-1.5%), and acceptable warpage (~2 mm), indicating consistent manufacturability under varying process conditions.

FEA further demonstrates that, although localised stress concentrations occur at snap-fit features, global structural performance remains within functional limits. These high-stress regions are predictable and can be targeted for design optimisation.

The strong correlation between analytical predictions and simulation results confirms that component behaviour is well characterised and controlled. Overall, the design is considered robust for high-volume production, with minor refinement required in critical stress regions.

## Dimensional accuracy

Dimensional accuracy was validated through both analytical and simulation-based shrinkage assessments. The calculated shrinkage (~1.2%) closely aligns with simulation results (1.2-1.5%), confirming model accuracy.

Dimensional variation is generally uniform, with minor deviations in thicker regions due to localised cooling differences. Warpage remains limited to approximately 2 mm, ensuring overall geometric stability.

Design improvements, including uniform wall thickness and optimised gate placement, have reduced shrinkage variation and enhanced dimensional stability. The component therefore meets functional requirements while maintaining acceptable manufacturing tolerances.

# Engineering Calculations

The calculations confirm that the design meets lightweight and material efficiency requirements, shrinkage remains within acceptable limits, ensuring dimensional accuracy, injection pressure and clamping force are sufficient for defect-free moulding, cooling time is the dominant factor influencing cycle time and cost, snap-fit regions require optimisation due to high local stress and the heat transfer supports efficient cooling but can be improved further.

Overall, the analytical results strongly support the simulation and demonstrate a technically viable design, with clear areas identified for further optimisation.

# Cost Calculation Analysis

## Material Costs.

## Manufacturing Costs

Injection moulding cost efficiency is primarily driven by labour, machine utilisation, tooling, and material usage. Maximising production rate and minimising material waste are key to reducing unit cost. Strategic improvements can significantly enhance margins, including the use of multi-cavity tooling to increase output without proportional cost increases, greater automation to reduce labour dependency (for example lowering labour costs from around £190k to £120k or outsourcing to another country), and running operations 24/7 to maximise asset use and dilute fixed costs. In addition, optimising material usage remains the most effective lever for reducing variable costs and improving overall profitability.

Figure 39- Average salaries of production workers and machine operators (Reshoring Institute, 2022)

When mass-producing an ABS-Polycarbonate mobile phone case at a scale of 1 million units, outsourcing to Asia (such as China or Vietnam) cuts initial tooling expenses by 30% to 50% and reduces the per-part cost by up to 40%. However, when importing to the UK, you trade off these upfront financial savings against longer lead times, shipping freight complexities, and import duties. Below in table 4 you will see the trade-off for the differences for outsourcing.

Table 4- UK vs Asia outsourcing costings (Li, 2024) (admin, 2024) (Mulan, 2026) (Hu, 2025)

## Break even analysis

Break-Even Analysis used to calculate the break-even production volume to justify high-volume manufacturing.

Figure 40- Break-even point graph (Schmidt, 2023)

The break-even point of this product shown below has been calculated using the fixed and variable costs from above and the selling price of the product.

# Sustainability Considerations

## Material Recyclability

ABS- PC is a thermoplastic blend, meaning it can be, melted, reprocessed and remoulded into new parts although recycling typically happens in industrial mechanical recycling processes. Reusing ABS-PC reduces raw fossil resource use but also energy consumption compared to virgin materials. It is categorised in category 7- other materials.

Figure 41- Plastic recycling categories (Everich, 2020)

Figure 42- Category 7 recycling details (Hall, 2023)

There are other alternatives which offer easier recyclability but these did not meet the criteria of the design specification, ABS-PC provides the robustness required for the phone case while still offering the option of recycling.

## Energy Efficiency

Energy efficiency in the injection mould design is primarily achieved through optimisation of cooling, geometry, material selection and process parameters. Conformal cooling channels significantly improves heat removal and reduces temperature gradients, shorter cycle times and lower energy consumption per part. Additionally, maintaining a uniform wall thickness (~2.1 mm) minimises unnecessary material mass and reduces cooling time, further improving efficiency. The material selection of PC-ABS supports energy efficiency due to good flow characteristics and moderate processing temperatures, reducing both thermal and mechanical energy requirements. Process optimisation including controlled melt temperature and injection pressure, ensures efficient operation without excessive energy input. Furthermore, the use of durable tooling materials (P20 and H13 steel) maintains consistent thermal performance over long production cycles, reducing inefficiencies caused by tool wear. Overall, these design decisions reduce cycle time, minimise waste, and improve energy efficiency, making the process more cost-effective and environmentally sustainable. To further enhance energy efficiency the introduction of renewable energy sources could be a possibility.

## Waste Reduction

In this design waste reduction is achieved through optimised part geometry, efficient mould design and controlled processing. The housing incorporates a uniform wall thickness (~2.1 mm) and cored features, minimising excess material while maintaining structural strength. This reduces material usage, prevents defects and lowers the number of rejected parts. The mould design includes a balanced runner system ensuring consistent material flow and reducing defects such as air traps and incomplete filling. This improves part quality and minimises scrap production. Additionally, runner material can be reused through regrind, improving overall material utilisation. The use of recyclable PC-ABS material further supports waste reduction by allowing scrap material to be reprocessed without significant loss of performance.

# Discussion and Recommendations

## Comparison with Customer Requirements

The simulation and FEA results indicate that the design largely satisfies the key customer requirements of manufacturability, structural performance, and defect mitigation, although some limitations remain.

Dimensional accuracy is achieved within acceptable industrial tolerances, with predicted warpage of approximately 2.1 mm and deflection up to 1.8 mm. While these values are suitable for non-precision consumer components, they approach upper acceptable limits, indicating that further refinement of cooling uniformity would be beneficial. This suggests that the current design is functional but not fully optimised for dimensional stability.

Shrinkage behaviour is well controlled, with values in the range of 1.2–1.5%, demonstrating good agreement between analytical and simulation results. This confirms that the selected material and geometry provide predictable behaviour during cooling, supporting consistent assembly performance. However, localised deviations in thicker sections highlight the continued influence of geometry on thermal behaviour.

From a manufacturability perspective, the design performs well, with balanced flow behaviour and acceptable injection pressure distribution (~200 MPa). Defect formation, including weld lines, air traps, and sink marks, has been significantly reduced through design iteration. However, these defects are not fully eliminated and remain dependent on local flow conditions, indicating that further optimisation of gate placement and cooling design could improve part quality.

Overall, the design meets most customer requirements, but the results demonstrate that performance is achieved through design compromise rather than full optimisation, particularly in relation to thermal management and deformation control.

## Design Trade-Offs

The final design is governed by several key engineering trade-offs, which highlight the challenges of balancing performance, cost, and manufacturability.

The most significant trade-off exists between cooling time and production efficiency. A cooling time of approximately 38-40 seconds improves dimensional stability and reduces residual stress, but increases cycle time and limits production throughput. While this improves quality, it directly impacts cost per unit, indicating that further cooling optimisation, such as conformal cooling, could provide a more efficient solution.

Wall thickness presents a further compromise between structural performance and defect formation. Increasing thickness improves strength and stiffness, particularly in snap-fit regions, but leads to higher shrinkage and increased risk of sink marks. Conversely, thinner sections reduce material usage and cooling time but increase deformation and stress concentration. The selected thickness of approximately 2.1 mm represents a balanced solution, although localised optimisation may further improve performance.

Gate configuration also introduces competing requirements. Multiple gate locations improve flow balance and reduce warpage, but increase the occurrence of weld lines, which can negatively affect surface quality and structural integrity. This reflects a common trade-off in injection moulding, where flow control must be balanced against cosmetic and mechanical requirements.

Finally, cost and tooling complexity are closely linked. A simpler mould design reduces initial tooling cost and manufacturing complexity, but limits the implementation of advanced solutions such as conformal cooling channels. While the current design is cost-effective, it sacrifices some performance potential that could be realised through more advanced tooling.

These trade-offs demonstrate that the final design represents a compromise solution, where improvements in one area are often achieved at the expense of another, requiring careful engineering judgement.

## Recommendations and Future Work

Based on the analysis, several targeted improvements are recommended to further enhance performance and move the design closer to full optimisation.

Improving the cooling system represents the most significant opportunity. The introduction of conformal cooling channels would reduce thermal gradients, leading to lower residual stress, reduced warpage, and shorter cycle times. Although this would increase tooling cost, the improvement in production efficiency could justify the investment in high-volume manufacturing.

Geometric refinement is also recommended, particularly in regions of varying wall thickness. Introducing smoother transitions and reducing abrupt thickness changes would improve uniform cooling behaviour and reduce localised shrinkage and deformation. This would also contribute to improved stress distribution, particularly in critical areas such as snap-fit features.

Further optimisation of gate placement should be considered to minimise weld line formation and improve flow uniformity in visible regions. While software limitations restricted this in the current study, advanced simulation tools or experimental validation could enable more refined gate configurations.

To address sink marks, local thickness reduction or the introduction of rib structures is recommended. This approach maintains structural integrity while reducing material accumulation and improving cooling efficiency.

Material enhancement could also be explored through modified PC-ABS blends or fibre-reinforced variants, which would increase stiffness and reduce deformation. However, this must be balanced against potential impacts on cost, processability, and recyclability.

Finally, experimental validation is recommended to confirm simulation predictions, particularly for warpage, surface defects, and snap-fit performance. Physical testing would provide further confidence in the design and allow calibration of simulation models.

# Conclusion

The results demonstrate that the optimised PC-ABS design is suitable for high-volume injection moulding, achieving a balance between performance, manufacturability, cost efficiency, and sustainability.

Simulation and analytical validation confirm controlled shrinkage (~1.2-1.5%), acceptable warpage (~2 mm), and stable flow behaviour, indicating reliable production capability. While minor defects such as weld lines and sink marks remain, their distribution is controlled and predictable.

FEA highlights that structural performance is primarily limited by stress concentrations at snap-fit features, indicating the need for further optimisation to improve durability under repeated loading.

Overall, the project demonstrates effective application of simulation-driven design and engineering analysis, delivering a technically viable and scalable solution for large-scale production, with clear opportunities for further refinement in cooling efficiency and stress reduction.

# Appendices

## Initial simulation analysis

Study Report

| Analyzed File | Phone case v8 | Version | Autodesk Fusion (2703.1.11) |
| --- | --- | --- | --- |
| Creation Date | 2026-05-29, 15:52:15 | Study Name | Study 1 - Injection Molding Simulation |
| Author | Kelly Jenkins_2510063 |  |  |

Report Properties

| Report Properties |  |
| --- | --- |
| Title | Studies |
| Author | 2510063 |

Study Setup

| Target body |  |
| --- | --- |
| Name | Body1 |

| Materials |  |
| --- | --- |
| Family name | BLENDS (PC+PBT, PC+ABS, ...) |
| Trade name | Generic PC+ABS |
| Manufacturer | Generic Shrinkage Characterised Material |
| Material structure | Amorphous |
| Environmental properties |  |

| Injection locations |  |
| --- | --- |
| Number | 2 |

| Aesthetic faces |  |
| --- | --- |
| Number | 0 |

| Process settings |  |
| --- | --- |
| Injection time | Automatic |
| Melt temperature | 260.00 C |
| Mold surface temperature | 70.00 C |

Molding Process

Geometry

| Machine setup |  |
| --- | --- |
| Material trade name | Generic PC+ABS |
| Melt temperature | 260.00 C |
| Mold surface temperature | 70.00 C |
| Injection time | Automatic |

| Filling |  |
| --- | --- |
| Time to fill | 1.80 s |
| Pressure at switch over | 62.103 MPa |
| Velocity/pressure switch-over at % | 99.239 % |
| Velocity/pressure switch-over at time | 1.78 s |

| Packing & Cooling |  |
| --- | --- |
| Packing time | 5.13 s |
| Max packing pressure | 70.272 MPa |
| Total part weight | 0.03 kg |
| Cooling time | 10.94 s |

| Final part shape |  |
| --- | --- |
| Recommended mold shrinkage allowance | 0.587 % |
| Total out-of-plane deflection | 0.198 mm |

Guided Results

Fill

With these study settings, your part will fill completely with a Time to fill of 1.80 s

| Visual defects |  |
| --- | --- |
| 7 faces on your model will have sink marks and 22 faces will have weld lines. |  |
| Advice | To reduce the appearance of sink marks: - Reduce the thickness, or the radius, on the backside of features - Edit model - Move injection locations to thicker sections of the model - Edit injection location - View an alternate surface finish - Surface finish To alter the appearance of weld lines: - Move the injection location - Edit injection location - Modify the local thickness of the model - Edit model - Reduce the number of injection locations - Edit injection location |

| Warpage |  |
| --- | --- |
| The maximum deflection from the center of your part is 0.525 mm. The warpage exceeds the tolerance of 0.434 mm that you have set. |  |
| Advice | To reduce warpage: - Place injection locations to create a balanced fill pattern - Edit injection location - Make wall thicknesses more uniform - Edit model - Increase or decrease the melt temperature - Edit process settings - Increase or decrease the injection time - Edit process settings - Increase the wall thickness of the part - Edit model |

Results

Fill animation

Fill confidence

Quality prediction

Injection pressure

Flow-front temperature

Avg. temperature (end of fill)

Time to ejection temperature

Volumetric shrinkage (ejection)

Solidified plastic (end of fill)

Solidified plastic (ejection)

Air traps

Weld lines

Filled from injection location

Sink mark depth - Threshold

Sink mark depth - Estimate

Sink mark depth - Visualization

Deflection (all effects)

Warpage tolerance

## Second simulation analysis

Simulation 6

| Analyzed File | Phone case v10 | Version | Autodesk Fusion (2703.1.11) |
| --- | --- | --- | --- |
| Creation Date | 2026-06-02, 11:49:22 | Study Name | Study 1 - Injection Molding Simulation |
| Author | Kelly Jenkins_2510063 |  |  |

Report Properties

| Report Properties |  |
| --- | --- |
| Title | Studies |
| Author | 2510063 |

Study Setup

| Target body |  |
| --- | --- |
| Name | Body1 |

| Materials |  |
| --- | --- |
| Family name | BLENDS (PC+PBT, PC+ABS, ...) |
| Trade name | Generic PC+ABS |
| Manufacturer | Generic Shrinkage Characterised Material |
| Material structure | Amorphous |
| Environmental properties |  |

| Injection locations |  |
| --- | --- |
| Number | 3 |

| Aesthetic faces |  |
| --- | --- |
| Number | 0 |

| Process settings |  |
| --- | --- |
| Injection time | Automatic |
| Melt temperature | 240.00 C |
| Mold surface temperature | 60.00 C |

Molding Process

Geometry

| Machine setup |  |
| --- | --- |
| Material trade name | Generic PC+ABS |
| Melt temperature | 240.00 C |
| Mold surface temperature | 60.00 C |
| Injection time | Automatic |

| Filling |  |
| --- | --- |
| Time to fill | 1.15 s |
| Pressure at switch over | 48.55 MPa |
| Velocity/pressure switch-over at % | 99.602 % |
| Velocity/pressure switch-over at time | 1.14 s |

| Packing & Cooling |  |
| --- | --- |
| Packing time | 3.97 s |
| Max packing pressure | 60.776 MPa |
| Total part weight | 0.03 kg |
| Cooling time | 10.21 s |

| Final part shape |  |
| --- | --- |
| Recommended mold shrinkage allowance | 0.571 % |
| Total out-of-plane deflection | 0.039 mm |

Guided Results

| Fill |  |
| --- | --- |
| With these study settings, your part may be difficult to fill with a Time to fill of 1.15 s, or may have quality problems. |  |
| Advice | To increase the temperature at the flow front: - Decrease the injection time - Edit process settings - Move injection locations away from thin sections of the model - Edit injection location - Increase the thickness of thin model sections - Edit model |

| Visual defects |  |
| --- | --- |
| 5 faces on your model will have sink marks and 18 faces will have weld lines. |  |
| Advice | To reduce the appearance of sink marks: - Reduce the thickness, or the radius, on the backside of features - Edit model - Move injection locations to thicker sections of the model - Edit injection location - View an alternate surface finish - Surface finish To alter the appearance of weld lines: - Move the injection location - Edit injection location - Modify the local thickness of the model - Edit model - Reduce the number of injection locations - Edit injection location |

| Warpage |  |
| --- | --- |
| The maximum deflection from the center of your part is 0.50 mm. The warpage exceeds the tolerance of 0.411 mm that you have set. |  |
| Advice | To reduce warpage: - Place injection locations to create a balanced fill pattern - Edit injection location - Make wall thicknesses more uniform - Edit model - Increase or decrease the melt temperature - Edit process settings - Increase or decrease the injection time - Edit process settings - Increase the wall thickness of the part - Edit model |

Results

Fill animation

Fill confidence

Quality prediction

Injection pressure

Flow-front temperature

Avg. temperature (end of fill)

Time to ejection temperature

Volumetric shrinkage (ejection)

Solidified plastic (end of fill)

Solidified plastic (ejection)

Air traps

Weld lines

Filled from injection location

Sink mark depth - Threshold

Sink mark depth - Estimate

Sink mark depth - Visualization

Deflection (all effects)

Warpage tolerance

## Final simulation Analysis

Simulation 4- PC-ABS

| Analyzed File | Phone case v11 | Version | Autodesk Fusion (2703.1.11) |
| --- | --- | --- | --- |
| Creation Date | 2026-06-02, 14:03:48 | Study Name | Study 1 - Injection Molding Simulation |
| Author | Kelly Jenkins_2510063 |  |  |

Report Properties

| Report Properties |  |
| --- | --- |
| Title | Studies |
| Author | 2510063 |

Study Setup

| Target body |  |
| --- | --- |
| Name | Body1 |

| Materials |  |
| --- | --- |
| Family name | BLENDS (PC+PBT, PC+ABS, ...) |
| Trade name | Generic PC+ABS |
| Manufacturer | Generic Shrinkage Characterised Material |
| Material structure | Amorphous |
| Environmental properties |  |

| Injection locations |  |
| --- | --- |
| Number | 3 |

| Aesthetic faces |  |
| --- | --- |
| Number | 0 |

| Process settings |  |
| --- | --- |
| Injection time | Automatic |
| Melt temperature | 240.00 C |
| Mold surface temperature | 40.00 C |

Molding Process

Geometry

| Machine setup |  |
| --- | --- |
| Material trade name | Generic PC+ABS |
| Melt temperature | 240.00 C |
| Mold surface temperature | 40.00 C |
| Injection time | Automatic |

| Filling |  |
| --- | --- |
| Time to fill | 1.05 s |
| Pressure at switch over | 51.129 MPa |
| Velocity/pressure switch-over at % | 99.606 % |
| Velocity/pressure switch-over at time | 1.04 s |

| Packing & Cooling |  |
| --- | --- |
| Packing time | 3.59 s |
| Max packing pressure | 62.594 MPa |
| Total part weight | 0.03 kg |
| Cooling time | 7.40 s |

| Final part shape |  |
| --- | --- |
| Recommended mold shrinkage allowance | 0.559 % |
| Total out-of-plane deflection | 0.052 mm |

Guided Results

| Fill |  |
| --- | --- |
| With these study settings, your part may be difficult to fill with a Time to fill of 1.05 s, or may have quality problems. |  |
| Advice | To increase the temperature at the flow front: - Decrease the injection time - Edit process settings - Move injection locations away from thin sections of the model - Edit injection location - Increase the thickness of thin model sections - Edit model |

| Visual defects |  |
| --- | --- |
| 3 faces on your model will have sink marks and 19 faces will have weld lines. |  |
| Advice | To reduce the appearance of sink marks: - Reduce the thickness, or the radius, on the backside of features - Edit model - Move injection locations to thicker sections of the model - Edit injection location - View an alternate surface finish - Surface finish To alter the appearance of weld lines: - Move the injection location - Edit injection location - Modify the local thickness of the model - Edit model - Reduce the number of injection locations - Edit injection location |

| Warpage |  |
| --- | --- |
| The maximum deflection from the center of your part is 0.49 mm. The warpage exceeds the tolerance of 0.403 mm that you have set. |  |
| Advice | To reduce warpage: - Place injection locations to create a balanced fill pattern - Edit injection location - Make wall thicknesses more uniform - Edit model - Increase or decrease the melt temperature - Edit process settings - Increase or decrease the injection time - Edit process settings - Increase the wall thickness of the part - Edit model |

Results

Fill animation

Fill confidence

Quality prediction

Injection pressure

Flow-front temperature

Avg. temperature (end of fill)

Time to ejection temperature

Volumetric shrinkage (ejection)

Solidified plastic (end of fill)

Solidified plastic (ejection)

Air traps

Weld lines

Filled from injection location

Sink mark depth - Threshold

Sink mark depth - Estimate

Sink mark depth - Visualization

Deflection (all effects)

Warpage tolerance

## Static stress full report

Study Report

| Analyzed File | Phone case v12 | Version | Autodesk Fusion (2703.1.11) |
| --- | --- | --- | --- |
| Creation Date | 2026-06-04, 15:16:56 | Author | Kelly Jenkins_2510063 |

Report Properties

| Report Properties |  |
| --- | --- |
| Title | Studies |
| Author | 2510063 |

Simulation Model 1

Study 4 - Static Stress

Study Properties

| Study Properties |  |
| --- | --- |
| Study Type | Static Stress |
| Last Modification Date | 2026-06-04, 15:12:33 |

Study Setup

Settings

General

Mesh

Average Element Size (% of model size) - Solids; 10. Scale Mesh Size Per Part; No. Average Element Size (absolute value); -. Element Order; Parabolic. Create Curved Mesh Elements; Yes. Max. Turn Angle on Curves (Deg.); 60. Max. Adjacent Mesh Size Ratio; 1.5. Max. Aspect Ratio; 10. Minimum Element Size (% of average size); 20..

Adaptive Mesh Refinement

Number of Refinement Steps; 0. Results Convergence Tolerance (%); 20. Portion of Elements to Refine (%); 10. Results for Baseline Accuracy; von Mises Stress..

| Contact Tolerance | 0.10 mm |
| --- | --- |
| Remove Rigid Body Modes | No |

Materials

PC/ABS Plastic

Components

Component; Strength. Body1; Yield Strength..

Properties

Density; 1.100E-06 kg / mm^3. Young's Modulus; 2780.00 MPa. Poisson's Ratio; 0.40. Yield Strength; 54.40 MPa. Ultimate Tensile Strength; 54.40 MPa. Thermal Conductivity; 2.400E-04 W / (mm C). Thermal Expansion Coefficient; 6.700E-05 / C. Specific Heat; 2133.00 J / (kg C)..

| Contacts |  |  |  |  |
| --- | --- | --- | --- | --- |
| Contact Type | Contact Set | Penetration Type | Bodies | Entities |

| Mesh |  |
| --- | --- |
| Type | Solids |
| Nodes | 41587 |
| Elements | 23208 |

Load Case1

| Constraints |  |
| --- | --- |
| Fixed1 |  |
| Type | Fixed |
| Ux | Fixed |
| Uy | Fixed |
| Uz | Fixed |

| Loads |  |
| --- | --- |
| Force1 |  |
| Type | Force |
| X Value | 15.00 N |
| Y Value | 15.00 N |
| Z Value | 0.00 N |
| Force Per Entity | No |

Load Case1 - Guided Results

Safety Factor

With the analysis criteria in this study setup, the design is expected to bend permanently or break.

Next Steps; Below Safety Factor Target. Validate your study setup - Check the loads are not set too high - Check the mesh refinement and consider increasing it in areas of high stress - Confirm your Safety Factor requirement - If the Displacement result shows high displacement, consider running a Nonlinear study to gain more insight. Check other results - Examine the Below target Result visualization to see where the weakest areas are - Check the stress result to see if, and where, the material might yield - Check the displacement result to see how far from its original alignment the model has moved - Look at other results, such as reaction forces to check your study set up, or strain to check your material performance. Strengthen weak areas - Add more material to weak areas - Select a material with a higher yield strength - Stiffen the design - Modify the shape with a Generative Design study. Generate alternative designs - Add more material to weak areas - Select a material with a higher yield strength - Stiffen the design - Modify the shape with a Generative Design study. Above Safety Factor Limit. Validate your study setup - Check the loads are not set too high - Check the mesh refinement and consider increasing it in areas of high stress - Confirm your Safety Factor requirement - If the Displacement result shows high displacement, consider running a Nonlinear study to gain more insight. Check other results - Examine the Below target Result visualization to see where the weakest areas are - Check the stress result to see if, and where, the material might yield - Check the displacement result to see how far from its original alignment the model has moved - Look at other results, such as reaction forces to check your study set up, or strain to check your material performance. Lightweight the design - Set a Safety Factor upper limit to find where material can be removed - Remove material from areas that exceed the Safety Factor upper limit. Generate alternative designs - In the Generative Design workspace, create design modifications - Remove unnecessary material using a Shape Optimization study..

Load Case1 - Results

| Result Summary |  |  |  |
| --- | --- | --- | --- |
| Result type | Sub-result | Minimum | Maximum |
| Safety Factor; 122.219; 1.278E+11. Safety Factor |
| Stress |  |  |  |
| Von Mises; 4.257E-10 MPa; 0.445 MPa. 1st Principal; −0.114 MPa; 0.443 MPa. 3rd Principal; −0.235 MPa; 0.074 MPa. Normal XX; −0.209 MPa; 0.233 MPa. Normal YY; −0.14 MPa; 0.314 MPa. Normal ZZ; −0.14 MPa; 0.174 MPa. Shear XY; −0.084 MPa; 0.192 MPa. Shear YZ; −0.166 MPa; 0.032 MPa. Shear XZ; −0.18 MPa; 0.062 MPa.. |
| Displacement |  |  |  |
| Total; 0 mm; 1.225E-04 mm. X; −2.16E-05 mm; 7.157E-05 mm. Y; −3.852E-07 mm; 1.035E-04 mm. Z; −3.051E-05 mm; 3.648E-05 mm.. |
| Total; 0 N; 0.12 N. X; −0.117 N; 0.038 N. Y; −0.071 N; 0.025 N. Z; −0.074 N; 0.107 N. Reaction Force |
| Strain |  |  |  |
| Equivalent; 2.193E-13; 2.903E-04. 1st Principal; 1.768E-14; 2.62E-04. 3rd Principal; −2.401E-04; 1.045E-08. Normal XX; −5.525E-05; 4.779E-05. Normal YY; −2.896E-05; 7.329E-05. Normal ZZ; −3.207E-05; 2.366E-05. Shear XY; −8.433E-05; 1.934E-04. Shear YZ; −1.676E-04; 3.236E-05. Shear XZ; −1.81E-04; 6.233E-05.. |
| Contact Force |  |  |  |
| Total; 0 N; 0 N. X; 0 N; 0 N. Y; 0 N; 0 N. Z; 0 N; 0 N.. |

Safety Factor

Safety Factor

Stress

Von Mises

1st Principal

Displacement

Total

## Thermal stress full report

| Analyzed File | Phone case v13 | Version | Autodesk Fusion (2703.1.11) |
| --- | --- | --- | --- |
| Creation Date | 2026-06-04, 15:55:49 | Author | Kelly Jenkins_2510063 |

| Report Properties |  |
| --- | --- |
| Title | Studies |
| Author | 2510063 |

| Study Properties |  |
| --- | --- |
| Study Type | Thermal Stress |
| Last Modification Date | 2026-06-04, 15:44:39 |

Settings

General

Mesh

Average Element Size (% of model size) - Solids; 10. Scale Mesh Size Per Part; No. Average Element Size (absolute value); -. Element Order; Parabolic. Create Curved Mesh Elements; Yes. Max. Turn Angle on Curves (Deg.); 60. Max. Adjacent Mesh Size Ratio; 1.5. Max. Aspect Ratio; 10. Minimum Element Size (% of average size); 20..

Adaptive Mesh Refinement

Number of Refinement Steps; 0. Results Convergence Tolerance (%); 20. Portion of Elements to Refine (%); 10. Results for Baseline Accuracy; von Mises Stress..

| Contact Tolerance | 0.10 mm |
| --- | --- |
| Remove Rigid Body Modes | No |
| Reference Temperature | 20.00 C |

Materials

PC/ABS Plastic

Components

Component; Strength. Body1; Yield Strength..

Properties

Density; 1.100E-06 kg / mm^3. Young's Modulus; 2780.00 MPa. Poisson's Ratio; 0.40. Yield Strength; 54.40 MPa. Ultimate Tensile Strength; 54.40 MPa. Thermal Conductivity; 2.400E-04 W / (mm C). Thermal Expansion Coefficient; 6.700E-05 / C. Specific Heat; 2133.00 J / (kg C)..

| Contacts |  |  |  |  |
| --- | --- | --- | --- | --- |
| Contact Type | Contact Set | Penetration Type | Bodies | Entities |

| Mesh |  |
| --- | --- |
| Type | Solids |
| Nodes | 41587 |
| Elements | 23208 |

| Constraints |  |
| --- | --- |
| Fixed1 |  |
| Type | Fixed |
| Ux | Fixed |
| Uy | Fixed |
| Uz | Fixed |

| Loads |  |
| --- | --- |
| Applied Temperature1 |  |
| Type | Applied Temperature |
| Value | 240.00 C |
| Applied Temperature2 |  |
| Type | Applied Temperature |
| Value | 40.00 C |

| Result Summary |  |  |  |
| --- | --- | --- | --- |
| Result type | Sub-result | Minimum | Maximum |
| Safety Factor |  |  |  |
| Safety Factor; 0.645; 12.659.. |
| Stress |  |  |  |
| Von Mises; 4.298 MPa; 84.327 MPa. 1st Principal; −53.361 MPa; 208.933 MPa. 3rd Principal; −113.634 MPa; 131.024 MPa. Normal XX; −94.434 MPa; 202.391 MPa. Normal YY; −93.708 MPa; 137.138 MPa. Normal ZZ; −85.152 MPa; 131.452 MPa. Shear XY; −36.008 MPa; 34.345 MPa. Shear YZ; −30.843 MPa; 23.825 MPa. Shear XZ; −28.044 MPa; 27.254 MPa.. |
| Displacement |  |  |  |
| Total; 0 mm; 0.089 mm. X; −0.077 mm; 0.078 mm. Y; −0.069 mm; 0.06 mm. Z; −0.068 mm; 0.052 mm.. |
| Reaction Force |  |  |  |
| Strain |  |  |  |
| Equivalent; 0.002; 0.049. 1st Principal; 0.002; 0.047. 3rd Principal; −0.041; 0.009. Normal XX; −0.013; 0.036. Normal YY; −0.014; 0.035. Normal ZZ; −0.011; 0.031. Shear XY; −0.036; 0.035. Shear YZ; −0.031; 0.024. Shear XZ; −0.028; 0.027.. |
| Contact Force |  |  |  |
| Total; 0 N; 0 N. X; 0 N; 0 N. Y; 0 N; 0 N. Z; 0 N; 0 N.. |
| Temperature |  |  |  |
| Temperature; 40.00°C; 271.151°C.. |
| Total; 7.186E-06 W/mm²; 0.042 W/mm². X; −0.027 W/mm²; 0.039 W/mm². Y; −0.023 W/mm²; 0.034 W/mm². Z; −0.024 W/mm²; 0.028 W/mm². Heat Flux |
| Thermal Gradient |  |  |  |
| Total; 0.03 °C/mm; 176.449 °C/mm. X; −163.348 °C/mm; 112.483 °C/mm. Y; −140.399 °C/mm; 94.628 °C/mm. Z; −115.503 °C/mm; 101.054 °C/mm.. |

| Total | 0 N | 222.931 N |
| --- | --- | --- |
| X | −158.877 N | 142.414 N |
| Y | −92.793 N | 155.62 N |
| Z | −155.899 N | 197.202 N |

Safety Factor

Safety Factor

Stress

Von Mises

1st Principal

Displacement

Total

## Non-Linear static stress

| Analyzed File | Phone case v14 |
| --- | --- |
| Version | Autodesk Fusion (2703.1.11) |
| Creation Date | 2026-06-04, 16:21:35 |
| Author | Kelly Jenkins_2510063 |

Report Properties

| Title | Studies |
| --- | --- |
| Author | 2510063 |

Simulation Model 1

Study 6 - Nonlinear Static Stress

Study Properties

| Study Type | Nonlinear Static Stress |
| --- | --- |
| Last Modification Date | 2026-06-04, 16:17:07 |

Settings

General

| Contact Tolerance | 0.10 mm |
| --- | --- |
| Remove Rigid Body Modes | No |

Mesh

| Average Element Size (% of model size) |  |
| --- | --- |
| Solids | 10 |
| Scale Mesh Size Per Part | No |
| Average Element Size (absolute value) | - |
| Element Order | Parabolic |
| Create Curved Mesh Elements | Yes |
| Max. Turn Angle on Curves (Deg.) | 60 |
| Max. Adjacent Mesh Size Ratio | 1.5 |
| Max. Aspect Ratio | 10 |
| Minimum Element Size (% of average size) | 20 |

Adaptive Mesh Refinement

| Number of Refinement Steps | 0 |
| --- | --- |
| Results Convergence Tolerance (%) | 20 |

Materials

| Component | Material | Safety Factor |
| --- | --- | --- |
| Body1 | PC/ABS Plastic | Yield Strength |

PC/ABS Plastic

| Density | 1.100E-06 kg / mm^3 |
| --- | --- |
| Young's Modulus | 2780.00 MPa |
| Poisson's Ratio | 0.40 |
| Yield Strength | 54.40 MPa |
| Ultimate Tensile Strength | 54.40 MPa |
| Thermal Conductivity | 2.400E-04 W / (mm C) |
| Thermal Expansion Coefficient | 6.700E-05 / C |
| Specific Heat | 2133.00 J / (kg C) |

Contacts

Mesh

| Type | Nodes | Elements |
| --- | --- | --- |
| Solids | 41587 | 23208 |

Load Case1

Constraints

Fixed1

| Type | Fixed |
| --- | --- |
| Ux | Fixed |
| Uy | Fixed |
| Uz | Fixed |

Selected Entities

Loads

Force1

| Type | Force |
| --- | --- |
| Magnitude | 50.00 N |
| X Value | -19.134 N |
| Y Value | -46.194 N |
| Z Value | 0.00 N |
| Force Per Entity | No |

Selected Entities

Results

Safety Factor

Safety Factor (Per Body)

Step 10

0.00  8.00

Stress

von Mises

Step 10

[MPa] 0.00  0.393

1st Principal

Step 10

[MPa] -0.192  0.28

3rd Principal

Step 10

[MPa] -0.505  0.132

Displacement

Total

Step 10

[mm] 0.00E-04  1.404E-04

# References

admin (2024). China Injection molding Cost, completely guide in 2025. [online] Plastic Injection Molding Service. Available at: https://plas.co/china-injection-molding-cost/ [Accessed 27 May 2026].

ANSYS (2025a). ANSYS Mechanical / Granta Selector. [online] www.ansys.com. Available at: https://www.ansys.com.

ANSYS (2025b). What is Finite Element Analysis (FEA)? | Ansys. [online] www.ansys.com. Available at: https://www.ansys.com/simulation-topics/what-is-finite-element-analysis.

ASQ (2019). What Is FMEA? Failure Mode & Effects Analysis. [online] Asq.org. Available at: https://asq.org/quality-resources/fmea [Accessed 15 Apr. 2026].

AutoDesk (2024). Autodesk | 3D Design, Engineering & Construction Software. [online] www.autodesk.com. Available at: https://www.autodesk.com.

Chu, W.-S., Kim, M.-S., Jang, K.-H., Song, J.-H., Rodrigue, H., Chun, D.-M., Cho, Y.T., Ko, S.H., Cho, K.-J., Cha, S.W., Min, S., Jeong, S.H., Jeong, H., Lee, C.-M., Chu, C.N. and Ahn, S.-H. (2016). From design for manufacturing (DFM) to manufacturing for design (MFD) via hybrid manufacturing and smart factory: A review and perspective of paradigm shift. International Journal of Precision Engineering and Manufacturing-Green Technology, 3(2), pp.209–222. doi:https://doi.org/10.1007/s40684-016-0028-0.

Conrad, R. (2023). What is injection molding? - Kuraray Elastomer. [online] www.elastomer.kuraray.com. Available at: https://www.elastomer.kuraray.com/blog/injection-molding/.

EnerTherm-Engineering (2024). Design Of Experiments - Improve Quality & Process Control. [online] EnerTherm Engineering. Available at: https://enertherm-engineering.com/design-of-experiments-doe/ [Accessed 15 Apr. 2026].

Erye Rubber and Plastic Product Co.Ltd (2025). Plastic Warpage: Solution for Injection Molding Warpage - Erye Molding. [online] Erye Plastic and Rubber Products. Available at: https://www.eycpu.com/blog/plastic-warpage/.

Everich (2020). Do You Know Plastic Recycling Symbols Mean - Everich Drinkware. [online] Available at: https://www.everich.com/do-you-know-plastic-recycling-symbols-mean/.

Hall, M. (2023). Recycling Code 7. [online] Business Waste. Available at: https://www.businesswaste.co.uk/news/recycling-code-7/.

Hasan, M. (2025). How Much Does a Phone Case Weigh? Exploring the Weight of Every Type of Phone Case. [online] Lifeproof Waterproof Coral Case. Available at: https://coralcase.com.au/how-much-does-a-phone-case-weigh/?srsltid=AfmBOopjx-ERZswFUtmK3ZH97b7vw9mPDY6uanOmx__CFE5yCRvlupSV [Accessed 23 Apr. 2026].

Hu, P. (2025). Injection Molding Costs: Asia vs. Europe Explained - Aaamould. [online] Aaamould.com. Available at: https://www.aaamould.com/news/injection-molding-costs-asia-vs-europe-explained.html.

IfM (2016). Quality Function Deployment - QFD. [online] Cam.ac.uk. Available at: https://www.ifm.eng.cam.ac.uk/research/dmg/tools-and-techniques/quality-function-deployment-qfd/ [Accessed 15 Apr. 2026].

ITM-LAB Testing Machine 1998 (2025). RS-DP-12A Precision Drop Tester for Phones & Tablets. [online] Linkedin.com. Available at: https://www.linkedin.com/pulse/iec-60068-2-32-standard-definitive-guide-fmw0c [Accessed 23 Apr. 2026].

Juracka, D., Bujdos, D. and Lehner, P. (2025). Numerical and experimental analysis of mechanical and fatigue properties of special shaped 3D printed sample. [online] Research Gate. Available at: https://www.researchgate.net/figure/S-N-curve-for-polycarbonate_fig1_395707039 [Accessed 27 May 2026].

Kehui Mold Co.,Limited (2025). Plastic Injection Molding Tolerance Standards - Kehui Mold Co., Limited. [online] kehuimold. Available at: https://kehuimold.com/plastic-injection-molding-tolerance-standards/ [Accessed 23 Apr. 2026].

Li, J. (2024). Which Country Provides Cheap Injection Mold-Making Services? [online] First Mold. Available at: https://firstmold.com/insights/cheap-injection-mold-making/.

Molcho, G., Cristal, A. and Shpitalni, M. (2014). Part cost estimation at early design phase. CIRP Annals, 63(1), pp.153–156. doi:https://doi.org/10.1016/j.cirp.2014.03.107.

Mulan (2026). Comparing Plastic Injection Moulding Services: China Vs. Other Countries. [online] China-plasticparts.com. Available at: https://www.china-plasticparts.com/a-comparing-plastic-injection-moulding-services-china-vs-other-countries.html [Accessed 27 May 2026].

ProtoLabs (2023). A Beginner’s Guide to Injection Moulding. [online] Protolabs.com. Available at: https://www.protolabs.com/en-gb/resources/guides-and-trend-reports/a-beginner-s-guide-to-injection-moulding/ [Accessed 15 Apr. 2026].

Reshoring Institute (2022). Global Labor Rate Comparisons. [online] Available at: https://reshoringinstitute.org/wp-content/uploads/2022/09/GlobalLaborRateComparisons.pdf.

Schmidt, J. (2023). Break Even Analysis. [online] Corporate Finance Institute. Available at: https://corporatefinanceinstitute.com/resources/accounting/break-even-analysis/.

Thom, M. (2025). Cost Modeling and Cost Models in Project Estimation. [online] Galorath. Available at: https://galorath.com/cost/modeling/.

University of Cambridge (2016). Kano model. [online] www.ifm.eng.cam.ac.uk. Available at: https://www.ifm.eng.cam.ac.uk/research/dmg/tools-and-techniques/kano-model/.

Vassallo, C., Rochman, A. and Refalo, P. (2020). The impact of polymer selection and recycling on the sustainability of injection moulded parts. Procedia CIRP, [online] 90, pp.504–509. doi:https://doi.org/10.1016/j.procir.2020.01.118.

Willson, D. and Willson, D. (2025). Design for Manufacturing and Assembly (DFMA): Principles, Best Practices, and Real-World Examples - Fictiv. [online] Fictiv. Available at: https://www.fictiv.com/articles/dfma-design-for-assembly-and-manufacturing [Accessed 15 Apr. 2026].