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Abstract
This report investigates the mechanical performance and sustainability implications of natural and synthetic fibre composites, using aluminium as a reference material. Tensile tests were conducted on woven and non-woven composites made from carbon, Kevlar, flax and hemp fibres, with both epoxy and bio-based resins. Results showed that aluminium reached the highest peak stress (up to 120 MPa), followed by carbon fibre composites, particularly those using woven architecture and epoxy resin, reaching 437 MPa. Bio-resin variants showed slightly reduced strength (352 MPa), while Kevlar, flax and hemp composites followed in decreasing order of performance. Natural fibre composites such as flax and hemp demonstrated lower strength and greater variability, with non-woven hemp performing the weakest (20–23 MPa). Despite this, these materials offered greater biodegradability and lower environmental impact. A sustainability comparison reinforced the trade-off between mechanical and ecological performance, supporting the viability of natural composites in non-critical applications. The findings suggest promising future use cases for bio-composites with improved processing and hybrid reinforcement strategies.
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Introduction
For many years, the motorsport and automotive industries have pursued advances in materials technology to achieve superior performance, safety and efficiency. Composite materials, particularly fibre-reinforced polymers such as carbon fibre and Kevlar, have revolutionised vehicle design due to their high strength-to-weight ratios, stiffness and durability (Mallick, 2007). However, as sustainability is taken more into consideration across all sectors, traditional composites, typically made from non-renewable resources which are challenging to recycle, face increased scrutiny (Pimenta and Pinho, 2011). Motorsport, historically a proving ground for cutting-edge technology, is now being called upon to also lead the way in sustainable innovation (FIA, 2023).
In response to global environmental pressures and emerging regulations, there is growing interest in bio-based composites, including natural fibre reinforcements such as flax and hemp, as well as resins made from renewable sources (Mohanty, Misra and Drzal, 2005). These materials potentially offer benefits such as reduced carbon footprint, lower energy-intensive manufacturing processes and improved end-of-life recyclability (Pickering, 2006). Nonetheless, questions remain on whether these sustainable composites can provide sufficient mechanical performance for high-demand applications traditionally dominated by synthetic materials (Yan et al., 2014).
The aim of this report is to investigate and evaluate the mechanical properties and sustainability of a range of composite materials relevant to the motorsport and automotive industries. This will be achieved through experimental tensile testing of both traditional and natural fibre composites manufactured with bio-resins and conventional epoxy resins. A baseline comparison with aluminium is also included, given its widespread use and recyclability in automotive structures (Davis, 1999). The mechanical performance data will be critically analysed alongside a sustainability assessment of each material’s lifecycle, from production through to disposal.
The findings of this investigation will inform recommendations on the selection and future development of sustainable composites suitable for automotive and motorsport applications. The report structure includes a review of relevant literature, a detailed account of the experimental testing procedure, an analysis of the results obtained, a sustainability discussion and final recommendations for future practice and research.





2.0 Literature Review
2.1 Properties of Traditional Fibre Composites
Traditional composites, notably carbon fibre reinforced polymers (CFRPs) and aramid fibre composites (e.g., Kevlar), are vastly used in motorsport and automotive applications due to their mechanical properties. Carbon fibre composites offer very high strength-to-weight and stiffness-to-weight ratios, allowing for performance advantages such as improved acceleration, handling and fuel efficiency (Mallick, 2007). Kevlar composites are known for their impact resistance and toughness, making them ideal for applications needing energy absorption, such as body armour and crash structures (Marsh, 2003).
Despite their performance, the manufacturing of CFRPs is energy-intensive, primarily due to the carbonisation process of fibres and the autoclave curing of epoxy matrices (Pickering, 2006). CFRPs are also difficult to recycle in large masses, posing major challenges for end-of-life disposal and diminishing their sustainability credentials (Pimenta and Pinho, 2011).
2.2 Properties of Natural Fibre Composites
Natural fibre composites (NFCs), using reinforcements like flax, hemp and jute, have recently gained attention for their lower environmental impact. Flax fibres, for example, are characterised by relatively high specific stiffness and low density, making them good candidates for semi-structural applications (Yan, Chouw and Jayaraman, 2014). Hemp fibres show similar mechanical performance with the advantage of having rapid growth rates and minimal agricultural inputs, enhancing their sustainability profile (Bourmaud et al., 2018).
Natural fibres exhibit lower tensile strength and durability compared to carbon and aramid fibres, they also tend to be sensitive to moisture absorption, which can degrade mechanical properties over time (Fiore, Scalici and Valenza, 2014). Nevertheless, the low energy of natural fibres and their renewability highlights them as promising options for secondary components, where extreme mechanical performance is not required.
2.3 Comparative Strength of Synthetic and Natural Composites
The mechanical performance of fibre-reinforced composites varies considerably depending on the type of fibre, resin matrix and layup configuration. Industry-grade carbon fibre composites, particularly those with epoxy matrices, typically exhibit tensile strengths in the range of 500–600 MPa (Pimenta and Pinho, 2011; Mallick, 2007). In the present study, carbon woven composites with epoxy achieved a peak stress of 437 MPa, which, while slightly lower than industrial benchmarks, remains consistent with expectations for lab-fabricated composites where factors such as fibre volume fraction, layup precision and curing conditions can affect final strength.
Similarly, Kevlar-based composites in industrial applications often exceed 300 MPa (Campbell, 2010). The Kevlar woven bio-resin specimens tested here reached between 290–310 MPa, falling within this expected range. This validates both the material choice and fabrication method for capturing meaningful comparative results.
In contrast, natural fibre composites showed significantly lower tensile strengths. Flax woven peaked at 90 MPa, flax non-woven at 50 MPa and hemp non-woven between 20–23 MPa. These values reflect the known mechanical limitations of natural fibres, particularly in non-woven or poorly aligned formats. Nonetheless, the relative ranking of materials observed in this study aligns with trends in published literature, supporting the validity of the experimental results and allowing meaningful performance-to-sustainability comparisons.
2.4 Resin Systems: Traditional vs Bio-Based
The resin matrix is a big factor in composite behaviour, transferring loads between fibres and protecting them from environmental damage. Traditional epoxy resins are petroleum-based and provide excellent mechanical and thermal properties, but contribute heavily to the environmental footprint of composites (Pillay and Vaidya, 2011).
Bio-based resins, derived from renewable resources such as vegetable oils or lignin, offer a pathway to reduce the carbon footprint of composites (La Mantia and Morreale, 2011). Although current bio-resins have lower mechanical performance compared to petroleum-based systems, advances in formulation are closing this gap, making bio-composites a realistic possibility for certain automotive and motorsport applications (Rana, Fangueiro and Ramnath, 2016).
2.5 Sustainability Challenges and Opportunities
The sustainability challenges for composites come from the extraction of their raw materials, energy-intensive manufacturing process and difficult end-of-life disposal (Pimenta and Pinho, 2011). Most carbon fibre recycling methods, like pyrolysis, recover fibres with reduced mechanical performance, limiting their ability to be reuse in high-performance applications (Pickering, 2006).
By contrast, natural fibre composites offer advantages such as lower embodied energy, CO₂ absorption during plant growth and easier to biodegrade. Life cycle assessments have shown that NFCs can reduce the overall environmental impact of automotive components when compared to conventional materials (Shah, Porter and Vollrath, 2016).
Legislations, such as the EU’s End-of-Life Vehicle (ELV) Directive (European Parliament, 2000) and motorsport’s increasing focus on carbon neutrality (FIA, 2023), is driving demand for more sustainable materials. The implementation of bio-based and recyclable composites could play a leading role in meeting future regulatory and environmental objectives.
3.0 Experimental Testing
3.1 Materials
A range of composite materials and a metal baseline material were prepared for tensile testing. The composites consisted of fibre-reinforced polymers using either bio-based resins or conventional epoxy resins. The materials tested included twill woven carbon fibre, Kevlar and flax fibres reinforced with bio-resin, alongside a twill woven carbon fibre composite manufactured using traditional epoxy resin. Non-woven composite samples were also produced, incorporating flax, hemp and carbon fibres, all with bio-resin matrices. In addition, aluminium was included as a baseline reference material due to its established mechanical properties and excellent recyclability (Davis, 1999).
All composite samples were manufactured using a resin infusion process to ensure consistent fibre volume fractions and minimise void content. For the twill woven materials, three layers of 200 g/m² carbon or flax fabrics and two layers of 300 g/m² Kevlar fabrics were used, stacked with a 45-degree orientation between layers to simulate realistic multidirectional loading scenarios. The non-woven materials were constructed with either one layer of 300 g/m² flax or carbon fabric, or three layers of 100 g/m² hemp fabric, again with 45-degree fibre orientations to investigate the influence of ply arrangement on tensile performance (Gay, Hoa and Tsai, 2003).
Prior to testing, all samples were visually inspected and organised according to material type and manufacturing method. Figure 1 presents an overview of the prepared tensile specimens, showing clear distinctions between woven and non-woven structures, as well as between the use of bio-resins and traditional epoxy systems.
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Figure 1- Test specimens prepared for testing.

3.2 Testing Procedure
Before testing, each sample’s width and thickness was measured to allow calculation of cross-sectional area. During the tensile tests, load versus time data was collected automatically by the machine's instrumentation system. The testing procedure ensured proper sample gripping by incorporating mesh layers at the ends of each sample, preventing premature slippage or grip failures that could invalidate the results. To ensure safety and repeatability, all testing was carried out under the supervision of the laboratory technician, following strict Health and Safety protocols.
3.3 Data Processing
The raw data from each test was exported as CSV files and analysed using Microsoft Excel. Due to the nature of composite materials, the machine-calculated stress, strain and elongation values were disregarded, as they are typically inaccurate for non-isotropic materials (Pickering, 2006). Instead, stress was calculated by dividing the recorded load by the measured cross-sectional area, while strain was determined based on the change in gauge length relative to the original length. This allowed for accurate plotting of stress-strain curves for each material, capturing important parameters such as ultimate tensile strength and failure strain.
3.4 Observations During Testing
Throughout the testing process, qualitative observations were made regarding the samples' failure behaviour. Twill woven and non-woven composites exhibited distinctly different fracture characteristics, such as fibre pull-out, matrix cracking and delamination. The influence of resin type was also visually assessed, noting differences in brittleness and crack propagation between bio-resin and traditional epoxy composites. These observations provided valuable context to the quantitative data and were supported by photographic documentation where possible.
3.5 Planned Comparisons
The experimental programme was designed to enable clear comparisons between different material types. Key comparisons included the performance differences between twill woven and non-woven structures, the impact of resin type on mechanical properties, the performance of natural fibres versus synthetic carbon fibre and the relative behaviour of composites compared to the aluminium baseline. These comparisons formed the basis for subsequent analysis and discussion, helping to inform conclusions regarding the suitability of sustainable composite materials for use in motorsport and automotive industries.



4. Results and Discussion
This section presents the stress-time behaviour of various composite materials and a baseline aluminium sample under tensile loading. Each graph represents one of two replicate tests per material, with comparisons made between different fibre types, layup architectures and resin systems. Peak stress, time to failure and curve shape were used to interpret performance. 
4.1 Aluminium (Baseline)
[image: A close-up of a metal tool
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Figure 2- Image of the baseline Specimen (Aluminium).
Aluminium displayed steep initial stress rises followed by a yield plateau. The first specimen peaked around 115 MPa and the second slightly higher at 120 MPa (Figures 3 & 4). These trends display the characteristics of ductile metals, presenting distinct elastic and plastic regions followed by stable strain hardening. The similarity between both samples confirms high repeatability. Aluminium’s inclusion served as a reference to assess composite performance (Callister and Rethwisch, 2018; Davis, 1999).

Figure 3– Stress-time Graph for Aluminium 1.

Figure 4- Stress-time Graph for Aluminium 2.


4.2 Hemp Non-Woven (Bio-Resin)
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Figure 5- Post-failure image of Hemp Non-Woven specimen showing delamination and fibre pull-out.

For Hemp Non-Woven, specimen 1 peaked at 20 MPa and Specimen 2 at 23 MPa (Figures 6 & 7), with a 15% difference between them, highlighting poor repeatability and structural inconsistency. The first specimen failed rapidly, while the second showed a more drawn-out stress increase. The weak and inconsistent behaviour is likely a result of poor fibre alignment and weak bonding to the bio-resin, confirmed by frayed failure surfaces (Figure 5). The shallow slope of the stress curves indicates low initial stiffness and poor load transfer. These findings are consistent with the literature that describes hemp composites as mechanically limited unless treated or reinforced with hybrid fibres (Fiore et al., 2014; Shah et al., 2016).

Figure 6- Stress-time plot for Hemp Non-Woven Bio 1.

Figure 7- Stress-time plot for Hemp Non-Woven Bio 2.

4.3 Carbon Non-Woven (Bio-Resin)
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Figure 8- Carbon Non-Woven post-failure image showing brittle fracture and edge damage.
Carbon non-woven Specimens peaked at 210 MPa and 230 MPa respectively, a 9% difference, indicating moderate consistency despite the random fibre orientation (Figures 9 & 10). Compared to hemp, these samples had a more linear increase and better repeatability. However, the lack of a distinct drop at failure suggests a progressive failure mechanism such as internal fibre reorientation or delamination. The curve slope was moderate, indicating improved stiffness compared to hemp but still lower than woven structures. Despite using carbon fibres, the non-woven format and bio-resin matrix affected performance, this is supported by the fibre pull-out observed post-failure (Figure 8).

Figure 9- Stress-time plot for Carbon Non-Woven Bio 1.

Figure 10- Stress-time plot for Carbon Non-Woven Bio 2.
4.4 Carbon Woven (Bio-Resin and Epoxy)
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Figure 11- Carbon Woven Bio-Resin specimen after failure showing fibre continuity.
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Figure 12- Carbon Woven Bio-Resin close-up showing fibre bridging.
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Figure 13- Carbon Woven Epoxy Resin specimen after failure.
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Figure 14- Carbon Woven Epoxy close-up showing matrix-dominated fracture.
Woven carbon fibre with epoxy resin had the highest strength of all composites, with peak stresses around 437 MPa (Figures 15 & 16). The bio-resin reached 352 MPa (Figures 17 & 18), showing 19% lower peak strength on average. Both epoxy samples varied by less than 5%, while the bio-resin samples differed by nearly 12%, indicating reduced consistency with sustainable matrices. Both variants had steep linear gradients and abrupt failure drops, indicating high stiffness and brittle fracture. This was visually confirmed by clean, sharp fracture lines (Figures 11 to 14). The improved stress transfer and matrix adhesion in the epoxy variant was evident in higher slopes and less fibre bridging compared to the bio-resin samples. These results align with the expectations that epoxy offers superior mechanical bonding and curing behaviour (Pimenta and Pinho, 2011; Pillay and Vaidya, 2011).

Figure 15- Stress-time plot for Carbon Woven Epoxy 1.

Figure 16- Stress-time plot for Carbon Woven Epoxy 2.

Figure 17- Stress-time plot for Carbon Woven Bio 1.

Figure 18- Stress-time plot for Carbon Woven Bio 2.











4.5 Flax Non-Woven and Woven (Bio-Resin)
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Figure 19- Flax Woven sample after failure showing fibre bridging and cleaner break.
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Figure 20- Flax Non-Woven sample after failure showing tearing and matrix cracking.

Flax woven performed significantly better than non-woven. Woven flax peaked around 90 MPa, while non-woven averaged 50 MPa (Figures 21 to 24). The specimens differed by only 6%, whereas the non-woven samples showed a 20% discrepancy, reflecting the manufacturing challenges of non-aligned fibres. The woven samples showed a smoother linear increase and higher repeatability. Their stress gradients were moderate, showing a balance between stiffness and flexibility. In contrast, the non-woven samples had inconsistent gradients and early failure, likely due to voids and resin-rich areas. Visual inspection confirmed this, with woven specimens showing cracks and fibre bridging, while non-woven ones failed due to delamination (Figures 19 & 20). These outcomes reflect the structural advantage of woven layups in bio-composites (La Mantia and Morreale, 2011).

Figure 21- Stress-time plot for Flax Woven Bio 1.

Figure 22- Stress-time plot for Flax Woven Bio 2.

Figure 23- Stress-time plot for Flax Non-Woven Bio 1.

Figure 24- Stress-time plot for Flax Non-Woven Bio 2.









4.6 Kevlar Woven (Bio-Resin)
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Figure 25- Kevlar specimen post-failure showing fibre bridging and matrix cracking.
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Figure 26- Close-up of Kevlar specimen showing fibre bridging and matrix cracking at the failure site.
Both specimens recorded peak stresses of 290 MPa and 310 MPa respectively, with minimal variation (<7%), demonstrating good material consistency (Figures 27 & 28), placing it between carbon and flax composites. Their stress curves displayed consistent linearity and clean failure points. Kevlar’s known toughness and energy absorption were evident by the slightly less abrupt failure slopes compared to carbon and fibre bridging observed in post-failure surfaces (Figure 25 & 26). This validates the material’s role in applications requiring high durability with moderate strength (Mallick, 2007).

Figure 27- Stress-time plot for Kevlar Woven Bio 1.

Figure 28- Stress-time plot for Kevlar Woven Bio 2.








4.7 Summary and Interpretation
Carbon Woven (Epoxy) was over 20 times stronger than Hemp Non-Woven and nearly 1.5 times stronger than Kevlar Woven (Bio), underlining the influence of fibre type and matrix quality. After these, Flax Woven, Flax Non-Woven, Carbon Non-Woven followed, with Hemp Non-Woven in last showing the lowest stress resistance.
Woven structures consistently outperformed non-woven and epoxy resin outperformed bio-resin. Natural fibres varied and had lower peak stresses, presenting known limitations in consistency, bonding and durability (Faruk et al., 2012; Shah et al., 2016).
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4.8 Sustainability Insights
The mechanical performance of each composite was only part of the evaluation. Sustainability was also assessed using criteria such as recyclability, biodegradability and overall environmental impact, as shown in Table 2. Fully bio-based composites, such as flax and hemp with bio-resin, demonstrated clear ecological advantages despite their lower mechanical strength. These materials showed higher biodegradability and lower embodied energy, making them viable for applications where environmental performance outweighs structural demands.
Carbon and Kevlar composites, while mechanically superior, are challenging to recycle and rely on energy-intensive manufacturing. Epoxy-based systems are particularly difficult to repurpose due to their thermoset nature. However, switching to bio-resins showed some environmental gains with only moderate reductions in strength. The Kevlar composite, for instance, achieved 290–310 MPa with a bio-resin, offering a compromise between sustainability and performance.
These findings support the growing case for using bio-composites in non-critical applications such as interior automotive panels, consumer goods, or architectural cladding, where sustainability is a driving factor. Optimising natural fibre architecture and resin systems could further close the performance gap while reducing environmental impact.
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5. Conclusion
This study evaluated the tensile performance and sustainability characteristics of a range of composite materials, comparing traditional synthetic configurations with natural fibre bio-composites, using aluminium as a baseline. The results revealed that fibre architecture and resin choice are critical determinants of composite performance.
Aluminium achieved the highest peak stress at 120 MPa, as expected for a ductile metal with a well-defined yield point. Carbon woven composites with epoxy resin followed, reaching 437 MPa, while their bio-resin counterparts achieved 352 MPa, a 19% reduction, illustrating the mechanical trade-off when using more sustainable matrices. Kevlar woven composites performed at approximately 290–310 MPa, offering consistent strength and toughness.
Among the natural fibre composites, flax woven peaked at 90 MPa, outperforming non-woven flax (50 MPa) and hemp non-woven (20–23 MPa). These differences highlight the importance of fibre alignment and matrix bonding quality. Non-woven configurations showed greater variability, consistent with known manufacturing challenges like void formation and inconsistent fibre dispersion.
Although natural composites underperformed compared to synthetics in strength, they demonstrated superior sustainability characteristics, including improved biodegradability and lower environmental impact. As outlined in Table 2, fully bio-based composites such as woven flax with bio-resin offer the most promising balance for low-load applications.
To improve the viability of sustainable composites, future research should focus on optimising layup architecture, enhancing bio-resin chemistry and employing advanced manufacturing methods such as vacuum infusion or compression moulding. Additionally, hybridising natural and synthetic fibres could help bridge the performance gap.
In conclusion, while synthetic composites currently dominate in high-performance applications, this study shows that natural fibre composites, particularly woven flax with bio-resin, present a feasible alternative for sustainable engineering, provided that processing and material consistency can be refined.
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Stress (MPa)



Aluminium 2 Stress
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Hemp N-Woven 1 Stress
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Stress (MPa)



Bio-Hemp N-Woven 2 Stress

0	0	0.02	0.04	0.06	0.08	0.1	0.11899999999999999	0.13900000000000001	0.159	0.17899999999999999	0.2	0.22	0.24	0.25900000000000001	0.27900000000000003	0.29899999999999999	0.31900000000000001	0.33900000000000002	0.35899999999999999	0.38	0.39900000000000002	0.41899999999999998	0.439	0.45900000000000002	0.47899999999999998	0.5	0.51900000000000002	0.53900000000000003	0.55900000000000005	0.57999999999999996	0.59899999999999998	0.61899999999999999	0.63900000000000001	0.65900000000000003	0.67900000000000005	0.69899999999999995	0.71899999999999997	0.73799999999999999	0.75800000000000001	0.77900000000000003	0.79900000000000004	0.81899999999999995	0.83899999999999997	0.85899999999999999	0.879	0.89900000000000002	0.91900000000000004	0.93899999999999995	0.95899999999999996	0.97799999999999998	0.998	1.0189999999999999	1.0389999999999999	1.0580000000000001	1.0780000000000001	1.099	1.1180000000000001	1.1379999999999999	1.1579999999999999	1.1779999999999999	1.1990000000000001	1.218	1.2390000000000001	1.2589999999999999	1.2789999999999999	1.2989999999999999	1.319	1.339	1.3580000000000001	1.3779999999999999	1.399	1.419	1.4390000000000001	1.4590000000000001	1.478	1.498	1.518	1.538	1.5580000000000001	1.5780000000000001	1.5980000000000001	1.6180000000000001	1.6379999999999999	1.6579999999999999	1.6779999999999999	1.698	1.718	1.738	1.758	1.778	1.798	1.8180000000000001	1.8380000000000001	1.8580000000000001	1.8779999999999999	1.8979999999999999	1.9179999999999999	1.9379999999999999	1.958	1.978	1.998	2.0179999999999998	2.0379999999999998	2.0579999999999998	2.0779999999999998	2.0979999999999999	2.1179999999999999	2.1379999999999999	2.1579999999999999	2.1779999999999999	2.1970000000000001	2.218	2.2370000000000001	2.2570000000000001	2.2770000000000001	2.298	2.3180000000000001	2.3380000000000001	2.3580000000000001	2.3769999999999998	2.3980000000000001	2.4169999999999998	2.4380000000000002	2.4569999999999999	2.4769999999999999	2.4969999999999999	2.5169999999999999	2.5369999999999999	2.5579999999999998	2.5779999999999998	2.597	2.6179999999999999	2.6379999999999999	2.657	2.677	2.6970000000000001	2.7160000000000002	2.7370000000000001	2.7570000000000001	2.7770000000000001	2.7970000000000002	2.8170000000000002	2.8370000000000002	2.8570000000000002	2.8769999999999998	2.8969999999999998	2.9169999999999998	2.9369999999999998	2.9569999999999999	2.9769999999999999	2.9969999999999999	3.0169999999999999	3.0369999999999999	3.0569999999999999	3.0760000000000001	3.097	3.117	3.1360000000000001	3.157	3.1760000000000002	3.1970000000000001	3.2160000000000002	3.2370000000000001	3.2570000000000001	3.2770000000000001	3.2970000000000002	3.3159999999999998	3.3370000000000002	3.3559999999999999	3.3759999999999999	3.3959999999999999	3.4159999999999999	3.4359999999999999	3.4569999999999999	3.4769999999999999	3.496	3.516	3.5369999999999999	3.556	3.5760000000000001	3.597	3.6160000000000001	3.6360000000000001	3.657	3.6760000000000002	3.6960000000000002	3.7160000000000002	3.7360000000000002	3.7559999999999998	3.7759999999999998	3.7959999999999998	3.8159999999999998	3.8359999999999999	3.8559999999999999	3.8759999999999999	3.8959999999999999	3.9159999999999999	3.9359999999999999	3.956	3.976	3.996	4.0149999999999997	4.0350000000000001	4.0549999999999997	4.0750000000000002	4.0960000000000001	4.1150000000000002	4.1349999999999998	4.1559999999999997	4.1760000000000002	4.1959999999999997	4.2160000000000002	4.2359999999999998	4.2549999999999999	4.2759999999999998	4.2949999999999999	4.3150000000000004	4.335	4.3550000000000004	4.375	4.3949999999999996	4.415	4.4349999999999996	4.4560000000000004	4.4749999999999996	4.4960000000000004	4.516	4.5359999999999996	4.556	4.5750000000000002	4.5960000000000001	4.6150000000000002	4.6349999999999998	4.6559999999999997	4.6749999999999998	4.6950000000000003	4.7149999999999999	4.7350000000000003	4.7549999999999999	4.7750000000000004	4.7949999999999999	4.8150000000000004	4.835	4.8550000000000004	4.875	4.8949999999999996	4.915	4.9349999999999996	4.9550000000000001	4.9749999999999996	4.9950000000000001	5.0140000000000002	5.0350000000000001	5.0540000000000003	5.0739999999999998	5.0949999999999998	5.1139999999999999	5.1340000000000003	5.1539999999999999	5.1749999999999998	5.194	5.2140000000000004	5.2350000000000003	5.2549999999999999	5.274	5.2939999999999996	5.3150000000000004	5.3339999999999996	5.3540000000000001	5.3739999999999997	5.3940000000000001	5.4139999999999997	5.4349999999999996	5.4539999999999997	5.4740000000000002	5.4939999999999998	5.5140000000000002	5.5339999999999998	5.5540000000000003	5.5739999999999998	5.5940000000000003	5.6150000000000002	5.6349999999999998	5.6539999999999999	5.6740000000000004	5.6950000000000003	5.7140000000000004	5.734	5.7539999999999996	5.774	5.7939999999999996	5.8140000000000001	5.8339999999999996	5.8540000000000001	5.8739999999999997	5.8940000000000001	5.9139999999999997	5.9340000000000002	5.9539999999999997	5.9740000000000002	5.9930000000000003	6.0129999999999999	6.0330000000000004	6.0540000000000003	6.0739999999999998	6.093	6.1139999999999999	6.1340000000000003	6.1529999999999996	6.173	6.194	6.2140000000000004	6.234	6.2539999999999996	6.274	6.2930000000000001	6.3140000000000001	6.3339999999999996	6.3540000000000001	6.3730000000000002	6.3929999999999998	6.4139999999999997	6.4329999999999998	6.4539999999999997	6.4740000000000002	6.4939999999999998	6.5140000000000002	6.5330000000000004	6.5529999999999999	6.5730000000000004	6.5940000000000003	6.6130000000000004	6.633	6.6529999999999996	6.673	6.6929999999999996	6.7130000000000001	6.7329999999999997	6.7530000000000001	6.7729999999999997	6.7930000000000001	6.8129999999999997	6.8330000000000002	6.8529999999999998	6.8730000000000002	6.8929999999999998	6.9130000000000003	6.9329999999999998	6.9530000000000003	6.9729999999999999	6.9930000000000003	7.0129999999999999	7.0330000000000004	7.0529999999999999	7.0730000000000004	7.0919999999999996	7.1130000000000004	7.133	7.1529999999999996	7.173	7.1929999999999996	7.2119999999999997	7.2320000000000002	7.2530000000000001	7.2720000000000002	7.2919999999999998	7.3120000000000003	7.3319999999999999	7.3520000000000003	7.3719999999999999	7.3920000000000003	7.4130000000000003	7.4320000000000004	7.452	7.4720000000000004	7.492	7.5119999999999996	7.5330000000000004	7.5519999999999996	7.5720000000000001	7.5919999999999996	7.6120000000000001	7.6319999999999997	7.6520000000000001	7.6719999999999997	7.6920000000000002	7.7119999999999997	7.7320000000000002	7.7519999999999998	7.7729999999999997	7.7919999999999998	7.8120000000000003	7.8319999999999999	7.8520000000000003	7.8719999999999999	7.8920000000000003	7.9119999999999999	7.9320000000000004	7.952	7.9720000000000004	7.992	8.0120000000000005	8.0329999999999995	8.0519999999999996	8.0719999999999992	8.0909999999999993	8.1120000000000001	8.1310000000000002	8.1519999999999992	8.1709999999999994	8.1920000000000002	8.2119999999999997	8.2319999999999993	8.2520000000000007	8.2720000000000002	8.2919999999999998	8.3119999999999994	8.3320000000000007	8.3520000000000003	8.3719999999999999	8.3919999999999995	8.4120000000000008	8.4320000000000004	8.4510000000000005	8.4710000000000001	8.4920000000000009	8.5120000000000005	8.5310000000000006	8.5510000000000002	8.5709999999999997	8.5909999999999993	8.6110000000000007	8.6310000000000002	8.6509999999999998	8.6709999999999994	8.6910000000000007	8.7119999999999997	8.7319999999999993	8.7520000000000007	8.7720000000000002	8.7910000000000004	8.8109999999999999	8.8309999999999995	8.8510000000000009	8.8710000000000004	8.891	8.9109999999999996	8.9309999999999992	8.9510000000000005	8.9710000000000001	8.9909999999999997	9.0109999999999992	9.0310000000000006	9.0510000000000002	9.0709999999999997	9.0909999999999993	9.1110000000000007	9.1310000000000002	9.1509999999999998	9.1709999999999994	9.1910000000000007	9.2110000000000003	9.2309999999999999	9.25	9.2710000000000008	9.2910000000000004	9.31	9.33	9.35	9.3699999999999992	9.39	9.41	9.4309999999999992	9.4510000000000005	9.4710000000000001	9.49	9.5109999999999992	9.5299999999999994	9.5500000000000007	9.57	9.59	9.61	9.6300000000000008	9.65	9.67	9.69	9.7100000000000009	9.73	9.75	9.77	9.7899999999999991	9.81	9.83	9.85	9.8699999999999992	9.89	9.91	9.93	9.9499999999999993	9.9700000000000006	9.99	10.01	10.029999999999999	10.050000000000001	10.07	10.09	10.11	10.130000000000001	10.15	10.17	10.19	10.210000000000001	10.228999999999999	10.25	10.27	10.29	10.31	10.33	10.349	10.369	10.388999999999999	10.409000000000001	10.43	10.45	10.468999999999999	10.49	10.51	10.529	10.55	10.57	10.589	10.609	10.629	10.648999999999999	10.669	10.689	10.71	10.73	10.749000000000001	10.769	10.79	10.808999999999999	10.829000000000001	10.849	10.869	10.888999999999999	10.909000000000001	10.929	10.949	10.968999999999999	10.989000000000001	11.009	11.029	11.048999999999999	11.069000000000001	11.09	11.108000000000001	11.129	11.148	11.167999999999999	11.189	11.209	11.228999999999999	11.247999999999999	11.269	11.289	11.308999999999999	11.327999999999999	11.349	11.368	11.388	11.409000000000001	11.428000000000001	11.448	11.468999999999999	11.488	11.507999999999999	11.528	11.548	11.569000000000001	11.587999999999999	11.608000000000001	11.628	11.648	11.667999999999999	11.688000000000001	11.708	11.728	11.749000000000001	11.768000000000001	11.788	11.808999999999999	11.829000000000001	11.849	11.869	11.888	11.907999999999999	11.928000000000001	11.948	11.968	11.988	12.007999999999999	12.028	12.048999999999999	12.069000000000001	12.087999999999999	12.108000000000001	12.128	12.148	12.167999999999999	12.186999999999999	12.208	12.227	12.247999999999999	12.268000000000001	12.287000000000001	12.308	12.327999999999999	12.348000000000001	12.368	12.388	12.407	12.427	12.446999999999999	12.467000000000001	12.487	12.507	12.526999999999999	12.548	12.568	12.587999999999999	12.608000000000001	12.628	12.647	12.667	12.686999999999999	12.708	12.727	12.747	12.768000000000001	12.787000000000001	12.808	12.827999999999999	12.848000000000001	12.867000000000001	12.887	12.907	12.927	12.946999999999999	12.967000000000001	12.987	13.007	13.026999999999999	13.047000000000001	13.067	13.087	13.106999999999999	13.127000000000001	13.147	13.167	13.186999999999999	13.207000000000001	13.226000000000001	13.246	13.266999999999999	13.286	13.305999999999999	13.326000000000001	13.347	13.366	13.385999999999999	13.407	13.426	13.446999999999999	13.467000000000001	13.487	13.507	13.526999999999999	13.547000000000001	13.566000000000001	13.587	13.606999999999999	13.627000000000001	13.647	13.666	13.686	13.707000000000001	13.726000000000001	13.747	13.766999999999999	13.787000000000001	13.805999999999999	13.827	13.847	13.866	13.885999999999999	13.906000000000001	13.926	13.946	13.965999999999999	13.986000000000001	14.006	14.026	14.045999999999999	14.066000000000001	14.086	14.106	14.127000000000001	14.146000000000001	14.166	14.186	14.206	14.226000000000001	14.246	14.266	14.286	14.305	14.324999999999999	14.346	14.366	14.385999999999999	14.406000000000001	14.426	14.445	14.465	14.484999999999999	14.505000000000001	14.525	14.545	14.565	14.585000000000001	14.606	14.625	14.646000000000001	14.664999999999999	14.685	14.705	14.725	14.744999999999999	14.766	14.785	14.805999999999999	14.824999999999999	14.845000000000001	14.865	14.885999999999999	14.904999999999999	14.926	14.945	14.965999999999999	14.984999999999999	15.005000000000001	15.025	15.045	15.065	15.085000000000001	15.106	15.125	15.146000000000001	15.164999999999999	15.185	15.205	15.225	15.244999999999999	15.265000000000001	15.285	15.305	15.324999999999999	15.345000000000001	15.364000000000001	15.385	15.404999999999999	15.425000000000001	15.445	15.464	15.484	15.504	15.523999999999999	15.544	15.565	15.584	15.603999999999999	15.624000000000001	15.644	15.664999999999999	15.683999999999999	15.704000000000001	15.725	15.744	15.763999999999999	15.784000000000001	15.805	15.824999999999999	15.843999999999999	15.865	15.884	15.904	15.923999999999999	15.944000000000001	15.964	15.984	16.004000000000001	16.024000000000001	16.044	16.064	16.084	16.103999999999999	16.123999999999999	16.145	16.164000000000001	16.184000000000001	16.204000000000001	16.224	16.244	16.263000000000002	16.283999999999999	16.303999999999998	16.324000000000002	16.343	16.364000000000001	16.384	16.404	16.423999999999999	16.443999999999999	16.463000000000001	16.483000000000001	16.504000000000001	16.524000000000001	16.544	16.562999999999999	16.584	16.603999999999999	16.623999999999999	16.643000000000001	16.663	16.684000000000001	16.704000000000001	16.724	16.742999999999999	16.763999999999999	16.783000000000001	16.803999999999998	16.823	16.844000000000001	16.863	16.882999999999999	16.902999999999999	16.922999999999998	16.943999999999999	16.963999999999999	16.983000000000001	17.003	17.023	17.042999999999999	17.062999999999999	17.082999999999998	17.103000000000002	17.123000000000001	17.143000000000001	17.163	17.183	17.202999999999999	17.222999999999999	17.242999999999999	17.263000000000002	17.283000000000001	17.303000000000001	17.323	17.343	17.361999999999998	17.382000000000001	17.402999999999999	17.422999999999998	17.443000000000001	17.462	17.483000000000001	17.503	17.523	17.542999999999999	17.562999999999999	17.582000000000001	17.603000000000002	17.623000000000001	17.643000000000001	17.663	17.683	17.702000000000002	17.722999999999999	17.742999999999999	17.762	17.782	17.802	17.821999999999999	17.843	17.863	17.882999999999999	17.902000000000001	17.922000000000001	17.942	17.962	17.983000000000001	18.001999999999999	18.021999999999998	18.042000000000002	18.062000000000001	18.082000000000001	18.102	18.122	18.141999999999999	18.163	18.181999999999999	18.202000000000002	18.222000000000001	18.242000000000001	18.262	18.282	18.302	18.321999999999999	18.341999999999999	18.361999999999998	18.382000000000001	18.402000000000001	18.422000000000001	18.442	18.462	18.481999999999999	18.501000000000001	18.521999999999998	18.541	18.561	18.582000000000001	18.602	18.622	18.640999999999998	18.661000000000001	18.681000000000001	18.702000000000002	18.722000000000001	18.742000000000001	18.762	18.782	18.800999999999998	18.821000000000002	18.841000000000001	18.861999999999998	18.881	18.902000000000001	18.920999999999999	18.942	18.960999999999999	18.981000000000002	19.001000000000001	19.021000000000001	19.042000000000002	19.061	19.081	19.100999999999999	19.120999999999999	19.140999999999998	19.161000000000001	19.181000000000001	19.201000000000001	19.221	19.241	19.260999999999999	19.280999999999999	19.300999999999998	19.321000000000002	19.341000000000001	19.361000000000001	19.381	19.399999999999999	19.420999999999999	19.440999999999999	19.460999999999999	19.481000000000002	19.501000000000001	19.521000000000001	19.541	19.561	19.581	19.600000000000001	19.62	19.64	19.661000000000001	19.681000000000001	19.701000000000001	19.721	19.741	19.760000000000002	19.78	19.8	19.821000000000002	19.841000000000001	19.861000000000001	19.88	19.899999999999999	19.920000000000002	19.940000000000001	19.96	19.98	20	20.02	20.04	20.059999999999999	20.079999999999998	20.100000000000001	20.12	20.14	20.16	20.18	20.2	20.22	20.239999999999998	20.260000000000002	20.28	20.300999999999998	20.321000000000002	20.34	20.359000000000002	20.38	20.399999999999999	20.420000000000002	20.440000000000001	20.46	20.48	20.498999999999999	20.52	20.539000000000001	20.56	20.579000000000001	20.599	20.619	20.64	20.66	20.678999999999998	20.699000000000002	20.719000000000001	20.74	20.76	20.779	20.8	20.82	20.84	20.859000000000002	20.88	20.9	20.919	20.94	20.96	20.978999999999999	21	21.018999999999998	21.039000000000001	21.059000000000001	21.079000000000001	21.099	21.119	21.138999999999999	21.158999999999999	21.178999999999998	21.199000000000002	21.219000000000001	21.24	21.259	21.279	21.298999999999999	21.318999999999999	21.338999999999999	21.359000000000002	21.379000000000001	21.398	21.419	21.439	21.459	21.478999999999999	21.498999999999999	21.518999999999998	21.539000000000001	21.559000000000001	21.579000000000001	21.599	21.617999999999999	21.638000000000002	21.658999999999999	21.678999999999998	21.699000000000002	21.718	21.739000000000001	21.759	21.777999999999999	21.797999999999998	21.818000000000001	21.838999999999999	21.859000000000002	21.879000000000001	21.898	21.917999999999999	21.937999999999999	21.957999999999998	21.978000000000002	21.998999999999999	22.018999999999998	22.038	22.058	22.077999999999999	22.097999999999999	22.117999999999999	22.138000000000002	22.158999999999999	22.178000000000001	22.198	22.218	22.238	22.259	22.277999999999999	22.297999999999998	22.318000000000001	22.338000000000001	22.358000000000001	22.378	22.398	22.417000000000002	22.437999999999999	22.457999999999998	22.478000000000002	22.498000000000001	22.518000000000001	22.536999999999999	22.558	22.577999999999999	22.597999999999999	22.617999999999999	22.637	22.657	22.678000000000001	22.698	22.718	22.738	22.757999999999999	22.777999999999999	22.797999999999998	22.817	22.838000000000001	22.858000000000001	22.878	22.896999999999998	22.917999999999999	22.937999999999999	22.957000000000001	22.978000000000002	22.998000000000001	23.016999999999999	23.036999999999999	23.056999999999999	23.077999999999999	23.097000000000001	23.117999999999999	23.137	23.157	23.177	23.196999999999999	23.218	23.236999999999998	23.257000000000001	23.277000000000001	23.297000000000001	23.317	23.338000000000001	23.356999999999999	23.376999999999999	23.396000000000001	23.417000000000002	23.437000000000001	23.457000000000001	23.477	23.497	23.516999999999999	23.536999999999999	23.556999999999999	23.577000000000002	23.597000000000001	23.617000000000001	23.637	23.657	23.675999999999998	23.696000000000002	23.716999999999999	23.736999999999998	23.756	23.776	23.797000000000001	23.815999999999999	23.837	23.856999999999999	23.876999999999999	23.896999999999998	23.916	23.937000000000001	23.956	23.977	23.995999999999999	24.016999999999999	24.036000000000001	24.056999999999999	24.077000000000002	24.097000000000001	24.117000000000001	24.137	24.155999999999999	24.175999999999998	24.196000000000002	24.216000000000001	24.236000000000001	24.256	24.276	24.295999999999999	24.315999999999999	24.335999999999999	24.356000000000002	24.376000000000001	24.396000000000001	24.416	24.434999999999999	24.456	24.475999999999999	24.495999999999999	24.515000000000001	24.536000000000001	24.555	24.576000000000001	24.596	24.616	24.635999999999999	24.655000000000001	24.675999999999998	24.695	24.716000000000001	24.736000000000001	24.756	24.774999999999999	24.795000000000002	24.815000000000001	24.835000000000001	24.856000000000002	24.876000000000001	24.896000000000001	24.914999999999999	24.934999999999999	24.954999999999998	24.975999999999999	24.995999999999999	25.015000000000001	25.035	25.056000000000001	25.076000000000001	25.094999999999999	25.114999999999998	25.135000000000002	25.155000000000001	25.175000000000001	25.195	25.215	25.234999999999999	25.254999999999999	25.274999999999999	25.295000000000002	25.315000000000001	25.335000000000001	25.355	25.375	25.395	25.414999999999999	25.434999999999999	25.454000000000001	25.474	25.495000000000001	25.515000000000001	25.535	25.555	25.574999999999999	25.594999999999999	25.614000000000001	25.635000000000002	25.654	25.675000000000001	25.695	25.715	25.734999999999999	25.754999999999999	25.774000000000001	25.794	25.814	25.834	25.853999999999999	25.875	25.895	25.914999999999999	25.934999999999999	25.954999999999998	25.975000000000001	25.994	26.013999999999999	26.035	26.055	26.074000000000002	26.094999999999999	26.114999999999998	26.135000000000002	26.155000000000001	26.175000000000001	26.193999999999999	26.213999999999999	26.234000000000002	26.254000000000001	26.274000000000001	26.294	26.314	26.334	26.353999999999999	26.373999999999999	26.395	26.414000000000001	26.434000000000001	26.454000000000001	26.474	26.494	26.513999999999999	26.533999999999999	26.553999999999998	26.573	26.594000000000001	26.614000000000001	26.632999999999999	26.652999999999999	26.673999999999999	26.693000000000001	26.713999999999999	26.734000000000002	26.754000000000001	26.774000000000001	26.792999999999999	26.812999999999999	26.832999999999998	26.853000000000002	26.873999999999999	26.893999999999998	26.913	26.933	26.954000000000001	26.974	26.994	27.013000000000002	27.033000000000001	27.053000000000001	27.074000000000002	27.094000000000001	27.114000000000001	27.134	27.154	27.172999999999998	27.193999999999999	27.213000000000001	27.233000000000001	27.254000000000001	27.273	27.292999999999999	27.312999999999999	27.334	27.353000000000002	27.373000000000001	27.393000000000001	27.414000000000001	27.433	27.452999999999999	27.472999999999999	27.492999999999999	27.513000000000002	27.533000000000001	27.553000000000001	27.573	27.593	27.613	27.632999999999999	27.652999999999999	27.672999999999998	27.693000000000001	27.713000000000001	27.733000000000001	27.751999999999999	27.773	27.792999999999999	27.812000000000001	27.832000000000001	27.852	27.873000000000001	27.891999999999999	27.913	27.931999999999999	27.952000000000002	27.972999999999999	27.992999999999999	28.012	28.033000000000001	28.053000000000001	28.073	28.093	28.113	28.132999999999999	28.152000000000001	28.172000000000001	28.193000000000001	28.213000000000001	28.233000000000001	28.253	28.273	28.292000000000002	28.312000000000001	28.332000000000001	28.352	28.372	28.391999999999999	28.413	28.431999999999999	28.452000000000002	28.472000000000001	28.492999999999999	28.512	28.532	28.552	28.571999999999999	28.591999999999999	28.611999999999998	28.632000000000001	28.652000000000001	28.672000000000001	28.692	28.710999999999999	28.731999999999999	28.751000000000001	28.771999999999998	28.792000000000002	28.812000000000001	28.831	28.852	28.872	28.891999999999999	28.911999999999999	28.931999999999999	28.951000000000001	28.972000000000001	28.991	29.012	29.032	29.052	29.071000000000002	29.091000000000001	29.111000000000001	29.131	29.151	29.170999999999999	29.192	29.210999999999999	29.231000000000002	29.251000000000001	29.271999999999998	29.291	29.311	29.331	29.350999999999999	29.370999999999999	29.390999999999998	29.411000000000001	29.431000000000001	29.451000000000001	29.471	29.491	29.510999999999999	29.530999999999999	29.550999999999998	29.571000000000002	29.591000000000001	29.611000000000001	29.631	29.651	29.67	29.690999999999999	29.710999999999999	29.731000000000002	29.751000000000001	29.771000000000001	29.791	29.811	29.831	29.850999999999999	29.870999999999999	29.890999999999998	29.91	29.931000000000001	29.95	29.97	29.991	30.010999999999999	30.030999999999999	30.050999999999998	30.07	30.09	30.11	30.131	30.151	30.17	30.19	30.21	30.23	30.251000000000001	30.271000000000001	30.29	30.31	30.33	30.350999999999999	30.37	30.390999999999998	30.411000000000001	30.431000000000001	30.45	30.47	30.49	30.51	30.53	30.55	30.57	30.59	30.61	30.629000000000001	30.65	30.67	30.69	30.71	30.73	30.75	30.77	30.789000000000001	30.809000000000001	30.83	30.85	30.869	30.89	30.91	30.93	30.95	30.969000000000001	30.99	31.01	31.03	31.048999999999999	31.07	31.088999999999999	31.109000000000002	31.129000000000001	31.15	31.17	31.189	31.209	31.228999999999999	31.25	31.27	31.29	31.309000000000001	31.33	31.349	31.369	31.388999999999999	31.408999999999999	31.43	31.45	31.47	31.49	31.509	31.53	31.55	31.568999999999999	31.588999999999999	31.609000000000002	31.629000000000001	31.649000000000001	31.669	31.689	31.709	31.728000000000002	31.748999999999999	31.768999999999998	31.789000000000001	31.809000000000001	31.829000000000001	31.847999999999999	31.867999999999999	31.888999999999999	31.908999999999999	31.928999999999998	31.949000000000002	31.969000000000001	31.989000000000001	32.009	32.027999999999999	32.048999999999999	32.067999999999998	32.088999999999999	32.107999999999997	32.128999999999998	32.149000000000001	32.168999999999997	32.189	32.209000000000003	32.228000000000002	32.247999999999998	32.268000000000001	32.287999999999997	32.308	32.328000000000003	32.348999999999997	32.369	32.387999999999998	32.408999999999999	32.427999999999997	32.448	32.469000000000001	32.488	32.508000000000003	32.527999999999999	32.548000000000002	32.567999999999998	32.588000000000001	32.607999999999997	32.628	32.648000000000003	32.667999999999999	32.688000000000002	32.707999999999998	32.728000000000002	32.747999999999998	32.768000000000001	32.787999999999997	32.808	32.828000000000003	32.847999999999999	32.868000000000002	32.887999999999998	32.908000000000001	32.927999999999997	32.948	32.968000000000004	32.988	33.008000000000003	33.027000000000001	33.048000000000002	33.067999999999998	33.088000000000001	33.106999999999999	33.127000000000002	33.148000000000003	33.167999999999999	33.188000000000002	33.207000000000001	33.228000000000002	33.247	33.268000000000001	33.286999999999999	33.308	33.326999999999998	33.347999999999999	33.368000000000002	33.387	33.408000000000001	33.427	33.447000000000003	33.466999999999999	33.487000000000002	33.506999999999998	33.527000000000001	33.546999999999997	33.567999999999998	33.587000000000003	33.606999999999999	33.628	33.646999999999998	33.667000000000002	33.686999999999998	33.707000000000001	33.726999999999997	33.747	33.767000000000003	33.786999999999999	33.807000000000002	33.826999999999998	33.847000000000001	33.866999999999997	33.887	33.906999999999996	33.926000000000002	33.947000000000003	33.966999999999999	33.987000000000002	34.006	34.026000000000003	34.046999999999997	34.067	34.087000000000003	34.106999999999999	34.127000000000002	34.146000000000001	34.165999999999997	34.186	34.206000000000003	34.226999999999997	34.247	34.267000000000003	34.286000000000001	34.307000000000002	34.326999999999998	34.345999999999997	34.366999999999997	34.387	34.405999999999999	34.426000000000002	34.445999999999998	34.466000000000001	34.485999999999997	34.506	34.526000000000003	34.545999999999999	34.566000000000003	34.587000000000003	34.606000000000002	34.625999999999998	34.646000000000001	34.665999999999997	34.686	34.706000000000003	34.725999999999999	34.746000000000002	34.765999999999998	34.786000000000001	34.805999999999997	34.826000000000001	34.845999999999997	34.866	34.886000000000003	34.905999999999999	34.926000000000002	34.945999999999998	34.966000000000001	34.985999999999997	35.006	35.026000000000003	35.045000000000002	35.064999999999998	35.085000000000001	35.104999999999997	35.125	35.146000000000001	35.164999999999999	35.185000000000002	35.204999999999998	35.225000000000001	35.244999999999997	35.265000000000001	35.286000000000001	35.305	35.325000000000003	35.345999999999997	35.365000000000002	35.384999999999998	35.405999999999999	35.426000000000002	35.445	35.465000000000003	35.484999999999999	35.505000000000003	35.526000000000003	35.545000000000002	35.564999999999998	35.585999999999999	35.604999999999997	35.625	35.645000000000003	35.664999999999999	35.685000000000002	35.704999999999998	35.725000000000001	35.744999999999997	35.765000000000001	35.784999999999997	35.805	35.825000000000003	35.844999999999999	35.866	35.884999999999998	35.905000000000001	35.924999999999997	35.944000000000003	35.965000000000003	35.984999999999999	36.005000000000003	36.024999999999999	36.045000000000002	36.064999999999998	36.085000000000001	36.104999999999997	36.125	36.145000000000003	36.164999999999999	36.183999999999997	36.204000000000001	36.225000000000001	36.244	36.265000000000001	36.284999999999997	36.304000000000002	36.325000000000003	36.344000000000001	36.365000000000002	36.384	36.404000000000003	36.423999999999999	36.445	36.465000000000003	36.484999999999999	36.505000000000003	36.524999999999999	36.543999999999997	36.564	36.584000000000003	36.604999999999997	36.624000000000002	36.645000000000003	36.664000000000001	36.683999999999997	36.704000000000001	36.723999999999997	36.744	36.764000000000003	36.783999999999999	36.804000000000002	36.823999999999998	36.844000000000001	36.863999999999997	36.884	36.904000000000003	36.923999999999999	36.944000000000003	36.963999999999999	36.984000000000002	37.003999999999998	37.023000000000003	37.043999999999997	37.064	37.084000000000003	37.103000000000002	37.124000000000002	37.143000000000001	37.164000000000001	37.183999999999997	37.204000000000001	37.223999999999997	37.243000000000002	37.262999999999998	37.283999999999999	37.302999999999997	37.323	37.344000000000001	37.363999999999997	37.384	37.402999999999999	37.423000000000002	37.444000000000003	37.463000000000001	37.482999999999997	37.503999999999998	37.523000000000003	37.542999999999999	37.563000000000002	37.584000000000003	37.603999999999999	37.624000000000002	37.643000000000001	37.662999999999997	37.683	37.704999999999998	37.723999999999997	37.743000000000002	37.762999999999998	37.783000000000001	37.802999999999997	37.823	37.843000000000004	37.863	37.883000000000003	37.902999999999999	37.923000000000002	37.942999999999998	37.963000000000001	37.982999999999997	38.003	38.023000000000003	38.042999999999999	38.061999999999998	38.082999999999998	38.103000000000002	38.122999999999998	38.143000000000001	38.162999999999997	38.183	38.203000000000003	38.222999999999999	38.241999999999997	38.262	38.283000000000001	38.302	38.322000000000003	38.341999999999999	38.362000000000002	38.381999999999998	38.402999999999999	38.421999999999997	38.442	38.463000000000001	38.482999999999997	38.502000000000002	38.523000000000003	38.542999999999999	38.561999999999998	38.582000000000001	38.601999999999997	38.622	38.642000000000003	38.661999999999999	38.682000000000002	38.701999999999998	38.722000000000001	38.741999999999997	38.762	38.783000000000001	38.802	38.822000000000003	38.841999999999999	38.862000000000002	38.881999999999998	38.902000000000001	38.921999999999997	38.942	38.962000000000003	38.981999999999999	39.002000000000002	39.021999999999998	39.042000000000002	39.061999999999998	39.081000000000003	39.100999999999999	39.121000000000002	39.142000000000003	39.161999999999999	39.182000000000002	39.201999999999998	39.222000000000001	39.241	39.262	39.280999999999999	39.301000000000002	39.322000000000003	39.341999999999999	39.360999999999997	39.381999999999998	39.402000000000001	39.420999999999999	39.442	39.462000000000003	39.481000000000002	39.502000000000002	39.521999999999998	39.540999999999997	39.561	39.581000000000003	39.600999999999999	39.621000000000002	39.640999999999998	39.661000000000001	39.682000000000002	39.701000000000001	39.720999999999997	39.741	39.761000000000003	39.780999999999999	39.801000000000002	39.820999999999998	39.841000000000001	39.860999999999997	39.881	39.901000000000003	39.920999999999999	39.941000000000003	39.960999999999999	39.981000000000002	40.000999999999998	40.021000000000001	40.04	40.06	40.08	40.100999999999999	40.121000000000002	40.140999999999998	40.161000000000001	40.180999999999997	40.201000000000001	40.220999999999997	40.241	40.261000000000003	40.28	40.301000000000002	40.32	40.341000000000001	40.36	40.380000000000003	40.401000000000003	40.420999999999999	40.44	40.460999999999999	40.481000000000002	40.5	40.521000000000001	40.540999999999997	40.56	40.58	40.6	40.619999999999997	40.64	40.659999999999997	40.68	40.701000000000001	40.72	40.74	40.76	40.78	40.799999999999997	40.82	40.840000000000003	40.86	40.880000000000003	40.9	40.92	40.94	40.96	40.98	41	41.02	41.04	41.06	41.08	41.1	41.12	41.14	41.16	41.18	41.2	41.22	41.24	41.259	41.28	41.298999999999999	41.32	41.338999999999999	41.359000000000002	41.38	41.4	41.42	41.439	41.459000000000003	41.478999999999999	41.5	41.52	41.54	41.56	41.579000000000001	41.598999999999997	41.619	41.639000000000003	41.66	41.679000000000002	41.698999999999998	41.719000000000001	41.738999999999997	41.759	41.779000000000003	41.8	41.82	41.838999999999999	41.859000000000002	41.878999999999998	41.899000000000001	41.918999999999997	41.939	41.959000000000003	41.978999999999999	41.999000000000002	42.018999999999998	42.039000000000001	42.058999999999997	42.08	42.098999999999997	42.119	42.139000000000003	42.158999999999999	42.179000000000002	42.198999999999998	42.218000000000004	42.238999999999997	42.259	42.277999999999999	42.298999999999999	42.319000000000003	42.338999999999999	42.357999999999997	42.378	42.399000000000001	42.418999999999997	42.439	42.459000000000003	42.478000000000002	42.499000000000002	42.518999999999998	42.537999999999997	42.558999999999997	42.578000000000003	42.597999999999999	42.618000000000002	42.637999999999998	42.658000000000001	42.677999999999997	42.698999999999998	42.718000000000004	42.738	42.759	42.777999999999999	42.798000000000002	42.817999999999998	42.838999999999999	42.857999999999997	42.877000000000002	42.898000000000003	42.917999999999999	42.938000000000002	42.957999999999998	42.978000000000002	42.997999999999998	43.018000000000001	43.037999999999997	43.058	43.078000000000003	43.097999999999999	43.118000000000002	43.137999999999998	43.158000000000001	43.177999999999997	43.198	43.218000000000004	43.238	43.258000000000003	43.277999999999999	43.298000000000002	43.317999999999998	43.338000000000001	43.357999999999997	43.378	43.396999999999998	43.417999999999999	43.438000000000002	43.457999999999998	43.478000000000002	43.497999999999998	43.518000000000001	43.536999999999999	43.557000000000002	43.576999999999998	43.597999999999999	43.618000000000002	43.637	43.656999999999996	43.677	43.697000000000003	43.716999999999999	43.738	43.756999999999998	43.777000000000001	43.796999999999997	43.817	43.837000000000003	43.856999999999999	43.877000000000002	43.898000000000003	43.917000000000002	43.936999999999998	43.957000000000001	43.978000000000002	43.997	44.017000000000003	44.036999999999999	44.057000000000002	44.076999999999998	44.097000000000001	44.116999999999997	44.137	44.155999999999999	44.176000000000002	44.197000000000003	44.216999999999999	44.237000000000002	44.256999999999998	44.277000000000001	44.296999999999997	44.317	44.337000000000003	44.356999999999999	44.377000000000002	44.396999999999998	44.417000000000002	44.436	44.457000000000001	44.476999999999997	44.496000000000002	44.515999999999998	44.536999999999999	44.557000000000002	44.576000000000001	44.597000000000001	44.616	44.637	44.655999999999999	44.676000000000002	44.695999999999998	44.716000000000001	44.735999999999997	44.756	44.777000000000001	44.795999999999999	44.816000000000003	44.835999999999999	44.856000000000002	44.875999999999998	44.896000000000001	44.915999999999997	44.936	44.957000000000001	44.975999999999999	44.996000000000002	45.015999999999998	45.036000000000001	45.055999999999997	45.076000000000001	45.095999999999997	45.116	45.136000000000003	45.155999999999999	45.174999999999997	45.195999999999998	45.216000000000001	45.235999999999997	45.256	45.274999999999999	45.295000000000002	45.314999999999998	45.335999999999999	45.356000000000002	45.375999999999998	45.396000000000001	45.415999999999997	45.436	45.454999999999998	45.475999999999999	45.494999999999997	45.515999999999998	45.534999999999997	45.555	45.575000000000003	45.594999999999999	45.615000000000002	45.636000000000003	45.655999999999999	45.676000000000002	45.695	45.715000000000003	45.734999999999999	45.755000000000003	45.774999999999999	45.795999999999999	45.814999999999998	45.835999999999999	45.856000000000002	45.875999999999998	45.896000000000001	45.915999999999997	45.935000000000002	45.954999999999998	45.975000000000001	45.996000000000002	46.015000000000001	46.034999999999997	46.055	46.075000000000003	46.094999999999999	46.116	46.134999999999998	46.155000000000001	46.174999999999997	46.194000000000003	46.215000000000003	46.234999999999999	46.255000000000003	46.274999999999999	46.295000000000002	46.314999999999998	46.335000000000001	46.353999999999999	46.375	46.395000000000003	46.414999999999999	46.433999999999997	46.454999999999998	46.475000000000001	46.494	46.514000000000003	46.534999999999997	46.554000000000002	46.573999999999998	46.594000000000001	46.613999999999997	46.634	46.655000000000001	46.674999999999997	46.695	46.713999999999999	46.734000000000002	46.753999999999998	46.774000000000001	46.795000000000002	46.814	46.834000000000003	46.854999999999997	46.874000000000002	46.893999999999998	46.914000000000001	46.935000000000002	46.954000000000001	46.973999999999997	46.994	47.014000000000003	47.033999999999999	47.054000000000002	47.073999999999998	47.094999999999999	47.113999999999997	47.134	47.154000000000003	47.173999999999999	47.194000000000003	47.213000000000001	47.232999999999997	47.253999999999998	47.273000000000003	47.292999999999999	47.313000000000002	47.334000000000003	47.353999999999999	47.374000000000002	47.393999999999998	47.414000000000001	47.433	47.454000000000001	47.472999999999999	47.494	47.514000000000003	47.533999999999999	47.554000000000002	47.573	47.593000000000004	47.613999999999997	47.633000000000003	47.654000000000003	47.673000000000002	47.694000000000003	47.713000000000001	47.732999999999997	47.753	47.773000000000003	47.792999999999999	47.814	47.832999999999998	47.853000000000002	47.872999999999998	47.893000000000001	47.912999999999997	47.933999999999997	47.953000000000003	47.972999999999999	47.993000000000002	48.012999999999998	48.033000000000001	48.052999999999997	48.073999999999998	48.093000000000004	48.113	48.133000000000003	48.152999999999999	48.173000000000002	48.192999999999998	48.213000000000001	48.232999999999997	48.253	48.273000000000003	48.292999999999999	48.313000000000002	48.332999999999998	48.353000000000002	48.372999999999998	48.393000000000001	48.411999999999999	48.433	48.451999999999998	48.472999999999999	48.493000000000002	48.512999999999998	48.531999999999996	48.552999999999997	48.572000000000003	48.591999999999999	48.613	48.631999999999998	48.652999999999999	48.673000000000002	48.692999999999998	48.712000000000003	48.731999999999999	48.753	48.771999999999998	48.792000000000002	48.813000000000002	48.832000000000001	48.851999999999997	48.872	48.892000000000003	48.912999999999997	48.933	48.951999999999998	48.972000000000001	48.991999999999997	49.012	49.031999999999996	49.052	49.073	49.091999999999999	49.112000000000002	49.131999999999998	49.152000000000001	49.171999999999997	49.192999999999998	49.212000000000003	49.231999999999999	49.252000000000002	49.271999999999998	49.292000000000002	49.311999999999998	49.332000000000001	49.351999999999997	49.372	49.392000000000003	49.411999999999999	49.432000000000002	49.451999999999998	49.472000000000001	49.491999999999997	49.512	49.531999999999996	49.552	49.572000000000003	49.591999999999999	49.612000000000002	49.631999999999998	49.652000000000001	49.670999999999999	49.691000000000003	49.710999999999999	49.731999999999999	49.752000000000002	49.771000000000001	49.790999999999997	49.811999999999998	49.832000000000001	49.851999999999997	49.872	49.890999999999998	49.911000000000001	49.930999999999997	49.951000000000001	49.970999999999997	49.991	50.012	50.030999999999999	50.051000000000002	50.070999999999998	50.091000000000001	50.110999999999997	50.131	50.152000000000001	50.171999999999997	50.191000000000003	50.210999999999999	50.231000000000002	50.250999999999998	50.271000000000001	50.290999999999997	50.311	50.331000000000003	50.35	50.371000000000002	50.390999999999998	50.411000000000001	50.430999999999997	50.451000000000001	50.47	50.491	50.511000000000003	50.530999999999999	50.55	50.570999999999998	50.591000000000001	50.61	50.631	50.65	50.67	50.691000000000003	50.710999999999999	50.731000000000002	50.750999999999998	50.771000000000001	50.79	50.81	50.83	50.85	50.871000000000002	50.890999999999998	50.91	50.930999999999997	50.951000000000001	50.970999999999997	50.99	51.01	51.03	51.05	51.070999999999998	51.09	51.11	51.13	51.15	51.17	51.19	51.21	51.23	51.250999999999998	51.27	51.29	51.31	51.33	51.348999999999997	51.37	51.39	51.408999999999999	51.43	51.45	51.47	51.49	51.51	51.529000000000003	51.55	51.57	51.588999999999999	51.609000000000002	51.63	51.65	51.67	51.69	51.709000000000003	51.73	51.749000000000002	51.77	51.789000000000001	51.808999999999997	51.829000000000001	51.848999999999997	51.87	51.889000000000003	51.908999999999999	51.93	51.948999999999998	51.97	51.988999999999997	52.01	52.03	52.05	52.069000000000003	52.088999999999999	52.109000000000002	52.128999999999998	52.149000000000001	52.168999999999997	52.189	52.209000000000003	52.228999999999999	52.249000000000002	52.27	52.289000000000001	52.308999999999997	52.329000000000001	52.348999999999997	52.369	52.389000000000003	52.408000000000001	52.429000000000002	52.448999999999998	52.469000000000001	52.488999999999997	52.509	52.529000000000003	52.548999999999999	52.569000000000003	52.588000000000001	52.609000000000002	52.628999999999998	52.648000000000003	52.668999999999997	52.689	52.709000000000003	52.728999999999999	52.749000000000002	52.768999999999998	52.789000000000001	52.808	52.828000000000003	52.847999999999999	52.869	52.887999999999998	52.908999999999999	52.927999999999997	52.948	52.969000000000001	52.988999999999997	53.009	53.027999999999999	53.048000000000002	53.067999999999998	53.088000000000001	53.107999999999997	53.128	53.148000000000003	53.167999999999999	53.188000000000002	53.207999999999998	53.228000000000002	53.247999999999998	53.268000000000001	53.287999999999997	53.308	53.328000000000003	53.347999999999999	53.368000000000002	53.387	53.408000000000001	53.427999999999997	53.448	53.468000000000004	53.488	53.506999999999998	53.527999999999999	53.548000000000002	53.567999999999998	53.588000000000001	53.607999999999997	53.627000000000002	53.648000000000003	53.667999999999999	53.686999999999998	53.707000000000001	53.728000000000002	53.747999999999998	53.768000000000001	53.787999999999997	53.808	53.828000000000003	53.847000000000001	53.866999999999997	53.887999999999998	53.908000000000001	53.927999999999997	53.947000000000003	53.966999999999999	53.987000000000002	54.006999999999998	54.027000000000001	54.046999999999997	54.067999999999998	54.087000000000003	54.107999999999997	54.127000000000002	54.146999999999998	54.167000000000002	54.186999999999998	54.207000000000001	54.226999999999997	54.247	54.267000000000003	54.287999999999997	54.307000000000002	54.326999999999998	54.347000000000001	54.366999999999997	54.387	54.406999999999996	54.427	54.445999999999998	54.466999999999999	54.487000000000002	54.506999999999998	54.527000000000001	54.546999999999997	54.567	54.587000000000003	54.606999999999999	54.627000000000002	54.646999999999998	54.665999999999997	54.686999999999998	54.707000000000001	54.726999999999997	54.747	54.767000000000003	54.786000000000001	54.807000000000002	54.826000000000001	54.845999999999997	54.866	54.886000000000003	54.905999999999999	54.926000000000002	54.947000000000003	54.966999999999999	54.987000000000002	55.006	55.027000000000001	55.046999999999997	55.066000000000003	55.085999999999999	55.106999999999999	55.125999999999998	55.146000000000001	55.165999999999997	55.186	55.206000000000003	55.225999999999999	55.246000000000002	55.267000000000003	55.286999999999999	55.305999999999997	55.326000000000001	55.345999999999997	55.366	55.386000000000003	55.405000000000001	55.426000000000002	55.445999999999998	55.466000000000001	55.485999999999997	55.506	55.526000000000003	55.545000000000002	55.566000000000003	55.585999999999999	55.606000000000002	55.625999999999998	55.646000000000001	55.664999999999999	55.686	55.706000000000003	55.725000000000001	55.744999999999997	55.765000000000001	55.786000000000001	55.805999999999997	55.825000000000003	55.845999999999997	55.866	55.884999999999998	55.905999999999999	55.924999999999997	55.945	55.966000000000001	55.984999999999999	56.006	56.024999999999999	56.045999999999999	56.064999999999998	56.085999999999999	56.104999999999997	56.125	56.145000000000003	56.164999999999999	56.185000000000002	56.204999999999998	56.225000000000001	56.244999999999997	56.265000000000001	56.284999999999997	56.305	56.325000000000003	56.344999999999999	56.365000000000002	56.386000000000003	56.405000000000001	56.424999999999997	56.445	56.465000000000003	56.484999999999999	56.505000000000003	56.524999999999999	56.545000000000002	56.564999999999998	56.585000000000001	56.604999999999997	56.625	56.645000000000003	56.664999999999999	56.685000000000002	56.704999999999998	56.723999999999997	56.744999999999997	56.765000000000001	56.784999999999997	56.805	56.823999999999998	56.844000000000001	56.865000000000002	56.884999999999998	56.905000000000001	56.924999999999997	56.945	56.965000000000003	56.984000000000002	57.003999999999998	57.024000000000001	57.045000000000002	57.064999999999998	57.085000000000001	57.103999999999999	57.124000000000002	57.143999999999998	57.164999999999999	57.183999999999997	57.204000000000001	57.225000000000001	57.244999999999997	57.265000000000001	57.283999999999999	57.304000000000002	57.323999999999998	57.344000000000001	57.363999999999997	57.384	57.404000000000003	57.423999999999999	57.444000000000003	57.463000000000001	57.482999999999997	57.503999999999998	57.524000000000001	57.543999999999997	57.564	57.584000000000003	57.603999999999999	57.624000000000002	57.643999999999998	57.664000000000001	57.683999999999997	57.704000000000001	57.723999999999997	57.744	57.762999999999998	57.783000000000001	57.802999999999997	57.823999999999998	57.844000000000001	57.863999999999997	57.883000000000003	57.904000000000003	57.923999999999999	57.944000000000003	57.963000000000001	57.982999999999997	58.003	58.023000000000003	58.042999999999999	58.063000000000002	58.084000000000003	58.103999999999999	58.124000000000002	58.143000000000001	58.162999999999997	58.183999999999997	58.203000000000003	58.222999999999999	58.243000000000002	58.262999999999998	58.283000000000001	58.302999999999997	58.323	58.343000000000004	58.363	58.383000000000003	58.402999999999999	58.423000000000002	58.442999999999998	58.463000000000001	58.482999999999997	58.503	58.523000000000003	58.542999999999999	58.563000000000002	58.582999999999998	58.603000000000002	58.622999999999998	58.643000000000001	58.662999999999997	58.683	58.703000000000003	58.722999999999999	58.743000000000002	58.762999999999998	58.781999999999996	58.802999999999997	58.823	58.843000000000004	58.863	58.881999999999998	58.902999999999999	58.923000000000002	58.942999999999998	58.962000000000003	58.981999999999999	59.003	59.021999999999998	59.042000000000002	59.061999999999998	59.082999999999998	59.103000000000002	59.122	59.143000000000001	59.162999999999997	59.183	59.201999999999998	59.222000000000001	59.241999999999997	59.262	59.281999999999996	59.302	59.322000000000003	59.341999999999999	59.362000000000002	59.381999999999998	59.402000000000001	59.421999999999997	59.442	59.462000000000003	59.481999999999999	59.500999999999998	59.521999999999998	59.542000000000002	59.561999999999998	59.582000000000001	59.601999999999997	59.622	59.642000000000003	59.661999999999999	59.682000000000002	59.701999999999998	59.720999999999997	59.741999999999997	59.762	59.781999999999996	59.801000000000002	59.822000000000003	59.841000000000001	59.862000000000002	59.881999999999998	59.902000000000001	59.920999999999999	59.941000000000003	59.960999999999999	59.981999999999999	60.002000000000002	60.021000000000001	60.042000000000002	60.061999999999998	60.081000000000003	60.100999999999999	60.122	60.142000000000003	60.161000000000001	60.180999999999997	60.201000000000001	60.222000000000001	60.241	60.261000000000003	60.280999999999999	60.301000000000002	60.320999999999998	60.341000000000001	60.360999999999997	60.381999999999998	60.401000000000003	60.420999999999999	60.441000000000003	60.462000000000003	60.481000000000002	60.500999999999998	60.521000000000001	60.540999999999997	60.561	60.581000000000003	60.600999999999999	60.621000000000002	60.640999999999998	60.661000000000001	60.680999999999997	60.701000000000001	60.720999999999997	60.741	60.761000000000003	60.780999999999999	60.8	60.82	60.841000000000001	60.86	60.88	60.9	60.920999999999999	60.941000000000003	60.960999999999999	60.98	61	61.021000000000001	61.04	61.06	61.08	61.100999999999999	61.121000000000002	61.14	61.16	61.18	61.2	61.22	61.24	61.261000000000003	61.28	61.3	61.32	61.34	61.360999999999997	61.38	61.4	61.42	61.44	61.46	61.48	61.5	61.52	61.54	61.56	61.58	61.6	61.62	61.639000000000003	61.66	61.68	61.7	61.72	61.74	61.76	61.78	61.798999999999999	61.82	61.84	61.86	61.878999999999998	61.899000000000001	61.918999999999997	61.94	61.96	61.98	62	62.02	62.039000000000001	62.06	62.079000000000001	62.1	62.12	62.139000000000003	62.158999999999999	62.18	62.2	62.22	62.238999999999997	62.259	62.279000000000003	62.298999999999999	62.32	62.338999999999999	62.359000000000002	62.378999999999998	62.399000000000001	62.418999999999997	62.439	62.459000000000003	62.48	62.499000000000002	62.518999999999998	62.539000000000001	62.558999999999997	62.579000000000001	62.598999999999997	62.619	62.639000000000003	62.658999999999999	62.679000000000002	62.698999999999998	62.719000000000001	62.738999999999997	62.759	62.779000000000003	62.798999999999999	62.819000000000003	62.838999999999999	62.859000000000002	62.878	62.899000000000001	62.917999999999999	62.938000000000002	62.959000000000003	62.978999999999999	62.999000000000002	63.018000000000001	63.039000000000001	63.058999999999997	63.079000000000001	63.097999999999999	63.119	63.139000000000003	63.158999999999999	63.177999999999997	63.198999999999998	63.219000000000001	63.238	63.258000000000003	63.277999999999999	63.298000000000002	63.319000000000003	63.338999999999999	63.357999999999997	63.378	63.398000000000003	63.417999999999999	63.439	63.459000000000003	63.478000000000002	63.497999999999998	63.518000000000001	63.537999999999997	63.558999999999997	63.578000000000003	63.597999999999999	63.618000000000002	63.637	63.656999999999996	63.677999999999997	63.698	63.718000000000004	63.737000000000002	63.758000000000003	63.777000000000001	63.798000000000002	63.817999999999998	63.838000000000001	63.856999999999999	63.877000000000002	63.898000000000003	63.917000000000002	63.938000000000002	63.957999999999998	63.978000000000002	63.997999999999998	64.018000000000001	64.037999999999997	64.057000000000002	64.076999999999998	64.097999999999999	64.117999999999995	64.138000000000005	64.156999999999996	64.177000000000007	64.197999999999993	64.216999999999999	64.236999999999995	64.257999999999996	64.278000000000006	64.298000000000002	64.316999999999993	64.337000000000003	64.356999999999999	64.376999999999995	64.397000000000006	64.417000000000002	64.436999999999998	64.456999999999994	64.477000000000004	64.497	64.518000000000001	64.537999999999997	64.558000000000007	64.576999999999998	64.596999999999994	64.617000000000004	64.635999999999996	64.656999999999996	64.677000000000007	64.697000000000003	64.716999999999999	64.736999999999995	64.757000000000005	64.777000000000001	64.796999999999997	64.816999999999993	64.837000000000003	64.856999999999999	64.876999999999995	64.897000000000006	64.917000000000002	64.936999999999998	64.956999999999994	64.975999999999999	64.995999999999995	65.016000000000005	65.036000000000001	65.055999999999997	65.076999999999998	65.096999999999994	65.116	65.135999999999996	65.156000000000006	65.176000000000002	65.197000000000003	65.216999999999999	65.236000000000004	65.257000000000005	65.275999999999996	65.296000000000006	65.316000000000003	65.335999999999999	65.355999999999995	65.376999999999995	65.396000000000001	65.415999999999997	65.436000000000007	65.456000000000003	65.475999999999999	65.495999999999995	65.516000000000005	65.536000000000001	65.555999999999997	65.575999999999993	65.596000000000004	65.616	65.637	65.656000000000006	65.676000000000002	65.697000000000003	65.715999999999994	65.736000000000004	65.756	65.775999999999996	65.796000000000006	65.816000000000003	65.835999999999999	65.855999999999995	65.876000000000005	65.896000000000001	65.915999999999997	65.936000000000007	65.954999999999998	65.974999999999994	65.995999999999995	66.016000000000005	66.036000000000001	66.055999999999997	66.075999999999993	66.096000000000004	66.116	66.135999999999996	66.156000000000006	66.176000000000002	66.195999999999998	66.215999999999994	66.234999999999999	66.256	66.275999999999996	66.295000000000002	66.314999999999998	66.335999999999999	66.355000000000004	66.375	66.396000000000001	66.415000000000006	66.435000000000002	66.456000000000003	66.474999999999994	66.495000000000005	66.515000000000001	66.536000000000001	66.555000000000007	66.575999999999993	66.594999999999999	66.614999999999995	66.635999999999996	66.656000000000006	66.674000000000007	66.694999999999993	66.715000000000003	66.734999999999999	66.754999999999995	66.774000000000001	66.793999999999997	66.814999999999998	66.834999999999994	66.855000000000004	66.875	66.894999999999996	66.915000000000006	66.935000000000002	66.954999999999998	66.974999999999994	66.994	67.015000000000001	67.034000000000006	67.054000000000002	67.075000000000003	67.093999999999994	67.114999999999995	67.134	67.153999999999996	67.174999999999997	67.194999999999993	67.213999999999999	67.234999999999999	67.254999999999995	67.274000000000001	67.293999999999997	67.313999999999993	67.334000000000003	67.353999999999999	67.375	67.394000000000005	67.415000000000006	67.435000000000002	67.453999999999994	67.474000000000004	67.494	67.513999999999996	67.534999999999997	67.554000000000002	67.573999999999998	67.593999999999994	67.614000000000004	67.634	67.653999999999996	67.674000000000007	67.694000000000003	67.713999999999999	67.733999999999995	67.754000000000005	67.774000000000001	67.793999999999997	67.813999999999993	67.834000000000003	67.853999999999999	67.873000000000005	67.894000000000005	67.914000000000001	67.933999999999997	67.953999999999994	67.974000000000004	67.994	68.013999999999996	68.034000000000006	68.054000000000002	68.073999999999998	68.093999999999994	68.113	68.134	68.153999999999996	68.174000000000007	68.192999999999998	68.212999999999994	68.233000000000004	68.254000000000005	68.272999999999996	68.293000000000006	68.313999999999993	68.332999999999998	68.352999999999994	68.373999999999995	68.394000000000005	68.412999999999997	68.433000000000007	68.453000000000003	68.472999999999999	68.492999999999995	68.513000000000005	68.534000000000006	68.552999999999997	68.572999999999993	68.593000000000004	68.613	68.634	68.653000000000006	68.673000000000002	68.692999999999998	68.712999999999994	68.733000000000004	68.753	68.772999999999996	68.793000000000006	68.813000000000002	68.832999999999998	68.852999999999994	68.873000000000005	68.893000000000001	68.912999999999997	68.933000000000007	68.953000000000003	68.972999999999999	68.992999999999995	69.013000000000005	69.033000000000001	69.052999999999997	69.072999999999993	69.093000000000004	69.113	69.132999999999996	69.153000000000006	69.173000000000002	69.192999999999998	69.212999999999994	69.233000000000004	69.251999999999995	69.272000000000006	69.292000000000002	69.311999999999998	69.331999999999994	69.352000000000004	69.373000000000005	69.393000000000001	69.412999999999997	69.432000000000002	69.453000000000003	69.472999999999999	69.492999999999995	69.513000000000005	69.531999999999996	69.552000000000007	69.572000000000003	69.591999999999999	69.611999999999995	69.632000000000005	69.652000000000001	69.671999999999997	69.691999999999993	69.712000000000003	69.731999999999999	69.751999999999995	69.772000000000006	69.792000000000002	69.811000000000007	69.831999999999994	69.852000000000004	69.872	69.891999999999996	69.912000000000006	69.932000000000002	69.951999999999998	69.971999999999994	69.992000000000004	70.012	70.031999999999996	70.052000000000007	70.070999999999998	70.091999999999999	70.111999999999995	70.132000000000005	70.152000000000001	70.171999999999997	70.191000000000003	70.212000000000003	70.231999999999999	70.251000000000005	70.272000000000006	70.290999999999997	70.311999999999998	70.331999999999994	70.352000000000004	70.370999999999995	70.391000000000005	70.411000000000001	70.432000000000002	70.451999999999998	70.471999999999994	70.491	70.510999999999996	70.531000000000006	70.552000000000007	70.572000000000003	70.590999999999994	70.611000000000004	70.631	70.650999999999996	70.671999999999997	70.691000000000003	70.710999999999999	70.730999999999995	70.751000000000005	70.771000000000001	70.790999999999997	70.811000000000007	70.831000000000003	70.850999999999999	70.870999999999995	70.891999999999996	70.911000000000001	70.930999999999997	70.950999999999993	70.971000000000004	70.991	71.010999999999996	71.031000000000006	71.051000000000002	71.070999999999998	71.090999999999994	71.111000000000004	71.131	71.150000000000006	71.171000000000006	71.19	71.210999999999999	71.230999999999995	71.251000000000005	71.27	71.290000000000006	71.311000000000007	71.331000000000003	71.350999999999999	71.37	71.391000000000005	71.41	71.430999999999997	71.45	71.47	71.491	71.510000000000005	71.53	71.551000000000002	71.569999999999993	71.59	71.61	71.631	71.650999999999996	71.67	71.69	71.709999999999994	71.73	71.75	71.771000000000001	71.790000000000006	71.81	71.83	71.850999999999999	71.87	71.89	71.91	71.930000000000007	71.95	71.97	71.989999999999995	72.010000000000005	72.028999999999996	72.049000000000007	72.069000000000003	72.09	72.11	72.13	72.150000000000006	72.17	72.19	72.209999999999994	72.228999999999999	72.248999999999995	72.27	72.290000000000006	72.308999999999997	72.328999999999994	72.349999999999994	72.37	72.39	72.409000000000006	72.430000000000007	72.45	72.468999999999994	72.489999999999995	72.510000000000005	72.528999999999996	72.549000000000007	72.569000000000003	72.588999999999999	72.61	72.629000000000005	72.649000000000001	72.668999999999997	72.69	72.709000000000003	72.728999999999999	72.748999999999995	72.769000000000005	72.790000000000006	72.808999999999997	72.828999999999994	72.849000000000004	72.869	72.888999999999996	72.909000000000006	72.929000000000002	72.948999999999998	72.968999999999994	72.989000000000004	73.009	73.028999999999996	73.049000000000007	73.069000000000003	73.088999999999999	73.108999999999995	73.129000000000005	73.149000000000001	73.168999999999997	73.188999999999993	73.207999999999998	73.227999999999994	73.248999999999995	73.269000000000005	73.289000000000001	73.308000000000007	73.328000000000003	73.347999999999999	73.369	73.388999999999996	73.409000000000006	73.427999999999997	73.447999999999993	73.468000000000004	73.489000000000004	73.509	73.528999999999996	73.548000000000002	73.567999999999998	73.588999999999999	73.608000000000004	73.628	73.647999999999996	73.668999999999997	73.688999999999993	73.707999999999998	73.727999999999994	73.748000000000005	73.768000000000001	73.787999999999997	73.808000000000007	73.828000000000003	73.847999999999999	73.867999999999995	73.888000000000005	73.908000000000001	73.927999999999997	73.947999999999993	73.968000000000004	73.988	74.007999999999996	74.028000000000006	74.048000000000002	74.067999999999998	74.087999999999994	74.108000000000004	74.128	74.147999999999996	74.168000000000006	74.186999999999998	74.207999999999998	74.227999999999994	74.248000000000005	74.266999999999996	74.287999999999997	74.307000000000002	74.328000000000003	74.347999999999999	74.367999999999995	74.387	74.406999999999996	74.427999999999997	74.447000000000003	74.468000000000004	74.486999999999995	74.507999999999996	74.527000000000001	74.548000000000002	74.567999999999998	74.587999999999994	74.606999999999999	74.626999999999995	74.647000000000006	74.667000000000002	74.688000000000002	74.707999999999998	74.727000000000004	74.747	74.766999999999996	74.787000000000006	74.807000000000002	74.826999999999998	74.846999999999994	74.867999999999995	74.887	74.906999999999996	74.927000000000007	74.947000000000003	74.966999999999999	74.988	75.007000000000005	75.027000000000001	75.046999999999997	75.066999999999993	75.087000000000003	75.106999999999999	75.126999999999995	75.146000000000001	75.167000000000002	75.186999999999998	75.206999999999994	75.227000000000004	75.247	75.266999999999996	75.287000000000006	75.307000000000002	75.326999999999998	75.346999999999994	75.367000000000004	75.387	75.406000000000006	75.427000000000007	75.447000000000003	75.465999999999994	75.486000000000004	75.507000000000005	75.527000000000001	75.546999999999997	75.566000000000003	75.587000000000003	75.606999999999999	75.626999999999995	75.646000000000001	75.665999999999997	75.686000000000007	75.706000000000003	75.725999999999999	75.745999999999995	75.766000000000005	75.786000000000001	75.805999999999997	75.825999999999993	75.846999999999994	75.866	75.885999999999996	75.906000000000006	75.927000000000007	75.945999999999998	75.965999999999994	75.986000000000004	76.006	76.025999999999996	76.046000000000006	76.066000000000003	76.087000000000003	76.105999999999995	76.126000000000005	76.146000000000001	76.165999999999997	76.185000000000002	76.206000000000003	76.224999999999994	76.245999999999995	76.266000000000005	76.286000000000001	76.305999999999997	76.325999999999993	76.346000000000004	76.366	76.385000000000005	76.405000000000001	76.424999999999997	76.445999999999998	76.465000000000003	76.486000000000004	76.506	76.525999999999996	76.545000000000002	76.564999999999998	76.585999999999999	76.605999999999995	76.625	76.646000000000001	76.665000000000006	76.685000000000002	76.704999999999998	76.724999999999994	76.745000000000005	76.765000000000001	76.786000000000001	76.805000000000007	76.825000000000003	76.844999999999999	76.864999999999995	76.885999999999996	76.905000000000001	76.924999999999997	76.944999999999993	76.965000000000003	76.984999999999999	77.004999999999995	77.025000000000006	77.045000000000002	77.064999999999998	77.084999999999994	77.105000000000004	77.125	77.146000000000001	77.165000000000006	77.185000000000002	77.204999999999998	77.224999999999994	77.245000000000005	77.265000000000001	77.284999999999997	77.304000000000002	77.325000000000003	77.344999999999999	77.364999999999995	77.385000000000005	77.405000000000001	77.424999999999997	77.444999999999993	77.465000000000003	77.484999999999999	77.504000000000005	77.524000000000001	77.545000000000002	77.564999999999998	77.584999999999994	77.605000000000004	77.625	77.644999999999996	77.664000000000001	77.685000000000002	77.704999999999998	77.724999999999994	77.744	77.763999999999996	77.784999999999997	77.804000000000002	77.825000000000003	77.843999999999994	77.864000000000004	77.884	77.903999999999996	77.924000000000007	77.944000000000003	77.963999999999999	77.983999999999995	78.004000000000005	78.024000000000001	78.043999999999997	78.063999999999993	78.084000000000003	78.103999999999999	78.123999999999995	78.144000000000005	78.164000000000001	78.183999999999997	78.203999999999994	78.224000000000004	78.242999999999995	78.263999999999996	78.284000000000006	78.304000000000002	78.323999999999998	78.343999999999994	78.364000000000004	78.382999999999996	78.403000000000006	78.424000000000007	78.442999999999998	78.462999999999994	78.483000000000004	78.503	78.524000000000001	78.543000000000006	78.563000000000002	78.584000000000003	78.603999999999999	78.623000000000005	78.643000000000001	78.662999999999997	78.683000000000007	78.703000000000003	78.722999999999999	78.742999999999995	78.763000000000005	78.783000000000001	78.802999999999997	78.822999999999993	78.843000000000004	78.863	78.882999999999996	78.903000000000006	78.923000000000002	78.944000000000003	78.962999999999994	78.983000000000004	79.004000000000005	79.022999999999996	79.043000000000006	79.063999999999993	79.082999999999998	79.103999999999999	79.123000000000005	79.143000000000001	79.162999999999997	79.183000000000007	79.203000000000003	79.222999999999999	79.242999999999995	79.263000000000005	79.283000000000001	79.302999999999997	79.322000000000003	79.343000000000004	79.363	79.382999999999996	79.403000000000006	79.423000000000002	79.441999999999993	79.462000000000003	79.481999999999999	79.501999999999995	79.522999999999996	79.543000000000006	79.563000000000002	79.581999999999994	79.602999999999994	79.623000000000005	79.641999999999996	79.662999999999997	79.683000000000007	79.701999999999998	79.721999999999994	79.742000000000004	79.763000000000005	79.783000000000001	79.802999999999997	79.822000000000003	79.841999999999999	79.861999999999995	79.882999999999996	79.903000000000006	79.921999999999997	79.941999999999993	79.962999999999994	79.981999999999999	80.001999999999995	80.022000000000006	80.042000000000002	80.061999999999998	80.081999999999994	80.102000000000004	80.122	80.141999999999996	80.162999999999997	80.182000000000002	80.201999999999998	80.221999999999994	80.242000000000004	80.262	80.281999999999996	80.302000000000007	80.322000000000003	80.340999999999994	80.361999999999995	80.382000000000005	80.402000000000001	80.421999999999997	80.441999999999993	80.462000000000003	80.480999999999995	80.501999999999995	80.521000000000001	80.540999999999997	80.561000000000007	80.581999999999994	80.602000000000004	80.620999999999995	80.641999999999996	80.662000000000006	80.682000000000002	80.700999999999993	80.721999999999994	80.741	80.760999999999996	80.781000000000006	80.802000000000007	80.822000000000003	80.840999999999994	80.861000000000004	80.882000000000005	80.900999999999996	80.921000000000006	80.941000000000003	80.962000000000003	80.981999999999999	81.001999999999995	81.021000000000001	81.040999999999997	81.061999999999998	81.081000000000003	81.100999999999999	81.122	81.141000000000005	81.161000000000001	81.180999999999997	81.201999999999998	81.221000000000004	81.241	81.260999999999996	81.281000000000006	81.3	81.320999999999998	81.340999999999994	81.361000000000004	81.381	81.400999999999996	81.421000000000006	81.441000000000003	81.460999999999999	81.480999999999995	81.501000000000005	81.52	81.540000000000006	81.561000000000007	81.581000000000003	81.599999999999994	81.620999999999995	81.64	81.661000000000001	81.680999999999997	81.700999999999993	81.721000000000004	81.739999999999995	81.760999999999996	81.781000000000006	81.8	81.819999999999993	81.84	81.86	81.88	81.900999999999996	81.92	81.94	81.96	81.98	82	82.021000000000001	82.04	82.06	82.08	82.100999999999999	82.12	82.14	82.16	82.18	82.2	82.22	82.24	82.26	82.278999999999996	82.299000000000007	82.32	82.338999999999999	82.36	82.38	82.4	82.42	82.44	82.46	82.48	82.5	82.52	82.54	82.56	82.578999999999994	82.599000000000004	82.619	82.64	82.66	82.68	82.698999999999998	82.718999999999994	82.74	82.76	82.778999999999996	82.8	82.819000000000003	82.84	82.858999999999995	82.88	82.9	82.92	82.938999999999993	82.959000000000003	82.978999999999999	82.998999999999995	83.019000000000005	83.04	83.058999999999997	83.078999999999994	83.099000000000004	83.119	83.138999999999996	83.159000000000006	83.179000000000002	83.198999999999998	83.218999999999994	83.24	83.259	83.278999999999996	83.3	83.319000000000003	83.338999999999999	83.358000000000004	83.379000000000005	83.399000000000001	83.418999999999997	83.438999999999993	83.459000000000003	83.478999999999999	83.498000000000005	83.519000000000005	83.539000000000001	83.558999999999997	83.578999999999994	83.597999999999999	83.617999999999995	83.638000000000005	83.659000000000006	83.679000000000002	83.698999999999998	83.718000000000004	83.738	83.759	83.778999999999996	83.799000000000007	83.817999999999998	83.837999999999994	83.858000000000004	83.879000000000005	83.897999999999996	83.918000000000006	83.938000000000002	83.957999999999998	83.977999999999994	83.998999999999995	84.018000000000001	84.037999999999997	84.058000000000007	84.078000000000003	84.097999999999999	84.117999999999995	84.138000000000005	84.158000000000001	84.177999999999997	84.197999999999993	84.218000000000004	84.238	84.257999999999996	84.278000000000006	84.298000000000002	84.317999999999998	84.337999999999994	84.358000000000004	84.378	84.397999999999996	84.418000000000006	84.438000000000002	84.457999999999998	84.477999999999994	84.498000000000005	84.518000000000001	84.537999999999997	84.558000000000007	84.578000000000003	84.597999999999999	84.617000000000004	84.637	84.658000000000001	84.677000000000007	84.697000000000003	84.718000000000004	84.738	84.757999999999996	84.777000000000001	84.796999999999997	84.817999999999998	84.837999999999994	84.856999999999999	84.876999999999995	84.897000000000006	84.918000000000006	84.938000000000002	84.956999999999994	84.977000000000004	84.997	85.016999999999996	85.037000000000006	85.057000000000002	85.076999999999998	85.096999999999994	85.117999999999995	85.138000000000005	85.156999999999996	85.177000000000007	85.197000000000003	85.216999999999999	85.236999999999995	85.257000000000005	85.277000000000001	85.296999999999997	85.316999999999993	85.337000000000003	85.356999999999999	85.376999999999995	85.397000000000006	85.417000000000002	85.436999999999998	85.456999999999994	85.477000000000004	85.497	85.516999999999996	85.537000000000006	85.557000000000002	85.575999999999993	85.596000000000004	85.617000000000004	85.637	85.656999999999996	85.677000000000007	85.697000000000003	85.715999999999994	85.736999999999995	85.757000000000005	85.777000000000001	85.796000000000006	85.816999999999993	85.837000000000003	85.855999999999995	85.876999999999995	85.897000000000006	85.915999999999997	85.936999999999998	85.956999999999994	85.975999999999999	85.995999999999995	86.016000000000005	86.036000000000001	86.057000000000002	86.075999999999993	86.096000000000004	86.116	86.135999999999996	86.156000000000006	86.176000000000002	86.195999999999998	86.216999999999999	86.236000000000004	86.256	86.275999999999996	86.296000000000006	86.316000000000003	86.335999999999999	86.355999999999995	86.375	86.394999999999996	86.415999999999997	86.436000000000007	86.456000000000003	86.475999999999999	86.495999999999995	86.516000000000005	86.536000000000001	86.555999999999997	86.575999999999993	86.596000000000004	86.616	86.635999999999996	86.655000000000001	86.676000000000002	86.694999999999993	86.715999999999994	86.736000000000004	86.756	86.775000000000006	86.795000000000002	86.816000000000003	86.835999999999999	86.855999999999995	86.875	86.896000000000001	86.915000000000006	86.935000000000002	86.954999999999998	86.975999999999999	86.995000000000005	87.015000000000001	87.034999999999997	87.055000000000007	87.075000000000003	87.094999999999999	87.114999999999995	87.135999999999996	87.155000000000001	87.176000000000002	87.194999999999993	87.215000000000003	87.234999999999999	87.254999999999995	87.275000000000006	87.295000000000002	87.314999999999998	87.335999999999999	87.355000000000004	87.375	87.394999999999996	87.415000000000006	87.435000000000002	87.454999999999998	87.474999999999994	87.494	87.513999999999996	87.534000000000006	87.555000000000007	87.575000000000003	87.593999999999994	87.614999999999995	87.635000000000005	87.655000000000001	87.674000000000007	87.694999999999993	87.715000000000003	87.733999999999995	87.754999999999995	87.775000000000006	87.793999999999997	87.814999999999998	87.834999999999994	87.853999999999999	87.873999999999995	87.894000000000005	87.915000000000006	87.933999999999997	87.954999999999998	87.974000000000004	87.994	88.013999999999996	88.034999999999997	88.054000000000002	88.075000000000003	88.093999999999994	88.114000000000004	88.134	88.155000000000001	88.174000000000007	88.194000000000003	88.215000000000003	88.233999999999995	88.254000000000005	88.274000000000001	88.293999999999997	88.313999999999993	88.334000000000003	88.353999999999999	88.373999999999995	88.394999999999996	88.414000000000001	88.433999999999997	88.453999999999994	88.474000000000004	88.494	88.513999999999996	88.534000000000006	88.554000000000002	88.573999999999998	88.593000000000004	88.614000000000004	88.634	88.653999999999996	88.674000000000007	88.694000000000003	88.713999999999999	88.733999999999995	88.753	88.772999999999996	88.793000000000006	88.813999999999993	88.834000000000003	88.853999999999999	88.873000000000005	88.893000000000001	88.912999999999997	88.933999999999997	88.953999999999994	88.974000000000004	88.992999999999995	89.013000000000005	89.033000000000001	89.052999999999997	89.073999999999998	89.093999999999994	89.113	89.132999999999996	89.153000000000006	89.173000000000002	89.192999999999998	89.212999999999994	89.233000000000004	89.254000000000005	89.272999999999996	89.293000000000006	89.313000000000002	89.332999999999998	89.352999999999994	89.373000000000005	89.393000000000001	89.412999999999997	89.433000000000007	89.453000000000003	89.471999999999994	89.492999999999995	89.513000000000005	89.533000000000001	89.552999999999997	89.572999999999993	89.593000000000004	89.613	89.632000000000005	89.653000000000006	89.673000000000002	89.692999999999998	89.712000000000003	89.731999999999999	89.753	89.772999999999996	89.793000000000006	89.813000000000002	89.831999999999994	89.852000000000004	89.872	89.893000000000001	89.912000000000006	89.932000000000002	89.953000000000003	89.971999999999994	89.992000000000004	90.013000000000005	90.031999999999996	90.052999999999997	90.072000000000003	90.093000000000004	90.111999999999995	90.132000000000005	90.153000000000006	90.173000000000002	90.191999999999993	90.212000000000003	90.231999999999999	90.253	90.272000000000006	90.292000000000002	90.311999999999998	90.331999999999994	90.352000000000004	90.372	90.391999999999996	90.412000000000006	90.432000000000002	90.451999999999998	90.471999999999994	90.492000000000004	90.512	90.531999999999996	90.552000000000007	90.572000000000003	90.591999999999999	90.611999999999995	90.632000000000005	90.652000000000001	90.671999999999997	90.691999999999993	90.712000000000003	90.731999999999999	90.751000000000005	90.772000000000006	90.792000000000002	90.811999999999998	90.831999999999994	90.850999999999999	90.870999999999995	90.891000000000005	90.912000000000006	90.932000000000002	90.950999999999993	90.971999999999994	90.991	91.010999999999996	91.031000000000006	91.052000000000007	91.072000000000003	91.090999999999994	91.111000000000004	91.131	91.152000000000001	91.171000000000006	91.191000000000003	91.212000000000003	91.231999999999999	91.251000000000005	91.271000000000001	91.290999999999997	91.311000000000007	91.331999999999994	91.350999999999999	91.370999999999995	91.391000000000005	91.411000000000001	91.430999999999997	91.450999999999993	91.471000000000004	91.491	91.510999999999996	91.53	91.551000000000002	91.570999999999998	91.590999999999994	91.611000000000004	91.63	91.650999999999996	91.67	91.691000000000003	91.710999999999999	91.730999999999995	91.75	91.771000000000001	91.790999999999997	91.811000000000007	91.831000000000003	91.850999999999999	91.870999999999995	91.891000000000005	91.911000000000001	91.930999999999997	91.950999999999993	91.97	91.991	92.01	92.031000000000006	92.05	92.070999999999998	92.090999999999994	92.11	92.13	92.15	92.17	92.19	92.21	92.23	92.25	92.27	92.29	92.31	92.33	92.35	92.37	92.39	92.41	92.43	92.45	92.47	92.491	92.510999999999996	92.53	92.55	92.569000000000003	92.59	92.61	92.63	92.65	92.67	92.69	92.71	92.73	92.75	92.77	92.79	92.81	92.828999999999994	92.85	92.87	92.89	92.91	92.93	92.948999999999998	92.97	92.989000000000004	93.01	93.028999999999996	93.049000000000007	93.07	93.088999999999999	93.108999999999995	93.13	93.15	93.17	93.188999999999993	93.209000000000003	93.228999999999999	93.248999999999995	93.269000000000005	93.289000000000001	93.308999999999997	93.33	93.349000000000004	93.369	93.388999999999996	93.409000000000006	93.429000000000002	93.448999999999998	93.468999999999994	93.489000000000004	93.509	93.528999999999996	93.549000000000007	93.569000000000003	93.588999999999999	93.608999999999995	93.629000000000005	93.649000000000001	93.668999999999997	93.688999999999993	93.709000000000003	93.728999999999999	93.748999999999995	93.769000000000005	93.789000000000001	93.808999999999997	93.828999999999994	93.847999999999999	93.869	93.888999999999996	93.909000000000006	93.927999999999997	93.948999999999998	93.968999999999994	93.989000000000004	94.009	94.028999999999996	94.049000000000007	94.069000000000003	94.087999999999994	94.108000000000004	94.128	94.147999999999996	94.168999999999997	94.188000000000002	94.209000000000003	94.228999999999999	94.248999999999995	94.268000000000001	94.287999999999997	94.308000000000007	94.328000000000003	94.347999999999999	94.367999999999995	94.388999999999996	94.408000000000001	94.427999999999997	94.447999999999993	94.468000000000004	94.488	94.507999999999996	94.528999999999996	94.549000000000007	94.567999999999998	94.587999999999994	94.608000000000004	94.628	94.647999999999996	94.668000000000006	94.688000000000002	94.707999999999998	94.727000000000004	94.748000000000005	94.768000000000001	94.787999999999997	94.807000000000002	94.826999999999998	94.846999999999994	94.867999999999995	94.888000000000005	94.908000000000001	94.927999999999997	94.947999999999993	94.968000000000004	94.988	95.007999999999996	95.028000000000006	95.048000000000002	95.067999999999998	95.087000000000003	95.108000000000004	95.128	95.147000000000006	95.167000000000002	95.186999999999998	95.206999999999994	95.227000000000004	95.248000000000005	95.266999999999996	95.287999999999997	95.307000000000002	95.326999999999998	95.346999999999994	95.367000000000004	95.387	95.406999999999996	95.427000000000007	95.447000000000003	95.466999999999999	95.486999999999995	95.507000000000005	95.527000000000001	95.546999999999997	95.566999999999993	95.587000000000003	95.606999999999999	95.628	95.647000000000006	95.667000000000002	95.686999999999998	95.706000000000003	95.727000000000004	95.747	95.766999999999996	95.787000000000006	95.807000000000002	95.825999999999993	95.846999999999994	95.866	95.887	95.906999999999996	95.927000000000007	95.947000000000003	95.965999999999994	95.986999999999995	96.007000000000005	96.025999999999996	96.046000000000006	96.066999999999993	96.087000000000003	96.106999999999999	96.126999999999995	96.147000000000006	96.167000000000002	96.186000000000007	96.206000000000003	96.225999999999999	96.245999999999995	96.266000000000005	96.287000000000006	96.305999999999997	96.326999999999998	96.346000000000004	96.366	96.385999999999996	96.406000000000006	96.426000000000002	96.445999999999998	96.465999999999994	96.486000000000004	96.506	96.525999999999996	96.546000000000006	96.566000000000003	96.585999999999999	96.605999999999995	96.626000000000005	96.646000000000001	96.665999999999997	96.686000000000007	96.706000000000003	96.725999999999999	96.745999999999995	96.766000000000005	96.786000000000001	96.805999999999997	96.825999999999993	96.846000000000004	96.866	96.885000000000005	96.905000000000001	96.926000000000002	96.944999999999993	96.965000000000003	96.986000000000004	97.006	97.025999999999996	97.045000000000002	97.064999999999998	97.084999999999994	97.105999999999995	97.126000000000005	97.144999999999996	97.165999999999997	97.186000000000007	97.204999999999998	97.225999999999999	97.245000000000005	97.265000000000001	97.286000000000001	97.305999999999997	97.325999999999993	97.344999999999999	97.364999999999995	97.385000000000005	97.405000000000001	97.424999999999997	97.445999999999998	97.465000000000003	97.484999999999999	97.504999999999995	97.525000000000006	97.545000000000002	97.564999999999998	97.584999999999994	97.605000000000004	97.625	97.644999999999996	97.665000000000006	97.685000000000002	97.704999999999998	97.724999999999994	97.745000000000005	97.765000000000001	97.784999999999997	97.805000000000007	97.825000000000003	97.844999999999999	97.864999999999995	97.885000000000005	97.905000000000001	97.924999999999997	97.944999999999993	97.965000000000003	97.984999999999999	98.004999999999995	98.025000000000006	98.043999999999997	98.064999999999998	98.084999999999994	98.103999999999999	98.125	98.144999999999996	98.165000000000006	98.185000000000002	98.204999999999998	98.224000000000004	98.245000000000005	98.265000000000001	98.284000000000006	98.305000000000007	98.325000000000003	98.343999999999994	98.364999999999995	98.384	98.405000000000001	98.424000000000007	98.444000000000003	98.463999999999999	98.484999999999999	98.504000000000005	98.524000000000001	98.543999999999997	98.563999999999993	98.584999999999994	98.603999999999999	98.625	98.644000000000005	98.664000000000001	98.683000000000007	98.703999999999994	98.724000000000004	98.744	98.763999999999996	98.784000000000006	98.804000000000002	98.823999999999998	98.843999999999994	98.864000000000004	98.884	98.903999999999996	98.924000000000007	98.942999999999998	98.963999999999999	98.983999999999995	99.004000000000005	99.022999999999996	99.043000000000006	99.063000000000002	99.082999999999998	99.102999999999994	99.123999999999995	99.144000000000005	99.164000000000001	99.183999999999997	99.203999999999994	99.222999999999999	99.244	99.263000000000005	99.283000000000001	99.302999999999997	99.323999999999998	99.343000000000004	99.363	99.382999999999996	99.403999999999996	99.424000000000007	99.444000000000003	99.462999999999994	99.483000000000004	99.503	99.522999999999996	99.543000000000006	99.563000000000002	99.584000000000003	99.602999999999994	99.623000000000005	99.643000000000001	99.662999999999997	99.683000000000007	99.703000000000003	99.722999999999999	99.742999999999995	99.763000000000005	99.783000000000001	99.802999999999997	99.822999999999993	99.843000000000004	99.863	99.882999999999996	99.903000000000006	99.923000000000002	99.942999999999998	99.962999999999994	99.983000000000004	100.003	100.023	100.04300000000001	100.062	100.083	100.10299999999999	100.122	100.143	100.163	100.18300000000001	100.202	100.22199999999999	100.242	100.26300000000001	100.283	100.30200000000001	100.32299999999999	100.342	100.36199999999999	100.38200000000001	100.402	100.422	100.44199999999999	100.462	100.482	100.502	100.523	100.542	100.562	100.58199999999999	100.602	100.622	100.643	100.66200000000001	100.68300000000001	100.703	100.72199999999999	100.742	100.762	100.782	100.80200000000001	100.822	100.842	100.86199999999999	100.88200000000001	100.902	100.922	100.94199999999999	100.962	100.982	101.002	101.02200000000001	101.041	101.062	101.081	101.101	101.122	101.142	101.16200000000001	101.182	101.20099999999999	101.221	101.241	101.261	101.282	101.301	101.321	101.342	101.36199999999999	101.38200000000001	101.401	101.42100000000001	101.44199999999999	101.461	101.48099999999999	101.501	101.521	101.541	101.56100000000001	101.581	101.601	101.622	101.642	101.661	101.681	101.70099999999999	101.721	101.741	101.761	101.78100000000001	101.801	101.821	101.84099999999999	101.861	101.881	101.901	101.92100000000001	101.941	101.96	101.98	102.001	102.021	102.041	102.06100000000001	102.081	102.101	102.121	102.14100000000001	102.16	102.181	102.2	102.221	102.241	102.26	102.28100000000001	102.3	102.32	102.34	102.361	102.38	102.401	102.42	102.441	102.46	102.48099999999999	102.501	102.52	102.54	102.56	102.58	102.6	102.62	102.64	102.66	102.68	102.7	102.72	102.74	102.76	102.78	102.8	102.82	102.84	102.86	102.88	102.9	102.92	102.94	102.96	102.98	103	103.02	103.039	103.06	103.08	103.1	103.12	103.14	103.16	103.18	103.2	103.22	103.24	103.26	103.28	103.3	103.32	103.339	103.36	103.38	103.4	103.42	103.43899999999999	103.459	103.479	103.5	103.51900000000001	103.539	103.559	103.57899999999999	103.599	103.619	103.639	103.65900000000001	103.679	103.699	103.72	103.74	103.759	103.779	103.79900000000001	103.819	103.839	103.85899999999999	103.879	103.899	103.919	103.93899999999999	103.959	103.979	103.998	104.01900000000001	104.039	104.059	104.07899999999999	104.099	104.119	104.139	104.158	104.179	104.199	104.21899999999999	104.239	104.259	104.27800000000001	104.298	104.318	104.339	104.35899999999999	104.378	104.399	104.419	104.438	104.458	104.47799999999999	104.498	104.51900000000001	104.539	104.559	104.578	104.598	104.61799999999999	104.639	104.65900000000001	104.679	104.69799999999999	104.718	104.738	104.758	104.77800000000001	104.798	104.818	104.83799999999999	104.858	104.878	104.898	104.91800000000001	104.938	104.958	104.97799999999999	104.998	105.018	105.038	105.05800000000001	105.077	105.098	105.11799999999999	105.137	105.158	105.178	105.19799999999999	105.218	105.238	105.25700000000001	105.27800000000001	105.298	105.318	105.337	105.357	105.377	105.398	105.41800000000001	105.437	105.458	105.477	105.497	105.518	105.53700000000001	105.557	105.577	105.59699999999999	105.617	105.637	105.658	105.67700000000001	105.69799999999999	105.717	105.73699999999999	105.75700000000001	105.777	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	0.85470085470085455	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.1396011396011396	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.4245014245014245	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.7094017094017091	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	1.9943019943019944	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.2792022792022792	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.5641025641025643	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	2.8490028490028489	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.1339031339031336	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.4188034188034182	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.7037037037037037	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	3.9886039886039888	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.2735042735042734	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.5584045584045585	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	4.8433048433048436	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.1282051282051286	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.4131054131054128	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.6980056980056979	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	5.9829059829059821	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.2678062678062672	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.5527065527065522	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	6.8376068376068364	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.1225071225071224	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.4074074074074074	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.6923076923076925	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	7.9772079772079776	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.2621082621082618	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.5470085470085468	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	8.8319088319088319	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.116809116809117	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.4017094017094021	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.6866096866096871	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	9.9715099715099704	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.256410256410257	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.541310541310541	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	10.826210826210826	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.518518518518519	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.373219373219374	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.227920227920229	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.652421652421651	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.367521367521366	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	21.082621082621081	20.7977207977208	20.7977207977208	20.7977207977208	20.7977207977208	20.512820512820515	20.512820512820515	20.512820512820515	20.512820512820515	20.227920227920229	20.227920227920229	20.227920227920229	19.943019943019941	19.943019943019941	19.943019943019941	19.943019943019941	19.658119658119656	19.658119658119656	19.658119658119656	19.658119658119656	19.373219373219374	19.373219373219374	19.373219373219374	19.088319088319089	19.088319088319089	19.088319088319089	19.088319088319089	18.803418803418804	18.803418803418804	18.803418803418804	18.803418803418804	18.518518518518519	18.518518518518519	18.518518518518519	18.233618233618234	18.233618233618234	18.233618233618234	18.233618233618234	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.948717948717949	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.663817663817664	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.378917378917379	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	17.094017094017094	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.809116809116809	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.524216524216524	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	16.239316239316238	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.954415954415955	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.66951566951567	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.384615384615385	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	15.0997150997151	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.814814814814815	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.52991452991453	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	14.245014245014245	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.960113960113958	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.675213675213673	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.390313390313388	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	13.105413105413104	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.820512820512819	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.535612535612534	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	12.250712250712249	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.965811965811964	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.680911680911679	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.396011396011396	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	11.111111111111111	10.826210826210826	10.541310541310541	10.541310541310541	10.256410256410257	9.9715099715099704	9.6866096866096871	9.4017094017094021	9.116809116809117	9.116809116809117	8.8319088319088319	8.5470085470085468	8.2621082621082618	7.9772079772079776	7.9772079772079776	7.6923076923076925	7.4074074074074074	7.1225071225071224	6.8376068376068364	6.2678062678062672	6.2678062678062672	5.6980056980056979	5.4131054131054128	5.1282051282051286	4.8433048433048436	4.5584045584045585	3.9886039886039888	3.7037037037037037	3.4188034188034182	3.1339031339031336	2.5641025641025643	2.2792022792022792	1.7094017094017091	1.4245014245014245	1.1396011396011396	0.56980056980056981	0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	-0.28490028490028491	Time (s)


Stress (MPa)



Carbon N-Woven 1 Stress
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Stress (MPa)



Carbon N-Woven 2 Stress
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Stress (MPa)



Carbon Woven Epoxy 1
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Stress (MPa)



Carbon Woven Epoxy 2
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Stress (MPa)



Carbon Woven Bio 1
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Stress (MPa)



Carbon Woven Bio 2
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Stress (MPa)



Flax Woven Bio 1 Stress
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Stress (MPa)



Flax Woven Bio 2 Stress
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Stress (MPa)



Flax N-Woven Bio 1 Stress
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Stress (MPa)



Flax N-Woven Bio 2 Stress
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Stress ( MPa)



Kevlar Woven 1 Stress
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Stress (MPa)



Kevlar Woven 2 Stress
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Aluminium Metal N/A 120 Yield plateau High stiffness and ductility; baseline control

Carbon Woven (Epoxy) Woven Carbon Epoxy 437 Brittle fracture Sharp failure, high strength and stiffness

Carbon Woven (Bio) Woven Carbon Bio 352 Brittle fracture + fibre bridging Lower stiffness due to bio-resin, slight fibre bridging
Kevlar Woven (Bio) Woven Kevlar Bio 300 Gradual failure with fibre bridging Moderate strength, consistent response

Flax Woven (Bio) Woven Flax Bio 90 Cohesive crack, moderate bridging Good bonding; benefit of woven architecture

Flax Non-Woven (Bio) Non-Woven Flax Bio 50 Tearing and matrix cracking Inconsistent, early failure likely due to voids

Carbon Non-Woven (Bio) Non-Woven Carbon Bio 220 Progressive delamination Gradual rise, indicates internal damage

Hemp Non-Woven (Bio) Non-Woven Hemp Bio 20 Sudden fibre pull-out Very weak; poor alignment and bonding
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energy-intensive fibre

Carbon Woven (Bio)

Moderate — Bio-resin recovery possible

Partially (resin-dependent)

Medium — Bio-resin lowers impact

Kevlar Woven (Bio)

Difficult — Kevlar degradation is complex

Non-biodegradable

Medium — Energy-intensive fibre, bio-resin helps

Flax Woven (Bio) Good — Natural fibre, bio-resin High Low — Natural fibre and bio-resin

Flax Non-Woven (Bio) Moderate — High variability, but bio-based Moderate Low — Fully bio-based

Carbon Non-Woven (Bio) Moderate - Difficult fibre recovery Low Medium — Synthetic fibre

Hemp Non-Woven (Bio) Good — Fully bio-based High Very Low — Fully natural and low energy input
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