## Slide 1: Ordnance, Munitions and Explosives Principles of OME Level 4 ACDA 4019 Propulsion Systems

## Slide 2
Aim: To understand the scientific and thermodynamic principles associated with propellant design and use.
Learning Outcomes: Upon the successful completion of this module, the student should be able to:
Specify the requirements of a propellant;
Recognise the main types of gun and rocket propellant compositions;
Assess the properties of the major propellant types;
Outline the role of some key propellant additives; and
Identify some applications of propellants in gun systems.
Propellants

## Slide 6: Charge Components
COMBUSTIBLE CASE
END CAP
STICK PROPELLANT
IGNITER
PAD
Separate
loading
round
Primer
Fixed
Round
PRIMER
CARTRIDGE CASE
GRANULAR PROPELLANT
WEAR LINER

## Slide 7: Cartridge Cases
Why have cartridge cases?
FOR
  To contain the propellant
    To allow the propelling charge and projectile to be loaded as one ‘Fixed’ round
  To provide environmental protection to the propellant and primer
    To provide obturation
  The composition can be varied to aid wear reduction and extend barrel life
    Can contain anti wear, anti flash and de-coppering packs
Against:
    Added mass
  Metal case remains in chamber after firing and must be disposed of
    Hot components ejected from gun are potentially hazardous
  Brass case manufacture must be closely controlled to provide consistent and effective obturation

## Slide 8: Cartridge Cases
FULLY
COMBUSTIBLE
CASE
BRASS
CARTRIDGE
CASE
STEEL
STUB
CASE
COMBUSTIBLE
CASE
BRASS
STUB
CASE

## Slide 9: Cartridge Cases
Which Case?
FIXED ROUNDS Brass Cased
  Small arms: Medium Cal: Large Cal Tk up to 120mm (low Pressure)
FIXED ROUNDS Brass Stub Cased
  Large cal Tk up to 120mm (low Pressure)
FIXED ROUNDS Steel Stub Cased
  Large cal Tk 105mm to 120mm (High Pressure) and 140mm
SEPARATELY LOADING Brass Cased
  Large cal 105mm Fd
SEPARATELY LOADING Full combustible cased
  Large cal 155mm Fd: 120mm Tk (UK)
SEPARATELY LOADING ‘Bag’ cased
  Large cal 155mm Fd: (US and UK ‘M’ and ‘L’ series)

## Slide 10: Cartridge Cases
The Gun Interface
SELF OBTURATING GUNS
Separately Loading Ammunition
Combustible cased or bag charges

## Slide 11: Cartridge Cases
The Gun Interface
CASE OBTURATING GUNS
Fixed Ammunition
Full or stub brass at low pressure Steel stub at high pressure

## Slide 12: Function of Cartridge Case
cannelure

## Slide 13: Function of Cartridge Case

## Slide 14: Charge Components
CONVENTIONAL ARTILLERY CHARGE SYSTEM - “subtractive” increments
INC 2
INC 1
INC 3
CHARGE 1
IGNITER
CONTAINER
INC
INC
INC
INC
INC
MODULAR CHARGE SYSTEM – “additive” increments
Note - in example shown, each increment contains a central igniter

## Slide 15: Charge M3A1, US 155mm Gun
Charge 2 Increment
Base Charge Increment
Tie Strap
Charge 3 Increment
Charge 4 Increment
Charge 5 Increment
Tie
Igniter Pad
Flash Reducer
Flash Reducer

## Slide 16: SOMCHEM 155 mm Modular Charge System

## Slide 17
L8 Artillery Charge System

## Slide 18: Muzzle Velocity vs Charge/Projectile Mass Ratio
0.0 0.2 0.4 0.6 0.8 1.0 1.2 1.4 1.6 1.8
2000
1500
1000
500
0
Mass Ratio MC/MP
Muzzle Velocity (m s-1)

## Slide 19: Projectile Range
High Angle Coverage of 155 mm Charge System with HE Shell

## Slide 20: Ignition Systems
BASE PAD
CENTRE CORE
Typical Applications –
UK 120mm Tank guns
155mm Artillery (conventional)
Typical Applications –
German 120mm SB Tank gun
155mm Artillery (MCS)
PROPELLANT
IGNITER
IGNITER
PROPELLANT
WHY THESE CONFIGURATIONS?
Granular propellant = centre ignition
Stick propellant = base ignition

## Slide 21: 155mm Ammunition System FH 70
Increment 6
Increment 5
Combustible Sleeve
Igniter Bag
Combustible Charge Bag
Increment 3
Increment 4
Increment 7

## Slide 24
There are 3 key aspects to propellant thermodynamics:
Specific Energy (F)
Calorimetric Value (Q) and Flame Temperature (To)
Oxygen Balance (Ω)
Propellant Thermodynamics

## Slide 25: Partition of Energy

## Slide 26
The chemical energy of the propellant gives an approximate indication of the resulting velocity imparted to the projectile. If the efficiency of the gun is expressed in a simplistic way as 𝜂 then:
where Q is the total chemical energy of the propellant, in Jkg-1, W is the propellant mass in kg, m is the projectile mass in kg, v is the muzzle velocity of the projectile in ms-1
Chemical Energy of Propellants
Note: Q varies by a factor of no more than 1.5 for Infantry / Common User / Artillery
But: the ratio of W:m can vary from 1:50 in pistols cartidges to 1:1 in APFSDS
Notes: The range of velocities required for different kinds of weapon is from about 300-1500 ms-1. The value of Q for various propellants differs by a factor of no more than 1.5 and the same is true for rifled weapons. It follows that the ratio of propellant mass to projectile mass must widely vary. In fact it ranges from 1:50 in pistol cartridges to nearly 1:1 in high-velocity tank gun rounds.

## Slide 27
Worked Example: A 155mm shell (mass 43.2 kg) needs to be fired at 853 m/s to achieve the required range according to tables. A triple-base propellant is to be used, with a calorific value (Q) of 3400 Jg-1 The gun is 34.41% efficient.
What is the required mass of propellant (W)?

## Slide 28
Q can be calculated the same has for high explosives from Hess’ Law:
And the flame temperature (To) as:
Where is the sum of the mean molar heat capacities of the combustion gases at constant volume. For conventional propellants, the value of the expression does not vary greatly, so To is approximately proportional to Q. The value of To is of considerable importance because it plays a large part in determining the characteristic performance of the gun in relation to heat transfer, bore erosion and muzzle flash. Therefore, since To depends on Q it is necessary to understand the way in which this is controlled by the combustion chemistry.
Calorimetric Value and Flame Temperature

## Slide 29
Energetic compounds in gun propellants
Oxygen Balance Ω
CO2 H2O
O2
Notes: All the major ingredients of propellants are essentially organic in nature, and are composed of carbon, hydrogen, nitrogen and oxygen. Thus, the atomic composition of the propellant can, like that of its constituents, be represented by the general formula CaHbNcOd. This implies that 'd’ moles of oxygen atoms are available to oxidise the fuel elements present, namely 'a' moles of carbon atoms and ‘b’ moles of hydrogen atoms, more or less completely to oxides of carbon and to water respectively. The dominant term in the thermochemistry Equation is Hf (products). In fact, if small quantities of methane, ammonia, nitrogen dioxide etc. are ignored, this term comprises:
pHf (CO) + qHf (CO2) + rHf (H2) + sHf (H2O) (liq) + tHf (N2) where p, q, r, s and t are the numbers of moles of CO, CO2, H2, H2O and N2 that
make up the composition of the products. The ratios p:q and r:s vary with propellant composition and are chiefly dependent on the oxygen balance. If the oxygen balance is high, these ratios will be smaller, and vice versa. The heats of formation of CO2 and H2O are considerably higher than those of CO and H2 respectively. Hence a high oxygen content increases the value of Q

## Slide 30
Changing conditions of Pressure and Temperature between ignition and all-burnt
Temperature at which propellant properties change from elastic to brittle
- HTPB (-70oC)
Notes: The shape of the pressure/time curve curve is determined by the way in which the mass rate of burning of the propellant varies under the changing conditions of pressure, temperature, grain size and grain shape which occur in the gun during the time between ignition and the ‘all-burnt’ point. This behaviour, which depends in a complex way on several factors, is called the ‘vivacity’ of the propellant.
A propellant must maintain its elastic properties within the intended operational temperature range. This means that the glass transition temperature of the binder must be lower than the minimum service temperature (usually –40 to –54°C depending on the application) in order to avoid failure of the motor during firing at low temperatures. Cured HTPB has a glass transition temperature of approximately -70°C

## Slide 34
To produce a high primer flame temperature (To)
To produce a flame which radiates thermal energy efficiently
To produce hot particles
To cause a directional flow of hot gases through and around the propellant charge (grain geometry – progressive, neutral, regressive)
Note: primers containing gunpowder and nitrocellulose can achieve Q of 3500 J g-1 and To of 3500K
Requirements of Primer

## Slide 35: Propulsion– Igniter Components
Typical example
4.5” Naval
INTERNAL TO CHARGE
EXTERNAL TO CHARGE
Typical example
UK 120mm tank gun
VENT HOLE
Mouth
Closure
SEAL
LINING
CAP
SECONDARY
IGNITION
MAIN
FILLING
BODY
Charge Components

## Slide 38
Propellant Combustion
Propellant
Burnt
Propellant
Burning
Propellant

## Slide 42
Propellant Geometries
CORD
TUBE
7 HOLE
Surface increases
as propellant burns
Surface decreases
as propellant burns
Surface remains almost constant
as propellant burns

## Slide 43
Before burning
Slivering – towards all-burnt

## Slide 44
Propellant Combustion
Surface  Circumference
2π (2r)
4 x 2 π r
r
2 r
Mass  CSA
π (2r)2
4 x (π r2)
Half propellant web size  Double surface area

## Slide 45
Propellant Combustion
Burning Rate = Coefficient x Pressure
Higher Pressure  Faster Burning Rate
Simple Burning Rate Equation
Beta (β) is the term for the Burn Rate Coefficient
(cm/s)
(MPa)
(cm/s/MPa)

## Slide 46
Propellant Combustion
Higher Pressure
Faster Burning Rate
Higher Pressure gives a Faster Burning Rate ……

## Slide 47
Propellant Combustion
Higher Pressure
Faster Burning Rate
but a Faster Burning Rate generates a higher pressure …….

## Slide 48
Propellant Combustion
Higher Pressure
Faster Burning Rate
which is gives a faster burning rate …..

## Slide 49
Propellant Combustion
Higher Pressure
Faster Burning Rate
Positive feedback system = inherently difficult to control
which is repeated in continuing increasing cycles …..

## Slide 50
Key Messages on Combustion
Rate of combustion depends on surface area
  Small web propellants burn more quickly than large web
  Must not lose control of the propellant surface area
Rate of combustion depends on pressure
Positive feedback system

## Slide 51
Grain shape and ratio of surface area burn
(the form function)
Z = fraction of grain mass burnt at given instant
f = fraction of grain mass remaining
𝜽=form coefficient for grain shape
𝜽=+1
𝜽=0
𝜽=-0.172
𝜽= +ve regressive, 0 neutral, -ve progressive
Notes: The way in which the surface area, and hence the mass burning rate, of a particular shape of grain changes with time during burning can be calculated. The mathematic function that describes the process is called the ‘geometrical form function’. Its standard expression is: z = (1- f) (1 + θf) where z in the fraction of grain mass burnt at a given instant, f is the fraction remaining, at the same instant, of the least original thickness, θ is the ‘form coefficient’ relating to the particular shape of the grain.
The numerical value of θ is positive for a degressive grain, zero for a neutral grain and negative for a progressive grain. Examples are +1 for long cord, zero for long tube and -0.172 for multitubular. Values of θ for other common shapes including slotted tube, ribbon and square flake, depend on the magnitude of their dimensions. Using these standard or calculated values of θ, the values of z for particular shapes of propellant can be calculated. This enables the ballistician to estimate the rate of gas production for any instant during combustion, and hence to predict the shape of the pressure/time curve for the propellant/gun combination. If the values of z are then plotted against the value of the changing surface area, At, at the corresponding instant (expressed as a fraction of the original area Ao) the characteristic burning behaviour of the various shapes is clearly seen. The curve for multitubular propellant does not show the change to degressive burning on slivering because it is based on a theoretical value of θ determined only up to sliver-point.

## Slide 52
Effect of grain shape on performance
𝜽>0
𝜽<0
𝜽=0

## Slide 53
Propellant Configuration - Geometry
More Progressive
Burning
RIBBON
CORD
TUBE
7 HOLE
19 HOLE
SLOTTED
TUBE

## Slide 54
PROJECTILE TRAVEL
PRESSURE
Pressure Distribution
Before projectile starts to move,
pressure is uniform in gun chamber
Burning Propellant
Generates gas
Increases Pressure

## Slide 58
Internal Ballistics –
in-bore pressure vs distance

## Slide 59
Real Propellant Ignition
Igniter Pad
Stick Propellant
Rear of projectile
Vent
Channel

## Slide 60
PRESSURE
1) TVE or Percussion Tube produces flash

## Slide 61
PRESSURE
2) Igniter pad ignites

## Slide 62
PRESSURE
3) Rear part of propellant ignites
Gas flows along chamber

## Slide 63
PRESSURE
4) Propellant ignition continues
Gas flow along chamber

## Slide 64
PRESSURE
5) Pressure front reaches projectile
Gas flow stopped by
stationary projectile

## Slide 65
PRESSURE
6) Front part of propellant starts to burn
Higher pressure → Faster propellant burn rate
→ More gas
→ Higher pressure
Pressure at front of chamber higher than at rear

## Slide 66
PRESSURE
7) Projectile starts to move
Pressure variation at front of chamber is reduced
Gas flows behind projectile

## Slide 67
PRESSURE
8) Projectile continues to move
Pressure variation at front of chamber is damped out

## Slide 68
Granular Propellant in Gun Chamber

## Slide 69
Granular Propellant in Gun Chamber
PRESSURE
Gas flow along chamber
Pressure acts on all individual granules

## Slide 70
Granular Propellant in Gun Chamber
PRESSURE
Gas flow along chamber
likely to move granules

## Slide 71
Granular Propellant in Gun Chamber
Where possible, prefer to ignite granular propellant charges from the centre of the propellant bed

## Slide 74
Importance of Nitrocellulose
The nitration of cellulose with concentrated nitric acid and sulphuric acid;
Provides mechanical strength and resilience during transport, handling and firing;
Provides a degree of choice relating to the amount of explosive energy available since it can be nitrated to differing percentages (up to 14.14%);
% of oxygen linked to % of nitrogen since each N is bonded to 3O.
Negative oxygen balance BUT the higher the % nitrogen, the greater the amount of oxygen to produce combustion gases (higher Q);
Ignition temperature 180oC so sensitive to percussion or electrical discharge so keep wet;
Thermal stability decreases with increasing N content; and
Degrades in long-term storage with loss of nitrate ester groups
Notes: It follows that single-base propellants derived from NC with 13.3 % N will be correspondingly richer in oxygen, and more energetic, than propellants derived from NC of lower N content. In some compositions a compromise requirement is achieved by blending two different grades of nitrocellulose.
In fact, all gun propellants are formulated to be deficient in oxygen and normally have oxygen balance values within the range -20 to -40 %. The reason for this is to ensure that the flame temperature is not too high, as it would be if the propellant had a zero oxygen balance, and that not too much hydrogen gas is produced, thereby increasing both flash and barrel erosion.
Of the three traditional basic ingredients of gun propellants, NC and NQ are heavily oxygen-deficient but NG has a slightly positive oxygen balance. The oxygen balance of double- and triple-base propellants is therefore very sensitive to the percentage of NG present and the adjustment of this percentage provides a second way of obtaining the required oxygen balance. An example of this can be seen with propellant types cordite-N and NQ. A difference of 2 % in the NG content causes a difference of 15 % in the respective calorimetric values.

## Slide 75
Ignition temperature reduces

## Slide 79
Single Base Propellants
A propellant in which NC is the only explosive ingredient is called a single-base type. These are employed in all kinds of guns from pistols to artillery weapons. Their heat of explosion (Q) is generally between 3100 J g-1 and 3700 J g-1. It should be noted that energy values of propellants are quoted on the conventional assumption that the water formed on combustion is in the liquid phase, unlike the case of high explosives. The water is in fact gaseous, and the difference in the calculated value of Q is of the order of 10 % higher for water gaseous (w.g) than for water liquid (w.l)

## Slide 81
Double Base Propellants
Double-base propellants contain NG in addition to NC. They are more energetic than single-base propellants, having Q values between 4300 J g-1 and 5200 J g-1 depending on the proportion of NG present. The percentage of NG is much lower than when double-base propellants were first introduced in the late nineteenth century, due to the erosive effect of 'hot' propellants.
Remember high value of Q and therefore To

## Slide 84
Triple Base Propellants
Triple-base propellants were developed between the World Wars to render gun positions less easy to locate during night firing. These contain NC and NG, as well as, up to about 55 % w/w, NQ. NQ, which has the pseudonym Picrite, is a white, finely divided crystalline solid, and was mixed with the NC/NG gel to form a particulate suspension. The old triple-base propellants have Q values similar to single-base, ranging from 3200 J g-1 to 3700 J g-1. The use of triple-base propellants has traditionally been restricted to the larger types of gun, where the production of minimal gun-flash, is of most value.

## Slide 86
High Energy Gun Propellants
The ideal properties required of a propellant have been enumerated previously in this chapter. Since World War II, when RDX was successfully used as a high explosive, much research has been conducted into the incorporation of this compound in gun propellants, to make them approximate more closely to the ideals.
Like NQ, which had been incorporated in gun propellants before World War II, RDX is a nitramine explosive, but its thermochemical properties are considerably different and, from certain points of view, better for propellant use.

## Slide 92
Propellant Additives

## Slide 93
Nitrocellulose and nitro-glycerine are nitrate esters and decompose slowly at normal temperatures to form oxides of nitrogen, mainly nitrogen dioxide (NO2). If these oxides are not chemically removed from the system as they are formed, they catalyse further decomposition, eventually leading to auto ignition and shortening the storage life of the propellant. The desirable properties of such a stabiliser are as follows:
Capacity to absorb oxides of nitrogen;
Ability to neutralise acids;
Ability to dissolve in the propellant matrix; and
Inertness to NC or NG before and after reaction with the decomposition products
Stabilisers
Notes: NC in all types of conventional gun propellant undergoes slow degradation at normal propellant storage temperatures as a result of the loss of nitrate ester groups. Such reactions lead ultimately to stabiliser depletion (see below) and hence to autocatalytic decomposition and potential auto ignition of the propellant. The onset of autocatalysis therefore defines the "chemical safe life" of the propellant but before this is reached the NC will have degraded to a point where both the ballistic and the mechanical performance of the propellant are severely compromised. The shelf life is therefore more usually determined not by stabiliser depletion but by the deterioration of physico-mechanical properties or ballistic performance which can render the propellant unsafe to handle or unreliable in use. "Physico-mechanical life" is strongly influenced by the degradation of NC, the reduction in its average molecular weight causing increased grain brittleness. The "ballistic life" of a propellant is also affected by the reduction in NC molecular weight with age but other factors such as surface moderant migration and changes in volatile content are often more important in this case.
The one additive common to all conventional gun propellants is the stabiliser. NC and NG are nitrate esters and decompose slowly at normal temperatures to form oxides of nitrogen, mainly nitrogen dioxide, NO2. If these oxides are not chemically removed from the system as they are formed they catalyse further decomposition, eventually leading to the shortening of storage life of the propellant and in extremis to auto ignition.

## Slide 94
Notes: The natural decomposition process is shown in Figure 12-3 as NO2 and then the acidic HNO2 are formed. If there was no stabiliser present the HNO2 would react with NC causing further decomposition leading to more acid and a more rapid decomposition (autocatalytic process). The stabiliser reacts with the HNO2 as it forms and prevents further reaction with the NC. Therefore during the life of the propellant the stabiliser content will decrease and finally to a level where autocatalytic reaction will occur

## Slide 96
Stability and Storage

## Slide 97
Requirements of a Stabiliser

## Slide 99
Notes: A coolant, in this connection is a substance that absorbs heat when it decomposes during combustion. The original stabiliser, mineral jelly, doubled in this role and so does carbamite. Dinitrotoluene represents 10% by mass of the artillery propellants NH and FNH and this accounts for the conveniently low flame temperatures of these compositions. Dinitrotoluene also imparts a moisture-repellent quality to propellants. The liquid plasticisers such as dibutyl phthalate, diethyl phthalate and glycerol triacetate double as coolants and are sometimes referred to as coolant-plasticisers.

## Slide 100
In a large gun the driving band of the shell becomes partially molten during its passage along the bore and leaves a deposit of copper there. If this deposit is allowed to accumulate it eventually affects the ballistic performance of the gun. To counter this a de-coppering agent is used with the propellant. This can be done in one of two ways. Firstly, the propellant composition can contain compounds of lead or tin, or secondly a piece of lead or tin foil can be juxtaposed to the propellant in the cartridge. In either case the metallic element combines with the copper deposit and forms a brittle alloy, which is removed by friction when the next projectile is fired.
De-coppering Agents

## Slide 101
Flash Inhibitors
The flash from a gun can be regarded as comprising two portions:
Muzzle glow - red in colour and probably due to incandescent particles in the hot gases from the propellant.
Secondary flash - a much larger flame, usually of considerable light intensity, occurring for some distance in front of the muzzle. This is due to the burning of the gases hydrogen and carbon monoxide after admixture with oxygen from the air.
Flash can be reduced by addition of metallic salts, especially by those of potassium, such as potassium sulphate or nitrate, and potassium cryolite. Sodium cryolite can also be used. However………..
Notes: The predominant mechanism of the reaction is probably the breaking of one of the chain reactions that occur in the oxidation of hydrogen, by radical removal processes. This theory is supported by the fact that potassium hydroxide, which is formed from the original potassium salt additive under the influence of the high in bore temperature, has been found to be a more effective flash-inhibiting additive than any potassium salt. Another mechanism for the reduction of muzzle flash by potassium salts is the inhibition of the water-gas shift reaction (CO + H2O ↔ CO2 + H2) that normally occurs as the propellant gases cool producing flammable hydrogen. However, the addition of such salts may increase the amount of smoke. Another method is to decrease the calorimetric value of the propellant by the addition of coolants such as dinitrotoluene. Experiments have shown that the gases from the ‘cooler’ propellants contain more methane than those from the ‘hotter’ propellants, and methane is less easily flammable than hydrogen. This may explain why the comparatively ‘cool’ single-base propellants (NH and FNH) give relatively little flash although the calculated compositions of their muzzle gases show a greater proportion of CO + H2 than for the ‘hotter’ double-base propellants.

## Slide 102
Flash Inhibitors
Points to remember:
The obvious thought is to make the oxygen balance less negative so that complete combustion occurs within the gun barrel.
This would prevent admixture of hydrogen gas and carbon monoxide with air at muzzle.
BUT, this will increase the amount of H2O and CO2, leading to:
  A higher Flame Temperature (To)
  Increased transfer of heat to barrel
  Increased bore erosion
  Reduced life of gun

## Slide 103: Flash Suppression
5 G6 Guns firing
base bleed rounds at night
Effect varies between -46°C
and + 63°C.
Flash suppression also reduces
muzzle blast overpressure.

## Slide 104
Flash Inhibitors and Anti-Wear Additives

## Slide 105
Possible functions of gun propellant additives

## Slide 106
To summarise, the calorimetric value of a gun propellant composition can be adjusted by:
Varying the nitrogen content, and hence the oxygen content of the universal ingredient NC
Varying the proportion (if any) of NG
Including small amounts of non-explosive additives called coolants
Adjusting the calorimetric value?

## Slide 109
Summary – Gun Propellants
Propellant | Constituent | Q (Jg-1) | Flame Temperature (To) K | Force Constant (Jg-1)
Single Base | NC | 3100 - 3700 | 2500 - 3000 | 920 - 1075
Double Base | NC+NG | 4300 - 5200 | 2600 - 3600 | 1075 - 1175
Triple Base | NC+NG+NQ | 3200 - 3700 | 2400 - 3300 | 1000 - 1100
Multi-Base, High Energy or Nitramine | NC+NG+NQ+RDX (NTO etc) |  | 2900 - 3200 | 1100 - 1250
LOVA | HMX/RDX+Binder+ Plasticiser | 3410 | 2853 | 1100 - 1300
HAN | HAN, Nitrate salt of amine, water |  | 2730 | 970 - 1000

## Slide 110: Case Study - 81 mm Mortar

## Slide 111: 81mm System
Ctg. Primary L33
Ctg. Augmenting L32
160 g NC30
Ctg. Augmenting L34
285 g NC30

## Slide 112: Obturating Ring
Obturating ring in groove
showing scarfed joint
Air flow through windage
Bomb Firing
Gas sealed
Bomb Loading
Operation of obturating ring

## Slide 113: 81mm Primary Cartridge
Small Powder Case
(aluminium alloy)
Connecting Element
(aluminium alloy)
Large Powder Case
(aluminium alloy)
Base
(aluminium alloy)
Primary Cap Carrier
Gun Powder
Percussion Pin
(aluminium alloy)
Flake Propellant
Boxer Primer

## Slide 114: 81mm Augmenting Charge Systems
Monogram of
Filling Factory
Propellant Lot
Number
Celluloid Seal
Celluloid Container
Filling NC30 465 gr
Celluloid Seal
Celluloid Container
Filling NC30 465 gr
Filling NC30 130 gr
L31A1
L32A2

## Slide 115: Rocket Propellants

## Slide 116: General Principles
In a closed pressurized cylinder, gas exerts a pressure, which is equal and opposite in all directions.
If, as in a rocket, an opening is made in one end and pressure maintained by a burning propellant, the pressure at the closed end will be higher than at the open end, and combustion gases will escape through the open end
The effect of the gas escape produces thrust
Acceleration is directly proportional to the rate at which the fuel is burnt
If fuel consumption is constant, the rocket will accelerate as the propellant mass decreases due to burning
The higher the gas velocity the greater the velocity of the rocket.

## Slide 117
General Principles
The basic design of a rocket is as follows:

## Slide 118
Performance Parameters
Rocket Propulsion
  Relies on thrust created by burning propellant
  Overcoming gravity and drag
  Thermal efficiency about 20% (>30% guns)
Calorimetric Value and Gas Production
Thrust and Specific Impulse
Characteristic Velocity
Notes: Rocket propulsion is produced by the reaction of the missile to the thrust created by burning propellant in a combustion chamber or tube. As in the case of gun propellants, only a portion of the heat released by the combustion of the propellant can be converted into useful work, in this instance the acceleration of the rocket and the overcoming of gravity and drag. The remainder of the heat is lost in sensible heat transfer to the hardware, in the residual heat and kinetic energy of the exhaust plume and in the emission of light and sound. The thermal efficiency of the motor is the ratio of useful work output to the chemical energy (heat of combustion, Q), of the propellant(s), and is in the region of 20 % for rockets generally. This percentage increases with the exit velocity of the gases, but is still less than the corresponding figure of >30 % for a typical gun.

## Slide 119
Calorimetric Value for propellant (Qp)
=
Heat of combustion for a gun propellant (Qv)
Calorimetric Value
Notes: The total chemical energy of a rocket propellant, or of a bipropellant combination, is called its heat of combustion or, as for a gun propellant, its calorimetric value. (Strictly, the latter is an experimentally determined value). It is designated Qp, the p denoting that the value is measured under conditions of constant pressure as distinct from the (theoretically) constant volume conditions of a gun. Like its gun propellant counterpart Qv, the parameter Qp is measured in kJ kg-1. On combustion of the propellant its whole mass is converted (ideally) into a mixture of gases, each of which has its own characteristic molar mass (or, in older terminology, molecular weight), expressed in grams per mole. For some purposes of thermochemistry, as will be seen later, a ‘mean molar mass' value, designated 𝑀, for a gas mixture is used. This is simply the mass of mixture in grams divided by the number of moles of gas present. 𝑀 is the inverse of the n value more commonly used in connection with gun propellants.

## Slide 120: Specific Impulse
Notes: Rocket propulsion is produced by the reaction to the force exerted on gas molecules to accelerate them though a convergent-divergent nozzle. In a conventional rocket motor both the gases which constitute the working fluid and the heat energy which is partly converted into the kinetic energy of those gases are produced by the burning of a propellant in a combustion chamber. Rocket propellants burn at an approximately constant pressure which is considerably lower than the peak pressure observed in guns. The thrust of a rocket motor can be controlled in various ways but the total impulse (thrust x time) provided by unit mass of propellant in a given motor has a definite value, known as the Specific Impulse.

## Slide 121
Specific Impulse
Notes: One of the internal forces (𝐹 ) in a motor is that acting over the nozzle exit plane 1 (𝐴 ) which is subject to a pressure 𝑃 , from inside the motor. Since force = pressure × area, therefore, 𝑭𝟏 = 𝑷𝒆𝑨𝒆
In addition there is a significant internal force (𝐹 ) resulting from the change in momentum of the combustion products as they pass through the nozzle exit plane at a velocity 𝑣𝑒 which is assumed to be constant. If the mass of the combustion gases passing through in the time interval (𝑑𝑡) is 𝑚̇, then this momentum change is given by F2.
There is also an external force (F3) which acts over the nozzle exit area (𝐴𝑒) from outside the rocket where the pressure is the ambient pressure (𝑃 ). This force is opposed to the internal forces, therefore, 𝐹3 = −𝑃a𝐴𝑒
It is the reaction to the sum of these three principal forces which provides the propulsion of a rocket. The total force (𝐹𝑇), called the thrust of the rocket motor, is therefore given by:
𝐹 = 𝑚̇ 𝑣e + 𝐴e (𝑃e − 𝑃a )
The thrust of a rocket motor can be controlled in various ways, but the total impulse (thrust × time) provided by unit mass of propellant in a given motor has a finite value, known as the specific impulse (𝐼𝑠). This parameter is used to assess the performance of a rocket motor, and it is defined as the thrust per unit mass flow rate through the nozzle.

## Slide 122: Rocket Motor Grain Shapes and Burning Profiles

## Slide 123: Rocket Motor Boost and Sustain Profiles

## Slide 124
An acceptable high energy / bulk ratio (F)
A predictable burning rate over a wide range of pressures (Vieille’s Law)
An acceptably low flame temperature (To)
Capable of being easily and rapidly ignited
An acceptably low sensitiveness to other forms of ignition
Capable of cheap, easy and rapid manufacture
Long shelf life under all environmental conditions (degradation)
Minimum tendency to produce flash / smoke and toxic fumes
Summary – Propellants