Lv.5 Advanced CHEMISTY – ACDA6020, PRESENTATION

BEN LLOYD - 2219811

AGEING OF POLYMER BONDED EXPLOSIVES (PBXs)

- Abstract

Polymer Bonded Explosives (PBXs) are extremely common in OME for a variety of reasons; they show excellent resistance to physical shock, Electro-Static Discharge (ESD), friction and can remain functional after decades of long-term storage. However, this does not mean they are immune to the passage of time; they are still subject to ageing throughout their lifecycle like another explosive. Older PBXs can suffer a multitude of Functional Failure Modes (FFMs), which are Mitigated by the inclusion of certain ingredients within a PBX mixture. This data, along with which Tests may be performed to monitor the integrity of the Energetic Material (EM), was identified and presented to an audience. This report serves as a summary of this learning and shows how understanding the ageing of PBXs contributes to the wider context of OME Safety Management.

Table Of Contents

- Abstract (Page 1)

- Introduction (Page 1  – Page 2)

- Researched Topics – Functional Failure Modes (Page 2 – Page 3)

- Researched Topics – Tests (Page 3 – Page 4)

  - Figure 1 – Arrhenius Equation

- Conclusion (Page 4 – Page 5)

- References & Appendices (Page 7 - Page 16)

- Introduction

PBXs are popular for EM fillings in modern munitions for the aforementioned reasons listed in Para i, it is therefore unsurprising that their use has become the defacto standard across NATO nations. In basic terms, a PBX consists of two components; the EM and a Binder, the EM is the “raw” explosive content of the PBX and is usually a high-energy Secondary explosive such as RDX or HMX due to strong compatibility with Binders and relative low cost. Binders are long-chain Hydrocarbons that envelop the explosive, acting as a barrier between it and outside stimuli that may lead to inadvertent detonation. The example chosen in Appendix C is Hydroxyl Terminated Polybutadiene (HTPB), which is a popular choice for PBX blends for its low cost and ability to retain elastic behaviour even when fully cured. This is useful as PBX blends that use HTPB show excellent resistance to shock as military EM is often subjected to harsh usage environments and this resistance enhances the insensitiveness of the EM [11].

To understand how PBXs age, the Ministry of Defence’s Standardisation Database (STANMIS) was consulted for information, STANMIS highlighted a number of NATO Standardisation Agreements (STANAGs) that informs member nations on how to comply with NATO Insensitive Munitions (IM) policy, chief among these was STANAG 4666 [25] which details methods to test the integrity of PBXs in service. The reference table found in STANAG 4666, as seen in Appendix M, listed potential FFMs that may be found within a PBX, how these manifest in reality and what tests may be carried out to monitor the condition of the tested PBX.

- Researched Topics – Functional Failure Modes

STANAG 4666 listed a number of detrimental effects that an EM may suffer, the refence table in Appendix M notes four main mechanisms of damage within a PBX composition: Dewetting, Plasticiser Migration,  Oxidative Cross-link and Chainscission.

Dewetting occurs when, through absorption of moisture and excessive heat, the Binder detaches from the explosive, leaving voids where the Binder used to be as seen in Appendix P [19]. This is a severe problem as the EM has created its own “Hot Spots”; areas in which gas collects and can be subjected to adiabatic heating when placed under shock. In practice, this manifests as a vast increase to the sensitivity to the EM and should be avoided at all costs. It is for this reason that DSA.03 OME [21] places strong limits on the temperature and humidity that an EM may be stored in.

Plasticisers are included within a PBX mixture to add an additional “layer” of protection to the explosive and provide further improvement to mechanical properties, such as granting an increased shock resistance and therefore provide greater insensitiveness [9].

Excessive temperature can also result in Plasticiser Migration, as the name implies, it refers to the Plasticiser transitioning from being an element in a homogenous mix into a separate component of a heterogenous mix [16] as the Plasticiser gathers on the interior walls of the munition. This is a problem as the EM is no longer receiving the benefit of the Plasticiser, resulting in higher sensitivity and thus, a greater chance of inadvertent detonation. As a counter to this, Plasticisers with a high Molecular Weight should be used. The larger molecules will be less able to travel the gaps between atoms and thus slow down the rate of migration [24].

Also listed in the reference chart is Oxidative Cross-Link and Chainscission. These two as the opposites of one another, Oxidative Cross-Link as shown in Appendix F refers to unintended bonds being formed between molecules while Chainscission refers to bonds being broken apart.

Oxidative Cross-Link occurs when the EM is subjected to an overly hot and moist environment. This results in the Molecular Weight of the EM increasing, with the EM becoming harder in the process, this is also to be avoided as the PBX has a tendency to crack as seen in Appendix F. This is of particular concern in Rocket Motors as the desired behaviour of consistent fuel burn can easily transition into a Detonation, potentially placing lives at risk if undetected. It is for this reason Anti-Oxidants are included within a PBX mix to prevent this from happening. A02246 identified in Appendix F is a popular choice for PBX blends for it’s low cost and ability to share an OH bond with HTPB, resulting in a better homogeneity within the EM [18].

Chainscission can also occur when the EM is incorrectly stored, particularly in high-humidity conditions. As previously stated, bonds between molecules are broken apart and this results in a drastically lower Molecular Weight. This manifests as a softening of the EM, in extreme cases this results in the PBX crumbling to a dust-like consistency in an effect known as Chalking [6]. In such cases, the EM becomes completely unusable as consistent performance cannot be guaranteed and thus people may be unnecessarily placed in harm’s way, massively increasing the probability of an OME Accident.

These damage mechanisms highlights just how crucial correct storage procedures are to maintain the integrity of the PBX as allowing the temperature and / or humidity of an Explosive Storehouse (ES) to exceed the set limits of DSA.03 OME increases the risk of any of the FFMs to occur, thus increasing the sensitivity of the EM to unsafe levels, placing lives at an unnecessary level of Risk and in extreme cases, may cause lives to be lost.

- Researched Topics – Tests

While the previously mentioned FFMs are a serious threat to Safety, they may also be deliberately inducted to understand how a PBX behaves over time in  a process called Accelerated Ageing. As stated in Appendix K, the EM is placed into an oven and “cooked” to simulate the passage of time. Understanding the behaviour of PBX ageing is critical for long-term OME Safety Management; recognising the effects of various FFMs as well as being able to test for these damage mechanisms allows governments to monitor the overall condition of the EM. This in turn provides trend data; governing authorities can make more accurate hypotheses on how the PBX will age over time; this is especially important as munitions are expected to have service lives multiple decades long.

However, this process is not perfect; as each ingredient within a PBX has its own Arrenhius Constant value, denoted by A in Figure 1, it can be extremely difficult to create a definitive K value for the entire PBX, thus the answer obtained may not be accurate to reality. However, Accelerated Ageing is still a useful tool to give a general overview of the EM’s ageing behaviour.

STANAG 4666 contains a comprehensive testing regimen for PBXs in service intended to address all of the FFMs outlined in Appendix M, three of these were chosen as examples. The Compression test outlined in Appendix N is used to determine if Chainscission or Oxidative Cross-Linking has occurred; the sample is soaked in Toluene to improve pliability and placed under increasing increments of pressure. The level of material deflection is compared to the deflection of a fresh sample. This can show how the material has changed; less deflection than expected shows that Oxidative Cross-Linking has occurred as the EM has hardened, a large degree of deflection notes that the EM has softened, showing that  Chainscission has taken place. The degree of deflection indicates how severe the damage is [22] [23].

To test for the integrity of the Plasticiser, Gas Chromatography is used. The sample is dissolved in Acetone and vaporised. The Gas Chromatographer then separates the PBX into its constituent ingredients and the quantities of each are compared to a fresh sample. This is useful as not only can the level of remaining plasticiser be obtained, but performing multiple tests over an extended period of time can reveal the rate of Plasticiser depletion and quantities remaining in future can be extrapolated [22] [23].

Dewetting is a major Hazard within PBX blends as already established, testing for this FFM is comparatively simple; the sample can be inspected with a Scanning Electron Microscope. Any voids left behind by Dewetting are immediately obvious as seen in Appendix P, however this only tests for surface-level defects. For a more comprehensive impression of the EM, a sample can be subjected to Computed Tomography, using X-Rays to gain a three-dimensional view of the sample and determine if any Dewetting has occurred beneath the surface [22] [23].

- Conclusions

All of this data is critical to informing the EM’s Safety Argument; the ability to predict whether or not the EM will remain safe to use over the course of it’s service life is critical as changes in the EM can be predicted ahead of time, before the explosive becomes unsafe. Understanding when the EM becomes unusable also influences financial planning, explosives that become unsafe over a short period of time will be more expensive on a long-term basis as constant replacement will be required. The opposite is true; EM that can survive for decades in long-term storage will not need to be replaced as often and therefore will be cheaper throughout the Concept, Assessment, Demonstration, Manufacture, In-Service, Disposal (CADMID) cycle.

- References & Appendices

[1] – C.Williams, 01 April 2015, Weapons Systems Division Defence Science and Technology Organisation Australia, Investigation into the Interaction of Dantocol in Polymer Bonded Explosives and Bonding Agent Development, Accessed 09 January 2026, https://flex.flinders.edu.au/file/7b760c25-12bc-4897-81d6-f841e5b3563b/1/ThesisWilliams2015.pdf

[2] – J.Pietron & P.Mirkarimi, 28 February 2022, Wiley-Verlag Chemie Publishing, Review of the Effects of Polymer Binder Properties on Microstructure and Irreversible Volume Growth of Plastic Bonded Explosives Formulations, Accessed on 10 January 2026,  https://d-nb.info/1258485303/34

[3] – K.Dongwoo & K.Hyejoo, 25 November 2025, Journal of Industrial & Chemical Engineering,  Effect of a polymer binder on the extraction and crystallization-based recovery of HMX from polymer-bonded explosives, Accessed on 10 January 2026, https://www.sciencedirect.com/science/article/abs/pii/S1226086X19303041

[4] – L.Haoying & L.Hong, 16 January 2025, Thermochemica Acta Volume 749, University of Nanjing China, The influence of temperature and humidity on the decomposition of HMX-HTPB polymer-bonded explosives, Accessed 10 January 2025, Accessed on 10 January 2026, https://www.sciencedirect.com/science/article/abs/pii/S0040603125000796#:~:text=Highlights,Introduction

[5] – R.Cammack, 1999, King’s College London, Encyclopaedia of Spectroscopy & Spectrometry,  Accessed 10 January 2026,  https://www.sciencedirect.com/topics/physics-and-astronomy/free-radical

[6] – M.Salazar & J.Kress, December 2019, Polymer Degredation & Stability, Los Alamos National Laboratory New Mexico, Low-temperature oxidative degradation of PBX 9501 and its components determined via molecular weight analysis of the Poly[ester urethane] binder, Accessed 12 January 2026, https://www.sciencedirect.com/science/article/abs/pii/S0141391009002845#:~:text=In%20these%20studies%2C%20the%20sorption,results%20are%20reported%20in%20Ref.

[7] – M.Salazar, 13 September 2006, Fall American Chemical Society National Meeting San Francisco, Aging of PBX 9501: Hydrolysis and Free-Radical Oxidation, Accessed 12 January 2026, https://www.uu.edu/dept/chemistry/salazar/PMSEFallACS06.pdf

[8] – D.Wrobleski & D.Langois, 01 January 2007,  The International Journal for the Science and Technology of Polymers Volume 48, AGING OF THE BINDER IN PLASTIC-BONDED EXPLOSIVE PBX 9501 AND FREE-RADICAL OXIDATION, Accessed 13 January 2026, https://laro.lanl.gov/esploro/outputs/journalArticle/AGING-OF-THE-BINDER-IN-PLASTIC-BONDED/9916364070803761

[9] – G.Yilmaz & Z.Kaya, 23 January 2024, Journal of Applied Polymer Science, Effect of Inert Plasticizers on Mechanical, Thermal, and Sensitivity Properties of Polyurethane-Based Plastic Bonded Explosives, Accessed 15 January 2026, https://www.researchgate.net/publication/262343855_Effect_of_Inert_Plasticizers_on_Mechanical_Thermal_and_Sensitivity_Properties_of_Polyurethane-Based_Plastic_Bonded_Explosives

[10] – T.Riveria & M.Mutaszak, May 1983, Journal of Colloid & Interface Science Volume 93, Surface properties of potential plastic-bonded explosives (PBX), Accessed 16 January 2026, https://www.sciencedirect.com/science/article/abs/pii/0021979783903892

[11] – M.Daniel, December 2006, Weapons Systems Division Defence Science and Technology Organisation Australia, Polyurethane Binder Systems for Polymer Bonded Explosives, Accessed 16 January 2026, https://apps.dtic.mil/sti/pdfs/ADA467800.pdf

[12] – S.Zhiang & Y.Wang, 04 July 2024, Defence Technology Volume 45, KeAi Publishing China, Effects of aging on mechanical sensitivity threshold and thermal decomposition characteristic of RDX/HMX, Accessed 16 January 2026, https://www.sciencedirect.com/science/article/pii/S221491472400254X

[13] – R.Zito, 13 November 2019, Mathematical Foundations of Safety Engineering, Springer Publishing Tucson Arizona, Accelerated Age Testing of Explosives and Propellants, Accessed 17 January 2025, https://link.springer.com/chapter/10.1007/978-3-030-26241-9_16

[14] – B.Vogelsanger, 30 March 2004, Schweizerische Chemische Gesellschaft (Swiss Chemical Society) Volume 58, Chemical Stability, Compatibility and Shelf Life of Explosives, Accessed 18 January 2026,  https://www.chimia.ch/chimia/article/view/2004_401/3154

[15] – X.Liu & Y.Luo, 21 January 2025, Case Studies in Thermal Engineering Volume 72, HTPB propellant aging mechanisms and safety characteristics: microscopic structural changes, thermal stability, and self-accelerating decomposition temperature, Accessed 18 January 2026, https://www.sciencedirect.com/science/article/pii/S2214157X25005556?via%3Dihub

[16] – P.Rae & S.Palmer, 2001, Ageing Studies: Lifetime Extension Materials, St. Catherine's College Oxford, Ageing Effects on the Mechanical Properties of a Polymer Bonded Explosive.

[17] – J.Dou & M.Xu, 19 April 2022, FirePhysChem Volume 3, KeAi Publishing China, Research progress of nitrate ester binders, Accessed 19 January 2026, https://www.sciencedirect.com/science/article/pii/S2667134422000475

[18] – S.Walley, 10 September 2018, The European Physical Journal - Special Topics Volume 227, Temperature and strain rate effects on the mechanical properties of a polymer-bonded explosive, Accessed 19 January 2026, https://link.springer.com/article/10.1140/epjst/e2018-00060-6

[19] – A.Provotas, April 2000, Aeronautical and Maritime Research Laboratory Australia, Energetic Polymers and Plasticisers for Explosive Formulations - A Review of Recent Advances, Accessed 20 January 2026, https://scispace.com/pdf/energetic-polymers-and-plasticisers-for-explosive-2n3jswoa3i.pdf

[20] - V.Komanschek & Q. Axthammer, 13 May 2024, Energetic Materials Technology Working Group Oslo, Characterization and evaluation of alternative plasticizers to mitigate exudation from pressed PBX, Accessed 22 January 2026, https://imemg.org/wp-content/uploads/2024/05/24117_Paper-EMTWG_24117_Plasticizer_Paper-final.pdf

[21] – Defence OME Safety Regulator (DOSR), 19 November 2020, Defence Safety Authority (DSA),  Defence Code of Practice (DCOP) and Guidance Notes for In-Service and Operational Safety Management of OME, Accessed 22 January 2026, https://assets.publishing.service.gov.uk/media/5ee8ccb8e90e070429b2d2fc/DSA_03_OME_PART_2__JSP_482__CH_17__Nov_19__-_mod_gov_uk.pdf

[22] – North Atlantic Treaty Organisation (NATO), 16 November 2016, NATO Standardisation Office (NSO),  STANAG 4666 (EDITION 1) - EXPLOSIVES, ASSESSMENT OF AGEING OF POLYMER BONDED EXPLOSIVES (PBXS) CAST -CURED COMPOSITIONS USING INERT OR ENERGETIC BINDERS

[23] - North Atlantic Treaty Organisation (NATO), 16 November 2016, NATO Standardisation Office (NSO), Allied Ordnance Publication (AOP) 64 - IN-SERVICE SURVEILLANCE OF MUNITIONS CONDITION MONITORING OF ENERGETIC MATERIALS.

[24] - A.Provotas, March 2003, Aeronautical and Maritime Research Laboratory Australia, Formulation and Performance Studies of Polymer Bonded Explosives (PBX) Containing Energetic Binder Systems, Accessed 25 January 2026, https://apps.dtic.mil/sti/tr/pdf/ADA415676.pdf

Appendices

Appendix A – Introduction Slide

Appendix B – Presentation Aims Slide

Appendix C – PBX Introduction Slide

Appendix D – Plasticisers Slide

Appendix E – Anti-Oxidant Slide

Appendix F – Oxidative Cross-Link Slide

Appendix G – Chainscission Slide

Appendix H – Dewetting Slide

Appendix I – Plasticiser Migration Slide

Appendix J – Storage Conditions Slide

Appendix K – Accelerated Ageing Slide

Appendix L – Rowanex 1400 Trial Slide

Appendix M – STANAG 4666 Testing Slide

Appendix N – Oxidative Cross-Link Testing Slide

Appendix O – Plasticiser Depletion Slide

Appendix P – Microscope Inspection Slide

Appendix Q – Lifecycle Slide

Appendix R – Questions Slide