## Slide 1
Aim: To describe the mechanics associated with the penetration of targets by rigid or deforming projectiles.
Learning Outcomes: Upon the successful completion of this lesson, the student should be able to:
Understand the mechanics associated with penetration and perforation; and
Select the appropriate ballistic methodology to overmatch a given target.
Penetration Mechanics

## Slide 2
Penetration Equations (Arrows)

## Slide 3
Bows and Arrows

## Slide 4
Penetration Mechanics
A 0.5 calibre round hitting a steel shelter plate at Pendine Ranges
George Atkins – Apprentice Graduate 2023/24

## Slide 5
Shaped Charge

## Slide 6
Explosively Formed Penetrator

## Slide 7
Sam Darcy-Page

## Slide 10
Long Rod Penetrator

## Slide 11
High Explosive Squash Head
https://www.youtube.com/watch?v=m_LhAveOAgM

## Slide 12
Matthew Satterthwaite

## Slide 15
Penetration Mechanics
Material science of interest
  Stress and Strain
  Definitions
  Failure modes
  Velocity Limit (Vl) and V50
  Oblique penetration
  Sloping armour
Kinetic Energy Projectiles
  Penetration Behaviour
  Hydrodynamics
  Ballistic requirements
Chemical energy defeat of armour
  Shaped charges (HEAT rounds)
  Explosively formed penetrators (EFP)
  High explosive squash heads (HESH)

## Slide 16
Typical tensile test curves for ductile metals
Strain hardening
Notes: The proportional limit is defined as the highest stress at which the stress-strain curve is a straight line. Up until that point the material will return to its original dimensions without permanent deformation

## Slide 18
Toughness – the area under the stress strain curve

## Slide 19
Penetration is defined as an event during which a projectile creates a discontinuity in the original surface of the target.
Perforation requires that, after the projectile or its remnants are removed, light may be seen through the target.
Adiabatic shear is one of the many mechanisms of failure that occur in metals and other materials that are deformed at a high strain rate such as ballistic impact.
Work hardening. The hardness of a projectile can increase during impact. Although the first few deformations imposed on metal by such treatment weakens it, its strength is increased by continued deformations. As stress is exerted, crystalline structures slip across one another, each slippage causing an obstruction to the next.
Definitions
Notes: Adiabatic is a thermodynamic term meaning an absence of heat transfer. Strain rate is the change in deformation over time. It basically means the change in distance of layers of metal over time.

## Slide 20
Typical failure modes on impacted steel plates (Backman and Goldsmith 1978)
Brittle failure – weak low density targets.
Ductile hole growth (piercing) – plastic flow due to adiabatic heating and high strain rate
Radial fracture – tensile strength low, compressive strength high
Plugging – fairly ductile materials -> ballistic limit
Fragmentation – Less ductile targets -> ballistic limit
Petaling – radial stress high, thin targets -> ballistic limit
Spall failure (scabbing) – wave reflections (compressive shock meets reflected shock)
Notes: There are several methods by which a target will fail when subject to an impact. Spalling is very common and a result of wave reflection from the rear face of the plate. It is common for materials stronger in compression. Scabbing is similar to spalling, but the fracture results predominantly from large plate deformation, which begins a crack at a local inhomogeneity (such as an inclusion). Brittle fracture occurs in weak and lower density targets. Radial cracking is common in ceramic type materials where the tensile strength is lower than the compressive strength. Plugging occurs in materials that are fairly ductile and usually when the projectile impact velocity is very close to the ballistic limit. It is due to the formation of adiabatic shear (Zener and Holloman 1944). Petaling occurs when the radial and circumferential stresses are high and the impact velocity of the projectile is close to the ballistic limit.

## Slide 21
Adiabatic shear (<1000ms-1)
On initial impact a local ring of intense shear is generated (microseconds).
The target material is massive and has no time to build up motion.
Locally intense heat is generated
Because of the time scale and high deformation rate, the heat cannot be conducted away.
Since the target material properties are weaker at this increased temperature, the material yields readily and flows plastically.
Finally, a plug is formed and breaks free.
If the minimum perforation velocity is exceeded by more than 5-10% then the plug will break up.
Notes: Adiabatic is a thermodynamic term meaning an absence of heat transfer

## Slide 22
Without Dislocation Motion, Plastic (Ductile Deformation Cannot Occur!
Notes: Defects in atomic structure cause slip along the atomic plane. Defects tend to move in a particular direction along the slip plane. Dislocation 'pile-ups' occur in crystals when a number of similar dislocations, gliding in a common slip plane, are driven by an applied stress towards an obstacle that they cannot overcome.

## Slide 23
Work hardening
Notes: When metals are subjected to cold working (deformation at temperatures which are relatively low as compared to the material's absolute melting temperature) the dislocation density increases due to the formation of new dislocations. The consequent increasing overlap between the strain fields of adjacent dislocations gradually increases the resistance to further dislocation motion. This causes a hardening of the metal as deformation progresses. This effect is known as strain hardening or work hardening.

## Slide 24
50% penetration velocity
V10
V50
V90
Notes: "V-50" or" Velocity-50%" - is a ballistic test where bullets are fired at higher and higher velocities until they start penetrating. The velocity of the bullets where 50% of the bullets DON'T penetrate, and 50% of the bullets DO penetrate is the V-50 rating for that ballistic protection.

## Slide 25
Limit Velocity
The limit velocity Vl is the velocity below which a given projectile will not defeat a given target (shot velocity vs shot residual velocity after penetration)
The following affect Vl: material hardness, angle of impact, projectile density, projectile nose shape, L/D of projectile
Vs
Vr

## Slide 26
Oblique penetration
0-15 degrees angle of obliquity – mechanism of penetration similar to normal
15 – 70 degrees angle of obliquity – shot turned away from normal, penetration begins to decrease rapidly beyond 30 degrees
>70 degrees – onset of ricochet
Damage characteristics of semi-infinite aluminium targets subjected to
normal and oblique projectile impact. Materials Today 2022.

## Slide 27
Sloping and Composite Armour
Sloping the armour at 60o to the normal doubles the amount of armour that must be penetrated and increases the chances of ricochet

## Slide 28
Ballistic Limit Curve for Solid Shot at Semi-Infinite RHA

## Slide 29
The harder the target, the higher the V50;
The harder the penetrator, the lower V50 becomes
The greater the angle of impact, the greater the chance of projectile break-up or ricochet and the higher V50 becomes
The more dense the projectile the lower V50 becomes
A blunter nose cone the higher V50 (nose shape negligible if target significantly over-matched).
L/D V50 depends on obliquity of impact.
Generally speaking:

## Slide 30
Penetration Equations (De Marre)

## Slide 31
K ranges from 6200 to 73300 in value. When estimating, K usually takes the value 67650
Vbl signifies the limiting velocity
K expresses the composite coefficient of armour piercing
D indicates the diameter of projectile (m)
T denotes the thickness of target plate (m)
M represents the mass of the projectile (kg)
is the angle of attack. For example if the projectile is striking the target along the normal, this value would be zero.
But, De Marre does not consider the influence of target plate strength on the critical penetration velocity, or the breakage and erosion of projectile during the process of penetration

## Slide 32
Penetration Equations (Zhao)
Where:
In which:

## Slide 33
is yield strength of the target plate.
In which T denotes the thickness of target plate (m) and D indicates the diameter of projectile (m)
In which M represents the mass of the projectile (kg) and D indicates the diameter of projectile (m).
is the angle of attack.
Penetration Equations (Zhao)

## Slide 35
Kinetic Energy Ammunition
The case for KE ammunition:
Time of flight is crucial to ensure a kill (shaped charge – seconds)
Shaped charge and HESH have to be fired at low muzzle velocity
Design and cost of other methods – guidance systems, geometry, explosive shaping

## Slide 37
High Kinetic Energy
  Maximum muzzle velocity
  Leads to low mass and high pressure gun
  Low parasitic mass of sabot – we want energy in the penetrator, not the sabot.
Leads to high acceleration for given shot travel
  High charge to projectile mass
  Ratio/good thermal efficiency
Leads to limits in material properties
  Impact on gun design – strong and thick walled chamber to achieve velocities
  High energy propellants – barrel wear
Internal Ballistic Requirements of KE Shot

## Slide 38
External Ballistic Requirements of KE Shot
Maintaining High Kinetic Energy and accuracy leads to minimizing yaw at launch and velocity drop
  Low drag coefficient
  Small cross-section and dense materials
  High L/D ratio
Leads to projectile stability from spin to fin stabilisation
  Long Rod Penetrator

## Slide 39
Terminal Ballistic Requirements of KE Shot
Maximising KE Density leads to a small cross-section and dense materials
  Highest L/D ratio
  Stiff rods to avoid bending on oblique targets
  Material properties on impact and penetration
  Effects on gun design and stowage

## Slide 41
It is convenient to consider three regimes of penetration:
  Sub-hydrodynamic (strike velocities of lower than 1200 ms-1) – strength of materials applies:
    Brittle fracture – a fracture of the armour occurs with the formation of cracks due to excessive strain energy
    Ductile failure – the material is forced aside by the nose of the projectile due to high pressures of impact. Petaling at the entry and exit is evident
    Plugging (shear failure) – as described
  Hydrodynamic transition (strike velocities between 800 – 1200 ms-1)
  Hydrodynamic penetration (strike velocities above 1200 ms-1)
At speeds >12000 ms-1 energy exchange occurs at such a high rate that colliding material can evaporate!
Penetration Behaviour
Notes: So far, the theoretical study has focused on the first and the third regimes. There has been little known about the second response region due to the complexity of this problem.

## Slide 42
Notes: The difficulty of this work is to construct an appropriate theoretical model for the second region (transition zone). This is due to the complicated penetration mechanism in this region involving large plastic deformation in projectile head leading to the reduction of its length, blunted head resulting in the increase of target resistance and the weakening of penetration capability. If erosion happens, the penetration depth will decline sharply, almost halved. What's more, it is a relatively narrow velocity range, almost 100 m/s–200 m/s, in which penetrator head changes easily from large deformation to erosion. Such velocity range is 892 m/s–1042 m/s, 967 m/s–1037 m/s and 1086 m/s–1174 m/s respectively, in the experiments of spherical nosed steel rods impacting the aluminum targets. In the case of penetration by tungsten projectiles, the velocity range is 695 m/s–785 m/s.

## Slide 45
Hydrodynamic KE Penetration by
Long Rod Penetrator
The impact pressure of long rod penetrators at strike velocities in excess of 1200 m/s is the order of 100 x the yield stress of RHA. The mechanical properties can be largely ignored and the problem treated as one of hydrodynamics. During the penetration process, material flows at the target-rod interface and a mushroom nose shape* is formed in the rod and a crater in the target.
Long rod penetration is deeply influenced by the diameter ratio of nose to rod. The greater the ratio, the greater the loss of KE and the greater the erosion of rod tip.

## Slide 46
Hydrodynamic Penetration by
Long Rod Penetrator
Penetration is proportional to the length of the penetrator. Unlike normal penetration in the sub-hydrodynamic regime a larger diameter hole is made in the target
Pressures and stresses associated with impact

## Slide 47
Terminal effects dictate a small diameter shot with a high velocity. The final radius of the crater will be larger than the radius of the rod.
The sabot provides the sacrificial support in the barrel at launch
For the impact to be stable the penetrator must not topple - APFSDS
L/D around 23 with yaw 1%
Penetration above this value of yaw degraded about 6% per degree
“Self sharpening” for greater penetration
Rod length decreases as erosion occurs during penetration (only at nose tip). Increased diameter ratios increase erosion and reduce penetration

## Slide 48
Self Sharpening Penetrator (W-Cu-Zn)
Yield strength of 80W-14Cu-6Zn = 1350MPa
Strain rate in order of 105s-1
Less likely to form a mushroom head through plastic deformation since process allows adiabatic shear (but, higher strain rate than U alloys).
Hole shot diameter smaller – maintains higher KED therefore greater penetration
The process – due to the intense heat, the Cu-Zn matrix melts and is squeezed out from the tungsten skeleton near to the surface of the penetrator head. The molten Cu-Zn matrix overlays on the wall of the shot hole and lubricates the penetrator.
Notes: Note that Cu and Zn have melting points of 1084 and 420 degrees, whilst tungsten has a melting point of 3400 degrees. Nickel 1453. Alloyed steel around 1400 – 1500 degrees.

## Slide 49
Ratio of Rod Nose and Shank
Nose Shape Factor N*
N*=1
N*=1/4
N*=7/24
N*=1/2
N*=7/8

## Slide 50
Self Sharpening Penetrator (WF/MG)
The adiabatic shearing property of DU makes the nose of DU rods sharper than that of WHA rods.
Shear bands in W are generated at strains twice greater than for uranium alloys.
DU (density 19gcm-3) around 10% greater penetration than W alloy (17gcm-3)
Tungsten fiber/metal glass matrix (WF/MG) composite are found to have the similar “self-sharpening” behavior to DU (adiabatic shear bands)
We can achieve similar penetration with WF/MG by altering nose shape (N) and nose-diameter ratio .
Penetration increases with nose sharpness (ogive or conical)
Penetration increases with as close to 1 as possible
A greater length of rod remains at perforation
No further gains beyond 3kms-1 unless N<1
An environmentally friendly Long Rod?
Notes: Tungsten fibre and metal glass matrix penetrators. Self-sharpening has been observed in experiments and simulations of long-rod penetration. Penetration performances are influenced by different nose shapes. Nose geometry during the long rod penetration is represented by two main parameters, i.e., the diameter ratio of rod nose and shank η and the nose shape factor N∗. The penetration performance decreases with an increasing diameter ratio η, whose physical basis is the increased radial flow of rod material around the nose, which in turn, leads to the loss of kinetic energy due to larger cavity formed in the targets. The nose shape factor N∗ reflects the sharpness of nose shapes, and a smaller value of N∗ corresponds to a sharper nose (nose shapes are blunt, semi-spherical, ogive and conical). N∗ obviously affects the ballistic performance of long-rod penetration, however, depending on the initial impact velocity. In general, the influence of N∗ is relatively smaller than that of η.
1 The effect of the diameter ratio η is relatively great. The penetration performance decreases with increasing the diameter ratio, and the increase of the radial flowing of rod material leads to the loss of kinetic energy. The value of η is determined by the material parameters such as the densities and strengths of rod and target, the impact velocity and the resistance of the target.
2 The nose shape factor N∗ reflects the sharpness of nose shapes, which affects the ballistic performance of long-rod penetration, however, depending on the initial impact velocity. In general, the influence of N∗ is relatively smaller than that of η.

## Slide 51
For flat nose shape N*=1
N must approach unity

## Slide 52
For a fixed n, the nose shape must be ogive or conical

## Slide 53
For similar velocities, L/D, ogive nose and n = 1, a WF/MG penetrator will have greater residual rod length remaining at point of penetration

## Slide 54
Ballistic limit function of dynamic compression shear banding failure strain for uranium and tungsten alloys
Notes: Shear banding prone uranium alloys like the U 1Mo and U 0.75Ti uranium alloys are the most performing materials with regard to the erosion of metallic targets

## Slide 55
Long Rod Penetrator and N/ERA
The explosive contained in ERA is insensitive to anything other than high energy attack
It will not react against small-arms fire or artillery fragmentation
It does react if penetrated by an APFSDS projectile, consuming some of the mass and energy of the penetrator.
HOWEVER, the AFPSDS projectile has much greater mass than a shaped charge jet so its performance is degraded only marginally

## Slide 57
Directed Explosive Energy Warheads
Shaped charges (SC);
Explosively Formed Penetrators (EFP); and
High Explosive Squash Heads (HESH)
Steel EFP on Humvee – Baghdad 2007

## Slide 58
Introduction – the Monroe Effect
Shaped charges and EFPs exploit the effect of specifically shaped metallic liners in intimate contact with HE charges:
  If a block if explosive detonated on the surface of a target plate it causes a crater, which is wide but not deep
  If the charge is hollowed out the crater in the plate mirrors the crater in the explosive and the penetration is deeper
  If the cavity is lined with a metallic material the penetration deepens further
  If stand-off between the charge and plate is made, the cavity narrows and deepens further
First noticed by miners in 1790’s
Claimed by Charles Monroe 1888
Patented by von Neumann in 1913
Used extensively in the attack of armour since WW1
1938 – 43 development of EFP by Misnay & Schardin

## Slide 59
The Shaped Charge
Jet Formation:
  Hydrodynamic considerations.
  Pressure exerted by detonation wave ~ 35 GPa (x1000 target strength)
  Detonation wave sweeps along the cone from apex to base, collapsing the liner symmetrically towards its axis and extruding it along a velocity gradient
  Material originating to inside of cone extruded as a high velocity thin jet (~ 8-12 km/s), with material at outside of cone forming a low velocity slug (~300 - 1500m/s)

## Slide 61
Penetration by the shaped charge
Given that the ‘jet’ is travelling so fast, and the pressure exerted at target is so high, the interaction between jet and target is treated as a hydrodynamic problem
The jet strikes the target and erodes it
The jet is consumed during penetration, flowing into the target along a narrow cavity, with target material flowing away and around.
The faster front portion of the jet produces a wider hole than the rearward slower portion.
If the jet is too long it begins to particulate (becomes incoherent), reducing penetration
Penetration estimated by the application of Bernoulli’s principle.
t
L
t

## Slide 62: Or……Penetration (Mott, Pack and Hill – MPH)
Where:
P = penetration of jet (m)
𝛒j = density of jet material (kg/m3)
𝛒t = density of target material (kg/m3)
Lj = length of the jet (m)
λ = 1 (pure hydrodynamic behaviour), 2 (particulate jet), 1<λ<2 (hydrodynamic, but particulate jet)
S = stand off [m]
Ɣ = sqrt of densities

## Slide 63
Effectiveness of the shaped charge
Penetration is necessary, but not adequate to defeat a target
There should be sufficient energy after penetration to cause casualties, know as OVERMATCH. As a guide, about 20% overmatch is the aim of the weapon
Damage will come from:
  The unconsumed part of the jet
  Fragments of metal spalled from the inside of the plate as the jet emerges
  The high pressures and hot gases entering the compartment
Additional secondary effects could be provided by the use of pyrophoric materials in the cone material or fragmentation control in the casing
Notes: BLU-97. The BLU-97 contains: High Explosive charge: 290g of TNT/RDX, Anti-armour shaped charge liner , Pre-scored fragmentation jacket, Zirconium sponge incendiary.

## Slide 64
Factors affecting performance
Charge diameter
Stand-off
Density of Liner and Target
Cone Angle
Case Shape
Confinement
Explosive Type
Initiation Method
Precision / symmetry
Spin

## Slide 65
Charge Diameter (Liner Diameter)
A conical shaped charge at twice diameter will penetrate the same target twice as deeply, provided it has twice the stand-off. It is therefore common to express shaped charge performance and stand-off in terms of cone diameters CD

## Slide 66
The effect of stand-off
Notes: For a jet the maximum performance is at about 4CD standoff. The jet requires an air path of 2CD to fully form. For most weapons there is a 3CD stand-off. EFP are insensitive to stand-off and with a good shape can achieve penetration performance out to 1000 CD. This is helpful for OTA using proximity fuzing systems.

## Slide 67
The effect of stand-off
EFP
Notes: For a precision charge perhaps 2 – 8CD

## Slide 69
Density of Liner and Target
Notes: Density of liner. The more dense the cone material the deeper the penetration. At constant stand-off the effect of the liner and target material can be predicted using the Hill, Mott and Pack (1944) equation for hydrodynamic penetration. For ductile metal liners where L is fairly similar, the equation correctly predicts penetration in cone density order. We can also predict for aluminium armours, or armours less dense than steel.

## Slide 70
Density of Liner and Target
For the same warhead, L rho and lambda are constant. As such, Al armour needs to be 70% thicker than steel to stop the jet penetrating. But Al can be nearly 3 x the thickness of steel begore it is heavier. Thus, on an areal density basis, Al armour is more effective at keeping out a shaped charge although it is more deeply penetrated

## Slide 71
But Liner Material Also Important for Application
– Let us look at a Mg cone on concrete and compare it to…..

## Slide 72
………. a Cu cone on concrete

## Slide 73
A Cu cone on steel compared to…..

## Slide 74
A Mg cone on steel

## Slide 75
Cone Angle
Notes: At the same stand-off penetration reduces as the cone apex angle widens. The jet becomes thicker, more massive and slower. The slug gets smaller. At cone angles steeper than about 40 degrees jet instability occurs. Hydrodynamic flow from the cone wall into the jet becomes more difficult.

## Slide 77
Case Shape and Confinement
Various attempts to increase jet length by boosting velocity have been attempted. However, packing too much explosive around the base region causes the hole to widen with less penetration depth. As such, a full calibre cone with a cylindrical case works well, or boat tailing to save weight without detriment to detonation wave propagation
Confinement rigidity affects penetration performance by altering the strength of reflected shock waves. Using a stiffer or thicker metal walled case is better than a thin case.
The minimum explosive head for normal shock-wave incidence on cone apex should be at least 0.5CD

## Slide 78
Explosive type
An explosive with higher detonation shock pressure P gives better penetration. The explosives tabulated below have, 10,000 times the cone collapse pressure for copper.
Good filling quality is necessary to minimize jet perturbations
Explosive | Density (g/cc) | Vd (m/s) | P (Kbar)
PE4 | 1.6 | 8200 | 270
COMP B | 1.6 | 7840 | 246
EDC1/S | 1.8 | 8600 | 333
TORPEX | 1.7 | 7370 | 231

## Slide 79
Initiation method
Whilst central initiation requires a head space of 0.5CD, peripheral initiation can be created using a wave shaper. This can save further head space if necessary. PI as opposed to CI can create jet perturbations if symmetry is not aligned (manufacturing costs etc)

## Slide 80
Precision symmetry
For best penetration and with the least round variation, axial and radial symmetry must be excellent. An offset or inhomogeneous charge is a disaster leading to lateral velocity VL.
If the jet elements stay on axis they all contribute to hole deepening.
As VL reduces penetration improves

## Slide 81
Spin
The effect of charge rotation or spin is to degrade penetration – centripetal force diffuses the jet
At 30 revolutions per second the penetration is roughly halved (Schofield)
Warheads are therefore fin-stabilized in flight, or if fired from a rifled gun adopt slipping driving bands (like the LRP)

## Slide 82
Shaped charge and N/ERA
On impact by a HEAT jet the explosive in the ERA is initiated.
  For NERA confined non-metallic material with elastic properties
The plates fly apart in opposite directions through the path of the jet
At high rates of obliquity the jet is faced by a continuous path of metal and its mass flow rate is reduced
The jet becomes incoherent and penetration of the main aromour reduced considerably.

## Slide 83
Explosively Formed Projectile

## Slide 84
EFP Liner Collapse
This is the Misnay-Schardin Effect
Wide angle cones and other liner shapes such as plates or dishes do not jet, but give, instead, an EFP, sometimes called a self-forging fragment (SFF).
The fragment or slug forms by plastic flow and has a velocity or around 1 – 3 km/s. Target penetration is much less than a shaped charge jet but hole diameter is larger with more armour backspall. Liner does not separate into high velocity jet and low velocity slug; it simply folds into a single fragment.
In general, the thinner the liner the higher the slug velocity
Stand-off can be up to 1000 CD! Frequently used for OTA, side attack and belly attack where armour is usually weakest.
Note: Slide 45, which stated that after 14CD stand-off a shaped charge is nugatory in armour attack

## Slide 85
EFP Liner Collapse

## Slide 87
Effect of cone angle on jet / slug formation
As the apex angle of the cone increases, so does the tendency to form a high velocity slug as opposed to a coherent jet. The graph shows the velocity effects on jet tip and slug as the angle increases for a copper liner. As can be seen, at about 140 degrees the two masses of jet and slug do not separate and only a high velocity slug is formed.
The bending and collapsing process is not always easily achieved to produce a small cylindrical fragment (high KED) to attack armour. Explosive formation of the fragment is influenced by liner shape, liner wall thickness, liner material and strength of detonation wave.

## Slide 88
Effect of liner material on fragment shape and penetration
Notes: The liner material can also have an effect on the profile of the fragment formed. The pictures above demonstrate a constant liner shape of 150 degrees hyperbolic. One point to mention is that a heavily confined charge will tend to force the liner into a ball shape, reducing the opportunity of forming a L/D ratio of 3 (ideal for EFP).

## Slide 89
Effect of liner shape on fragment profile
Notes: Shallow dishes are used rather than cones, and results can be improved using a liner with a digressive thickness, which is usually called a ballistic disc. Such a shape encourages the folding back of the dish to form the EFP.

## Slide 90
Effect of liner shape on penetration performance

## Slide 91
Effect of explosive type of fragment shape
Notes: The intense detonating wave striking the liner has an effect on the formation of the EFP as well as its velocity. Detonation wave affected by type of explosive, explosive geometry, initiation system, explosive confinement.

## Slide 92
Performance of EFPs
Notes: Forming an aerodynamically stable EFP is of great interest to assist in penetration at great stand-off. The disadvantage is that producing stabilization by inducing a tail shape means the EFP loses velocity rapidly, ergo penetration performance drops. Armco iron does, however, produce reasonable results as shown in the notes on the slide itself.

## Slide 94
The EFP - weapon of insurgent choice?

## Slide 95
Stand off 5 m for 65 mm dia disk

## Slide 96
High Explosive Squash Head
Notes: HESH rounds are thin metal shells filled with inert material (like coal-tar pitch), plastic explosive and a delayed-action base fuze. Upon impacting, the inert material followed by plastic explosive is "squashed" against the surface of the target and spreads out to form a disc or "pat" of explosive. The inert material helps to prevent premature detonation of the plastic explosive and to sustain the impact pressure and temperature.
The base fuze then detonates the explosive milliseconds later, creating a shock wave that, owing to its large surface area and direct contact with the target, is transmitted through the material. In the case of the metal armour of a tank, the compression shock wave is conducted through the armour to the point where it reaches the metal-air interface (the hollow crew compartment), where some of the energy is reflected as a tension wave, a phenomenon called impulsive loading. At the point where the compression and tension waves intersect, a high-stress zone is created in the metal, causing pieces of steel to be projected off the interior wall at high velocity.
This fragmentation by blast wave is known as scabbing or spalling, with the fragments themselves known as scabs or spall.
Depending upon the armour thickness, a heavy chunk of target material (4 to 10 kg for a standard 120 mm round) can separate out from the other end of the target with supersonic velocities. This spall is sufficient to permanently damage the essentials of a tank, igniting the ammunition or fuel storage and severely damaging the crew to achieve a "total kill" of the target. In general, the higher the armour thickness, the higher the scab weight will be.
The fragmentation achieved by impulsive loading of armour block by an HESH round is more lethal compared to similar high explosive rounds.

## Slide 97
Schematic illustration of wave transmission
And reflection at the boundary of two materials of differing impedance
Impedance
Notes: When a stress of shock wave encounters an interface, the nature of the subsequent transmitted and reflected waves is a function of the properties of the materials either side of the interface. Wave interaction is governed by a property known as impedance (Z). Where 𝜌0 is the initial material density and 𝑈𝑠 the shock speed under given loading conditions.
Z = 𝜌0𝑈𝑠 (1)
However, in the event that the material is in the elastic regime, Z is termed acoustic impedance and 𝑈𝑠 → cL. In general, the use of acoustic impedance is sufficient to predict the nature of wave interaction across an interface. This allows for the following modification to be made to Equation (1).
Z=𝜌0𝑐𝐿 (2)
Knowledge of the impedance of different materials can subsequently be used to predict wave propagation across an interface from material A to material B via conservation of force (equilibrium) and particle velocity (continuity) across the interface.
From Equations above the effect of removing the rear-most material (Material 2) leads to an air or ‘free’ rear surface. Essentially, 𝐸2 and 𝜌2 will→0, leading to a reflected stress wave, σ𝐵, with the opposite sign and same magnitude as the originally incident wave. Assuming an initially compressive loading, such a reflection will therefore be tensile in nature. This phenomenon is exploited in the High Explosive Squashed Head (HESH) round. This munition deposits and subsequently detonates an explosive charge on the surface of a target (e.g. armour plating on a vehicle); the resultant compressive wave reflects at the rear surface of the target as a tensile wave, moving back into the target. Eventually, the material will enter a state of net tension. At this point, as materials are, in general, very-much stronger in compression that tension, the target will fail under dynamic tensile loading and a plate of material (a ‘scab’) will spall / separate, moving away in the direction of the initial compressive loading.

## Slide 99
HESH Historic
Developed by Dennistoun Burney in the 1940’s:
  Anti-fortification ‘wall-buster’
  Defeat of armour
  Remains secondary armament of CR2
  The precursor to 120mm thermobaric rounds
Mostly fired from guns with rifled barrels due to the need for spin stabilisation in flight.

## Slide 100
Factors affecting performance
Explosive charge
  Plastically deformable with high brisance (RDX/Wax)
Angle of Attack
  With sloping targets performance is not degraded (the detonation wave still takes the shortest route through armour)
  Performance remains consistent until about 65 degreees (ricochet)
Warhead Calibre
  The thickness of plate defeated is directly proportional to calibre (good scab will be 1.25 – 1.5 calibre)
  Performance related to quantity of explosive used – the more explosive the larger the shock wave
Strike Velocity
  >700 m/s can cause reverse impact detonation (adiabatic heating of hot spots causes burn-to-detonation)
  Shock wave travels away from the target

## Slide 101
Design Limitations of HESH
Spaced armour or perforated armour – the scab produced is unlikely to possess sufficient KED to penetrate the next plate
Corrugated plate – prevents ‘pat’ forming effectively, thereby limiting coherent shockwave formation
Layered composite armour – acoustic impedence
Spall liners such as kevlar
Secondary role on concrete – the warhead may ‘skip’ due to delayed base fuze and not function at correct time

## Slide 102
Penetration Mechanics Summary
It is all about material properties and kinetic energy density for attack of armour
Sub-hydrodynamic, transition and hydrodynamic penetration
A KE round relies on KED to overmatch the mechanical properties of the target and is resistant to counter measures - L/D, nose shape and adiabatic shear
A shaped charge relies on directed energy to form a jet and slug with a velocity gradient from 8000m/s to 1500m/s. Penetration in RHA can reach 8CD with a stand-off of 2-4CD
A shaped charge is susceptible to N/ERA counter measures and is an EFP from 14CD stand-off
An EFP produces a single high velocity slug (up to 3000m/s) with an ideal L/D ratio of 3
The impact velocity is orders of magnitude less than a SCJ with penetration close to 2CD. However, accuracy and lethality out to 1000CD
HESH – somewhat antiquated but effective against monolithic armour and concrete structures. Readily defeated by spaced and composite armours but…….