## Slide 1: Ordnance, Munitions and Explosives Principles of OME Level 5 ACDA5010 Pyrotechnics OME (Part 3)
Notes: This is the slide pack from the lecture on propellant and CCC manufacture for the Bae Ammunition course 22-25 November 2004. The pack contains all of the slides used and a number of others which were not used (hidden) but which provide expansion and further details of the processes. The hidden slides may be viewed in the edit window (not slideshow!).
Any questions relating to this lecture or any other aspect of the course, please contact me on the following numbers.
Mobile 07710843580
Bishopton Office 01505 832107
Email ian.martin@baesystems.com

## Slide 2: Thermal Batteries
Missiles
  Seekers, Electronics, Actuators
Very long storage
No maintenance
High reliability
Rapid availability of power
Resistance to shock and vibration
Wide ambient temperature range
High power (e.g. for actuators)
Safe

## Slide 3: Thermal Battery
Depolariser - K2Cr2O7
Electrolyte - a salt mixture
Binder - silica

## Slide 4: Thermal Battery
Mica wrap
Fuse trains
Battery stack
Terminal
Steel container
Insulator discs
Fuze lead
Glass ribbon
Fuze train
Section of Battery Stack

## Slide 5: Thermal Battery Activation
Fire igniter
Igniter flame ignites heat paper (Zr/BaCrO4)
Heat paper rapidly ignites heat pellets (Fe/KClO4)
Heat pellets burn
Heat diffuses through anode and cathode pellets
Electrolyte melts
Battery activates

## Slide 6: Requirements for Heater Mixture
Pellet is part of the electrical circuit, therefore combustion products must be electrically conducting.
Reacting mass must remain in place during and after combustion.
System is sealed, therefore minimal gas production must be assured.
Pellets must be readily ignitable, fast burning and melt the electrolyte under all design ambient conditions.

## Slide 7: Iron - Potassium Perchlorate
8Fe + 3KClO4 = 4Fe2O3 + 3KCl
51.8% Fe, DH = -3317 kJ, q = -3846 kJ kg-1
3Fe + KClO4 = Fe3O4 + KCl
54.7% Fe, DH = -1125 kJ, q = -3676 kJ kg-1
4Fe + KClO4 = 4FeO + KCl
55.8% Fe, DH = -1095 kJ, q = -3024 kJ kg-1
Which of these reactions is most likely?

## Slide 8: Oxidation of Iron

## Slide 9: Iron - Potassium Perchlorate
J Callaway, N Davies and M Stringer.
Pyrotechnic heater compositions for use in thermal batteries.
Proc. 28th Intl. Pyro. Seminar, Adelaide, Australia 153-168 (2001)
Fe source

## Slide 10: Flash Compositions
4Mg + KClO4 = 4MgO + KCl
41%
DH = -2413 kJ; q = -10.2 kJ.g-1
8Al + 3KClO4 = 4Al2O3 + 3KCl
27%
DH = -6722 kJ; q = -10.6 kJ.g-1
SR801B
magnesium 57
potassium perchlorate 37
graphite 6
SR811
aluminium 70
potassium perchlorate 30
SR812
aluminium 50
potassium perchlorate 50
Violent reaction required – loose powder fill

## Slide 11: Thunderflash Mk 8
quick match (108 mm)
match composition
striker
tear off tape
quickmatch
flash composition SR 801B (11.7 g)
gunpowder
paper wad
hollow paper tube
magnesium 57
potassium perchlorate 37
graphite 6

## Slide 12: Stun Grenade
High energy, high temperature mixture.
  aluminium / potassium perchlorate
Loose powder fill for maximum reaction rate.
Composition confined in aluminium tube for maximum effect.
Grenades are scattered before functioning.
No two grenades should function simultaneously to cause excessively high overpressure.
Haley & Weller

## Slide 13: Stun Grenade

## Slide 14: System Issues and Manufacturing
We’ve already discussed the failure modes in tracer.
There is the potential for similar failures in an illuminating candle.
As we have more composition the effects can be very dramatic.
Getting the material to burn at the right rate and with the right spectrum is but half the battle.
We now have to ensure that the system survives launch and deploys correctly
Key features are press loads, the state of the press tooling, the condition of the liner etc.

## Slide 15: Failure of IR Candle
The lid is all that remained of the candle case!
The rest had been blown apart
Compare the debris to a simple “failure to ignite”.

## Slide 16: Locking in the Devil!
Compatibility with the system.
Protection against Moisture
  In process.
  In storage.

## Slide 17: Magnesium Samples
Fresh Mg Supplied
Mg Recovered from
Cart #1

## Slide 18: SR 800 Samples Submitted for Laboratory Analysis
Fresh SR 800
SR 800 recovered
from Cart. #1

## Slide 19: Elemental Mapping
Advanced scanning electron microscopy (SEM) and energy dispersive
x-ray spectrometry (EDX) SEM techniques will allow us to establish the
Position and depth of the oxide layer that has been formed.

## Slide 20: Elemental Mapping
SEM image and spectra after exposure to moisture.

## Slide 21: Comparison of Fresh and Recovered SR 800
Chart: 
Chart: SR800 emission (4-5 microns)

## Slide 22: Summary
Ignition
Smoke munitions – screening, signalling
Light munitions – illumination, distraction, signalling
Gas production – nitrogen, oxygen
Propulsion

## Slide 23
Questions?

## Slide 24: More on Phosphorus

## Slide 25: Toxicity of Phosphine

## Slide 26: The Match Industry
White phosphorus and phosphorus vapour are extremely poisonous.
Lethal dose (oral, adult) 15-100 mg.
WP used as a poison in notorious murder cases
Extensive use of WP in the match industry led to many cases of “phossy jaw” – painful, suppurating lesions and destruction of bone tissue.

## Slide 27: The Match Industry

## Slide 28: The Match Industry

## Slide 29: The Match Industry
Osteonecrosis “phossy jaw”
Painful, suppurating lesions and destruction of bone tissue

## Slide 30: The Match Industry

## Slide 31: The Match Industry
Lethal dose of WP could be obtained from a box of Lucifer matches.
WP was also used in rat poisons.
Death can occur within :
  hours from large doses
    attacks stomach lining, intense pain, vomiting, destruction of liver
  days from small doses

## Slide 32: Phosphorus Nerve Agents
All belong to one family of chemicals – organophosphorus esters
    colourless liquids
    slight odour
Some members of the family are commercial insecticides.

## Slide 33: Nerve Agents
IG Farben Industrie
Investigated in Germany as part of a Research programme into insecticides.
The organophosphate compounds were found to have a high lethality when inhaled by animals.
GA was synthesized in 1937 by Gerhard Schrader.

## Slide 34: Nerve Agents
GA tabun
GB sarin
GD soman
GF cyclosoman
VG amiton, tetram
VX
VE

## Slide 35: Nerve Agents
First Nerve agent discovered in 1937
Faint smell of almonds
Vapour Toxicity
LCt50 (inhalation) 140 mg min m-3
Liquid Toxicity
LD50 (skin) 15 to 20 mg/kg body weight
More volatile than GA. Rather more toxic.
More difficult and costlier to synthesize.
Vapour Toxicity
LCt50 (inhalation) 50-100 mg min m-3
Liquid Toxicity
LD50 (skin) 24 mg/kg body weight

## Slide 36: V Agents
The most toxic and persistent of the nerve agents.
‘Discovered’ in the UK in early 1950s by chemical industry researching improved organo-phosphate insecticides.
American VX
Russian VX
Both have very low volatility and are more effective through skin than vapour absorption

## Slide 37: VX
highly persistent
most toxic
major hazard is percutaneous from liquid drops
lethal dose < 10 mg
Time to death ~20-30 mins
Household Pin
Droplets
of VX
Any one of these drops is a potential lethal dose

## Slide 38: Some Commercial Organophosphate Insecticides
Structure Similar to G Agents
Structure Similar to V Agents
Dimefox
Paraoxan
Parathion
Amiton (Tetram)
Systox

## Slide 39: Some Commercial Organophosphate Insecticides
Nerve agents and Insecticides are closely related chemically.
A factory that can make one can probably make the other.

## Slide 40: Use of Nerve Agents
Used by Iraq in Iran/Iraq war (1980s)
and against civil populations such as in the Kurdish town of Halabja
Sarin attack 1995
13 dead immediately,
50 injured (some died later)

## Slide 41: Speed of Action - GB
Zero Time
15 sec
35 sec
Death by inhalation route is fast

## Slide 42: Timeline in Moderate to Severe Nerve Agent Poisoning
Within 30 seconds
  miosis, tightness in chest dizziness, incoordination
Within 1 minute
  prostration, +++ secretions, loss of consciousness
Within 5 minutes
  generalized muscle spasms, convulsions, obstructed airway
From 5 to 15 minutes
  respiratory failure, circulatory collapse, death

## Slide 43: Red Phosphorus as Flame Retardant
The growing use of plastics and other flammable synthetic materials in construction, home furnishings, and various industrial applications is creating opportunities for polymer compatible, thermally stable, environmentally friendly, and cost-efficient flame retardants. New legislation emphasizing test methods that provide input for mathematical fire modeling is changing the focus of interest in preferred flame retardant action from simple ignition resistance to fire propagation and rate-of-heat release. These factors together with concerns about combustion product toxicity and corrosivity, long-term worker exposure, and manufacturing waste minimization are creating product parameters uniquely met by various phosphorus compounds. The best phosphorus compounds for both new and existing applications will be significantly different from those compounds in the marketplace today. This paper will describe some new compounds and the driving forces defining the product parameters that will challenge phosphorus chemists for the next decade.
Aaronson A M. Phosphorus chemistry. Chapter 17. Phosphorus flame retardants for a changing world. ACS Symposium Series (1992) 486 218-228

## Slide 44: Red Phosphorus as Flame Retardant
Microencapsulated red phosphorus (MRP) is a powerful flame-retardant additive in halogen-free flame retardant polyolefin materials. Only 5% MRP
additive can greatly decrease the peak heat release rate, effective heat of combustion and increase the limiting oxygen index, time to ignition, and pyrolysis temperature of PO materials. MRP acts as a flame retardant both in the gas and condensed phases of polyolefins. In the condensed phase, MRP form phosphoric acid derivatives, which promote formation of more stable carbonaceous charred layers with P—O and P—O—C complexes. In the gas phase, phosphorus monoxide (PO*) species produced from the combustion of red phosphorus can quench active radicals produced by burning.
Qiang Wu et al., Preparation and characterization of microcapsulated red phosphorus and its flame-retardant mechanism in halogen-free flame retardant polyolefins. Polymer Intl. (2003) 52 1326-1331

## Slide 45
Military Uses of Phosphorus
Incendiary
Smoke

## Slide 46: Incendiary
White phosphorus used in WWI
  primarily for smoke screens
    UK production 1914 1000 tons,
    1918 2500 tons
  tracers
  incendiaries
    used against Zepplins flying over London in 1915

## Slide 47: Incendiary
WWII saw more extensive use particularly as incendiary :
Molotov Cocktails
  stockpiled in UK following Dunkirk (250k/week)
Incendiary bombs
  Mg/thermite bombs were small with low penetration
  30lb WP bomb penetrated within structure then an explosive charge scattered the payload

## Slide 48: Incendiary
Advantages of white phosphorus
  high heat of oxidation
  efficient packing of payload, readily filled
  readily dispersed
  spontaneously flammable
Disadvantages of white phosphorus
  high toxicity
  fearful injuries
  severe local environmental impact

## Slide 49: Incendiary
Burns from phosphorus are serious and usually require hospitalisation.
Old treatment for WP burns was to bathe in a solution of a copper salt to coat the WP particles with copper.
Copper now considered too toxic for safe application.

## Slide 50: Incendiary
Phosphorus – Sulphur
  low-melting liquids available for use in flame throwers
  mixtures of WP and phosphorus sesquisulphide

## Slide 51: Red Phosphorus Smoke Applications
Rapid screening of military vehicles against visual or infrared detection and observation.
Long duration naval signal from floating munition.

## Slide 52: Screening (land)
AC/225 Panel VI/SP.6 D/10

## Slide 53: Screening (nomenclature)
AC/225 Panel VI/SP.6 D/10

## Slide 54: Requirements for Screening
Important characteristics
Mass extinction coefficient
Concentration
Yield Factor = (Mass of smoke)  (Mass of Payload)
Beer Lambert Law
where I0 is intensity of incident radiation
I is intensity of transmitted radiation
a m2 kg-1 mass extinction coefficient - n.b. a(l)
c kg m-3 concentration
l m path length

## Slide 55: Phosphorus Smokes
White phosphorus
  obsolescent
  good visual smoke – tends to pillar
  toxicity, incendiary nature
Red phosphorus
  increasingly used
  excellent visual smoke, good infrared effect
  undesirably incendiary

## Slide 56: Phosphorus Smoke – Yield Factor
4P + 5O2 = P4O10
yield = 284  (4 x 31) = 2.3
Assume 85% P in composition : yield = 2.0
(c.f 2.3 for white phosphorus)
But P4O10 is very hygroscopic.
Based on measurements for pure phosphorus, likely yield factors are :
2.0 in air of 0% RH
3.2 10% RH
13.8 90% RH

## Slide 57: Yield factor against humidity for phosphorus smoke
Chart: relative humidity (%)
| 10 | 20 | 30 | 40 | 50 | 60 | 70 | 80 | 90
WP/RP | 3.53 | 3.72 | 3.91 | 4.11 | 4.34 | 4.65 | 5.1 | 5.88 | 7.85

## Slide 58: Infrared Screen
Mass extinction coefficient usually smaller in the infrared than in the visible.
Particles of size comparable to visible radiation are readily generated ; those of size comparable to infrared are not.
Therefore:
  Infrared screening requires higher concentration along line of sight than visual screening.
A practical point : particles of IR size do not readily remain afloat in air

## Slide 59: Mass Extinction Coefficient (a)

## Slide 60: Red Phosphorus Smoke
red phosphorus 85
magnesium 5
potassium nitrate 5
Viton 5
The heat from the reaction of magnesium with potassium nitrate helps the phosphorus burn to extinction.
The burning rate can be varied by changing the amount of Mg/KNO3.
Burning characteristics can be improved by incorporation of a pyrotechnic heater mixture.

## Slide 61: RP Smoke Composition
Red Phosphorus Clariant grade HB300 microencapsulated | ~73%
Magnesium Grade 5 Cut | ~9%
Sodium nitrate milled | ~9%
Viton A | 9%

## Slide 62: Mass extinction coefficient of red phosphorus smoke against wavelength
Chart: Wavelength (mm)
Visible
Mid IR
Far IR
Near IR

## Slide 63: Why use phosphorus?
Less toxic than HCE smokes
  The US NRC short exposure guideline is 10mg/m3 compared with the 40mg/m3 for red phosphorus smoke.
Screen over wider wavebands.
Chart: Wavelength (mm)

## Slide 64: Phosphorus Smokes
Scheunemann W. Über die optischen Eigenschaften von Nebelpartikeln im Infraroten. Proc. Internationale ICT-Jahrestagung (12th), Karlsruhe, Germany 235-251

## Slide 65: HC Smoke
Scheunemann W. Über die optischen Eigenschaften von Nebelpartikeln im Infraroten. Proc. Internationale ICT-Jahrestagung (12th), Karlsruhe, Germany 235-251

## Slide 66: Red Phosphorus Smoke
4P + 5O2 = P4O10 DH = -3010 kJ, q = -10,600 kJ kg-1
PN841
red phosphorus 95
butyl rubber 5
This is not a true pyrotechnic composition.
Forms a surface char which can help extinguish pellet in wet conditions.

## Slide 67: Red Phosphorus Smoke
PN841
red phosphorus 95
butyl rubber 5
The pellets of red phosphorus used in the L8 grenade are formed by mixing the phosphorus with a synthetic rubber, which acts as a binder and also coats the phosphorus, providing some protection against oxidation and pick-up of water vapour.
Initially, butyl rubber was used, but it proved difficult to handle on a production scale because it only slowly formed a dispersion with common solvents.
Intol 1500 (a butadiene-styrene copolymer) which is dispersed easily in methylene chloride, was proposed as a binder for the red phosphorus.

## Slide 68: Red Phosphorus Smoke
An investigation (Ref CDE TP 154) showed that the red phosphorus supplied contained small amounts of copper which catalyses the oxidation of phosphorus.
The copper could not be removed easily, but it was found that the incorporation of 1% UOP 88 rubber anti-oxidant into the composition gave good protection against the action of the copper. It was therefore proposed that the composition of the filling for the L8A1 grenades should be changed to take into account these findings. As a result, a programme of trials was carried out under Programme 17/74.
PN841
red phosphorus 95
butyl rubber 5
PN884
red phosphorus 96
INTOL 1500 3
UOP 88 antioxidant 1

## Slide 69: Red Phosphorus Smoke – L8

## Slide 70: Red Phosphorus Smoke – L8
Requirement was for visual screening to allow crew to escape
  rapid build up of smoke with ~ 1 minute duration
With thermal imager obscuration lasts <<1 s
Grenade did not meet later requirements for infrared screening
  very rapid build up
  short duration

## Slide 71: Red Phosphorus Smoke – L8
Rate of smoke production was inadequate for new requirements for rapid protection.
  increase surface area of composition
  perhaps increase burning rate of composition (but this is likely to reduce phosphorus content)
Ageing problems had been identified with phosphine evolution
  attention to quality/type of RP

## Slide 72: Red Phosphorus Smoke – L114
RP/binder pellets
RP/binder leaves
Rapid smoke production
for quick screening.
Slower smoke production
for prolonged screening.

## Slide 73: Red Phosphorus Smoke – VIRSS
VIRSS
  Vehicle, infrared smoke screening system
  Provides protection in the IR
“Milk crate” of 24 sealed plastic bottles containing encapsulated RP furnished with expulsion charge and gunpowder delay.
Initiated sequentially by pyrotechnic delay cord in groove in base plate.
Expelled from discharger and burst in air.

## Slide 74: Red Phosphorus Smoke – VIRSS
body
bottle with RP
delay/expulsion unit
vent
pyro delay cord

## Slide 75: Visual and Infra Red Screening Smoke

## Slide 76: VIRSS…the anatomy of a poor design!

## Slide 77: VIRSS…the anatomy of a poor design!
Composition.
  Degraded in hot / humid SET (Phosphine evolution)
Sub-munition
  Plastic “milkman’s hat” cap did not provide environmental seal
  Barrel not parallel
  Sub-munition body did not perform over the required temperature range
  Sub-munition body filling difficulties. Base overstressed
Munition
  Welded into unit frame by “Bovvie Sh*t”
  Untried ultrasonic welding used in assembly resulting in failure
  Unreliable electrical contact (Interface of unit frame and munition.)
  Unreliable sealing at barrel base
Firing Circuit
  Fired on a negative going pulse, Shudder and recoil led to failure
  Integration with vehicle more complex than previous design
  Gun shock not considered
Manufacture
  No productionised filling facility developed
  Production of main composition batches too small
  Final assembly of munition not considered
System integration
  Re-load not considered
  Stowage on vehicle inadequate

## Slide 78: VIRSS
Composition.
  Degraded in hot / humid SET (Phosphine evolution)
Sub-munition
  Plastic “milkman’s hat” cap did not provide environmental seal
  Barrel not parallel
  Sub-munition body did not perform over the required temperature range
  Sub-munition body filling difficulties. Base overstressed
Munition
  Welded into unit frame by “Bovvie Sh*t”
  Untried ultrasonic welding used in assembly resulting in failure
  Unreliable electrical contact (Interface of unit frame and munition.)
  Unreliable sealing at barrel base
Firing Circuit
  Fired on a negative going pulse, Shudder and recoil led to failure
  Integration with vehicle more complex than previous design
  Gun shock not considered
Manufacture
  No productionised filling facility developed
  Production of main composition batches too small
  Final assembly of munition not considered
System integration
  Re-load not considered
  Stowage on vehicle inadequate

## Slide 79: VIRSS…the anatomy of a poor design!

## Slide 80: Red Phosphorus Smoke – FSF.
Float Smoke and Flame N2 Mk3
Explosive Train of Float
Smoke and Flame N2 Mk3
Float Smoke and Flame N2 Mk3 (FSF) is a UK service munition designed to function when submersed in salt water with salinity greater than 3.5%.
Vine T A and Fletcher W. An investigation of failures to function of a red phosphorus marine marker.
Proc. Intl. Pyro. Seminar (2002) (29th), Westminster, Colorado, USA 477-490

## Slide 81: Red Phosphorus Smoke – FSF.

## Slide 82: Red Phosphorus Smoke – Marker Marine No 4.
Rupture disc
Parasheet unit
Emission tube
Baffle plates
Igniter assembly
Candle unit
Perforated tube
Sea cell unit
Drogue and sinker assembly
Nose ejection spring
Press cap

## Slide 83: Red Phosphorus Smoke – CSW.
15 m drop test (onto side)
Ignited and smoke produced for 10 mins
P Barnes, C Shepperson, A E Cardell and J Queay.
The vulnerability of pyrotechnic stores. DOSG ES351-94-9 (1994)
SR414
red phosphorus 60 ± 10
magnesium 5.65
manganese dioxide 28
calcium silicide 6
acaroid resin 0.34
Candle Smoke White

## Slide 84: Smokes
We’ve now ejected an illuminating payload!
Can we do the same for a smoke payload?
Why not?
Igniferous
input
Compatibility!

## Slide 85: 105mm LIMAWS smoke pot
Input Data:
Acceleration: 22,000 g
Maximum Force: 690 kN
Smoke Pot Data:
Diameter: 69.75 mm
Length: 83.25 mm
Total Weight: 1.065 kg
Total amount of RP- Compound: 0.365 kg
Burning Time: 2 min

## Slide 86: Artillery bi-spectral smoke rounds
155 mm, DM 125
105 mm, XMR102

## Slide 87: RP Smoke Composition
Red Phosphorus Clariant grade HB300 microencapsulated | ~73%
Magnesium Grade 5 Cut | ~9%
Sodium nitrate milled | ~9%
Viton A | 9%

## Slide 88: Mortar
If we deploy a pot we have room for only one (perhaps) two if well designed.
Use pellets (Cheeses).
Why do we want to get more sources on the ground?

## Slide 89: PH3 generation with RP grades
PH3 generation
Conditions: 25°C and 65% relative humidity:
RP powder grade PH3 µg/g RP
1 day 2 days 14 days 28 days
SF (non stabilised) 150 290 1300 2400
SFD 15 48 770 na
HB 251 18 40 507 na
HB 100 14 27 109 na
HB 300 3 5 24 38
HB 700 2 3 7 8
HB 714 0,8 1,2 3 5 HB 801 0,07 0,11 0,33 0,5

## Slide 90: But it can go wrong!
Phosphorus and Water react.
  Hence the need for the micro-encapsulation!
A simplistic view of the problem is as follows.
2.P4 + 12.H2O  5.PH3 + 3.H3PO4
Other researchers, (V. Norris et al in their Frank Carver Award winning paper presented at the 27th IPS) suggest a more complex reaction.
3.5 P4 + 21 H2O + 11.275 O2  5.2 H3PO4 + 7.15 H3PO3 + 0.65 H3PO2 + PH3

## Slide 91: What does the equation mean?
PH3
PH3
We are also consuming OXYGEN so when the concentration of
Oxygen = 0 Reaction progress = 0!

## Slide 92: Phosphine Corrodes!

## Slide 93: RP Smoke Composition
Red Phosphorus Clariant grade HB800 microencapsulated | ~73%
Silicon Powder | ~9%
Potassium nitrate milled | ~9%
Viton A | 9%

## Slide 94: 16. Nanotechnology

## Slide 95: Effect of Particle Size
Thermal Decomposition of RDX / binder PBX.
TG/DTG DSC
Temperatures for micron and nano sized RDX differ by ~1°C

## Slide 96: Effect of Particle Size
Thermal Decomposition of RDX / binder PBX.
Activation energy
micron-sized RDX 129.7 kJ.mol-1
nano-sized RDX 127.1 kJ.mol-1
Liu Jie et al.,. Preparation of nano-RDX-based PBX and its thermal decomposition properties. J. Thermal Anal. Calorim. (2018) 131(3) 2693-2698

## Slide 97: Effect of Particle Size
Over recent years increasing attention has been paid to the use of very fine particles to produce very reactive compositions.
After - Miziolek A W. Nanoenergetics : an emerging technology area of national importance. AMPTIAC (2002) 6(1) 43-48
Conventional (mm sized)
Energetic nanocomposite (nm sized)
Mass transport an issue
Lower power
Lower energy (incomplete reaction)
Mass transport minimised
Higher power (faster reaction)
Higher total energy

## Slide 98: Preparation of nanoaluminium
Hou Conghua et al., Preparation of Al nanoparticles and their influence on the thermal decomposition of RDX. Central European J. Energ. Mater. (2013) 10(1) 123-133
H2 + He atmosphere
+
-
Al ~ 61 nm

## Slide 99: Nano thermite
Standard method might be by mixing appropriate volumes of suspensions of the nanoingredients dispersed in hexane by sonication.
Malchi J Y, Foley T J and Yetter R A. Electrostatically self-assembled nanocomposite reactive microspheres.
ACS Appl. Mater. Interfaces (2009) 1(11) 2420-2423
Sonicated thermites have been shown to propagate a reaction in rectangular microchannels having hydraulic diameters from∼100 to 800 μm. (Son, S. F et al., J. Propul. Power 2007, 23, 715).
Flame velocities typically 100-700 m/s in these channels.

## Slide 100: Electrostatic Self-Assembly
Nanocomposite reactive microspheres with diameters of ∼1-5 μm were created via electrostatic self-assembly of aluminium and copper (II) oxide nanoparticles.
The more intimate mixture between the two nanoreactants allowed a more energetic combustion process.
Experiments with the self-assembled material demonstrate the ability to achieve ignition and sustain a combustion wave in rectangular microchannels, which does not occur with material having similar amounts of organics mixed via the traditional sonication method
Malchi J Y, Foley T J and Yetter R A. Electrostatically self-assembled nanocomposite reactive microspheres.
ACS Appl. Mater. Interfaces (2009) 1(11) 2420-2423

## Slide 101: Electrostatic Self-Assembly
Malchi J Y, Foley T J and Yetter R A. Electrostatically self-assembled nanocomposite reactive microspheres.
ACS Appl. Mater. Interfaces (2009) 1(11) 2420-2423

## Slide 102: Porous Ingredients
Provided that the pore structure is accessible, a greatly increased surface area for reaction may be achieved.
Porous silicon (PS) films up to ∼150 μm thick with specific surface area similar to 700 m2/g and pore diameters similar to 3 nm are fabricated using a galvanic corrosion etching mechanism that does not require a power supply. After fabrication, the pores are impregnated with the strong oxidizer sodium perchlorate (NaClO4) to create a composite that constitutes a highly energetic
system capable of explosion. Using bomb calorimetry, the heat of reaction is determined to be 9.9 ± 1.8 and 27.3 ± 3.2 kJ/g of PS when ignited under N2 and O2, respectively.
Becker C R et al., Thermal analysis of the exothermic reaction between galvanic porous silicon and sodium perchlorate. ACS Appl. Mater. Interfaces 2(11) 2998-3003 (2010)

## Slide 103: Porous Ingredients
Nanoporous thermite
A two-dimensional NiO nano honeycomb was produced by thermal oxidation of a Ni thin film deposited by thermal evaporation onto a silicon substrate. Then aluminium was thermally deposited into the NiO nano honeycomb to realize an Al/NiO based nano energetic material.
Zhang Kaili, et al., Integrating Al with NiO nano honeycomb to realize an energetic material on silicon substrate. Appl. Phys. A (2009) 94 957-962

## Slide 104: Porous Ingredients
Nanoporous thermite..
Zhang Kaili, et al., Integrating Al with NiO nano honeycomb to realize an energetic material on silicon substrate. Appl. Phys. A (2009) 94 957-962
30° tilted view cross-section

## Slide 105: Porous Ingredients
Zhang Kaili, et al., Integrating Al with NiO nano honeycomb to realize an energetic material on silicon substrate. Appl. Phys. A (2009) 94 957-962
DTA and DSC results suggest that nano Al reacts with NiO nano honeycomb with an onset temperature of about 400°C. The reaction is based on the solid–solid diffusion mechanism. The total heat of the reaction of the thermite reactions is estimated to be about 2200 J/g.
The realized Al/NiO nano energetic material has the advantages of enhanced interfacial contact area, lowered ignition temperature, reduced impurities, and tailored dimensions.
Most interestingly, the Al/NiO nano energetic material is realized onto a silicon substrate, a basic material for microelectronics and microsystems. Therefore, this will probably open the door to integrate the nano energetic material into microsystems, thus leading to functional nanodevices.

## Slide 106: RAM
Advent of RAM mixing (Resonant Acoustic Mixing) game changer for nano mixing technology.
  Zac Durenbos, US Navy.
  Prof. Steve Son. Perdue University (Papers in IPS proceedings)
Advances in mixes for delay and ignition train compositions and devices
Printed ignition trains
  ttps://www.purdue.edu/newsroom/releases/2018/Q1/inkjet-printed-thermite-deposits-energetic-materials-safely.html