## Slide 1: Real Life Issues
These SLIDES PROVIDE THE SOLUTIONS TO THE QUESTIONS – THIS IS NOT EXAMINABLE

## Slide 2: Over-range Projectile
Problem :-
  During practice with 105mm ammunition from the Larkhill battery one projectile missed the impact area and left the range boundary, narrowly missing the Paddington to Penzance railway line. A total of 5 miles off course.
Cause
  The incident was attributed to the incorrect charge increments being used by the gun crew
Solution
  105mm practice charge re-introduced. Charge contains only increments 1, 2, and 3.

## Slide 3: Sawtoothing of pressure readings.
Chart: 
| Firing 1 | Firing 3 | Firing 4 | Firing 5 | Firing 6 | Firing 1 | Firing 3 | Firing 4 | Firing 5 | Firing 6 | Firing 1 | Firing 3 | Firing 4 | Firing 5 | Firing 6
Serial 1 | 822 | 830 | 835 | 842 | 827
Serial 2 | 835 | 840 | 849 | 832 | 839
Serial 3 | 845 | 850 | 857 | 867 | 832
Problem
Cause.
Main cause is de-coppering. Build-up of driving band material on the barrel which then clears. Series are either subject to ballistic creep or the early stages of ballistic hump. (Barrel surface crazes and expands then wears classically to give crash)
Solution.
Be aware of gun condition (Prefer to use gun in second quarter.)
Fire sufficient “warmers” on trials.

## Slide 4: Tin Coating Barrel
Problem.
  Globules of tin found inside a 4.5 inch naval gun after experimental firings.
Cause.
  Triple base propellant in 4.5 inch ammunition nor hot enough to vaporise tin and achieve effective de-coppering.
Solution
  Continue to use lead.

## Slide 5: Strange result at low temperatures
Problem
  Higher than expected pressure during low temperature firings.
Cause
  Propellant shatter due to incorrect quantities of plasticiser. Surface area increase. Pressure goes up!
Solution
  Investigate manufacturing process. REACH banned use of Di-Butyl Phthalate. Di-Octyl Sebacate and Di-Octyl Adipate were not “Plug and play” replacements!
Pressure
Temperature

## Slide 6: Increased Pressure 1
Problem
  Whilst firing a standard proof of 155mm Charges a firing of increment four gave a higher than anticipated pressure and MV.
Cause
  After an investigation calculating the degree of the effect (Which did not exceed system design parameters but was a statistical outlier) and counting back through the disposal / firing records it was concluded that an extra increment 2 was included in the firing.
Solution
  Increased training for proof range staff.
  Increased supervision during firing trials.

## Slide 7: Increased Pressure 2
Problem.
  During strength of design trials for 105mm ammunition a high-pressure proof charge gave a result which exceeded the design pressure for the gun (The gun was rendered US after the firing)
  The design pressure for the ammunition was also exceeded. However, the round fired was inert filled. Thus, potential consequences were not as severe.
Cause.
  The proof charges had to be specially built for the trials and were assembled in a shop which normally handles tank charges, The tank charge propellant, whist similar in size (0.6mm OD difference) uses a formulation with a much higher force constant. Both propellants are white slotted sticks. In the past the tank propellant would have been made with a coloured dye.
  The charges are manufactured at the factory then extra propellant is added to the charge on the trials site to adjust the pressure according to the needs of the trial. It is believed the extra propellant supplied was of the more vigorous type and that sticks were inserted in error.
Solutions
  Housekeeping improvements on the factory shop floor.
  Better segregation of propellant in magazines
  Pre-cutting of propelling sticks at the manufacturer to add an additional differentiator.
  Education and training of proof staff.