## Slide 1: Mechanical properties vs Furnace Times
William Jake Taylor
1909829
ACMA5009

## Slide 2: Introduction
William Jake Taylor
Pontyates Carmarthen
Gestamp talent Llanelli
Laboratory Technician
Mechanical properties
Weld integrity
Microscopic analysis

## Slide 3: Project Overview
USIBORE1500 material
Hot stamping
Resistance spot welding
Task at hand
Mechanical properties
NDT ultrasonic testing
Data
Conclusion
AlSi Coating
Hot Mount Resin
Diffusion Layer
Microstructure

## Slide 4: USIBOR1500
Intention to be heat treated
AlSi coating
Pros & Cons
Chemical composition
How the diffusion layer is created

## Slide 5: Hot stamping
purpose of hot stamping
Stages of hot stamping
What it does to the material
BCC lattice to FCC lattice
Phase Diagram
Over all performance of the part

## Slide 6: Resistance spot welding
How does it work ?
What is the purpose?
Why is it widely used?
Performance
Uses of resistance spot welding

## Slide 7: Task at hand
How does the material react with different furnace times
Bracket of dwell time to be conforming to customer standard
To find out how much the diffusion layer differs between each time
How thicker diffusion layer affects weld ability
Does longer furnace times change the mechanical properties
300 Seconds
1000 Seconds

## Slide 8: Mechanical properties testing
How the tensile test were conducted
How the Hardness test were conducted
How the Microscopic examination were conducted
Results
observations

## Slide 9: DT &NDT Ultra sonic testing
How the NDT test were conducted
Results
observations
How the DT test were conducted
Results
observations

## Slide 10: Data
What does the data show ?
        Diffusion layer increases per time in furnace
        NDT stopped detecting fusion at 800 seconds
        DT shows spot welds failing at 700 seconds
        Coating un affected because of supplier
Time seconds | Diffusion um | al coating um
300 | 7.08 | 39.24
400 | 14.42 | 42.47
500 | 15.5 | 43.18
600 | 18.39 | 47.84
700 | 19.5 | 45.63
800 | 23.23 | 41.7
900 | 24.11 | 44.23
1000 | 25.39 | 50.64
Spot 1 |  |  |  | Spot 2 |  | 
Time Seconds | T1 mm | T2 mm | Weld Length/ Dia mm | T1 mm | T2 mm | Weld Length / Dia mm
300 | 2.6 | 2.6 | 6.89 | 1.33 | 1.36 | 7.27
400 | 2.6 | 2.6 | 6.97 | 1.38 | 1.39 | 6.99
500 | 2.6 | 2.6 | 6.33 | 1.38 | 1.35 | 6.57
600 | 2.6 | 2.6 | 5.67 | 1.41 | 1.38 | 5.98
700 | 2.6 | 2.6 | 5.1 | 1.41 | 1.37 | 5.81
800 | 1.33 | 1.33 | 4.36 | 1.4 | 1.33 | 4.51
900 | 1.33 | 1.33 | 3.87 | 1.4 | 1.39 | 4.85
1000 | 1.33 | 1.33 | 3.48 | 1.36 | 1.38 | 3.35

## Slide 11: Conclusion
Overview of data analysis
Did it come out as intended
Does this support gestamp
What could have been done to improve

## Slide 12: Thanks for listening William Jake Taylor