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[bookmark: _Toc197264532]1.0 Introduction

In recent years, composite materials have become increasingly more popular and widely used in the automotive and motorsport industries and are even used to replace materials such as aluminium. This study aims to analyse and evaluate the properties of some of these materials and determine the benefits and setbacks that are associated with them. This includes a direct comparison between tensile strengths through testing, in addition to a comprehensive literature review. 
This study will also discuss the environmental and sustainability concerns that come with the use of these materials, as increasing environmental regulation and demand for sustainable materials have increased the interest in natural composites such as flax and hemp. These materials have shown promise in the use of components such as interior panels, and so further development to use them in a broader range of areas would be massively beneficial. Nonetheless, questions remain regarding their mechanical properties and degradation over time when compared to their synthetic counterparts.
The purpose of this investigation is to analyse and compare different carbon fibre, Kevlar, flax and hemp composites, and discuss the practicality and use case of each material, along with their environmental impacts and sustainability factors.






[bookmark: _Toc197264533]2.0 Composites Literature Review

[bookmark: _Toc197264534]2.1 Composite Materials Abstract
The increased popularity of composite materials in the automotive and motorsport industries is mostly due to the weight to strength ratio that many different composites have to offer, in addition to their resistance to corrosion, affordability, and design flexibility. All composite materials are formed by combining a fibre fabric (such as carbon, hemp, glass fibre etc.) with a resin. This combination maintains the spatial arrangement of fibres, preventing misalignment under stress (National Research Council, 2005). 
When forming these materials, the resin is soaked through each layer of fibre creating an extremely strong bond between the two materials, with the highest strength being along the direction of the fibres. For this reason, many composites are created with fibres in random directions, whereas some have the fibres aligned, to increase tensile strength across one specific axis.
There are however some downsides to using composite materials, one example of this is that the tensile strength is very unlikely to be equal in all directions. This is a major cause for concern when engineering components such as a vehicle chassis, which is likely to experience both stress and strain across a multitude of directions as it can be difficult to predict when a composite component may fail due to its structure having a weaker axis. 
Composite materials are also extremely sensitive to crack propagation and sudden failure due to their brittle nature. Surface imperfections from the manufacturing process or general wear can cause a very sudden, and catastrophic failure which is often unpredictable. These areas act as stress concentrators, and when under tension or shear deformation, a dominant crack often dictates the failure process, with its propagation path determining the strength of the composite (Zhang et al., 2021).
Another disadvantage to using composite materials, is the cost and difficulty to repair them.
[bookmark: _Toc197264535]2.2 Carbon Fiber Reinforced Polymer (CFRP)
Carbon Fibre Reinforced Polymers, commonly known as simply ‘carbon fibre’, is used in the higher end of the automotive and motorsport industries. Due to its high production cost, it is generally reserved for high performance vehicles and race applications where the reduced weight of the material is essential.
· Most widely used in motorsports (Formula 1, Le Mans, NASCAR, etc.).
· Extremely lightweight and strong.
· Used in monocoques, body panels, aerodynamic components, wheels, and suspension parts.
· Often combined with epoxy resin for high stiffness.
[bookmark: _Toc197264536]2.3 Glass Fibre Reinforced Polymer (GFRP)
· More affordable than carbon fibre but heavier.
· Commonly used in body kits, bumpers, interior panels, and aftermarket parts.
· Provides good impact resistance but lower stiffness than CFRP.
[bookmark: _Toc197264537]2.4 Kevlar (Aramid Fiber) Composites
· Often used in bullet-proofing, safety components, and reinforcement layers in CFRP.
· Highly resistant to impact and abrasion.
· Found in fuel tanks, cockpit safety structures, and wheel arch liners.
· Commonly used in safety equipment due to high impact and abrasion resistance, most notably motorcycle clothing.
[bookmark: _Toc197264538]2.5 Natural Fiber Composites (Flax, Hemp, and Basalt Fibers)
· Increasingly used for sustainability in production vehicles.
· Found in door panels, dashboards, and interior trims.
· Lightweight with decent mechanical properties but lower performance than CFRP.
[bookmark: _Toc197264539]2.6 Hybrid Composites (Carbon/Kevlar, Carbon/Basalt, etc.)
· Used to optimize material properties, such as improving impact resistance while maintaining strength.
· Found in protective structures, crash zones, and aerodynamic parts.
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[bookmark: _Toc197264541]3.1 Sustainability Abstract
The sustainability implications of using composite materials within the motorsport and automotive industries is becoming a growing concern, particularly around the environmental impacts of production, recyclability, and the availability of resources. To be discussed are the environmental impacts and sustainability issues with each of the composite materials tested in this investigation.
[bookmark: _Toc197264542]3.2 Carbon Fibre Composites
The production of carbon fibre is extremely energy-intensive and will typically consume between 198 – 595 MJ/kg of material produced. This is primarily due to the to the high temperature processing that is required (up to 3000°C) in an oxygen-free environment. This can result in substantial greenhouse gas emissions which is a huge obstacle and drawback to its production. In addition to this, the primary precursor for carbon fibre, polyacrylonitrile, is derived from petroleum, which raises concerns about resource availability (NitPro Composites, 2023; Zhang et al., 2020). 
Recycling carbon fibre composites can also be complicated due to the durability of the material and use of resins. Recycling methods will often degrade fibre quality, limiting reuse in high-performance applications. Pyrolysis is a method used to remove resin from the composite, however due to the thermal requirements this is also incredibly energy-intensive and can release harmful emissions (Composites Construction, 2022; NitPro Composites, 2023).
There have been many attempts at mitigating the environmental impact of producing carbon fibre composites, most notably Carbonium®, which is developed using aerospace by-products and offers a more sustainable alternative by reducing the environmental impact by 40-50% (Financial Times, 2024).
[bookmark: _Toc197264543]3.3 Kevlar Composites
The production of Kevlar involves the use of hazardous chemicals, most notably sulphuric acid which is used during the spinning process. This raises many environmental and safety concerns for its development in mass-production (Kevlar Web, 2023).
Unlike carbon fibre composites, Kevlar is 100% recyclable and can be repurposed in many ways. This involves chopping the material into small fibres which can then be re-spun into new products, however, if not properly disposed of then Kevlar can persist in landfills for very long periods due to its high resistance to degradation (Kevlar Web, 2023).
Whilst recyclable, Kevlar is a synthetic aramid fibre produced from petrochemical sources, making its availability dependant on fossil fuels, there is however some development in bio-based Kevlar alternatives, this research into natural fibre composites could potentially offer substitutes in the future.
[bookmark: _Toc197264544]3.4 Flax Composites
Flax fibres are generally considered to be much more environmentally friendly as they are biodegradable and require less energy during production. However, the cultivation of flax can contribute towards eutrophication and ecotoxicity due to the use of fertilisers and pesticides. Additionally, processing flax can be labour-intensive (Deng et al., 2015; Ma et al., 2023).
Flax fibres are often considered to be recyclable, however this can be debated. Natural fibres such as flax as susceptible to degradation during recycling which can compromise the integrity of the recycled material (Parodo et al., 2024). Flax is widely cultivated; however, the global production capacity has dropped from a peak of 1,000,000 tonnes in 2004 to approximately 300,000 tonnes in 2010. This raises concerns about its future availability (Deng et al., 2015).
[bookmark: _Toc197264545]3.5 Hemp Composites
Hemp cultivation is environmentally beneficial as it requires minimal pesticides and herbicides. It can also improve soil health and has a low water footprint. However, processing hemp into fibres can be an energy-intensive process. Hemp-based composites are also biodegradable and can be recycled, more so when combined with biodegradable resins. This makes them an attractive option for applications where end-of-life disposal is a consideration (Alliance for European Flax-Linen & Hemp, Unknown).
As hemp is cultivated globally, with China and France being leading producers, the crops adaptability to rapid growth makes it a very sustainable and available resource for composite materials. Overall, it is an excellent choice for an environmentally friendly composite material, especially when formed with a biodegradable resin.



[bookmark: _Toc197264546]4.0 Methodology

[bookmark: _Toc197264547]4.1 Equipment
The necessary equipment required for the investigation is as follows.
· Material Samples
· Tensile Testing Equipment
· Computer
· Vernier Callipers
· Safety Goggles
[bookmark: _Toc197264548]4.2 Safety Measures
To ensure a safe working environment, safety goggles are used throughout the entire experiment. In addition to this, it is imperative that nobody is to operate the computer at the same time as somebody installing or removing material from the machine. This is to ensure the safety of the person using the machine and reduces the risk of fingers or hands becoming trapped or cut by moving components.
[bookmark: _Toc197264549]4.3 Experimentation
The experimentation begins by selecting the material that is to be tested from the selection of material samples provided. From here, the testing samples width and thickness are accurately measured using vernier callipers, and this data is then entered into the computer software (figure 1) so that it’s tensile properties can be calculated accordingly. 
[image: A computer monitor with a blue screen
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Figure 1 - Computer Software During Experimentation
Once this is done, the material sample is fitted into the testing equipment (figure 2). This is done by loosening an upper and lower clamp and tightening them around the material sample at either end. A command is then made on the computer, telling the testing equipment to apply the correct amount of preload, until the material is firmly in place, but not under any significant tensile load. 
[image: A yellow liquid being poured into a machine
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Figure 2 - Material Testing Equipment Post-Failure
The tensile testing can then begin, with the testing equipment applying an increasing load to the component, whilst logging the applied force and total distance moved (how much the material has ‘stretched’) throughout the process. Once the material has failed, the test is stopped, and results are logged into a ‘.txt.’ file on the computer. In this file, key factors are logged such as the total time elapsed, the total load applied, stress, stress, and the total displacement. The material sample is then removed from the machine and the clamps are manually returned to their original position. This process is repeated twice for each material, to ensure that any outliers in the results are noticeable. 
The next material sample can then be tested, and the experiment can be repeated, once a new profile for the next material is made, including the name of the material, and its dimensions. Figure shows each material sample after testing.
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Figure 3 - Selection of Material Samples Post-Failure
[bookmark: _Toc197264550]5.0 Raw Data

[bookmark: _Toc197264551]5.1 Time vs. Applied Load


Figure 4 - Aluminium, Time vs. Load

Figure 5 - Carbon Non-Woven (Bio Resin), Time vs. Load

Figure 6 - Carbon Woven (Bio Resin), Time vs. Load

Figure 7 - Carbon Woven (Epoxy Resin), Time vs. Load

Figure 8 - Flax Non-Woven (Bio Resin), Time vs. Load

Figure 9 - Flax Woven (Bio Resin), Time vs. Load

Figure 10 - Hemp (Bio Resin), Time vs. Load

Figure 11 - Kevlar Woven (Bio Resin), Time vs. Load

[bookmark: _Toc197264552]5.2 Time vs. Stress


Figure 12 - Aluminium, Time vs. Stress

Figure 13 - Carbon Non-Woven (Bio Resin), Time vs. Stress

Figure 14 - Carbon Woven (Bio Resin), Time vs. Stress

Figure 15 - Carbon Woven (Epoxy Resin), Time vs. Stress

Figure 16 - Flax Non-Woven (Bio Resin), Time vs. Stress

Figure 17 - Flax Woven (Bio Resin), Time vs. Stress

Figure 18 - Hemp (Bio Resin), Time vs. Stress

Figure 19 - Kevlar Woven (Bio Resin), Time vs. Stress

[bookmark: _Toc197264553]5.3 Applied Load vs. Stress


Figure 20 - Aluminium, Load vs. Stress

Figure 21 - Carbon Non-Woven (Bio Resin), Load vs. Stress

Figure 22 - Carbon Non-Woven (Bio Resin), Load vs. Stress

Figure 23 - Carbon Woven (Epoxy Resin), Load vs. Stress

Figure 24 - Flax Non-Woven (Bio Resin), Load vs. Stress

Figure 25 - Flax Woven (Bio Resin), Load vs. Stress

Figure 26 - Hemp (Bio Resin), Load vs. Stress

Figure 27 - Kevlar Woven (Bio Resin), Load vs. Stress
[bookmark: _Toc197264554]5.4 Average Point of Failure
	Material
	Point of Failure (MPa)

	Aluminium
	23.27

	Non-Woven Carbon (Bio Resin)
	191.46

	Woven Carbon (Bio Resin)
	421.91

	Woven Carbon (Epoxy Resin)
	505.99

	Non-Woven Flax (Bio Resin)
	56.36

	Woven Flax (Bio Resin)
	76.37

	Non-Woven Hemp (Bio Resin)
	16.02

	Woven Kevlar (Bio Resin)
	317.87


Figure 28 - Average Point of Failure Data
[bookmark: _Toc197264555]5.5 Tensile Mechanical Properties
Below are the mechanical properties of each material, supplied as part of data sheets from Easy Composites Ltd, EcoTechnilin, and Pyrofil.
	
	Non-Woven Carbon Fibre Comp
	Twill Weave Kevlar Cloth
	Epoxy Infusion Bio-Resin
	Epoxy Infusion Resin
	Non-Woven Flax Fibre Comp
	Non-Woven Hemp Fibre
Comp
	Twill 3K Carbon Fibre Mat
	Twill Flax Fibre Comp

	Upper Tensile Strength (MPa)
	330
	3,000
	68
	72.25

	44
	108
	4,120
	61

	Lower Tensile Strength (MPa)
	290
	3,000
	68
	72.25
	37
	46
	4,120
	58

	Upper Modulus of Elasticity (GPa)
	35
	112.4
	3.04
	3.3
	5
	11
	234
	7

	Lower Modulus of Elasticity (GPa)
	25
	112.4
	3.04
	3.3
	5
	6
	234
	6


Figure 29 - Provided Material Properties
From here, the modulus of elasticity and tensile strength of the woven carbon fibre composites and Kevlar composite can be calculated using the rule of mixtures and composites. These calculations assume that the materials are combined at a 1:1 ratio by volume.
Shown below is each of these composites calculated material properties.
	
	Woven Kevlar (Bio Resin)
	Woven Carbon Fibre (Bio Resin)
	Woven Carbon Fibre (Epoxy Resin)

	Upper Tensile Strength (MPa)
	1,534
	2,094
	2,096.13

	Lower Tensile Strength (MPa)
	132.99
	133.79
	142.01

	Upper Modulus of Elasticity (GPa)
	57.72
	118.52
	118.65

	Lower Modulus of Elasticity (GPa)
	5.92
	6
	6.51


Figure 30 - Calculated Composite Material Properties




[bookmark: _Toc197264556]6.0 Results Analysis

The data collected from the tensile testing of composite materials shows varying mechanical behaviours between them, however these correlate with the inherent properties of each fibre, and their structural arrangements within the matrix. 
The three carbon fibre composites demonstrated the highest tensile strength among the tested material samples, which aligns with the calculated material properties (figure 30). Most notably, the woven carbon fibre and epoxy resin performed best with an average breaking point of nearly 506 MPa (figure 28). This is expected as the epoxy resin features the highest tensile strength, and modulus of elasticity out of the two resins, and the woven carbon fibre also has the strongest qualities amongst all the tested fibres (figure 28). This is likely due to the woven structure of interlaced fibres providing a higher tensile strength in the tested direction. The carbon fibre composites also demonstrated brittle characteristics, with little deformation prior to fracture. This can be seen when comparing figures 12 and 15, as the curved shape seen in figure 12 shows the aluminium deforming before failure, this however is not as present anywhere else.
The Kevlar composite proved to be another high-performance option but displayed slightly lower tensile strength compared to carbon fibre. It did however display marginally more deformation prior to failure. This is consistent with literature describing Kevlar’s toughness and impact resistance (Chung, 2010).
In contrast, the flax and hemp composites failed under considerably lower loads. Both materials failed in a progressive manner which suggests a more ductile failure mode. This variability in these results can be attributed towards inconsistencies in fibre alignment or natural defects inherent to biological materials (Dittenber and GangaRao, 2012). Despite their lower mechanical performance, these materials have much better potential for renewability and biodegradability which contribute positively to their overall sustainability.

[bookmark: _Toc197264557]7.0 Summary

Overall, the results from this experiment demonstrate a clear trade-off between mechanical performance and environmental impact. Synthetic fibres such as carbon fibre and Kevlar provide exceptional strength but pose significant challenges in terms of sustainability, particularly regarding recyclability and energy-intensive manufacturing. Natural fibres like flax and hemp offer environmentally advantageous alternatives with lower mechanical capabilities, suitable for non-structural or semi-structural applications where high strength is not as essential. These findings suggest that material selection for composites must be guided by both performance requirements and sustainability goals, especially in industries increasingly governed by environmental regulations. 
This experiment was able to successfully demonstrate the material properties of each sample and calculate their theoretical properties which aligned with both the test data, and external literature. Given more time and resources, further research could be conducted into analysing the effects of fibre alignment with a composite and how this may affect tensile strength in different directions, as well as surface imperfections.


[bookmark: _Toc197264558]7.0 Bibliography

· Alliance for European Flax-Linen & Hemp. (Unknown). Eco-design and composite materials. Available at: https://allianceflaxlinenhemp.eu/en/flax-lin-tex-tech/flax-tex-and-tech/eco-design-composite-materials [Accessed: 4 May 2025].

· Chung, D.D.L. (2010). Composite Materials: Science and Applications. 2nd ed. London: Springer.

· Composites Construction UK. (2022). Is Carbon Fibre a Sustainable Material for Strengthening Buildings and Structures? Available at: https://www.fibrwrap-ccuk.com/carbon-fibre-strengthening/is-carbon-fibre-a-sustainable-material-for-strengthening-buildings-and-structures/ [Accessed: 4 May 2025].

· Deng, Y. & Tian, Y. (2015). Assessing the Environmental Impact of Flax Fibre Reinforced Polymer Composite from a Consequential Life Cycle Assessment Perspective. Sustainability, 7(9), pp.11462–11484.

· Dittenber, D.B. & GangaRao, H.V.S. (2012). Critical review of recent publications on use of natural composites in infrastructure. Composites Part A: Applied Science and Manufacturing, 43(8), pp.1419–1429.

· Financial Times. (2024). Industry warms up to sustainable carbonium alloy. Available at: https://www.ft.com/content/1d376690-2c75-454e-88bd-e291349a97e2 [Accessed: 4 May 2025].

· Ma, H., Guna, V., Raju, T., Murthy, A. & Reddy, N. (2023). Converting flax processing waste into value added biocomposites. Industrial Crops and Products, 195, 116434.

· National Research Council. (2005). High-Performance Structural Fibers for Advanced Polymer Matrix Composites. Washington, DC: The National Academies Press.

· NitPro Composites. (2023). Sustainability in Carbon Fiber Production: Challenges and Green Solutions. Available at: https://www.nitprocomposites.com/blog/sustainability-in-carbon-fiber-production [Accessed: 4 May 2025].

· Parodo, G., Sorrentino, L., Turchetta, S. & Moffa, G. (2024). Manufacturing of Sustainable Composite Materials: The Challenge of Flax Fiber and Polypropylene. Materials, 17(19), p.4768.

· Zhang, J., Chevali, V., Wang, H. & Wang, C. (2020). Current status of carbon fibre and carbon fibre composites recycling. Composites Part B: Engineering, 193, 108053.

· Zhang, Y., Li, J. & Wang, Q. (2021). Influence of Cracks and Voids on the Responses of Composites. Composites Part B: Engineering, 223, 109102.
Aluminium - Time vs Load

Alu 1 Time v lLoad	0	0	0.02	0.04	0.06	0.08	0.10100000000000001	0.121	0.14099999999999999	0.16	0.18099999999999999	0.20100000000000001	0.221	0.24099999999999999	0.26	0.28000000000000003	0.3	0.32	0.34	0.36099999999999999	0.38	0.4	0.42	0.441	0.46100000000000002	0.48	0.5	0.51900000000000002	0.53900000000000003	0.56000000000000005	0.57999999999999996	0.6	0.62	0.64	0.66	0.68	0.7	0.72	0.74	0.75900000000000001	0.78	0.8	0.82	0.84	0.86	0.88	0.9	0.92	0.94	0.96	0.98	0.999	1.0189999999999999	1.04	1.0589999999999999	1.079	1.1000000000000001	1.1200000000000001	1.1399999999999999	1.1599999999999999	1.179	1.1990000000000001	1.2190000000000001	1.2390000000000001	1.2589999999999999	1.2789999999999999	1.2989999999999999	1.319	1.339	1.359	1.379	1.399	1.419	1.4390000000000001	1.4590000000000001	1.4790000000000001	1.4990000000000001	1.5189999999999999	1.5389999999999999	1.5589999999999999	1.579	1.599	1.619	1.639	1.659	1.679	1.6990000000000001	1.7190000000000001	1.7390000000000001	1.7589999999999999	1.7789999999999999	1.7989999999999999	1.819	1.839	1.8580000000000001	1.879	1.899	1.919	1.9390000000000001	1.9590000000000001	1.9790000000000001	1.9990000000000001	2.0190000000000001	2.0390000000000001	2.0590000000000002	2.0790000000000002	2.0990000000000002	2.1190000000000002	2.1379999999999999	2.1589999999999998	2.1779999999999999	2.198	2.218	2.2389999999999999	2.258	2.278	2.2989999999999999	2.319	2.339	2.359	2.3780000000000001	2.3980000000000001	2.419	2.4380000000000002	2.4590000000000001	2.4780000000000002	2.4980000000000002	2.5179999999999998	2.5379999999999998	2.5579999999999998	2.5779999999999998	2.5979999999999999	2.6179999999999999	2.6379999999999999	2.6579999999999999	2.6779999999999999	2.698	2.7189999999999999	2.738	2.758	2.778	2.798	2.8180000000000001	2.8380000000000001	2.8580000000000001	2.8780000000000001	2.8980000000000001	2.9180000000000001	2.9380000000000002	2.9580000000000002	2.9780000000000002	2.9980000000000002	3.0179999999999998	3.0369999999999999	3.0579999999999998	3.0779999999999998	3.097	3.117	3.1379999999999999	3.1579999999999999	3.1779999999999999	3.1970000000000001	3.218	3.238	3.258	3.278	3.2970000000000002	3.3170000000000002	3.3370000000000002	3.3570000000000002	3.3769999999999998	3.3969999999999998	3.4169999999999998	3.4369999999999998	3.4569999999999999	3.4769999999999999	3.4969999999999999	3.5169999999999999	3.5369999999999999	3.5569999999999999	3.577	3.597	3.6160000000000001	3.637	3.657	3.677	3.6970000000000001	3.7170000000000001	3.7370000000000001	3.7570000000000001	3.7770000000000001	3.7970000000000002	3.8170000000000002	3.8370000000000002	3.8570000000000002	3.8769999999999998	3.8969999999999998	3.9159999999999999	3.9369999999999998	3.9569999999999999	3.9769999999999999	3.9969999999999999	4.0170000000000003	4.0369999999999999	4.0570000000000004	4.077	4.0960000000000001	4.1159999999999997	4.1369999999999996	4.1559999999999997	4.1760000000000002	4.1970000000000001	4.2169999999999996	4.2370000000000001	4.2560000000000002	4.2770000000000001	4.2969999999999997	4.3159999999999998	4.3360000000000003	4.3559999999999999	4.3760000000000003	4.3970000000000002	4.4160000000000004	4.4359999999999999	4.4560000000000004	4.4770000000000003	4.4960000000000004	4.516	4.5359999999999996	4.5570000000000004	4.5759999999999996	4.5960000000000001	4.6159999999999997	4.6360000000000001	4.6559999999999997	4.6760000000000002	4.6959999999999997	4.7160000000000002	4.7359999999999998	4.7560000000000002	4.7759999999999998	4.7960000000000003	4.8159999999999998	4.8360000000000003	4.8559999999999999	4.8760000000000003	4.8949999999999996	4.915	4.9359999999999999	4.9560000000000004	4.976	4.9960000000000004	5.016	5.0350000000000001	5.0549999999999997	5.0759999999999996	5.0960000000000001	5.1159999999999997	5.1349999999999998	5.1550000000000002	5.1760000000000002	5.1950000000000003	5.2149999999999999	5.2359999999999998	5.2560000000000002	5.2759999999999998	5.2960000000000003	5.3150000000000004	5.335	5.3550000000000004	5.375	5.3949999999999996	5.415	5.4349999999999996	5.4550000000000001	5.4749999999999996	5.4950000000000001	5.5149999999999997	5.5350000000000001	5.5549999999999997	5.5759999999999996	5.5949999999999998	5.6150000000000002	5.6349999999999998	5.6550000000000002	5.6749999999999998	5.6950000000000003	5.7149999999999999	5.7350000000000003	5.7549999999999999	5.7759999999999998	5.7949999999999999	5.8150000000000004	5.835	5.8540000000000001	5.8739999999999997	5.8949999999999996	5.915	5.9349999999999996	5.9550000000000001	5.9740000000000002	5.9950000000000001	6.0140000000000002	6.0350000000000001	6.0549999999999997	6.0739999999999998	6.0949999999999998	6.1139999999999999	6.1340000000000003	6.1539999999999999	6.1740000000000004	6.1950000000000003	6.2140000000000004	6.2350000000000003	6.2549999999999999	6.274	6.2939999999999996	6.3150000000000004	6.3339999999999996	6.3540000000000001	6.3739999999999997	6.3940000000000001	6.4139999999999997	6.4349999999999996	6.4539999999999997	6.4749999999999996	6.4950000000000001	6.5140000000000002	6.5339999999999998	6.5549999999999997	6.5739999999999998	6.5940000000000003	6.6139999999999999	6.6340000000000003	6.6539999999999999	6.6740000000000004	6.694	6.7140000000000004	6.734	6.7539999999999996	6.774	6.7939999999999996	6.8140000000000001	6.8339999999999996	6.8540000000000001	6.8730000000000002	6.8940000000000001	6.9130000000000003	6.9329999999999998	6.9539999999999997	6.9729999999999999	6.9930000000000003	7.0140000000000002	7.0330000000000004	7.0529999999999999	7.0730000000000004	7.0940000000000003	7.1139999999999999	7.1340000000000003	7.1529999999999996	7.173	7.1929999999999996	7.2140000000000004	7.234	7.2539999999999996	7.274	7.2930000000000001	7.3129999999999997	7.3339999999999996	7.3529999999999998	7.3730000000000002	7.3940000000000001	7.4130000000000003	7.4340000000000002	7.4539999999999997	7.4729999999999999	7.4939999999999998	7.5140000000000002	7.5330000000000004	7.5540000000000003	7.5730000000000004	7.5940000000000003	7.6130000000000004	7.633	7.6529999999999996	7.673	7.6929999999999996	7.7130000000000001	7.7329999999999997	7.7530000000000001	7.7729999999999997	7.7930000000000001	7.8129999999999997	7.8330000000000002	7.8529999999999998	7.8730000000000002	7.8929999999999998	7.9130000000000003	7.9329999999999998	7.9530000000000003	7.9729999999999999	7.9930000000000003	8.0120000000000005	8.032	8.0530000000000008	8.0730000000000004	8.0920000000000005	8.1120000000000001	8.1329999999999991	8.1519999999999992	8.1720000000000006	8.1920000000000002	8.2129999999999992	8.2319999999999993	8.2530000000000001	8.2729999999999997	8.2919999999999998	8.3130000000000006	8.3330000000000002	8.3529999999999998	8.3719999999999999	8.3930000000000007	8.4120000000000008	8.4329999999999998	8.4529999999999994	8.4719999999999995	8.4920000000000009	8.5120000000000005	8.532	8.5519999999999996	8.5719999999999992	8.593	8.6129999999999995	8.6319999999999997	8.6519999999999992	8.6720000000000006	8.6920000000000002	8.7119999999999997	8.7319999999999993	8.7520000000000007	8.7720000000000002	8.7919999999999998	8.8119999999999994	8.8320000000000007	8.8520000000000003	8.8719999999999999	8.8919999999999995	8.9120000000000008	8.9320000000000004	8.952	8.9719999999999995	8.9920000000000009	9.0120000000000005	9.032	9.0519999999999996	9.0719999999999992	9.0909999999999993	9.1120000000000001	9.1319999999999997	9.1519999999999992	9.1720000000000006	9.1920000000000002	9.2119999999999997	9.2319999999999993	9.2520000000000007	9.2710000000000008	9.2910000000000004	9.3109999999999999	9.3320000000000007	9.3510000000000009	9.3719999999999999	9.3919999999999995	9.4120000000000008	9.4320000000000004	9.452	9.4710000000000001	9.4909999999999997	9.5120000000000005	9.5310000000000006	9.5519999999999996	9.5709999999999997	9.5920000000000005	9.6120000000000001	9.6310000000000002	9.6519999999999992	9.6709999999999994	9.6910000000000007	9.7110000000000003	9.7309999999999999	9.7509999999999994	9.7710000000000008	9.7910000000000004	9.8109999999999999	9.8309999999999995	9.8510000000000009	9.8710000000000004	9.891	9.9109999999999996	9.9309999999999992	9.9510000000000005	9.9710000000000001	9.9909999999999997	10.01	10.031000000000001	10.051	10.07	10.090999999999999	10.111000000000001	10.131	10.15	10.17	10.191000000000001	10.211	10.23	10.250999999999999	10.271000000000001	10.29	10.311	10.331	10.35	10.37	10.391	10.411	10.43	10.45	10.47	10.49	10.510999999999999	10.53	10.55	10.57	10.59	10.61	10.63	10.65	10.670999999999999	10.69	10.71	10.73	10.75	10.77	10.791	10.81	10.83	10.85	10.87	10.89	10.91	10.930999999999999	10.95	10.97	10.99	11.01	11.03	11.048999999999999	11.069000000000001	11.09	11.11	11.13	11.148999999999999	11.17	11.19	11.21	11.228999999999999	11.249000000000001	11.27	11.29	11.31	11.329000000000001	11.349	11.369	11.388999999999999	11.41	11.43	11.45	11.47	11.489000000000001	11.509	11.529	11.55	11.57	11.59	11.61	11.629	11.648999999999999	11.669	11.689	11.71	11.73	11.749000000000001	11.769	11.789	11.808999999999999	11.829000000000001	11.849	11.869	11.888999999999999	11.909000000000001	11.929	11.949	11.968999999999999	11.989000000000001	12.007999999999999	12.029	12.048999999999999	12.068	12.089	12.108000000000001	12.128	12.148	12.169	12.189	12.209	12.228	12.247999999999999	12.269	12.288	12.308999999999999	12.329000000000001	12.348000000000001	12.368	12.388	12.407999999999999	12.428000000000001	12.449	12.468	12.488	12.509	12.528	12.548	12.568	12.587999999999999	12.608000000000001	12.628	12.648	12.669	12.688000000000001	12.708	12.728999999999999	12.749000000000001	12.768000000000001	12.788	12.808	12.829000000000001	12.848000000000001	12.868	12.888	12.907999999999999	12.928000000000001	12.948	12.968	12.988	13.007999999999999	13.028	13.048	13.068	13.087999999999999	13.108000000000001	13.128	13.148	13.167	13.188000000000001	13.208	13.228	13.247999999999999	13.268000000000001	13.287000000000001	13.307	13.327	13.348000000000001	13.367000000000001	13.388	13.407	13.427	13.446999999999999	13.468	13.488	13.507	13.528	13.548	13.568	13.587	13.606999999999999	13.627000000000001	13.648	13.667999999999999	13.686999999999999	13.708	13.728	13.747999999999999	13.766999999999999	13.787000000000001	13.807	13.827	13.847	13.867000000000001	13.887	13.907999999999999	13.927	13.946999999999999	13.967000000000001	13.987	14.007	14.026999999999999	14.047000000000001	14.067	14.086	14.106999999999999	14.127000000000001	14.147	14.167	14.186999999999999	14.207000000000001	14.227	14.247	14.266	14.286	14.307	14.327	14.347	14.366	14.385999999999999	14.407	14.426	14.446	14.465999999999999	14.487	14.507	14.526	14.545999999999999	14.566000000000001	14.587	14.606	14.625999999999999	14.646000000000001	14.666	14.686	14.706	14.726000000000001	14.746	14.766999999999999	14.786	14.805999999999999	14.826000000000001	14.846	14.866	14.885999999999999	14.906000000000001	14.926	14.946	14.965999999999999	14.986000000000001	15.006	15.026	15.045999999999999	15.066000000000001	15.086	15.105	15.125999999999999	15.146000000000001	15.166	15.186	15.206	15.225	15.246	15.266	15.285	15.305999999999999	15.326000000000001	15.346	15.366	15.385	15.406000000000001	15.427	15.445	15.465999999999999	15.486000000000001	15.505000000000001	15.525	15.545	15.566000000000001	15.586	15.606	15.625	15.645	15.666	15.685	15.705	15.725	15.746	15.765000000000001	15.786	15.805	15.824999999999999	15.845000000000001	15.865	15.885	15.904999999999999	15.925000000000001	15.945	15.965	15.984999999999999	16.004999999999999	16.024999999999999	16.045000000000002	16.065000000000001	16.085000000000001	16.103999999999999	16.125	16.145	16.164000000000001	16.184999999999999	16.204999999999998	16.224	16.245000000000001	16.265000000000001	16.285	16.305	16.324999999999999	16.344000000000001	16.364000000000001	16.384	16.405000000000001	16.425000000000001	16.445	16.463999999999999	16.484000000000002	16.504999999999999	16.524999999999999	16.545000000000002	16.565000000000001	16.585000000000001	16.603999999999999	16.625	16.645	16.664000000000001	16.684000000000001	16.704000000000001	16.724	16.745000000000001	16.765000000000001	16.783999999999999	16.803999999999998	16.824000000000002	16.844999999999999	16.864000000000001	16.884	16.904	16.925000000000001	16.943999999999999	16.963999999999999	16.984999999999999	17.004000000000001	17.024999999999999	17.044	17.064	17.084	17.103999999999999	17.123999999999999	17.143999999999998	17.164000000000001	17.184000000000001	17.204000000000001	17.224	17.244	17.263000000000002	17.283999999999999	17.303999999999998	17.323	17.343	17.363	17.382999999999999	17.402999999999999	17.422999999999998	17.443000000000001	17.463000000000001	17.483000000000001	17.503	17.524000000000001	17.544	17.562999999999999	17.584	17.603000000000002	17.623999999999999	17.643999999999998	17.663	17.684000000000001	17.704000000000001	17.722999999999999	17.744	17.763999999999999	17.783000000000001	17.803000000000001	17.823	17.844000000000001	17.863	17.882999999999999	17.902999999999999	17.922999999999998	17.943000000000001	17.963000000000001	17.984000000000002	18.003	18.023	18.042999999999999	18.062999999999999	18.082999999999998	18.103000000000002	18.123000000000001	18.143000000000001	18.163	18.183	18.202999999999999	18.222999999999999	18.242999999999999	18.263000000000002	18.283000000000001	18.303000000000001	18.323	18.341999999999999	18.361999999999998	18.382999999999999	18.402000000000001	18.422000000000001	18.443000000000001	18.463000000000001	18.481999999999999	18.501999999999999	18.521999999999998	18.542000000000002	18.562000000000001	18.582000000000001	18.602	18.622	18.643000000000001	18.661999999999999	18.683	18.702000000000002	18.722999999999999	18.742999999999999	18.762	18.783000000000001	18.803000000000001	18.823	18.841999999999999	18.861999999999998	18.882000000000001	18.902000000000001	18.922000000000001	18.942	18.962	18.981999999999999	19.001999999999999	19.021999999999998	19.042000000000002	19.062000000000001	19.082000000000001	19.102	19.123000000000001	19.141999999999999	19.161000000000001	19.181999999999999	19.202000000000002	19.221	19.242000000000001	19.262	19.282	19.302	19.321999999999999	19.341000000000001	19.361999999999998	19.382000000000001	19.402000000000001	19.422000000000001	19.442	19.462	19.481999999999999	19.501999999999999	19.521000000000001	19.542000000000002	19.561	19.582000000000001	19.602	19.622	19.640999999999998	19.661000000000001	19.681000000000001	19.701000000000001	19.721	19.741	19.762	19.782	19.800999999999998	19.821000000000002	19.841000000000001	19.861000000000001	19.881	19.901	19.920999999999999	19.940999999999999	19.960999999999999	19.981000000000002	20.001000000000001	20.021000000000001	20.042000000000002	20.061	20.081	20.100999999999999	20.120999999999999	20.140999999999998	20.161000000000001	20.181000000000001	20.201000000000001	20.221	20.239999999999998	20.260999999999999	20.280999999999999	20.300999999999998	20.321000000000002	20.341000000000001	20.36	20.38	20.401	20.420999999999999	20.440000000000001	20.460999999999999	20.481000000000002	20.501000000000001	20.52	20.541	20.56	20.581	20.600999999999999	20.62	20.640999999999998	20.66	20.681000000000001	20.7	20.721	20.74	20.76	20.78	20.8	20.82	20.84	20.86	20.881	20.901	20.92	20.94	20.96	20.98	21	21.02	21.04	21.06	21.08	21.1	21.12	21.140999999999998	21.16	21.181000000000001	21.2	21.22	21.24	21.26	21.279	21.3	21.32	21.338999999999999	21.36	21.38	21.4	21.42	21.44	21.46	21.478999999999999	21.498999999999999	21.518999999999998	21.54	21.56	21.58	21.599	21.619	21.64	21.66	21.68	21.7	21.719000000000001	21.74	21.759	21.78	21.798999999999999	21.818999999999999	21.838999999999999	21.859000000000002	21.879000000000001	21.899000000000001	21.919	21.939	21.96	21.978999999999999	21.998999999999999	22.018999999999998	22.039000000000001	22.059000000000001	22.079000000000001	22.099	22.119	22.14	22.158999999999999	22.178999999999998	22.199000000000002	22.219000000000001	22.239000000000001	22.259	22.279	22.298999999999999	22.318999999999999	22.338999999999999	22.359000000000002	22.379000000000001	22.398	22.419	22.439	22.459	22.478999999999999	22.498000000000001	22.518999999999998	22.539000000000001	22.559000000000001	22.579000000000001	22.599	22.617999999999999	22.638000000000002	22.658000000000001	22.678999999999998	22.699000000000002	22.719000000000001	22.738	22.757999999999999	22.777999999999999	22.797999999999998	22.818000000000001	22.838999999999999	22.859000000000002	22.879000000000001	22.898	22.919	22.937999999999999	22.959	22.978999999999999	22.998000000000001	23.018999999999998	23.038	23.058	23.077999999999999	23.097999999999999	23.119	23.138000000000002	23.158000000000001	23.178000000000001	23.198	23.218	23.239000000000001	23.257000000000001	23.277999999999999	23.297999999999998	23.318000000000001	23.337	23.358000000000001	23.376999999999999	23.398	23.417000000000002	23.437999999999999	23.457999999999998	23.478000000000002	23.498000000000001	23.518000000000001	23.538	23.558	23.577999999999999	23.597000000000001	23.617999999999999	23.637	23.658000000000001	23.677	23.696999999999999	23.718	23.736999999999998	23.757999999999999	23.777000000000001	23.797999999999998	23.818000000000001	23.837	23.856999999999999	23.876999999999999	23.896999999999998	23.917000000000002	23.937000000000001	23.957999999999998	23.977	23.997	24.018000000000001	24.038	24.056999999999999	24.077999999999999	24.097999999999999	24.117000000000001	24.137	24.157	24.177	24.196999999999999	24.216999999999999	24.236999999999998	24.257000000000001	24.277000000000001	24.297000000000001	24.317	24.337	24.356999999999999	24.376999999999999	24.396999999999998	24.417000000000002	24.437000000000001	24.457000000000001	24.477	24.497	24.516999999999999	24.536000000000001	24.556000000000001	24.577000000000002	24.597000000000001	24.616	24.635999999999999	24.657	24.677	24.696999999999999	24.716999999999999	24.736999999999998	24.756	24.777000000000001	24.795999999999999	24.815999999999999	24.835999999999999	24.856000000000002	24.876000000000001	24.896000000000001	24.916	24.936	24.957000000000001	24.975999999999999	24.995999999999999	25.015999999999998	25.036000000000001	25.056000000000001	25.076000000000001	25.096	25.116	25.135999999999999	25.155999999999999	25.175999999999998	25.196000000000002	25.216000000000001	25.236000000000001	25.256	25.276	25.295999999999999	25.315999999999999	25.335999999999999	25.356000000000002	25.376000000000001	25.396000000000001	25.416	25.436	25.454999999999998	25.475999999999999	25.495999999999999	25.515999999999998	25.536000000000001	25.556000000000001	25.574999999999999	25.594999999999999	25.614999999999998	25.635999999999999	25.655999999999999	25.675999999999998	25.695	25.716000000000001	25.734999999999999	25.756	25.776	25.795999999999999	25.815000000000001	25.835000000000001	25.856000000000002	25.876000000000001	25.896000000000001	25.916	25.934999999999999	25.956	25.975000000000001	25.995000000000001	26.015000000000001	26.036000000000001	26.056000000000001	26.074999999999999	26.094999999999999	26.114999999999998	26.135000000000002	26.155000000000001	26.175000000000001	26.195	26.215	26.234999999999999	26.254999999999999	26.276	26.295000000000002	26.315000000000001	26.334	26.355	26.375	26.393999999999998	26.414999999999999	26.434999999999999	26.454999999999998	26.475000000000001	26.495000000000001	26.515000000000001	26.535	26.555	26.574999999999999	26.594999999999999	26.614000000000001	26.635000000000002	26.654	26.675000000000001	26.695	26.715	26.734999999999999	26.754999999999999	26.774999999999999	26.795000000000002	26.815000000000001	26.835000000000001	26.853999999999999	26.873999999999999	26.893999999999998	26.914999999999999	26.934999999999999	26.954000000000001	26.974	26.994	27.015000000000001	27.035	27.055	27.074000000000002	27.094000000000001	27.114000000000001	27.134	27.155000000000001	27.173999999999999	27.193999999999999	27.213999999999999	27.234000000000002	27.254999999999999	27.274000000000001	27.294	27.314	27.334	27.353999999999999	27.373999999999999	27.393999999999998	27.414000000000001	27.433	27.454000000000001	27.472999999999999	27.492999999999999	27.513999999999999	27.533999999999999	27.553999999999998	27.574000000000002	27.593	27.614000000000001	27.634	27.652999999999999	27.673999999999999	27.693000000000001	27.713000000000001	27.734000000000002	27.754000000000001	27.774000000000001	27.794	27.814	27.834	27.853000000000002	27.873000000000001	27.893000000000001	27.914000000000001	27.933	27.952999999999999	27.974	27.992999999999999	28.013000000000002	28.033999999999999	28.053000000000001	28.073	28.094000000000001	28.114000000000001	28.132999999999999	28.154	28.172999999999998	28.193000000000001	28.213000000000001	28.233000000000001	28.253	28.274000000000001	28.292999999999999	28.312999999999999	28.332999999999998	28.353000000000002	28.373000000000001	28.393000000000001	28.413	28.433	28.452999999999999	28.472000000000001	28.492999999999999	28.513000000000002	28.533000000000001	28.553000000000001	28.573	28.593	28.613	28.632999999999999	28.652000000000001	28.672000000000001	28.692	28.713000000000001	28.733000000000001	28.753	28.771999999999998	28.792999999999999	28.812000000000001	28.832999999999998	28.853000000000002	28.873000000000001	28.893000000000001	28.913	28.933	28.952000000000002	28.972000000000001	28.992000000000001	29.012	29.032	29.052	29.073	29.093	29.113	29.132000000000001	29.152000000000001	29.172999999999998	29.192	29.213000000000001	29.231999999999999	29.253	29.271999999999998	29.292000000000002	29.312000000000001	29.332999999999998	29.352	29.372	29.391999999999999	29.411999999999999	29.431999999999999	29.452000000000002	29.472000000000001	29.492000000000001	29.512	29.532	29.552	29.571999999999999	29.591999999999999	29.611999999999998	29.632000000000001	29.651	29.672000000000001	29.692	29.710999999999999	29.731999999999999	29.751999999999999	29.771999999999998	29.792000000000002	29.812000000000001	29.832000000000001	29.852	29.872	29.891999999999999	29.911999999999999	29.931999999999999	29.951000000000001	29.971	29.991	30.010999999999999	30.030999999999999	30.052	30.071999999999999	30.091999999999999	30.111000000000001	30.132000000000001	30.151	30.170999999999999	30.190999999999999	30.212	30.231000000000002	30.251999999999999	30.271000000000001	30.291	30.311	30.331	30.352	30.370999999999999	30.391999999999999	30.411999999999999	30.431000000000001	30.451000000000001	30.471	30.491	30.510999999999999	30.530999999999999	30.550999999999998	30.571000000000002	30.591000000000001	30.611000000000001	30.631	30.651	30.670999999999999	30.69	30.710999999999999	30.731000000000002	30.75	30.77	30.791	30.811	30.83	30.850999999999999	30.870999999999999	30.890999999999998	30.91	30.931000000000001	30.951000000000001	30.971	30.991	31.010999999999999	31.030999999999999	31.050999999999998	31.07	31.09	31.11	31.131	31.151	31.170999999999999	31.190999999999999	31.210999999999999	31.23	31.25	31.27	31.29	31.311	31.33	31.35	31.370999999999999	31.390999999999998	31.411000000000001	31.43	31.45	31.47	31.49	31.51	31.53	31.55	31.57	31.59	31.61	31.63	31.65	31.669	31.69	31.709	31.73	31.75	31.77	31.79	31.81	31.829000000000001	31.85	31.87	31.89	31.91	31.928999999999998	31.949000000000002	31.97	31.99	32.009	32.029000000000003	32.049999999999997	32.069000000000003	32.088999999999999	32.109000000000002	32.130000000000003	32.15	32.17	32.19	32.209000000000003	32.228999999999999	32.249000000000002	32.268999999999998	32.29	32.31	32.329000000000001	32.35	32.369999999999997	32.389000000000003	32.408999999999999	32.43	32.448999999999998	32.468000000000004	32.488999999999997	32.509	32.529000000000003	32.548999999999999	32.569000000000003	32.588999999999999	32.61	32.628	32.649000000000001	32.668999999999997	32.689	32.709000000000003	32.728999999999999	32.749000000000002	32.768999999999998	32.787999999999997	32.808	32.829000000000001	32.848999999999997	32.869	32.889000000000003	32.908999999999999	32.929000000000002	32.948999999999998	32.969000000000001	32.988	33.008000000000003	33.027999999999999	33.048999999999999	33.069000000000003	33.088999999999999	33.109000000000002	33.128	33.149000000000001	33.168999999999997	33.188000000000002	33.209000000000003	33.228999999999999	33.249000000000002	33.268000000000001	33.287999999999997	33.308	33.328000000000003	33.347999999999999	33.368000000000002	33.387999999999998	33.408000000000001	33.427999999999997	33.448	33.468000000000004	33.488	33.508000000000003	33.527999999999999	33.548000000000002	33.567999999999998	33.588999999999999	33.607999999999997	33.628	33.648000000000003	33.667000000000002	33.688000000000002	33.707999999999998	33.728000000000002	33.747	33.768000000000001	33.787999999999997	33.808	33.826999999999998	33.847000000000001	33.868000000000002	33.887999999999998	33.908000000000001	33.927	33.947000000000003	33.968000000000004	33.988	34.008000000000003	34.027000000000001	34.046999999999997	34.067999999999998	34.088000000000001	34.106999999999999	34.128	34.148000000000003	34.167000000000002	34.186999999999998	34.207000000000001	34.228000000000002	34.247999999999998	34.267000000000003	34.286999999999999	34.307000000000002	34.328000000000003	34.347000000000001	34.366999999999997	34.387	34.406999999999996	34.427	34.447000000000003	34.466999999999999	34.487000000000002	34.506999999999998	34.527000000000001	34.546999999999997	34.567	34.587000000000003	34.606999999999999	34.627000000000002	34.646999999999998	34.667000000000002	34.686999999999998	34.706000000000003	34.726999999999997	34.747	34.767000000000003	34.786999999999999	34.807000000000002	34.826999999999998	34.847000000000001	34.866999999999997	34.886000000000003	34.906999999999996	34.926000000000002	34.947000000000003	34.966999999999999	34.987000000000002	35.006999999999998	35.027000000000001	35.046999999999997	35.067	35.087000000000003	35.106000000000002	35.127000000000002	35.146000000000001	35.167000000000002	35.186	35.206000000000003	35.226999999999997	35.246000000000002	35.265999999999998	35.286000000000001	35.305999999999997	35.326000000000001	35.345999999999997	35.366	35.387	35.405999999999999	35.426000000000002	35.447000000000003	35.466000000000001	35.487000000000002	35.506	35.526000000000003	35.545999999999999	35.566000000000003	35.585999999999999	35.606000000000002	35.625999999999998	35.646000000000001	35.665999999999997	35.686	35.706000000000003	35.725999999999999	35.747	35.765999999999998	35.786000000000001	35.805999999999997	35.826000000000001	35.844999999999999	35.865000000000002	35.886000000000003	35.905999999999999	35.926000000000002	35.945	35.965000000000003	35.984999999999999	36.006	36.026000000000003	36.045999999999999	36.066000000000003	36.085000000000001	36.106000000000002	36.125	36.145000000000003	36.165999999999997	36.186	36.206000000000003	36.225000000000001	36.244999999999997	36.265000000000001	36.284999999999997	36.305	36.325000000000003	36.344999999999999	36.365000000000002	36.384999999999998	36.405000000000001	36.424999999999997	36.445	36.465000000000003	36.484999999999999	36.505000000000003	36.524999999999999	36.545000000000002	36.564999999999998	36.585000000000001	36.604999999999997	36.625999999999998	36.645000000000003	36.664999999999999	36.685000000000002	36.704999999999998	36.725000000000001	36.744999999999997	36.765000000000001	36.784999999999997	36.805	36.825000000000003	36.844000000000001	36.865000000000002	36.884999999999998	36.905000000000001	36.924999999999997	36.945	36.965000000000003	36.984999999999999	37.005000000000003	37.024999999999999	37.043999999999997	37.064	37.084000000000003	37.104999999999997	37.125	37.145000000000003	37.164999999999999	37.185000000000002	37.204999999999998	37.225000000000001	37.244	37.264000000000003	37.284999999999997	37.305	37.323999999999998	37.344999999999999	37.365000000000002	37.384999999999998	37.404000000000003	37.423999999999999	37.444000000000003	37.463999999999999	37.484000000000002	37.503999999999998	37.524999999999999	37.545000000000002	37.564	37.585000000000001	37.603999999999999	37.624000000000002	37.643999999999998	37.664000000000001	37.683999999999997	37.704000000000001	37.723999999999997	37.744	37.764000000000003	37.783999999999999	37.804000000000002	37.823999999999998	37.844000000000001	37.863999999999997	37.884	37.904000000000003	37.923999999999999	37.944000000000003	37.963999999999999	37.984000000000002	38.003	38.024000000000001	38.042999999999999	38.064	38.084000000000003	38.103999999999999	38.122999999999998	38.143000000000001	38.162999999999997	38.183999999999997	38.203000000000003	38.222999999999999	38.244	38.264000000000003	38.283999999999999	38.302999999999997	38.323	38.343000000000004	38.363	38.384	38.402999999999999	38.423000000000002	38.442999999999998	38.463000000000001	38.482999999999997	38.503	38.524000000000001	38.543999999999997	38.564	38.584000000000003	38.603999999999999	38.622999999999998	38.643000000000001	38.662999999999997	38.683	38.703000000000003	38.722999999999999	38.743000000000002	38.762999999999998	38.783000000000001	38.802999999999997	38.823	38.843000000000004	38.863	38.881999999999998	38.902000000000001	38.921999999999997	38.942999999999998	38.963000000000001	38.981999999999999	39.003	39.021999999999998	39.042999999999999	39.061999999999998	39.082999999999998	39.103000000000002	39.122	39.142000000000003	39.162999999999997	39.183	39.203000000000003	39.222999999999999	39.243000000000002	39.262999999999998	39.283000000000001	39.302	39.322000000000003	39.341999999999999	39.363	39.381999999999998	39.402999999999999	39.423000000000002	39.442	39.463000000000001	39.482999999999997	39.502000000000002	39.523000000000003	39.542000000000002	39.561999999999998	39.582999999999998	39.601999999999997	39.622	39.642000000000003	39.661999999999999	39.682000000000002	39.701999999999998	39.722000000000001	39.741999999999997	39.762	39.781999999999996	39.802	39.822000000000003	39.841999999999999	39.862000000000002	39.881999999999998	39.902000000000001	39.921999999999997	39.942	39.962000000000003	39.981999999999999	40.002000000000002	40.021000000000001	40.040999999999997	40.061999999999998	40.082000000000001	40.100999999999999	40.122	40.142000000000003	40.161999999999999	40.182000000000002	40.201999999999998	40.222000000000001	40.241999999999997	40.262	40.281999999999996	40.302	40.320999999999998	40.341000000000001	40.360999999999997	40.381	40.401000000000003	40.421999999999997	40.441000000000003	40.460999999999999	40.481999999999999	40.500999999999998	40.521000000000001	40.540999999999997	40.561	40.582000000000001	40.601999999999997	40.621000000000002	40.640999999999998	40.661000000000001	40.680999999999997	40.701000000000001	40.720999999999997	40.741	40.761000000000003	40.780999999999999	40.801000000000002	40.820999999999998	40.841000000000001	40.860999999999997	40.881	40.901000000000003	40.920999999999999	40.94	40.960999999999999	40.981000000000002	41	41.02	41.040999999999997	41.061	41.081000000000003	41.1	41.121000000000002	41.140999999999998	41.161000000000001	41.18	41.201000000000001	41.22	41.24	41.26	41.280999999999999	41.3	41.32	41.341000000000001	41.360999999999997	41.38	41.4	41.420999999999999	41.44	41.46	41.48	41.500999999999998	41.52	41.54	41.56	41.58	41.6	41.62	41.64	41.66	41.68	41.7	41.72	41.74	41.76	41.78	41.8	41.82	41.84	41.86	41.88	41.9	41.92	41.94	41.96	41.98	42	42.018999999999998	42.04	42.06	42.08	42.1	42.12	42.14	42.158999999999999	42.18	42.2	42.22	42.24	42.259	42.28	42.3	42.319000000000003	42.34	42.36	42.38	42.4	42.418999999999997	42.44	42.459000000000003	42.478999999999999	42.499000000000002	42.518999999999998	42.539000000000001	42.56	42.58	42.598999999999997	42.619	42.639000000000003	42.658999999999999	42.679000000000002	42.698999999999998	42.719000000000001	42.738999999999997	42.759	42.779000000000003	42.798999999999999	42.819000000000003	42.838999999999999	42.859000000000002	42.878999999999998	42.899000000000001	42.92	42.939	42.959000000000003	42.978999999999999	42.999000000000002	43.018999999999998	43.039000000000001	43.058999999999997	43.079000000000001	43.098999999999997	43.119	43.139000000000003	43.158999999999999	43.179000000000002	43.198999999999998	43.218000000000004	43.238	43.259	43.277999999999999	43.298000000000002	43.317999999999998	43.338999999999999	43.359000000000002	43.378999999999998	43.398000000000003	43.417999999999999	43.438000000000002	43.457999999999998	43.478000000000002	43.497999999999998	43.518000000000001	43.537999999999997	43.558	43.578000000000003	43.598999999999997	43.618000000000002	43.639000000000003	43.658000000000001	43.679000000000002	43.698999999999998	43.718000000000004	43.738	43.758000000000003	43.777999999999999	43.798000000000002	43.817999999999998	43.838000000000001	43.857999999999997	43.878	43.898000000000003	43.917999999999999	43.938000000000002	43.957999999999998	43.978000000000002	43.997999999999998	44.017000000000003	44.037999999999997	44.057000000000002	44.078000000000003	44.097999999999999	44.118000000000002	44.137	44.156999999999996	44.177	44.198	44.218000000000004	44.238	44.258000000000003	44.277999999999999	44.298000000000002	44.317999999999998	44.338000000000001	44.357999999999997	44.377000000000002	44.396999999999998	44.417999999999999	44.438000000000002	44.457999999999998	44.476999999999997	44.497999999999998	44.517000000000003	44.536999999999999	44.558	44.578000000000003	44.597999999999999	44.618000000000002	44.637	44.656999999999996	44.677	44.697000000000003	44.716999999999999	44.737000000000002	44.756999999999998	44.777000000000001	44.798000000000002	44.817	44.838000000000001	44.856999999999999	44.877000000000002	44.896999999999998	44.917000000000002	44.936999999999998	44.957000000000001	44.976999999999997	44.997	45.017000000000003	45.036999999999999	45.057000000000002	45.076999999999998	45.097000000000001	45.116999999999997	45.137	45.155999999999999	45.177	45.197000000000003	45.216000000000001	45.237000000000002	45.256999999999998	45.277000000000001	45.296999999999997	45.316000000000003	45.335999999999999	45.356000000000002	45.377000000000002	45.396999999999998	45.417000000000002	45.436	45.457000000000001	45.475999999999999	45.497	45.515999999999998	45.536999999999999	45.555999999999997	45.576999999999998	45.597000000000001	45.616	45.636000000000003	45.656999999999996	45.676000000000002	45.695999999999998	45.716999999999999	45.735999999999997	45.756	45.776000000000003	45.795999999999999	45.816000000000003	45.835999999999999	45.856999999999999	45.875999999999998	45.896000000000001	45.915999999999997	45.936	45.956000000000003	45.975999999999999	45.996000000000002	46.015999999999998	46.036000000000001	46.055999999999997	46.076000000000001	46.095999999999997	46.115000000000002	46.136000000000003	46.155999999999999	46.176000000000002	46.195	46.216000000000001	46.234999999999999	46.256	46.274999999999999	46.295999999999999	46.316000000000003	46.335999999999999	46.356000000000002	46.375999999999998	46.395000000000003	46.415999999999997	46.435000000000002	46.456000000000003	46.475000000000001	46.496000000000002	46.515000000000001	46.536000000000001	46.555	46.575000000000003	46.595999999999997	46.615000000000002	46.634999999999998	46.655000000000001	46.676000000000002	46.695	46.716000000000001	46.735999999999997	46.756	46.774999999999999	46.795999999999999	46.814999999999998	46.835000000000001	46.854999999999997	46.875	46.895000000000003	46.915999999999997	46.935000000000002	46.954999999999998	46.975000000000001	46.994999999999997	47.015999999999998	47.036000000000001	47.055	47.073999999999998	47.094000000000001	47.115000000000002	47.134999999999998	47.155000000000001	47.174999999999997	47.195	47.215000000000003	47.234999999999999	47.255000000000003	47.274999999999999	47.295000000000002	47.314	47.335000000000001	47.354999999999997	47.374000000000002	47.393999999999998	47.414000000000001	47.435000000000002	47.454999999999998	47.475000000000001	47.494	47.514000000000003	47.534999999999997	47.555	47.573999999999998	47.594999999999999	47.613999999999997	47.634	47.654000000000003	47.673999999999999	47.694000000000003	47.715000000000003	47.734999999999999	47.753999999999998	47.774000000000001	47.795000000000002	47.814999999999998	47.834000000000003	47.853999999999999	47.874000000000002	47.893999999999998	47.914000000000001	47.933999999999997	47.954000000000001	47.973999999999997	47.994	48.014000000000003	48.033999999999999	48.054000000000002	48.073999999999998	48.094000000000001	48.113999999999997	48.134	48.154000000000003	48.173999999999999	48.194000000000003	48.213999999999999	48.234000000000002	48.253999999999998	48.274000000000001	48.293999999999997	48.314	48.334000000000003	48.353999999999999	48.372999999999998	48.393999999999998	48.414000000000001	48.433999999999997	48.453000000000003	48.473999999999997	48.494	48.512999999999998	48.533000000000001	48.552999999999997	48.573	48.594000000000001	48.613999999999997	48.633000000000003	48.652999999999999	48.673000000000002	48.694000000000003	48.713999999999999	48.732999999999997	48.753	48.774000000000001	48.792999999999999	48.813000000000002	48.832999999999998	48.853000000000002	48.874000000000002	48.893000000000001	48.912999999999997	48.933	48.953000000000003	48.972999999999999	48.993000000000002	49.012999999999998	49.033000000000001	49.052999999999997	49.073	49.093000000000004	49.113	49.133000000000003	49.152999999999999	49.171999999999997	49.192999999999998	49.213000000000001	49.232999999999997	49.253	49.273000000000003	49.292999999999999	49.313000000000002	49.332999999999998	49.351999999999997	49.372	49.392000000000003	49.412999999999997	49.433	49.453000000000003	49.472999999999999	49.493000000000002	49.512	49.533000000000001	49.552	49.573	49.591999999999999	49.613	49.631999999999998	49.652999999999999	49.673000000000002	49.692	49.713000000000001	49.732999999999997	49.752000000000002	49.773000000000003	49.792000000000002	49.811999999999998	49.832000000000001	49.851999999999997	49.872999999999998	49.893000000000001	49.911999999999999	49.932000000000002	49.951999999999998	49.972000000000001	49.991999999999997	50.012	50.031999999999996	50.052	50.072000000000003	50.091999999999999	50.113	50.131999999999998	50.152000000000001	50.171999999999997	50.192	50.212000000000003	50.231999999999999	50.252000000000002	50.271999999999998	50.292000000000002	50.311999999999998	50.331000000000003	50.350999999999999	50.372	50.392000000000003	50.411999999999999	50.430999999999997	50.451000000000001	50.472000000000001	50.491999999999997	50.512	50.530999999999999	50.551000000000002	50.572000000000003	50.591000000000001	50.612000000000002	50.631999999999998	50.651000000000003	50.671999999999997	50.691000000000003	50.710999999999999	50.731000000000002	50.750999999999998	50.771000000000001	50.792000000000002	50.811	50.832000000000001	50.851999999999997	50.872	50.892000000000003	50.911000000000001	50.930999999999997	50.951000000000001	50.970999999999997	50.991	51.012	51.030999999999999	51.051000000000002	51.070999999999998	51.091000000000001	51.110999999999997	51.131	51.151000000000003	51.170999999999999	51.191000000000003	51.21	51.231000000000002	51.250999999999998	51.271000000000001	51.290999999999997	51.311	51.331000000000003	51.350999999999999	51.371000000000002	51.390999999999998	51.411000000000001	51.43	51.451000000000001	51.470999999999997	51.491	51.51	51.53	51.55	51.570999999999998	51.59	51.61	51.631	51.65	51.67	51.69	51.710999999999999	51.731000000000002	51.75	51.77	51.79	51.811	51.831000000000003	51.850999999999999	51.87	51.89	51.911000000000001	51.93	51.95	51.97	51.99	52.01	52.030999999999999	52.05	52.07	52.09	52.11	52.13	52.15	52.170999999999999	52.189	52.21	52.23	52.25	52.268999999999998	52.29	52.31	52.33	52.35	52.37	52.39	52.408999999999999	52.43	52.448999999999998	52.47	52.49	52.51	52.529000000000003	52.548999999999999	52.57	52.588999999999999	52.609000000000002	52.628999999999998	52.65	52.67	52.69	52.709000000000003	52.728999999999999	52.749000000000002	52.77	52.79	52.81	52.829000000000001	52.848999999999997	52.87	52.889000000000003	52.91	52.929000000000002	52.948999999999998	52.969000000000001	52.988999999999997	53.009	53.029000000000003	53.048999999999999	53.069000000000003	53.088999999999999	53.109000000000002	53.13	53.149000000000001	53.168999999999997	53.189	53.209000000000003	53.228999999999999	53.249000000000002	53.268999999999998	53.289000000000001	53.308	53.328000000000003	53.348999999999997	53.369	53.389000000000003	53.408999999999999	53.427999999999997	53.448	53.469000000000001	53.488999999999997	53.509	53.529000000000003	53.548999999999999	53.567999999999998	53.588999999999999	53.607999999999997	53.628999999999998	53.648000000000003	53.667999999999999	53.688000000000002	53.707999999999998	53.728999999999999	53.747999999999998	53.768000000000001	53.789000000000001	53.808	53.828000000000003	53.848999999999997	53.868000000000002	53.889000000000003	53.908000000000001	53.927999999999997	53.948	53.968000000000004	53.988	54.008000000000003	54.027999999999999	54.048000000000002	54.067999999999998	54.088999999999999	54.109000000000002	54.128	54.148000000000003	54.167999999999999	54.188000000000002	54.207999999999998	54.228000000000002	54.247999999999998	54.268000000000001	54.287999999999997	54.308	54.328000000000003	54.347999999999999	54.368000000000002	54.387999999999998	54.408000000000001	54.427999999999997	54.448	54.468000000000004	54.488	54.508000000000003	54.527999999999999	54.548000000000002	54.567	54.588000000000001	54.606999999999999	54.628	54.648000000000003	54.667999999999999	54.686999999999998	54.707000000000001	54.728000000000002	54.747	54.767000000000003	54.787999999999997	54.807000000000002	54.826999999999998	54.847000000000001	54.868000000000002	54.887999999999998	54.906999999999996	54.927999999999997	54.948	54.968000000000004	54.987000000000002	55.006999999999998	55.027000000000001	55.046999999999997	55.067	55.087000000000003	55.106999999999999	55.127000000000002	55.146999999999998	55.167000000000002	55.186999999999998	55.207000000000001	55.226999999999997	55.247	55.267000000000003	55.286999999999999	55.307000000000002	55.326999999999998	55.345999999999997	55.366999999999997	55.387	55.406999999999996	55.427	55.447000000000003	55.466999999999999	55.487000000000002	55.506	55.527000000000001	55.546999999999997	55.567	55.585999999999999	55.606000000000002	55.627000000000002	55.646000000000001	55.667000000000002	55.686	55.707000000000001	55.726999999999997	55.746000000000002	55.767000000000003	55.786000000000001	55.805999999999997	55.826999999999998	55.847000000000001	55.866999999999997	55.886000000000003	55.906999999999996	55.927	55.945999999999998	55.966000000000001	55.987000000000002	56.006	56.026000000000003	56.045999999999999	56.066000000000003	56.085999999999999	56.106000000000002	56.125999999999998	56.146000000000001	56.167000000000002	56.186	56.206000000000003	56.225999999999999	56.246000000000002	56.267000000000003	56.284999999999997	56.305999999999997	56.326000000000001	56.345999999999997	56.366	56.386000000000003	56.405999999999999	56.426000000000002	56.445999999999998	56.465000000000003	56.485999999999997	56.506	56.526000000000003	56.545999999999999	56.566000000000003	56.585000000000001	56.606000000000002	56.625999999999998	56.646000000000001	56.665999999999997	56.686	56.704999999999998	56.725999999999999	56.744999999999997	56.765999999999998	56.786000000000001	56.805999999999997	56.826000000000001	56.844999999999999	56.865000000000002	56.884999999999998	56.905000000000001	56.924999999999997	56.945	56.966000000000001	56.985999999999997	57.006	57.024999999999999	57.045000000000002	57.064999999999998	57.085000000000001	57.104999999999997	57.125	57.146000000000001	57.164999999999999	57.186	57.204999999999998	57.225000000000001	57.244999999999997	57.265000000000001	57.284999999999997	57.305	57.325000000000003	57.344999999999999	57.365000000000002	57.384999999999998	57.405000000000001	57.424999999999997	57.445	57.465000000000003	57.484999999999999	57.505000000000003	57.524999999999999	57.545000000000002	57.564	57.584000000000003	57.603999999999999	57.624000000000002	57.645000000000003	57.664999999999999	57.685000000000002	57.704999999999998	57.723999999999997	57.744999999999997	57.765000000000001	57.783999999999999	57.804000000000002	57.823999999999998	57.844000000000001	57.865000000000002	57.884999999999998	57.905000000000001	57.924999999999997	57.944000000000003	57.965000000000003	57.984000000000002	58.005000000000003	58.024000000000001	58.045000000000002	58.064999999999998	58.084000000000003	58.103999999999999	58.124000000000002	58.145000000000003	58.164000000000001	58.183999999999997	58.204000000000001	58.223999999999997	58.244	58.264000000000003	58.283999999999999	58.304000000000002	58.323999999999998	58.344000000000001	58.363999999999997	58.384	58.404000000000003	58.423999999999999	58.444000000000003	58.463000000000001	58.484000000000002	58.503999999999998	58.524000000000001	58.543999999999997	58.564	58.582999999999998	58.603000000000002	58.622999999999998	58.643000000000001	58.664000000000001	58.683999999999997	58.704000000000001	58.723999999999997	58.743000000000002	58.762999999999998	58.783999999999999	58.804000000000002	58.823999999999998	58.843000000000004	58.863999999999997	58.884	58.902999999999999	58.923000000000002	58.942999999999998	58.963000000000001	58.984000000000002	59.003999999999998	59.023000000000003	59.043999999999997	59.063000000000002	59.082999999999998	59.103999999999999	59.122999999999998	59.143000000000001	59.162999999999997	59.183	59.203000000000003	59.222999999999999	59.243000000000002	59.262999999999998	59.283000000000001	59.302999999999997	59.323999999999998	59.343000000000004	59.363	59.383000000000003	59.402999999999999	59.423000000000002	59.442999999999998	59.463000000000001	59.482999999999997	59.503	59.523000000000003	59.542999999999999	59.563000000000002	59.582999999999998	59.603000000000002	59.622999999999998	59.643000000000001	59.662999999999997	59.683	59.701999999999998	59.722000000000001	59.741999999999997	59.762999999999998	59.781999999999996	59.802	59.823	59.841999999999999	59.862000000000002	59.883000000000003	59.902999999999999	59.923000000000002	59.942	59.962000000000003	59.981999999999999	60.002000000000002	60.021999999999998	60.042999999999999	60.061999999999998	60.082000000000001	60.101999999999997	60.122	60.142000000000003	60.161999999999999	60.182000000000002	60.201999999999998	60.222000000000001	60.241999999999997	60.262	60.281999999999996	60.302	60.322000000000003	60.341999999999999	60.362000000000002	60.381999999999998	60.402000000000001	60.421999999999997	60.442	60.462000000000003	60.481999999999999	60.502000000000002	60.521999999999998	60.542000000000002	60.561999999999998	60.582000000000001	60.601999999999997	60.622	60.640999999999998	60.661000000000001	60.682000000000002	60.701999999999998	60.722000000000001	60.741	60.762	60.781999999999996	60.801000000000002	60.822000000000003	60.841999999999999	60.862000000000002	60.881999999999998	60.902000000000001	60.921999999999997	60.942	60.962000000000003	60.981000000000002	61.000999999999998	61.021000000000001	61.040999999999997	61.061	61.081000000000003	61.101999999999997	61.122	61.142000000000003	61.161000000000001	61.180999999999997	61.201000000000001	61.220999999999997	61.241	61.261000000000003	61.280999999999999	61.301000000000002	61.320999999999998	61.341000000000001	61.360999999999997	61.381	61.401000000000003	61.420999999999999	61.441000000000003	61.460999999999999	61.481000000000002	61.500999999999998	61.521000000000001	61.540999999999997	61.561	61.58	61.600999999999999	61.62	61.640999999999998	61.661000000000001	61.680999999999997	61.701000000000001	61.72	61.741	61.761000000000003	61.78	61.8	61.820999999999998	61.84	61.86	61.88	61.901000000000003	61.920999999999999	61.941000000000003	61.96	61.98	62.000999999999998	62.02	62.040999999999997	62.06	62.081000000000003	62.100999999999999	62.121000000000002	62.14	62.16	62.18	62.2	62.22	62.24	62.26	62.28	62.3	62.32	62.34	62.36	62.381	62.401000000000003	62.42	62.44	62.46	62.48	62.5	62.52	62.54	62.56	62.58	62.6	62.62	62.64	62.66	62.68	62.7	62.72	62.738999999999997	62.759	62.78	62.8	62.819000000000003	62.838999999999999	62.86	62.88	62.9	62.92	62.939	62.959000000000003	62.98	63	63.018999999999998	63.039000000000001	63.058999999999997	63.08	63.1	63.12	63.139000000000003	63.158999999999999	63.179000000000002	63.198999999999998	63.219000000000001	63.24	63.259	63.279000000000003	63.298999999999999	63.32	63.338999999999999	63.359000000000002	63.378999999999998	63.399000000000001	63.418999999999997	63.44	63.459000000000003	63.478999999999999	63.499000000000002	63.518999999999998	63.539000000000001	63.558999999999997	63.579000000000001	63.598999999999997	63.619	63.639000000000003	63.658999999999999	63.679000000000002	63.698	63.718000000000004	63.738999999999997	63.759	63.779000000000003	63.798000000000002	63.817999999999998	63.838999999999999	63.859000000000002	63.878	63.899000000000001	63.918999999999997	63.938000000000002	63.957999999999998	63.978999999999999	63.997999999999998	64.018000000000001	64.037999999999997	64.058999999999997	64.078999999999994	64.099000000000004	64.119	64.138999999999996	64.159000000000006	64.177999999999997	64.198999999999998	64.218000000000004	64.239000000000004	64.257999999999996	64.278999999999996	64.298000000000002	64.319000000000003	64.337999999999994	64.358000000000004	64.378	64.397999999999996	64.418000000000006	64.438000000000002	64.459000000000003	64.477999999999994	64.498000000000005	64.518000000000001	64.537999999999997	64.558000000000007	64.578000000000003	64.597999999999999	64.617999999999995	64.637	64.658000000000001	64.677999999999997	64.697999999999993	64.718000000000004	64.738	64.757000000000005	64.778000000000006	64.798000000000002	64.817999999999998	64.837999999999994	64.858000000000004	64.876999999999995	64.897999999999996	64.917000000000002	64.938000000000002	64.957999999999998	64.977999999999994	64.998000000000005	65.016999999999996	65.037000000000006	65.057000000000002	65.076999999999998	65.096999999999994	65.117000000000004	65.137	65.156999999999996	65.177999999999997	65.197999999999993	65.218000000000004	65.236999999999995	65.257000000000005	65.277000000000001	65.296999999999997	65.316999999999993	65.337000000000003	65.356999999999999	65.376999999999995	65.397000000000006	65.417000000000002	65.438000000000002	65.457999999999998	65.477000000000004	65.497	65.516999999999996	65.537000000000006	65.557000000000002	65.576999999999998	65.596999999999994	65.617000000000004	65.637	65.656999999999996	65.677000000000007	65.697000000000003	65.716999999999999	65.736000000000004	65.757000000000005	65.775999999999996	65.796999999999997	65.816999999999993	65.837000000000003	65.856999999999999	65.876000000000005	65.897000000000006	65.917000000000002	65.936999999999998	65.956999999999994	65.977000000000004	65.997	66.016000000000005	66.036000000000001	66.055999999999997	66.075999999999993	66.096999999999994	66.117000000000004	66.135999999999996	66.156999999999996	66.177000000000007	66.197000000000003	66.215999999999994	66.236000000000004	66.256	66.275999999999996	66.296000000000006	66.316000000000003	66.335999999999999	66.355999999999995	66.376000000000005	66.396000000000001	66.415999999999997	66.436000000000007	66.456999999999994	66.475999999999999	66.495999999999995	66.516000000000005	66.536000000000001	66.555999999999997	66.575000000000003	66.596000000000004	66.616	66.635999999999996	66.656000000000006	66.676000000000002	66.695999999999998	66.715999999999994	66.736000000000004	66.756	66.775999999999996	66.796000000000006	66.816000000000003	66.834999999999994	66.855999999999995	66.875	66.894999999999996	66.915000000000006	66.936000000000007	66.956000000000003	66.975999999999999	66.995999999999995	67.016000000000005	67.036000000000001	67.055999999999997	67.075999999999993	67.094999999999999	67.114999999999995	67.135000000000005	67.156000000000006	67.174999999999997	67.195999999999998	67.215000000000003	67.236000000000004	67.256	67.275999999999996	67.295000000000002	67.316000000000003	67.334999999999994	67.355000000000004	67.376000000000005	67.394999999999996	67.415999999999997	67.435000000000002	67.456000000000003	67.474999999999994	67.495000000000005	67.515000000000001	67.534999999999997	67.555000000000007	67.575000000000003	67.596000000000004	67.614999999999995	67.635000000000005	67.655000000000001	67.674999999999997	67.694999999999993	67.715000000000003	67.734999999999999	67.754999999999995	67.775000000000006	67.795000000000002	67.814999999999998	67.834999999999994	67.853999999999999	67.875	67.894999999999996	67.914000000000001	67.933999999999997	67.954999999999998	67.974999999999994	67.994	68.015000000000001	68.034999999999997	68.055000000000007	68.075000000000003	68.093999999999994	68.114000000000004	68.135000000000005	68.155000000000001	68.174999999999997	68.194000000000003	68.213999999999999	68.233999999999995	68.254999999999995	68.275000000000006	68.293999999999997	68.313999999999993	68.334000000000003	68.353999999999999	68.373999999999995	68.394000000000005	68.414000000000001	68.433999999999997	68.453999999999994	68.474000000000004	68.494	68.515000000000001	68.534999999999997	68.554000000000002	68.573999999999998	68.593999999999994	68.614000000000004	68.634	68.653999999999996	68.674000000000007	68.694000000000003	68.713999999999999	68.733999999999995	68.754000000000005	68.774000000000001	68.793999999999997	68.813999999999993	68.834000000000003	68.853999999999999	68.873999999999995	68.894000000000005	68.914000000000001	68.933999999999997	68.953999999999994	68.974000000000004	68.994	69.013999999999996	69.034000000000006	69.054000000000002	69.073999999999998	69.093999999999994	69.113	69.132999999999996	69.153000000000006	69.173000000000002	69.194000000000003	69.213999999999999	69.233999999999995	69.254000000000005	69.274000000000001	69.293000000000006	69.313999999999993	69.332999999999998	69.352999999999994	69.373999999999995	69.393000000000001	69.412999999999997	69.433999999999997	69.453000000000003	69.474000000000004	69.492999999999995	69.513000000000005	69.533000000000001	69.552999999999997	69.572999999999993	69.593000000000004	69.613	69.632999999999996	69.653000000000006	69.673000000000002	69.692999999999998	69.712999999999994	69.733999999999995	69.753	69.772999999999996	69.793000000000006	69.813000000000002	69.832999999999998	69.852000000000004	69.872	69.893000000000001	69.912999999999997	69.932000000000002	69.953000000000003	69.972999999999999	69.992999999999995	70.012	70.033000000000001	70.052999999999997	70.072999999999993	70.093000000000004	70.113	70.132000000000005	70.152000000000001	70.171999999999997	70.192999999999998	70.212999999999994	70.233000000000004	70.251999999999995	70.272000000000006	70.292000000000002	70.313000000000002	70.331999999999994	70.352000000000004	70.372	70.391999999999996	70.412999999999997	70.432000000000002	70.451999999999998	70.471999999999994	70.492999999999995	70.512	70.533000000000001	70.552000000000007	70.572000000000003	70.591999999999999	70.611999999999995	70.632000000000005	70.652000000000001	70.671999999999997	70.691999999999993	70.712000000000003	70.731999999999999	70.751999999999995	70.772000000000006	70.792000000000002	70.811999999999998	70.831999999999994	70.852000000000004	70.872	70.891999999999996	70.912000000000006	70.932000000000002	70.951999999999998	70.971999999999994	70.991	71.012	71.031000000000006	71.051000000000002	71.070999999999998	71.091999999999999	71.111999999999995	71.132000000000005	71.150999999999996	71.171999999999997	71.191000000000003	71.212000000000003	71.231999999999999	71.251999999999995	71.271000000000001	71.292000000000002	71.311999999999998	71.331000000000003	71.352000000000004	71.372	71.391000000000005	71.412000000000006	71.432000000000002	71.450999999999993	71.471000000000004	71.491	71.512	71.531999999999996	71.552000000000007	71.570999999999998	71.590999999999994	71.611000000000004	71.632000000000005	71.650999999999996	71.671000000000006	71.691000000000003	71.710999999999999	71.730999999999995	71.751000000000005	71.771000000000001	71.790999999999997	71.811000000000007	71.831000000000003	71.850999999999999	71.870999999999995	71.891000000000005	71.911000000000001	71.930000000000007	71.950999999999993	71.971000000000004	71.991	72.010999999999996	72.031000000000006	72.051000000000002	72.070999999999998	72.090999999999994	72.111000000000004	72.131	72.150000000000006	72.17	72.191000000000003	72.209999999999994	72.230999999999995	72.251000000000005	72.271000000000001	72.290999999999997	72.311000000000007	72.331000000000003	72.349999999999994	72.37	72.39	72.411000000000001	72.430000000000007	72.450999999999993	72.47	72.489999999999995	72.510000000000005	72.531000000000006	72.551000000000002	72.569999999999993	72.59	72.61	72.631	72.650000000000006	72.67	72.69	72.709999999999994	72.73	72.75	72.77	72.790000000000006	72.81	72.83	72.849999999999994	72.87	72.89	72.91	72.930000000000007	72.95	72.97	72.989999999999995	73.010000000000005	73.03	73.05	73.069999999999993	73.09	73.11	73.13	73.150000000000006	73.17	73.19	73.209000000000003	73.228999999999999	73.25	73.27	73.290000000000006	73.308999999999997	73.328999999999994	73.349000000000004	73.37	73.39	73.41	73.429000000000002	73.45	73.47	73.489000000000004	73.510000000000005	73.528999999999996	73.549000000000007	73.569999999999993	73.588999999999999	73.61	73.629000000000005	73.650000000000006	73.668999999999997	73.688999999999993	73.709000000000003	73.728999999999999	73.748999999999995	73.769000000000005	73.789000000000001	73.808999999999997	73.828999999999994	73.849000000000004	73.869	73.888999999999996	73.91	73.929000000000002	73.948999999999998	73.968999999999994	73.989000000000004	74.009	74.028000000000006	74.049000000000007	74.069000000000003	74.088999999999999	74.108999999999995	74.129000000000005	74.149000000000001	74.168999999999997	74.188999999999993	74.207999999999998	74.228999999999999	74.248999999999995	74.268000000000001	74.287999999999997	74.308000000000007	74.328999999999994	74.349000000000004	74.369	74.388000000000005	74.409000000000006	74.429000000000002	74.447999999999993	74.468999999999994	74.488	74.507999999999996	74.528000000000006	74.549000000000007	74.569000000000003	74.587999999999994	74.608000000000004	74.628	74.647999999999996	74.668000000000006	74.688000000000002	74.707999999999998	74.727999999999994	74.748000000000005	74.768000000000001	74.787999999999997	74.808000000000007	74.828000000000003	74.849000000000004	74.867999999999995	74.888000000000005	74.908000000000001	74.927999999999997	74.947999999999993	74.968000000000004	74.988	75.007999999999996	75.027000000000001	75.048000000000002	75.067999999999998	75.087999999999994	75.108000000000004	75.126999999999995	75.147999999999996	75.168000000000006	75.186999999999998	75.206999999999994	75.227000000000004	75.248000000000005	75.268000000000001	75.287999999999997	75.307000000000002	75.326999999999998	75.346999999999994	75.367000000000004	75.387	75.408000000000001	75.427999999999997	75.447999999999993	75.466999999999999	75.488	75.507000000000005	75.528000000000006	75.546999999999997	75.566999999999993	75.587000000000003	75.606999999999999	75.626999999999995	75.647999999999996	75.667000000000002	75.688000000000002	75.706999999999994	75.727999999999994	75.747	75.766999999999996	75.787000000000006	75.807000000000002	75.826999999999998	75.846999999999994	75.867000000000004	75.887	75.908000000000001	75.927000000000007	75.947000000000003	75.966999999999999	75.986999999999995	76.007000000000005	76.027000000000001	76.046999999999997	76.066999999999993	76.087000000000003	76.106999999999999	76.126000000000005	76.147000000000006	76.167000000000002	76.186999999999998	76.206000000000003	76.227000000000004	76.245999999999995	76.266999999999996	76.286000000000001	76.305999999999997	76.325999999999993	76.346000000000004	76.367000000000004	76.385999999999996	76.406000000000006	76.427000000000007	76.445999999999998	76.466999999999999	76.486999999999995	76.507000000000005	76.525999999999996	76.546999999999997	76.566999999999993	76.587000000000003	76.606999999999999	76.626000000000005	76.646000000000001	76.665999999999997	76.686000000000007	76.706000000000003	76.725999999999999	76.747	76.766000000000005	76.786000000000001	76.805999999999997	76.825999999999993	76.846000000000004	76.866	76.885999999999996	76.906000000000006	76.926000000000002	76.945999999999998	76.965999999999994	76.986000000000004	77.006	77.025000000000006	77.046000000000006	77.066000000000003	77.085999999999999	77.105999999999995	77.126000000000005	77.146000000000001	77.165999999999997	77.186000000000007	77.206000000000003	77.224999999999994	77.245999999999995	77.265000000000001	77.284999999999997	77.305000000000007	77.325000000000003	77.346000000000004	77.366	77.385000000000005	77.406000000000006	77.426000000000002	77.445999999999998	77.465999999999994	77.486000000000004	77.506	77.525000000000006	77.545000000000002	77.566000000000003	77.584999999999994	77.605999999999995	77.625	77.646000000000001	77.665000000000006	77.686000000000007	77.704999999999998	77.724999999999994	77.745000000000005	77.765000000000001	77.784999999999997	77.805000000000007	77.825000000000003	77.844999999999999	77.864999999999995	77.885000000000005	77.906000000000006	77.924999999999997	77.944999999999993	77.965000000000003	77.984999999999999	78.004999999999995	78.025000000000006	78.045000000000002	78.064999999999998	78.084000000000003	78.105000000000004	78.123999999999995	78.144999999999996	78.164000000000001	78.185000000000002	78.204999999999998	78.224999999999994	78.245000000000005	78.265000000000001	78.284999999999997	78.304000000000002	78.325000000000003	78.343999999999994	78.364999999999995	78.384	78.405000000000001	78.424000000000007	78.444999999999993	78.463999999999999	78.483999999999995	78.504000000000005	78.525000000000006	78.543999999999997	78.563999999999993	78.584999999999994	78.605000000000004	78.625	78.644000000000005	78.664000000000001	78.683999999999997	78.703999999999994	78.724999999999994	78.745000000000005	78.763999999999996	78.784999999999997	78.804000000000002	78.823999999999998	78.843999999999994	78.864000000000004	78.884	78.905000000000001	78.924000000000007	78.944000000000003	78.963999999999999	78.984999999999999	79.004000000000005	79.024000000000001	79.043999999999997	79.063999999999993	79.084000000000003	79.102999999999994	79.123000000000005	79.144000000000005	79.164000000000001	79.183999999999997	79.203999999999994	79.224000000000004	79.244	79.263000000000005	79.283000000000001	79.304000000000002	79.323999999999998	79.343999999999994	79.364000000000004	79.384	79.403999999999996	79.424000000000007	79.444000000000003	79.463999999999999	79.483999999999995	79.504000000000005	79.524000000000001	79.543999999999997	79.563999999999993	79.584000000000003	79.602999999999994	79.623000000000005	79.643000000000001	79.662999999999997	79.683000000000007	79.703000000000003	79.722999999999999	79.742999999999995	79.763999999999996	79.784000000000006	79.802999999999997	79.823999999999998	79.843000000000004	79.863	79.882999999999996	79.903000000000006	79.923000000000002	79.942999999999998	79.963999999999999	79.983000000000004	80.003	80.022999999999996	80.043000000000006	80.063000000000002	80.082999999999998	80.102999999999994	80.123000000000005	80.143000000000001	80.162999999999997	80.183000000000007	80.203000000000003	80.222999999999999	80.242999999999995	80.263000000000005	80.283000000000001	80.302999999999997	80.322999999999993	80.341999999999999	80.361999999999995	80.382999999999996	80.403000000000006	80.421999999999997	80.442999999999998	80.462999999999994	80.483000000000004	80.503	80.522999999999996	80.542000000000002	80.561999999999998	80.582999999999998	80.602999999999994	80.622	80.641999999999996	80.662999999999997	80.682000000000002	80.701999999999998	80.721999999999994	80.742000000000004	80.762	80.781999999999996	80.802000000000007	80.822000000000003	80.841999999999999	80.861999999999995	80.882000000000005	80.902000000000001	80.921999999999997	80.941999999999993	80.962000000000003	80.981999999999999	81.001999999999995	81.022000000000006	81.042000000000002	81.061999999999998	81.081999999999994	81.102000000000004	81.122	81.141000000000005	81.161000000000001	81.182000000000002	81.201999999999998	81.221999999999994	81.242000000000004	81.262	81.281000000000006	81.301000000000002	81.322000000000003	81.341999999999999	81.361999999999995	81.381	81.400999999999996	81.421999999999997	81.441999999999993	81.460999999999999	81.481999999999999	81.501000000000005	81.521000000000001	81.540999999999997	81.561999999999998	81.581000000000003	81.602000000000004	81.622	81.641999999999996	81.662000000000006	81.680999999999997	81.700999999999993	81.721999999999994	81.742000000000004	81.760999999999996	81.781999999999996	81.802000000000007	81.820999999999998	81.841999999999999	81.861999999999995	81.881	81.900999999999996	81.921000000000006	81.941000000000003	81.962000000000003	81.980999999999995	82.001000000000005	82.021000000000001	82.040999999999997	82.061000000000007	82.081000000000003	82.100999999999999	82.120999999999995	82.141000000000005	82.161000000000001	82.180999999999997	82.200999999999993	82.221000000000004	82.241	82.260999999999996	82.281000000000006	82.301000000000002	82.320999999999998	82.340999999999994	82.361000000000004	82.381	82.4	82.42	82.441000000000003	82.460999999999999	82.480999999999995	82.501000000000005	82.52	82.540999999999997	82.561000000000007	82.58	82.600999999999999	82.620999999999995	82.64	82.661000000000001	82.68	82.700999999999993	82.72	82.741	82.76	82.78	82.8	82.82	82.840999999999994	82.86	82.88	82.9	82.92	82.94	82.96	82.98	83	83.02	83.04	83.06	83.08	83.1	83.12	83.14	83.16	83.179000000000002	83.2	83.218999999999994	83.24	83.26	83.28	83.3	83.319000000000003	83.34	83.36	83.38	83.4	83.42	83.44	83.459000000000003	83.48	83.5	83.52	83.539000000000001	83.558999999999997	83.58	83.6	83.62	83.638999999999996	83.659000000000006	83.679000000000002	83.698999999999998	83.718999999999994	83.739000000000004	83.759	83.778999999999996	83.8	83.82	83.838999999999999	83.858999999999995	83.879000000000005	83.9	83.92	83.938999999999993	83.959000000000003	83.978999999999999	83.998999999999995	84.019000000000005	84.04	84.06	84.078999999999994	84.099000000000004	84.119	84.138999999999996	84.159000000000006	84.179000000000002	84.198999999999998	84.218999999999994	84.238	84.259	84.278999999999996	84.299000000000007	84.319000000000003	84.338999999999999	84.358999999999995	84.379000000000005	84.399000000000001	84.418999999999997	84.438000000000002	84.457999999999998	84.478999999999999	84.498999999999995	84.519000000000005	84.537999999999997	84.558999999999997	84.578999999999994	84.599000000000004	84.617999999999995	84.638000000000005	84.659000000000006	84.677999999999997	84.698999999999998	84.718999999999994	84.738	84.759	84.778000000000006	84.799000000000007	84.817999999999998	84.838999999999999	84.858000000000004	84.878	84.897999999999996	84.918000000000006	84.938999999999993	84.957999999999998	84.977999999999994	84.998000000000005	85.018000000000001	85.037999999999997	85.058999999999997	85.078000000000003	85.097999999999999	85.117999999999995	85.138000000000005	85.158000000000001	85.177999999999997	85.197999999999993	85.218000000000004	85.238	85.257999999999996	85.278000000000006	85.296999999999997	85.317999999999998	85.337999999999994	85.358000000000004	85.378	85.397999999999996	85.417000000000002	85.438000000000002	85.457999999999998	85.477000000000004	85.498000000000005	85.516999999999996	85.537000000000006	85.557000000000002	85.578000000000003	85.597999999999999	85.617999999999995	85.638000000000005	85.656999999999996	85.677999999999997	85.697999999999993	85.716999999999999	85.738	85.757999999999996	85.777000000000001	85.796999999999997	85.816999999999993	85.837999999999994	85.858000000000004	85.878	85.897000000000006	85.917000000000002	85.938000000000002	85.956999999999994	85.977000000000004	85.997	86.016999999999996	86.037000000000006	86.057000000000002	86.078000000000003	86.096999999999994	86.117000000000004	86.137	86.156999999999996	86.177000000000007	86.197000000000003	86.218000000000004	86.236999999999995	86.257000000000005	86.277000000000001	86.296999999999997	86.316999999999993	86.337000000000003	86.356999999999999	86.376999999999995	86.397000000000006	86.417000000000002	86.436000000000007	86.456999999999994	86.477000000000004	86.495999999999995	86.516999999999996	86.537000000000006	86.555999999999997	86.576999999999998	86.596000000000004	86.616	86.635999999999996	86.656999999999996	86.677000000000007	86.697000000000003	86.715999999999994	86.736999999999995	86.756	86.775999999999996	86.796999999999997	86.816000000000003	86.837000000000003	86.855999999999995	86.876000000000005	86.896000000000001	86.917000000000002	86.936000000000007	86.956000000000003	86.975999999999999	86.995999999999995	87.016000000000005	87.036000000000001	87.055999999999997	87.075999999999993	87.096999999999994	87.116	87.135999999999996	87.156000000000006	87.176000000000002	87.195999999999998	87.215999999999994	87.236000000000004	87.256	87.275999999999996	87.296000000000006	87.316000000000003	87.335999999999999	87.355999999999995	87.376000000000005	87.396000000000001	87.415999999999997	87.436000000000007	87.456000000000003	87.475999999999999	87.495999999999995	87.516000000000005	87.536000000000001	87.555999999999997	87.575999999999993	87.596000000000004	87.616	87.635999999999996	87.656000000000006	87.674999999999997	87.694999999999993	87.715000000000003	87.736000000000004	87.756	87.775999999999996	87.796000000000006	87.814999999999998	87.835999999999999	87.855999999999995	87.875	87.894999999999996	87.915000000000006	87.936000000000007	87.956000000000003	87.975999999999999	87.995000000000005	88.015000000000001	88.034999999999997	88.055000000000007	88.075000000000003	88.094999999999999	88.114999999999995	88.135999999999996	88.155000000000001	88.174999999999997	88.194999999999993	88.215000000000003	88.234999999999999	88.256	88.275000000000006	88.295000000000002	88.314999999999998	88.334999999999994	88.355000000000004	88.375	88.394999999999996	88.415000000000006	88.435000000000002	88.454999999999998	88.474999999999994	88.495000000000005	88.515000000000001	88.534999999999997	88.555000000000007	88.575000000000003	88.593999999999994	88.614000000000004	88.634	88.655000000000001	88.674999999999997	88.694999999999993	88.713999999999999	88.733999999999995	88.754000000000005	88.775000000000006	88.793999999999997	88.813999999999993	88.834000000000003	88.853999999999999	88.873999999999995	88.894999999999996	88.914000000000001	88.935000000000002	88.953999999999994	88.974000000000004	88.995000000000005	89.013999999999996	89.034000000000006	89.055000000000007	89.073999999999998	89.093999999999994	89.114000000000004	89.134	89.153999999999996	89.174000000000007	89.194000000000003	89.213999999999999	89.233999999999995	89.254000000000005	89.274000000000001	89.295000000000002	89.313999999999993	89.334000000000003	89.353999999999999	89.373999999999995	89.394000000000005	89.414000000000001	89.433999999999997	89.453999999999994	89.472999999999999	89.494	89.513999999999996	89.534000000000006	89.554000000000002	89.573999999999998	89.593999999999994	89.613	89.634	89.653000000000006	89.674000000000007	89.694000000000003	89.713999999999999	89.733999999999995	89.754000000000005	89.774000000000001	89.793000000000006	89.813000000000002	89.832999999999998	89.852999999999994	89.873999999999995	89.894000000000005	89.912999999999997	89.933000000000007	89.953000000000003	89.974000000000004	89.995000000000005	90.013999999999996	90.033000000000001	90.052999999999997	90.073999999999998	90.093000000000004	90.113	90.132999999999996	90.153000000000006	90.174000000000007	90.194000000000003	90.212999999999994	90.233000000000004	90.253	90.272999999999996	90.293000000000006	90.313000000000002	90.332999999999998	90.352999999999994	90.373000000000005	90.391999999999996	90.412999999999997	90.433000000000007	90.453000000000003	90.471999999999994	90.492999999999995	90.513000000000005	90.531999999999996	90.552999999999997	90.572999999999993	90.593000000000004	90.613	90.632999999999996	90.652000000000001	90.673000000000002	90.692999999999998	90.712999999999994	90.733000000000004	90.753	90.772999999999996	90.792000000000002	90.811999999999998	90.831999999999994	90.852999999999994	90.873000000000005	90.893000000000001	90.912999999999997	90.932000000000002	90.951999999999998	90.971999999999994	90.992999999999995	91.013000000000005	91.031999999999996	91.052999999999997	91.072999999999993	91.093000000000004	91.111999999999995	91.132000000000005	91.152000000000001	91.173000000000002	91.191999999999993	91.212000000000003	91.231999999999999	91.251999999999995	91.272000000000006	91.293000000000006	91.311999999999998	91.332999999999998	91.352000000000004	91.372	91.391999999999996	91.412000000000006	91.432000000000002	91.451999999999998	91.471999999999994	91.492000000000004	91.512	91.531999999999996	91.552000000000007	91.572000000000003	91.591999999999999	91.611999999999995	91.632000000000005	91.650999999999996	91.671000000000006	91.691000000000003	91.712000000000003	91.731999999999999	91.751999999999995	91.771000000000001	91.792000000000002	91.811000000000007	91.831999999999994	91.852000000000004	91.872	91.891000000000005	91.912000000000006	91.932000000000002	91.950999999999993	91.971000000000004	91.992000000000004	92.010999999999996	92.031999999999996	92.052000000000007	92.070999999999998	92.090999999999994	92.111000000000004	92.131	92.150999999999996	92.171000000000006	92.191000000000003	92.212000000000003	92.230999999999995	92.251000000000005	92.271000000000001	92.290999999999997	92.311999999999998	92.331999999999994	92.350999999999999	92.370999999999995	92.391000000000005	92.411000000000001	92.430999999999997	92.450999999999993	92.471000000000004	92.491	92.51	92.531000000000006	92.551000000000002	92.570999999999998	92.590999999999994	92.611000000000004	92.63	92.65	92.671000000000006	92.691000000000003	92.71	92.730999999999995	92.751000000000005	92.771000000000001	92.79	92.81	92.831000000000003	92.850999999999999	92.870999999999995	92.891000000000005	92.91	92.93	92.950999999999993	92.971000000000004	92.99	93.01	93.031000000000006	93.051000000000002	93.07	93.09	93.11	93.13	93.15	93.17	93.191000000000003	93.21	93.230999999999995	93.25	93.27	93.29	93.31	93.33	93.350999999999999	93.370999999999995	93.39	93.41	93.43	93.45	93.47	93.49	93.51	93.53	93.55	93.57	93.59	93.61	93.629000000000005	93.65	93.67	93.69	93.709000000000003	93.73	93.748999999999995	93.77	93.79	93.81	93.83	93.85	93.869	93.888999999999996	93.909000000000006	93.93	93.95	93.968999999999994	93.99	94.009	94.028999999999996	94.05	94.069000000000003	94.088999999999999	94.108999999999995	94.13	94.149000000000001	94.168999999999997	94.188999999999993	94.209000000000003	94.228999999999999	94.25	94.269000000000005	94.289000000000001	94.308999999999997	94.328999999999994	94.349000000000004	94.37	94.388999999999996	94.409000000000006	94.429000000000002	94.448999999999998	94.468999999999994	94.489000000000004	94.509	94.528999999999996	94.549000000000007	94.569000000000003	94.588999999999999	94.608999999999995	94.629000000000005	94.649000000000001	94.668999999999997	94.688999999999993	94.707999999999998	94.727999999999994	94.748000000000005	94.769000000000005	94.789000000000001	94.808999999999997	94.828000000000003	94.847999999999999	94.869	94.888000000000005	94.908000000000001	94.927999999999997	94.948999999999998	94.968999999999994	94.989000000000004	95.007999999999996	95.028999999999996	95.049000000000007	95.067999999999998	95.088999999999999	95.108000000000004	95.129000000000005	95.149000000000001	95.168999999999997	95.188000000000002	95.207999999999998	95.227999999999994	95.248000000000005	95.268000000000001	95.287999999999997	95.308000000000007	95.328000000000003	95.347999999999999	95.367999999999995	95.388000000000005	95.408000000000001	95.429000000000002	95.448999999999998	95.468000000000004	95.488	95.507999999999996	95.528000000000006	95.548000000000002	95.566999999999993	95.587999999999994	95.608000000000004	95.628	95.647000000000006	95.668000000000006	95.688000000000002	95.707999999999998	95.727999999999994	95.747	95.766999999999996	95.787999999999997	95.807000000000002	95.826999999999998	95.847999999999999	95.867999999999995	95.888000000000005	95.906999999999996	95.927000000000007	95.947000000000003	95.966999999999999	95.986999999999995	96.007000000000005	96.028000000000006	96.048000000000002	96.066999999999993	96.087999999999994	96.108000000000004	96.128	96.147000000000006	96.167000000000002	96.186999999999998	96.207999999999998	96.227999999999994	96.248000000000005	96.266999999999996	96.287000000000006	96.307000000000002	96.326999999999998	96.346999999999994	96.367000000000004	96.388000000000005	96.406999999999996	96.427000000000007	96.447000000000003	96.466999999999999	96.486999999999995	96.507000000000005	96.527000000000001	96.546999999999997	96.566999999999993	96.587000000000003	96.606999999999999	96.626999999999995	96.647000000000006	96.667000000000002	96.686999999999998	96.706999999999994	96.727000000000004	96.747	96.766999999999996	96.786000000000001	96.807000000000002	96.826999999999998	96.846999999999994	96.866	96.885999999999996	96.906999999999996	96.926000000000002	96.945999999999998	96.965999999999994	96.986999999999995	97.007000000000005	97.025999999999996	97.046999999999997	97.066999999999993	97.087000000000003	97.105999999999995	97.126000000000005	97.147000000000006	97.167000000000002	97.186000000000007	97.206000000000003	97.225999999999999	97.245999999999995	97.266000000000005	97.286000000000001	97.305999999999997	97.325999999999993	97.346000000000004	97.366	97.385999999999996	97.406000000000006	97.426000000000002	97.445999999999998	97.465999999999994	97.486999999999995	97.506	97.525999999999996	97.546000000000006	97.566000000000003	97.585999999999999	97.605999999999995	97.626000000000005	97.646000000000001	97.665999999999997	97.686000000000007	97.706000000000003	97.725999999999999	97.745000000000005	97.766000000000005	97.786000000000001	97.805999999999997	97.825000000000003	97.844999999999999	97.864999999999995	97.885999999999996	97.906000000000006	97.926000000000002	97.945999999999998	97.965999999999994	97.986000000000004	98.004999999999995	98.025999999999996	98.046000000000006	98.064999999999998	98.084999999999994	98.105000000000004	98.126000000000005	98.144999999999996	98.165999999999997	98.186000000000007	98.204999999999998	98.224999999999994	98.245000000000005	98.266000000000005	98.286000000000001	98.305999999999997	98.325000000000003	98.344999999999999	98.364999999999995	98.385000000000005	98.405000000000001	98.424999999999997	98.444999999999993	98.465000000000003	98.484999999999999	98.504999999999995	98.525000000000006	98.545000000000002	98.564999999999998	98.585999999999999	98.605000000000004	98.625	98.644999999999996	98.665000000000006	98.685000000000002	98.704999999999998	98.724999999999994	98.745000000000005	98.765000000000001	98.784000000000006	98.804000000000002	98.823999999999998	98.844999999999999	98.864999999999995	98.885000000000005	98.905000000000001	98.924999999999997	98.944999999999993	98.963999999999999	98.984999999999999	99.004999999999995	99.025000000000006	99.043999999999997	99.063999999999993	99.084000000000003	99.103999999999999	99.123999999999995	99.144999999999996	99.164000000000001	99.183999999999997	99.204999999999998	99.224000000000004	99.245000000000005	99.263999999999996	99.284000000000006	99.304000000000002	99.323999999999998	99.343999999999994	99.364000000000004	99.384	99.403999999999996	99.424000000000007	99.444000000000003	99.463999999999999	99.483999999999995	99.504000000000005	99.525000000000006	99.543999999999997	99.563999999999993	99.584000000000003	99.603999999999999	99.623999999999995	99.644000000000005	99.664000000000001	99.683999999999997	99.703999999999994	99.724000000000004	99.744	99.763999999999996	99.784000000000006	99.804000000000002	99.822999999999993	99.843000000000004	99.864000000000004	99.884	99.903999999999996	99.923000000000002	99.944000000000003	99.962999999999994	99.983999999999995	100.003	100.024	100.044	100.06399999999999	100.084	100.10299999999999	100.124	100.143	100.164	100.184	100.20399999999999	100.223	100.24299999999999	100.26300000000001	100.283	100.304	100.32299999999999	100.343	100.364	100.383	100.40300000000001	100.42400000000001	100.443	100.464	100.483	100.503	100.523	100.54300000000001	100.563	100.583	100.60299999999999	100.623	100.643	100.663	100.68300000000001	100.703	100.723	100.74299999999999	100.76300000000001	100.783	100.803	100.822	100.843	100.863	100.88200000000001	100.902	100.923	100.943	100.96299999999999	100.983	101.003	101.023	101.042	101.062	101.08199999999999	101.10299999999999	101.123	101.142	101.16200000000001	101.18300000000001	101.202	101.223	101.242	101.26300000000001	101.283	101.30200000000001	101.32299999999999	101.342	101.36199999999999	101.38200000000001	101.402	101.422	101.44199999999999	101.462	101.482	101.502	101.52200000000001	101.542	101.562	101.583	101.602	101.622	101.642	101.66200000000001	101.68300000000001	101.702	101.72199999999999	101.742	101.762	101.782	101.80200000000001	101.822	101.842	101.86199999999999	101.88200000000001	101.902	101.922	101.94199999999999	101.962	101.982	102.002	102.02200000000001	102.042	102.062	102.08199999999999	102.102	102.122	102.14100000000001	102.16200000000001	102.181	102.202	102.221	102.241	102.261	102.28100000000001	102.301	102.322	102.34099999999999	102.36199999999999	102.381	102.401	102.42100000000001	102.44199999999999	102.461	102.48099999999999	102.502	102.521	102.541	102.56100000000001	102.58199999999999	102.601	102.621	102.64100000000001	102.661	102.681	102.70099999999999	102.721	102.741	102.761	102.78100000000001	102.801	102.821	102.84099999999999	102.861	102.881	102.901	102.92100000000001	102.941	102.961	102.98	103.001	103.021	103.041	103.06100000000001	103.081	103.101	103.12	103.14100000000001	103.16	103.181	103.20099999999999	103.22	103.241	103.26	103.28100000000001	103.301	103.321	103.34099999999999	103.36	103.38	103.4	103.42	103.44	103.461	103.48099999999999	103.501	103.52	103.54	103.56	103.581	103.6	103.62	103.64	103.66	103.68	103.7	103.72	103.74	103.76	103.78	103.8	103.82	103.84	103.86	103.88	103.899	103.919	103.93899999999999	103.96	103.98	104	104.02	104.04	104.06	104.08	104.1	104.12	104.14	104.16	104.18	104.199	104.21899999999999	104.239	104.26	104.279	104.29900000000001	104.32	104.34	104.36	104.38	104.4	104.419	104.43899999999999	104.459	104.48	104.499	104.51900000000001	104.539	104.559	104.57899999999999	104.6	104.619	104.639	104.65900000000001	104.679	104.699	104.71899999999999	104.739	104.759	104.779	104.79900000000001	104.819	104.839	104.85899999999999	104.879	104.899	104.919	104.93899999999999	104.959	104.979	104.999	105.01900000000001	105.039	105.059	105.07899999999999	105.099	105.119	105.139	105.15900000000001	105.178	105.199	105.21899999999999	105.239	105.258	105.27800000000001	105.29900000000001	105.318	105.339	105.35899999999999	105.379	105.399	105.41800000000001	105.43899999999999	105.458	105.479	105.498	105.518	105.538	105.55800000000001	105.57899999999999	105.598	105.61799999999999	105.63800000000001	105.658	105.678	105.69799999999999	105.718	105.738	105.758	105.77800000000001	105.798	105.818	105.83799999999999	105.858	105.878	105.898	105.91800000000001	105.938	105.958	105.97799999999999	105.998	106.018	106.03700000000001	106.05800000000001	106.078	106.098	106.117	106.13800000000001	106.157	106.178	106.197	106.218	106.238	106.258	106.277	106.297	106.318	106.33799999999999	106.357	106.378	106.398	106.41800000000001	106.438	106.458	106.477	106.497	106.517	106.53700000000001	106.557	106.577	106.59699999999999	106.61799999999999	106.637	106.657	106.678	106.697	106.717	106.73699999999999	106.75700000000001	106.777	106.797	106.81699999999999	106.837	106.857	106.877	106.89700000000001	106.917	106.937	106.95699999999999	106.977	106.996	107.017	107.036	107.056	107.077	107.096	107.117	107.136	107.15600000000001	107.176	107.197	107.217	107.236	107.256	107.276	107.297	107.31699999999999	107.336	107.357	107.376	107.39700000000001	107.417	107.43600000000001	107.45699999999999	107.476	107.497	107.517	107.536	107.556	107.57599999999999	107.59699999999999	107.616	107.636	107.657	107.67700000000001	107.697	107.71599999999999	107.736	107.756	107.776	107.79600000000001	107.816	107.836	107.85599999999999	107.876	107.89700000000001	107.916	107.93600000000001	107.956	107.976	107.996	108.01600000000001	108.035	108.05500000000001	108.07599999999999	108.096	108.116	108.13500000000001	108.15600000000001	108.176	108.196	108.21599999999999	108.236	108.255	108.276	108.29600000000001	108.315	108.33499999999999	108.355	108.376	108.396	108.416	108.43600000000001	108.455	108.476	108.496	108.515	108.536	108.55500000000001	108.57599999999999	108.595	108.61499999999999	108.63500000000001	108.655	108.675	108.696	108.71599999999999	108.735	108.756	108.77500000000001	108.79600000000001	108.815	108.836	108.855	108.875	108.895	108.91500000000001	108.935	108.955	108.97499999999999	108.995	109.015	109.03400000000001	109.05500000000001	109.075	109.095	109.11499999999999	109.13500000000001	109.155	109.175	109.19499999999999	109.215	109.23399999999999	109.255	109.27500000000001	109.294	109.315	109.33499999999999	109.354	109.375	109.395	109.414	109.434	109.455	109.474	109.494	109.515	109.53400000000001	109.55500000000001	109.574	109.59399999999999	109.614	109.63500000000001	109.654	109.67400000000001	109.694	109.715	109.735	109.754	109.774	109.794	109.81399999999999	109.834	109.854	109.874	109.89400000000001	109.914	109.934	109.955	109.974	109.994	110.015	110.03400000000001	110.053	110.074	110.09399999999999	110.114	110.133	110.154	110.17400000000001	110.194	110.214	110.23399999999999	110.254	110.274	110.294	110.313	110.333	110.35299999999999	110.373	110.393	110.413	110.43300000000001	110.453	110.473	110.49299999999999	110.51300000000001	110.533	110.553	110.57299999999999	110.593	110.613	110.633	110.65300000000001	110.673	110.693	110.71299999999999	110.733	110.753	110.773	110.794	110.813	110.833	110.85299999999999	110.873	110.893	110.913	110.93300000000001	110.953	110.974	110.994	111.01300000000001	111.033	111.053	111.07299999999999	111.092	111.113	111.133	111.15300000000001	111.173	111.193	111.21299999999999	111.233	111.253	111.273	111.29300000000001	111.313	111.333	111.352	111.373	111.392	111.413	111.432	111.453	111.473	111.49299999999999	111.51300000000001	111.533	111.55200000000001	111.57299999999999	111.593	111.61199999999999	111.63200000000001	111.65300000000001	111.673	111.69199999999999	111.712	111.732	111.753	111.77200000000001	111.792	111.812	111.83199999999999	111.852	111.872	111.892	111.91200000000001	111.932	111.952	111.97199999999999	111.992	112.012	112.032	112.05200000000001	112.072	112.092	112.11199999999999	112.131	112.152	112.172	112.19199999999999	112.212	112.232	112.252	112.27200000000001	112.292	112.312	112.33199999999999	112.351	112.371	112.39100000000001	112.41200000000001	112.432	112.452	112.471	112.491	112.512	112.532	112.55200000000001	112.571	112.592	112.611	112.631	112.651	112.67100000000001	112.691	112.712	112.73099999999999	112.751	112.77200000000001	112.792	112.812	112.831	112.851	112.871	112.89100000000001	112.911	112.932	112.95099999999999	112.971	112.991	113.011	113.03100000000001	113.051	113.071	113.092	113.111	113.131	113.151	113.17100000000001	113.191	113.211	113.23099999999999	113.251	113.271	113.291	113.31100000000001	113.331	113.351	113.37	113.39	113.411	113.431	113.45099999999999	113.47	113.491	113.511	113.53100000000001	113.551	113.571	113.59	113.611	113.631	113.65	113.67100000000001	113.691	113.71	113.73	113.75	113.77	113.791	113.81	113.831	113.85	113.871	113.89	113.91	113.931	113.95	113.97	113.99	114.01	114.03100000000001	114.05	114.07	114.09	114.111	114.13	114.15	114.17	114.19	114.21	114.23	114.25	114.27	114.29	114.31	114.32899999999999	114.35	114.37	114.39	114.41	114.43	114.45	114.46899999999999	114.49	114.51	114.53	114.55	114.569	114.589	114.61	114.63	114.65	114.67	114.69	114.709	114.73	114.749	114.77	114.79	114.81	114.82899999999999	114.849	114.869	114.889	114.90900000000001	114.929	114.949	114.97	114.989	115.009	115.029	115.04900000000001	115.069	115.089	115.10899999999999	115.129	115.15	115.169	115.18899999999999	115.209	115.22799999999999	115.249	115.26900000000001	115.289	115.309	115.32899999999999	115.349	115.369	115.389	115.40900000000001	115.429	115.449	115.46899999999999	115.488	115.509	115.52800000000001	115.54900000000001	115.569	115.589	115.60899999999999	115.628	115.649	115.669	115.688	115.709	115.72799999999999	115.749	115.76900000000001	115.788	115.809	115.82899999999999	115.849	115.869	115.889	115.908	115.928	115.94799999999999	115.968	115.988	116.008	116.02800000000001	116.04900000000001	116.068	116.08799999999999	116.108	116.128	116.148	116.16800000000001	116.187	116.208	116.22799999999999	116.248	116.268	116.288	116.30800000000001	116.328	116.34699999999999	116.36799999999999	116.38800000000001	116.408	116.428	116.44799999999999	116.468	116.488	116.508	116.527	116.548	116.568	116.58799999999999	116.608	116.628	116.648	116.667	116.687	116.70699999999999	116.727	116.747	116.767	116.78700000000001	116.80800000000001	116.828	116.848	116.86799999999999	116.88800000000001	116.908	116.928	116.947	116.967	116.98699999999999	117.00700000000001	117.027	117.047	117.06699999999999	117.087	117.107	117.127	117.14700000000001	117.167	117.187	117.206	117.226	117.246	117.267	117.28700000000001	117.307	117.32599999999999	117.34699999999999	117.367	117.387	117.407	117.426	117.447	117.467	117.48699999999999	117.50700000000001	117.527	117.547	117.566	117.586	117.607	117.627	117.64700000000001	117.667	117.687	117.706	117.726	117.747	117.76600000000001	117.786	117.806	117.82599999999999	117.84699999999999	117.866	117.886	117.90600000000001	117.92700000000001	117.947	117.96599999999999	117.986	118.006	118.026	118.047	118.06699999999999	118.086	118.10599999999999	118.126	118.146	118.167	118.187	118.206	118.226	118.246	118.26600000000001	118.286	118.306	118.32599999999999	118.346	118.366	118.38500000000001	118.405	118.425	118.446	118.46599999999999	118.486	118.506	118.52500000000001	118.545	118.566	118.586	118.60599999999999	118.625	118.645	118.66500000000001	118.68600000000001	118.705	118.726	118.746	118.76600000000001	118.786	118.806	118.825	118.845	118.86499999999999	118.886	118.90600000000001	118.926	118.94499999999999	118.96599999999999	118.985	119.005	119.026	119.045	119.065	119.08499999999999	119.105	119.126	119.145	119.166	119.185	119.205	119.22499999999999	119.245	119.265	119.285	119.30500000000001	119.325	119.345	119.36499999999999	119.38500000000001	119.405	119.425	119.44499999999999	119.465	119.485	119.505	119.52500000000001	119.545	119.565	119.58499999999999	119.604	119.624	119.64400000000001	119.66500000000001	119.684	119.70399999999999	119.72499999999999	119.744	119.764	119.785	119.80500000000001	119.825	119.84399999999999	119.864	119.884	119.904	119.925	119.944	119.964	119.985	120.004	120.024	120.045	120.065	120.084	120.104	120.124	120.14400000000001	120.164	120.184	120.20399999999999	120.22499999999999	120.244	120.264	120.28400000000001	120.304	120.324	120.34399999999999	120.364	120.384	120.404	120.42400000000001	120.444	120.464	120.48399999999999	120.504	120.524	120.544	120.56399999999999	120.584	120.604	120.624	120.64400000000001	120.664	120.684	120.70399999999999	120.723	120.744	120.76300000000001	120.78400000000001	120.804	120.82299999999999	120.84399999999999	120.864	120.883	120.904	120.923	120.943	120.96299999999999	120.98399999999999	121.004	121.023	121.04300000000001	121.06399999999999	121.083	121.10299999999999	121.124	121.143	121.163	121.18300000000001	121.203	121.224	121.24299999999999	121.26300000000001	121.283	121.30200000000001	121.32299999999999	121.343	121.363	121.383	121.40300000000001	121.423	121.443	121.46299999999999	121.483	121.503	121.52200000000001	121.542	121.563	121.583	121.60299999999999	121.623	121.643	121.663	121.682	121.702	121.723	121.742	121.762	121.782	121.803	121.82299999999999	121.843	121.86199999999999	121.88200000000001	121.90300000000001	121.922	121.94199999999999	121.962	121.982	122.003	122.023	122.042	122.062	122.08199999999999	122.10299999999999	122.123	122.143	122.16200000000001	122.182	122.202	122.223	122.242	122.262	122.282	122.30200000000001	122.322	122.342	122.36199999999999	122.38200000000001	122.402	122.422	122.44199999999999	122.462	122.482	122.502	122.52200000000001	122.542	122.562	122.58199999999999	122.602	122.622	122.642	122.66200000000001	122.681	122.702	122.721	122.742	122.761	122.78100000000001	122.80200000000001	122.822	122.842	122.86199999999999	122.881	122.901	122.922	122.94199999999999	122.962	122.98099999999999	123.001	123.02200000000001	123.042	123.06100000000001	123.08199999999999	123.101	123.121	123.14100000000001	123.161	123.181	123.20099999999999	123.221	123.242	123.261	123.282	123.301	123.321	123.34099999999999	123.361	123.381	123.401	123.42100000000001	123.441	123.461	123.48099999999999	123.501	123.521	123.541	123.56100000000001	123.581	123.601	123.621	123.64	123.661	123.681	123.70099999999999	123.721	123.74	123.761	123.78100000000001	123.801	123.821	123.84099999999999	123.86	123.88	123.901	123.92100000000001	123.941	123.96	123.98	124	124.021	124.04	124.06	124.081	124.1	124.121	124.14	124.16	124.18	124.2	124.221	124.24	124.26	124.28	124.3	124.321	124.34	124.36	124.38	124.4	124.42	124.44	124.46	124.48	124.5	124.52	124.54	124.56	124.58	124.6	124.62	124.64	124.65900000000001	124.679	124.7	124.72	124.74	124.76	124.78	124.8	124.82	124.84	124.85899999999999	124.88	124.9	124.92	124.94	124.959	124.98	124.999	125.01900000000001	125.039	125.06	125.08	125.1	125.119	125.14	125.15900000000001	125.179	125.199	125.21899999999999	125.239	125.259	125.279	125.29900000000001	125.32	125.339	125.36	125.38	125.399	125.419	125.43899999999999	125.459	125.479	125.499	125.51900000000001	125.539	125.559	125.57899999999999	125.599	125.619	125.639	125.65900000000001	125.678	125.699	125.71899999999999	125.739	125.759	125.779	125.79900000000001	125.819	125.839	125.85899999999999	125.879	125.898	125.919	125.93899999999999	125.958	125.97799999999999	125.998	126.018	126.038	126.059	126.078	126.098	126.11799999999999	126.13800000000001	126.15900000000001	126.178	126.19799999999999	126.218	126.238	126.258	126.279	126.298	126.318	126.339	126.358	126.378	126.398	126.41800000000001	126.438	126.458	126.47799999999999	126.498	126.518	126.538	126.557	126.578	126.598	126.61799999999999	126.63800000000001	126.658	126.67700000000001	126.697	126.718	126.738	126.758	126.77800000000001	126.797	126.818	126.837	126.858	126.878	126.89700000000001	126.91800000000001	126.937	126.958	126.97799999999999	126.997	127.017	127.03700000000001	127.057	127.077	127.09699999999999	127.117	127.137	127.158	127.178	127.197	127.217	127.238	127.25700000000001	127.277	127.297	127.31699999999999	127.337	127.357	127.377	127.39700000000001	127.417	127.437	127.45699999999999	127.477	127.497	127.517	127.53700000000001	127.557	127.577	127.59699999999999	127.617	127.637	127.657	127.67700000000001	127.697	127.717	127.73699999999999	127.75700000000001	127.777	127.797	127.81699999999999	127.837	127.857	127.877	127.89700000000001	127.916	127.93600000000001	127.956	127.976	127.996	128.01599999999999	128.036	128.05699999999999	128.07599999999999	128.096	128.11600000000001	128.136	128.15700000000001	128.17599999999999	128.196	128.21600000000001	128.23599999999999	128.256	128.27600000000001	128.297	128.316	128.33699999999999	128.35599999999999	128.376	128.39599999999999	128.416	128.43600000000001	128.45699999999999	128.476	128.49600000000001	128.51599999999999	128.536	128.55600000000001	128.57599999999999	128.596	128.61600000000001	128.636	128.65600000000001	128.67599999999999	128.696	128.71600000000001	128.73599999999999	128.755	128.77600000000001	128.79499999999999	128.816	128.83500000000001	128.85499999999999	128.876	128.89500000000001	128.91499999999999	128.93600000000001	128.95599999999999	128.976	128.99600000000001	129.01599999999999	129.036	129.05600000000001	129.07599999999999	129.096	129.11600000000001	129.136	129.15600000000001	129.17500000000001	129.19499999999999	129.215	129.23599999999999	129.255	129.27500000000001	129.29499999999999	129.315	129.33500000000001	129.35499999999999	129.375	129.39500000000001	129.41499999999999	129.435	129.45599999999999	129.476	129.495	129.51499999999999	129.535	129.55500000000001	129.57499999999999	129.59399999999999	129.61500000000001	129.63499999999999	129.655	129.67500000000001	129.69499999999999	129.715	129.73500000000001	129.755	129.77500000000001	129.79400000000001	129.815	129.83500000000001	129.85499999999999	129.875	129.89500000000001	129.91499999999999	129.935	129.95500000000001	129.97499999999999	129.995	130.01400000000001	130.03399999999999	130.05500000000001	130.07499999999999	130.09399999999999	130.11500000000001	130.13499999999999	130.155	130.17400000000001	130.19499999999999	130.214	130.23500000000001	130.25399999999999	130.274	130.29400000000001	130.31399999999999	130.334	130.35499999999999	130.375	130.39500000000001	130.41399999999999	130.434	130.45400000000001	130.47499999999999	130.495	130.51400000000001	130.53399999999999	130.554	130.57400000000001	130.59399999999999	130.614	130.63399999999999	130.654	130.67400000000001	130.69399999999999	130.714	130.73400000000001	130.75399999999999	130.774	130.79400000000001	130.81299999999999	130.834	130.85400000000001	130.874	130.89400000000001	130.91399999999999	130.934	130.95400000000001	130.97300000000001	130.99299999999999	131.01400000000001	131.03399999999999	131.053	131.07400000000001	131.09399999999999	131.114	131.13300000000001	131.15299999999999	131.173	131.19399999999999	131.214	131.233	131.25399999999999	131.274	131.29400000000001	131.31299999999999	131.333	131.35300000000001	131.37299999999999	131.39400000000001	131.41399999999999	131.43299999999999	131.453	131.47300000000001	131.494	131.51400000000001	131.53299999999999	131.553	131.57300000000001	131.59299999999999	131.613	131.63399999999999	131.65299999999999	131.673	131.69300000000001	131.71299999999999	131.733	131.75299999999999	131.773	131.79300000000001	131.81299999999999	131.833	131.852	131.87299999999999	131.893	131.91200000000001	131.93199999999999	131.953	131.97200000000001	131.99199999999999	132.01300000000001	132.03299999999999	132.053	132.07300000000001	132.09200000000001	132.11199999999999	132.13200000000001	132.15199999999999	132.172	132.19300000000001	132.21199999999999	132.232	132.25299999999999	132.27199999999999	132.292	132.31200000000001	132.333	132.352	132.37299999999999	132.392	132.41200000000001	132.43199999999999	132.452	132.47200000000001	132.49299999999999	132.512	132.53200000000001	132.55199999999999	132.572	132.59200000000001	132.61199999999999	132.63200000000001	132.65199999999999	132.672	132.69200000000001	132.71199999999999	132.732	132.75200000000001	132.77199999999999	132.792	132.81200000000001	132.83199999999999	132.852	132.87100000000001	132.89099999999999	132.911	132.93199999999999	132.952	132.97200000000001	132.99100000000001	133.011	133.03100000000001	133.05199999999999	133.072	133.09100000000001	133.11199999999999	133.131	133.15100000000001	133.17099999999999	133.19200000000001	133.21199999999999	133.232	133.251	133.27099999999999	133.291	133.31200000000001	133.33199999999999	133.351	133.37100000000001	133.39099999999999	133.411	133.43199999999999	133.45099999999999	133.471	133.49199999999999	133.511	133.53200000000001	133.55099999999999	133.571	133.59100000000001	133.61099999999999	133.631	133.65100000000001	133.67099999999999	133.691	133.71100000000001	133.73099999999999	133.751	133.77099999999999	133.791	133.81100000000001	133.83099999999999	133.85	133.87	133.88999999999999	133.911	133.93100000000001	133.95099999999999	133.97	133.99100000000001	134.01	134.03100000000001	134.05099999999999	134.071	134.09100000000001	134.11099999999999	134.131	134.15100000000001	134.17099999999999	134.191	134.21	134.22999999999999	134.25	134.27099999999999	134.291	134.31	134.33000000000001	134.35	134.37	134.38999999999999	134.41	134.43100000000001	134.44999999999999	134.47	134.49	134.51	134.53100000000001	134.55099999999999	134.57	134.59	134.61000000000001	134.63	134.65	134.66999999999999	134.69	134.71	134.72999999999999	134.75	134.77000000000001	134.79	134.81	134.83000000000001	134.85	134.87	134.88999999999999	134.90899999999999	134.929	134.94999999999999	134.97	134.99	135.01	135.03	135.05000000000001	135.07	135.09	135.11000000000001	135.12899999999999	135.15	135.16900000000001	135.18899999999999	135.21	135.22999999999999	135.25	135.26900000000001	135.28899999999999	135.309	135.33000000000001	135.35	135.37	135.38900000000001	135.40899999999999	135.429	135.44999999999999	135.46899999999999	135.489	135.50899999999999	135.529	135.54900000000001	135.56899999999999	135.589	135.60900000000001	135.62899999999999	135.649	135.66900000000001	135.68899999999999	135.709	135.72900000000001	135.749	135.76900000000001	135.78899999999999	135.809	135.82900000000001	135.84899999999999	135.869	135.88900000000001	135.90799999999999	135.929	135.94900000000001	135.96899999999999	135.988	136.00899999999999	136.029	136.04900000000001	136.06899999999999	136.089	136.108	136.12799999999999	136.148	136.16900000000001	136.18899999999999	136.209	136.22800000000001	136.24799999999999	136.268	136.28899999999999	136.309	136.328	136.34899999999999	136.36799999999999	136.38800000000001	136.40899999999999	136.429	136.44900000000001	136.46799999999999	136.488	136.50800000000001	136.52799999999999	136.548	136.56899999999999	136.58799999999999	136.608	136.62799999999999	136.649	136.66900000000001	136.68799999999999	136.708	136.72800000000001	136.74799999999999	136.768	136.78800000000001	136.80799999999999	136.82900000000001	136.84899999999999	136.86799999999999	136.88800000000001	136.90799999999999	136.928	136.94800000000001	136.96799999999999	136.988	137.00800000000001	137.02799999999999	137.048	137.06800000000001	137.08799999999999	137.108	137.12799999999999	137.148	137.16800000000001	137.18799999999999	137.208	137.22800000000001	137.24700000000001	137.268	137.28800000000001	137.30699999999999	137.328	137.34800000000001	137.36699999999999	137.38800000000001	137.40700000000001	137.428	137.447	137.46799999999999	137.48699999999999	137.50700000000001	137.52699999999999	137.547	137.56700000000001	137.58699999999999	137.607	137.62700000000001	137.64699999999999	137.667	137.68700000000001	137.70699999999999	137.727	137.74700000000001	137.767	137.78800000000001	137.80699999999999	137.827	137.84700000000001	137.86699999999999	137.887	137.90700000000001	137.92699999999999	137.947	137.96700000000001	137.98699999999999	138.00700000000001	138.02699999999999	138.047	138.06700000000001	138.08699999999999	138.107	138.12700000000001	138.14599999999999	138.167	138.18600000000001	138.20699999999999	138.227	138.24700000000001	138.267	138.28700000000001	138.30699999999999	138.32599999999999	138.34700000000001	138.36699999999999	138.386	138.40700000000001	138.42699999999999	138.447	138.46700000000001	138.48699999999999	138.506	138.52600000000001	138.54599999999999	138.566	138.58699999999999	138.60599999999999	138.626	138.64599999999999	138.666	138.68600000000001	138.70599999999999	138.726	138.74700000000001	138.76599999999999	138.786	138.80699999999999	138.827	138.846	138.86600000000001	138.886	138.90600000000001	138.92599999999999	138.946	138.965	138.98500000000001	139.006	139.02600000000001	139.04599999999999	139.066	139.08600000000001	139.10599999999999	139.126	139.14599999999999	139.166	139.18600000000001	139.20599999999999	139.226	139.24600000000001	139.26599999999999	139.285	139.30500000000001	139.32499999999999	139.346	139.36500000000001	139.38499999999999	139.40600000000001	139.42500000000001	139.44499999999999	139.465	139.48500000000001	139.505	139.52500000000001	139.54499999999999	139.565	139.58500000000001	139.60599999999999	139.625	139.64599999999999	139.66499999999999	139.685	139.70599999999999	139.72499999999999	139.745	139.76499999999999	139.785	139.80500000000001	139.82499999999999	139.845	139.86500000000001	139.88499999999999	139.905	139.92500000000001	139.94499999999999	139.965	139.98500000000001	140.005	140.02500000000001	140.04400000000001	140.065	140.08500000000001	140.10499999999999	140.124	140.14500000000001	140.16499999999999	140.185	140.20500000000001	140.22399999999999	140.245	140.26499999999999	140.285	140.30500000000001	140.32499999999999	140.345	140.36500000000001	140.38499999999999	140.405	140.42500000000001	140.44499999999999	140.465	140.48400000000001	140.50399999999999	140.524	140.54400000000001	140.56399999999999	140.584	140.60499999999999	140.625	140.64500000000001	140.66399999999999	140.684	140.70400000000001	140.72499999999999	140.744	140.76400000000001	140.78399999999999	140.804	140.82400000000001	140.84399999999999	140.864	140.88399999999999	140.904	140.92400000000001	140.94399999999999	140.964	140.98400000000001	141.00399999999999	141.024	141.04300000000001	141.06399999999999	141.084	141.10400000000001	141.124	141.14400000000001	141.16300000000001	141.184	141.20400000000001	141.22399999999999	141.244	141.26400000000001	141.28299999999999	141.303	141.32300000000001	141.34299999999999	141.363	141.38399999999999	141.40299999999999	141.423	141.44399999999999	141.464	141.48400000000001	141.50299999999999	141.523	141.54300000000001	141.56399999999999	141.583	141.60300000000001	141.62299999999999	141.643	141.66300000000001	141.684	141.70400000000001	141.72300000000001	141.74299999999999	141.76300000000001	141.78399999999999	141.803	141.82300000000001	141.84299999999999	141.863	141.88300000000001	141.90299999999999	141.923	141.94300000000001	141.96299999999999	141.983	142.00299999999999	142.023	142.042	142.06200000000001	142.08199999999999	142.10300000000001	142.12299999999999	142.143	142.16300000000001	142.18199999999999	142.203	142.22300000000001	142.24299999999999	142.26300000000001	142.28299999999999	142.303	142.32300000000001	142.34200000000001	142.36199999999999	142.38300000000001	142.40199999999999	142.422	142.44200000000001	142.46299999999999	142.483	142.50299999999999	142.52199999999999	142.54300000000001	142.56200000000001	142.58199999999999	142.60300000000001	142.62299999999999	142.642	142.66200000000001	142.68199999999999	142.702	142.72300000000001	142.74299999999999	142.762	142.78200000000001	142.80199999999999	142.822	142.84200000000001	142.86199999999999	142.88200000000001	142.90199999999999	142.922	142.94200000000001	142.96299999999999	142.982	143.00200000000001	143.02199999999999	143.042	143.06200000000001	143.08199999999999	143.102	143.12200000000001	143.142	143.16200000000001	143.18199999999999	143.202	143.22200000000001	143.24199999999999	143.262	143.28200000000001	143.30199999999999	143.322	143.34200000000001	143.36099999999999	143.38200000000001	143.40199999999999	143.422	143.441	143.46100000000001	143.482	143.50200000000001	143.52199999999999	143.542	143.56100000000001	143.58099999999999	143.601	143.62200000000001	143.642	143.66200000000001	143.68100000000001	143.70099999999999	143.72200000000001	143.74199999999999	143.762	143.78100000000001	143.80099999999999	143.821	143.84100000000001	143.86099999999999	143.881	143.90100000000001	143.92099999999999	143.941	143.96100000000001	143.98099999999999	144.001	144.02099999999999	144.041	144.06100000000001	144.08099999999999	144.101	144.12100000000001	144.14099999999999	144.161	144.18	144.20099999999999	144.221	144.24100000000001	144.261	144.28100000000001	144.30099999999999	144.321	144.34100000000001	144.36099999999999	144.381	144.4	144.41999999999999	144.44	144.46	144.47999999999999	144.501	144.52099999999999	144.541	144.56	144.58099999999999	144.6	144.62	144.63999999999999	144.661	144.68	144.70099999999999	144.721	144.74	144.761	144.78	144.80000000000001	144.821	144.84	144.86099999999999	144.88	144.9	144.91999999999999	144.941	144.96	144.97999999999999	145	145.02000000000001	145.04	145.06	145.08000000000001	145.1	145.12	145.13999999999999	145.16	145.18	145.19999999999999	145.22	145.24	145.26	145.279	145.30000000000001	145.31899999999999	145.34	145.36000000000001	145.38	145.399	145.41999999999999	145.44	145.46	145.47999999999999	145.5	145.51900000000001	145.54	145.559	145.58000000000001	145.59899999999999	145.62	145.63900000000001	145.66	145.679	145.69900000000001	145.71899999999999	145.739	145.76	145.779	145.79900000000001	145.81899999999999	145.84	145.86000000000001	145.87899999999999	145.899	145.91900000000001	145.94	145.959	145.97900000000001	145.999	146.01900000000001	146.03899999999999	146.059	146.07900000000001	146.09899999999999	146.12	146.13900000000001	146.15899999999999	146.179	146.19900000000001	146.21799999999999	146.239	146.25899999999999	146.279	146.29900000000001	146.31800000000001	146.339	146.35900000000001	146.37899999999999	146.398	146.41800000000001	146.43899999999999	146.458	146.47900000000001	146.499	146.518	146.53800000000001	146.559	146.578	146.59800000000001	146.61799999999999	146.63800000000001	146.65899999999999	146.679	146.69900000000001	146.71799999999999	146.739	146.75800000000001	146.779	146.79900000000001	146.81899999999999	146.839	146.85900000000001	146.87899999999999	146.898	146.91900000000001	146.93799999999999	146.958	146.97800000000001	146.99799999999999	147.018	147.03800000000001	147.05799999999999	147.07900000000001	147.09800000000001	147.11799999999999	147.13800000000001	147.15799999999999	147.178	147.19800000000001	147.21799999999999	147.238	147.25800000000001	147.27799999999999	147.298	147.31800000000001	147.33799999999999	147.358	147.37799999999999	147.398	147.41800000000001	147.43700000000001	147.458	147.47800000000001	147.49799999999999	147.518	147.53700000000001	147.55699999999999	147.577	147.59700000000001	147.61799999999999	147.637	147.65700000000001	147.67699999999999	147.69800000000001	147.71799999999999	147.73699999999999	147.75700000000001	147.77699999999999	147.797	147.81800000000001	147.83799999999999	147.857	147.87700000000001	147.89699999999999	147.91800000000001	147.93700000000001	147.95699999999999	147.977	147.99700000000001	148.017	148.03700000000001	148.05799999999999	148.078	148.09700000000001	148.11799999999999	148.137	148.15700000000001	148.17699999999999	148.197	148.21700000000001	148.23699999999999	148.25700000000001	148.27699999999999	148.297	148.31700000000001	148.33699999999999	148.357	148.37700000000001	148.39699999999999	148.417	148.43700000000001	148.45599999999999	148.477	148.49700000000001	148.51599999999999	148.536	148.55600000000001	148.57599999999999	148.59700000000001	148.61699999999999	148.637	148.65600000000001	148.67599999999999	148.696	148.71700000000001	148.73699999999999	148.756	148.77600000000001	148.79599999999999	148.81700000000001	148.83600000000001	148.85599999999999	148.876	148.89699999999999	148.916	148.93600000000001	148.95599999999999	148.976	148.99600000000001	149.01599999999999	149.036	149.05600000000001	149.07599999999999	149.09700000000001	149.11600000000001	149.136	149.15600000000001	149.17699999999999	149.196	149.21600000000001	149.23599999999999	149.256	149.27600000000001	149.29599999999999	149.316	149.33600000000001	149.35499999999999	149.376	149.39599999999999	149.416	149.435	149.45500000000001	149.47499999999999	149.49600000000001	149.51499999999999	149.535	149.55600000000001	149.57599999999999	149.596	149.61500000000001	149.636	149.65600000000001	149.67599999999999	149.69499999999999	149.71600000000001	149.73500000000001	149.755	149.77500000000001	149.79599999999999	149.815	149.83500000000001	149.85499999999999	149.876	149.89599999999999	149.91499999999999	149.93600000000001	149.95500000000001	149.97499999999999	149.995	150.01499999999999	150.035	150.05500000000001	150.07499999999999	150.095	150.11500000000001	150.13499999999999	150.155	150.17500000000001	150.19499999999999	150.215	150.23500000000001	150.255	150.27500000000001	150.29499999999999	150.315	150.33500000000001	150.35499999999999	150.374	150.39500000000001	150.41499999999999	150.435	150.45500000000001	150.47499999999999	150.494	150.51400000000001	150.53399999999999	150.554	150.57499999999999	150.595	150.614	150.63499999999999	150.654	150.67500000000001	150.69499999999999	150.715	150.73400000000001	150.75399999999999	150.774	150.79400000000001	150.81399999999999	150.83500000000001	150.85499999999999	150.875	150.89400000000001	150.91399999999999	150.934	150.95500000000001	150.97499999999999	150.994	151.01499999999999	151.03399999999999	151.054	151.07400000000001	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	0.01	0.01	0.01	0.01	0.01	0.01	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	0.02	0.02	0.02	0.02	2.5000000000000001E-2	2.5000000000000001E-2	0.03	0.03	0.03	3.5000000000000003E-2	3.5000000000000003E-2	0.04	0.04	4.4999999999999998E-2	4.4999999999999998E-2	0.05	0.05	5.5E-2	5.5E-2	0.06	6.5000000000000002E-2	6.5000000000000002E-2	7.0000000000000007E-2	7.4999999999999997E-2	7.4999999999999997E-2	0.08	8.5000000000000006E-2	8.5000000000000006E-2	0.09	9.5000000000000001E-2	9.5000000000000001E-2	0.1	0.105	0.11	0.11	0.115	0.12	0.125	0.13	0.13	0.14000000000000001	0.14499999999999999	0.15	0.155	0.16	0.17	0.17499999999999999	0.18	0.185	0.19	0.2	0.20499999999999999	0.21	0.215	0.22	0.22500000000000001	0.23499999999999999	0.24	0.245	0.25	0.255	0.26500000000000001	0.26500000000000001	0.27500000000000002	0.28000000000000003	0.28499999999999998	0.28999999999999998	0.29499999999999998	0.30499999999999999	0.31	0.315	0.32	0.32500000000000001	0.33500000000000002	0.34	0.34499999999999997	0.34499999999999997	0.35499999999999998	0.36	0.36499999999999999	0.37	0.38	0.38500000000000001	0.39	0.39500000000000002	0.4	0.40500000000000003	0.41	0.41499999999999998	0.42	0.42499999999999999	0.43	0.435	0.44	0.45	0.45500000000000002	0.46	0.46500000000000002	0.47	0.47499999999999998	0.48	0.48499999999999999	0.49	0.495	0.5	0.505	0.51500000000000001	0.52	0.52500000000000002	0.53	0.53500000000000003	0.54	0.55000000000000004	0.55500000000000005	0.56000000000000005	0.56499999999999995	0.56999999999999995	0.57499999999999996	0.57999999999999996	0.58499999999999996	0.59	0.59499999999999997	0.60499999999999998	0.61	0.61499999999999999	0.62	0.625	0.63	0.63500000000000001	0.64	0.64500000000000002	0.65500000000000003	0.66	0.66500000000000004	0.67	0.67500000000000004	0.68	0.68500000000000005	0.69	0.69499999999999995	0.7	0.71	0.71499999999999997	0.72	0.72499999999999998	0.73499999999999999	0.74	0.745	0.75	0.755	0.76	0.76500000000000001	0.77	0.77500000000000002	0.78500000000000003	0.79	0.79500000000000004	0.8	0.80500000000000005	0.81	0.81499999999999995	0.82	0.83	0.83499999999999996	0.84	0.84499999999999997	0.85	0.85499999999999998	0.86	0.87	0.875	0.88	0.88500000000000001	0.89500000000000002	0.9	0.90500000000000003	0.91	0.91500000000000004	0.92	0.93	0.93500000000000005	0.94	0.94499999999999995	0.95	0.95499999999999996	0.96	0.97	0.97499999999999998	0.98	0.98499999999999999	0.99	0.995	1	1.01	1.0149999999999999	1.02	1.0249999999999999	1.03	1.0349999999999999	1.0449999999999999	1.05	1.0549999999999999	1.06	1.0649999999999999	1.07	1.075	1.085	1.0900000000000001	1.095	1.1000000000000001	1.105	1.1100000000000001	1.115	1.125	1.1299999999999999	1.135	1.1399999999999999	1.145	1.1499999999999999	1.155	1.1599999999999999	1.17	1.175	1.18	1.1850000000000001	1.19	1.1950000000000001	1.2	1.21	1.2150000000000001	1.22	1.2250000000000001	1.23	1.2350000000000001	1.24	1.2450000000000001	1.25	1.26	1.2649999999999999	1.27	1.2749999999999999	1.28	1.2849999999999999	1.29	1.2949999999999999	1.3049999999999999	1.31	1.3149999999999999	1.32	1.325	1.33	1.34	1.345	1.35	1.355	1.36	1.365	1.37	1.375	1.38	1.385	1.39	1.395	1.405	1.41	1.415	1.42	1.425	1.43	1.4350000000000001	1.44	1.4450000000000001	1.45	1.46	1.4650000000000001	1.47	1.4750000000000001	1.48	1.4850000000000001	1.49	1.4950000000000001	1.5	1.5049999999999999	1.51	1.52	1.5249999999999999	1.53	1.5349999999999999	1.54	1.5449999999999999	1.55	1.5549999999999999	1.56	1.5649999999999999	1.57	1.575	1.585	1.59	1.595	1.6	1.605	1.61	1.615	1.62	1.625	1.63	1.635	1.64	1.645	1.65	1.655	1.66	1.665	1.675	1.68	1.6850000000000001	1.69	1.6950000000000001	1.7	1.7050000000000001	1.71	1.7150000000000001	1.72	1.7250000000000001	1.73	1.7350000000000001	1.74	1.7450000000000001	1.75	1.7549999999999999	1.76	1.7649999999999999	1.77	1.7749999999999999	1.78	1.7849999999999999	1.79	1.7949999999999999	1.8	1.8049999999999999	1.81	1.8149999999999999	1.82	1.825	1.83	1.835	1.84	1.845	1.85	1.855	1.86	1.865	1.87	1.875	1.88	1.885	1.89	1.895	1.9	1.905	1.91	1.915	1.92	1.925	1.93	1.9350000000000001	1.94	1.9450000000000001	1.95	1.9550000000000001	1.96	1.9650000000000001	1.97	1.9750000000000001	1.98	1.9850000000000001	1.99	1.9950000000000001	2	2.0049999999999999	2.0099999999999998	2.0150000000000001	2.02	2.0249999999999999	2.0299999999999998	2.0350000000000001	2.04	2.0449999999999999	2.0499999999999998	2.0550000000000002	2.06	2.0649999999999999	2.0699999999999998	2.0750000000000002	2.08	2.085	2.09	2.0950000000000002	2.1	2.105	2.11	2.1150000000000002	2.12	2.12	2.125	2.13	2.1349999999999998	2.14	2.145	2.15	2.1549999999999998	2.16	2.165	2.17	2.1749999999999998	2.1800000000000002	2.1850000000000001	2.19	2.1949999999999998	2.2000000000000002	2.2050000000000001	2.21	2.2149999999999999	2.2200000000000002	2.2250000000000001	2.23	2.2349999999999999	2.2400000000000002	2.2450000000000001	2.25	2.25	2.2549999999999999	2.2599999999999998	2.2650000000000001	2.27	2.2749999999999999	2.2799999999999998	2.2850000000000001	2.29	2.2949999999999999	2.2999999999999998	2.2999999999999998	2.3050000000000002	2.31	2.3149999999999999	2.3199999999999998	2.3250000000000002	2.33	2.335	2.34	2.3450000000000002	2.3450000000000002	2.35	2.355	2.36	2.3650000000000002	2.37	2.375	2.38	2.3849999999999998	2.39	2.39	2.395	2.4	2.4049999999999998	2.41	2.415	2.42	2.4249999999999998	2.4300000000000002	2.4300000000000002	2.4350000000000001	2.44	2.4449999999999998	2.4500000000000002	2.4550000000000001	2.46	2.4649999999999999	2.4649999999999999	2.4700000000000002	2.4750000000000001	2.48	2.48	2.4849999999999999	2.4900000000000002	2.4950000000000001	2.5	2.5049999999999999	2.5049999999999999	2.5099999999999998	2.5150000000000001	2.52	2.5249999999999999	2.5299999999999998	2.5350000000000001	2.5350000000000001	2.54	2.5449999999999999	2.5499999999999998	2.5550000000000002	2.5550000000000002	2.56	2.5649999999999999	2.57	2.5750000000000002	2.5750000000000002	2.58	2.585	2.59	2.59	2.5950000000000002	2.6	2.605	2.61	2.61	2.6150000000000002	2.62	2.625	2.63	2.63	2.6349999999999998	2.64	2.645	2.645	2.65	2.6549999999999998	2.66	2.665	2.665	2.67	2.67	2.6749999999999998	2.68	2.6850000000000001	2.6850000000000001	2.69	2.6949999999999998	2.7	2.7050000000000001	2.7050000000000001	2.71	2.7149999999999999	2.7149999999999999	2.72	2.7250000000000001	2.73	2.73	2.7349999999999999	2.7349999999999999	2.74	2.7450000000000001	2.75	2.75	2.7549999999999999	2.76	2.76	2.7650000000000001	2.77	2.7749999999999999	2.7749999999999999	2.78	2.78	2.7850000000000001	2.79	2.79	2.7949999999999999	2.8	2.8	2.8050000000000002	2.81	2.81	2.8149999999999999	2.82	2.82	2.8250000000000002	2.8250000000000002	2.83	2.835	2.835	2.84	2.8450000000000002	2.8450000000000002	2.85	2.855	2.855	2.86	2.86	2.8650000000000002	2.8650000000000002	2.87	2.875	2.875	2.88	2.88	2.8849999999999998	2.89	2.89	2.895	2.895	2.9	2.9	2.9049999999999998	2.91	2.91	2.915	2.915	2.92	2.92	2.9249999999999998	2.9249999999999998	2.93	2.9350000000000001	2.9350000000000001	2.94	2.94	2.9449999999999998	2.9449999999999998	2.95	2.95	2.9550000000000001	2.9550000000000001	2.96	2.96	2.9649999999999999	2.9649999999999999	2.97	2.97	2.9750000000000001	2.9750000000000001	2.98	2.98	2.9849999999999999	2.9849999999999999	2.99	2.99	2.9950000000000001	2.9950000000000001	3	3	3	3.0049999999999999	3.0049999999999999	3.01	3.01	3.0150000000000001	3.0150000000000001	3.02	3.02	3.0249999999999999	3.0249999999999999	3.03	3.03	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.04	3.04	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.05	3.05	3.0550000000000002	3.0550000000000002	3.06	3.06	3.06	3.0649999999999999	3.0649999999999999	3.07	3.07	3.07	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.08	3.08	3.08	3.085	3.085	3.09	3.09	3.09	3.0950000000000002	3.0950000000000002	3.1	3.1	3.1	3.105	3.105	3.105	3.105	3.11	3.11	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.12	3.12	3.12	3.125	3.125	3.125	3.13	3.13	3.13	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.14	3.14	3.14	3.14	3.145	3.145	3.145	3.15	3.15	3.15	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.16	3.16	3.16	3.165	3.165	3.165	3.17	3.17	3.17	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.18	3.18	3.18	3.18	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.19	3.19	3.19	3.19	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.2	3.2	3.2	3.2	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.21	3.21	3.21	3.21	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.22	3.22	3.22	3.22	3.22	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.23	3.23	3.23	3.23	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.24	3.24	3.24	3.24	3.24	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.25	3.25	3.25	3.25	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.26	3.26	3.26	3.26	3.26	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.27	3.27	3.27	3.27	3.27	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.28	3.28	3.28	3.28	3.28	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.47	3.47	3.47	3.47	3.47	3.4649999999999999	3.4649999999999999	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.47	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.4649999999999999	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.46	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.4550000000000001	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.45	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.4449999999999998	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.44	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.4350000000000001	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.43	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.4249999999999998	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.42	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.415	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.41	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4049999999999998	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.4	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.395	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.39	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.3849999999999998	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.38	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.375	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.37	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.3650000000000002	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.36	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.355	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.35	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.3450000000000002	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.34	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.335	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.33	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.3250000000000002	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.32	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.3149999999999999	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.31	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3050000000000002	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.3	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.2949999999999999	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.29	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.2850000000000001	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.28	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.2749999999999999	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.27	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.2650000000000001	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.26	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.2549999999999999	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.25	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.2450000000000001	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.24	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.2349999999999999	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.23	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.2250000000000001	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.22	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.2149999999999999	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.21	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2050000000000001	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.2	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.1949999999999998	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.19	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.1850000000000001	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.18	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.1749999999999998	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.17	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.165	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.16	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.1549999999999998	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.15	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.145	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.14	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.13	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.125	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.12	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.1150000000000002	3.11	3.11	3.11	3.11	3.11	3.11	3.11	3.11	3.11	3.11	3.11	3.11	3.11	3.105	3.105	3.105	3.105	3.105	3.105	3.105	3.105	3.105	3.105	3.105	3.105	3.105	3.1	3.1	3.1	3.1	3.1	3.1	3.1	3.1	3.1	3.1	3.1	3.1	3.1	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.0950000000000002	3.09	3.09	3.09	3.09	3.09	3.09	3.09	3.09	3.09	3.09	3.09	3.09	3.085	3.085	3.085	3.085	3.085	3.085	3.085	3.085	3.085	3.085	3.085	3.085	3.08	3.08	3.08	3.08	3.08	3.08	3.08	3.08	3.08	3.08	3.08	3.08	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.0750000000000002	3.07	3.07	3.07	3.07	3.07	3.07	3.07	3.07	3.07	3.07	3.07	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.0649999999999999	3.06	3.06	3.06	3.06	3.06	3.06	3.06	3.06	3.06	3.06	3.06	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.0550000000000002	3.05	3.05	3.05	3.05	3.05	3.05	3.05	3.05	3.05	3.05	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.0449999999999999	3.04	3.04	3.04	3.04	3.04	3.04	3.04	3.04	3.04	3.04	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.0350000000000001	3.03	3.03	3.03	3.03	3.03	3.03	3.03	3.03	3.03	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.0249999999999999	3.02	3.02	3.02	3.02	3.02	3.02	3.02	3.02	3.02	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.0150000000000001	3.01	3.01	3.01	3.01	3.01	3.01	3.01	3.01	3.01	3.0049999999999999	3.0049999999999999	3.0049999999999999	3.0049999999999999	3.0049999999999999	3.0049999999999999	3.0049999999999999	3.0049999999999999	3.0049999999999999	3	3	3	3	3	3	3	3	3	2.9950000000000001	2.9950000000000001	2.9950000000000001	2.9950000000000001	2.9950000000000001	2.9950000000000001	2.9950000000000001	2.9950000000000001	2.9950000000000001	2.99	2.99	2.99	2.99	2.99	2.99	2.99	2.99	2.9849999999999999	2.9849999999999999	2.9849999999999999	2.9849999999999999	2.9849999999999999	2.9849999999999999	2.9849999999999999	2.9849999999999999	2.9849999999999999	2.98	2.98	2.98	2.98	2.98	2.98	2.98	2.98	2.9750000000000001	2.9750000000000001	2.9750000000000001	2.9750000000000001	2.9750000000000001	2.9750000000000001	2.9750000000000001	2.9750000000000001	2.9750000000000001	2.97	2.97	2.97	2.97	2.97	2.97	2.97	2.97	2.9649999999999999	2.9649999999999999	2.9649999999999999	2.9649999999999999	2.9649999999999999	2.9649999999999999	2.9649999999999999	2.9649999999999999	2.9649999999999999	2.96	2.96	2.96	2.96	2.96	2.96	2.96	2.96	2.9550000000000001	2.9550000000000001	2.9550000000000001	2.9550000000000001	2.9550000000000001	2.9550000000000001	2.9550000000000001	2.9550000000000001	2.95	2.95	2.95	2.95	2.95	2.95	2.95	2.95	2.9449999999999998	2.9449999999999998	2.9449999999999998	2.9449999999999998	2.9449999999999998	2.9449999999999998	2.9449999999999998	2.9449999999999998	2.94	2.94	2.94	2.94	2.94	2.94	2.94	2.9350000000000001	2.9350000000000001	2.9350000000000001	2.9350000000000001	2.9350000000000001	2.9350000000000001	2.9350000000000001	2.9350000000000001	2.93	2.93	2.93	2.93	2.93	2.93	2.93	2.9249999999999998	2.9249999999999998	2.9249999999999998	2.9249999999999998	2.9249999999999998	2.9249999999999998	2.9249999999999998	2.9249999999999998	2.92	2.92	2.92	2.92	2.92	2.92	2.92	2.915	2.915	2.915	2.915	2.915	2.915	2.915	2.915	2.91	2.91	2.91	2.91	2.91	2.91	2.91	2.9049999999999998	2.9049999999999998	2.9049999999999998	2.9049999999999998	2.9049999999999998	2.9049999999999998	2.9049999999999998	2.9	2.9	2.9	2.9	2.9	2.9	2.9	2.895	2.895	2.895	2.895	2.895	2.895	2.895	2.89	2.89	2.89	2.89	2.89	2.89	2.89	2.8849999999999998	2.8849999999999998	2.8849999999999998	2.8849999999999998	2.8849999999999998	2.8849999999999998	2.8849999999999998	2.88	2.88	2.88	2.88	2.88	2.88	2.875	2.875	2.875	2.875	2.875	2.875	2.875	2.87	2.87	2.87	2.87	2.87	2.87	2.87	2.8650000000000002	2.8650000000000002	2.8650000000000002	2.8650000000000002	2.8650000000000002	2.8650000000000002	2.86	2.86	2.86	2.86	2.86	2.86	2.855	2.855	2.855	2.855	2.855	2.855	2.855	2.85	2.85	2.85	2.85	2.85	2.85	2.8450000000000002	2.8450000000000002	2.8450000000000002	2.8450000000000002	2.8450000000000002	2.8450000000000002	2.84	2.84	2.84	2.84	2.84	2.84	2.835	2.835	2.835	2.835	2.835	2.835	2.83	2.83	2.83	2.83	2.83	2.83	2.8250000000000002	2.8250000000000002	2.8250000000000002	2.8250000000000002	2.8250000000000002	2.8250000000000002	2.82	2.82	2.82	2.82	2.82	2.82	2.8149999999999999	2.8149999999999999	2.8149999999999999	2.8149999999999999	2.8149999999999999	2.8149999999999999	2.81	2.81	2.81	2.81	2.81	2.81	2.8050000000000002	2.8050000000000002	2.8050000000000002	2.8050000000000002	2.8050000000000002	2.8050000000000002	2.8	2.8	2.8	2.8	2.8	2.7949999999999999	2.7949999999999999	2.7949999999999999	2.7949999999999999	2.7949999999999999	2.7949999999999999	2.79	2.79	2.79	2.79	2.79	2.79	2.7850000000000001	2.7850000000000001	2.7850000000000001	2.7850000000000001	2.7850000000000001	2.78	2.78	2.78	2.78	2.78	2.78	2.7749999999999999	2.7749999999999999	2.7749999999999999	2.7749999999999999	2.7749999999999999	2.77	2.77	2.77	2.77	2.77	2.7650000000000001	2.7650000000000001	2.7650000000000001	2.7650000000000001	2.7650000000000001	2.7650000000000001	2.76	2.76	2.76	2.76	2.76	2.7549999999999999	2.7549999999999999	2.7549999999999999	2.7549999999999999	2.7549999999999999	2.75	2.75	2.75	2.75	2.75	2.7450000000000001	2.7450000000000001	2.7450000000000001	2.7450000000000001	2.7450000000000001	2.74	2.74	2.74	2.74	2.74	2.7349999999999999	2.7349999999999999	2.7349999999999999	2.7349999999999999	2.7349999999999999	2.73	2.73	2.73	2.73	2.73	2.7250000000000001	2.7250000000000001	2.7250000000000001	2.7250000000000001	2.7250000000000001	2.72	2.72	2.72	2.72	2.72	2.7149999999999999	2.7149999999999999	2.7149999999999999	2.7149999999999999	2.7149999999999999	2.71	2.71	2.71	2.71	2.71	2.7050000000000001	2.7050000000000001	2.7050000000000001	2.7050000000000001	2.7050000000000001	2.7	2.7	2.7	2.7	2.6949999999999998	2.6949999999999998	2.6949999999999998	2.6949999999999998	2.6949999999999998	2.69	2.69	2.69	2.69	2.69	2.6850000000000001	2.6850000000000001	2.6850000000000001	2.6850000000000001	2.6850000000000001	2.68	2.68	2.68	2.68	2.6749999999999998	2.6749999999999998	2.6749999999999998	2.6749999999999998	2.6749999999999998	2.67	2.67	2.67	2.67	2.665	2.665	2.665	2.665	2.665	2.66	2.66	2.66	2.66	2.6549999999999998	2.6549999999999998	2.6549999999999998	2.6549999999999998	2.65	2.65	2.65	2.65	2.65	2.645	2.645	2.645	2.645	2.64	2.64	2.64	2.64	2.6349999999999998	2.6349999999999998	2.6349999999999998	2.6349999999999998	2.6349999999999998	2.63	2.63	2.63	2.63	2.625	2.625	2.625	2.625	2.62	2.62	2.62	2.62	2.6150000000000002	2.6150000000000002	2.6150000000000002	2.6150000000000002	2.61	2.61	2.61	2.61	2.61	2.605	2.605	2.605	2.605	2.6	2.6	2.6	2.6	2.5950000000000002	2.5950000000000002	2.5950000000000002	2.5950000000000002	2.59	2.59	2.59	2.59	2.585	2.585	2.585	2.585	2.58	2.58	2.58	2.5750000000000002	2.5750000000000002	2.5750000000000002	2.5750000000000002	2.57	2.57	2.57	2.57	2.5649999999999999	2.5649999999999999	2.5649999999999999	2.5649999999999999	2.56	2.56	2.56	2.56	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.54	2.54	2.54	2.54	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.52	2.52	2.52	2.52	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5	2.5	2.5	2.5	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.48	2.48	2.48	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.46	2.46	2.46	2.46	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.44	2.44	2.44	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.42	2.42	2.42	2.415	2.415	2.415	2.41	2.41	2.41	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4	2.4	2.4	2.395	2.395	2.395	2.39	2.39	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.38	2.38	2.38	2.375	2.375	2.375	2.37	2.37	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.36	2.36	2.355	2.355	2.355	2.35	2.35	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.34	2.34	2.335	2.335	2.33	2.33	2.33	2.3250000000000002	2.3250000000000002	2.3199999999999998	2.3199999999999998	2.3149999999999999	2.3149999999999999	2.31	2.31	2.31	2.3050000000000002	2.3050000000000002	2.2999999999999998	2.2999999999999998	2.2949999999999999	2.2949999999999999	2.29	2.29	2.2850000000000001	2.2850000000000001	2.2799999999999998	2.2799999999999998	2.2749999999999999	2.2749999999999999	2.27	2.27	2.2650000000000001	2.2650000000000001	2.2599999999999998	2.2599999999999998	2.2549999999999999	2.2549999999999999	2.25	2.25	2.2450000000000001	2.2450000000000001	2.2400000000000002	2.2400000000000002	2.2349999999999999	2.2349999999999999	2.23	2.23	2.2250000000000001	2.2200000000000002	2.2200000000000002	2.2149999999999999	2.2149999999999999	2.21	2.2050000000000001	2.2050000000000001	2.2000000000000002	2.2000000000000002	2.1949999999999998	2.19	2.19	2.1850000000000001	2.1850000000000001	2.1800000000000002	2.1749999999999998	2.1749999999999998	2.17	2.165	2.165	2.16	2.16	2.1549999999999998	2.15	2.15	2.145	2.145	2.14	2.1349999999999998	2.13	2.13	2.125	2.125	2.12	2.1150000000000002	2.1150000000000002	2.11	2.105	2.1	2.1	2.0950000000000002	2.09	2.09	2.085	2.08	2.08	2.0750000000000002	2.0699999999999998	2.0649999999999999	2.0649999999999999	2.06	2.0550000000000002	2.0550000000000002	2.0499999999999998	2.0449999999999999	2.04	2.0350000000000001	2.0350000000000001	2.0299999999999998	2.0249999999999999	2.02	2.0150000000000001	2.0150000000000001	2.0099999999999998	2.0049999999999999	2	1.9950000000000001	1.9950000000000001	1.99	1.9850000000000001	1.98	1.9750000000000001	1.97	1.9650000000000001	1.96	1.96	1.9550000000000001	1.9450000000000001	1.9450000000000001	1.94	1.9350000000000001	1.93	1.925	1.92	1.915	1.91	1.905	1.9	1.895	1.89	1.88	1.875	1.87	1.865	1.86	1.855	1.85	1.84	1.835	1.83	1.82	1.8149999999999999	1.81	1.8	1.7949999999999999	1.7849999999999999	1.78	1.77	1.76	1.75	1.74	1.73	1.72	1.7050000000000001	1.6950000000000001	1.68	1.67	1.66	1.645	1.635	1.615	1.6	1.59	1.57	1.5549999999999999	1.54	1.52	1.5049999999999999	1.49	1.47	1.4550000000000001	1.44	1.425	1.405	1.39	1.37	1.355	1.335	1.32	1.3049999999999999	1.29	1.2749999999999999	1.2649999999999999	1.25	1.24	1.23	1.22	1.21	1.1950000000000001	1.1850000000000001	1.18	1.17	1.165	1.155	1.1499999999999999	1.145	1.135	1.1299999999999999	1.125	1.115	1.1100000000000001	1.105	1.1000000000000001	1.095	1.085	1.08	1.075	1.07	1.0649999999999999	1.06	1.05	1.0449999999999999	1.04	1.0349999999999999	1.0249999999999999	1.02	1.0149999999999999	1.01	1.0049999999999999	0.995	0.99	0.98499999999999999	0.97499999999999998	0.97	0.96499999999999997	0.96	0.95499999999999996	0.95	0.94499999999999995	0.94	0.93	0.92500000000000004	0.91500000000000004	0.91	0.90500000000000003	0.89500000000000002	0.88500000000000001	0.88	0.87	0.86	0.85499999999999998	0.84499999999999997	0.83499999999999996	0.83	0.82	0.80500000000000005	0.79500000000000004	0.78500000000000003	0.77500000000000002	0.76500000000000001	0.75	0.74	0.73	0.72	0.72	0.71	0.7	0.69	0.68500000000000005	0.67500000000000004	0.67	0.66	0.65500000000000003	0.64500000000000002	0.63500000000000001	0.63	0.625	0.61499999999999999	0.60499999999999998	0.6	0.59499999999999997	0.58499999999999996	0.57499999999999996	0.56999999999999995	0.56000000000000005	0.55500000000000005	0.54500000000000004	0.53500000000000003	0.53	0.52	0.51	0.5	0.49	0.48	0.47	0.46	0.45	0.435	0.42	0.41	0.39500000000000002	0.38	0.36	0.34499999999999997	0.315	0.29499999999999998	0.27500000000000002	0.25	0.23	0.21	0.19	0.17499999999999999	0.155	0.14000000000000001	0.115	0.105	9.5000000000000001E-2	8.5000000000000006E-2	0.08	7.4999999999999997E-2	6.5000000000000002E-2	0.06	5.5E-2	0.05	0.04	3.5000000000000003E-2	2.5000000000000001E-2	0.01	-0.01	-2.5000000000000001E-2	-0.04	-5.5E-2	-6.5000000000000002E-2	-0.08	-0.09	-0.1	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	-0.11	Time (s)


Load (kN)



Carbon Non Woven (Bio Resin) - Time vs Load
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Load (N)



Carbon Woven (Bio Resin) - Time vs Load
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Load (N)



Carbon Woven (Epoxy Resin) - Time vs Load
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Flax Non Woven (Bio Resin) - Time vs Load
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Load (N)



Flax Woven (Bio Resin) - Time vs Load

0	0	0.02	0.04	0.06	0.08	0.1	0.12	0.14000000000000001	0.16	0.18	0.20100000000000001	0.221	0.24	0.26	0.28000000000000003	0.3	0.32	0.34100000000000003	0.36	0.38	0.40100000000000002	0.42	0.44	0.46100000000000002	0.48099999999999998	0.5	0.52	0.54	0.56000000000000005	0.57999999999999996	0.6	0.62	0.64	0.66	0.68	0.7	0.72	0.74	0.76	0.78	0.8	0.82	0.84	0.86	0.88	0.9	0.92	0.94	0.96	0.98	1	1.02	1.0389999999999999	1.06	1.08	1.099	1.119	1.139	1.159	1.18	1.2	1.22	1.2390000000000001	1.2589999999999999	1.2789999999999999	1.2989999999999999	1.319	1.339	1.359	1.379	1.399	1.419	1.4390000000000001	1.46	1.48	1.5	1.52	1.5389999999999999	1.5589999999999999	1.5780000000000001	1.599	1.619	1.639	1.659	1.679	1.6990000000000001	1.7190000000000001	1.7390000000000001	1.7589999999999999	1.7789999999999999	1.7989999999999999	1.819	1.8380000000000001	1.859	1.879	1.899	1.919	1.9390000000000001	1.9590000000000001	1.9790000000000001	1.9990000000000001	2.0179999999999998	2.0379999999999998	2.0579999999999998	2.0779999999999998	2.0979999999999999	2.1179999999999999	2.1379999999999999	2.1589999999999998	2.1779999999999999	2.198	2.218	2.2389999999999999	2.2589999999999999	2.2789999999999999	2.2989999999999999	2.319	2.3380000000000001	2.3580000000000001	2.3780000000000001	2.399	2.4180000000000001	2.4380000000000002	2.4590000000000001	2.4790000000000001	2.4980000000000002	2.5190000000000001	2.5390000000000001	2.5579999999999998	2.5779999999999998	2.597	2.6179999999999999	2.6389999999999998	2.6579999999999999	2.6779999999999999	2.698	2.718	2.738	2.758	2.778	2.798	2.8180000000000001	2.8370000000000002	2.8580000000000001	2.8780000000000001	2.8980000000000001	2.9180000000000001	2.9380000000000002	2.9580000000000002	2.9780000000000002	2.9980000000000002	3.0179999999999998	3.0379999999999998	3.0579999999999998	3.077	3.097	3.117	3.137	3.157	3.177	3.1970000000000001	3.218	3.238	3.258	3.278	3.2970000000000002	3.3170000000000002	3.3380000000000001	3.3570000000000002	3.3769999999999998	3.3969999999999998	3.4169999999999998	3.4369999999999998	3.4580000000000002	3.4780000000000002	3.4969999999999999	3.5169999999999999	3.5379999999999998	3.5569999999999999	3.577	3.597	3.617	3.637	3.657	3.677	3.6970000000000001	3.7170000000000001	3.7370000000000001	3.7570000000000001	3.7770000000000001	3.7970000000000002	3.8170000000000002	3.8370000000000002	3.8570000000000002	3.8769999999999998	3.8969999999999998	3.9159999999999999	3.9369999999999998	3.9569999999999999	3.9769999999999999	3.9969999999999999	4.0170000000000003	4.0359999999999996	4.0570000000000004	4.077	4.0960000000000001	4.117	4.1369999999999996	4.1559999999999997	4.1769999999999996	4.1970000000000001	4.2169999999999996	4.2359999999999998	4.2560000000000002	4.2759999999999998	4.2969999999999997	4.3170000000000002	4.3369999999999997	4.3559999999999999	4.3769999999999998	4.3959999999999999	4.4169999999999998	4.4370000000000003	4.4560000000000004	4.476	4.4960000000000004	4.516	4.5359999999999996	4.5570000000000004	4.577	4.5960000000000001	4.6159999999999997	4.6360000000000001	4.6559999999999997	4.6760000000000002	4.6959999999999997	4.7160000000000002	4.7350000000000003	4.7569999999999997	4.7759999999999998	4.7960000000000003	4.8159999999999998	4.8360000000000003	4.8559999999999999	4.875	4.8959999999999999	4.9160000000000004	4.9349999999999996	4.9550000000000001	4.9749999999999996	4.9960000000000004	5.016	5.0359999999999996	5.056	5.0759999999999996	5.0949999999999998	5.1159999999999997	5.1349999999999998	5.1550000000000002	5.1749999999999998	5.1950000000000003	5.2149999999999999	5.2350000000000003	5.2560000000000002	5.2750000000000004	5.2960000000000003	5.3159999999999998	5.3360000000000003	5.3559999999999999	5.375	5.3959999999999999	5.415	5.4349999999999996	5.4560000000000004	5.476	5.4960000000000004	5.5149999999999997	5.5350000000000001	5.5549999999999997	5.5750000000000002	5.5949999999999998	5.6159999999999997	5.6349999999999998	5.6550000000000002	5.6749999999999998	5.6959999999999997	5.7149999999999999	5.7359999999999998	5.7549999999999999	5.7750000000000004	5.7949999999999999	5.8150000000000004	5.835	5.8550000000000004	5.875	5.8949999999999996	5.915	5.9349999999999996	5.9550000000000001	5.9749999999999996	5.9950000000000001	6.0149999999999997	6.0350000000000001	6.0549999999999997	6.0750000000000002	6.0949999999999998	6.1150000000000002	6.1349999999999998	6.1550000000000002	6.1749999999999998	6.1950000000000003	6.2149999999999999	6.234	6.2539999999999996	6.274	6.2949999999999999	6.3150000000000004	6.335	6.3550000000000004	6.3739999999999997	6.3940000000000001	6.4139999999999997	6.4340000000000002	6.4539999999999997	6.4749999999999996	6.4939999999999998	6.5149999999999997	6.5350000000000001	6.5549999999999997	6.5750000000000002	6.5940000000000003	6.6139999999999999	6.6349999999999998	6.6550000000000002	6.6740000000000004	6.694	6.7140000000000004	6.7350000000000003	6.7539999999999996	6.774	6.7939999999999996	6.8140000000000001	6.8339999999999996	6.8540000000000001	6.8739999999999997	6.8940000000000001	6.9130000000000003	6.9340000000000002	6.9530000000000003	6.9740000000000002	6.9939999999999998	7.0140000000000002	7.0339999999999998	7.0540000000000003	7.0739999999999998	7.0940000000000003	7.1139999999999999	7.1340000000000003	7.1539999999999999	7.1740000000000004	7.194	7.2140000000000004	7.234	7.2530000000000001	7.2729999999999997	7.2930000000000001	7.3140000000000001	7.3330000000000002	7.3529999999999998	7.3739999999999997	7.3940000000000001	7.4130000000000003	7.4329999999999998	7.4530000000000003	7.4729999999999999	7.4930000000000003	7.5129999999999999	7.5330000000000004	7.5529999999999999	7.5730000000000004	7.593	7.6130000000000004	7.633	7.6529999999999996	7.6740000000000004	7.6929999999999996	7.7130000000000001	7.7329999999999997	7.7530000000000001	7.7729999999999997	7.7930000000000001	7.8129999999999997	7.8330000000000002	7.8529999999999998	7.8730000000000002	7.8929999999999998	7.9130000000000003	7.9329999999999998	7.9530000000000003	7.9729999999999999	7.9930000000000003	8.0129999999999999	8.0329999999999995	8.0530000000000008	8.0730000000000004	8.093	8.1129999999999995	8.1329999999999991	8.1519999999999992	8.173	8.1929999999999996	8.2129999999999992	8.2319999999999993	8.2530000000000001	8.2729999999999997	8.2929999999999993	8.3119999999999994	8.3320000000000007	8.3520000000000003	8.3719999999999999	8.3930000000000007	8.4120000000000008	8.4329999999999998	8.452	8.4719999999999995	8.4920000000000009	8.5120000000000005	8.532	8.5519999999999996	8.5719999999999992	8.5920000000000005	8.6120000000000001	8.6319999999999997	8.6530000000000005	8.6720000000000006	8.6920000000000002	8.7129999999999992	8.7319999999999993	8.7520000000000007	8.7720000000000002	8.7919999999999998	8.8119999999999994	8.8320000000000007	8.8520000000000003	8.8729999999999993	8.8919999999999995	8.9120000000000008	8.9320000000000004	8.952	8.9719999999999995	8.9920000000000009	9.0120000000000005	9.032	9.0519999999999996	9.0719999999999992	9.0920000000000005	9.1120000000000001	9.1310000000000002	9.1519999999999992	9.1709999999999994	9.1910000000000007	9.2119999999999997	9.2309999999999999	9.2520000000000007	9.2720000000000002	9.2919999999999998	9.3109999999999999	9.3320000000000007	9.3520000000000003	9.3719999999999999	9.3919999999999995	9.4120000000000008	9.4320000000000004	9.452	9.4710000000000001	9.4920000000000009	9.5120000000000005	9.5310000000000006	9.5519999999999996	9.5709999999999997	9.5909999999999993	9.6110000000000007	9.6319999999999997	9.6509999999999998	9.6709999999999994	9.6920000000000002	9.7110000000000003	9.7309999999999999	9.7509999999999994	9.7710000000000008	9.7910000000000004	9.8109999999999999	9.8309999999999995	9.8510000000000009	9.8710000000000004	9.891	9.9109999999999996	9.9309999999999992	9.952	9.9710000000000001	9.99	10.010999999999999	10.031000000000001	10.051	10.071	10.090999999999999	10.11	10.131	10.151	10.17	10.19	10.211	10.231	10.25	10.271000000000001	10.291	10.311	10.331	10.351000000000001	10.37	10.39	10.411	10.43	10.451000000000001	10.471	10.49	10.51	10.531000000000001	10.55	10.571	10.590999999999999	10.611000000000001	10.631	10.65	10.67	10.69	10.71	10.731	10.75	10.77	10.79	10.81	10.83	10.85	10.87	10.89	10.91	10.93	10.95	10.97	10.99	11.01	11.029	11.05	11.07	11.09	11.11	11.13	11.15	11.17	11.19	11.209	11.23	11.25	11.269	11.29	11.31	11.33	11.35	11.369	11.39	11.41	11.43	11.45	11.47	11.49	11.51	11.529	11.548999999999999	11.569000000000001	11.589	11.61	11.63	11.648999999999999	11.669	11.689	11.71	11.73	11.749000000000001	11.77	11.789	11.808999999999999	11.829000000000001	11.849	11.87	11.888999999999999	11.909000000000001	11.929	11.95	11.968999999999999	11.989000000000001	12.009	12.029	12.048	12.069000000000001	12.087999999999999	12.108000000000001	12.128	12.148	12.169	12.189	12.209	12.228999999999999	12.249000000000001	12.269	12.288	12.308	12.327999999999999	12.349	12.369	12.388999999999999	12.409000000000001	12.428000000000001	12.448	12.468	12.489000000000001	12.509	12.529	12.548	12.568	12.587999999999999	12.609	12.628	12.648	12.669	12.689	12.709	12.728	12.747999999999999	12.768000000000001	12.789	12.808	12.827999999999999	12.848000000000001	12.868	12.888	12.907999999999999	12.928000000000001	12.949	12.968	12.988	13.007999999999999	13.029	13.048	13.068	13.087999999999999	13.108000000000001	13.128	13.148	13.167999999999999	13.188000000000001	13.208	13.228	13.247999999999999	13.266999999999999	13.288	13.308	13.327	13.347	13.367000000000001	13.387	13.407999999999999	13.428000000000001	13.448	13.468	13.488	13.507999999999999	13.526999999999999	13.547000000000001	13.567	13.587	13.608000000000001	13.627000000000001	13.647	13.667	13.686999999999999	13.707000000000001	13.728	13.747	13.766999999999999	13.787000000000001	13.807	13.827	13.847	13.867000000000001	13.887	13.907	13.927	13.946999999999999	13.967000000000001	13.987	14.007	14.026999999999999	14.047000000000001	14.067	14.087	14.106999999999999	14.127000000000001	14.147	14.167	14.186999999999999	14.207000000000001	14.227	14.247	14.266999999999999	14.287000000000001	14.307	14.327	14.346	14.367000000000001	14.385999999999999	14.406000000000001	14.427	14.446999999999999	14.467000000000001	14.486000000000001	14.506	14.526	14.547000000000001	14.567	14.587	14.606999999999999	14.625999999999999	14.646000000000001	14.666	14.686	14.706	14.726000000000001	14.746	14.766	14.787000000000001	14.805999999999999	14.826000000000001	14.847	14.866	14.885999999999999	14.906000000000001	14.926	14.946	14.965999999999999	14.986000000000001	15.006	15.026	15.045999999999999	15.066000000000001	15.086	15.106	15.125999999999999	15.146000000000001	15.166	15.186	15.206	15.225	15.246	15.266	15.285	15.305	15.326000000000001	15.346	15.366	15.385999999999999	15.406000000000001	15.426	15.445	15.465	15.484999999999999	15.506	15.526	15.545999999999999	15.565	15.586	15.605	15.625	15.646000000000001	15.666	15.686	15.706	15.725	15.744999999999999	15.766	15.786	15.805	15.824999999999999	15.845000000000001	15.865	15.885	15.904999999999999	15.925000000000001	15.946	15.965	15.984999999999999	16.004999999999999	16.024999999999999	16.045000000000002	16.065000000000001	16.085000000000001	16.105	16.125	16.145	16.164999999999999	16.184999999999999	16.204999999999998	16.225000000000001	16.245000000000001	16.263999999999999	16.285	16.305	16.324999999999999	16.344999999999999	16.364999999999998	16.385000000000002	16.405000000000001	16.425000000000001	16.445	16.463999999999999	16.484999999999999	16.504999999999999	16.524000000000001	16.544	16.564	16.585000000000001	16.605	16.625	16.645	16.664000000000001	16.684000000000001	16.704000000000001	16.724	16.745000000000001	16.763999999999999	16.785	16.803999999999998	16.824999999999999	16.844000000000001	16.864000000000001	16.884	16.904	16.923999999999999	16.943999999999999	16.963999999999999	16.984000000000002	17.004000000000001	17.024000000000001	17.044	17.064	17.084	17.103999999999999	17.123999999999999	17.143999999999998	17.164000000000001	17.184000000000001	17.204000000000001	17.224	17.242999999999999	17.263999999999999	17.283000000000001	17.303999999999998	17.324000000000002	17.344000000000001	17.364000000000001	17.384	17.404	17.422999999999998	17.443999999999999	17.463999999999999	17.483000000000001	17.504000000000001	17.524000000000001	17.544	17.562999999999999	17.582999999999998	17.603000000000002	17.623000000000001	17.643000000000001	17.663	17.683	17.702999999999999	17.724	17.742999999999999	17.763999999999999	17.783000000000001	17.803000000000001	17.823	17.843	17.864000000000001	17.884	17.904	17.923999999999999	17.943999999999999	17.963000000000001	17.983000000000001	18.003	18.023	18.042999999999999	18.064	18.082999999999998	18.103000000000002	18.123000000000001	18.143000000000001	18.163	18.181999999999999	18.202999999999999	18.222000000000001	18.242999999999999	18.263000000000002	18.283000000000001	18.303000000000001	18.323	18.343	18.363	18.382999999999999	18.402999999999999	18.422999999999998	18.443000000000001	18.462	18.481999999999999	18.501999999999999	18.523	18.542000000000002	18.562999999999999	18.582999999999998	18.603000000000002	18.622	18.641999999999999	18.661999999999999	18.683	18.702999999999999	18.722999999999999	18.742000000000001	18.762	18.782	18.803000000000001	18.823	18.843	18.863	18.882999999999999	18.902999999999999	18.922000000000001	18.943000000000001	18.962	18.981999999999999	19.001999999999999	19.021999999999998	19.042000000000002	19.062000000000001	19.082000000000001	19.103000000000002	19.122	19.141999999999999	19.161999999999999	19.181999999999999	19.202000000000002	19.222000000000001	19.242000000000001	19.262	19.282	19.302	19.321999999999999	19.341999999999999	19.361999999999998	19.382000000000001	19.402000000000001	19.422000000000001	19.442	19.462	19.481000000000002	19.501000000000001	19.521999999999998	19.542000000000002	19.562000000000001	19.582000000000001	19.602	19.620999999999999	19.641999999999999	19.661999999999999	19.681999999999999	19.702000000000002	19.721	19.742000000000001	19.760999999999999	19.780999999999999	19.800999999999998	19.821000000000002	19.841000000000001	19.861000000000001	19.881	19.901	19.920999999999999	19.942	19.962	19.981000000000002	20.001000000000001	20.021000000000001	20.041	20.061	20.081	20.100999999999999	20.120999999999999	20.140999999999998	20.161000000000001	20.181000000000001	20.201000000000001	20.221	20.241	20.260999999999999	20.28	20.3	20.32	20.341000000000001	20.36	20.381	20.401	20.420999999999999	20.440999999999999	20.460999999999999	20.481000000000002	20.501000000000001	20.52	20.54	20.561	20.58	20.6	20.620999999999999	20.64	20.661000000000001	20.681000000000001	20.701000000000001	20.721	20.74	20.76	20.78	20.8	20.821000000000002	20.841000000000001	20.861000000000001	20.881	20.9	20.920999999999999	20.940999999999999	20.960999999999999	20.981000000000002	21	21.02	21.04	21.06	21.08	21.100999999999999	21.12	21.140999999999998	21.16	21.181000000000001	21.2	21.22	21.24	21.26	21.28	21.3	21.32	21.34	21.36	21.38	21.4	21.419	21.44	21.46	21.48	21.5	21.52	21.54	21.56	21.579000000000001	21.599	21.62	21.638999999999999	21.66	21.68	21.7	21.72	21.74	21.76	21.78	21.8	21.818999999999999	21.84	21.859000000000002	21.879000000000001	21.9	21.919	21.939	21.96	21.98	21.998999999999999	22.018999999999998	22.039000000000001	22.059000000000001	22.079000000000001	22.099	22.119	22.138999999999999	22.158999999999999	22.178999999999998	22.199000000000002	22.219000000000001	22.239000000000001	22.259	22.279	22.298999999999999	22.318999999999999	22.338999999999999	22.359000000000002	22.379000000000001	22.398	22.419	22.439	22.459	22.478999999999999	22.498999999999999	22.518999999999998	22.538	22.558	22.579000000000001	22.597999999999999	22.619	22.638000000000002	22.658000000000001	22.678999999999998	22.698	22.719000000000001	22.739000000000001	22.759	22.779	22.797999999999998	22.818000000000001	22.838000000000001	22.858000000000001	22.878	22.898	22.919	22.937999999999999	22.957999999999998	22.978999999999999	22.998999999999999	23.018999999999998	23.039000000000001	23.058	23.077999999999999	23.097999999999999	23.117999999999999	23.138000000000002	23.158000000000001	23.178000000000001	23.198	23.218	23.238	23.257999999999999	23.277999999999999	23.297999999999998	23.317	23.337	23.358000000000001	23.378	23.396999999999998	23.417999999999999	23.437999999999999	23.457999999999998	23.478000000000002	23.498000000000001	23.516999999999999	23.538	23.558	23.577999999999999	23.597999999999999	23.617999999999999	23.637	23.657	23.677	23.696999999999999	23.716999999999999	23.738	23.757999999999999	23.777999999999999	23.797999999999998	23.818000000000001	23.838000000000001	23.858000000000001	23.876999999999999	23.898	23.917999999999999	23.937000000000001	23.957000000000001	23.977	23.997	24.016999999999999	24.036999999999999	24.056999999999999	24.077000000000002	24.097000000000001	24.117000000000001	24.137	24.157	24.177	24.196999999999999	24.216999999999999	24.236999999999998	24.257000000000001	24.277000000000001	24.297000000000001	24.317	24.337	24.356999999999999	24.376999999999999	24.396999999999998	24.417000000000002	24.437000000000001	24.457000000000001	24.477	24.497	24.516999999999999	24.536999999999999	24.556999999999999	24.577000000000002	24.597000000000001	24.617000000000001	24.635999999999999	24.655999999999999	24.677	24.696000000000002	24.716999999999999	24.736999999999998	24.757000000000001	24.777000000000001	24.797000000000001	24.817	24.837	24.856999999999999	24.876999999999999	24.896000000000001	24.916	24.937000000000001	24.956	24.975999999999999	24.995999999999999	25.015999999999998	25.036000000000001	25.056000000000001	25.076000000000001	25.096	25.116	25.135999999999999	25.155999999999999	25.177	25.196000000000002	25.216999999999999	25.236000000000001	25.256	25.276	25.295999999999999	25.315999999999999	25.335999999999999	25.356000000000002	25.376000000000001	25.396000000000001	25.416	25.436	25.456	25.475999999999999	25.495999999999999	25.515999999999998	25.536000000000001	25.556000000000001	25.576000000000001	25.596	25.614999999999998	25.635000000000002	25.655000000000001	25.675999999999998	25.695	25.716000000000001	25.736000000000001	25.756	25.774999999999999	25.795000000000002	25.815999999999999	25.835999999999999	25.855	25.875	25.895	25.914999999999999	25.934999999999999	25.956	25.975000000000001	25.995000000000001	26.015999999999998	26.035	26.056000000000001	26.074999999999999	26.094999999999999	26.114999999999998	26.135999999999999	26.155000000000001	26.175000000000001	26.196000000000002	26.215	26.234999999999999	26.256	26.274999999999999	26.295999999999999	26.315999999999999	26.335000000000001	26.356000000000002	26.375	26.393999999999998	26.414999999999999	26.434999999999999	26.454000000000001	26.474	26.495000000000001	26.515000000000001	26.533999999999999	26.555	26.574999999999999	26.594999999999999	26.614999999999998	26.635000000000002	26.655000000000001	26.675000000000001	26.693999999999999	26.713999999999999	26.734999999999999	26.754999999999999	26.774000000000001	26.795000000000002	26.815000000000001	26.835000000000001	26.853999999999999	26.873999999999999	26.895	26.914999999999999	26.934999999999999	26.954999999999998	26.974	26.994	27.013999999999999	27.035	27.053999999999998	27.074999999999999	27.094999999999999	27.114999999999998	27.135000000000002	27.155000000000001	27.173999999999999	27.195	27.213999999999999	27.234000000000002	27.254000000000001	27.274000000000001	27.294	27.314	27.335000000000001	27.353999999999999	27.375	27.393999999999998	27.414000000000001	27.434000000000001	27.454000000000001	27.474	27.494	27.513000000000002	27.533999999999999	27.553999999999998	27.574000000000002	27.594000000000001	27.614000000000001	27.634	27.654	27.673999999999999	27.693999999999999	27.713999999999999	27.734000000000002	27.754000000000001	27.774000000000001	27.794	27.814	27.832999999999998	27.853999999999999	27.873999999999999	27.893000000000001	27.914000000000001	27.933	27.952999999999999	27.974	27.992999999999999	28.013000000000002	28.033999999999999	28.053999999999998	28.074000000000002	28.094000000000001	28.114000000000001	28.132999999999999	28.152999999999999	28.172999999999998	28.193000000000001	28.213999999999999	28.233000000000001	28.254000000000001	28.273	28.292999999999999	28.312999999999999	28.332999999999998	28.353000000000002	28.373999999999999	28.393000000000001	28.413	28.433	28.452999999999999	28.472999999999999	28.492999999999999	28.513000000000002	28.533000000000001	28.552	28.573	28.593	28.613	28.632999999999999	28.652999999999999	28.672000000000001	28.693000000000001	28.713000000000001	28.733000000000001	28.751999999999999	28.773	28.792000000000002	28.812999999999999	28.832999999999998	28.852	28.873000000000001	28.893000000000001	28.913	28.933	28.952999999999999	28.972000000000001	28.992999999999999	29.013000000000002	29.033000000000001	29.053000000000001	29.073	29.091999999999999	29.111999999999998	29.132000000000001	29.152999999999999	29.172000000000001	29.192	29.212	29.233000000000001	29.251999999999999	29.271999999999998	29.292000000000002	29.312000000000001	29.332000000000001	29.353000000000002	29.373000000000001	29.391999999999999	29.411999999999999	29.431999999999999	29.452000000000002	29.472000000000001	29.492000000000001	29.512	29.532	29.553000000000001	29.571999999999999	29.591999999999999	29.611999999999998	29.632000000000001	29.652000000000001	29.672000000000001	29.692	29.712	29.731999999999999	29.751999999999999	29.771999999999998	29.792000000000002	29.812000000000001	29.832000000000001	29.852	29.870999999999999	29.891999999999999	29.911000000000001	29.931999999999999	29.952000000000002	29.972000000000001	29.991	30.010999999999999	30.030999999999999	30.050999999999998	30.071999999999999	30.091999999999999	30.111000000000001	30.132000000000001	30.151	30.172000000000001	30.190999999999999	30.210999999999999	30.231000000000002	30.251000000000001	30.271999999999998	30.292000000000002	30.311	30.331	30.350999999999999	30.370999999999999	30.390999999999998	30.411999999999999	30.431000000000001	30.451000000000001	30.471	30.491	30.51	30.530999999999999	30.550999999999998	30.571000000000002	30.591000000000001	30.611000000000001	30.631	30.651	30.670999999999999	30.690999999999999	30.710999999999999	30.731000000000002	30.751000000000001	30.771000000000001	30.79	30.81	30.831	30.850999999999999	30.870999999999999	30.89	30.911000000000001	30.931000000000001	30.951000000000001	30.971	30.991	31.010999999999999	31.03	31.05	31.07	31.091000000000001	31.11	31.131	31.15	31.170999999999999	31.19	31.21	31.23	31.25	31.27	31.29	31.31	31.331	31.350999999999999	31.37	31.39	31.41	31.43	31.45	31.47	31.49	31.51	31.53	31.55	31.57	31.59	31.61	31.63	31.65	31.67	31.690999999999999	31.71	31.73	31.75	31.768999999999998	31.789000000000001	31.81	31.83	31.85	31.87	31.888999999999999	31.91	31.93	31.95	31.969000000000001	31.99	32.01	32.029000000000003	32.049999999999997	32.07	32.090000000000003	32.11	32.128999999999998	32.149000000000001	32.168999999999997	32.189	32.21	32.228999999999999	32.249000000000002	32.268999999999998	32.29	32.31	32.329000000000001	32.348999999999997	32.369	32.389000000000003	32.409999999999997	32.429000000000002	32.448999999999998	32.469000000000001	32.488999999999997	32.509	32.529000000000003	32.548999999999999	32.569000000000003	32.588999999999999	32.609000000000002	32.628999999999998	32.649000000000001	32.668999999999997	32.689	32.709000000000003	32.728999999999999	32.749000000000002	32.768000000000001	32.789000000000001	32.808	32.829000000000001	32.848999999999997	32.869	32.887999999999998	32.908000000000001	32.929000000000002	32.948999999999998	32.969000000000001	32.988999999999997	33.009	33.027999999999999	33.048000000000002	33.069000000000003	33.088000000000001	33.107999999999997	33.128999999999998	33.148000000000003	33.167999999999999	33.189	33.207999999999998	33.228000000000002	33.249000000000002	33.268000000000001	33.289000000000001	33.308	33.328000000000003	33.347999999999999	33.369	33.387999999999998	33.408000000000001	33.427999999999997	33.448	33.468000000000004	33.488	33.509	33.527999999999999	33.548000000000002	33.567999999999998	33.588999999999999	33.607999999999997	33.628	33.648000000000003	33.667999999999999	33.688000000000002	33.707999999999998	33.728000000000002	33.747999999999998	33.768000000000001	33.787999999999997	33.808	33.828000000000003	33.847999999999999	33.868000000000002	33.887	33.906999999999996	33.927999999999997	33.948	33.968000000000004	33.987000000000002	34.008000000000003	34.027999999999999	34.048000000000002	34.067	34.088000000000001	34.107999999999997	34.128	34.148000000000003	34.167000000000002	34.186999999999998	34.207000000000001	34.228000000000002	34.247	34.268000000000001	34.286999999999999	34.307000000000002	34.326999999999998	34.347000000000001	34.366999999999997	34.387	34.406999999999996	34.427	34.447000000000003	34.466999999999999	34.487000000000002	34.506999999999998	34.527999999999999	34.548000000000002	34.567	34.587000000000003	34.606999999999999	34.627000000000002	34.646999999999998	34.667000000000002	34.686999999999998	34.707000000000001	34.726999999999997	34.747	34.767000000000003	34.787999999999997	34.807000000000002	34.826000000000001	34.845999999999997	34.866999999999997	34.887	34.905999999999999	34.927	34.947000000000003	34.966999999999999	34.985999999999997	35.006	35.027000000000001	35.046999999999997	35.067	35.085999999999999	35.106999999999999	35.125999999999998	35.146999999999998	35.167000000000002	35.186999999999998	35.206000000000003	35.225999999999999	35.246000000000002	35.267000000000003	35.286999999999999	35.305999999999997	35.326000000000001	35.345999999999997	35.366	35.386000000000003	35.406999999999996	35.426000000000002	35.445999999999998	35.466999999999999	35.485999999999997	35.506	35.526000000000003	35.545999999999999	35.566000000000003	35.585999999999999	35.606000000000002	35.625999999999998	35.646000000000001	35.665999999999997	35.686	35.706000000000003	35.725999999999999	35.746000000000002	35.765999999999998	35.786000000000001	35.805999999999997	35.826000000000001	35.844999999999999	35.865000000000002	35.886000000000003	35.905999999999999	35.924999999999997	35.945	35.966000000000001	35.984999999999999	36.006	36.026000000000003	36.045999999999999	36.066000000000003	36.085000000000001	36.106000000000002	36.125999999999998	36.146000000000001	36.165999999999997	36.186	36.206000000000003	36.225999999999999	36.246000000000002	36.265999999999998	36.286000000000001	36.305	36.325000000000003	36.344999999999999	36.365000000000002	36.384999999999998	36.405000000000001	36.424999999999997	36.445	36.466000000000001	36.484999999999999	36.505000000000003	36.524999999999999	36.545000000000002	36.564999999999998	36.585000000000001	36.606000000000002	36.625999999999998	36.645000000000003	36.664999999999999	36.685000000000002	36.704999999999998	36.725000000000001	36.744999999999997	36.765000000000001	36.784999999999997	36.805	36.825000000000003	36.844999999999999	36.865000000000002	36.884999999999998	36.905000000000001	36.924999999999997	36.945	36.965000000000003	36.984000000000002	37.005000000000003	37.024999999999999	37.045000000000002	37.064999999999998	37.084000000000003	37.104999999999997	37.125	37.143999999999998	37.164999999999999	37.185000000000002	37.204999999999998	37.225000000000001	37.244999999999997	37.264000000000003	37.283999999999999	37.304000000000002	37.325000000000003	37.344000000000001	37.363999999999997	37.384999999999998	37.405000000000001	37.423999999999999	37.444000000000003	37.463999999999999	37.484000000000002	37.503999999999998	37.524000000000001	37.543999999999997	37.564	37.584000000000003	37.604999999999997	37.624000000000002	37.643999999999998	37.664000000000001	37.683999999999997	37.704000000000001	37.723999999999997	37.744	37.764000000000003	37.783999999999999	37.804000000000002	37.823999999999998	37.844000000000001	37.863999999999997	37.884	37.904000000000003	37.923999999999999	37.944000000000003	37.963000000000001	37.984000000000002	38.003999999999998	38.024000000000001	38.043999999999997	38.064	38.084000000000003	38.103999999999999	38.124000000000002	38.143000000000001	38.162999999999997	38.183999999999997	38.203000000000003	38.223999999999997	38.244	38.262999999999998	38.283999999999999	38.304000000000002	38.323999999999998	38.344000000000001	38.363999999999997	38.384	38.402999999999999	38.423000000000002	38.444000000000003	38.463000000000001	38.482999999999997	38.503	38.523000000000003	38.543999999999997	38.563000000000002	38.582999999999998	38.603000000000002	38.622999999999998	38.643000000000001	38.662999999999997	38.683	38.703000000000003	38.722999999999999	38.743000000000002	38.762999999999998	38.783000000000001	38.802999999999997	38.823	38.843000000000004	38.863	38.883000000000003	38.902999999999999	38.923000000000002	38.942999999999998	38.963000000000001	38.982999999999997	39.002000000000002	39.021999999999998	39.042999999999999	39.061999999999998	39.082000000000001	39.103000000000002	39.122999999999998	39.143000000000001	39.162999999999997	39.183	39.203000000000003	39.222000000000001	39.241999999999997	39.262999999999998	39.281999999999996	39.302	39.322000000000003	39.341999999999999	39.362000000000002	39.383000000000003	39.402000000000001	39.421999999999997	39.442	39.462000000000003	39.482999999999997	39.502000000000002	39.523000000000003	39.542000000000002	39.563000000000002	39.582999999999998	39.601999999999997	39.622	39.643000000000001	39.662999999999997	39.682000000000002	39.701999999999998	39.722000000000001	39.741999999999997	39.762	39.781999999999996	39.802	39.822000000000003	39.841999999999999	39.862000000000002	39.881999999999998	39.902000000000001	39.921999999999997	39.941000000000003	39.962000000000003	39.981999999999999	40.002000000000002	40.021999999999998	40.042000000000002	40.061	40.082000000000001	40.101999999999997	40.122	40.140999999999998	40.161000000000001	40.180999999999997	40.201999999999998	40.222000000000001	40.241	40.262	40.281999999999996	40.302	40.322000000000003	40.341999999999999	40.362000000000002	40.381	40.402000000000001	40.420999999999999	40.442	40.460999999999999	40.481000000000002	40.502000000000002	40.521000000000001	40.540999999999997	40.561	40.582000000000001	40.600999999999999	40.621000000000002	40.640999999999998	40.661000000000001	40.680999999999997	40.701000000000001	40.720999999999997	40.741	40.761000000000003	40.780999999999999	40.802	40.820999999999998	40.841000000000001	40.860999999999997	40.881	40.901000000000003	40.920999999999999	40.941000000000003	40.960999999999999	40.981000000000002	41.000999999999998	41.021000000000001	41.040999999999997	41.061	41.081000000000003	41.100999999999999	41.121000000000002	41.140999999999998	41.161000000000001	41.18	41.2	41.220999999999997	41.241	41.261000000000003	41.280999999999999	41.301000000000002	41.320999999999998	41.341000000000001	41.360999999999997	41.38	41.401000000000003	41.42	41.441000000000003	41.46	41.48	41.500999999999998	41.521000000000001	41.540999999999997	41.56	41.58	41.6	41.62	41.640999999999998	41.661000000000001	41.68	41.7	41.72	41.74	41.76	41.78	41.8	41.82	41.84	41.86	41.88	41.9	41.92	41.94	41.96	41.98	42	42.02	42.04	42.06	42.08	42.1	42.12	42.139000000000003	42.16	42.18	42.2	42.219000000000001	42.238999999999997	42.259	42.28	42.3	42.32	42.338999999999999	42.359000000000002	42.38	42.399000000000001	42.42	42.44	42.46	42.478999999999999	42.499000000000002	42.518999999999998	42.54	42.56	42.58	42.598999999999997	42.619	42.639000000000003	42.658999999999999	42.679000000000002	42.698999999999998	42.719000000000001	42.738999999999997	42.759	42.779000000000003	42.798999999999999	42.819000000000003	42.838999999999999	42.86	42.878999999999998	42.899000000000001	42.918999999999997	42.939	42.959000000000003	42.978999999999999	42.999000000000002	43.018999999999998	43.039000000000001	43.058999999999997	43.079000000000001	43.097999999999999	43.118000000000002	43.139000000000003	43.158999999999999	43.179000000000002	43.198999999999998	43.218000000000004	43.238	43.259	43.279000000000003	43.298999999999999	43.317999999999998	43.338000000000001	43.357999999999997	43.378	43.398000000000003	43.417999999999999	43.439	43.457999999999998	43.478000000000002	43.499000000000002	43.518999999999998	43.537999999999997	43.558	43.578000000000003	43.597999999999999	43.618000000000002	43.637999999999998	43.658000000000001	43.677999999999997	43.698999999999998	43.718000000000004	43.738999999999997	43.759	43.777999999999999	43.798000000000002	43.817999999999998	43.838000000000001	43.857999999999997	43.878	43.898000000000003	43.917999999999999	43.938000000000002	43.957999999999998	43.978000000000002	43.997999999999998	44.018000000000001	44.037999999999997	44.058	44.078000000000003	44.097999999999999	44.118000000000002	44.137999999999998	44.156999999999996	44.177999999999997	44.198	44.218000000000004	44.238	44.258000000000003	44.277000000000001	44.296999999999997	44.317999999999998	44.338000000000001	44.357999999999997	44.378	44.396999999999998	44.417999999999999	44.438000000000002	44.457000000000001	44.476999999999997	44.497	44.518000000000001	44.537999999999997	44.558	44.578000000000003	44.597000000000001	44.618000000000002	44.637999999999998	44.656999999999996	44.677	44.698	44.716999999999999	44.737000000000002	44.756999999999998	44.777999999999999	44.798000000000002	44.817	44.837000000000003	44.856999999999999	44.877000000000002	44.896999999999998	44.917000000000002	44.936999999999998	44.957000000000001	44.978000000000002	44.997999999999998	45.017000000000003	45.036999999999999	45.057000000000002	45.076000000000001	45.095999999999997	45.116999999999997	45.136000000000003	45.156999999999996	45.177	45.197000000000003	45.216999999999999	45.237000000000002	45.256999999999998	45.276000000000003	45.296999999999997	45.317	45.337000000000003	45.356000000000002	45.377000000000002	45.396999999999998	45.417000000000002	45.436999999999998	45.457000000000001	45.476999999999997	45.497	45.515999999999998	45.536999999999999	45.555999999999997	45.576000000000001	45.595999999999997	45.616	45.636000000000003	45.655999999999999	45.677	45.697000000000003	45.716000000000001	45.737000000000002	45.756999999999998	45.777000000000001	45.795999999999999	45.816000000000003	45.837000000000003	45.856000000000002	45.875999999999998	45.896000000000001	45.915999999999997	45.936	45.956000000000003	45.975999999999999	45.996000000000002	46.015999999999998	46.036000000000001	46.057000000000002	46.076000000000001	46.095999999999997	46.116	46.136000000000003	46.155999999999999	46.176000000000002	46.195999999999998	46.216000000000001	46.235999999999997	46.256	46.276000000000003	46.295999999999999	46.316000000000003	46.335000000000001	46.356000000000002	46.375999999999998	46.396000000000001	46.414999999999999	46.436	46.454999999999998	46.475999999999999	46.494999999999997	46.515999999999998	46.536000000000001	46.555	46.575000000000003	46.595999999999997	46.615000000000002	46.636000000000003	46.655000000000001	46.676000000000002	46.695999999999998	46.715000000000003	46.734999999999999	46.755000000000003	46.774999999999999	46.795999999999999	46.814999999999998	46.835000000000001	46.854999999999997	46.875	46.895000000000003	46.914999999999999	46.935000000000002	46.954999999999998	46.975000000000001	46.994999999999997	47.015000000000001	47.034999999999997	47.055	47.075000000000003	47.094999999999999	47.115000000000002	47.134999999999998	47.155000000000001	47.173999999999999	47.194000000000003	47.213999999999999	47.234000000000002	47.255000000000003	47.274000000000001	47.295000000000002	47.314	47.334000000000003	47.354999999999997	47.375	47.395000000000003	47.414999999999999	47.435000000000002	47.454999999999998	47.475000000000001	47.494	47.515000000000001	47.534999999999997	47.555	47.573999999999998	47.594999999999999	47.615000000000002	47.634999999999998	47.655000000000001	47.673999999999999	47.694000000000003	47.713999999999999	47.734000000000002	47.755000000000003	47.774000000000001	47.793999999999997	47.814	47.834000000000003	47.853999999999999	47.874000000000002	47.895000000000003	47.914000000000001	47.933999999999997	47.954000000000001	47.973999999999997	47.994	48.014000000000003	48.034999999999997	48.055	48.073999999999998	48.094000000000001	48.113999999999997	48.134	48.154000000000003	48.173000000000002	48.192999999999998	48.213999999999999	48.232999999999997	48.253999999999998	48.274000000000001	48.293999999999997	48.314	48.334000000000003	48.353999999999999	48.374000000000002	48.393999999999998	48.412999999999997	48.433	48.454000000000001	48.473999999999997	48.494	48.514000000000003	48.533999999999999	48.554000000000002	48.573999999999998	48.594000000000001	48.613999999999997	48.634	48.652999999999999	48.673000000000002	48.694000000000003	48.713000000000001	48.732999999999997	48.753999999999998	48.773000000000003	48.793999999999997	48.813000000000002	48.832999999999998	48.853999999999999	48.874000000000002	48.893000000000001	48.912999999999997	48.933	48.953000000000003	48.972999999999999	48.993000000000002	49.012999999999998	49.033000000000001	49.054000000000002	49.073	49.093000000000004	49.113999999999997	49.134	49.152999999999999	49.173000000000002	49.192999999999998	49.213000000000001	49.232999999999997	49.253	49.273000000000003	49.292999999999999	49.313000000000002	49.332999999999998	49.351999999999997	49.372999999999998	49.392000000000003	49.412999999999997	49.433	49.453000000000003	49.472000000000001	49.491999999999997	49.512	49.533000000000001	49.552999999999997	49.573	49.593000000000004	49.613	49.633000000000003	49.652999999999999	49.671999999999997	49.692	49.712000000000003	49.732999999999997	49.752000000000002	49.771999999999998	49.792999999999999	49.813000000000002	49.832999999999998	49.851999999999997	49.872999999999998	49.893000000000001	49.911999999999999	49.932000000000002	49.951999999999998	49.972000000000001	49.991999999999997	50.012	50.031999999999996	50.052999999999997	50.073	50.091999999999999	50.112000000000002	50.131999999999998	50.152000000000001	50.173000000000002	50.192	50.212000000000003	50.231999999999999	50.252000000000002	50.271999999999998	50.292000000000002	50.311	50.332000000000001	50.351999999999997	50.372	50.392000000000003	50.411999999999999	50.432000000000002	50.451999999999998	50.472000000000001	50.491	50.511000000000003	50.531999999999996	50.552	50.572000000000003	50.591000000000001	50.610999999999997	50.631	50.652000000000001	50.671999999999997	50.691000000000003	50.710999999999999	50.731000000000002	50.750999999999998	50.771000000000001	50.790999999999997	50.811	50.832000000000001	50.850999999999999	50.871000000000002	50.892000000000003	50.911000000000001	50.930999999999997	50.951999999999998	50.972000000000001	50.991	51.011000000000003	51.030999999999999	51.052	51.070999999999998	51.091000000000001	51.110999999999997	51.131	51.151000000000003	51.170999999999999	51.191000000000003	51.210999999999999	51.231000000000002	51.250999999999998	51.271000000000001	51.290999999999997	51.311	51.331000000000003	51.350999999999999	51.371000000000002	51.39	51.411000000000001	51.430999999999997	51.451000000000001	51.470999999999997	51.49	51.51	51.53	51.551000000000002	51.570999999999998	51.591000000000001	51.61	51.63	51.65	51.670999999999999	51.691000000000003	51.710999999999999	51.73	51.75	51.77	51.79	51.81	51.831000000000003	51.85	51.87	51.890999999999998	51.91	51.930999999999997	51.95	51.97	51.99	52.01	52.03	52.05	52.070999999999998	52.09	52.11	52.13	52.151000000000003	52.17	52.19	52.21	52.23	52.25	52.268999999999998	52.29	52.31	52.33	52.35	52.37	52.389000000000003	52.408999999999999	52.43	52.45	52.47	52.488999999999997	52.51	52.53	52.55	52.57	52.588999999999999	52.61	52.628999999999998	52.65	52.67	52.69	52.709000000000003	52.728999999999999	52.749000000000002	52.77	52.789000000000001	52.808999999999997	52.829000000000001	52.848999999999997	52.869	52.89	52.91	52.93	52.948999999999998	52.969000000000001	52.988999999999997	53.009	53.029000000000003	53.048999999999999	53.069000000000003	53.088999999999999	53.109000000000002	53.128999999999998	53.149000000000001	53.168999999999997	53.189	53.21	53.23	53.247999999999998	53.268999999999998	53.289000000000001	53.308999999999997	53.329000000000001	53.348999999999997	53.369	53.389000000000003	53.408999999999999	53.429000000000002	53.448	53.468000000000004	53.488999999999997	53.509	53.529000000000003	53.548000000000002	53.569000000000003	53.588999999999999	53.607999999999997	53.628999999999998	53.648000000000003	53.667999999999999	53.689	53.709000000000003	53.728999999999999	53.747999999999998	53.768000000000001	53.787999999999997	53.81	53.828000000000003	53.847999999999999	53.868000000000002	53.889000000000003	53.908000000000001	53.929000000000002	53.948	53.968000000000004	53.988	54.008000000000003	54.029000000000003	54.048000000000002	54.067999999999998	54.088000000000001	54.107999999999997	54.128	54.148000000000003	54.167999999999999	54.188000000000002	54.207999999999998	54.228000000000002	54.247999999999998	54.268000000000001	54.287999999999997	54.308	54.328000000000003	54.347000000000001	54.368000000000002	54.387	54.406999999999996	54.427999999999997	54.448	54.468000000000004	54.488	54.508000000000003	54.527000000000001	54.548000000000002	54.567999999999998	54.588000000000001	54.607999999999997	54.628	54.648000000000003	54.667999999999999	54.688000000000002	54.707999999999998	54.728000000000002	54.747	54.768000000000001	54.787999999999997	54.808	54.826999999999998	54.847000000000001	54.866999999999997	54.887	54.906999999999996	54.927999999999997	54.948	54.968000000000004	54.987000000000002	55.008000000000003	55.027999999999999	55.046999999999997	55.067	55.087000000000003	55.106999999999999	55.127000000000002	55.148000000000003	55.167000000000002	55.186999999999998	55.207000000000001	55.226999999999997	55.247999999999998	55.267000000000003	55.287999999999997	55.307000000000002	55.326999999999998	55.347000000000001	55.366999999999997	55.387	55.406999999999996	55.427	55.447000000000003	55.466999999999999	55.487000000000002	55.506999999999998	55.527000000000001	55.546999999999997	55.567	55.587000000000003	55.606999999999999	55.625999999999998	55.646999999999998	55.667000000000002	55.686999999999998	55.707000000000001	55.726999999999997	55.747	55.765999999999998	55.786999999999999	55.807000000000002	55.826000000000001	55.845999999999997	55.866	55.887	55.905999999999999	55.926000000000002	55.947000000000003	55.966000000000001	55.985999999999997	56.006	56.027000000000001	56.045999999999999	56.067	56.085999999999999	56.106000000000002	56.125999999999998	56.146000000000001	56.165999999999997	56.186	56.207000000000001	56.225999999999999	56.246000000000002	56.265999999999998	56.286000000000001	56.305999999999997	56.326000000000001	56.344999999999999	56.366	56.386000000000003	56.405999999999999	56.426000000000002	56.445999999999998	56.466000000000001	56.485999999999997	56.506	56.526000000000003	56.545999999999999	56.566000000000003	56.585999999999999	56.606000000000002	56.625	56.645000000000003	56.664999999999999	56.686	56.706000000000003	56.725000000000001	56.746000000000002	56.765000000000001	56.786000000000001	56.805	56.826000000000001	56.844999999999999	56.866	56.884999999999998	56.905000000000001	56.926000000000002	56.945	56.965000000000003	56.984999999999999	57.006	57.026000000000003	57.045000000000002	57.064999999999998	57.085000000000001	57.104999999999997	57.125	57.145000000000003	57.165999999999997	57.185000000000002	57.204999999999998	57.225999999999999	57.244999999999997	57.265999999999998	57.284999999999997	57.305	57.325000000000003	57.344999999999999	57.365000000000002	57.384999999999998	57.405000000000001	57.424999999999997	57.445	57.465000000000003	57.484999999999999	57.505000000000003	57.524999999999999	57.545000000000002	57.564	57.585000000000001	57.603999999999999	57.624000000000002	57.645000000000003	57.664999999999999	57.685000000000002	57.704999999999998	57.725000000000001	57.744999999999997	57.764000000000003	57.784999999999997	57.805	57.823999999999998	57.844000000000001	57.865000000000002	57.884	57.904000000000003	57.923999999999999	57.945	57.965000000000003	57.984999999999999	58.003999999999998	58.024999999999999	58.043999999999997	58.064999999999998	58.085000000000001	58.104999999999997	58.124000000000002	58.145000000000003	58.164000000000001	58.183999999999997	58.204000000000001	58.223999999999997	58.244	58.264000000000003	58.283999999999999	58.304000000000002	58.325000000000003	58.344999999999999	58.363999999999997	58.384	58.404000000000003	58.423999999999999	58.444000000000003	58.463999999999999	58.484000000000002	58.503999999999998	58.524000000000001	58.543999999999997	58.564	58.584000000000003	58.603999999999999	58.624000000000002	58.643999999999998	58.662999999999997	58.683999999999997	58.703000000000003	58.723999999999997	58.744	58.764000000000003	58.783999999999999	58.804000000000002	58.823	58.844000000000001	58.863999999999997	58.883000000000003	58.902999999999999	58.923000000000002	58.944000000000003	58.963999999999999	58.984000000000002	59.003	59.023000000000003	59.042999999999999	59.063000000000002	59.084000000000003	59.103999999999999	59.122999999999998	59.143000000000001	59.162999999999997	59.183	59.203000000000003	59.222999999999999	59.243000000000002	59.264000000000003	59.283999999999999	59.302999999999997	59.323	59.343000000000004	59.363	59.384	59.402999999999999	59.423000000000002	59.442999999999998	59.462000000000003	59.482999999999997	59.503	59.523000000000003	59.542999999999999	59.563000000000002	59.582000000000001	59.603000000000002	59.622999999999998	59.643000000000001	59.662999999999997	59.683	59.701999999999998	59.722999999999999	59.743000000000002	59.762999999999998	59.783000000000001	59.802	59.823	59.841999999999999	59.863	59.883000000000003	59.902999999999999	59.921999999999997	59.942999999999998	59.963000000000001	59.981999999999999	60.003	60.023000000000003	60.042000000000002	60.061999999999998	60.082000000000001	60.103000000000002	60.122	60.143000000000001	60.161999999999999	60.182000000000002	60.201999999999998	60.222000000000001	60.243000000000002	60.262999999999998	60.283000000000001	60.302999999999997	60.323	60.341999999999999	60.362000000000002	60.381999999999998	60.402000000000001	60.421999999999997	60.442	60.462000000000003	60.481999999999999	60.502000000000002	60.521999999999998	60.542000000000002	60.561999999999998	60.582000000000001	60.600999999999999	60.622	60.642000000000003	60.661999999999999	60.682000000000002	60.701999999999998	60.720999999999997	60.741999999999997	60.762	60.781999999999996	60.802	60.822000000000003	60.841000000000001	60.860999999999997	60.881	60.901000000000003	60.921999999999997	60.941000000000003	60.962000000000003	60.981000000000002	61.000999999999998	61.021999999999998	61.040999999999997	61.061	61.081000000000003	61.100999999999999	61.121000000000002	61.140999999999998	61.161000000000001	61.180999999999997	61.201000000000001	61.220999999999997	61.241	61.261000000000003	61.280999999999999	61.302	61.320999999999998	61.341000000000001	61.362000000000002	61.381	61.401000000000003	61.420999999999999	61.441000000000003	61.460999999999999	61.481000000000002	61.500999999999998	61.521000000000001	61.540999999999997	61.561	61.581000000000003	61.600999999999999	61.621000000000002	61.640999999999998	61.66	61.680999999999997	61.701000000000001	61.720999999999997	61.741	61.761000000000003	61.780999999999999	61.8	61.820999999999998	61.841000000000001	61.86	61.88	61.901000000000003	61.920999999999999	61.941000000000003	61.960999999999999	61.98	62	62.02	62.04	62.06	62.08	62.100999999999999	62.12	62.14	62.16	62.180999999999997	62.201000000000001	62.220999999999997	62.24	62.261000000000003	62.280999999999999	62.3	62.32	62.34	62.36	62.38	62.4	62.42	62.44	62.46	62.48	62.5	62.52	62.54	62.56	62.58	62.6	62.62	62.64	62.66	62.68	62.7	62.72	62.74	62.76	62.779000000000003	62.8	62.82	62.84	62.86	62.878999999999998	62.9	62.918999999999997	62.939	62.96	62.978999999999999	62.999000000000002	63.02	63.039000000000001	63.06	63.079000000000001	63.1	63.119	63.139000000000003	63.16	63.179000000000002	63.2	63.219000000000001	63.238999999999997	63.259	63.279000000000003	63.298999999999999	63.319000000000003	63.338999999999999	63.36	63.378999999999998	63.399000000000001	63.418999999999997	63.44	63.459000000000003	63.478999999999999	63.499000000000002	63.518999999999998	63.539000000000001	63.558999999999997	63.579000000000001	63.598999999999997	63.619	63.639000000000003	63.658999999999999	63.679000000000002	63.698999999999998	63.719000000000001	63.738999999999997	63.759	63.779000000000003	63.798000000000002	63.819000000000003	63.838999999999999	63.857999999999997	63.878999999999998	63.898000000000003	63.917999999999999	63.939	63.959000000000003	63.978000000000002	63.999000000000002	64.018000000000001	64.037999999999997	64.058999999999997	64.078999999999994	64.099000000000004	64.119	64.138999999999996	64.158000000000001	64.179000000000002	64.198999999999998	64.218999999999994	64.238	64.259	64.278000000000006	64.299000000000007	64.317999999999998	64.337999999999994	64.358999999999995	64.378	64.397999999999996	64.418000000000006	64.438000000000002	64.457999999999998	64.478999999999999	64.498000000000005	64.516999999999996	64.537999999999997	64.558000000000007	64.578000000000003	64.597999999999999	64.617999999999995	64.638000000000005	64.658000000000001	64.677999999999997	64.697999999999993	64.718000000000004	64.739000000000004	64.757999999999996	64.778000000000006	64.798000000000002	64.817999999999998	64.837000000000003	64.856999999999999	64.878	64.897999999999996	64.918000000000006	64.938000000000002	64.956999999999994	64.977999999999994	64.998000000000005	65.018000000000001	65.037000000000006	65.057000000000002	65.076999999999998	65.096999999999994	65.117999999999995	65.137	65.156999999999996	65.177999999999997	65.197999999999993	65.218000000000004	65.236999999999995	65.257000000000005	65.277000000000001	65.296999999999997	65.317999999999998	65.337000000000003	65.356999999999999	65.376999999999995	65.397000000000006	65.417000000000002	65.438000000000002	65.457999999999998	65.477999999999994	65.497	65.516999999999996	65.537000000000006	65.557000000000002	65.576999999999998	65.596999999999994	65.617000000000004	65.637	65.656999999999996	65.677000000000007	65.697000000000003	65.716999999999999	65.736999999999995	65.757000000000005	65.777000000000001	65.796999999999997	65.816999999999993	65.837000000000003	65.856999999999999	65.876999999999995	65.896000000000001	65.915999999999997	65.936999999999998	65.956999999999994	65.975999999999999	65.997	66.016000000000005	66.036000000000001	66.057000000000002	66.076999999999998	66.096000000000004	66.116	66.137	66.156999999999996	66.176000000000002	66.197000000000003	66.215999999999994	66.236999999999995	66.257000000000005	66.277000000000001	66.296999999999997	66.316999999999993	66.335999999999999	66.355999999999995	66.376000000000005	66.396000000000001	66.415999999999997	66.436000000000007	66.456999999999994	66.475999999999999	66.495999999999995	66.516000000000005	66.536000000000001	66.555999999999997	66.575999999999993	66.596000000000004	66.616	66.635999999999996	66.656000000000006	66.676000000000002	66.695999999999998	66.715999999999994	66.736000000000004	66.756	66.775999999999996	66.796000000000006	66.814999999999998	66.834999999999994	66.855999999999995	66.876000000000005	66.896000000000001	66.915999999999997	66.935000000000002	66.956000000000003	66.975999999999999	66.995999999999995	67.015000000000001	67.034999999999997	67.055999999999997	67.075999999999993	67.096000000000004	67.114999999999995	67.135000000000005	67.156000000000006	67.174999999999997	67.194999999999993	67.215999999999994	67.234999999999999	67.256	67.275999999999996	67.295000000000002	67.316000000000003	67.334999999999994	67.355999999999995	67.375	67.394999999999996	67.415000000000006	67.435000000000002	67.454999999999998	67.474999999999994	67.495000000000005	67.515000000000001	67.534999999999997	67.555000000000007	67.575000000000003	67.594999999999999	67.614999999999995	67.635999999999996	67.655000000000001	67.674999999999997	67.694999999999993	67.715000000000003	67.734999999999999	67.754999999999995	67.775000000000006	67.795000000000002	67.814999999999998	67.834999999999994	67.855000000000004	67.875	67.894000000000005	67.914000000000001	67.935000000000002	67.954999999999998	67.974999999999994	67.995000000000005	68.015000000000001	68.034999999999997	68.055000000000007	68.075000000000003	68.093999999999994	68.114999999999995	68.135000000000005	68.155000000000001	68.174999999999997	68.194000000000003	68.213999999999999	68.233999999999995	68.254999999999995	68.275000000000006	68.295000000000002	68.313999999999993	68.334999999999994	68.355000000000004	68.375	68.394000000000005	68.415000000000006	68.433999999999997	68.454999999999998	68.474999999999994	68.494	68.513999999999996	68.534000000000006	68.555000000000007	68.573999999999998	68.593999999999994	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	0.03	0.03	0.03	0.03	0.03	0.03	0.03	0.03	0.03	0.03	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	0.04	0.04	0.04	0.04	0.04	4.4999999999999998E-2	4.4999999999999998E-2	4.4999999999999998E-2	4.4999999999999998E-2	4.4999999999999998E-2	0.05	0.05	0.05	0.05	0.05	5.5E-2	5.5E-2	5.5E-2	5.5E-2	0.06	0.06	0.06	0.06	6.5000000000000002E-2	6.5000000000000002E-2	6.5000000000000002E-2	6.5000000000000002E-2	7.0000000000000007E-2	7.0000000000000007E-2	7.0000000000000007E-2	7.0000000000000007E-2	7.4999999999999997E-2	7.4999999999999997E-2	7.4999999999999997E-2	7.4999999999999997E-2	0.08	0.08	0.08	0.08	8.5000000000000006E-2	8.5000000000000006E-2	8.5000000000000006E-2	8.5000000000000006E-2	0.09	0.09	0.09	0.09	9.5000000000000001E-2	9.5000000000000001E-2	9.5000000000000001E-2	9.5000000000000001E-2	0.1	0.1	0.1	0.105	0.105	0.105	0.105	0.11	0.11	0.11	0.11	0.115	0.115	0.115	0.115	0.12	0.12	0.12	0.12	0.125	0.125	0.125	0.125	0.13	0.13	0.13	0.13500000000000001	0.13500000000000001	0.13500000000000001	0.13500000000000001	0.14000000000000001	0.14000000000000001	0.14000000000000001	0.14000000000000001	0.14499999999999999	0.14499999999999999	0.14499999999999999	0.14499999999999999	0.15	0.15	0.15	0.15	0.155	0.155	0.155	0.16	0.16	0.16	0.16	0.16500000000000001	0.16500000000000001	0.16500000000000001	0.16500000000000001	0.17	0.17	0.17	0.17	0.17499999999999999	0.17499999999999999	0.17499999999999999	0.17499999999999999	0.18	0.18	0.18	0.18	0.185	0.185	0.185	0.185	0.19	0.19	0.19	0.19	0.19500000000000001	0.19500000000000001	0.19500000000000001	0.2	0.2	0.2	0.2	0.20499999999999999	0.20499999999999999	0.20499999999999999	0.20499999999999999	0.21	0.21	0.21	0.21	0.215	0.215	0.215	0.215	0.22	0.22	0.22	0.22	0.22500000000000001	0.22500000000000001	0.22500000000000001	0.22500000000000001	0.23	0.23	0.23	0.23	0.23499999999999999	0.23499999999999999	0.23499999999999999	0.23499999999999999	0.24	0.24	0.24	0.24	0.245	0.245	0.245	0.245	0.25	0.25	0.25	0.25	0.255	0.255	0.255	0.255	0.26	0.26	0.26	0.26500000000000001	0.26500000000000001	0.26500000000000001	0.26500000000000001	0.27	0.27	0.27	0.27	0.27500000000000002	0.27500000000000002	0.27500000000000002	0.27500000000000002	0.28000000000000003	0.28000000000000003	0.28000000000000003	0.28000000000000003	0.28499999999999998	0.28499999999999998	0.28499999999999998	0.28499999999999998	0.28999999999999998	0.28999999999999998	0.28999999999999998	0.28999999999999998	0.29499999999999998	0.29499999999999998	0.29499999999999998	0.29499999999999998	0.29499999999999998	0.3	0.3	0.3	0.3	0.30499999999999999	0.30499999999999999	0.30499999999999999	0.30499999999999999	0.31	0.31	0.31	0.31	0.315	0.315	0.315	0.315	0.32	0.32	0.32	0.32	0.32500000000000001	0.32500000000000001	0.32500000000000001	0.32500000000000001	0.33	0.33	0.33	0.33	0.33500000000000002	0.33500000000000002	0.33500000000000002	0.33500000000000002	0.33500000000000002	0.34	0.34	0.34	0.34	0.34499999999999997	0.34499999999999997	0.34499999999999997	0.34499999999999997	0.35	0.35	0.35	0.35	0.35499999999999998	0.35499999999999998	0.35499999999999998	0.35499999999999998	0.36	0.36	0.36	0.36	0.36	0.36499999999999999	0.36499999999999999	0.36499999999999999	0.36499999999999999	0.37	0.37	0.37	0.37	0.375	0.375	0.375	0.375	0.375	0.38	0.38	0.38	0.38	0.38500000000000001	0.38500000000000001	0.38500000000000001	0.38500000000000001	0.39	0.39	0.39	0.39	0.39500000000000002	0.39500000000000002	0.39500000000000002	0.39500000000000002	0.39500000000000002	0.4	0.4	0.4	0.4	0.40500000000000003	0.40500000000000003	0.40500000000000003	0.40500000000000003	0.40500000000000003	0.41	0.41	0.41	0.41	0.41499999999999998	0.41499999999999998	0.41499999999999998	0.41499999999999998	0.42	0.42	0.42	0.42	0.42	0.42499999999999999	0.42499999999999999	0.42499999999999999	0.42499999999999999	0.43	0.43	0.43	0.43	0.435	0.435	0.435	0.435	0.435	0.44	0.44	0.44	0.44	0.44500000000000001	0.44500000000000001	0.44500000000000001	0.44500000000000001	0.44500000000000001	0.45	0.45	0.45	0.45	0.45500000000000002	0.45500000000000002	0.45500000000000002	0.45500000000000002	0.45500000000000002	0.46	0.46	0.46	0.46	0.46500000000000002	0.46500000000000002	0.46500000000000002	0.46500000000000002	0.47	0.47	0.47	0.47	0.47	0.47499999999999998	0.47499999999999998	0.47499999999999998	0.47499999999999998	0.48	0.48	0.48	0.48	0.48	0.48499999999999999	0.48499999999999999	0.48499999999999999	0.48499999999999999	0.49	0.49	0.49	0.49	0.49	0.495	0.495	0.495	0.495	0.495	0.5	0.5	0.5	0.5	0.505	0.505	0.505	0.505	0.505	0.51	0.51	0.51	0.51	0.51	0.51500000000000001	0.51500000000000001	0.51500000000000001	0.51500000000000001	0.52	0.52	0.52	0.52	0.52	0.52500000000000002	0.52500000000000002	0.52500000000000002	0.52500000000000002	0.52500000000000002	0.53	0.53	0.53	0.53	0.53500000000000003	0.53500000000000003	0.53500000000000003	0.53500000000000003	0.53500000000000003	0.54	0.54	0.54	0.54	0.54	0.54500000000000004	0.54500000000000004	0.54500000000000004	0.54500000000000004	0.55000000000000004	0.55000000000000004	0.55000000000000004	0.55000000000000004	0.55000000000000004	0.55500000000000005	0.55500000000000005	0.55500000000000005	0.55500000000000005	0.55500000000000005	0.56000000000000005	0.56000000000000005	0.56000000000000005	0.56000000000000005	0.56000000000000005	0.56499999999999995	0.56499999999999995	0.56499999999999995	0.56499999999999995	0.56999999999999995	0.56999999999999995	0.56999999999999995	0.56999999999999995	0.56999999999999995	0.57499999999999996	0.57499999999999996	0.57499999999999996	0.57499999999999996	0.57499999999999996	0.57999999999999996	0.57999999999999996	0.57999999999999996	0.57999999999999996	0.57999999999999996	0.58499999999999996	0.58499999999999996	0.58499999999999996	0.58499999999999996	0.58499999999999996	0.59	0.59	0.59	0.59	0.59499999999999997	0.59499999999999997	0.59499999999999997	0.59499999999999997	0.59499999999999997	0.6	0.6	0.6	0.6	0.6	0.60499999999999998	0.60499999999999998	0.60499999999999998	0.60499999999999998	0.60499999999999998	0.61	0.61	0.61	0.61	0.61	0.61499999999999999	0.61499999999999999	0.61499999999999999	0.61499999999999999	0.61499999999999999	0.62	0.62	0.62	0.62	0.625	0.625	0.625	0.625	0.625	0.63	0.63	0.63	0.63	0.63	0.63500000000000001	0.63500000000000001	0.63500000000000001	0.63500000000000001	0.63500000000000001	0.64	0.64	0.64	0.64	0.64	0.64500000000000002	0.64500000000000002	0.64500000000000002	0.64500000000000002	0.64500000000000002	0.65	0.65	0.65	0.65	0.65	0.65500000000000003	0.65500000000000003	0.65500000000000003	0.65500000000000003	0.65500000000000003	0.66	0.66	0.66	0.66	0.66500000000000004	0.66500000000000004	0.66500000000000004	0.66500000000000004	0.66500000000000004	0.67	0.67	0.67	0.67	0.67	0.67500000000000004	0.67500000000000004	0.67500000000000004	0.67500000000000004	0.67500000000000004	0.68	0.68	0.68	0.68	0.68	0.68500000000000005	0.68500000000000005	0.68500000000000005	0.68500000000000005	0.68500000000000005	0.69	0.69	0.69	0.69	0.69	0.69499999999999995	0.69499999999999995	0.69499999999999995	0.69499999999999995	0.69499999999999995	0.7	0.7	0.7	0.7	0.7	0.70499999999999996	0.70499999999999996	0.70499999999999996	0.70499999999999996	0.70499999999999996	0.71	0.71	0.71	0.71	0.71	0.71499999999999997	0.71499999999999997	0.71499999999999997	0.71499999999999997	0.71499999999999997	0.72	0.72	0.72	0.72	0.72	0.72499999999999998	0.72499999999999998	0.72499999999999998	0.72499999999999998	0.72499999999999998	0.73	0.73	0.73	0.73	0.73	0.73499999999999999	0.73499999999999999	0.73499999999999999	0.73499999999999999	0.73499999999999999	0.74	0.74	0.74	0.74	0.74	0.74	0.745	0.745	0.745	0.745	0.745	0.75	0.75	0.75	0.75	0.75	0.755	0.755	0.755	0.755	0.755	0.76	0.76	0.76	0.76	0.76	0.76500000000000001	0.76500000000000001	0.76500000000000001	0.76500000000000001	0.76500000000000001	0.77	0.77	0.77	0.77	0.77	0.77500000000000002	0.77500000000000002	0.77500000000000002	0.77500000000000002	0.77500000000000002	0.78	0.78	0.78	0.78	0.78	0.78	0.78500000000000003	0.78500000000000003	0.78500000000000003	0.78500000000000003	0.78500000000000003	0.79	0.79	0.79	0.79	0.79	0.79500000000000004	0.79500000000000004	0.79500000000000004	0.79500000000000004	0.79500000000000004	0.8	0.8	0.8	0.8	0.8	0.80500000000000005	0.80500000000000005	0.80500000000000005	0.80500000000000005	0.80500000000000005	0.80500000000000005	0.81	0.81	0.81	0.81	0.81	0.81499999999999995	0.81499999999999995	0.81499999999999995	0.81499999999999995	0.81499999999999995	0.82	0.82	0.82	0.82	0.82	0.82499999999999996	0.82499999999999996	0.82499999999999996	0.82499999999999996	0.82499999999999996	0.83	0.83	0.83	0.83	0.83	0.83	0.83499999999999996	0.83499999999999996	0.83499999999999996	0.83499999999999996	0.83499999999999996	0.84	0.84	0.84	0.84	0.84	0.84499999999999997	0.84499999999999997	0.84499999999999997	0.84499999999999997	0.84499999999999997	0.85	0.85	0.85	0.85	0.85	0.85	0.85499999999999998	0.85499999999999998	0.85499999999999998	0.85499999999999998	0.85499999999999998	0.86	0.86	0.86	0.86	0.86	0.86499999999999999	0.86499999999999999	0.86499999999999999	0.86499999999999999	0.86499999999999999	0.87	0.87	0.87	0.87	0.87	0.87	0.875	0.875	0.875	0.875	0.875	0.88	0.88	0.88	0.88	0.88	0.88500000000000001	0.88500000000000001	0.88500000000000001	0.88500000000000001	0.88500000000000001	0.88500000000000001	0.89	0.89	0.89	0.89	0.89	0.89500000000000002	0.89500000000000002	0.89500000000000002	0.89500000000000002	0.89500000000000002	0.89500000000000002	0.9	0.9	0.9	0.9	0.9	0.90500000000000003	0.90500000000000003	0.90500000000000003	0.90500000000000003	0.90500000000000003	0.91	0.91	0.91	0.91	0.91	0.91	0.91500000000000004	0.91500000000000004	0.91500000000000004	0.91500000000000004	0.91500000000000004	0.92	0.92	0.92	0.92	0.92	0.92	0.92500000000000004	0.92500000000000004	0.92500000000000004	0.92500000000000004	0.92500000000000004	0.93	0.93	0.93	0.93	0.93	0.93	0.93500000000000005	0.93500000000000005	0.93500000000000005	0.93500000000000005	0.93500000000000005	0.94	0.94	0.94	0.94	0.94	0.94	0.94499999999999995	0.94499999999999995	0.94499999999999995	0.94499999999999995	0.94499999999999995	0.95	0.95	0.95	0.95	0.95	0.95	0.95499999999999996	0.95499999999999996	0.95499999999999996	0.95499999999999996	0.95499999999999996	0.96	0.96	0.96	0.96	0.96	0.96	0.96499999999999997	0.96499999999999997	0.96499999999999997	0.96499999999999997	0.96499999999999997	0.97	0.97	0.97	0.97	0.97	0.97	0.97499999999999998	0.97499999999999998	0.97499999999999998	0.97499999999999998	0.97499999999999998	0.98	0.98	0.98	0.98	0.98	0.98	0.98499999999999999	0.98499999999999999	0.98499999999999999	0.98499999999999999	0.98499999999999999	0.99	0.99	0.99	0.99	0.99	0.99	0.995	0.995	0.995	0.995	0.995	0.995	1	1	1	1	1	1.0049999999999999	1.0049999999999999	1.0049999999999999	1.0049999999999999	1.0049999999999999	1.0049999999999999	1.01	1.01	1.01	1.01	1.01	1.01	1.0149999999999999	1.0149999999999999	1.0149999999999999	1.0149999999999999	1.0149999999999999	1.02	1.02	1.02	1.02	1.02	1.02	1.0249999999999999	1.0249999999999999	1.0249999999999999	1.0249999999999999	1.0249999999999999	1.0249999999999999	1.03	1.03	1.03	1.03	1.03	1.0349999999999999	1.0349999999999999	1.0349999999999999	1.0349999999999999	1.0349999999999999	1.0349999999999999	1.04	1.04	1.04	1.04	1.04	1.04	1.0449999999999999	1.0449999999999999	1.0449999999999999	1.0449999999999999	1.0449999999999999	1.05	1.05	1.05	1.05	1.05	1.05	1.0549999999999999	1.0549999999999999	1.0549999999999999	1.0549999999999999	1.0549999999999999	1.0549999999999999	1.06	1.06	1.06	1.06	1.06	1.0649999999999999	1.0649999999999999	1.0649999999999999	1.0649999999999999	1.0649999999999999	1.0649999999999999	1.07	1.07	1.07	1.07	1.07	1.07	1.075	1.075	1.075	1.075	1.075	1.075	1.08	1.08	1.08	1.08	1.08	1.08	1.085	1.085	1.085	1.085	1.085	1.0900000000000001	1.0900000000000001	1.0900000000000001	1.0900000000000001	1.0900000000000001	1.0900000000000001	1.095	1.095	1.095	1.095	1.095	1.095	1.1000000000000001	1.1000000000000001	1.1000000000000001	1.1000000000000001	1.1000000000000001	1.1000000000000001	1.105	1.105	1.105	1.105	1.105	1.1100000000000001	1.1100000000000001	1.1100000000000001	1.1100000000000001	1.1100000000000001	1.1100000000000001	1.115	1.115	1.115	1.115	1.115	1.115	1.1200000000000001	1.1200000000000001	1.1200000000000001	1.1200000000000001	1.1200000000000001	1.1200000000000001	1.125	1.125	1.125	1.125	1.125	1.125	1.1299999999999999	1.1299999999999999	1.1299999999999999	1.1299999999999999	1.1299999999999999	1.1299999999999999	1.135	1.135	1.135	1.135	1.135	1.135	1.1399999999999999	1.1399999999999999	1.1399999999999999	1.1399999999999999	1.1399999999999999	1.1399999999999999	1.145	1.145	1.145	1.145	1.145	1.145	1.1499999999999999	1.1499999999999999	1.1499999999999999	1.1499999999999999	1.1499999999999999	1.1499999999999999	1.155	1.155	1.155	1.155	1.155	1.155	1.1599999999999999	1.1599999999999999	1.1599999999999999	1.1599999999999999	1.1599999999999999	1.1599999999999999	1.165	1.165	1.165	1.165	1.165	1.165	1.17	1.17	1.17	1.17	1.17	1.17	1.175	1.175	1.175	1.175	1.175	1.175	1.18	1.18	1.18	1.18	1.18	1.18	1.1850000000000001	1.1850000000000001	1.1850000000000001	1.1850000000000001	1.1850000000000001	1.1850000000000001	1.19	1.19	1.19	1.19	1.19	1.19	1.1950000000000001	1.1950000000000001	1.1950000000000001	1.1950000000000001	1.1950000000000001	1.1950000000000001	1.1950000000000001	1.2	1.2	1.2	1.2	1.2	1.2	1.2050000000000001	1.2050000000000001	1.2050000000000001	1.2050000000000001	1.2050000000000001	1.2050000000000001	1.21	1.21	1.21	1.21	1.21	1.21	1.2150000000000001	1.2150000000000001	1.2150000000000001	1.2150000000000001	1.2150000000000001	1.2150000000000001	1.22	1.22	1.22	1.22	1.22	1.22	1.2250000000000001	1.2250000000000001	1.2250000000000001	1.2250000000000001	1.2250000000000001	1.2250000000000001	1.2250000000000001	1.23	1.23	1.23	1.23	1.23	1.23	1.2350000000000001	1.2350000000000001	1.2350000000000001	1.2350000000000001	1.2350000000000001	1.2350000000000001	1.24	1.24	1.24	1.24	1.24	1.24	1.2450000000000001	1.2450000000000001	1.2450000000000001	1.2450000000000001	1.2450000000000001	1.2450000000000001	1.2450000000000001	1.25	1.25	1.25	1.25	1.25	1.25	1.2549999999999999	1.2549999999999999	1.2549999999999999	1.2549999999999999	1.2549999999999999	1.2549999999999999	1.26	1.26	1.26	1.26	1.26	1.26	1.26	1.2649999999999999	1.2649999999999999	1.2649999999999999	1.2649999999999999	1.2649999999999999	1.2649999999999999	1.27	1.27	1.27	1.27	1.27	1.27	1.2749999999999999	1.2749999999999999	1.2749999999999999	1.2749999999999999	1.2749999999999999	1.2749999999999999	1.2749999999999999	1.28	1.28	1.28	1.28	1.28	1.28	1.2849999999999999	1.2849999999999999	1.2849999999999999	1.2849999999999999	1.2849999999999999	1.2849999999999999	1.29	1.29	1.29	1.29	1.29	1.29	1.29	1.2949999999999999	1.2949999999999999	1.2949999999999999	1.2949999999999999	1.2949999999999999	1.2949999999999999	1.3	1.3	1.3	1.3	1.3	1.3	1.3	1.3049999999999999	1.3049999999999999	1.3049999999999999	1.3049999999999999	1.3049999999999999	1.3049999999999999	1.31	1.31	1.31	1.31	1.31	1.31	1.3149999999999999	1.3149999999999999	1.3149999999999999	1.3149999999999999	1.3149999999999999	1.3149999999999999	1.3149999999999999	1.32	1.32	1.32	1.32	1.32	1.32	1.325	1.325	1.325	1.325	1.325	1.325	1.325	1.33	1.33	1.33	1.33	1.33	1.33	1.335	1.335	1.335	1.335	1.335	1.335	1.335	1.34	1.34	1.34	1.34	1.34	1.34	1.345	1.345	1.345	1.345	1.345	1.345	1.345	1.35	1.35	1.35	1.35	1.35	1.35	1.35	1.355	1.355	1.355	1.355	1.355	1.355	1.36	1.36	1.36	1.36	1.36	1.36	1.36	1.365	1.365	1.365	1.365	1.365	1.365	1.365	1.37	1.37	1.37	1.37	1.37	1.37	1.375	1.375	1.375	1.375	1.375	1.375	1.375	1.38	1.38	1.38	1.38	1.38	1.38	1.38	1.385	1.385	1.385	1.385	1.385	1.385	1.39	1.39	1.39	1.39	1.39	1.39	1.39	1.395	1.395	1.395	1.395	1.395	1.395	1.395	1.4	1.4	1.4	1.4	1.4	1.4	1.405	1.405	1.405	1.405	1.405	1.405	1.405	1.41	1.41	1.41	1.41	1.41	1.41	1.41	1.415	1.415	1.415	1.415	1.415	1.415	1.415	1.42	1.42	1.42	1.42	1.42	1.42	1.425	1.425	1.425	1.425	1.425	1.425	1.425	1.43	1.43	1.43	1.43	1.43	1.43	1.43	1.4350000000000001	1.4350000000000001	1.4350000000000001	1.4350000000000001	1.4350000000000001	1.4350000000000001	1.4350000000000001	1.44	1.44	1.44	1.44	1.44	1.44	1.4450000000000001	1.4450000000000001	1.4450000000000001	1.4450000000000001	1.4450000000000001	1.4450000000000001	1.4450000000000001	1.45	1.45	1.45	1.45	1.45	1.45	1.45	1.4550000000000001	1.4550000000000001	1.4550000000000001	1.4550000000000001	1.4550000000000001	1.4550000000000001	1.4550000000000001	1.46	1.46	1.46	1.46	1.46	1.46	1.46	1.4650000000000001	1.4650000000000001	1.4650000000000001	1.4650000000000001	1.4650000000000001	1.4650000000000001	1.4650000000000001	1.47	1.47	1.47	1.47	1.47	1.47	1.4750000000000001	1.4750000000000001	1.4750000000000001	1.4750000000000001	1.4750000000000001	1.4750000000000001	1.4750000000000001	1.48	1.48	1.48	1.48	1.48	1.48	1.48	1.4850000000000001	1.4850000000000001	1.4850000000000001	1.4850000000000001	1.4850000000000001	1.4850000000000001	1.4850000000000001	1.49	1.49	1.49	1.49	1.49	1.49	1.49	1.4950000000000001	1.4950000000000001	1.4950000000000001	1.4950000000000001	1.4950000000000001	1.4950000000000001	1.4950000000000001	1.5	1.5	1.5	1.5	1.5	1.5	1.5	1.5049999999999999	1.5049999999999999	1.5049999999999999	1.5049999999999999	1.5049999999999999	1.5049999999999999	1.5049999999999999	1.51	1.51	1.51	1.51	1.51	1.51	1.5149999999999999	1.5149999999999999	1.5149999999999999	1.5149999999999999	1.5149999999999999	1.5149999999999999	1.5149999999999999	1.52	1.52	1.52	1.52	1.52	1.52	1.52	1.5249999999999999	1.5249999999999999	1.5249999999999999	1.5249999999999999	1.5249999999999999	1.5249999999999999	1.5249999999999999	1.53	1.53	1.53	1.53	1.53	1.53	1.53	1.5349999999999999	1.5349999999999999	1.5349999999999999	1.5349999999999999	1.5349999999999999	1.5349999999999999	1.5349999999999999	1.54	1.54	1.54	1.54	1.54	1.54	1.54	1.54	1.5449999999999999	1.5449999999999999	1.5449999999999999	1.5449999999999999	1.5449999999999999	1.5449999999999999	1.5449999999999999	1.55	1.55	1.55	1.55	1.55	1.55	1.55	1.5549999999999999	1.5549999999999999	1.5549999999999999	1.5549999999999999	1.5549999999999999	1.5549999999999999	1.5549999999999999	1.5549999999999999	1.56	1.56	1.56	1.56	1.56	1.56	1.56	1.5649999999999999	1.5649999999999999	1.5649999999999999	1.5649999999999999	1.5649999999999999	1.5649999999999999	1.5649999999999999	1.57	1.57	1.57	1.57	1.57	1.57	1.57	1.57	1.575	1.575	1.575	1.575	1.575	1.575	1.575	1.58	1.58	1.58	1.58	1.58	1.58	1.58	1.585	1.585	1.585	1.585	1.585	1.585	1.585	1.59	1.59	1.59	1.59	1.59	1.59	1.59	1.595	1.595	1.595	1.595	1.595	1.595	1.595	1.595	1.6	1.6	1.6	1.6	1.6	1.6	1.6	1.605	1.605	1.605	1.605	1.605	1.605	1.605	1.61	1.61	1.61	1.61	1.61	1.61	1.61	1.615	1.615	1.615	1.615	1.615	1.615	1.615	1.62	1.62	1.62	1.62	1.62	1.62	1.62	1.625	1.625	1.625	1.625	1.625	1.625	1.625	1.625	1.63	1.63	1.63	1.63	1.63	1.63	1.63	1.635	1.635	1.635	1.635	1.635	1.635	1.635	1.64	1.64	1.64	1.64	1.64	1.64	1.64	1.64	1.645	1.645	1.645	1.645	1.645	1.645	1.645	1.65	1.65	1.65	1.65	1.65	1.65	1.65	1.655	1.655	1.655	1.655	1.655	1.655	1.655	1.655	1.66	1.66	1.66	1.66	1.66	1.66	1.66	1.665	1.665	1.665	1.665	1.665	1.665	1.665	1.665	1.67	1.67	1.67	1.67	1.67	1.67	1.67	1.675	1.675	1.675	1.675	1.675	1.675	1.675	1.675	1.68	1.68	1.68	1.68	1.68	1.68	1.68	1.6850000000000001	1.6850000000000001	1.6850000000000001	1.6850000000000001	1.6850000000000001	1.6850000000000001	1.6850000000000001	1.6850000000000001	1.69	1.69	1.69	1.69	1.69	1.69	1.69	1.6950000000000001	1.6950000000000001	1.6950000000000001	1.6950000000000001	1.6950000000000001	1.6950000000000001	1.6950000000000001	1.7	1.7	1.7	1.7	1.7	1.7	1.7	1.7	1.7050000000000001	1.7050000000000001	1.7050000000000001	1.7050000000000001	1.7050000000000001	1.7050000000000001	1.7050000000000001	1.7050000000000001	1.71	1.71	1.71	1.71	1.71	1.71	1.71	1.7150000000000001	1.7150000000000001	1.7150000000000001	1.7150000000000001	1.7150000000000001	1.7150000000000001	1.7150000000000001	1.7150000000000001	1.72	1.72	1.72	1.72	1.72	1.72	1.72	1.72	1.7250000000000001	1.7250000000000001	1.7250000000000001	1.7250000000000001	1.7250000000000001	1.7250000000000001	1.7250000000000001	1.7250000000000001	1.73	1.73	1.73	1.73	1.73	1.73	1.73	1.7350000000000001	1.7350000000000001	1.7350000000000001	1.7350000000000001	1.7350000000000001	1.7350000000000001	1.7350000000000001	1.7350000000000001	1.74	1.74	1.74	1.74	1.74	1.74	1.74	1.74	1.7450000000000001	1.7450000000000001	1.7450000000000001	1.7450000000000001	1.7450000000000001	1.7450000000000001	1.7450000000000001	1.7450000000000001	1.75	1.75	1.75	1.75	1.75	1.75	1.75	1.75	1.7549999999999999	1.7549999999999999	1.7549999999999999	1.7549999999999999	1.7549999999999999	1.7549999999999999	1.7549999999999999	1.7549999999999999	1.76	1.76	1.76	1.76	1.76	1.76	1.76	1.7649999999999999	1.7649999999999999	1.7649999999999999	1.7649999999999999	1.7649999999999999	1.7649999999999999	1.7649999999999999	1.7649999999999999	1.77	1.77	1.77	1.77	1.77	1.77	1.77	1.77	1.7749999999999999	1.7749999999999999	1.7749999999999999	1.7749999999999999	1.7749999999999999	1.7749999999999999	1.7749999999999999	1.7749999999999999	1.78	1.78	1.78	1.78	1.78	1.78	1.78	1.78	1.7849999999999999	1.7849999999999999	1.7849999999999999	1.7849999999999999	1.7849999999999999	1.7849999999999999	1.7849999999999999	1.7849999999999999	1.79	1.79	1.79	1.79	1.79	1.79	1.79	1.79	1.7949999999999999	1.7949999999999999	1.7949999999999999	1.7949999999999999	1.7949999999999999	1.7949999999999999	1.7949999999999999	1.7949999999999999	1.8	1.8	1.8	1.8	1.8	1.8	1.8	1.8	1.8049999999999999	1.8049999999999999	1.8049999999999999	1.8049999999999999	1.8049999999999999	1.8049999999999999	1.8049999999999999	1.8049999999999999	1.81	1.81	1.81	1.81	1.81	1.81	1.81	1.81	1.8149999999999999	1.8149999999999999	1.8149999999999999	1.8149999999999999	1.8149999999999999	1.8149999999999999	1.8149999999999999	1.8149999999999999	1.82	1.82	1.82	1.82	1.82	1.82	1.82	1.82	1.82	1.825	1.825	1.825	1.825	1.825	1.825	1.825	1.825	1.83	1.83	1.83	1.83	1.83	1.83	1.83	1.83	1.835	1.835	1.835	1.835	1.835	1.835	1.835	1.835	1.84	1.84	1.84	1.84	1.84	1.84	1.84	1.84	1.845	1.845	1.845	1.845	1.845	1.845	1.845	1.845	1.85	1.85	1.85	1.85	1.85	1.85	1.85	1.85	1.85	1.855	1.855	1.855	1.855	1.855	1.855	1.855	1.855	1.86	1.86	1.86	1.86	1.86	1.86	1.86	1.86	1.86	1.865	1.865	1.865	1.865	1.865	1.865	1.865	1.865	1.87	1.87	1.87	1.87	1.87	1.87	1.87	1.87	1.875	1.875	1.875	1.875	1.875	1.875	1.875	1.875	1.875	1.88	1.88	1.88	1.88	1.88	1.88	1.88	1.88	1.885	1.885	1.885	1.885	1.885	1.885	1.885	1.885	1.89	1.89	1.89	1.89	1.89	1.89	1.89	1.89	1.89	1.895	1.895	1.895	1.895	1.895	1.895	1.895	1.895	1.9	1.9	1.9	1.9	1.9	1.9	1.9	1.9	1.905	1.905	1.905	1.905	1.905	1.905	1.905	1.905	1.905	1.91	1.91	1.91	1.91	1.91	1.91	1.91	1.91	1.915	1.915	1.915	1.915	1.915	1.915	1.915	1.915	1.915	1.92	1.92	1.92	1.92	1.92	1.92	1.92	1.92	1.925	1.925	1.925	1.925	1.925	1.925	1.925	1.925	1.925	1.93	1.93	1.93	1.93	1.93	1.93	1.93	1.93	1.93	1.9350000000000001	1.9350000000000001	1.9350000000000001	1.9350000000000001	1.9350000000000001	1.9350000000000001	1.9350000000000001	1.9350000000000001	1.94	1.94	1.94	1.94	1.94	1.94	1.94	1.94	1.94	1.9450000000000001	1.9450000000000001	1.9450000000000001	1.9450000000000001	1.9450000000000001	1.9450000000000001	1.9450000000000001	1.9450000000000001	1.95	1.95	1.95	1.95	1.95	1.95	1.95	1.95	1.95	1.9550000000000001	1.9550000000000001	1.9550000000000001	1.9550000000000001	1.9550000000000001	1.9550000000000001	1.9550000000000001	1.9550000000000001	1.9550000000000001	1.96	1.96	1.96	1.96	1.96	1.96	1.96	1.96	1.9650000000000001	1.9650000000000001	1.9650000000000001	1.9650000000000001	1.9650000000000001	1.9650000000000001	1.9650000000000001	1.9650000000000001	1.9650000000000001	1.97	1.97	1.97	1.97	1.97	1.97	1.97	1.97	1.9750000000000001	1.9750000000000001	1.9750000000000001	1.9750000000000001	1.9750000000000001	1.9750000000000001	1.9750000000000001	1.9750000000000001	1.98	1.98	1.98	1.98	1.98	1.98	1.98	1.98	1.98	1.9850000000000001	1.9850000000000001	1.9850000000000001	1.9850000000000001	1.9850000000000001	1.9850000000000001	1.9850000000000001	1.9850000000000001	1.9850000000000001	1.99	1.99	1.99	1.99	1.99	1.99	1.99	1.99	1.9950000000000001	1.9950000000000001	1.9950000000000001	1.9950000000000001	1.9950000000000001	1.9950000000000001	1.9950000000000001	1.9950000000000001	1.9950000000000001	2	2	2	2	2	2	2	2	2.0049999999999999	2.0049999999999999	2.0049999999999999	2.0049999999999999	2.0049999999999999	2.0049999999999999	2.0049999999999999	2.0049999999999999	2.0049999999999999	2.0099999999999998	2.0099999999999998	2.0099999999999998	2.0099999999999998	2.0099999999999998	2.0099999999999998	2.0099999999999998	2.0099999999999998	2.0099999999999998	2.0150000000000001	2.0150000000000001	2.0150000000000001	2.0150000000000001	2.0150000000000001	2.0150000000000001	2.0150000000000001	2.0150000000000001	2.02	2.02	2.02	2.02	2.02	2.02	2.02	2.02	2.02	2.0249999999999999	2.0249999999999999	2.0249999999999999	2.0249999999999999	2.0249999999999999	2.0249999999999999	2.0249999999999999	2.0249999999999999	2.0249999999999999	2.0299999999999998	2.0299999999999998	2.0299999999999998	2.0299999999999998	2.0299999999999998	2.0299999999999998	2.0299999999999998	2.0299999999999998	2.0299999999999998	2.0350000000000001	2.0350000000000001	2.0350000000000001	2.0350000000000001	2.0350000000000001	2.0350000000000001	2.0350000000000001	2.0350000000000001	2.04	2.04	2.04	2.04	2.04	2.04	2.04	2.04	2.04	2.0449999999999999	2.0449999999999999	2.0449999999999999	2.0449999999999999	2.0449999999999999	2.0449999999999999	2.0449999999999999	2.0449999999999999	2.0449999999999999	2.0499999999999998	2.0499999999999998	2.0499999999999998	2.0499999999999998	2.0499999999999998	2.0499999999999998	2.0499999999999998	2.0499999999999998	2.0499999999999998	2.0550000000000002	2.0550000000000002	2.0550000000000002	2.0550000000000002	2.0550000000000002	2.0550000000000002	2.0550000000000002	2.0550000000000002	2.0550000000000002	2.06	2.06	2.06	2.06	2.06	2.06	2.06	2.06	2.0649999999999999	2.0649999999999999	2.0649999999999999	2.0649999999999999	2.0649999999999999	2.0649999999999999	2.0649999999999999	2.0649999999999999	2.0649999999999999	2.0699999999999998	2.0699999999999998	2.0699999999999998	2.0699999999999998	2.0699999999999998	2.0699999999999998	2.0699999999999998	2.0699999999999998	2.0699999999999998	2.0750000000000002	2.0750000000000002	2.0750000000000002	2.0750000000000002	2.0750000000000002	2.0750000000000002	2.0750000000000002	2.0750000000000002	2.0750000000000002	2.08	2.08	2.08	2.08	2.08	2.08	2.08	2.08	2.08	2.085	2.085	2.085	2.085	2.085	2.085	2.085	2.085	2.085	2.09	2.09	2.09	2.09	2.09	2.09	2.09	2.09	2.09	2.0950000000000002	2.0950000000000002	2.0950000000000002	2.0950000000000002	2.0950000000000002	2.0950000000000002	2.0950000000000002	2.0950000000000002	2.0950000000000002	2.1	2.1	2.1	2.1	2.1	2.1	2.1	2.1	2.1	2.105	2.105	2.105	2.105	2.105	2.105	2.105	2.105	2.105	2.11	2.11	2.11	2.11	2.11	2.11	2.11	2.11	2.11	2.1150000000000002	2.1150000000000002	2.1150000000000002	2.1150000000000002	2.1150000000000002	2.1150000000000002	2.1150000000000002	2.1150000000000002	2.1150000000000002	2.12	2.12	2.12	2.12	2.12	2.12	2.12	2.12	2.12	2.125	2.125	2.125	2.125	2.125	2.125	2.125	2.125	2.125	2.13	2.13	2.13	2.13	2.13	2.13	2.13	2.13	2.13	2.1349999999999998	2.1349999999999998	2.1349999999999998	2.1349999999999998	2.1349999999999998	2.1349999999999998	2.1349999999999998	2.1349999999999998	2.1349999999999998	2.14	2.14	2.14	2.14	2.14	2.14	2.14	2.14	2.14	2.145	2.145	2.145	2.145	2.145	2.145	2.145	2.145	2.145	2.15	2.15	2.15	2.15	2.15	2.15	2.15	2.15	2.15	2.1549999999999998	2.1549999999999998	2.1549999999999998	2.1549999999999998	2.1549999999999998	2.1549999999999998	2.1549999999999998	2.1549999999999998	2.1549999999999998	2.16	2.16	2.16	2.16	2.16	2.16	2.16	2.16	2.16	2.165	2.165	2.165	2.165	2.165	2.165	2.165	2.165	2.165	2.17	2.17	2.17	2.17	2.17	2.17	2.17	2.17	2.17	2.1749999999999998	2.1749999999999998	2.1749999999999998	2.1749999999999998	2.1749999999999998	2.1749999999999998	2.1749999999999998	2.1749999999999998	2.1749999999999998	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1800000000000002	2.1850000000000001	2.1850000000000001	2.1850000000000001	2.1850000000000001	2.1850000000000001	2.1850000000000001	2.1850000000000001	2.1850000000000001	2.1850000000000001	2.19	2.19	2.19	2.19	2.19	2.19	2.19	2.19	2.19	2.1949999999999998	2.1949999999999998	2.1949999999999998	2.1949999999999998	2.1949999999999998	2.1949999999999998	2.1949999999999998	2.1949999999999998	2.1949999999999998	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2000000000000002	2.2050000000000001	2.2050000000000001	2.2050000000000001	2.2050000000000001	2.2050000000000001	2.2050000000000001	2.2050000000000001	2.2050000000000001	2.2050000000000001	2.21	2.21	2.21	2.21	2.21	2.21	2.21	2.21	2.21	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2149999999999999	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2200000000000002	2.2250000000000001	2.2250000000000001	2.2250000000000001	2.2250000000000001	2.2250000000000001	2.2250000000000001	2.2250000000000001	2.2250000000000001	2.2250000000000001	2.23	2.23	2.23	2.23	2.23	2.23	2.23	2.23	2.23	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2349999999999999	2.2400000000000002	2.2400000000000002	2.2400000000000002	2.2400000000000002	2.2400000000000002	2.2400000000000002	2.2400000000000002	2.2400000000000002	2.2400000000000002	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.2450000000000001	2.25	2.25	2.25	2.25	2.25	2.25	2.25	2.25	2.25	2.2549999999999999	2.2549999999999999	2.2549999999999999	2.2549999999999999	2.2549999999999999	2.2549999999999999	2.2549999999999999	2.2549999999999999	2.2549999999999999	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2599999999999998	2.2650000000000001	2.2650000000000001	2.2650000000000001	2.2650000000000001	2.2650000000000001	2.2650000000000001	2.2650000000000001	2.2650000000000001	2.2650000000000001	2.27	2.27	2.27	2.27	2.27	2.27	2.27	2.27	2.27	2.27	2.2749999999999999	2.2749999999999999	2.2749999999999999	2.2749999999999999	2.2749999999999999	2.2749999999999999	2.2749999999999999	2.2749999999999999	2.2749999999999999	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2799999999999998	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.2850000000000001	2.29	2.29	2.29	2.29	2.29	2.29	2.29	2.29	2.29	2.29	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2949999999999999	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.2999999999999998	2.3050000000000002	2.3050000000000002	2.3050000000000002	2.3050000000000002	2.3050000000000002	2.3050000000000002	2.3050000000000002	2.3050000000000002	2.3050000000000002	2.31	2.31	2.31	2.31	2.31	2.31	2.31	2.31	2.31	2.31	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3149999999999999	2.3199999999999998	2.3199999999999998	2.3199999999999998	2.3199999999999998	2.3199999999999998	2.3199999999999998	2.3199999999999998	2.3199999999999998	2.3199999999999998	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.3250000000000002	2.33	2.33	2.33	2.33	2.33	2.33	2.33	2.33	2.33	2.33	2.335	2.335	2.335	2.335	2.335	2.335	2.335	2.335	2.335	2.34	2.34	2.34	2.34	2.34	2.34	2.34	2.34	2.34	2.34	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.3450000000000002	2.35	2.35	2.35	2.35	2.35	2.35	2.35	2.35	2.35	2.35	2.355	2.355	2.355	2.355	2.355	2.355	2.355	2.355	2.355	2.355	2.36	2.36	2.36	2.36	2.36	2.36	2.36	2.36	2.36	2.36	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.3650000000000002	2.37	2.37	2.37	2.37	2.37	2.37	2.37	2.37	2.37	2.37	2.375	2.375	2.375	2.375	2.375	2.375	2.375	2.375	2.375	2.375	2.38	2.38	2.38	2.38	2.38	2.38	2.38	2.38	2.38	2.38	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.3849999999999998	2.39	2.39	2.39	2.39	2.39	2.39	2.39	2.39	2.39	2.39	2.395	2.395	2.395	2.395	2.395	2.395	2.395	2.395	2.395	2.395	2.4	2.4	2.4	2.4	2.4	2.4	2.4	2.4	2.4	2.4	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.4049999999999998	2.41	2.41	2.41	2.41	2.41	2.41	2.41	2.41	2.41	2.41	2.41	2.415	2.415	2.415	2.415	2.415	2.415	2.415	2.415	2.415	2.415	2.42	2.42	2.42	2.42	2.42	2.42	2.42	2.42	2.42	2.42	2.42	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4249999999999998	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4300000000000002	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.4350000000000001	2.44	2.44	2.44	2.44	2.44	2.44	2.44	2.44	2.44	2.44	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4449999999999998	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4500000000000002	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.4550000000000001	2.46	2.46	2.46	2.46	2.46	2.46	2.46	2.46	2.46	2.46	2.46	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4649999999999999	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4700000000000002	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.4750000000000001	2.48	2.48	2.48	2.48	2.48	2.48	2.48	2.48	2.48	2.48	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4849999999999999	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4900000000000002	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.4950000000000001	2.5	2.5	2.5	2.5	2.5	2.5	2.5	2.5	2.5	2.5	2.5	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5049999999999999	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5099999999999998	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.5150000000000001	2.52	2.52	2.52	2.52	2.52	2.52	2.52	2.52	2.52	2.52	2.52	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5249999999999999	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5299999999999998	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.5350000000000001	2.54	2.54	2.54	2.54	2.54	2.54	2.54	2.54	2.54	2.54	2.54	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5449999999999999	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5499999999999998	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.5550000000000002	2.56	2.56	2.56	2.56	2.56	2.56	2.56	2.56	2.56	2.56	2.56	2.5649999999999999	2.5649999999999999	Time (s)


Load (N)



Hemp (Bio Resin) - Time vs Load
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Kevlar Woven (Bio Resin) - Time vs Load
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Load (N)



Aluminium - Time vs Stress
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Stress (MPa)



Carbon Non Woven (Bio Resin) - Time vs Stress
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Stress (MPa)



Carbon Woven (Bio Resin) - Time vs Stress
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Carbon Woven (Epoxy Resin) - Time vs Stress
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Stress (MPa)



Flax Non Woven (Bio Resin) - Time vs Stress
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Flax Woven (Bio Resin) - Time vs Stress
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Hemp (Bio Resin) - Time vs Stress
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Kevlar Woven (Bio Resin) - Time vs Stress
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Stress (MPa)



Aluminium - Load vs Stress
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Carbon Non Woven (Bio Resin) - Load vs Stress
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Stress (MPa)



Carbon Woven (Bio Resin) - Load vs Stress
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Stress (MPa)



Carbon Woven (Epoxy Resin) - Load vs Stress
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Stress (MPa)



Flax Non Woven (Bio Resin) - Load vs Stress
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Stress (MPa)



Flax Woven (Bio Resin) - Load vs Stress
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Stress (MPa)



Hemp (Bio Resin) - Load vs Stress
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Kevlar Woven (Bio Resin) - Load vs Stress
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