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[bookmark: _Toc228108689]Introduction

Composite materials are widely used in engineering due to their ability to combine desirable properties, resulting in optimised mechanical performance (Bhong, 2023). Figure 1 confirms fibres provide high strength and stiffness, while the matrix contributes to the elongation of the composite, allowing a balance of properties not achievable by individual materials (Rajak et al., 2019).
[image: ]
[bookmark: _Toc228108727]Figure 1 - Demonstrating the possible optimisation of properties when combining fibres and resin to form a composite material (Hatton, 2019)
With motorsport’s ongoing challenge of balancing increased pressures of sustainability, there is growing interest in alternative materials such as natural fibres and bio-based resins. 
[bookmark: _Toc228108690]Aims
To evaluate the mechanical performance of a range of composite materials through tensile testing, focusing on the influence of fibre type, resin and weaves, whilst analysing the sustainability of composites through a life cycle assessment. 

[bookmark: _Toc228108691]Literature Review

[bookmark: _Toc228108692]Structure of a composite
[bookmark: _Toc228108693]Fibres
Fibres are the primary load-carrying component in composite materials, providing strength and stiffness (Clyne and Hull, 2019). Hatton (2019) highlights how fibres are effective in tension, however, become weak under compression and bending loads, explaining why they are embedded within a polymer matrix, to provide structural support and stability. Fibre orientation and arrangement play a critical role in the mechanical properties and structural behaviour of a composite, with aligned fibres providing high strength in one direction, whilst complex arrangements improve load distribution (Rajak et al, 2019).
[bookmark: _Toc228108694]Matrix
The matrix binds fibres together and maintain their required position (Rajak et al, 2019). As demonstrated by Hatton (2019), matrices support the fibres, enabling them to carry compressive loads, and transfer shear stresses between fibres so loads can be distributed evenly throughout the material. Epoxy resins are used in motorsport engine bays or brake ducts due to their ability to retain mechanical properties at elevated temperatures, unlike thermoplastics, which soften when above their glass transition temperature (Hatton, 2019). Bio-based resins offer a sustainable alternative, derived from renewable sources such as plant oils (Capretti, 2023). Compared to petroleum-based resins, they offer reduced environmental impact but lower mechanical and thermal performance (Pickering, 2016). Therefore, bioresins are used in motorsport for non-structural components where sustainability can be prioritised without significantly compromising performance.
[bookmark: _Toc228108695]Weave
Chowdhury (2024) explains that woven composites are constructed by weaving yarns together, providing a more controlled fibre orientation and improved strength in multiple directions, making them suitable for applications including bodywork (Hatton, 2019). Non-woven composites are produced by bonding fibres through chemical, mechanical or thermal processes, resulting in random fibre orientation (Chowdhury, 2024). Although non-woven materials can be strengthened by increasing the number of layers, they generally produce lower stiffness and strength compared to woven structures due to less efficient load transfer (Ratim, 2012).


[bookmark: _Toc228108696]Composite Types

[bookmark: _Toc228108747]Table 1 - Comparing carbon fibre, natural fibres (flax) and synthetic fibres (Kevlar) and discussing their application in motorsport.
	Composite Type
	Key Properties
	Motorsport Application

	Carbon Fibre
	Exceptional strength to weight ratio and great mouldability (Hatton, 2019).
Combined with honeycomb cores to form sandwich structures, significantly increasing stiffness whilst maintaining low mass through plies being bonded either side of the low-density core material.
	F1 monocoque chassis due to their excellent energy absorption which is critical for safety (O’Rourke,1990).
Complex geometries (underfloor and bodywork) due to mouldability.

	Natural Fibres (Flax)
	Derived from plant-based sources (such as Linum usitatissimum for flax), so are biodegradable, renewable, widely available and low cost per unit volume (Pickering, 2016).
	Interior components due to ability to absorb sound and vibration, as well as their capacity to withstand bending loads (Rajak et al, 2019).

	Synthetic Fibres (Kevlar)
	Human made fibres produced through chemical synthesis (Rajak et al, 2019).
Kevlar is known for high tensile strength and good impact resistance. 
	Crash structures where energy absorption is important.
Fuel tanks and protective layers within composite panels, where resistance to impact helps improve safety. 





[bookmark: _Toc228108697]Manufacturing Processes

[bookmark: _Toc228108748]Table 2 - Comparing differing composite manufacturing types using literature from Rajak et al (2019) and Rusnakova (1970).
	Manufacturing Type
	Description
	Advantages
	Disadvantages

	Pre-impregnation

	Fibres are pre-impregnated with resin and require heat and pressure (autoclave or oven) to cure.
	High consistency and fibre volume fractions, low void content.
	High cost due to specialised equipment such as the autoclave, also time consuming so not suitable for rapid production.

	Vacuum bag moulding
	A sealed vacuum bag is applied over the laminate to compress layers and remove air during curing.
	Improves fibre-resin interaction and reduces defects.
	Risk of leaks and less consistent than pre-impregnation. 

	Resin Infusion
	Dry fibres are place into a mould, sealed with a vacuum bag, and resin introduced under vacuum pressure.
	Reduced emissions due to closed mould system, as well as being practical for large-scale productions.
	Complex set up due to sealing and vacuum checks, also high initial costs due to the requirement of specialised equipment.

	Wet lay
	Manually placing fibres into a mould and applying resin using brushes or rollers.
	Cost effective as requires minimal investment in equipment and tooling, as well as its immediate application enabling on-the-spot repairs.
	Variability in resin distribution, with higher void content due to risk of air entrapment. Also limited quality control as uniformity is difficult.



[bookmark: _Toc228108698]Material Properties
The mechanical behaviour of materials is characterised using a stress-strain curve, which provides insight into key properties (Clyne and Hull, 2019).
[image: Schematic representation of a typical polymer stress-strain curve. ]
[bookmark: _Toc228108728]Figure 2 - Typical stress-strain curve for a polymer (Li et al, 2017).
Qualitest (2025) explains the initial linear region represents elastic deformation, with its gradient defining stiffness (Young’s Modulus). Deviations from linearity show plastic deformation in ductile materials, whilst brittle materials fail at minimal strain. The area under the curve represents toughness (energy absorption), critical in motorsport for impact resistance and structural integrity. 
[bookmark: _Toc228108699]Young’s Modulus
In fibre composites, stiffness is governed by the reinforcing fibres, with carbon fibres producing higher modulus values than natural fibres including flax (Clyne and Hull, 2019), resulting in carbon fibre composites demonstrating superior resistance to deformation under load.
[bookmark: _Toc228108700]Tensile Strength (UTS)
UTS represents the maximum stress a material can withstand before failure, indicating its load-carrying capability. Carbon fibre composites produce high tensile strength due to strong fibre bonding and alignment, whereas flax composites show lower strength due to fibre variability and weaker fibre-matrix interaction (Pickering, 2016). Fibre orientation and defects can significantly influence tensile performance (Rajak et al, 2019).
[bookmark: _Toc228108701]Failure Strain
Failure strain indicates failure behaviour, with higher strain values corresponding to ductile materials. Fibre composites show linear elastic behaviour followed by brittle failure, due to limited plastic deformation in fibres and matrix (Clyne and Hull, 2019). Ductile metals demonstrate a distinct yield point and an extended plastic region prior to failure (demonstrated by aluminium) (Ashby, 2025).

[bookmark: _Toc228108702]Sustainability Analysis 

The increasing pressure on motorsport to improve environmental performance has led to growing interest in sustainable material selection.
[bookmark: _Toc228108703]Life Cycle Analysis
A Life Cycle Assessment (LCA) is used to quantify the environmental impact of materials across their lifespan (figure 3 by Barbhuiya, 2023). Sectors including transportation and manufacturing contribute significantly to global greenhouse gas emissions, with manufacturing alone accounting for approximately 30% of emissions (Ramachandran, 2023). 
[image: Life Cycle Assessment (LCA), the key to a sustainable energy storage ...]
[bookmark: _Toc228108729]Figure 3 - Life-cycle assessment process (Mi, 2024).
[image: The diagram illustrates a comparison of environmental impacts, measured in various units, of carbon fiber composites and biocomposites, showing differences in factors such as eco-toxicity, energy use, and contributions to global warming potential.

AI-generated content may be incorrect.]
[bookmark: _Toc228108730]Figure 4 - Environmental Analysis of carbon fibre composites and bio composites (Ramachandran, 2023).
A study by Ramachandran (2023) compares carbon fibre composites and bio composites. Carbon fibre composites produce higher global warming potential, with values of approximately 54.3 kgCO₂Eq compared to 12.5 kgCO₂Eq for bio composites (Ramachandran, 2023). This is reflected across energy consumption (1100 MJ vs 203 MJ), acidification and human toxicity (figure 4). This is attributed to the high energy carbonisation process in carbon fibre production. However, bio composites show increased eco-toxicity and eutrophication impacts, which are associated with fertiliser and pesticide use. This highlights the need for investigations into the lifecycle of materials to understand their environmental impact if adopted in motorsport, to conform to the EU End-of-Life Vehicles Regulation (European Parliament, 2025), which states that vehicles are designed for disassembly and sets recycled material targets across the full vehicle lifecycle.
[bookmark: _Toc228108704]Raw Material Extraction

[bookmark: _Toc228108749]Table 3 – Comparing the sustainability of differing fibre types in the raw material extraction stage.
	Carbon Fibre
	Flax Fibre
	Kevlar

	Rely on polyacrylonitrile (PAN), a petroleum-derived precursor making carbon fibre dependent on non-renewable resources. (Ramachandran (2023)
	Derived from renewable plant sources, reducing reliance on fossil fuels and lower energy requirements
(Ramachandran, 2023).
	Derived from petrochemical sources and requires high energy processing, resulting in resource depletion (Heqin, 2026).

	Extraction of these materials contribute to high energy demand and greenhouse gases. (Ramachandran, 2023)
	Agricultural production -introduce environmental concerns including fertiliser and pesticide use, contributing to water pollution and soil degradation (Ramesh, 2020).
	Relies on fossil-based chains with harmful environmental risks. 

	Environmental damage including habitat destruction associated with oil extraction, such as spills that contribute to biodiversity loss.
	Land use for crops can lead to deforestation and biodiversity loss (Ramesh, 2020).
	




[bookmark: _Toc228108705]Manufacturing

[bookmark: _Toc228108750]Table 4 - Comparing the sustainability of differing fibre types in the manufacturing stage.
	Carbon Fibre
	Flax Fibre
	Kevlar

	Carbonisation of PAN fibres requires temperatures exceeding 1000 degrees which increases energy consumption and high toxicity levels (Li, 2021).
	Reduced energy demand due to lower processing temperatures.
	High energy polymerisation and fibre spinning processes contribute to environmental harm.

	Autoclave curing can increase energy demand due to high pressure and temperature requirements. 
	Wet spinning and resin curing contribute to emissions (Ramachandran, 2023).
	Difficult to process due to fibre toughness.

	Non-woven and random fibre composites are easier and cheaper to produce (Li, 2021).
	Variability in fibre quality leads to increased material waste during manufacturing (Ramachandran, 2023).
	



[bookmark: _Toc228108706]Material Use

[bookmark: _Toc228108751]Table 5 - Comparing the sustainability of differing fibre types in the material use stage.
	Carbon Fibre
	Flax Fibre
	Kevlar

	High strength to weight ratio enables mass reduction, improving fuel efficiency and operational emissions (Duflou et al, 2012).
	Improved vibration damping and reduced noise, improving vehicle efficiency. (Pickering et al, 2016)
	Lower compressive strength compared to carbon fibre limits use in primary structural components.

	Expensive repairs due to delamination requiring specialised inspection and repair techniques (Mallick, 2007).
	Lower mechanical performance limits their application to non-structural components. 
	High impact resistance and energy absorption allows for use in safety-critical components.

	Mechanical performance allows use in structural components.
	Moisture sensitivity reduces long-term durability. 
	





[bookmark: _Toc228108707]Recycling and end-of-life disposal

[bookmark: _Toc228108752]Table 6 - Comparing the sustainability of differing fibre types in recycling and end-of-life disposal stage.
	Carbon Fibre
	Flax Fibre
	Kevlar

	Thermoset resins within carbon fibre composites cannot be remelted or recycled (Li, 2021).
	Biodegradable and reduce long-term environmental impact, reducing long-term environmental persistence (Ramesh, 2020).
	High durability and resistance to degradation resulting in long environmental persistence.

	Disposed of through landfills or incineration, contributing to environmental pollution (Ramachandran, 2023).
	The synthetic resins within bio composites limits full biodegradability, meaning they cannot be completely composted (Ramesh, 2020).
	Limited recycling options mean that Kevlar-based composites are also commonly disposed of through landfill (Heqin, 2026).


	Pyrolysis recycling method - energy intensive and results in reduced fibre quality, limiting reuse in high-performance application (Li, 2021).
	Can be incinerated for energy recovery, improving environmental impact.
	



When considering all lifecycle stages, flax fibre demonstrates the strongest sustainability, benefiting from renewable sourcing and biodegradability at extraction and end-of-life stages. However, its reliance on synthetic resins limits full biodegradability. Carbon fibre provides sustainability benefits during the use stage through mass reduction and improved fuel efficiency (Duflou et al., 2012), however, its high energy carbonisation process and poor recyclability result in the greatest environmental impact, making it difficult to justify under FIA net-zero targets despite its mechanical superiority. No material satisfies all lifecycle stages, highlighting the need for development of hybrid and thermoplastic matrix systems (chapter 6.1), to meet the requirements of the EU End-of-Life Vehicles Regulation (European Parliament, 2025) and FIA net-zero targets (FIA, 2023).
[bookmark: _Toc228108708]Legislations
Motorsport is influenced by sustainability regulations that aim to reduce environmental impact. F1 (2019) explains that the FIA and Formula 1 have introduced the goal to achieve net-zero carbon emissions by 2030, covering cars, on-track activity, manufacturing and operational processes. This is supported by the FIA’s broader sustainability strategy, promoting carbon reduction and sustainable material use across motorsport (FIA, 2023). This impacts material selection as whilst carbon fibre offers desirable mechanical properties (discussed in chapter 5), it has poor sustainability with limited recyclability. Biocomposites including flax and bioresins align closer with the net-zero goal due to their lower carbon footprint, demonstrating the potential for incorporation in the new sustainable era. Future regulations are likely to drive the development of these materials to enhance their mechanical properties making them an improved replacement to carbon fibre. Furthermore, optimising manufacturing processes, such as reducing energy consumption in autoclave curing or increasing the use of resin infusion techniques, can further minimise environmental impact (Duflou, 2012).  Recycling methods such as pyrolysis may also be utilised to recover carbon fibres.
[bookmark: _Toc228108709]Feasibility of introducing sustainable alternatives in motorsport
There are limitations to sustainable implementations as addressed by Oliveux (2015), with the main barrier being cost. Carbon fibre has a well-established supply chain, enabling consistent quality and predictable production costs. Sustainable alternatives require additional processing, enhanced quality control, and extensive material validation, increasing manufacturing complexity and cost. Transitioning to bioresins may require modifications to existing production processes and to meet strict motorsport safety standards, introducing significant financial and time-related limitations.


[bookmark: _Toc228108710]Methodology 

Using the Denison Test Equipment (figure 5), a tensile test was conducted to evaluate the properties of different composite materials as displayed in table 7.[bookmark: _Toc228108753]Table 7 - Materials tested in the experimental test, with their cross-sectional area (mm^2).

[image: ][image: ]

[bookmark: _Toc228108731]Figure 5 - Experimental image of the Denison tensile testing machine.


Hatton (2019) states that the lay-up and orientation of fibres impact the composites’ mechanical properties. The twill materials consisted of 3 layers of 200g carbon and flax twill, resulting in 600g for each laminate. These plies were placed at 45 degrees, meaning the sample is not perfectly unidirectional. The non-woven materials consisted of 1 layer of 300g non-woven flax and carbon. 
The Denison tensile testing machine outputted each materials properties using the following equations:

[bookmark: _Toc228108757]Equation 1 - Stress.

[bookmark: _Toc228108758]Equation 2 - Strain.

[bookmark: _Toc228108759]Equation 3 - Youngs Modulus.
[bookmark: _Toc228108711]Validation Example
Easy Composites (EZ) datasheets were provided for each material and used to obtain expected values of Young’s Modulus and Ultimate Tensile Strength (UTS). 
However, for the carbon woven composites, the datasheets provided the properties for the fibre and matrix separately, and so a Law of Mixtures calculation was required to determine the range of Young’s Modulus expected for these laminates. 
[bookmark: _Toc228108712]Law of Mixtures
A fibre volume fraction of 50% was assumed for the carbon composites, as specified in the testing methodology. The Young’s Modulus of the carbon fibre was taken as 234 GPa from the supplier datasheet (3000K filaments), while the epoxy resin was taken as 3.3 GPa (converted from average of 3300 M N/mm^2).

[bookmark: _Toc228108760]Equation 4 - Youngs Modulus Upper Limit calculation.

[bookmark: _Toc228108761]Equation 5 - Youngs Modulus Lower Limit calculation.
Carbon Epoxy:

[bookmark: _Toc228108762]Equation 6 - Experimental carbon epoxy upper limit calculation.

[bookmark: _Toc228108763]Equation 7 - Experimental carbon epoxy lower limit calculation.
The same method was applied for both woven epoxy and bioresins, with full calculations for the Bioresin in the appendix.


[bookmark: _Toc228108713]Experimental Results and Analysis

Table 8 highlights agreement and deviation between experimental and manufacturer data. The carbon woven bioresin results show good alignment with expected ranges for UTS and Young’s Modulus. The carbon non-woven bioresin exhibits lower UTS and stiffness than the datasheet values, likely due to inaccuracies in lay-up orientation and fibre distribution during manufacturing, reducing load transfer efficiency. (Clyne and Hull, 2019) Flax composites show lower stiffness values consistent with the datasheet, however, the experimental UTS values are higher. This can be attributed to variations in fibre volume fraction, specimen quality, or testing conditions, particularly in natural fibre composites where material variability is inherently higher (Pickering, 2016). 
The greater deviation in UTS compared to Young’s Modulus can be explained by the sensitivity of failure to material defects. Young’s Modulus is determined from the initial elastic region, where the material remains unaffected by defects, whereas UTS depends on the onset of failure, which is influenced by fibre distribution and material variability (Callister and Rethwisch, 2021).
[bookmark: _Toc228108754]Table 8 - Comparing the materials UTS and Youngs Modulus to reference data sheets, whilst also displaying experimental failure strain of each material (EZ Composites; Oliwa, 2020; Smiths, 2023).
[image: The table lists various composites and their tensile strength (UTS) and failure strain percentages (YM), comparing the performance of aluminum, carbon-epoxy, carbon-woven bio, carbon-non-woven bio, and Kevlar materials.
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Deviations between experimental and EZ composite values can be attributed to the differing layup and manufacturing processes. For example, EZ composites states that the carbon non-woven bioresin laminate was hand laid-up with 70:30 fibre-fraction volume, compared to the experimental being 50:50 resin infused.
[bookmark: _Toc228108714]Test Observations
Figure 6 shows aluminium with a central fracture and clear necking. Agreeing with literature, Callister and Rethwisch (2021) explains ductile materials plastic deformation localises before fracture. Composite materials show few signs of necking, suggesting sudden, brittle fracture with delamination between plies.
[image: ]
[bookmark: _Toc228108732]Figure 6 - Materials post failure left to right Aluminium 1050A, Carbon Fibre Non-Woven Bio, Carbon Fibre Woven Bio, Flax Woven Bio, Flax Non-Woven Bio, Carbon Fibre Woven Epoxy, Kevlar.
The woven composites, as expected, show non-uniform fractures with uneven breaks, explained by their intertwined fibres in multiple directions, causing crack propagation to follow complex paths (Clyne and Hull, 2019).
[bookmark: _Toc228108715]Mechanical Behaviour
[bookmark: _Toc228108716]Aluminium Baseline
Aluminium 1050 was tested as a baseline due to its well reported mechanical properties and typical ductile behaviour. As an isotropic metal, it provides a clear comparison to fibre-reinforced composites which are anisotropic and result in brittle failure (Mallick, 2007). 

[bookmark: _Toc228108733]Figure 7 - Aluminium stress-strain sample comparison (experimental results).
Figure 7 demonstrates all three samples producing a short elastic region which, as supported by Bhuyan (2025), means that aluminium undergoes little strain before yielding. The long elongation phase is a direct response to aluminium’s high ductility, reaching approximately 20% strain before failing. This is higher than the composite materials which reach 4.46% (table 8). This occurs due to dislocation movement within the aluminium face-centred cubic lattice, allowing the material to deform plastically under load (Bell, 1965). As a result, aluminium can absorb significant energy prior to fracture, making it suitable for applications requiring deformation and energy absorption, such as crash structures in motorsport.

[image: ]
[bookmark: _Toc228108734]Figure 8 - Literature stress-strain curve for aluminium (Chen, 2014).
Comparing to literature (figure 8), there is a clear agreement in trends, with the transition from elastic to plastic behaviour occurring within 0.5% strain for literature (Chen, 2014) and experimental data. However, the UTS proves below literature, with collated data being 114.89 MPa, compared to approximately 200 MPa by Chen, (2014). This is explained by the literature using 7075 aluminium alloy compared to the experimental test using aluminium 1050 (as explained in the appendix). This is supported by Smiths data sheet confirming UTS of aluminium 1050 being between 100-135 MPa. Furthermore, gripping conditions in the Denison tensile test can result in a reduce stress measurement, especially due to only 3 samples investigated. 
[bookmark: _Toc228108717]Carbon Woven Bioresin
Contrasting from aluminium’s ductile behaviour, carbon woven bioresin shows brittle behaviour failing at approximately 2% strain. However, the composite achieves a higher UTS, exceeding 400 MPa, which is consistent with literature by Tosto (2024) (figure 10), where carbon fibre composites demonstrate high stiffness and strength but limited strain to failure (Callister and Rethwisch, 2020).

[bookmark: _Toc228108735]Figure 9 - Carbon Woven bioresin stress-strain sample comparison (experimental results).
[image: ]
[bookmark: _Toc228108736]Figure 10 - Literature carbon epoxy stress strain curve (Tosto, 2024).
The low strain is governed by the carbon fibres, which have strong covalent bonds. This results in high stiffness but restricts plastic deformation, causing failure to occur through bonds breaking rather than continuous yielding (Mallick, 2007). Additionally, as supported by the differing stress-strain curves between literature of aluminium and carbon fibre (figures 8 & 10), the polymer matrix in the composite limits the ductility due to its high cross-linked structure reducing plastic deformation (Callister and Rethwisch, 2021). The gradual stress increase between 0.5-2% strain indicates stable load transfer between fibres with desirable structural integrity under loading, consistent with carbon fibres high durability. 
[bookmark: _Toc228108718]Fibre Comparison
Carbon fibre shows the highest UTS due to its aligned covalent carbon bonds which require high forces to fail (Bhuyan, 2025). Kevlar, whilst achieving a lower UTS, has greater failure strain as its polymer chains are linked by weaker hydrogen bonds, allowing more energy absorption before failure (Heqin, 2026). Flax achieves the lowest UTS due to its natural variability in fibre properties, resulting in poor bonding and inefficient load transfer (Foulk, 2009). This deficit is still observed in non-woven carbon vs flax (as shown in the appendix), confirming this trade-off between fibres, regardless of weave arrangement. This suggests flax is yet to become a desired replacement to carbon fibre, despite its sustainable properties mention in chapter 3. 

[bookmark: _Toc228108737]Figure 11 – Comparing the experimental stress-strain curves of different Woven Bioresin fibres (Carbon, Flax and Kevlar).
The Young’s Modulus values in table 8 and demonstrated in figure 11 show a clear dependence on fibre type, with carbon fibre composites showing the highest stiffness. This is consistent with The Department of Materials Science and Metallurgy - University of Cambridge (2026) (figure 12), where carbon fibre composites occupy a high stiffness region compared to natural fibres. However, the Ashby chart illustrates that composite stiffness is lower than individual carbon fibres due to the influence of polymer matrix and fibre orientation, which reduces the overall modulus (Callister and Rethwisch, 2021). The overlap between Kevlar and carbon fibre composites indicates that stiffness is not solely governed by fibre type but is dependent on factors including fibre alignment and volume fraction. 
[image: ]
[bookmark: _Toc228108738]Figure 12 - Ashby chart comparing the Youngs Modulus of differing composites (Department of Materials Science and Metallurgy - University of Cambridge, 2026)
[bookmark: _Toc228108719]Weave Comparison
Figure 13 shows carbon woven bioresin achieving a higher UTS than carbon non-woven. This is expected, as woven fibres provide controlled and continuous load paths, allowing stress to be transferred efficiently through the laminate (Mallick, 2007). The non-woven material contains randomly orientated shorter fibres, meaning load transfer is less efficient and failure occurs at a much lower stress. Agreeing with literature which explains that fibre orientation and continuity influence composite strength and stiffness (Clyne and Hull, 2019).

[bookmark: _Toc228108739]Figure 13 - Comparing woven and non-woven carbon fibres stress-strain curve.
The failure strain remains similar (woven with 2% and non-woven with 2.27%), suggesting that weave pattern has a greater influence on load-carrying capacity than elongation. This is supported by Mallick (2007), where strain is less sensitive to fibre alignment and more dependent on the behaviour of the fibre-matrix system. The large difference in strength may be influenced by the methodology, as the woven laminates used three 200 g layers, whereas the non-woven laminates used only one 300 g layer, meaning the comparison is not purely based on woven type but also the total fibre content. However, the flax woven and non-woven comparison proves less prominent (graph shown in the appendix), with only a 2.51% UTS increase between the two, suggesting the manufacturing process inaccuracies have a large impact on figure 13 deviation. 
[bookmark: _Toc228108720]Resin Comparison
Figure 14 shows a small difference (10% difference in UTS) between epoxy and bioresin in carbon fibre, with the bioresin producing a higher UTS. This contradicts literature, where epoxy systems are expected to provide superior mechanical performance due to their higher stiffness and stronger fibre-matrix bonding (Callister and Rethwisch, 2021). However, the minimal difference observed supports the understanding that composite strength is governed by the fibres rather than the matrix, as explained in chapter 2.1.1. This suggests that bioresin is an appropriate sustainable replacement for epoxy, conforming with the EU End-of-Life Vehicles Directive (European Commission, 2000), which requires manufacturers to reduce hazardous substances and improve material recyclability across the automotive industry.

[bookmark: _Toc228108740]Figure 14 – Comparing stress-strain curves of resin types (epoxy and bioresin) of carbon fibres.
The small variation between the two curves can be attributed to experimental factors such as inconsistencies in resin-infusion through uneven resin flow, due to a lack of resin control. This is supported by Shen et al (2024a) explaining variability is still seen in fibre volume fraction for resin-infused processes compared to pre-impregnated manufacturing methods. As a result, the difference may not be statistically significant and requires a larger sample size to draw conclusions (chapter 5.6).
[bookmark: _Toc228108721]Variation Study
To enable a fair comparison of variability across materials with different values, the coefficient of variation (CoV) was used. Unlike standard deviation, CoV normalises variability relative to the mean, providing a more representative measure of consistency (Feng, 2011). Table 9 shows that for UTS, carbon woven bioresin and flax non-woven bioresin produce the highest coefficient of variation, whereas for Young’s Modulus, the greatest variation is seen in both non-woven fibres. 
[bookmark: _Toc228108755]Table 9 - Comparing the experimental UTS and Young's Modulus across the full 20 sample set, excluding samples which prove error ridden and unrealistic.
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The increased variability in non-woven composites is expected as their random fibre orientation results in inconsistent load paths and uneven stress distribution, leading to greater deviations in mechanical properties (Clyne and Hull, 2019). Woven composites provide a controlled fibre alignment, and so the unexpected increase in variation for the UTS of carbon woven is attributed to manufacturing factors including the layer alignment of 45 degrees, which is more complex and creates an increased chance of misalignment and uneven resin distribution. This is supported by the wide range between minimum and maximum values, indicating that small differences in lay-up quality can significantly influence failure behaviour.
In terms of fibre type, flax composites produce the highest overall variability, which is consistent with literature describing the inherent inconsistency of natural fibres due to variations in fibre quality and extraction processes (Pickering et al, 2016).
[bookmark: _Toc228108722]Limitations of the test
While resin infusion improves consistency, full control over resin distribution and fibre wetting is not guaranteed, which may introduce local variations in fibre volume fraction (Oliveux, 2015). Inaccuracies in cross-sectional area measurement can influence calculated stress values due to the relationship (equation 1), meaning small measurement errors may lead to poor estimations of UTS (Gauber, 2000). The small sample size reduces the statistical reliability of the results with coefficient of variation values above 50% suggesting that deviations are not solely due to material behaviour, but rather the sample preparation.


[bookmark: _Toc228108723]Conclusion
The experimental results demonstrate fibre type as the dominant factor influencing tensile behaviour, with carbon fibre composites achieving UTS values of 370-410 MPa, compared to 70-90 MPa for flax. The weave type was the second most influential factor, with woven configurations outperforming non-woven due to improved load transfer through continuous fibre paths. Resin type showed minimal influence, with only a 10% variation between epoxy and bioresin systems, confirming that tensile behaviour is primarily fibre-dominated and bioresin is an appropriate sustainable alternative for epoxy.
[bookmark: _Toc228108724]Recommendations and Sustainable Developments
Table 10 demonstrates that no material achieves optimal performance across all criteria, confirming material selection requires compromise. Carbon fibre composites provide superior strength and stiffness but are associated with high energy consumption and poor recyclability (54 kgCO₂Eq), making them most suitable for high-performance structural applications including monocoque chassis. Flax composites offer improved sustainability (12.5 kgCO₂Eq) and higher failure strain, but their reduced strength (79% reduction in UTS according to experimental results) limits their use in structural components. 
[bookmark: _Toc228108756]Table 10 - Performance and sustainability trade-offs across composites, scored out of 5 based on experimental results, LCA analysis, feasibility section and literature (chapters 3 and 5).
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Building on the findings of this report, future development of thermoplastic matrix composites, such as biodegradable polylactic acid (PLA) would address epoxy and bioresins poor end-of-life issues, as thermoplastics can be reprocessed and remelted, improving recyclability (Oliveux et al., 2015). The observed trade-off between carbon fibre strength and flax sustainability leads to investigation into hybrid carbon-flax composites, retaining carbon fibre in primary load-bearing plies, whilst incorporating flax in secondary layers to reduce overall environmental impact without compromising structural performance (Ramesh, 2020).
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[bookmark: _Toc228108741]Figure 15 - Comparing stress-strain curves of flax woven and non-woven.

[bookmark: _Toc228108742]Figure 16 – Carbon Woven Epoxy stress-strain sample comparison (experimental results).

[bookmark: _Toc228108743]Figure 17 - Carbon Non-Woven bioresin stress-strain sample comparison (experimental results).

[bookmark: _Toc228108744]Figure 18 -Flax Woven bioresin stress-strain sample comparison (experimental results).

[bookmark: _Toc228108745]Figure 19 - Flax Non-Woven bioresin stress-strain sample comparison (experimental results).
[image: The image displays a technical specification sheet for a 1050A aluminum alloy sheet, detailing its chemical composition, mechanical properties, and performance characteristics.

AI-generated content may be incorrect.]
[bookmark: _Toc228108746]Figure 20 - Smiths (2023) 1050 Aluminium datasheet.
Figure 20 consolidates aluminium 1050 as the material used in the experimental test with a tensile strength range of 100–135 N/mm^2, consistent with the experimental UTS of 114.89 MPa recorded in this report.
Aluminium Stress vs Strain Comparison between samples

Sample 1	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	0	0	0	0	1E-3	1E-3	1E-3	0	0	0	0	0	0	1E-3	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	0	1E-3	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-2E-3	-2E-3	-2E-3	-2E-3	-1E-3	-1E-3	-1E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-3.0000000000000001E-3	-3.0000000000000001E-3	-3.0000000000000001E-3	-3.0000000000000001E-3	-3.0000000000000001E-3	-3.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-5.0000000000000001E-3	-5.0000000000000001E-3	-5.0000000000000001E-3	-5.0000000000000001E-3	-5.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-7.0000000000000001E-3	-7.0000000000000001E-3	-7.0000000000000001E-3	-7.0000000000000001E-3	-7.0000000000000001E-3	-8.0000000000000002E-3	-8.0000000000000002E-3	-8.0000000000000002E-3	-8.0000000000000002E-3	-8.0000000000000002E-3	-8.0000000000000002E-3	-8.9999999999999993E-3	-8.9999999999999993E-3	-8.9999999999999993E-3	-8.9999999999999993E-3	-8.9999999999999993E-3	-8.9999999999999993E-3	-8.9999999999999993E-3	-0.01	-0.01	-0.01	-0.01	-0.01	-0.01	-0.01	-0.01	-1.0999999999999999E-2	-1.0999999999999999E-2	-1.0999999999999999E-2	-1.0999999999999999E-2	-1.0999999999999999E-2	-1.0999999999999999E-2	-1.2E-2	-1.2E-2	-1.2E-2	-1.2E-2	-1.2E-2	-1.2E-2	-1.2E-2	-1.2999999999999999E-2	-1.2999999999999999E-2	-1.2999999999999999E-2	-1.2999999999999999E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4999999999999999E-2	-1.4999999999999999E-2	-1.4999999999999999E-2	-1.4999999999999999E-2	-1.4999999999999999E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.7000000000000001E-2	-1.7000000000000001E-2	-1.7000000000000001E-2	-1.7000000000000001E-2	-1.7000000000000001E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.9E-2	-1.9E-2	-1.9E-2	-1.9E-2	-1.9E-2	-0.02	-0.02	-0.02	-0.02	-0.02	-0.02	-0.02	-0.02	-0.02	-0.02	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.4E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.3E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1999999999999999E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-2.1000000000000001E-2	-0.02	-0.02	-0.02	-0.02	-0.02	-1.9E-2	-1.9E-2	-1.9E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7999999999999999E-2	-1.7000000000000001E-2	-1.7000000000000001E-2	-1.7000000000000001E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.6E-2	-1.4999999999999999E-2	-1.4999999999999999E-2	-1.4999999999999999E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.4E-2	-1.2999999999999999E-2	-1.2999999999999999E-2	-1.2E-2	-1.2E-2	-1.2E-2	-1.0999999999999999E-2	-1.0999999999999999E-2	-1.0999999999999999E-2	-0.01	-0.01	-0.01	-8.9999999999999993E-3	-8.9999999999999993E-3	-8.0000000000000002E-3	-8.0000000000000002E-3	-8.0000000000000002E-3	-7.0000000000000001E-3	-7.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-6.0000000000000001E-3	-5.0000000000000001E-3	-5.0000000000000001E-3	-4.0000000000000001E-3	-4.0000000000000001E-3	-3.0000000000000001E-3	-3.0000000000000001E-3	-2E-3	-2E-3	-2E-3	-1E-3	0	0	0	1E-3	1E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.9E-2	1.9E-2	0.02	0.02	0.02	2.1000000000000001E-2	2.1000000000000001E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.3E-2	2.3E-2	2.4E-2	2.4E-2	2.4E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.7E-2	2.7E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.9000000000000001E-2	2.9000000000000001E-2	0.03	0.03	0.03	3.1E-2	3.1E-2	3.2000000000000001E-2	3.2000000000000001E-2	3.2000000000000001E-2	3.3000000000000002E-2	3.3000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5999999999999997E-2	3.5999999999999997E-2	3.5999999999999997E-2	3.6999999999999998E-2	3.6999999999999998E-2	3.7999999999999999E-2	3.7999999999999999E-2	3.9E-2	3.9E-2	0.04	0.04	0.04	4.1000000000000002E-2	4.1000000000000002E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2999999999999997E-2	4.2999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.4999999999999998E-2	4.4999999999999998E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.7E-2	4.7E-2	4.8000000000000001E-2	4.8000000000000001E-2	4.8000000000000001E-2	4.9000000000000002E-2	0.05	0.05	0.05	5.0999999999999997E-2	5.1999999999999998E-2	5.1999999999999998E-2	5.2999999999999999E-2	5.2999999999999999E-2	5.3999999999999999E-2	5.3999999999999999E-2	5.5E-2	5.5E-2	5.6000000000000001E-2	5.6000000000000001E-2	5.7000000000000002E-2	5.8000000000000003E-2	5.8000000000000003E-2	5.8999999999999997E-2	5.8999999999999997E-2	0.06	0.06	6.0999999999999999E-2	6.2E-2	6.2E-2	6.3E-2	6.3E-2	6.4000000000000001E-2	6.4000000000000001E-2	6.5000000000000002E-2	6.6000000000000003E-2	6.6000000000000003E-2	6.7000000000000004E-2	6.8000000000000005E-2	6.8000000000000005E-2	6.9000000000000006E-2	7.0000000000000007E-2	7.0000000000000007E-2	7.0999999999999994E-2	7.0999999999999994E-2	7.1999999999999995E-2	7.1999999999999995E-2	7.2999999999999995E-2	7.3999999999999996E-2	7.3999999999999996E-2	7.4999999999999997E-2	7.5999999999999998E-2	7.5999999999999998E-2	7.6999999999999999E-2	7.8E-2	7.8E-2	7.9000000000000001E-2	0.08	0.08	8.1000000000000003E-2	8.2000000000000003E-2	8.2000000000000003E-2	8.3000000000000004E-2	8.4000000000000005E-2	8.4000000000000005E-2	8.5000000000000006E-2	8.5000000000000006E-2	8.5999999999999993E-2	8.5999999999999993E-2	8.6999999999999994E-2	8.7999999999999995E-2	8.7999999999999995E-2	8.8999999999999996E-2	0.09	0.09	9.0999999999999998E-2	9.1999999999999998E-2	9.1999999999999998E-2	9.2999999999999999E-2	9.4E-2	9.4E-2	9.5000000000000001E-2	9.6000000000000002E-2	9.6000000000000002E-2	9.7000000000000003E-2	9.8000000000000004E-2	9.8000000000000004E-2	9.9000000000000005E-2	9.9000000000000005E-2	0.1	0.10100000000000001	0.10100000000000001	0.10199999999999999	0.10299999999999999	0.10299999999999999	0.104	0.104	0.105	0.106	0.106	0.107	0.108	0.108	0.109	0.109	0.11	0.11	0.111	0.112	0.112	0.113	0.114	0.114	0.115	0.115	0.11600000000000001	0.11600000000000001	0.11700000000000001	0.11799999999999999	0.11799999999999999	0.11899999999999999	0.11899999999999999	0.12	0.12	0.121	0.122	0.122	0.123	0.123	0.124	0.124	0.125	0.126	0.126	0.127	0.127	0.128	0.128	0.129	0.13	0.13	0.13100000000000001	0.13100000000000001	0.13200000000000001	0.13200000000000001	0.13300000000000001	0.13400000000000001	0.13400000000000001	0.13500000000000001	0.13500000000000001	0.13600000000000001	0.13600000000000001	0.13700000000000001	0.13800000000000001	0.13800000000000001	0.13900000000000001	0.13900000000000001	0.14000000000000001	0.14000000000000001	0.14099999999999999	0.14199999999999999	0.14199999999999999	0.14199999999999999	0.14299999999999999	0.14399999999999999	0.14399999999999999	0.14499999999999999	0.14499999999999999	0.14599999999999999	0.14599999999999999	0.14699999999999999	0.14799999999999999	0.14799999999999999	0.14799999999999999	0.14899999999999999	0.14899999999999999	0.14899999999999999	0.15	0.15	0.15	0.15	0.15	0.15	0.15	0.15	0.15	0.15	0.15	0.15	0.15	0.151	0.152	0.152	0.153	0.154	0.155	0.155	0.156	0.157	0.158	0.158	0.159	0.16	0.16	0.161	0.16200000000000001	0.16200000000000001	0.16300000000000001	0.16400000000000001	0.16400000000000001	0.16500000000000001	0.16500000000000001	0.16600000000000001	0.16700000000000001	0.16700000000000001	0.16800000000000001	0.16800000000000001	0.16900000000000001	0.17	0.17	0.17100000000000001	0.17199999999999999	0.17199999999999999	0.17299999999999999	0.17299999999999999	0.17399999999999999	0.17399999999999999	0.17499999999999999	0.17599999999999999	0.17599999999999999	0.17699999999999999	0.17699999999999999	0.17799999999999999	0.17799999999999999	0.17899999999999999	0.18	0.18	0.18099999999999999	0.18099999999999999	0.182	0.182	0.183	0.184	0.184	0.184	0.185	0.186	0.186	0.187	0.187	0.188	0.188	0.189	0.19	0.19	0.19	0.191	0.192	0.192	0.193	0.193	0.19400000000000001	0.19400000000000001	0.19500000000000001	0.19500000000000001	0.19600000000000001	0.19600000000000001	0.19700000000000001	0.19700000000000001	0.19800000000000001	0.19800000000000001	0.19900000000000001	0.19900000000000001	0.2	0.2	0.20100000000000001	0.20200000000000001	0.20200000000000001	0.20200000000000001	0.20300000000000001	0.20399999999999999	0.20399999999999999	0.20399999999999999	0.20499999999999999	0.20599999999999999	0.20599999999999999	0.20599999999999999	0.20699999999999999	0.20799999999999999	0.20799999999999999	0.20899999999999999	0.20899999999999999	0.21	0.21	0.21	0.21099999999999999	0.21199999999999999	0.21199999999999999	0.21299999999999999	0.21299999999999999	0.214	0.214	0.215	0.215	0.216	0.216	0.217	0.217	0.218	0.218	0.218	0.219	0.22	0.22	0.221	0.221	0.222	0.222	0.223	0.223	0.224	0.224	0.22500000000000001	0.22500000000000001	0.22600000000000001	0.22600000000000001	0.22600000000000001	0.22700000000000001	0.22800000000000001	0.22800000000000001	0.22800000000000001	0.22900000000000001	0.23	0.23	0.23	0.23100000000000001	0.23200000000000001	0.23200000000000001	0.23200000000000001	0.23300000000000001	0.23400000000000001	0.23400000000000001	0.23400000000000001	0.23499999999999999	0.23499999999999999	0.23599999999999999	0.23599999999999999	0.23699999999999999	0.23799999999999999	0.23799999999999999	0.23799999999999999	0.23899999999999999	0.23899999999999999	0.24	0.24	0.24099999999999999	0.24099999999999999	0.24199999999999999	0.24199999999999999	0.24299999999999999	0.24399999999999999	0.24399999999999999	0.24399999999999999	0.245	0.245	0.246	0.246	0.247	0.247	0.248	0.248	0.249	0.25	0.25	0.25	0.251	0.251	0.252	0.252	0.253	0.254	0.254	0.254	0.255	0.25600000000000001	0.25600000000000001	0.25600000000000001	0.25700000000000001	0.25800000000000001	0.25800000000000001	0.25800000000000001	0.25900000000000001	0.26	0.26	0.26	0.26100000000000001	0.26200000000000001	0.26200000000000001	0.26200000000000001	0.26300000000000001	0.26400000000000001	0.26400000000000001	0.26400000000000001	0.26500000000000001	0.26500000000000001	0.26600000000000001	0.26600000000000001	0.26700000000000002	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26900000000000002	0.26900000000000002	0.27	0.27	0.27100000000000002	0.27100000000000002	0.27200000000000002	0.27200000000000002	0.27300000000000002	0.27300000000000002	0.27400000000000002	0.27400000000000002	0.27500000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27800000000000002	0.27800000000000002	0.27900000000000003	0.27900000000000003	0.28000000000000003	0.28000000000000003	0.28100000000000003	0.28100000000000003	0.28199999999999997	0.28199999999999997	0.28299999999999997	0.28299999999999997	0.28399999999999997	0.28399999999999997	0.28499999999999998	0.28499999999999998	0.28599999999999998	0.28599999999999998	0.28699999999999998	0.28699999999999998	0.28799999999999998	0.28799999999999998	0.28899999999999998	0.28899999999999998	0.28999999999999998	0.28999999999999998	0.29099999999999998	0.29099999999999998	0.29199999999999998	0.29199999999999998	0.29299999999999998	0.29299999999999998	0.29399999999999998	0.29399999999999998	0.29499999999999998	0.29499999999999998	0.29599999999999999	0.29599999999999999	0.29699999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.29899999999999999	0.3	0.3	0.30099999999999999	0.30099999999999999	0.30199999999999999	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30499999999999999	0.30499999999999999	0.30599999999999999	0.30599999999999999	0.307	0.307	0.308	0.308	0.308	0.309	0.31	0.31	0.311	0.311	0.312	0.312	0.313	0.313	0.314	0.314	0.314	0.315	0.316	0.316	0.316	0.317	0.318	0.318	0.31900000000000001	0.31900000000000001	0.32	0.32	0.32100000000000001	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32500000000000001	0.32500000000000001	0.32600000000000001	0.32600000000000001	0.32700000000000001	0.32700000000000001	0.32800000000000001	0.32800000000000001	0.32900000000000001	0.32900000000000001	0.33	0.33	0.33100000000000002	0.33100000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33300000000000002	0.33400000000000002	0.33400000000000002	0.33500000000000002	0.33500000000000002	0.33600000000000002	0.33600000000000002	0.33700000000000002	0.33700000000000002	0.33800000000000002	0.33800000000000002	0.33900000000000002	0.33900000000000002	0.34	0.34	0.34100000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34300000000000003	0.34300000000000003	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34799999999999998	0.34799999999999998	0.34799999999999998	0.34899999999999998	0.35	0.35	0.35	0.35099999999999998	0.35199999999999998	0.35199999999999998	0.35199999999999998	0.35299999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35499999999999998	0.35599999999999998	0.35599999999999998	0.35599999999999998	0.35699999999999998	0.35799999999999998	0.35799999999999998	0.35799999999999998	0.35799999999999998	0.36	0.36	0.36	0.36099999999999999	0.36199999999999999	0.36199999999999999	0.36299999999999999	0.36299999999999999	0.36399999999999999	0.36399999999999999	0.36499999999999999	0.36499999999999999	0.36599999999999999	0.36599999999999999	0.36699999999999999	0.36699999999999999	0.36799999999999999	0.36799999999999999	0.36899999999999999	0.36899999999999999	0.37	0.37	0.371	0.371	0.372	0.372	0.373	0.373	0.374	0.374	0.375	0.375	0.376	0.376	0.377	0.377	0.378	0.378	0.379	0.379	0.38	0.38	0.38100000000000001	0.38100000000000001	0.38200000000000001	0.38200000000000001	0.38300000000000001	0.38400000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38600000000000001	0.38600000000000001	0.38600000000000001	0.38700000000000001	0.38800000000000001	0.38800000000000001	0.38900000000000001	0.38900000000000001	0.39	0.39	0.39100000000000001	0.39100000000000001	0.39200000000000002	0.39200000000000002	0.39300000000000002	0.39300000000000002	0.39400000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39600000000000002	0.39600000000000002	0.39700000000000002	0.39700000000000002	0.39800000000000002	0.39800000000000002	0.39900000000000002	0.39900000000000002	0.4	0.4	0.40100000000000002	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40400000000000003	0.40400000000000003	0.40400000000000003	0.40500000000000003	0.40600000000000003	0.40600000000000003	0.40600000000000003	0.40699999999999997	0.40799999999999997	0.40799999999999997	0.40799999999999997	0.40899999999999997	0.41	0.41	0.41	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41299999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41499999999999998	0.41499999999999998	0.41599999999999998	0.41599999999999998	0.41699999999999998	0.41699999999999998	0.41799999999999998	0.41799999999999998	0.41899999999999998	0.41899999999999998	0.42	0.42	0.42099999999999999	0.42099999999999999	0.42199999999999999	0.42199999999999999	0.42299999999999999	0.42299999999999999	0.42399999999999999	0.42399999999999999	0.42499999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42699999999999999	0.42799999999999999	0.42799999999999999	0.42899999999999999	0.42899999999999999	0.43	0.43	0.43099999999999999	0.43099999999999999	0.432	0.432	0.433	0.433	0.434	0.434	0.435	0.436	0.436	0.436	0.437	0.438	0.438	0.438	0.439	0.44	0.44	0.44	0.441	0.442	0.442	0.443	0.443	0.44400000000000001	0.44400000000000001	0.44500000000000001	0.44500000000000001	0.44600000000000001	0.44600000000000001	0.44700000000000001	0.44700000000000001	0.44800000000000001	0.44800000000000001	0.44900000000000001	0.44900000000000001	0.45	0.45	0.45100000000000001	0.45100000000000001	0.45200000000000001	0.45200000000000001	0.45300000000000001	0.45300000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45700000000000002	0.45800000000000002	0.45800000000000002	0.45900000000000002	0.46	0.46	0.46	0.46100000000000002	0.46200000000000002	0.46200000000000002	0.46200000000000002	0.46300000000000002	0.46400000000000002	0.46400000000000002	0.46500000000000002	0.46500000000000002	0.46600000000000003	0.46600000000000003	0.46700000000000003	0.46700000000000003	0.46800000000000003	0.46800000000000003	0.46899999999999997	0.46899999999999997	0.47	0.47	0.47099999999999997	0.47099999999999997	0.47199999999999998	0.47199999999999998	0.47299999999999998	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47499999999999998	0.47499999999999998	0.47599999999999998	0.47599999999999998	0.47699999999999998	0.47699999999999998	0.47799999999999998	0.47799999999999998	0.47899999999999998	0.48	0.48	0.48	0.48099999999999998	0.48099999999999998	0.48199999999999998	0.48199999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48399999999999999	0.48499999999999999	0.48599999999999999	0.48599999999999999	0.48599999999999999	0.48699999999999999	0.48799999999999999	0.48799999999999999	0.48899999999999999	0.48899999999999999	0.49	0.49	0.49099999999999999	0.49099999999999999	0.49199999999999999	0.49199999999999999	0.49299999999999999	0.49299999999999999	0.49399999999999999	0.49399999999999999	0.495	0.495	0.5	0.5	0.5	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50800000000000001	0.50800000000000001	0.51	0.51	0.51400000000000001	0.51600000000000001	0.51800000000000002	0.52	0.52400000000000002	0.52800000000000002	0.53	0.53400000000000003	0.53800000000000003	0.54	0.54600000000000004	0.55000000000000004	0.55400000000000005	0.55800000000000005	0.56399999999999995	0.56799999999999995	0.57399999999999995	0.57799999999999996	0.58599999999999997	0.59	0.59799999999999998	0.60399999999999998	0.60799999999999998	0.61599999999999999	0.624	0.63	0.63800000000000001	0.64600000000000002	0.65	0.66	0.66800000000000004	0.67600000000000005	0.68600000000000005	0.69399999999999995	0.70399999999999996	0.71	0.72	0.73	0.74	0.75	0.76	0.77	0.78	0.79	0.80400000000000005	0.81399999999999995	0.82599999999999996	0.83599999999999997	0.84799999999999998	0.86	0.87	0.88600000000000001	0.89600000000000002	0.90800000000000003	0.92	0.93600000000000005	0.94799999999999995	0.96	0.97599999999999998	0.98799999999999999	1.004	1.018	1.03	1.046	1.06	1.0760000000000001	1.0940000000000001	1.1080000000000001	1.1240000000000001	1.1379999999999999	1.1559999999999999	1.17	1.1879999999999999	1.206	1.22	1.238	1.256	1.274	1.29	1.3080000000000001	1.3260000000000001	1.3460000000000001	1.3640000000000001	1.38	1.4	1.42	1.4379999999999999	1.458	1.478	1.498	1.518	1.538	1.5580000000000001	1.5780000000000001	1.5980000000000001	1.6180000000000001	1.6379999999999999	1.6579999999999999	1.6779999999999999	1.7	1.72	1.74	1.76	1.78	1.8	1.82	1.84	1.86	1.8779999999999999	1.8939999999999999	1.91	1.9339999999999999	1.954	1.974	1.994	2.0139999999999998	2.032	2.052	2.0720000000000001	2.0920000000000001	2.1160000000000001	2.1320000000000001	2.1560000000000001	2.1720000000000002	2.1960000000000002	2.2160000000000002	2.2360000000000002	2.2559999999999998	2.2759999999999998	2.2959999999999998	2.3159999999999998	2.3359999999999999	2.3559999999999999	2.3759999999999999	2.3959999999999999	2.4159999999999999	2.4359999999999999	2.456	2.476	2.496	2.516	2.536	2.556	2.5760000000000001	2.5960000000000001	2.6160000000000001	2.6360000000000001	2.6560000000000001	2.6760000000000002	2.6960000000000002	2.718	2.7360000000000002	2.758	2.778	2.7959999999999998	2.8180000000000001	2.8380000000000001	2.8580000000000001	2.8780000000000001	2.8980000000000001	2.9180000000000001	2.9380000000000002	2.9580000000000002	2.9780000000000002	2.9980000000000002	3.0179999999999998	3.0379999999999998	3.0579999999999998	3.0779999999999998	3.0979999999999999	3.12	3.14	3.16	3.18	3.2	3.22	3.24	3.26	3.28	3.3	3.32	3.34	3.3620000000000001	3.38	3.4020000000000001	3.4220000000000002	3.44	3.4620000000000002	3.4820000000000002	3.5	3.5219999999999998	3.5419999999999998	3.5619999999999998	3.5819999999999999	3.6019999999999999	3.6219999999999999	3.6419999999999999	3.6619999999999999	3.6819999999999999	3.702	3.722	3.742	3.762	3.782	3.802	3.8220000000000001	3.8420000000000001	3.8620000000000001	3.8820000000000001	3.9060000000000001	3.9220000000000002	3.9420000000000002	3.9620000000000002	3.9860000000000002	4.0019999999999998	4.024	4.0419999999999998	4.0640000000000001	4.0819999999999999	4.1020000000000003	4.1239999999999997	4.1440000000000001	4.1639999999999997	4.1840000000000002	4.2039999999999997	4.2240000000000002	4.2439999999999998	4.2640000000000002	4.2839999999999998	4.3040000000000003	4.3239999999999998	4.3440000000000003	4.3680000000000003	4.3840000000000003	4.4039999999999999	4.4279999999999999	4.4480000000000004	4.468	4.4880000000000004	4.508	4.5279999999999996	4.548	4.5679999999999996	4.5880000000000001	4.6079999999999997	4.6280000000000001	4.6479999999999997	4.67	4.6879999999999997	4.7080000000000002	4.7279999999999998	4.75	4.7679999999999998	4.7880000000000003	4.8099999999999996	4.8280000000000003	4.8499999999999996	4.87	4.8899999999999997	4.91	4.9279999999999999	4.95	4.97	4.99	5.01	5.03	5.048	5.07	5.09	5.1079999999999997	5.1280000000000001	5.1479999999999997	5.1680000000000001	5.1879999999999997	5.2080000000000002	5.2279999999999998	5.2480000000000002	5.2679999999999998	5.2880000000000003	5.3079999999999998	5.3280000000000003	5.3479999999999999	5.3680000000000003	5.3879999999999999	5.4080000000000004	5.4279999999999999	5.4480000000000004	5.468	5.4880000000000004	5.508	5.5279999999999996	5.548	5.5679999999999996	5.5880000000000001	5.6079999999999997	5.6280000000000001	5.6479999999999997	5.6680000000000001	5.6879999999999997	5.7080000000000002	5.7279999999999998	5.7480000000000002	5.7679999999999998	5.7880000000000003	5.8079999999999998	5.8280000000000003	5.8479999999999999	5.8680000000000003	5.8879999999999999	5.9080000000000004	5.9279999999999999	5.9480000000000004	5.968	5.9880000000000004	6.008	6.0259999999999998	6.0460000000000003	6.0659999999999998	6.0860000000000003	6.1059999999999999	6.1260000000000003	6.1459999999999999	6.1660000000000004	6.1859999999999999	6.2060000000000004	6.226	6.2460000000000004	6.266	6.2859999999999996	6.306	6.3259999999999996	6.3460000000000001	6.3659999999999997	6.3860000000000001	6.4059999999999997	6.4260000000000002	6.4459999999999997	6.4660000000000002	6.4859999999999998	6.5039999999999996	6.5259999999999998	6.5439999999999996	6.5659999999999998	6.5839999999999996	6.6040000000000001	6.6239999999999997	6.6459999999999999	6.6660000000000004	6.6840000000000002	6.7039999999999997	6.726	6.7439999999999998	6.7640000000000002	6.7839999999999998	6.8040000000000003	6.8239999999999998	6.8440000000000003	6.8639999999999999	6.8860000000000001	6.9039999999999999	6.9240000000000004	6.944	6.9640000000000004	6.984	7.0060000000000002	7.0259999999999998	7.0460000000000003	7.0659999999999998	7.0860000000000003	7.1059999999999999	7.1260000000000003	7.1459999999999999	7.1660000000000004	7.1859999999999999	7.2060000000000004	7.226	7.2460000000000004	7.266	7.2859999999999996	7.306	7.3259999999999996	7.35	7.37	7.39	7.41	7.43	7.45	7.47	7.49	7.51	7.53	7.55	7.57	7.59	7.61	7.63	7.65	7.67	7.69	7.71	7.73	7.75	7.77	7.79	7.81	7.83	7.85	7.87	7.89	7.91	7.93	7.95	7.97	7.99	8.01	8.0280000000000005	8.048	8.0679999999999996	8.0860000000000003	8.1080000000000005	8.1259999999999994	8.1479999999999997	8.1679999999999993	8.1880000000000006	8.2059999999999995	8.2260000000000009	8.2479999999999993	8.266	8.2859999999999996	8.3059999999999992	8.3260000000000005	8.3460000000000001	8.3659999999999997	8.3859999999999992	8.4060000000000006	8.4260000000000002	8.4459999999999997	8.4659999999999993	8.4860000000000007	8.5060000000000002	8.5259999999999998	8.5459999999999994	8.5660000000000007	8.5860000000000003	8.6059999999999999	8.6280000000000001	8.6460000000000008	8.6660000000000004	8.6859999999999999	8.7080000000000002	8.7260000000000009	8.7460000000000004	8.7680000000000007	8.7880000000000003	8.8059999999999992	8.8260000000000005	8.8480000000000008	8.8680000000000003	8.8879999999999999	8.9079999999999995	8.9280000000000008	8.9480000000000004	8.9659999999999993	8.9860000000000007	9.0060000000000002	9.0259999999999998	9.0459999999999994	9.0679999999999996	9.0879999999999992	9.1059999999999999	9.1280000000000001	9.1460000000000008	9.1660000000000004	9.1859999999999999	9.2059999999999995	9.2260000000000009	9.2460000000000004	9.266	9.2859999999999996	9.3059999999999992	9.3260000000000005	9.3460000000000001	9.3659999999999997	9.3859999999999992	9.4060000000000006	9.4260000000000002	9.4459999999999997	9.4659999999999993	9.4860000000000007	9.5060000000000002	9.5259999999999998	9.5459999999999994	9.5640000000000001	9.5860000000000003	9.6059999999999999	9.6259999999999994	9.6460000000000008	9.6660000000000004	9.6859999999999999	9.7059999999999995	9.7260000000000009	9.7460000000000004	9.766	9.7859999999999996	9.8059999999999992	9.8260000000000005	9.8460000000000001	9.8659999999999997	9.8859999999999992	9.9060000000000006	9.9260000000000002	9.9459999999999997	9.9659999999999993	9.9860000000000007	10.006	10.026	10.045999999999999	10.066000000000001	10.086	10.106	10.125999999999999	10.148	10.167999999999999	10.188000000000001	10.208	10.228	10.247999999999999	10.268000000000001	10.288	10.308	10.327999999999999	10.348000000000001	10.368	10.388	10.407999999999999	10.428000000000001	10.448	10.468	10.488	10.507999999999999	10.528	10.548	10.568	10.587999999999999	10.608000000000001	10.628	10.648	10.667999999999999	10.688000000000001	10.708	10.728	10.747999999999999	10.768000000000001	10.788	10.808	10.827999999999999	10.846	10.866	10.888	10.906000000000001	10.928000000000001	10.946	10.968	10.988	11.006	11.028	11.048	11.068	11.086	11.106	11.125999999999999	11.146000000000001	11.166	11.186	11.208	11.226000000000001	11.246	11.266	11.288	11.305999999999999	11.327999999999999	11.346	11.366	11.385999999999999	11.406000000000001	11.426	11.448	11.465999999999999	11.488	11.507999999999999	11.528	11.548	11.568	11.587999999999999	11.608000000000001	11.628	11.648	11.667999999999999	11.688000000000001	11.708	11.728	11.747999999999999	11.768000000000001	11.788	11.808	11.827999999999999	11.848000000000001	11.868	11.888	11.907999999999999	11.928000000000001	11.948	11.968	11.988	12.007999999999999	12.028	12.048	12.068	12.087999999999999	12.108000000000001	12.128	12.148	12.167999999999999	12.188000000000001	12.208	12.228	12.247999999999999	12.268000000000001	12.288	12.308	12.327999999999999	12.348000000000001	12.368	12.385999999999999	12.407999999999999	12.428000000000001	12.448	12.465999999999999	12.486000000000001	12.507999999999999	12.526	12.545999999999999	12.566000000000001	12.587999999999999	12.606	12.628	12.646000000000001	12.666	12.688000000000001	12.706	12.726000000000001	12.746	12.766	12.788	12.805999999999999	12.826000000000001	12.846	12.868	12.888	12.906000000000001	12.928000000000001	12.948	12.968	12.986000000000001	13.007999999999999	13.026	13.045999999999999	13.068	13.087999999999999	13.108000000000001	13.128	13.148	13.166	13.188000000000001	13.206	13.228	13.247999999999999	13.266	13.288	13.308	13.326000000000001	13.346	13.366	13.388	13.406000000000001	13.426	13.446	13.465999999999999	13.486000000000001	13.506	13.526	13.545999999999999	13.566000000000001	13.586	13.606	13.625999999999999	13.646000000000001	13.666	13.682	13.706	13.722	13.742000000000001	13.762	13.782	13.802	13.821999999999999	13.842000000000001	13.862	13.882	13.901999999999999	13.922000000000001	13.942	13.962	13.981999999999999	14.002000000000001	14.022	14.042	14.061999999999999	14.082000000000001	14.102	14.122	14.141999999999999	14.162000000000001	14.182	14.2	14.22	14.242000000000001	14.262	14.282	14.302	14.321999999999999	14.342000000000001	14.362	14.382	14.401999999999999	14.422000000000001	14.442	14.462	14.481999999999999	14.502000000000001	14.522	14.542	14.561999999999999	14.582000000000001	14.602	14.622	14.641999999999999	14.662000000000001	14.682	14.702	14.722	14.742000000000001	14.762	14.782	14.802	14.821999999999999	14.842000000000001	14.862	14.882	14.9	14.92	14.94	14.96	14.98	15	15.02	15.04	15.061999999999999	15.08	15.1	15.12	15.14	15.16	15.18	15.2	15.22	15.24	15.26	15.28	15.3	15.32	15.34	15.36	15.38	15.4	15.42	15.44	15.46	15.48	15.5	15.52	15.54	15.56	15.58	15.6	15.62	15.64	15.66	15.68	15.7	15.72	15.74	15.76	15.78	15.8	15.82	15.84	15.86	15.88	15.9	15.92	15.938000000000001	15.96	15.98	15.997999999999999	16.02	16.04	16.056000000000001	16.076000000000001	16.096	16.12	16.135999999999999	16.155999999999999	16.175999999999998	16.196000000000002	16.216000000000001	16.236000000000001	16.256	16.276	16.295999999999999	16.315999999999999	16.335999999999999	16.356000000000002	16.376000000000001	16.393999999999998	16.414000000000001	16.434000000000001	16.454000000000001	16.474	16.494	16.513999999999999	16.533999999999999	16.553999999999998	16.574000000000002	16.594000000000001	16.614000000000001	16.634	16.654	16.673999999999999	16.693999999999999	16.713999999999999	16.734000000000002	16.754000000000001	16.774000000000001	16.794	16.814	16.834	16.853999999999999	16.873999999999999	16.893999999999998	16.914000000000001	16.934000000000001	16.954000000000001	16.974	16.994	17.013999999999999	17.033999999999999	17.053999999999998	17.074000000000002	17.094000000000001	17.114000000000001	17.134	17.154	17.173999999999999	17.193999999999999	17.213999999999999	17.234000000000002	17.254000000000001	17.274000000000001	17.294	17.314	17.334	17.353999999999999	17.376000000000001	17.393999999999998	17.414000000000001	17.434000000000001	17.454000000000001	17.474	17.494	17.513999999999999	17.533999999999999	17.553999999999998	17.574000000000002	17.594000000000001	17.614000000000001	17.634	17.654	17.673999999999999	17.693999999999999	17.713999999999999	17.734000000000002	17.754000000000001	17.774000000000001	17.794	17.814	17.834	17.853999999999999	17.873999999999999	17.893999999999998	17.914000000000001	17.934000000000001	17.954000000000001	17.974	17.994	18.013999999999999	18.033999999999999	18.053999999999998	18.074000000000002	18.094000000000001	18.114000000000001	18.134	18.154	18.173999999999999	18.193999999999999	18.213999999999999	18.234000000000002	18.254000000000001	18.274000000000001	18.294	18.314	18.335999999999999	18.356000000000002	18.376000000000001	18.396000000000001	18.416	18.436	18.456	18.475999999999999	18.495999999999999	18.515999999999998	18.536000000000001	18.556000000000001	18.576000000000001	18.596	18.616	18.635999999999999	18.655999999999999	18.675999999999998	18.696000000000002	18.716000000000001	18.736000000000001	18.756	18.776	18.795999999999999	18.815999999999999	18.835999999999999	18.856000000000002	18.876000000000001	18.896000000000001	18.916	18.936	18.956	18.975999999999999	18.995999999999999	19.015999999999998	19.033999999999999	19.053999999999998	19.074000000000002	19.094000000000001	19.114000000000001	19.134	19.154	19.173999999999999	19.193999999999999	19.213999999999999	19.234000000000002	19.254000000000001	19.274000000000001	19.294	19.314	19.334	19.353999999999999	19.373999999999999	19.393999999999998	19.414000000000001	19.434000000000001	19.454000000000001	19.474	19.494	19.513999999999999	19.532	19.552	19.571999999999999	19.591999999999999	19.611999999999998	19.632000000000001	19.652000000000001	19.672000000000001	19.692	19.712	19.731999999999999	19.751999999999999	19.771999999999998	19.792000000000002	19.812000000000001	19.832000000000001	19.852	19.872	19.891999999999999	19.911999999999999	19.934000000000001	19.954000000000001	19.972000000000001	19.992000000000001	20.013999999999999	20.03	20.05	20.07	20.094000000000001	20.11	20.13	20.149999999999999	20.170000000000002	20.193999999999999	20.213999999999999	20.234000000000002	20.25	20.27	20.294	20.309999999999999	20.329999999999998	20.350000000000001	20.37	20.39	20.41	20.43	20.45	20.47	20.49	20.51	20.53	20.55	20.57	20.59	20.61	20.63	20.65	20.67	20.69	20.71	20.73	20.75	20.77	20.79	20.81	20.83	20.85	20.87	20.89	20.91	20.93	20.95	20.97	20.99	21.01	21.03	21.05	21.07	21.09	21.11	21.13	21.15	21.17	21.19	21.21	21.23	21.254000000000001	21.274000000000001	21.294	21.31	21.33	21.353999999999999	21.37	21.393999999999998	21.414000000000001	21.434000000000001	21.454000000000001	21.474	21.494	21.513999999999999	21.533999999999999	21.553999999999998	21.574000000000002	21.594000000000001	21.614000000000001	21.634	21.654	21.673999999999999	21.693999999999999	21.716000000000001	21.736000000000001	21.754000000000001	21.774000000000001	21.794	21.815999999999999	21.835999999999999	21.856000000000002	21.873999999999999	21.893999999999998	21.914000000000001	21.934000000000001	21.954000000000001	21.974	21.994	22.013999999999999	22.036000000000001	22.052	22.071999999999999	22.091999999999999	22.111999999999998	22.132000000000001	22.152000000000001	22.172000000000001	22.192	22.212	22.231999999999999	22.251999999999999	22.271999999999998	22.292000000000002	22.312000000000001	22.332000000000001	22.352	22.372	22.391999999999999	22.411999999999999	22.431999999999999	22.452000000000002	22.472000000000001	22.492000000000001	22.512	22.532	22.552	22.571999999999999	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.778	1.778	1.778	1.778	1.778	1.778	1.778	1.778	2	2	2	2	2	2	2.222	2.222	2.222	2.222	2.222	2.444	2.444	2.444	2.444	2.6669999999999998	2.6669999999999998	2.6669999999999998	2.6669999999999998	2.8889999999999998	2.8889999999999998	2.8889999999999998	3.1110000000000002	3.1110000000000002	3.3330000000000002	3.3330000000000002	3.3330000000000002	3.556	3.556	3.778	3.778	3.778	4	4	4.2220000000000004	4.2220000000000004	4.444	4.6669999999999998	4.6669999999999998	4.8890000000000002	4.8890000000000002	5.1109999999999998	5.1109999999999998	5.3330000000000002	5.556	5.556	5.7779999999999996	6	6	6.2220000000000004	6.444	6.6669999999999998	6.6669999999999998	6.8890000000000002	7.1109999999999998	7.3330000000000002	7.556	7.7779999999999996	8	8.2219999999999995	8.6669999999999998	8.8889999999999993	9.1110000000000007	9.3330000000000002	9.5559999999999992	10	10.222	10.444000000000001	10.667	11.111000000000001	11.333	11.555999999999999	12	12.222	12.444000000000001	12.888999999999999	13.111000000000001	13.555999999999999	13.778	14.222	14.444000000000001	14.888999999999999	15.111000000000001	15.333	15.778	16.222000000000001	16.443999999999999	16.888999999999999	17.111000000000001	17.556000000000001	17.777999999999999	18.222000000000001	18.667000000000002	18.888999999999999	19.332999999999998	19.556000000000001	20	20.443999999999999	20.667000000000002	21.111000000000001	21.332999999999998	21.777999999999999	22	22.443999999999999	22.667000000000002	22.888999999999999	23.332999999999998	23.777999999999999	24	24.222000000000001	24.667000000000002	24.888999999999999	25.111000000000001	25.556000000000001	25.777999999999999	26.222000000000001	26.443999999999999	26.667000000000002	26.888999999999999	27.332999999999998	27.556000000000001	27.777999999999999	28	28.222000000000001	28.667000000000002	28.888999999999999	29.111000000000001	29.556000000000001	29.777999999999999	30	30.222000000000001	30.443999999999999	30.667000000000002	31.111000000000001	31.332999999999998	31.556000000000001	31.777999999999999	32	32.222000000000001	32.667000000000002	32.889000000000003	33.110999999999997	33.555999999999997	33.777999999999999	34	34.222000000000001	34.444000000000003	34.667000000000002	35.110999999999997	35.332999999999998	35.555999999999997	36	36.222000000000001	36.444000000000003	36.667000000000002	36.889000000000003	37.110999999999997	37.332999999999998	37.777999999999999	38	38.222000000000001	38.444000000000003	38.667000000000002	38.889000000000003	39.332999999999998	39.555999999999997	39.777999999999999	40	40.222000000000001	40.444000000000003	40.667000000000002	41.110999999999997	41.332999999999998	41.555999999999997	41.777999999999999	42	42.222000000000001	42.667000000000002	42.889000000000003	43.110999999999997	43.332999999999998	43.555999999999997	43.777999999999999	44	44.222000000000001	44.444000000000003	44.667000000000002	44.889000000000003	45.110999999999997	45.555999999999997	45.777999999999999	46	46.222000000000001	46.444000000000003	46.667000000000002	46.889000000000003	47.110999999999997	47.332999999999998	47.555999999999997	47.777999999999999	48.222000000000001	48.444000000000003	48.667000000000002	48.889000000000003	49.110999999999997	49.332999999999998	49.777999999999999	50	50.222000000000001	50.444000000000003	50.667000000000002	51.110999999999997	51.332999999999998	51.555999999999997	51.777999999999999	52	52.444000000000003	52.667000000000002	52.889000000000003	53.110999999999997	53.555999999999997	53.777999999999999	54	54.222000000000001	54.444000000000003	54.889000000000003	55.110999999999997	55.332999999999998	55.555999999999997	56	56.222000000000001	56.444000000000003	56.667000000000002	57.110999999999997	57.332999999999998	57.555999999999997	57.777999999999999	58.222000000000001	58.444000000000003	58.667000000000002	58.889000000000003	59.332999999999998	59.555999999999997	59.777999999999999	60	60.444000000000003	60.667000000000002	60.889000000000003	61.110999999999997	61.332999999999998	61.777999999999999	62	62.222000000000001	62.444000000000003	62.667000000000002	62.889000000000003	63.332999999999998	63.555999999999997	63.777999999999999	64	64.221999999999994	64.444000000000003	64.888999999999996	65.111000000000004	65.332999999999998	65.555999999999997	65.778000000000006	66	66.221999999999994	66.444000000000003	66.667000000000002	66.888999999999996	67.111000000000004	67.555999999999997	67.778000000000006	68	68.221999999999994	68.444000000000003	68.667000000000002	68.888999999999996	69.111000000000004	69.332999999999998	69.555999999999997	69.778000000000006	70	70.221999999999994	70.444000000000003	70.667000000000002	70.888999999999996	71.111000000000004	71.332999999999998	71.555999999999997	71.778000000000006	72	72.221999999999994	72.444000000000003	72.667000000000002	72.888999999999996	73.111000000000004	73.111000000000004	73.332999999999998	73.555999999999997	73.778000000000006	74	74.221999999999994	74.221999999999994	74.444000000000003	74.667000000000002	74.888999999999996	75.111000000000004	75.111000000000004	75.332999999999998	75.555999999999997	75.555999999999997	75.778000000000006	76	76.221999999999994	76.221999999999994	76.444000000000003	76.667000000000002	76.667000000000002	76.888999999999996	77.111000000000004	77.111000000000004	77.332999999999998	77.555999999999997	77.778000000000006	77.778000000000006	78	78	78.221999999999994	78.221999999999994	78.444000000000003	78.667000000000002	78.667000000000002	78.888999999999996	78.888999999999996	79.111000000000004	79.332999999999998	79.332999999999998	79.555999999999997	79.555999999999997	79.778000000000006	79.778000000000006	80	80	80.221999999999994	80.221999999999994	80.444000000000003	80.667000000000002	80.667000000000002	80.667000000000002	80.888999999999996	80.888999999999996	81.111000000000004	81.332999999999998	81.332999999999998	81.332999999999998	81.555999999999997	81.555999999999997	81.778000000000006	81.778000000000006	82	82	82.221999999999994	82.221999999999994	82.221999999999994	82.444000000000003	82.444000000000003	82.667000000000002	82.667000000000002	82.667000000000002	82.888999999999996	82.888999999999996	83.111000000000004	83.111000000000004	83.111000000000004	83.111000000000004	83.111000000000004	83.332999999999998	83.332999999999998	83.332999999999998	83.332999999999998	83.332999999999998	83.332999999999998	83.555999999999997	83.555999999999997	83.555999999999997	83.555999999999997	83.555999999999997	83.778000000000006	83.778000000000006	83.778000000000006	83.778000000000006	84	84	84	84	84.221999999999994	84.221999999999994	84.221999999999994	84.444000000000003	84.444000000000003	84.444000000000003	84.667000000000002	84.667000000000002	84.667000000000002	84.888999999999996	84.888999999999996	84.888999999999996	85.111000000000004	85.111000000000004	85.111000000000004	85.332999999999998	85.332999999999998	85.555999999999997	85.555999999999997	85.778000000000006	85.778000000000006	86	86	86.221999999999994	86.221999999999994	86.444000000000003	86.444000000000003	86.667000000000002	86.667000000000002	86.667000000000002	86.888999999999996	86.888999999999996	86.888999999999996	87.111000000000004	87.111000000000004	87.111000000000004	87.332999999999998	87.332999999999998	87.332999999999998	87.555999999999997	87.555999999999997	87.555999999999997	87.778000000000006	87.778000000000006	87.778000000000006	87.778000000000006	88	88	88	88.221999999999994	88.221999999999994	88.221999999999994	88.444000000000003	88.444000000000003	88.444000000000003	88.444000000000003	88.667000000000002	88.667000000000002	88.667000000000002	88.667000000000002	88.888999999999996	88.888999999999996	88.888999999999996	88.888999999999996	89.111000000000004	89.111000000000004	89.111000000000004	89.111000000000004	89.332999999999998	89.332999999999998	89.332999999999998	89.332999999999998	89.555999999999997	89.555999999999997	89.555999999999997	89.555999999999997	89.778000000000006	89.778000000000006	89.778000000000006	89.778000000000006	89.778000000000006	90	90	90	90	90.221999999999994	90.221999999999994	90.221999999999994	90.221999999999994	90.221999999999994	90.444000000000003	90.444000000000003	90.444000000000003	90.444000000000003	90.667000000000002	90.667000000000002	90.667000000000002	90.667000000000002	90.667000000000002	90.888999999999996	90.888999999999996	90.888999999999996	90.888999999999996	91.111000000000004	91.111000000000004	91.111000000000004	91.111000000000004	91.111000000000004	91.332999999999998	91.332999999999998	91.332999999999998	91.332999999999998	91.332999999999998	91.555999999999997	91.555999999999997	91.555999999999997	91.555999999999997	91.555999999999997	91.778000000000006	91.778000000000006	91.778000000000006	91.778000000000006	91.778000000000006	92	92	92	92	92	92.221999999999994	92.221999999999994	92.221999999999994	92.221999999999994	92.221999999999994	92.221999999999994	92.444000000000003	92.444000000000003	92.444000000000003	92.444000000000003	92.444000000000003	92.667000000000002	92.667000000000002	92.667000000000002	92.667000000000002	92.667000000000002	92.667000000000002	92.888999999999996	92.888999999999996	92.888999999999996	92.888999999999996	92.888999999999996	92.888999999999996	93.111000000000004	93.111000000000004	93.111000000000004	93.111000000000004	93.111000000000004	93.111000000000004	93.332999999999998	93.332999999999998	93.332999999999998	93.332999999999998	93.332999999999998	93.332999999999998	93.555999999999997	93.555999999999997	93.555999999999997	93.555999999999997	93.555999999999997	93.555999999999997	93.778000000000006	93.778000000000006	93.778000000000006	93.778000000000006	93.778000000000006	93.778000000000006	93.778000000000006	94	94	94	94	94	94	94.221999999999994	94.221999999999994	94.221999999999994	94.221999999999994	94.221999999999994	94.221999999999994	94.221999999999994	94.444000000000003	94.444000000000003	94.444000000000003	94.444000000000003	94.444000000000003	94.444000000000003	94.444000000000003	94.667000000000002	94.667000000000002	94.667000000000002	94.667000000000002	94.667000000000002	94.667000000000002	94.667000000000002	94.888999999999996	94.888999999999996	94.888999999999996	94.888999999999996	94.888999999999996	94.888999999999996	94.888999999999996	94.888999999999996	95.111000000000004	95.111000000000004	95.111000000000004	95.111000000000004	95.111000000000004	95.111000000000004	95.111000000000004	95.332999999999998	95.332999999999998	95.332999999999998	95.332999999999998	95.332999999999998	95.332999999999998	95.332999999999998	95.332999999999998	95.555999999999997	95.555999999999997	95.555999999999997	95.555999999999997	95.555999999999997	95.555999999999997	95.555999999999997	95.555999999999997	95.778000000000006	95.778000000000006	95.778000000000006	95.778000000000006	95.778000000000006	95.778000000000006	95.778000000000006	95.778000000000006	95.778000000000006	96	96	96	96	96	96	96	96	96.221999999999994	96.221999999999994	96.221999999999994	96.221999999999994	96.221999999999994	96.221999999999994	96.221999999999994	96.221999999999994	96.221999999999994	96.444000000000003	96.444000000000003	96.444000000000003	96.444000000000003	96.444000000000003	96.444000000000003	96.444000000000003	96.444000000000003	96.444000000000003	96.667000000000002	96.667000000000002	96.667000000000002	96.667000000000002	96.667000000000002	96.667000000000002	96.667000000000002	96.667000000000002	96.667000000000002	96.888999999999996	96.888999999999996	96.888999999999996	96.888999999999996	96.888999999999996	96.888999999999996	96.888999999999996	96.888999999999996	96.888999999999996	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	98	98	98	98	98	98	98	98	98	98	98	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	100	100	100	100	100	100	100	100	100	100	100	100	100	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.444	102.444	102.444	102.444	102.444	102.444	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102	102	102	102	102	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.556	101.556	101.556	101.556	101.556	101.556	101.333	101.333	101.333	101.333	101.333	101.333	101.333	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	101.111	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.889	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.667	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.444	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100	100	100	100	100	100	100	100	100	100	100	100	100	100	100	100	100	100	100	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98.221999999999994	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	98	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.778000000000006	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.111000000000004	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.555999999999997	97.555999999999997	97.555999999999997	97.778000000000006	97.778000000000006	98	98	98.221999999999994	98.221999999999994	98.444000000000003	98.444000000000003	98.667000000000002	98.888999999999996	98.888999999999996	99.111000000000004	99.332999999999998	99.332999999999998	99.555999999999997	99.778000000000006	100	100	100.22199999999999	100.444	100.667	100.889	100.889	101.111	101.333	101.556	101.77800000000001	102	102.22199999999999	102.22199999999999	102.444	102.667	102.889	103.111	103.333	103.556	103.77800000000001	104	104.22199999999999	104.667	104.889	105.111	105.333	105.556	105.77800000000001	106	106.22199999999999	106.444	106.667	106.667	106.889	107.111	107.111	107.333	107.556	107.556	107.77800000000001	107.77800000000001	108	108	108.22199999999999	108.22199999999999	108.444	108.444	108.667	108.667	108.889	108.889	109.111	109.111	109.111	109.333	109.333	109.333	109.556	109.556	109.556	109.556	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	110	110	110	110	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	112	112	112	112	112	112	112	112	112	112	112	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110	110	110	110	110	110	110	110	110	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.556	109.556	109.556	109.556	109.556	109.556	109.556	109.333	109.333	109.333	109.333	109.333	109.111	109.111	109.111	109.111	109.111	108.889	108.889	108.889	108.889	108.667	108.667	108.667	108.667	108.444	108.444	108.444	108.22199999999999	108.22199999999999	108.22199999999999	108	108	108	107.77800000000001	107.77800000000001	107.556	107.556	107.333	107.333	107.111	107.111	106.889	106.889	106.667	106.444	106.444	106.22199999999999	106	106	105.77800000000001	105.556	105.333	105.111	104.667	104.444	104	103.556	103.333	102.667	102.444	101.77800000000001	101.333	100.889	100.22199999999999	99.555999999999997	99.111000000000004	98.221999999999994	97.332999999999998	96	94.667000000000002	93.111000000000004	91.332999999999998	89.778000000000006	88.444000000000003	87.332999999999998	85.332999999999998	84.221999999999994	82.888999999999996	80.667000000000002	79.332999999999998	78	76.221999999999994	75.332999999999998	74.444000000000003	73.555999999999997	72.444000000000003	71.555999999999997	70.888999999999996	70	68.667000000000002	67.778000000000006	67.111000000000004	66.221999999999994	64.888999999999996	63.777999999999999	62.889000000000003	62	60.889000000000003	59.332999999999998	58.222000000000001	57.110999999999997	56	54.667000000000002	52.889000000000003	51.777999999999999	50.444000000000003	49.110999999999997	47.555999999999997	45.332999999999998	Sample 2	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	0	0	0	1E-3	1E-3	1E-3	1E-3	1E-3	0	0	0	0	1E-3	1E-3	1E-3	1E-3	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	1E-3	1E-3	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	0	0	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-2E-3	-1E-3	-1E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-2E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	0	0	0	0	-1E-3	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.9E-2	1.9E-2	1.9E-2	1.9E-2	0.02	0.02	0.02	0.02	0.02	2.1000000000000001E-2	2.1000000000000001E-2	2.1000000000000001E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.3E-2	2.3E-2	2.3E-2	2.3E-2	2.3E-2	2.4E-2	2.4E-2	2.4E-2	2.4E-2	2.4E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.7E-2	2.7E-2	2.7E-2	2.7E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.9000000000000001E-2	2.9000000000000001E-2	2.9000000000000001E-2	2.9000000000000001E-2	0.03	0.03	0.03	0.03	0.03	0.03	3.1E-2	3.1E-2	3.1E-2	3.1E-2	3.2000000000000001E-2	3.2000000000000001E-2	3.2000000000000001E-2	3.2000000000000001E-2	3.2000000000000001E-2	3.2000000000000001E-2	3.3000000000000002E-2	3.3000000000000002E-2	3.3000000000000002E-2	3.3000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5000000000000003E-2	3.5999999999999997E-2	3.5999999999999997E-2	3.5999999999999997E-2	3.5999999999999997E-2	3.5999999999999997E-2	3.6999999999999998E-2	3.6999999999999998E-2	3.6999999999999998E-2	3.6999999999999998E-2	3.7999999999999999E-2	3.7999999999999999E-2	3.7999999999999999E-2	3.7999999999999999E-2	3.7999999999999999E-2	3.7999999999999999E-2	3.9E-2	3.9E-2	3.9E-2	0.04	0.04	0.04	0.04	0.04	0.04	4.1000000000000002E-2	4.1000000000000002E-2	4.1000000000000002E-2	4.1000000000000002E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2999999999999997E-2	4.2999999999999997E-2	4.2999999999999997E-2	4.2999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.4999999999999998E-2	4.4999999999999998E-2	4.4999999999999998E-2	4.4999999999999998E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.7E-2	4.7E-2	4.7E-2	4.7E-2	4.8000000000000001E-2	4.8000000000000001E-2	4.8000000000000001E-2	4.8000000000000001E-2	4.8000000000000001E-2	4.9000000000000002E-2	4.9000000000000002E-2	4.9000000000000002E-2	0.05	0.05	0.05	0.05	0.05	0.05	5.0999999999999997E-2	5.0999999999999997E-2	5.0999999999999997E-2	5.1999999999999998E-2	5.1999999999999998E-2	5.1999999999999998E-2	5.1999999999999998E-2	5.2999999999999999E-2	5.2999999999999999E-2	5.2999999999999999E-2	5.3999999999999999E-2	5.3999999999999999E-2	5.3999999999999999E-2	5.3999999999999999E-2	5.5E-2	5.5E-2	5.6000000000000001E-2	5.6000000000000001E-2	5.6000000000000001E-2	5.7000000000000002E-2	5.7000000000000002E-2	5.7000000000000002E-2	5.8000000000000003E-2	5.8000000000000003E-2	5.8999999999999997E-2	5.8999999999999997E-2	5.8999999999999997E-2	0.06	0.06	6.0999999999999999E-2	6.0999999999999999E-2	6.2E-2	6.2E-2	6.2E-2	6.3E-2	6.4000000000000001E-2	6.4000000000000001E-2	6.4000000000000001E-2	6.5000000000000002E-2	6.6000000000000003E-2	6.6000000000000003E-2	6.7000000000000004E-2	6.7000000000000004E-2	6.8000000000000005E-2	6.8000000000000005E-2	6.9000000000000006E-2	7.0000000000000007E-2	7.0000000000000007E-2	7.0999999999999994E-2	7.0999999999999994E-2	7.1999999999999995E-2	7.1999999999999995E-2	7.2999999999999995E-2	7.3999999999999996E-2	7.3999999999999996E-2	7.4999999999999997E-2	7.4999999999999997E-2	7.5999999999999998E-2	7.5999999999999998E-2	7.6999999999999999E-2	7.8E-2	7.8E-2	7.9000000000000001E-2	0.08	0.08	8.1000000000000003E-2	8.2000000000000003E-2	8.2000000000000003E-2	8.3000000000000004E-2	8.3000000000000004E-2	8.4000000000000005E-2	8.4000000000000005E-2	8.5000000000000006E-2	8.5999999999999993E-2	8.5999999999999993E-2	8.6999999999999994E-2	8.7999999999999995E-2	8.7999999999999995E-2	8.8999999999999996E-2	8.8999999999999996E-2	0.09	9.0999999999999998E-2	9.0999999999999998E-2	9.1999999999999998E-2	9.1999999999999998E-2	9.2999999999999999E-2	9.4E-2	9.4E-2	9.5000000000000001E-2	9.6000000000000002E-2	9.6000000000000002E-2	9.7000000000000003E-2	9.8000000000000004E-2	9.8000000000000004E-2	9.9000000000000005E-2	0.1	0.1	0.10100000000000001	0.10199999999999999	0.10199999999999999	0.10299999999999999	0.104	0.104	0.105	0.105	0.106	0.107	0.107	0.108	0.108	0.109	0.11	0.11	0.111	0.112	0.112	0.113	0.114	0.114	0.115	0.115	0.11600000000000001	0.11600000000000001	0.11700000000000001	0.11799999999999999	0.11799999999999999	0.11899999999999999	0.12	0.12	0.12	0.12	0.12	0.12	0.12	0.11899999999999999	0.11899999999999999	0.11899999999999999	0.12	0.12	0.121	0.122	0.122	0.123	0.124	0.125	0.125	0.126	0.127	0.128	0.128	0.129	0.13	0.13	0.13100000000000001	0.13200000000000001	0.13200000000000001	0.13300000000000001	0.13400000000000001	0.13400000000000001	0.13500000000000001	0.13600000000000001	0.13600000000000001	0.13700000000000001	0.13800000000000001	0.13800000000000001	0.13900000000000001	0.14000000000000001	0.14000000000000001	0.14099999999999999	0.14199999999999999	0.14199999999999999	0.14299999999999999	0.14299999999999999	0.14399999999999999	0.14399999999999999	0.14499999999999999	0.14599999999999999	0.14599999999999999	0.14699999999999999	0.14799999999999999	0.14799999999999999	0.14899999999999999	0.14899999999999999	0.15	0.15	0.151	0.152	0.152	0.153	0.154	0.154	0.154	0.155	0.156	0.156	0.157	0.158	0.158	0.159	0.159	0.16	0.16	0.161	0.161	0.16200000000000001	0.16200000000000001	0.16300000000000001	0.16400000000000001	0.16400000000000001	0.16500000000000001	0.16600000000000001	0.16600000000000001	0.16600000000000001	0.16700000000000001	0.16800000000000001	0.16800000000000001	0.16900000000000001	0.16900000000000001	0.17	0.17	0.17100000000000001	0.17199999999999999	0.17199999999999999	0.17199999999999999	0.17299999999999999	0.17399999999999999	0.17399999999999999	0.17499999999999999	0.17499999999999999	0.17599999999999999	0.17599999999999999	0.17699999999999999	0.17699999999999999	0.17799999999999999	0.17799999999999999	0.17899999999999999	0.18	0.18	0.18099999999999999	0.18099999999999999	0.182	0.182	0.183	0.183	0.184	0.184	0.185	0.186	0.186	0.187	0.187	0.188	0.188	0.189	0.189	0.19	0.19	0.191	0.192	0.192	0.192	0.193	0.19400000000000001	0.19400000000000001	0.19500000000000001	0.19500000000000001	0.19600000000000001	0.19600000000000001	0.19700000000000001	0.19700000000000001	0.19800000000000001	0.19800000000000001	0.19900000000000001	0.2	0.2	0.20100000000000001	0.20100000000000001	0.20200000000000001	0.20200000000000001	0.20200000000000001	0.20300000000000001	0.20399999999999999	0.20399999999999999	0.20399999999999999	0.20399999999999999	0.20499999999999999	0.20699999999999999	0.20699999999999999	0.20699999999999999	0.20699999999999999	0.20799999999999999	0.20899999999999999	0.21	0.21	0.21	0.21099999999999999	0.21099999999999999	0.21199999999999999	0.21299999999999999	0.21299999999999999	0.21299999999999999	0.214	0.215	0.216	0.216	0.216	0.217	0.218	0.218	0.219	0.219	0.22	0.22	0.221	0.222	0.222	0.222	0.223	0.224	0.224	0.22500000000000001	0.22500000000000001	0.22600000000000001	0.22600000000000001	0.22700000000000001	0.22700000000000001	0.22800000000000001	0.22800000000000001	0.22900000000000001	0.22900000000000001	0.23	0.23100000000000001	0.23100000000000001	0.23100000000000001	0.23100000000000001	0.23300000000000001	0.23300000000000001	0.23400000000000001	0.23400000000000001	0.23499999999999999	0.23499999999999999	0.23599999999999999	0.23599999999999999	0.23699999999999999	0.23699999999999999	0.23799999999999999	0.23799999999999999	0.23899999999999999	0.23899999999999999	0.24	0.24	0.24099999999999999	0.24099999999999999	0.24199999999999999	0.24199999999999999	0.24299999999999999	0.24299999999999999	0.24399999999999999	0.24399999999999999	0.24399999999999999	0.246	0.246	0.246	0.247	0.248	0.248	0.248	0.249	0.25	0.25	0.25	0.251	0.252	0.252	0.253	0.253	0.254	0.254	0.255	0.255	0.25600000000000001	0.25600000000000001	0.25700000000000001	0.25700000000000001	0.25800000000000001	0.25800000000000001	0.25900000000000001	0.25900000000000001	0.26	0.26	0.26100000000000001	0.26200000000000001	0.26200000000000001	0.26200000000000001	0.26300000000000001	0.26400000000000001	0.26400000000000001	0.26400000000000001	0.26500000000000001	0.26600000000000001	0.26600000000000001	0.26600000000000001	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26800000000000002	0.26900000000000002	0.27	0.27	0.27	0.27100000000000002	0.27200000000000002	0.27200000000000002	0.27200000000000002	0.27300000000000002	0.27400000000000002	0.27400000000000002	0.27500000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27800000000000002	0.27800000000000002	0.27900000000000003	0.27900000000000003	0.28000000000000003	0.28000000000000003	0.28100000000000003	0.28100000000000003	0.28199999999999997	0.28199999999999997	0.28299999999999997	0.28299999999999997	0.28399999999999997	0.28399999999999997	0.28499999999999998	0.28499999999999998	0.28599999999999998	0.28599999999999998	0.28699999999999998	0.28699999999999998	0.28799999999999998	0.28799999999999998	0.28899999999999998	0.28899999999999998	0.28999999999999998	0.28999999999999998	0.29099999999999998	0.29199999999999998	0.29199999999999998	0.29199999999999998	0.29299999999999998	0.29399999999999998	0.29399999999999998	0.29399999999999998	0.29499999999999998	0.29599999999999999	0.29599999999999999	0.29599999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.29899999999999999	0.3	0.3	0.30099999999999999	0.30099999999999999	0.30199999999999999	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30499999999999999	0.30499999999999999	0.30599999999999999	0.30599999999999999	0.307	0.307	0.308	0.308	0.309	0.309	0.31	0.31	0.311	0.311	0.312	0.312	0.313	0.313	0.314	0.314	0.315	0.315	0.316	0.316	0.317	0.317	0.318	0.318	0.31900000000000001	0.32	0.32	0.32	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32400000000000001	0.32500000000000001	0.32600000000000001	0.32600000000000001	0.32600000000000001	0.32700000000000001	0.32800000000000001	0.32800000000000001	0.32800000000000001	0.32900000000000001	0.33	0.33	0.33	0.33100000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33300000000000002	0.33400000000000002	0.33400000000000002	0.33500000000000002	0.33500000000000002	0.33600000000000002	0.33600000000000002	0.33700000000000002	0.33700000000000002	0.33800000000000002	0.33800000000000002	0.33900000000000002	0.33900000000000002	0.34	0.34	0.34100000000000003	0.34100000000000003	0.34200000000000003	0.34200000000000003	0.34300000000000003	0.34300000000000003	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34699999999999998	0.34799999999999998	0.34799999999999998	0.34899999999999998	0.34899999999999998	0.35	0.35	0.35099999999999998	0.35099999999999998	0.35199999999999998	0.35199999999999998	0.35299999999999998	0.35299999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35499999999999998	0.35599999999999998	0.35599999999999998	0.35699999999999998	0.35699999999999998	0.35799999999999998	0.35799999999999998	0.35899999999999999	0.35899999999999999	0.36	0.36	0.36099999999999999	0.36199999999999999	0.36199999999999999	0.36199999999999999	0.36299999999999999	0.36399999999999999	0.36399999999999999	0.36399999999999999	0.36499999999999999	0.36599999999999999	0.36599999999999999	0.36599999999999999	0.36699999999999999	0.36799999999999999	0.36799999999999999	0.36899999999999999	0.36899999999999999	0.37	0.37	0.371	0.371	0.372	0.372	0.373	0.373	0.374	0.374	0.375	0.375	0.376	0.376	0.377	0.377	0.378	0.378	0.379	0.379	0.38	0.38	0.38100000000000001	0.38100000000000001	0.38200000000000001	0.38200000000000001	0.38300000000000001	0.38300000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38500000000000001	0.38600000000000001	0.38600000000000001	0.38700000000000001	0.38700000000000001	0.38800000000000001	0.38800000000000001	0.38900000000000001	0.38900000000000001	0.39	0.39	0.39100000000000001	0.39100000000000001	0.39200000000000002	0.39200000000000002	0.39300000000000002	0.39300000000000002	0.39400000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39600000000000002	0.39600000000000002	0.39700000000000002	0.39800000000000002	0.39800000000000002	0.39800000000000002	0.39900000000000002	0.4	0.4	0.4	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40400000000000003	0.40400000000000003	0.40400000000000003	0.40500000000000003	0.40600000000000003	0.40600000000000003	0.40600000000000003	0.40699999999999997	0.40799999999999997	0.40799999999999997	0.40799999999999997	0.40899999999999997	0.41	0.41	0.41	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41299999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41499999999999998	0.41499999999999998	0.41599999999999998	0.41599999999999998	0.41699999999999998	0.41699999999999998	0.41799999999999998	0.41799999999999998	0.41899999999999998	0.41899999999999998	0.42	0.42	0.42099999999999999	0.42099999999999999	0.42199999999999999	0.42199999999999999	0.42299999999999999	0.42299999999999999	0.42399999999999999	0.42399999999999999	0.42499999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42699999999999999	0.42799999999999999	0.42799999999999999	0.42899999999999999	0.42899999999999999	0.43	0.43	0.43099999999999999	0.43099999999999999	0.432	0.432	0.433	0.433	0.434	0.434	0.435	0.435	0.436	0.436	0.437	0.437	0.438	0.438	0.439	0.439	0.44	0.44	0.441	0.441	0.442	0.442	0.443	0.443	0.44400000000000001	0.44400000000000001	0.44500000000000001	0.44500000000000001	0.44600000000000001	0.44600000000000001	0.44700000000000001	0.44700000000000001	0.44800000000000001	0.44800000000000001	0.44900000000000001	0.45	0.45	0.45	0.45100000000000001	0.45100000000000001	0.45200000000000001	0.45200000000000001	0.45300000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45800000000000002	0.45800000000000002	0.45800000000000002	0.45900000000000002	0.46	0.46	0.46	0.46100000000000002	0.46200000000000002	0.46200000000000002	0.46200000000000002	0.46300000000000002	0.46400000000000002	0.46400000000000002	0.46400000000000002	0.46500000000000002	0.46600000000000003	0.46600000000000003	0.46600000000000003	0.46700000000000003	0.46800000000000003	0.46800000000000003	0.46800000000000003	0.46899999999999997	0.47	0.47	0.47	0.47099999999999997	0.47199999999999998	0.47199999999999998	0.47299999999999998	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47499999999999998	0.47499999999999998	0.47599999999999998	0.47599999999999998	0.47699999999999998	0.47699999999999998	0.47799999999999998	0.47799999999999998	0.47899999999999998	0.47899999999999998	0.48	0.48	0.48099999999999998	0.48099999999999998	0.48199999999999998	0.48199999999999998	0.48299999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48499999999999999	0.48499999999999999	0.48599999999999999	0.48599999999999999	0.48699999999999999	0.48699999999999999	0.48799999999999999	0.48799999999999999	0.48899999999999999	0.48899999999999999	0.49	0.49	0.49099999999999999	0.49099999999999999	0.49199999999999999	0.49199999999999999	0.49299999999999999	0.49299999999999999	0.49399999999999999	0.49399999999999999	0.495	0.495	0.496	0.496	0.497	0.497	0.498	0.498	0.499	0.499	0.5	0.5	0.501	0.501	0.502	0.502	0.503	0.503	0.504	0.504	0.505	0.505	0.50600000000000001	0.50600000000000001	0.50700000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50900000000000001	0.50900000000000001	0.51	0.51	0.51100000000000001	0.51100000000000001	0.51200000000000001	0.51200000000000001	0.51300000000000001	0.51400000000000001	0.51400000000000001	0.51400000000000001	0.51500000000000001	0.51600000000000001	0.51600000000000001	0.51600000000000001	0.51700000000000002	0.51800000000000002	0.51800000000000002	0.51800000000000002	0.51900000000000002	0.52	0.52	0.52	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.51	0.51200000000000001	0.51400000000000001	0.51800000000000002	0.51800000000000002	0.52	0.52400000000000002	0.52800000000000002	0.53	0.53200000000000003	0.53800000000000003	0.54	0.54400000000000004	0.55000000000000004	0.55400000000000005	0.55800000000000005	0.56200000000000006	0.56799999999999995	0.57199999999999995	0.57999999999999996	0.58399999999999996	0.59	0.59799999999999998	0.60199999999999998	0.61	0.61799999999999999	0.622	0.63	0.63800000000000001	0.64400000000000002	0.65200000000000002	0.66	0.66800000000000004	0.67800000000000005	0.68400000000000005	0.69199999999999995	0.70199999999999996	0.71199999999999997	0.72	0.73	0.74	0.75	0.76	0.77	0.78	0.79200000000000004	0.80200000000000005	0.81399999999999995	0.82399999999999995	0.83799999999999997	0.84799999999999998	0.86	0.872	0.88400000000000001	0.89800000000000002	0.91	0.92200000000000004	0.93400000000000005	0.94799999999999995	0.96199999999999997	0.97399999999999998	0.99	1.004	1.018	1.032	1.048	1.0620000000000001	1.0780000000000001	1.0920000000000001	1.1080000000000001	1.1240000000000001	1.1399999999999999	1.1539999999999999	1.1719999999999999	1.1879999999999999	1.204	1.222	1.24	1.258	1.274	1.292	1.31	1.3280000000000001	1.3440000000000001	1.3640000000000001	1.3819999999999999	1.4019999999999999	1.4219999999999999	1.44	1.46	1.48	1.5	1.52	1.54	1.56	1.58	1.6	1.62	1.64	1.66	1.68	1.702	1.72	1.74	1.76	1.782	1.802	1.8220000000000001	1.8420000000000001	1.8620000000000001	1.8819999999999999	1.9019999999999999	1.9219999999999999	1.9419999999999999	1.962	1.982	2.0019999999999998	2.0219999999999998	2.0419999999999998	2.0619999999999998	2.0739999999999998	2.0939999999999999	2.1139999999999999	2.1339999999999999	2.1539999999999999	2.1779999999999999	2.1960000000000002	2.214	2.234	2.254	2.2759999999999998	2.2959999999999998	2.3159999999999998	2.3359999999999999	2.3559999999999999	2.3759999999999999	2.3959999999999999	2.4159999999999999	2.4359999999999999	2.456	2.476	2.496	2.516	2.536	2.556	2.5760000000000001	2.5960000000000001	2.6160000000000001	2.6360000000000001	2.6560000000000001	2.6760000000000002	2.6960000000000002	2.7160000000000002	2.74	2.7559999999999998	2.7759999999999998	2.7959999999999998	2.8159999999999998	2.84	2.8559999999999999	2.88	2.9	2.92	2.94	2.96	2.98	3	3.02	3.04	3.06	3.08	3.1	3.12	3.1419999999999999	3.1619999999999999	3.1819999999999999	3.202	3.222	3.242	3.262	3.282	3.302	3.3220000000000001	3.3420000000000001	3.3620000000000001	3.3820000000000001	3.4020000000000001	3.4239999999999999	3.444	3.464	3.484	3.504	3.524	3.544	3.5640000000000001	3.5840000000000001	3.6040000000000001	3.6240000000000001	3.6440000000000001	3.6640000000000001	3.6840000000000002	3.7040000000000002	3.7240000000000002	3.7440000000000002	3.7639999999999998	3.7839999999999998	3.8039999999999998	3.8239999999999998	3.8439999999999999	3.8639999999999999	3.8839999999999999	3.9039999999999999	3.9239999999999999	3.9460000000000002	3.9660000000000002	3.984	4.0060000000000002	4.0259999999999998	4.0439999999999996	4.0640000000000001	4.0860000000000003	4.1059999999999999	4.1239999999999997	4.1459999999999999	4.1660000000000004	4.1859999999999999	4.2060000000000004	4.226	4.2460000000000004	4.266	4.2859999999999996	4.306	4.3259999999999996	4.3460000000000001	4.3659999999999997	4.3860000000000001	4.4059999999999997	4.4260000000000002	4.4480000000000004	4.468	4.4880000000000004	4.508	4.5279999999999996	4.548	4.5679999999999996	4.5880000000000001	4.6079999999999997	4.6280000000000001	4.6479999999999997	4.6680000000000001	4.6879999999999997	4.7119999999999997	4.7320000000000002	4.7519999999999998	4.7720000000000002	4.7919999999999998	4.8120000000000003	4.8319999999999999	4.8520000000000003	4.8719999999999999	4.8920000000000003	4.9119999999999999	4.9320000000000004	4.952	4.9720000000000004	4.992	5.0119999999999996	5.032	5.0519999999999996	5.0720000000000001	5.0880000000000001	5.1120000000000001	5.1319999999999997	5.1520000000000001	5.1719999999999997	5.1879999999999997	5.2080000000000002	5.2279999999999998	5.2480000000000002	5.2679999999999998	5.2880000000000003	5.3079999999999998	5.3280000000000003	5.3479999999999999	5.3719999999999999	5.3879999999999999	5.4080000000000004	5.4279999999999999	5.4480000000000004	5.468	5.4880000000000004	5.508	5.5279999999999996	5.548	5.5679999999999996	5.5880000000000001	5.6079999999999997	5.6280000000000001	5.6479999999999997	5.6680000000000001	5.6879999999999997	5.7080000000000002	5.7279999999999998	5.7480000000000002	5.7679999999999998	5.7880000000000003	5.8079999999999998	5.8280000000000003	5.8479999999999999	5.8719999999999999	5.8879999999999999	5.9080000000000004	5.9279999999999999	5.9480000000000004	5.968	5.9880000000000004	6.008	6.0279999999999996	6.048	6.0720000000000001	6.0880000000000001	6.1079999999999997	6.1280000000000001	6.1479999999999997	6.1719999999999997	6.1879999999999997	6.2080000000000002	6.2279999999999998	6.2480000000000002	6.2679999999999998	6.2880000000000003	6.3079999999999998	6.3280000000000003	6.3479999999999999	6.3680000000000003	6.3879999999999999	6.4080000000000004	6.4279999999999999	6.4480000000000004	6.468	6.4880000000000004	6.508	6.5279999999999996	6.548	6.5679999999999996	6.5880000000000001	6.6079999999999997	6.6280000000000001	6.6479999999999997	6.6680000000000001	6.6879999999999997	6.7080000000000002	6.7279999999999998	6.7480000000000002	6.7679999999999998	6.7880000000000003	6.8079999999999998	6.8280000000000003	6.8479999999999999	6.8680000000000003	6.8879999999999999	6.9080000000000004	6.9279999999999999	6.9480000000000004	6.968	6.9859999999999998	7.0060000000000002	7.0279999999999996	7.048	7.0679999999999996	7.0880000000000001	7.1079999999999997	7.1280000000000001	7.1479999999999997	7.1680000000000001	7.1879999999999997	7.2080000000000002	7.2279999999999998	7.2480000000000002	7.2679999999999998	7.2880000000000003	7.3079999999999998	7.33	7.35	7.37	7.39	7.41	7.43	7.45	7.47	7.49	7.51	7.53	7.55	7.57	7.59	7.61	7.63	7.65	7.67	7.69	7.71	7.73	7.75	7.77	7.79	7.8140000000000001	7.83	7.85	7.87	7.89	7.91	7.93	7.95	7.97	7.99	8.01	8.0299999999999994	8.0500000000000007	8.07	8.09	8.11	8.1300000000000008	8.15	8.17	8.19	8.2100000000000009	8.23	8.25	8.27	8.2880000000000003	8.31	8.33	8.3480000000000008	8.3699999999999992	8.39	8.41	8.4280000000000008	8.4480000000000004	8.4700000000000006	8.49	8.51	8.5299999999999994	8.548	8.5679999999999996	8.5879999999999992	8.6080000000000005	8.6300000000000008	8.6479999999999997	8.6679999999999993	8.6880000000000006	8.7100000000000009	8.73	8.75	8.77	8.7899999999999991	8.81	8.83	8.85	8.8699999999999992	8.89	8.91	8.93	8.9499999999999993	8.9700000000000006	8.99	9.01	9.0299999999999994	9.0500000000000007	9.07	9.09	9.11	9.1280000000000001	9.1479999999999997	9.1679999999999993	9.1880000000000006	9.2100000000000009	9.2279999999999998	9.2479999999999993	9.2680000000000007	9.2880000000000003	9.3079999999999998	9.3279999999999994	9.3480000000000008	9.3680000000000003	9.3879999999999999	9.4079999999999995	9.4280000000000008	9.4480000000000004	9.468	9.4879999999999995	9.5079999999999991	9.5280000000000005	9.548	9.5679999999999996	9.5879999999999992	9.6080000000000005	9.6280000000000001	9.6479999999999997	9.6679999999999993	9.6880000000000006	9.7080000000000002	9.7279999999999998	9.7479999999999993	9.7680000000000007	9.7880000000000003	9.8079999999999998	9.8279999999999994	9.8480000000000008	9.8680000000000003	9.8879999999999999	9.9079999999999995	9.9280000000000008	9.9480000000000004	9.968	9.9879999999999995	10.007999999999999	10.029999999999999	10.050000000000001	10.068	10.09	10.11	10.128	10.148	10.17	10.19	10.210000000000001	10.23	10.25	10.27	10.29	10.31	10.33	10.35	10.37	10.39	10.41	10.43	10.45	10.47	10.49	10.51	10.53	10.55	10.57	10.59	10.61	10.632	10.65	10.67	10.69	10.71	10.73	10.75	10.77	10.79	10.81	10.83	10.85	10.87	10.89	10.91	10.93	10.95	10.97	10.99	11.01	11.03	11.05	11.07	11.09	11.11	11.13	11.15	11.17	11.19	11.21	11.23	11.25	11.27	11.29	11.31	11.33	11.35	11.37	11.39	11.41	11.428000000000001	11.45	11.468	11.488	11.51	11.53	11.55	11.57	11.59	11.61	11.63	11.65	11.67	11.69	11.71	11.73	11.75	11.77	11.79	11.81	11.83	11.85	11.87	11.89	11.91	11.93	11.95	11.97	11.99	12.01	12.03	12.05	12.07	12.09	12.11	12.13	12.15	12.17	12.19	12.21	12.23	12.25	12.27	12.29	12.31	12.33	12.35	12.37	12.39	12.41	12.43	12.45	12.47	12.49	12.51	12.53	12.55	12.57	12.59	12.61	12.63	12.65	12.67	12.69	12.71	12.73	12.75	12.77	12.79	12.81	12.826000000000001	12.85	12.87	12.89	12.91	12.93	12.95	12.97	12.99	13.01	13.03	13.05	13.07	13.09	13.11	13.13	13.15	13.17	13.19	13.21	13.23	13.25	13.27	13.29	13.31	13.33	13.35	13.37	13.39	13.41	13.43	13.446	13.465999999999999	13.486000000000001	13.506	13.526	13.545999999999999	13.566000000000001	13.586	13.606	13.625999999999999	13.646000000000001	13.666	13.686	13.706	13.726000000000001	13.746	13.766	13.786	13.804	13.824	13.843999999999999	13.864000000000001	13.884	13.904	13.923999999999999	13.944000000000001	13.964	13.984	14.004	14.023999999999999	14.044	14.064	14.084	14.103999999999999	14.124000000000001	14.144	14.164	14.183999999999999	14.204000000000001	14.224	14.244	14.263999999999999	14.284000000000001	14.304	14.324	14.343999999999999	14.364000000000001	14.384	14.404	14.423999999999999	14.444000000000001	14.464	14.484	14.504	14.523999999999999	14.544	14.564	14.584	14.603999999999999	14.624000000000001	14.644	14.664	14.683999999999999	14.704000000000001	14.724	14.744	14.763999999999999	14.784000000000001	14.804	14.824	14.843999999999999	14.864000000000001	14.884	14.904	14.923999999999999	14.944000000000001	14.964	14.984	15.004	15.022	15.044	15.061999999999999	15.084	15.102	15.122	15.144	15.162000000000001	15.182	15.202	15.222	15.242000000000001	15.262	15.282	15.302	15.321999999999999	15.342000000000001	15.362	15.382	15.401999999999999	15.422000000000001	15.442	15.462	15.481999999999999	15.502000000000001	15.522	15.542	15.561999999999999	15.582000000000001	15.602	15.622	15.641999999999999	15.662000000000001	15.682	15.702	15.722	15.742000000000001	15.762	15.782	15.802	15.821999999999999	15.842000000000001	15.862	15.882	15.901999999999999	15.922000000000001	15.942	15.962	15.981999999999999	16.001999999999999	16.021999999999998	16.042000000000002	16.062000000000001	16.082000000000001	16.102	16.122	16.141999999999999	16.161999999999999	16.18	16.2	16.218	16.239999999999998	16.257999999999999	16.277999999999999	16.297999999999998	16.318000000000001	16.338000000000001	16.358000000000001	16.378	16.398	16.417999999999999	16.437999999999999	16.457999999999998	16.478000000000002	16.498000000000001	16.518000000000001	16.536000000000001	16.556000000000001	16.576000000000001	16.596	16.616	16.635999999999999	16.655999999999999	16.675999999999998	16.696000000000002	16.716000000000001	16.736000000000001	16.756	16.776	16.795999999999999	16.815999999999999	16.835999999999999	16.856000000000002	16.876000000000001	16.896000000000001	16.916	16.936	16.956	16.975999999999999	16.995999999999999	17.015999999999998	17.036000000000001	17.056000000000001	17.076000000000001	17.096	17.116	17.135999999999999	17.155999999999999	17.175999999999998	17.196000000000002	17.216000000000001	17.236000000000001	17.256	17.276	17.295999999999999	17.315999999999999	17.335999999999999	17.356000000000002	17.378	17.398	17.417999999999999	17.436	17.456	17.478000000000002	17.498000000000001	17.515999999999998	17.538	17.558	17.576000000000001	17.596	17.616	17.635999999999999	17.655999999999999	17.675999999999998	17.696000000000002	17.716000000000001	17.736000000000001	17.756	17.776	17.795999999999999	17.815999999999999	17.835999999999999	17.856000000000002	17.876000000000001	17.896000000000001	17.916	17.936	17.956	17.975999999999999	17.995999999999999	18.015999999999998	18.036000000000001	18.056000000000001	18.076000000000001	18.096	18.116	18.135999999999999	18.155999999999999	18.175999999999998	18.198	18.218	18.238	18.257999999999999	18.277999999999999	18.297999999999998	18.318000000000001	18.338000000000001	18.358000000000001	18.378	18.398	18.417999999999999	18.437999999999999	18.457999999999998	18.478000000000002	18.498000000000001	18.518000000000001	18.538	18.558	18.577999999999999	18.597999999999999	18.617999999999999	18.638000000000002	18.658000000000001	18.678000000000001	18.698	18.718	18.738	18.757999999999999	18.777999999999999	18.797999999999998	18.818000000000001	18.838000000000001	18.858000000000001	18.878	18.898	18.917999999999999	18.937999999999999	18.957999999999998	18.978000000000002	18.998000000000001	19.018000000000001	19.038	19.058	19.077999999999999	19.097999999999999	19.117999999999999	19.135999999999999	19.155999999999999	19.175999999999998	19.198	19.216000000000001	19.236000000000001	19.256	19.276	19.295999999999999	19.315999999999999	19.335999999999999	19.356000000000002	19.376000000000001	19.396000000000001	19.416	19.436	19.456	19.475999999999999	19.495999999999999	19.515999999999998	19.536000000000001	19.556000000000001	19.576000000000001	19.596	19.616	19.632000000000001	19.655999999999999	19.672000000000001	19.692	19.712	19.736000000000001	19.751999999999999	19.771999999999998	19.792000000000002	19.812000000000001	19.832000000000001	19.852	19.872	19.896000000000001	19.911999999999999	19.931999999999999	19.956	19.972000000000001	19.992000000000001	20.015999999999998	20.036000000000001	20.056000000000001	20.076000000000001	20.096	20.116	20.132000000000001	20.152000000000001	20.175999999999998	20.193999999999999	20.213999999999999	20.234000000000002	20.254000000000001	20.274000000000001	20.294	20.314	20.334	20.353999999999999	20.372	20.391999999999999	20.411999999999999	20.431999999999999	20.452000000000002	20.472000000000001	20.492000000000001	20.513999999999999	20.532	20.552	20.571999999999999	20.591999999999999	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.333	1.333	1.333	1.333	1.333	1.556	1.556	1.556	1.556	1.778	1.778	1.778	1.778	2	2	2	2	2.222	2.222	2.222	2.444	2.444	2.6669999999999998	2.6669999999999998	2.6669999999999998	2.8889999999999998	2.8889999999999998	3.1110000000000002	3.1110000000000002	3.1110000000000002	3.3330000000000002	3.3330000000000002	3.556	3.556	3.778	3.778	4	4	4.2220000000000004	4.2220000000000004	4.444	4.6669999999999998	4.6669999999999998	4.8890000000000002	4.8890000000000002	5.1109999999999998	5.3330000000000002	5.3330000000000002	5.556	5.7779999999999996	5.7779999999999996	6	6.2220000000000004	6.2220000000000004	6.444	6.6669999999999998	6.6669999999999998	6.8890000000000002	7.1109999999999998	7.3330000000000002	7.556	7.7779999999999996	8	8.2219999999999995	8.4440000000000008	8.6669999999999998	8.8889999999999993	9.1110000000000007	9.3330000000000002	9.5559999999999992	9.7780000000000005	10	10.222	10.444000000000001	10.667	10.888999999999999	11.111000000000001	11.333	11.555999999999999	11.778	12	12.222	12.444000000000001	12.667	12.888999999999999	13.111000000000001	13.333	13.555999999999999	13.778	14	14.222	14.444000000000001	14.667	14.888999999999999	15.111000000000001	15.333	15.555999999999999	15.778	15.778	16.222000000000001	16.443999999999999	16.443999999999999	16.667000000000002	16.888999999999999	17.111000000000001	17.332999999999998	17.556000000000001	17.777999999999999	18	18.222000000000001	18.443999999999999	18.667000000000002	18.888999999999999	18.888999999999999	19.332999999999998	19.556000000000001	19.556000000000001	19.777999999999999	20	20.222000000000001	20.443999999999999	20.667000000000002	20.667000000000002	20.888999999999999	21.111000000000001	21.332999999999998	21.556000000000001	21.777999999999999	22	22.222000000000001	22.222000000000001	22.443999999999999	22.667000000000002	22.888999999999999	22.888999999999999	23.111000000000001	23.332999999999998	23.556000000000001	23.556000000000001	23.777999999999999	24	24.222000000000001	24.222000000000001	24.443999999999999	24.667000000000002	24.888999999999999	24.888999999999999	25.111000000000001	25.332999999999998	25.332999999999998	25.556000000000001	25.777999999999999	26	26.222000000000001	26.222000000000001	26.443999999999999	26.667000000000002	26.667000000000002	26.888999999999999	27.111000000000001	27.111000000000001	27.332999999999998	27.556000000000001	27.556000000000001	27.777999999999999	28	28	28.222000000000001	28.443999999999999	28.443999999999999	28.667000000000002	28.667000000000002	28.888999999999999	29.111000000000001	29.332999999999998	29.332999999999998	29.556000000000001	29.777999999999999	29.777999999999999	30	30.222000000000001	30.222000000000001	30.443999999999999	30.443999999999999	30.667000000000002	30.888999999999999	30.888999999999999	31.111000000000001	31.332999999999998	31.332999999999998	31.556000000000001	31.777999999999999	31.777999999999999	32	32.222000000000001	32.222000000000001	32.444000000000003	32.444000000000003	32.667000000000002	32.889000000000003	32.889000000000003	33.110999999999997	33.110999999999997	33.332999999999998	33.555999999999997	33.555999999999997	33.777999999999999	34	34.222000000000001	34.222000000000001	34.444000000000003	34.444000000000003	34.667000000000002	34.889000000000003	34.889000000000003	35.110999999999997	35.332999999999998	35.332999999999998	35.555999999999997	35.555999999999997	35.777999999999999	36	36.222000000000001	36.222000000000001	36.444000000000003	36.667000000000002	36.667000000000002	36.889000000000003	37.110999999999997	37.110999999999997	37.332999999999998	37.555999999999997	37.555999999999997	37.777999999999999	37.777999999999999	38	38.222000000000001	38.222000000000001	38.444000000000003	38.667000000000002	38.667000000000002	38.889000000000003	39.110999999999997	39.332999999999998	39.332999999999998	39.555999999999997	39.777999999999999	40	40	40.222000000000001	40.444000000000003	40.444000000000003	40.667000000000002	40.889000000000003	41.110999999999997	41.332999999999998	41.555999999999997	41.555999999999997	41.777999999999999	42	42.222000000000001	42.444000000000003	42.667000000000002	42.889000000000003	43.110999999999997	43.332999999999998	43.555999999999997	43.777999999999999	44	44.222000000000001	44.444000000000003	44.889000000000003	45.110999999999997	45.332999999999998	45.555999999999997	45.777999999999999	46	46.444000000000003	46.667000000000002	47.110999999999997	47.332999999999998	47.555999999999997	48	48.222000000000001	48.444000000000003	48.889000000000003	49.332999999999998	49.555999999999997	49.777999999999999	50.222000000000001	50.667000000000002	50.889000000000003	51.110999999999997	51.555999999999997	51.777999999999999	52.222000000000001	52.667000000000002	52.889000000000003	53.332999999999998	53.555999999999997	54	54.444000000000003	54.667000000000002	55.110999999999997	55.332999999999998	55.777999999999999	56.222000000000001	56.444000000000003	56.889000000000003	57.110999999999997	57.555999999999997	57.777999999999999	58	58.667000000000002	58.889000000000003	59.110999999999997	59.555999999999997	59.777999999999999	60.222000000000001	60.444000000000003	60.889000000000003	61.110999999999997	61.555999999999997	61.777999999999999	62.222000000000001	62.444000000000003	62.667000000000002	63.110999999999997	63.332999999999998	63.777999999999999	64	64.444000000000003	64.667000000000002	64.888999999999996	65.332999999999998	65.555999999999997	65.778000000000006	66.221999999999994	66.444000000000003	66.888999999999996	67.111000000000004	67.332999999999998	67.778000000000006	68	68.221999999999994	68.444000000000003	68.888999999999996	69.111000000000004	69.332999999999998	69.555999999999997	70	70.221999999999994	70.667000000000002	70.888999999999996	71.111000000000004	71.332999999999998	71.555999999999997	72	72.221999999999994	72.444000000000003	72.667000000000002	72.888999999999996	73.111000000000004	73.332999999999998	73.555999999999997	73.778000000000006	74	74.221999999999994	74.444000000000003	74.667000000000002	74.667000000000002	74.888999999999996	74.888999999999996	75.111000000000004	75.111000000000004	75.332999999999998	75.332999999999998	75.332999999999998	75.555999999999997	75.555999999999997	75.555999999999997	75.778000000000006	75.778000000000006	76	76.221999999999994	76.221999999999994	76.444000000000003	76.667000000000002	76.888999999999996	77.111000000000004	77.555999999999997	77.778000000000006	78	78.221999999999994	78.667000000000002	78.888999999999996	79.111000000000004	79.332999999999998	79.555999999999997	79.778000000000006	80	80.221999999999994	80.444000000000003	80.667000000000002	80.888999999999996	81.111000000000004	81.332999999999998	81.555999999999997	81.778000000000006	82	82	82.221999999999994	82.444000000000003	82.667000000000002	82.888999999999996	82.888999999999996	83.111000000000004	83.332999999999998	83.555999999999997	83.555999999999997	83.778000000000006	84	84.221999999999994	84.221999999999994	84.444000000000003	84.667000000000002	84.888999999999996	84.888999999999996	85.111000000000004	85.332999999999998	85.332999999999998	85.555999999999997	85.778000000000006	85.778000000000006	86	86.221999999999994	86.221999999999994	86.444000000000003	86.444000000000003	86.667000000000002	86.888999999999996	86.888999999999996	87.111000000000004	87.111000000000004	87.332999999999998	87.555999999999997	87.555999999999997	87.778000000000006	87.778000000000006	88	88.221999999999994	88.221999999999994	88.444000000000003	88.444000000000003	88.667000000000002	88.888999999999996	88.888999999999996	89.111000000000004	89.111000000000004	89.332999999999998	89.332999999999998	89.555999999999997	89.555999999999997	89.778000000000006	89.778000000000006	90	90.221999999999994	90.444000000000003	90.444000000000003	90.667000000000002	90.888999999999996	90.888999999999996	91.111000000000004	91.332999999999998	91.332999999999998	91.555999999999997	91.555999999999997	91.778000000000006	91.778000000000006	92	92	92.221999999999994	92.221999999999994	92.444000000000003	92.444000000000003	92.444000000000003	92.667000000000002	92.667000000000002	92.888999999999996	92.888999999999996	92.888999999999996	93.111000000000004	93.111000000000004	93.332999999999998	93.332999999999998	93.555999999999997	93.555999999999997	93.555999999999997	93.778000000000006	93.778000000000006	94	94	94	94.221999999999994	94.221999999999994	94.221999999999994	94.444000000000003	94.444000000000003	94.667000000000002	94.667000000000002	94.667000000000002	94.888999999999996	94.888999999999996	95.111000000000004	95.111000000000004	95.111000000000004	95.332999999999998	95.332999999999998	95.332999999999998	95.555999999999997	95.555999999999997	95.555999999999997	95.778000000000006	95.778000000000006	95.778000000000006	96	96	96	96.221999999999994	96.221999999999994	96.221999999999994	96.444000000000003	96.444000000000003	96.444000000000003	96.667000000000002	96.667000000000002	96.667000000000002	96.888999999999996	96.888999999999996	96.888999999999996	96.888999999999996	97.111000000000004	97.111000000000004	97.332999999999998	97.332999999999998	97.332999999999998	97.332999999999998	97.555999999999997	97.555999999999997	97.555999999999997	97.555999999999997	97.778000000000006	97.778000000000006	97.778000000000006	98	98	98	98	98.221999999999994	98.221999999999994	98.221999999999994	98.444000000000003	98.444000000000003	98.444000000000003	98.444000000000003	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.888999999999996	98.888999999999996	98.888999999999996	98.888999999999996	99.111000000000004	99.111000000000004	99.111000000000004	99.111000000000004	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.555999999999997	99.555999999999997	99.555999999999997	99.555999999999997	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	100	100	100	100	100	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.444	100.444	100.444	100.444	100.444	100.667	100.667	100.667	100.667	100.667	100.889	100.889	100.889	100.889	100.889	101.111	101.111	101.111	101.111	101.111	101.333	101.333	101.333	101.333	101.333	101.556	101.556	101.556	101.556	101.556	101.556	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	102	102	102	102	102	102	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.444	102.444	102.444	102.444	102.444	102.444	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.889	102.889	102.889	102.889	102.889	102.889	102.889	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	104	104	104	104	104	104	104	104	104	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	106	106	106	106	106	106	106	106	106	106	106	106	106	106	106	106	106	106	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	106.889	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.333	107.333	107.333	107.333	107.333	107.111	107.111	107.111	107.111	107.111	106.889	106.889	106.889	106.889	106.889	106.667	106.667	106.667	106.667	106.667	106.444	106.444	106.444	106.444	106.444	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106	106	106	106	106	106	106	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	102	102	102	102.22199999999999	102.22199999999999	102.444	102.444	102.667	102.667	102.889	102.889	103.111	103.333	103.333	103.556	103.77800000000001	103.77800000000001	104	104.22199999999999	104.22199999999999	104.444	104.667	104.889	104.889	105.111	105.333	105.556	105.77800000000001	105.77800000000001	106	106.22199999999999	106.444	106.667	106.667	106.889	107.111	107.333	107.556	107.556	107.77800000000001	108	108.22199999999999	108.444	108.667	108.889	109.111	109.333	109.556	109.77800000000001	110	110	110.22199999999999	110.22199999999999	110.444	110.444	110.444	110.667	110.667	110.667	110.667	110.889	110.889	110.889	110.889	110.889	110.889	110.889	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	112	112	112	112	112	112	112	112	112	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.444	110.444	110.444	110.444	110.444	110.444	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110	110	110	110	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.556	109.556	109.556	109.333	109.333	109.333	109.111	109.111	109.111	108.889	108.889	108.889	108.667	108.667	108.444	108.444	108.444	108.22199999999999	108.22199999999999	108	107.77800000000001	107.77800000000001	107.556	107.556	107.333	107.111	107.111	106.889	106.667	106.444	106.22199999999999	106	105.556	105.111	104.889	104.444	104	103.556	103.111	102.444	102	101.556	100.889	100.444	99.778000000000006	99.111000000000004	98.444000000000003	97.778000000000006	96.888999999999996	96.221999999999994	95.332999999999998	94.444000000000003	93.555999999999997	92.888999999999996	92	90.888999999999996	90.221999999999994	89.111000000000004	87.778000000000006	86.888999999999996	85.778000000000006	84.221999999999994	83.332999999999998	81.778000000000006	80.667000000000002	79.111000000000004	77.778000000000006	76	73.778000000000006	72.221999999999994	Sample 3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	3.0000000000000001E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	2E-3	1E-3	1E-3	0	0	0	1E-3	2E-3	2E-3	3.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	0.01	8.9999999999999993E-3	7.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	1.0999999999999999E-2	0.01	0.01	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	8.9999999999999993E-3	8.0000000000000002E-3	8.9999999999999993E-3	0.01	1.0999999999999999E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.0999999999999999E-2	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.4E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.2999999999999999E-2	1.2E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2999999999999999E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.2999999999999999E-2	1.0999999999999999E-2	0.01	0.01	0.01	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.6E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	0.01	0.01	0.01	8.9999999999999993E-3	0.01	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	1.0999999999999999E-2	1.2E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.6E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.2E-2	1.0999999999999999E-2	8.9999999999999993E-3	8.0000000000000002E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	0.01	0.01	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	0.01	0.01	1.0999999999999999E-2	1.2E-2	1.2E-2	1.4E-2	1.4E-2	1.4E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	0.01	0.01	0.01	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.0999999999999999E-2	0.01	0.01	1.0999999999999999E-2	1.2E-2	1.2E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2E-2	1.0999999999999999E-2	0.01	0.01	0.01	1.0999999999999999E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.7000000000000001E-2	1.6E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.6E-2	1.6E-2	1.6E-2	1.4999999999999999E-2	1.4E-2	1.4E-2	1.2999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.9E-2	1.9E-2	1.9E-2	1.9E-2	1.9E-2	0.02	2.1000000000000001E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.3E-2	2.3E-2	2.1999999999999999E-2	0.02	1.9E-2	1.9E-2	0.02	2.1999999999999999E-2	2.3E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.7E-2	2.7E-2	2.7E-2	2.7E-2	2.8000000000000001E-2	2.7E-2	2.5999999999999999E-2	2.5999999999999999E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.7E-2	2.8000000000000001E-2	2.9000000000000001E-2	2.9000000000000001E-2	0.03	0.03	0.03	3.1E-2	3.2000000000000001E-2	3.3000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.4000000000000002E-2	3.5999999999999997E-2	3.6999999999999998E-2	3.9E-2	0.04	0.04	4.1000000000000002E-2	4.1000000000000002E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2000000000000003E-2	4.2999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.3999999999999997E-2	4.4999999999999998E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.7E-2	4.8000000000000001E-2	4.9000000000000002E-2	0.05	0.05	0.05	5.0999999999999997E-2	5.1999999999999998E-2	5.3999999999999999E-2	5.5E-2	5.6000000000000001E-2	5.8000000000000003E-2	5.8000000000000003E-2	5.8999999999999997E-2	0.06	0.06	0.06	0.06	0.06	0.06	6.0999999999999999E-2	6.2E-2	6.2E-2	6.2E-2	6.0999999999999999E-2	0.06	5.8999999999999997E-2	0.06	0.06	0.06	6.0999999999999999E-2	6.0999999999999999E-2	6.2E-2	6.3E-2	6.4000000000000001E-2	6.5000000000000002E-2	6.7000000000000004E-2	6.8000000000000005E-2	7.0000000000000007E-2	7.1999999999999995E-2	7.2999999999999995E-2	7.3999999999999996E-2	7.3999999999999996E-2	7.3999999999999996E-2	7.3999999999999996E-2	7.3999999999999996E-2	7.2999999999999995E-2	7.1999999999999995E-2	7.2999999999999995E-2	7.3999999999999996E-2	7.4999999999999997E-2	7.4999999999999997E-2	7.5999999999999998E-2	7.5999999999999998E-2	7.6999999999999999E-2	7.8E-2	7.8E-2	7.9000000000000001E-2	0.08	8.1000000000000003E-2	8.2000000000000003E-2	8.2000000000000003E-2	8.3000000000000004E-2	8.3000000000000004E-2	8.3000000000000004E-2	8.3000000000000004E-2	8.4000000000000005E-2	8.4000000000000005E-2	8.5999999999999993E-2	8.6999999999999994E-2	8.8999999999999996E-2	0.09	9.0999999999999998E-2	9.1999999999999998E-2	9.1999999999999998E-2	9.2999999999999999E-2	9.2999999999999999E-2	9.2999999999999999E-2	9.2999999999999999E-2	9.4E-2	9.2999999999999999E-2	9.4E-2	9.4E-2	9.5000000000000001E-2	9.6000000000000002E-2	9.7000000000000003E-2	9.7000000000000003E-2	9.7000000000000003E-2	9.7000000000000003E-2	9.8000000000000004E-2	9.8000000000000004E-2	9.9000000000000005E-2	0.1	0.10100000000000001	0.10199999999999999	0.104	0.106	0.107	0.108	0.108	0.109	0.108	0.108	0.107	0.106	0.105	0.104	0.10299999999999999	0.10299999999999999	0.10199999999999999	0.10199999999999999	0.10199999999999999	0.10199999999999999	0.10199999999999999	0.10199999999999999	0.10299999999999999	0.10299999999999999	0.104	0.104	0.105	0.107	0.11	0.112	0.114	0.11600000000000001	0.11700000000000001	0.11899999999999999	0.12	0.121	0.122	0.123	0.123	0.123	0.123	0.123	0.121	0.121	0.11899999999999999	0.11899999999999999	0.12	0.122	0.125	0.127	0.129	0.13100000000000001	0.13200000000000001	0.13400000000000001	0.13500000000000001	0.13600000000000001	0.13600000000000001	0.13600000000000001	0.13600000000000001	0.13600000000000001	0.13700000000000001	0.13800000000000001	0.13900000000000001	0.13900000000000001	0.13900000000000001	0.13900000000000001	0.14000000000000001	0.13900000000000001	0.13800000000000001	0.13800000000000001	0.13800000000000001	0.13900000000000001	0.14099999999999999	0.14299999999999999	0.14499999999999999	0.14699999999999999	0.14899999999999999	0.15	0.152	0.152	0.153	0.154	0.154	0.153	0.153	0.153	0.154	0.156	0.156	0.157	0.158	0.159	0.159	0.16	0.16	0.16	0.161	0.16200000000000001	0.16400000000000001	0.16500000000000001	0.16600000000000001	0.16600000000000001	0.16500000000000001	0.16500000000000001	0.16500000000000001	0.16600000000000001	0.16700000000000001	0.16800000000000001	0.16900000000000001	0.17	0.17199999999999999	0.17199999999999999	0.17299999999999999	0.17399999999999999	0.17399999999999999	0.17499999999999999	0.17599999999999999	0.17799999999999999	0.17799999999999999	0.17899999999999999	0.18	0.18099999999999999	0.18099999999999999	0.182	0.182	0.183	0.184	0.184	0.186	0.187	0.187	0.187	0.186	0.185	0.185	0.186	0.187	0.189	0.19	0.191	0.192	0.192	0.192	0.19400000000000001	0.19400000000000001	0.19400000000000001	0.193	0.192	0.192	0.192	0.192	0.193	0.19400000000000001	0.19600000000000001	0.19700000000000001	0.19700000000000001	0.19800000000000001	0.19900000000000001	0.2	0.2	0.20100000000000001	0.20200000000000001	0.20300000000000001	0.20399999999999999	0.20399999999999999	0.20399999999999999	0.20399999999999999	0.20399999999999999	0.20499999999999999	0.20599999999999999	0.20699999999999999	0.20799999999999999	0.20899999999999999	0.21	0.21099999999999999	0.21299999999999999	0.214	0.214	0.214	0.216	0.215	0.215	0.216	0.217	0.218	0.219	0.219	0.219	0.219	0.218	0.218	0.218	0.216	0.216	0.216	0.217	0.217	0.217	0.216	0.216	0.216	0.216	0.216	0.218	0.22	0.222	0.224	0.22600000000000001	0.22800000000000001	0.23	0.23100000000000001	0.23200000000000001	0.23200000000000001	0.23400000000000001	0.23400000000000001	0.23400000000000001	0.23300000000000001	0.23300000000000001	0.23400000000000001	0.23499999999999999	0.23599999999999999	0.23699999999999999	0.23799999999999999	0.23799999999999999	0.23799999999999999	0.23699999999999999	0.23599999999999999	0.23599999999999999	0.23599999999999999	0.23799999999999999	0.23899999999999999	0.24	0.24	0.23899999999999999	0.23799999999999999	0.23599999999999999	0.23499999999999999	0.23499999999999999	0.23499999999999999	0.23400000000000001	0.23400000000000001	0.23400000000000001	0.23300000000000001	0.23300000000000001	0.23499999999999999	0.23799999999999999	0.24	0.24199999999999999	0.245	0.247	0.247	0.246	0.246	0.246	0.246	0.246	0.247	0.248	0.248	0.248	0.247	0.246	0.247	0.249	0.249	0.25	0.251	0.252	0.254	0.252	0.252	0.252	0.254	0.254	0.255	0.25600000000000001	0.25800000000000001	0.26	0.26200000000000001	0.26200000000000001	0.26200000000000001	0.26100000000000001	0.26	0.26	0.26	0.26100000000000001	0.26200000000000001	0.26300000000000001	0.26500000000000001	0.26600000000000001	0.26700000000000002	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26700000000000002	0.26700000000000002	0.26700000000000002	0.26700000000000002	0.26700000000000002	0.26800000000000002	0.26900000000000002	0.27	0.27	0.27	0.27200000000000002	0.27400000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27600000000000002	0.27600000000000002	0.27600000000000002	0.27600000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27900000000000003	0.28100000000000003	0.28399999999999997	0.28599999999999998	0.28699999999999998	0.28899999999999998	0.28999999999999998	0.29099999999999998	0.29199999999999998	0.29299999999999998	0.29399999999999998	0.29599999999999999	0.29699999999999999	0.29699999999999999	0.29699999999999999	0.29799999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.3	0.3	0.3	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30399999999999999	0.30399999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30499999999999999	0.30499999999999999	0.30599999999999999	0.30499999999999999	0.30499999999999999	0.30499999999999999	0.30499999999999999	0.307	0.308	0.309	0.309	0.309	0.31	0.31	0.31	0.31	0.309	0.309	0.309	0.309	0.31	0.31	0.312	0.313	0.315	0.317	0.318	0.32	0.32100000000000001	0.32100000000000001	0.32100000000000001	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32300000000000001	0.32200000000000001	0.32100000000000001	0.32100000000000001	0.32200000000000001	0.32400000000000001	0.32500000000000001	0.32500000000000001	0.32500000000000001	0.32600000000000001	0.32700000000000001	0.32800000000000001	0.33	0.33	0.33100000000000002	0.33200000000000002	0.33400000000000002	0.33500000000000002	0.33600000000000002	0.33700000000000002	0.33800000000000002	0.33900000000000002	0.33900000000000002	0.33800000000000002	0.33700000000000002	0.33500000000000002	0.33400000000000002	0.33300000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33500000000000002	0.33800000000000002	0.34100000000000003	0.34300000000000003	0.34399999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34799999999999998	0.34899999999999998	0.35	0.35099999999999998	0.35199999999999998	0.35099999999999998	0.35	0.35	0.35099999999999998	0.35199999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35599999999999998	0.35499999999999998	0.35399999999999998	0.35299999999999998	0.35399999999999998	0.35499999999999998	0.35599999999999998	0.35699999999999998	0.35799999999999998	0.35899999999999999	0.36	0.36099999999999999	0.36299999999999999	0.36299999999999999	0.36099999999999999	0.35699999999999998	0.35199999999999998	0.34799999999999998	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34699999999999998	0.34699999999999998	0.34599999999999997	0.34599999999999997	0.34799999999999998	0.35	0.35299999999999998	0.35399999999999998	0.35499999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35699999999999998	0.35899999999999999	0.36099999999999999	0.36299999999999999	0.36399999999999999	0.36599999999999999	0.36799999999999999	0.36899999999999999	0.37	0.371	0.372	0.372	0.372	0.372	0.372	0.373	0.373	0.373	0.374	0.375	0.378	0.378	0.378	0.378	0.379	0.379	0.38	0.38200000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38600000000000001	0.38700000000000001	0.38700000000000001	0.38700000000000001	0.38800000000000001	0.38900000000000001	0.38900000000000001	0.38900000000000001	0.38800000000000001	0.38800000000000001	0.38700000000000001	0.38700000000000001	0.38700000000000001	0.38800000000000001	0.38900000000000001	0.39	0.39200000000000002	0.39400000000000002	0.39400000000000002	0.39400000000000002	0.39400000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39400000000000002	0.39400000000000002	0.39300000000000002	0.39200000000000002	0.39300000000000002	0.39500000000000002	0.39700000000000002	0.39800000000000002	0.4	0.4	0.40200000000000002	0.40300000000000002	0.40400000000000003	0.40500000000000003	0.40699999999999997	0.40899999999999997	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41	0.40899999999999997	0.40799999999999997	0.40699999999999997	0.40400000000000003	0.40100000000000002	0.4	0.4	0.4	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40500000000000003	0.40799999999999997	0.41	0.41	0.41	0.41199999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41299999999999998	0.41199999999999998	0.41099999999999998	0.41	0.41	0.41099999999999998	0.41299999999999998	0.41499999999999998	0.41699999999999998	0.41799999999999998	0.42	0.42199999999999999	0.42299999999999999	0.42399999999999999	0.42499999999999999	0.42599999999999999	0.42699999999999999	0.42699999999999999	0.42699999999999999	0.42599999999999999	0.42599999999999999	0.42499999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42799999999999999	0.42799999999999999	0.42899999999999999	0.42899999999999999	0.42799999999999999	0.42799999999999999	0.42699999999999999	0.42699999999999999	0.42799999999999999	0.42799999999999999	0.42899999999999999	0.43	0.43099999999999999	0.432	0.434	0.434	0.436	0.438	0.439	0.44	0.441	0.441	0.441	0.441	0.44	0.441	0.441	0.442	0.44400000000000001	0.44600000000000001	0.44800000000000001	0.45200000000000001	0.45400000000000001	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45700000000000002	0.45700000000000002	0.45600000000000002	0.45600000000000002	0.45600000000000002	0.45500000000000002	0.45500000000000002	0.45500000000000002	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45600000000000002	0.45600000000000002	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45800000000000002	0.46	0.46	0.46	0.46	0.46200000000000002	0.46300000000000002	0.46400000000000002	0.46500000000000002	0.46500000000000002	0.46500000000000002	0.46500000000000002	0.46600000000000003	0.46700000000000003	0.46700000000000003	0.46600000000000003	0.46600000000000003	0.46600000000000003	0.46600000000000003	0.46800000000000003	0.46899999999999997	0.47	0.47	0.47	0.47099999999999997	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47199999999999998	0.47099999999999997	0.47099999999999997	0.47299999999999998	0.47499999999999998	0.47599999999999998	0.47699999999999998	0.47799999999999998	0.47899999999999998	0.48	0.48199999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48399999999999999	0.48299999999999998	0.48199999999999998	0.48199999999999998	0.48099999999999998	0.48	0.47899999999999998	0.47899999999999998	0.47899999999999998	0.47899999999999998	0.48	0.48199999999999998	0.48299999999999998	0.48499999999999999	0.48799999999999999	0.49	0.49099999999999999	0.49299999999999999	0.495	0.497	0.498	0.499	0.499	0.498	0.496	0.49399999999999999	0.49199999999999999	0.49199999999999999	0.49099999999999999	0.49199999999999999	0.49399999999999999	0.496	0.496	0.498	0.498	0.5	0.502	0.504	0.504	0.504	0.504	0.504	0.503	0.503	0.503	0.504	0.505	0.50600000000000001	0.50600000000000001	0.50700000000000001	0.50900000000000001	0.50900000000000001	0.50900000000000001	0.50900000000000001	0.51	0.51200000000000001	0.51200000000000001	0.51200000000000001	0.51200000000000001	0.51	0.50900000000000001	0.50900000000000001	0.50800000000000001	0.50800000000000001	0.51	0.51200000000000001	0.51400000000000001	0.51500000000000001	0.51500000000000001	0.51400000000000001	0.51300000000000001	0.51300000000000001	0.51300000000000001	0.51300000000000001	0.51200000000000001	0.51200000000000001	0.51100000000000001	0.51200000000000001	0.51200000000000001	0.51400000000000001	0.51500000000000001	0.51600000000000001	0.51800000000000002	0.51800000000000002	0.52	0.52400000000000002	0.52600000000000002	0.52800000000000002	0.53	0.53	0.52900000000000003	0.52900000000000003	0.53	0.53	0.53	0.53100000000000003	0.53	0.52900000000000003	0.52900000000000003	0.52900000000000003	0.52800000000000002	0.52700000000000002	0.52600000000000002	0.52600000000000002	0.52700000000000002	0.53	0.53200000000000003	0.53600000000000003	0.53800000000000003	0.54	0.54	0.504	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50800000000000001	0.51	0.51	0.51400000000000001	0.51600000000000001	0.51800000000000002	0.52	0.52400000000000002	0.52600000000000002	0.53	0.53400000000000003	0.53800000000000003	0.54	0.54600000000000004	0.54800000000000004	0.55400000000000005	0.55800000000000005	0.56399999999999995	0.56799999999999995	0.57399999999999995	0.57799999999999996	0.58599999999999997	0.59	0.59599999999999997	0.60399999999999998	0.61	0.61599999999999999	0.624	0.63	0.63600000000000001	0.64400000000000002	0.65400000000000003	0.66	0.66800000000000004	0.67600000000000005	0.68400000000000005	0.69399999999999995	0.7	0.71	0.72	0.73	0.74	0.75	0.75800000000000001	0.77	0.78	0.79	0.80400000000000005	0.81399999999999995	0.82399999999999995	0.83599999999999997	0.84799999999999998	0.85799999999999998	0.87	0.88400000000000001	0.89600000000000002	0.90800000000000003	0.92	0.93600000000000005	0.94799999999999995	0.96	0.97599999999999998	0.98799999999999999	1.004	1.018	1.03	1.046	1.06	1.0760000000000001	1.0900000000000001	1.1060000000000001	1.1240000000000001	1.1379999999999999	1.1559999999999999	1.17	1.1879999999999999	1.204	1.22	1.238	1.256	1.274	1.29	1.3080000000000001	1.3280000000000001	1.3460000000000001	1.3640000000000001	1.3839999999999999	1.4039999999999999	1.42	1.44	1.46	1.48	1.5	1.52	1.54	1.56	1.58	1.6	1.6240000000000001	1.6439999999999999	1.6639999999999999	1.6839999999999999	1.704	1.724	1.744	1.764	1.784	1.806	1.8260000000000001	1.8460000000000001	1.8660000000000001	1.8859999999999999	1.9059999999999999	1.9259999999999999	1.946	1.966	1.986	2.0059999999999998	2.028	2.0459999999999998	2.0659999999999998	2.0859999999999999	2.1080000000000001	2.1280000000000001	2.1480000000000001	2.1680000000000001	2.1880000000000002	2.2080000000000002	2.2280000000000002	2.2480000000000002	2.2679999999999998	2.2879999999999998	2.3079999999999998	2.3279999999999998	2.3479999999999999	2.3679999999999999	2.3879999999999999	2.4079999999999999	2.4279999999999999	2.448	2.468	2.488	2.508	2.528	2.548	2.5680000000000001	2.5880000000000001	2.6080000000000001	2.6259999999999999	2.6480000000000001	2.6680000000000001	2.6880000000000002	2.7080000000000002	2.7280000000000002	2.7480000000000002	2.7679999999999998	2.7879999999999998	2.8079999999999998	2.8279999999999998	2.8479999999999999	2.8679999999999999	2.8879999999999999	2.9079999999999999	2.9279999999999999	2.948	2.968	2.988	3.008	3.03	3.048	3.0680000000000001	3.09	3.11	3.13	3.15	3.17	3.19	3.21	3.23	3.25	3.27	3.29	3.31	3.33	3.35	3.37	3.39	3.41	3.43	3.45	3.47	3.49	3.51	3.53	3.55	3.57	3.59	3.61	3.63	3.65	3.67	3.69	3.7080000000000002	3.73	3.7480000000000002	3.7679999999999998	3.79	3.8079999999999998	3.8279999999999998	3.8479999999999999	3.8679999999999999	3.8879999999999999	3.91	3.93	3.948	3.968	3.99	4.008	4.0279999999999996	4.048	4.0679999999999996	4.0880000000000001	4.1079999999999997	4.13	4.1479999999999997	4.17	4.1879999999999997	4.2080000000000002	4.2300000000000004	4.25	4.2699999999999996	4.29	4.3099999999999996	4.33	4.3499999999999996	4.37	4.3899999999999997	4.41	4.43	4.45	4.47	4.492	4.5119999999999996	4.532	4.55	4.5720000000000001	4.5919999999999996	4.6120000000000001	4.6319999999999997	4.6520000000000001	4.6719999999999997	4.6920000000000002	4.7119999999999997	4.7320000000000002	4.7519999999999998	4.7720000000000002	4.7919999999999998	4.8120000000000003	4.8319999999999999	4.8520000000000003	4.8739999999999997	4.8920000000000003	4.9119999999999999	4.9340000000000002	4.952	4.9720000000000004	4.992	5.0119999999999996	5.0339999999999998	5.0519999999999996	5.0720000000000001	5.0919999999999996	5.1120000000000001	5.1319999999999997	5.1520000000000001	5.1719999999999997	5.1920000000000002	5.2119999999999997	5.2320000000000002	5.2519999999999998	5.2720000000000002	5.2919999999999998	5.3120000000000003	5.3319999999999999	5.35	5.3719999999999999	5.3920000000000003	5.4119999999999999	5.43	5.45	5.4720000000000004	5.49	5.5119999999999996	5.53	5.5519999999999996	5.57	5.59	5.6120000000000001	5.63	5.65	5.6719999999999997	5.69	5.71	5.7320000000000002	5.75	5.77	5.79	5.81	5.8319999999999999	5.85	5.87	5.8920000000000003	5.91	5.9320000000000004	5.95	5.97	5.992	6.0119999999999996	6.03	6.0519999999999996	6.0720000000000001	6.09	6.1120000000000001	6.13	6.15	6.1719999999999997	6.19	6.21	6.2320000000000002	6.25	6.2720000000000002	6.29	6.31	6.33	6.35	6.37	6.39	6.41	6.43	6.45	6.47	6.49	6.51	6.53	6.55	6.57	6.59	6.61	6.63	6.65	6.67	6.69	6.71	6.73	6.75	6.77	6.79	6.81	6.83	6.85	6.87	6.89	6.91	6.93	6.95	6.9720000000000004	6.99	7.01	7.03	7.05	7.0720000000000001	7.09	7.1120000000000001	7.13	7.15	7.1719999999999997	7.1920000000000002	7.2119999999999997	7.2320000000000002	7.2519999999999998	7.2720000000000002	7.2919999999999998	7.3120000000000003	7.3319999999999999	7.3520000000000003	7.3719999999999999	7.3920000000000003	7.4119999999999999	7.4320000000000004	7.452	7.4740000000000002	7.4939999999999998	7.5140000000000002	7.5339999999999998	7.5540000000000003	7.5739999999999998	7.5940000000000003	7.6139999999999999	7.6340000000000003	7.6539999999999999	7.6740000000000004	7.694	7.7140000000000004	7.734	7.7539999999999996	7.774	7.7939999999999996	7.8140000000000001	7.8339999999999996	7.8540000000000001	7.8739999999999997	7.8940000000000001	7.9139999999999997	7.9340000000000002	7.9539999999999997	7.9740000000000002	7.9939999999999998	8.0139999999999993	8.0340000000000007	8.0540000000000003	8.0739999999999998	8.0920000000000005	8.1120000000000001	8.1319999999999997	8.1519999999999992	8.1739999999999995	8.1920000000000002	8.2140000000000004	8.2319999999999993	8.2539999999999996	8.2720000000000002	8.2919999999999998	8.3140000000000001	8.3320000000000007	8.3520000000000003	8.3740000000000006	8.3919999999999995	8.4120000000000008	8.4339999999999993	8.452	8.4719999999999995	8.4939999999999998	8.5120000000000005	8.532	8.5540000000000003	8.5719999999999992	8.5920000000000005	8.6140000000000008	8.6319999999999997	8.6519999999999992	8.6739999999999995	8.6940000000000008	8.7140000000000004	8.734	8.7539999999999996	8.7739999999999991	8.7940000000000005	8.8140000000000001	8.8339999999999996	8.8520000000000003	8.8740000000000006	8.8940000000000001	8.9139999999999997	8.9339999999999993	8.9540000000000006	8.9740000000000002	8.9939999999999998	9.0139999999999993	9.0340000000000007	9.0540000000000003	9.0739999999999998	9.0939999999999994	9.1120000000000001	9.1340000000000003	9.1539999999999999	9.1739999999999995	9.1940000000000008	9.2140000000000004	9.234	9.2539999999999996	9.2739999999999991	9.2919999999999998	9.3140000000000001	9.3339999999999996	9.3520000000000003	9.3719999999999999	9.3919999999999995	9.4139999999999997	9.4320000000000004	9.452	9.4719999999999995	9.4920000000000009	9.5120000000000005	9.532	9.5519999999999996	9.5739999999999998	9.5920000000000005	9.6140000000000008	9.6319999999999997	9.6519999999999992	9.6720000000000006	9.6920000000000002	9.7119999999999997	9.7319999999999993	9.7520000000000007	9.7739999999999991	9.7919999999999998	9.8119999999999994	9.8320000000000007	9.8520000000000003	9.8719999999999999	9.8919999999999995	9.9120000000000008	9.9320000000000004	9.952	9.9719999999999995	9.9920000000000009	10.012	10.029999999999999	10.050000000000001	10.074	10.09	10.11	10.130000000000001	10.15	10.173999999999999	10.19	10.210000000000001	10.23	10.25	10.27	10.29	10.314	10.33	10.35	10.37	10.39	10.414	10.43	10.45	10.47	10.49	10.51	10.53	10.55	10.57	10.59	10.61	10.63	10.65	10.67	10.69	10.71	10.73	10.75	10.77	10.79	10.81	10.827999999999999	10.85	10.868	10.888	10.907999999999999	10.928000000000001	10.948	10.968	10.988	11.007999999999999	11.028	11.048	11.068	11.087999999999999	11.108000000000001	11.128	11.148	11.167999999999999	11.188000000000001	11.208	11.228	11.247999999999999	11.268000000000001	11.288	11.305999999999999	11.327999999999999	11.348000000000001	11.368	11.388	11.407999999999999	11.428000000000001	11.448	11.468	11.488	11.507999999999999	11.528	11.548	11.566000000000001	11.587999999999999	11.608000000000001	11.628	11.648	11.667999999999999	11.688000000000001	11.708	11.728	11.747999999999999	11.768000000000001	11.788	11.808	11.827999999999999	11.848000000000001	11.868	11.888	11.907999999999999	11.928000000000001	11.948	11.968	11.988	12.006	12.028	12.045999999999999	12.068	12.086	12.108000000000001	12.125999999999999	12.146000000000001	12.166	12.186	12.208	12.226000000000001	12.246	12.266	12.286	12.305999999999999	12.326000000000001	12.346	12.366	12.385999999999999	12.406000000000001	12.426	12.446	12.465999999999999	12.486000000000001	12.506	12.526	12.545999999999999	12.566000000000001	12.586	12.606	12.622	12.646000000000001	12.666	12.686	12.706	12.726000000000001	12.746	12.766	12.782	12.805999999999999	12.826000000000001	12.846	12.866	12.885999999999999	12.906000000000001	12.926	12.946	12.965999999999999	12.986000000000001	13.006	13.026	13.042	13.061999999999999	13.082000000000001	13.106	13.125999999999999	13.141999999999999	13.166	13.182	13.202	13.222	13.246	13.262	13.282	13.302	13.321999999999999	13.342000000000001	13.362	13.382	13.401999999999999	13.422000000000001	13.442	13.462	13.481999999999999	13.5	13.52	13.542	13.56	13.58	13.6	13.62	13.64	13.66	13.68	13.7	13.72	13.74	13.76	13.78	13.8	13.82	13.84	13.86	13.88	13.9	13.92	13.94	13.96	13.98	14	14.02	14.04	14.06	14.08	14.1	14.12	14.14	14.16	14.18	14.2	14.22	14.24	14.26	14.28	14.3	14.32	14.34	14.36	14.38	14.4	14.42	14.44	14.46	14.48	14.5	14.52	14.54	14.56	14.58	14.6	14.62	14.64	14.66	14.68	14.7	14.72	14.74	14.76	14.78	14.8	14.82	14.84	14.86	14.88	14.9	14.92	14.94	14.96	14.98	15	15.02	15.04	15.06	15.08	15.1	15.12	15.14	15.16	15.18	15.2	15.22	15.24	15.26	15.28	15.3	15.32	15.34	15.36	15.38	15.4	15.42	15.44	15.46	15.48	15.5	15.522	15.54	15.561999999999999	15.58	15.602	15.622	15.641999999999999	15.662000000000001	15.682	15.702	15.722	15.742000000000001	15.762	15.782	15.802	15.821999999999999	15.842000000000001	15.862	15.882	15.901999999999999	15.922000000000001	15.942	15.962	15.981999999999999	16	16.021999999999998	16.042000000000002	16.059999999999999	16.082000000000001	16.102	16.12	16.14	16.16	16.181999999999999	16.2	16.22	16.239999999999998	16.260000000000002	16.28	16.3	16.32	16.34	16.36	16.38	16.399999999999999	16.420000000000002	16.440000000000001	16.456	16.48	16.495999999999999	16.515999999999998	16.54	16.556000000000001	16.576000000000001	16.596	16.616	16.635999999999999	16.655999999999999	16.675999999999998	16.696000000000002	16.716000000000001	16.736000000000001	16.756	16.776	16.795999999999999	16.815999999999999	16.835999999999999	16.856000000000002	16.876000000000001	16.896000000000001	16.916	16.936	16.956	16.975999999999999	16.995999999999999	17.015999999999998	17.036000000000001	17.056000000000001	17.076000000000001	17.096	17.116	17.135999999999999	17.155999999999999	17.175999999999998	17.196000000000002	17.216000000000001	17.236000000000001	17.256	17.276	17.295999999999999	17.315999999999999	17.335999999999999	17.356000000000002	17.376000000000001	17.396000000000001	17.416	17.436	17.456	17.475999999999999	17.495999999999999	17.515999999999998	17.536000000000001	17.556000000000001	17.576000000000001	17.596	17.616	17.635999999999999	17.655999999999999	17.675999999999998	17.696000000000002	17.716000000000001	17.736000000000001	17.756	17.776	17.795999999999999	17.815999999999999	17.835999999999999	17.856000000000002	17.873999999999999	17.896000000000001	17.916	17.936	17.956	17.975999999999999	17.995999999999999	18.015999999999998	18.036000000000001	18.056000000000001	18.076000000000001	18.096	18.116	18.135999999999999	18.155999999999999	18.175999999999998	18.196000000000002	18.216000000000001	18.236000000000001	18.256	18.276	18.295999999999999	18.315999999999999	18.335999999999999	18.356000000000002	18.376000000000001	18.396000000000001	18.416	18.436	18.457999999999998	18.478000000000002	18.498000000000001	18.518000000000001	18.538	18.558	18.577999999999999	18.597999999999999	18.617999999999999	18.638000000000002	18.658000000000001	18.678000000000001	18.698	18.718	18.738	18.757999999999999	18.777999999999999	18.797999999999998	18.818000000000001	18.838000000000001	18.861999999999998	18.878	18.898	18.917999999999999	18.942	18.962	18.978000000000002	18.998000000000001	19.021999999999998	19.038	19.058	19.077999999999999	19.102	19.117999999999999	19.138000000000002	19.158000000000001	19.178000000000001	19.198	19.218	19.238	19.257999999999999	19.277999999999999	19.297999999999998	19.318000000000001	19.338000000000001	19.358000000000001	19.378	19.398	19.417999999999999	19.437999999999999	19.457999999999998	19.478000000000002	19.498000000000001	19.518000000000001	19.538	19.558	19.577999999999999	19.597999999999999	19.617999999999999	19.638000000000002	19.658000000000001	19.678000000000001	19.698	19.718	19.738	19.757999999999999	19.777999999999999	19.797999999999998	19.818000000000001	19.838000000000001	19.858000000000001	19.878	19.898	19.917999999999999	19.937999999999999	19.957999999999998	19.978000000000002	19.998000000000001	20.018000000000001	20.038	20.058	20.077999999999999	20.097999999999999	20.117999999999999	20.138000000000002	20.158000000000001	20.178000000000001	20.198	20.218	20.238	20.257999999999999	20.277999999999999	20.295999999999999	20.318000000000001	20.338000000000001	20.358000000000001	20.376000000000001	20.396000000000001	20.416	20.436	20.456	20.475999999999999	20.495999999999999	20.515999999999998	20.536000000000001	20.556000000000001	20.576000000000001	20.596	20.616	20.635999999999999	20.654	20.673999999999999	20.693999999999999	20.713999999999999	20.736000000000001	20.754000000000001	20.776	20.794	20.814	20.834	20.853999999999999	20.873999999999999	20.896000000000001	20.914000000000001	20.934000000000001	20.954000000000001	20.974	20.994	21.013999999999999	21.033999999999999	21.053999999999998	21.074000000000002	21.094000000000001	21.114000000000001	21.134	21.155999999999999	21.173999999999999	21.193999999999999	21.213999999999999	21.236000000000001	21.254000000000001	21.274000000000001	21.295999999999999	21.315999999999999	21.335999999999999	21.356000000000002	21.376000000000001	21.393999999999998	21.416	21.436	21.456	21.475999999999999	21.495999999999999	21.515999999999998	21.536000000000001	21.556000000000001	21.576000000000001	21.596	21.616	21.635999999999999	21.655999999999999	21.675999999999998	21.696000000000002	21.716000000000001	21.736000000000001	21.756	21.776	21.795999999999999	21.815999999999999	21.835999999999999	21.856000000000002	21.876000000000001	21.896000000000001	21.916	21.936	21.956	21.975999999999999	21.995999999999999	22.015999999999998	22.038	22.056000000000001	22.076000000000001	22.096	22.117999999999999	22.138000000000002	22.158000000000001	22.178000000000001	22.198	22.216000000000001	22.238	22.256	22.277999999999999	22.297999999999998	22.318000000000001	22.338000000000001	22.358000000000001	22.378	22.398	22.417999999999999	22.437999999999999	22.457999999999998	22.478000000000002	22.498000000000001	22.518000000000001	22.538	22.558	22.577999999999999	22.597999999999999	22.617999999999999	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.222	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.66700000000000004	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	0.88900000000000001	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.111	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.333	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.556	1.778	1.778	1.778	1.778	1.778	1.778	1.778	1.778	1.778	2	2	2	2	2	2	2	2.222	2.222	2.222	2.222	2.222	2.222	2.444	2.444	2.444	2.444	2.444	2.6669999999999998	2.6669999999999998	2.6669999999999998	2.6669999999999998	2.6669999999999998	2.8889999999999998	2.8889999999999998	2.8889999999999998	3.1110000000000002	3.1110000000000002	3.1110000000000002	3.1110000000000002	3.3330000000000002	3.3330000000000002	3.3330000000000002	3.556	3.556	3.556	3.778	3.778	3.778	4	4	4.2220000000000004	4.2220000000000004	4.444	4.444	4.444	4.6669999999999998	4.6669999999999998	4.8890000000000002	4.8890000000000002	5.1109999999999998	5.1109999999999998	5.3330000000000002	5.3330000000000002	5.556	5.7779999999999996	5.7779999999999996	6	6	6.2220000000000004	6.444	6.444	6.6669999999999998	6.8890000000000002	6.8890000000000002	7.1109999999999998	7.3330000000000002	7.556	7.7779999999999996	8.2219999999999995	8.4440000000000008	8.6669999999999998	8.8889999999999993	9.3330000000000002	9.5559999999999992	9.7780000000000005	10.222	10.444000000000001	10.888999999999999	11.111000000000001	11.555999999999999	11.778	12.222	12.444000000000001	12.888999999999999	13.333	13.778	14.222	14.667	15.111000000000001	15.333	16	16.222000000000001	16.667000000000002	17.111000000000001	17.556000000000001	18	18.667000000000002	18.888999999999999	19.556000000000001	20	20.222000000000001	20.888999999999999	21.332999999999998	21.777999999999999	22.222000000000001	22.667000000000002	23.111000000000001	23.777999999999999	24	24.443999999999999	24.888999999999999	25.556000000000001	25.777999999999999	26.222000000000001	26.667000000000002	27.111000000000001	27.556000000000001	28	28.443999999999999	28.667000000000002	29.111000000000001	29.556000000000001	30	30.443999999999999	30.667000000000002	31.111000000000001	31.332999999999998	32	32.222000000000001	32.667000000000002	33.110999999999997	33.332999999999998	33.777999999999999	34	34.444000000000003	34.889000000000003	35.332999999999998	35.555999999999997	36	36.444000000000003	36.667000000000002	37.110999999999997	37.332999999999998	37.777999999999999	38	38.667000000000002	38.889000000000003	39.332999999999998	39.777999999999999	40	40.444000000000003	40.667000000000002	41.110999999999997	41.332999999999998	41.777999999999999	42	42.444000000000003	42.889000000000003	43.110999999999997	43.555999999999997	44	44.222000000000001	44.667000000000002	44.889000000000003	45.332999999999998	45.777999999999999	46	46.444000000000003	46.667000000000002	47.110999999999997	47.332999999999998	47.777999999999999	48	48.444000000000003	48.667000000000002	49.110999999999997	49.332999999999998	49.777999999999999	50	50.444000000000003	50.667000000000002	51.110999999999997	51.332999999999998	51.777999999999999	52	52.444000000000003	52.667000000000002	53.110999999999997	53.332999999999998	53.777999999999999	54	54.444000000000003	54.667000000000002	54.889000000000003	55.332999999999998	55.555999999999997	56	56.222000000000001	56.667000000000002	56.889000000000003	57.110999999999997	57.555999999999997	57.777999999999999	57.777999999999999	58	58.222000000000001	58.444000000000003	58.667000000000002	58.667000000000002	58.889000000000003	59.110999999999997	59.110999999999997	59.332999999999998	59.332999999999998	59.555999999999997	59.777999999999999	59.777999999999999	60	60.222000000000001	60.444000000000003	60.889000000000003	61.110999999999997	61.332999999999998	61.777999999999999	62	62.444000000000003	62.667000000000002	63.110999999999997	63.332999999999998	63.777999999999999	64	64.444000000000003	64.667000000000002	65.111000000000004	65.332999999999998	65.778000000000006	66	66.221999999999994	66.667000000000002	66.888999999999996	67.332999999999998	67.555999999999997	67.778000000000006	68.221999999999994	68.444000000000003	68.667000000000002	68.888999999999996	69.111000000000004	69.555999999999997	69.778000000000006	70	70.444000000000003	70.667000000000002	70.888999999999996	71.332999999999998	71.555999999999997	71.778000000000006	72	72.221999999999994	72.667000000000002	72.888999999999996	73.111000000000004	73.332999999999998	73.555999999999997	73.778000000000006	74.221999999999994	74.444000000000003	74.667000000000002	74.888999999999996	75.332999999999998	75.555999999999997	75.778000000000006	76	76.444000000000003	76.667000000000002	76.888999999999996	77.111000000000004	77.555999999999997	77.555999999999997	77.778000000000006	78.221999999999994	78.444000000000003	78.667000000000002	78.888999999999996	79.111000000000004	79.332999999999998	79.555999999999997	79.778000000000006	80	80.221999999999994	80.444000000000003	80.667000000000002	80.888999999999996	81.111000000000004	81.332999999999998	81.555999999999997	81.778000000000006	82	82.221999999999994	82.444000000000003	82.667000000000002	82.888999999999996	83.111000000000004	83.332999999999998	83.555999999999997	83.778000000000006	84	84.221999999999994	84.444000000000003	84.444000000000003	84.667000000000002	84.888999999999996	85.111000000000004	85.111000000000004	85.332999999999998	85.555999999999997	85.778000000000006	85.778000000000006	86	86.221999999999994	86.221999999999994	86.444000000000003	86.444000000000003	86.667000000000002	86.667000000000002	86.888999999999996	86.888999999999996	87.111000000000004	87.332999999999998	87.332999999999998	87.555999999999997	87.555999999999997	87.555999999999997	87.778000000000006	87.778000000000006	88	88	88.221999999999994	88.221999999999994	88.444000000000003	88.444000000000003	88.444000000000003	88.667000000000002	88.667000000000002	88.888999999999996	88.888999999999996	89.111000000000004	89.111000000000004	89.111000000000004	89.332999999999998	89.332999999999998	89.555999999999997	89.555999999999997	89.555999999999997	89.778000000000006	89.778000000000006	90	90	90.221999999999994	90.221999999999994	90.444000000000003	90.444000000000003	90.444000000000003	90.667000000000002	90.667000000000002	90.888999999999996	90.888999999999996	90.888999999999996	91.111000000000004	91.111000000000004	91.332999999999998	91.332999999999998	91.332999999999998	91.555999999999997	91.555999999999997	91.555999999999997	91.778000000000006	91.778000000000006	91.778000000000006	92	92	92	92.221999999999994	92.221999999999994	92.221999999999994	92.221999999999994	92.444000000000003	92.444000000000003	92.444000000000003	92.444000000000003	92.667000000000002	92.667000000000002	92.667000000000002	92.667000000000002	92.888999999999996	92.888999999999996	92.888999999999996	93.111000000000004	93.111000000000004	93.111000000000004	93.111000000000004	93.332999999999998	93.332999999999998	93.332999999999998	93.555999999999997	93.555999999999997	93.555999999999997	93.778000000000006	93.778000000000006	93.778000000000006	94	94	94	94.221999999999994	94.221999999999994	94.221999999999994	94.444000000000003	94.444000000000003	94.444000000000003	94.444000000000003	94.667000000000002	94.667000000000002	94.667000000000002	94.667000000000002	94.888999999999996	94.888999999999996	94.888999999999996	95.111000000000004	95.111000000000004	95.111000000000004	95.111000000000004	95.332999999999998	95.332999999999998	95.332999999999998	95.332999999999998	95.555999999999997	95.555999999999997	95.555999999999997	95.555999999999997	95.778000000000006	95.778000000000006	95.778000000000006	95.778000000000006	96	96	96	96.221999999999994	96.221999999999994	96.221999999999994	96.221999999999994	96.444000000000003	96.444000000000003	96.444000000000003	96.444000000000003	96.667000000000002	96.667000000000002	96.667000000000002	96.888999999999996	96.888999999999996	96.888999999999996	97.111000000000004	97.111000000000004	97.111000000000004	97.332999999999998	97.332999999999998	97.332999999999998	97.555999999999997	97.555999999999997	97.555999999999997	97.778000000000006	97.778000000000006	97.778000000000006	98	98	98	98.221999999999994	98.221999999999994	98.221999999999994	98.444000000000003	98.444000000000003	98.444000000000003	98.667000000000002	98.667000000000002	98.667000000000002	98.667000000000002	98.888999999999996	98.888999999999996	98.888999999999996	99.111000000000004	99.111000000000004	99.111000000000004	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.332999999999998	99.555999999999997	99.555999999999997	99.555999999999997	99.778000000000006	99.778000000000006	99.778000000000006	99.778000000000006	100	100	100	100	100.22199999999999	100.22199999999999	100.22199999999999	100.22199999999999	100.444	100.444	100.444	100.444	100.667	100.667	100.667	100.667	100.889	100.889	100.889	100.889	100.889	101.111	101.111	101.111	101.111	101.111	101.333	101.333	101.333	101.333	101.333	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.111	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	104	104	104	104	104	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.444	104.444	104.444	104.444	104.444	104.667	104.667	104.667	104.667	104.889	104.889	104.889	104.889	104.889	105.111	105.111	105.111	105.111	105.111	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	106	106	106	106	106	106	106	106	106	106	106	106	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.444	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.667	106.889	106.889	106.889	106.889	106.889	106.889	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.111	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	108	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.77800000000001	107.556	107.556	107.556	107.556	107.556	107.556	107.556	107.333	107.333	107.333	107.333	107.333	107.333	107.333	107.111	107.111	107.111	107.111	107.111	106.889	106.889	106.889	106.889	106.889	106.667	106.667	106.667	106.667	106.667	106.444	106.444	106.444	106.444	106.444	106.444	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106.22199999999999	106	106	106	106	106	106	106	106	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.77800000000001	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.556	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.333	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	105.111	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.889	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.667	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.444	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104.22199999999999	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	104	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.77800000000001	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.556	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.333	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	103.111	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.889	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.667	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.444	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102.22199999999999	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	102	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.556	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	101.77800000000001	102	102	102	102.22199999999999	102.22199999999999	102.22199999999999	102.444	102.444	102.667	102.889	102.889	103.111	103.333	103.333	103.556	103.77800000000001	103.77800000000001	104	104.22199999999999	104.444	104.444	104.667	104.889	105.111	105.111	105.333	105.556	105.77800000000001	106	106	106.22199999999999	106.444	106.667	106.889	107.111	107.111	107.333	107.556	107.77800000000001	108	108.22199999999999	108.22199999999999	108.667	108.889	109.111	109.333	109.556	109.77800000000001	110	110.22199999999999	110.22199999999999	110.444	110.444	110.667	110.667	110.667	110.889	110.889	110.889	110.889	110.889	111.111	111.111	111.111	111.111	111.111	111.111	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	112	112	112	112	112	112	112	112	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.889	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.667	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.444	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114.22199999999999	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	114	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.77800000000001	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.556	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.333	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	113.111	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.889	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.667	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.444	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112.22199999999999	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	112	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.77800000000001	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.556	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.333	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	111.111	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.889	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.667	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.444	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110.22199999999999	110	110	110	110	110	110	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.77800000000001	109.556	109.556	109.556	109.556	109.333	109.333	109.333	109.333	109.333	109.111	109.111	109.111	109.111	108.889	108.889	108.889	108.667	108.667	108.667	108.444	108.444	108.444	108.22199999999999	108.22199999999999	108	108	108	107.77800000000001	107.77800000000001	107.556	107.556	107.333	107.333	107.111	107.111	106.889	106.667	106.667	106.444	106.444	106.22199999999999	106	105.77800000000001	105.77800000000001	105.556	105.333	104.889	104.667	104.22199999999999	104	103.77800000000001	103.333	102.889	102.444	102	101.556	101.111	100.667	100.22199999999999	99.778000000000006	98.888999999999996	98.444000000000003	97.778000000000006	97.111000000000004	96.444000000000003	95.332999999999998	94.221999999999994	92.667000000000002	91.111000000000004	89.555999999999997	87.778000000000006	85.778000000000006	83.332999999999998	81.778000000000006	79.111000000000004	77.111000000000004	75.332999999999998	73.555999999999997	72	70.667000000000002	68.888999999999996	67.778000000000006	66.888999999999996	66.221999999999994	65.555999999999997	64.888999999999996	64.221999999999994	63.332999999999998	62.667000000000002	62	61.332999999999998	60.667000000000002	60	59.332999999999998	58.667000000000002	57.777999999999999	57.110999999999997	56.444000000000003	55.777999999999999	55.110999999999997	54.444000000000003	53.777999999999999	53.110999999999997	52.444000000000003	51.777999999999999	50.667000000000002	50	49.332999999999998	48.667000000000002	48	47.332999999999998	46.444000000000003	45.777999999999999	44.889000000000003	44.222000000000001	42.889000000000003	42	40.889000000000003	39.777999999999999	38.667000000000002	37.332999999999998	36	33.777999999999999	31.556000000000001	29.111000000000001	26.222000000000001	Percentage Strain (%)


Stress (MPa)




Carbon Woven Bioresin Stress vs Strain

Sample 1	0	0	0	0	0	0	0	0	1E-3	1E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	8.9999999999999993E-3	0.01	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.9E-2	1.9E-2	1.9E-2	1.9E-2	0.02	0.02	0.02	0.02	0.02	2.1000000000000001E-2	2.1000000000000001E-2	2.1000000000000001E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.1999999999999999E-2	2.3E-2	2.4E-2	2.4E-2	2.5000000000000001E-2	2.5000000000000001E-2	2.5999999999999999E-2	2.7E-2	2.8000000000000001E-2	2.8000000000000001E-2	2.9000000000000001E-2	0.03	3.1E-2	3.2000000000000001E-2	3.3000000000000002E-2	3.4000000000000002E-2	3.5000000000000003E-2	3.5999999999999997E-2	3.7999999999999999E-2	3.9E-2	0.04	4.1000000000000002E-2	4.2000000000000003E-2	4.2999999999999997E-2	4.2999999999999997E-2	4.3999999999999997E-2	4.5999999999999999E-2	4.7E-2	4.9000000000000002E-2	0.05	5.1999999999999998E-2	5.2999999999999999E-2	5.1999999999999998E-2	5.1999999999999998E-2	5.3999999999999999E-2	5.6000000000000001E-2	5.8000000000000003E-2	0.06	6.2E-2	6.3E-2	6.5000000000000002E-2	6.7000000000000004E-2	6.9000000000000006E-2	7.1999999999999995E-2	7.3999999999999996E-2	7.5999999999999998E-2	7.8E-2	0.08	8.2000000000000003E-2	8.4000000000000005E-2	8.5999999999999993E-2	8.7999999999999995E-2	0.09	9.1999999999999998E-2	9.4E-2	9.5000000000000001E-2	9.7000000000000003E-2	9.9000000000000005E-2	0.1	0.10199999999999999	0.105	0.107	0.109	0.11	0.112	0.114	0.11600000000000001	0.11799999999999999	0.12	0.122	0.123	0.125	0.127	0.129	0.13100000000000001	0.13300000000000001	0.13500000000000001	0.13700000000000001	0.13900000000000001	0.14000000000000001	0.14199999999999999	0.14399999999999999	0.14599999999999999	0.14799999999999999	0.15	0.152	0.154	0.156	0.158	0.159	0.161	0.16300000000000001	0.16500000000000001	0.16700000000000001	0.16800000000000001	0.17	0.17199999999999999	0.17399999999999999	0.17599999999999999	0.17799999999999999	0.18	0.182	0.184	0.186	0.187	0.189	0.191	0.193	0.19400000000000001	0.19600000000000001	0.19800000000000001	0.19800000000000001	0.20200000000000001	0.20300000000000001	0.20499999999999999	0.20699999999999999	0.20799999999999999	0.21	0.21199999999999999	0.214	0.215	0.217	0.218	0.22	0.221	0.222	0.224	0.22500000000000001	0.22700000000000001	0.22800000000000001	0.22900000000000001	0.23100000000000001	0.23200000000000001	0.23300000000000001	0.23400000000000001	0.23499999999999999	0.23599999999999999	0.23799999999999999	0.23799999999999999	0.24	0.24	0.24199999999999999	0.24199999999999999	0.24299999999999999	0.24399999999999999	0.245	0.246	0.246	0.247	0.248	0.249	0.249	0.25	0.25	0.251	0.252	0.252	0.252	0.253	0.253	0.254	0.254	0.254	0.255	0.255	0.25600000000000001	0.25600000000000001	0.25600000000000001	0.25600000000000001	0.25700000000000001	0.25700000000000001	0.25800000000000001	0.25800000000000001	0.25800000000000001	0.25900000000000001	0.25900000000000001	0.26	0.26	0.26	0.26100000000000001	0.26100000000000001	0.26200000000000001	0.26200000000000001	0.26200000000000001	0.26300000000000001	0.26300000000000001	0.26400000000000001	0.26400000000000001	0.26400000000000001	0.26500000000000001	0.26500000000000001	0.26600000000000001	0.26600000000000001	0.26600000000000001	0.26700000000000002	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26800000000000002	0.26800000000000002	0.26900000000000002	0.27	0.27	0.27100000000000002	0.27100000000000002	0.27200000000000002	0.27200000000000002	0.27200000000000002	0.27300000000000002	0.27300000000000002	0.27400000000000002	0.27400000000000002	0.27400000000000002	0.27500000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27800000000000002	0.27800000000000002	0.27800000000000002	0.27900000000000003	0.28000000000000003	0.28000000000000003	0.28000000000000003	0.28100000000000003	0.28100000000000003	0.28199999999999997	0.28199999999999997	0.28199999999999997	0.28299999999999997	0.28299999999999997	0.28399999999999997	0.28399999999999997	0.28399999999999997	0.28499999999999998	0.28599999999999998	0.28599999999999998	0.28599999999999998	0.28699999999999998	0.28699999999999998	0.28799999999999998	0.28799999999999998	0.28799999999999998	0.28899999999999998	0.28899999999999998	0.28999999999999998	0.28999999999999998	0.29099999999999998	0.29099999999999998	0.29199999999999998	0.29199999999999998	0.29199999999999998	0.29299999999999998	0.29299999999999998	0.29399999999999998	0.29399999999999998	0.29499999999999998	0.29499999999999998	0.29599999999999999	0.29599999999999999	0.29599999999999999	0.29699999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.29899999999999999	0.3	0.3	0.3	0.30099999999999999	0.30199999999999999	0.30199999999999999	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30499999999999999	0.30499999999999999	0.30599999999999999	0.30599999999999999	0.30599999999999999	0.307	0.308	0.308	0.308	0.309	0.309	0.31	0.31	0.311	0.311	0.312	0.312	0.313	0.313	0.314	0.314	0.314	0.315	0.316	0.316	0.316	0.317	0.317	0.318	0.318	0.31900000000000001	0.31900000000000001	0.32	0.32	0.32	0.32100000000000001	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32500000000000001	0.32500000000000001	0.32600000000000001	0.32600000000000001	0.32600000000000001	0.32700000000000001	0.32700000000000001	0.32800000000000001	0.32800000000000001	0.32900000000000001	0.32900000000000001	0.33	0.33	0.33	0.33100000000000002	0.33200000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33300000000000002	0.33400000000000002	0.33400000000000002	0.33500000000000002	0.33500000000000002	0.33600000000000002	0.33600000000000002	0.33600000000000002	0.33700000000000002	0.33800000000000002	0.33800000000000002	0.33800000000000002	0.33900000000000002	0.33900000000000002	0.34	0.34	0.34100000000000003	0.34100000000000003	0.34200000000000003	0.34200000000000003	0.34300000000000003	0.34300000000000003	0.34399999999999997	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34699999999999998	0.34799999999999998	0.34799999999999998	0.34899999999999998	0.34899999999999998	0.35	0.35	0.35	0.35099999999999998	0.35099999999999998	0.35199999999999998	0.35199999999999998	0.35299999999999998	0.35299999999999998	0.35399999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35599999999999998	0.35599999999999998	0.35599999999999998	0.35699999999999998	0.35699999999999998	0.35799999999999998	0.35799999999999998	0.35799999999999998	0.35899999999999999	0.36	0.36	0.36	0.36099999999999999	0.36099999999999999	0.36199999999999999	0.36199999999999999	0.36199999999999999	0.36299999999999999	0.36299999999999999	0.36399999999999999	0.36399999999999999	0.36499999999999999	0.36499999999999999	0.36599999999999999	0.36599999999999999	0.36599999999999999	0.36699999999999999	0.36699999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36899999999999999	0.37	0.37	0.37	0.371	0.371	0.372	0.372	0.373	0.373	0.374	0.374	0.375	0.375	0.376	0.376	0.376	0.377	0.377	0.378	0.378	0.379	0.379	0.38	0.38	0.38	0.38100000000000001	0.38200000000000001	0.38200000000000001	0.38200000000000001	0.38300000000000001	0.38400000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38600000000000001	0.38600000000000001	0.38600000000000001	0.38700000000000001	0.38700000000000001	0.38800000000000001	0.38800000000000001	0.38900000000000001	0.38900000000000001	0.39	0.39	0.39100000000000001	0.39100000000000001	0.39200000000000002	0.39200000000000002	0.39300000000000002	0.39300000000000002	0.39400000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39600000000000002	0.39600000000000002	0.39600000000000002	0.39700000000000002	0.39800000000000002	0.39800000000000002	0.39800000000000002	0.39900000000000002	0.4	0.4	0.4	0.40100000000000002	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40300000000000002	0.40400000000000003	0.40400000000000003	0.40500000000000003	0.40500000000000003	0.40600000000000003	0.40600000000000003	0.40699999999999997	0.40699999999999997	0.40799999999999997	0.40799999999999997	0.40899999999999997	0.41	0.41	0.41	0.41099999999999998	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41299999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41499999999999998	0.41499999999999998	0.41599999999999998	0.41599999999999998	0.41699999999999998	0.41699999999999998	0.41799999999999998	0.41799999999999998	0.41799999999999998	0.41899999999999998	0.41899999999999998	0.42	0.42	0.42099999999999999	0.42099999999999999	0.42199999999999999	0.42199999999999999	0.42299999999999999	0.42299999999999999	0.42399999999999999	0.42399999999999999	0.42499999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42699999999999999	0.42799999999999999	0.42799999999999999	0.42899999999999999	0.42899999999999999	0.43	0.43	0.43099999999999999	0.432	0.432	0.432	0.433	0.434	0.434	0.434	0.435	0.436	0.436	0.436	0.437	0.437	0.438	0.438	0.439	0.439	0.44	0.44	0.441	0.441	0.442	0.442	0.443	0.443	0.44400000000000001	0.44400000000000001	0.44500000000000001	0.44500000000000001	0.44600000000000001	0.44600000000000001	0.44700000000000001	0.44700000000000001	0.44800000000000001	0.44800000000000001	0.44900000000000001	0.44900000000000001	0.45	0.45	0.45	0.45100000000000001	0.45200000000000001	0.45200000000000001	0.45200000000000001	0.45300000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45800000000000002	0.45800000000000002	0.45800000000000002	0.45900000000000002	0.46	0.46	0.46	0.46100000000000002	0.46100000000000002	0.46200000000000002	0.46200000000000002	0.46300000000000002	0.46300000000000002	0.46400000000000002	0.46400000000000002	0.46500000000000002	0.46500000000000002	0.46600000000000003	0.46600000000000003	0.46700000000000003	0.46700000000000003	0.46800000000000003	0.46800000000000003	0.46899999999999997	0.46899999999999997	0.47	0.47	0.47	0.47099999999999997	0.47099999999999997	0.47199999999999998	0.47199999999999998	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47399999999999998	0.47499999999999998	0.47599999999999998	0.47599999999999998	0.47599999999999998	0.47699999999999998	0.47699999999999998	0.47799999999999998	0.47799999999999998	0.47899999999999998	0.47899999999999998	0.48	0.48	0.48099999999999998	0.48099999999999998	0.48199999999999998	0.48199999999999998	0.48199999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48399999999999999	0.48499999999999999	0.48599999999999999	0.48599999999999999	0.48599999999999999	0.48699999999999999	0.48699999999999999	0.48799999999999999	0.48799999999999999	0.48899999999999999	0.48899999999999999	0.49	0.49	0.49	0.49099999999999999	0.49099999999999999	0.49199999999999999	0.49199999999999999	0.49299999999999999	0.49299999999999999	0.49399999999999999	0.49399999999999999	0.495	0.495	0.496	0.496	0.497	0.497	0.498	0.498	0.498	0.499	0.499	0.5	0.5	0.501	0.501	0.502	0.502	0.503	0.503	0.504	0.504	0.504	0.505	0.505	0.50600000000000001	0.50600000000000001	0.50700000000000001	0.50700000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50900000000000001	0.51	0.51	0.51100000000000001	0.51100000000000001	0.51200000000000001	0.51200000000000001	0.51200000000000001	0.51300000000000001	0.51400000000000001	0.51400000000000001	0.51400000000000001	0.51500000000000001	0.51500000000000001	0.51600000000000001	0.51600000000000001	0.51700000000000002	0.51700000000000002	0.51800000000000002	0.51800000000000002	0.51900000000000002	0.51900000000000002	0.52	0.52	0.52	0.52100000000000002	0.52200000000000002	0.52200000000000002	0.52200000000000002	0.52300000000000002	0.52300000000000002	0.52400000000000002	0.52400000000000002	0.52400000000000002	0.52500000000000002	0.52500000000000002	0.52600000000000002	0.52600000000000002	0.52700000000000002	0.52700000000000002	0.52800000000000002	0.52800000000000002	0.52900000000000003	0.52900000000000003	0.53	0.53	0.53100000000000003	0.53100000000000003	0.53200000000000003	0.53200000000000003	0.53300000000000003	0.53300000000000003	0.53400000000000003	0.53400000000000003	0.53500000000000003	0.53500000000000003	0.53600000000000003	0.53600000000000003	0.53700000000000003	0.53700000000000003	0.53800000000000003	0.53800000000000003	0.53900000000000003	0.53900000000000003	0.54	0.54	0.54100000000000004	0.54100000000000004	0.54200000000000004	0.54200000000000004	0.54200000000000004	0.54300000000000004	0.54300000000000004	0.54400000000000004	0.54400000000000004	0.54500000000000004	0.54500000000000004	0.54600000000000004	0.54600000000000004	0.54700000000000004	0.54700000000000004	0.54800000000000004	0.54800000000000004	0.54800000000000004	0.54900000000000004	0.55000000000000004	0.55000000000000004	0.55000000000000004	0.55100000000000005	0.55100000000000005	0.55200000000000005	0.55200000000000005	0.55200000000000005	0.55300000000000005	0.55400000000000005	0.55400000000000005	0.55500000000000005	0.502	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.502	0.502	0.502	0.502	0.502	0.502	0.502	0.502	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.498	0.498	0.502	0.502	0.504	0.50600000000000001	0.50800000000000001	0.50800000000000001	0.51200000000000001	0.51600000000000001	0.51800000000000002	0.52200000000000002	0.52400000000000002	0.52800000000000002	0.53200000000000003	0.53600000000000003	0.54200000000000004	0.54400000000000004	0.54800000000000004	0.55400000000000005	0.55800000000000005	0.56399999999999995	0.57199999999999995	0.57599999999999996	0.58199999999999996	0.58799999999999997	0.59399999999999997	0.60199999999999998	0.60599999999999998	0.61399999999999999	0.622	0.628	0.63600000000000001	0.64400000000000002	0.65200000000000002	0.65800000000000003	0.66800000000000004	0.67600000000000005	0.68400000000000005	0.69399999999999995	0.70199999999999996	0.71199999999999997	0.72199999999999998	0.73199999999999998	0.74199999999999999	0.752	0.76200000000000001	0.77200000000000002	0.78200000000000003	0.79400000000000004	0.80400000000000005	0.81599999999999995	0.82599999999999996	0.83799999999999997	0.85199999999999998	0.85399999999999998	0.86599999999999999	0.878	0.89200000000000002	0.90400000000000003	0.91800000000000004	0.93	0.94399999999999995	0.95799999999999996	0.97	0.98599999999999999	1	1.014	1.028	1.044	1.06	1.0740000000000001	1.0900000000000001	1.1060000000000001	1.1240000000000001	1.1379999999999999	1.1539999999999999	1.17	1.1879999999999999	1.206	1.22	1.238	1.258	1.274	1.294	1.31	1.3280000000000001	1.3480000000000001	1.3680000000000001	1.3859999999999999	1.4059999999999999	1.4239999999999999	1.444	1.464	1.484	1.504	1.524	1.544	1.5640000000000001	1.5860000000000001	1.6040000000000001	1.6240000000000001	1.6459999999999999	1.6659999999999999	1.6859999999999999	1.706	1.726	1.746	1.766	1.786	1.806	1.8280000000000001	1.8480000000000001	1.8680000000000001	1.8879999999999999	1.9079999999999999	1.9279999999999999	1.948	1.968	1.988	2.008	2.028	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.313	0.313	0.313	0.313	0.313	0.313	0.313	0.313	0.313	0.627	0.627	0.627	0.627	0.627	0.94	0.94	0.94	0.94	0.94	1.254	1.254	1.254	1.254	1.254	1.5669999999999999	1.5669999999999999	1.5669999999999999	1.5669999999999999	1.5669999999999999	1.881	1.881	1.881	1.881	1.881	2.194	2.194	2.194	2.194	2.508	2.508	2.508	2.508	2.508	2.8210000000000002	2.8210000000000002	2.8210000000000002	2.8210000000000002	2.8210000000000002	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.1349999999999998	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.448	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	3.762	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.0750000000000002	4.0750000000000002	4.0750000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.0750000000000002	4.0750000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.3890000000000002	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	4.702	5.016	5.016	5.016	5.016	5.016	5.016	5.016	5.016	5.016	5.016	5.3289999999999997	5.3289999999999997	5.3289999999999997	5.3289999999999997	5.3289999999999997	5.3289999999999997	5.3289999999999997	5.6429999999999998	5.6429999999999998	5.6429999999999998	5.6429999999999998	5.6429999999999998	5.6429999999999998	5.6429999999999998	5.9560000000000004	5.9560000000000004	5.9560000000000004	5.9560000000000004	5.9560000000000004	6.27	6.27	6.27	6.27	6.27	6.27	6.5830000000000002	6.5830000000000002	6.5830000000000002	6.5830000000000002	6.8970000000000002	6.8970000000000002	6.8970000000000002	6.8970000000000002	6.8970000000000002	7.21	7.21	7.21	7.21	7.524	7.524	7.524	7.524	7.8369999999999997	7.8369999999999997	7.8369999999999997	7.8369999999999997	8.15	8.15	8.15	8.15	8.4640000000000004	8.4640000000000004	8.4640000000000004	8.7769999999999992	8.7769999999999992	8.7769999999999992	9.0909999999999993	9.0909999999999993	9.0909999999999993	9.4039999999999999	9.4039999999999999	9.718	9.718	10.031000000000001	10.031000000000001	10.345000000000001	10.657999999999999	10.657999999999999	10.972	11.285	11.285	11.599	11.912000000000001	12.539	12.853	13.48	14.106999999999999	14.42	15.361000000000001	15.987	16.614000000000001	17.241	18.181999999999999	18.495000000000001	19.122	19.748999999999999	20.376000000000001	21.63	22.571000000000002	23.510999999999999	24.451000000000001	25.704999999999998	26.646000000000001	27.585999999999999	28.527000000000001	29.780999999999999	31.033999999999999	31.975000000000001	33.228999999999999	34.482999999999997	35.423000000000002	36.991	37.930999999999997	39.497999999999998	40.752000000000002	41.692999999999998	43.26	44.514000000000003	45.454999999999998	47.021999999999998	48.276000000000003	49.216000000000001	50.783999999999999	51.723999999999997	52.664999999999999	53.604999999999997	55.171999999999997	56.113	57.052999999999997	58.307000000000002	59.247999999999998	60.502000000000002	61.755000000000003	62.695999999999998	63.636000000000003	64.576999999999998	66.144000000000005	67.084999999999994	68.025000000000006	68.965999999999994	69.906000000000006	70.846000000000004	72.099999999999994	73.353999999999999	74.295000000000002	75.234999999999999	76.176000000000002	77.429000000000002	78.37	79.31	80.251000000000005	81.504999999999995	82.444999999999993	83.385999999999996	84.325999999999993	85.58	86.52	87.460999999999999	88.400999999999996	89.341999999999999	90.281999999999996	91.536000000000001	92.475999999999999	93.417000000000002	94.356999999999999	95.298000000000002	96.238	97.179000000000002	98.119	99.06	100	100.94	101.881	102.821	103.762	104.702	105.643	106.27	107.21	108.15	109.09099999999999	110.03100000000001	111.285	111.91200000000001	112.85299999999999	113.48	114.42	115.047	115.67400000000001	116.301	117.241	117.86799999999999	118.495	119.122	119.749	120.376	121.003	121.63	122.25700000000001	122.571	123.197	123.824	124.13800000000001	124.765	125.078	125.705	126.01900000000001	126.646	126.959	127.273	127.9	128.21299999999999	128.52699999999999	128.84	129.154	129.46700000000001	129.78100000000001	130.09399999999999	130.40799999999999	130.721	130.721	131.03399999999999	131.34800000000001	131.34800000000001	131.661	131.661	131.97499999999999	132.28800000000001	132.28800000000001	132.602	132.602	132.91499999999999	132.91499999999999	133.22900000000001	133.22900000000001	133.542	133.542	133.85599999999999	134.16900000000001	134.16900000000001	134.483	134.483	134.79599999999999	135.11000000000001	135.11000000000001	135.423	135.73699999999999	135.73699999999999	136.05000000000001	136.05000000000001	136.364	136.364	136.67699999999999	136.99100000000001	136.99100000000001	137.304	137.61799999999999	137.61799999999999	137.93100000000001	137.93100000000001	138.245	138.245	138.55799999999999	138.87100000000001	138.87100000000001	139.185	139.185	139.49799999999999	139.81200000000001	139.81200000000001	140.125	140.125	140.43899999999999	140.75200000000001	140.75200000000001	141.066	141.066	141.37899999999999	141.69300000000001	141.69300000000001	142.006	142.006	142.32	142.63300000000001	142.63300000000001	142.947	142.947	143.26	143.57400000000001	143.57400000000001	143.887	143.887	144.20099999999999	144.51400000000001	144.51400000000001	144.828	144.828	145.14099999999999	145.45500000000001	145.45500000000001	145.768	145.768	146.08199999999999	146.39500000000001	146.39500000000001	146.708	147.02199999999999	147.02199999999999	147.33500000000001	147.33500000000001	147.649	147.96199999999999	147.96199999999999	148.27600000000001	148.27600000000001	148.589	148.90299999999999	148.90299999999999	149.21600000000001	149.21600000000001	149.53	149.84299999999999	150.15700000000001	150.15700000000001	150.47	150.47	150.78399999999999	151.09700000000001	151.09700000000001	151.411	151.411	151.72399999999999	152.03800000000001	152.351	152.351	152.66499999999999	152.66499999999999	152.97800000000001	153.292	153.292	153.60499999999999	153.91800000000001	153.91800000000001	154.232	154.232	154.54499999999999	154.85900000000001	155.172	155.172	155.48599999999999	155.48599999999999	155.79900000000001	156.113	156.42599999999999	156.42599999999999	156.74	157.053	157.053	157.36699999999999	157.36699999999999	157.68	157.994	158.30699999999999	158.30699999999999	158.62100000000001	158.62100000000001	158.934	159.24799999999999	159.56100000000001	159.56100000000001	159.875	159.875	160.18799999999999	160.50200000000001	160.50200000000001	160.815	161.12899999999999	161.12899999999999	161.44200000000001	161.755	162.06899999999999	162.06899999999999	162.38200000000001	162.696	162.696	163.00899999999999	163.32300000000001	163.636	163.636	163.95	164.26300000000001	164.577	164.577	164.89	165.20400000000001	165.20400000000001	165.517	165.83099999999999	166.14400000000001	166.14400000000001	166.458	166.77099999999999	166.77099999999999	167.08500000000001	167.398	167.71199999999999	167.71199999999999	168.02500000000001	168.339	168.65199999999999	168.65199999999999	168.96600000000001	169.279	169.279	169.59200000000001	169.90600000000001	170.21899999999999	170.21899999999999	170.53299999999999	170.846	170.846	171.16	171.47300000000001	171.78700000000001	172.1	172.1	172.41399999999999	172.41399999999999	172.727	173.041	173.35400000000001	173.35400000000001	173.66800000000001	173.98099999999999	174.29499999999999	174.29499999999999	174.608	174.922	174.922	175.23500000000001	175.54900000000001	175.86199999999999	175.86199999999999	176.17599999999999	176.489	176.803	176.803	177.11600000000001	177.429	177.429	177.74299999999999	178.05600000000001	178.37	178.37	178.68299999999999	178.99700000000001	178.99700000000001	179.31	179.624	179.93700000000001	179.93700000000001	180.251	180.56399999999999	180.87799999999999	180.87799999999999	181.191	181.505	181.505	181.81800000000001	182.13200000000001	182.13200000000001	182.44499999999999	182.75899999999999	183.072	183.072	183.386	183.69900000000001	183.69900000000001	184.01300000000001	184.32599999999999	184.63900000000001	184.63900000000001	184.953	185.26599999999999	185.26599999999999	185.58	185.893	186.20699999999999	186.20699999999999	186.52	186.834	186.834	187.14699999999999	187.46100000000001	187.46100000000001	187.774	188.08799999999999	188.40100000000001	188.40100000000001	188.715	189.02799999999999	189.34200000000001	189.34200000000001	189.655	189.96899999999999	189.96899999999999	190.28200000000001	190.596	190.90899999999999	190.90899999999999	191.22300000000001	191.536	191.85	191.85	192.16300000000001	192.476	192.79	192.79	193.10300000000001	193.417	193.73	193.73	194.04400000000001	194.357	194.67099999999999	194.67099999999999	194.98400000000001	195.298	195.61099999999999	195.92500000000001	196.238	196.238	196.55199999999999	196.86500000000001	197.179	197.49199999999999	197.49199999999999	197.80600000000001	198.119	198.43299999999999	198.43299999999999	198.74600000000001	199.06	199.37299999999999	199.37299999999999	199.68700000000001	200	200.31299999999999	200.62700000000001	200.62700000000001	200.94	201.25399999999999	201.56700000000001	201.881	201.881	202.19399999999999	202.50800000000001	202.821	202.821	203.13499999999999	203.44800000000001	203.762	204.07499999999999	204.38900000000001	204.702	204.702	205.01599999999999	205.32900000000001	205.643	205.95599999999999	205.95599999999999	206.27	206.583	206.89699999999999	207.21	207.21	207.524	207.83699999999999	208.15	208.464	208.464	208.77699999999999	209.09100000000001	209.404	209.71799999999999	210.03100000000001	210.345	210.65799999999999	210.65799999999999	210.97200000000001	211.285	211.59899999999999	211.91200000000001	211.91200000000001	212.226	212.53899999999999	212.85300000000001	213.166	213.166	213.48	213.79300000000001	214.107	214.42	214.42	214.73400000000001	215.047	215.36099999999999	215.67400000000001	215.67400000000001	215.98699999999999	216.30099999999999	216.614	216.928	217.24100000000001	217.24100000000001	217.55500000000001	217.86799999999999	218.18199999999999	218.495	218.495	218.809	219.12200000000001	219.43600000000001	219.749	220.06299999999999	220.376	220.69	220.69	221.00299999999999	221.31700000000001	221.63	221.94399999999999	222.25700000000001	222.25700000000001	222.571	222.88399999999999	223.197	223.511	223.511	223.82400000000001	224.13800000000001	224.45099999999999	224.76499999999999	224.76499999999999	225.078	225.392	225.70500000000001	226.01900000000001	226.01900000000001	226.33199999999999	226.64599999999999	226.959	227.273	227.273	227.58600000000001	227.9	228.21299999999999	228.52699999999999	228.52699999999999	228.84	229.154	229.46700000000001	229.46700000000001	229.78100000000001	230.09399999999999	230.40799999999999	230.721	230.721	231.03399999999999	231.34800000000001	231.661	231.97499999999999	231.97499999999999	232.28800000000001	232.602	232.91499999999999	233.22900000000001	233.22900000000001	233.542	233.85599999999999	234.16900000000001	234.16900000000001	234.483	234.79599999999999	235.11	235.423	235.423	235.73699999999999	236.05	236.364	236.67699999999999	236.67699999999999	236.99100000000001	237.304	237.61799999999999	237.93100000000001	237.93100000000001	238.245	238.55799999999999	238.87100000000001	239.185	239.185	239.49799999999999	239.81200000000001	239.81200000000001	240.125	240.43899999999999	240.75200000000001	240.75200000000001	241.066	241.37899999999999	241.69300000000001	242.006	242.006	242.32	242.63300000000001	242.947	243.26	243.26	243.57400000000001	243.887	244.20099999999999	244.20099999999999	244.51400000000001	244.828	245.14099999999999	245.45500000000001	245.45500000000001	245.768	246.08099999999999	246.39500000000001	246.39500000000001	246.708	247.02199999999999	247.33500000000001	247.649	247.649	247.96199999999999	248.27600000000001	248.589	248.589	248.90299999999999	249.21600000000001	249.53	249.53	249.84299999999999	250.15700000000001	250.47	250.47	250.78399999999999	251.09700000000001	251.411	251.411	251.72399999999999	252.03800000000001	252.351	252.66499999999999	252.66499999999999	252.97800000000001	253.292	253.60499999999999	253.60499999999999	253.91900000000001	254.232	254.54499999999999	254.54499999999999	254.85900000000001	255.172	255.48599999999999	255.48599999999999	255.79900000000001	256.113	256.42599999999999	256.74	256.74	257.053	257.36700000000002	257.68	257.68	257.99400000000003	258.30700000000002	258.30700000000002	258.62099999999998	258.93400000000003	259.24799999999999	259.24799999999999	259.56099999999998	259.875	260.18799999999999	260.18799999999999	260.50200000000001	260.815	261.12900000000002	261.44200000000001	261.44200000000001	261.755	262.06900000000002	262.38200000000001	262.38200000000001	262.69600000000003	263.00900000000001	263.32299999999998	263.63600000000002	263.63600000000002	263.95	264.26299999999998	264.577	264.89	264.89	265.20400000000001	265.517	265.83100000000002	266.14400000000001	266.14400000000001	266.45800000000003	266.77100000000002	267.08499999999998	267.39800000000002	267.39800000000002	267.71199999999999	268.02499999999998	268.339	268.65199999999999	268.65199999999999	269.279	269.279	269.59199999999998	269.90600000000001	270.21899999999999	270.53300000000002	270.53300000000002	270.846	271.16000000000003	271.47300000000001	271.78699999999998	271.78699999999998	272.10000000000002	272.41399999999999	272.72699999999998	273.041	273.041	273.35399999999998	273.66800000000001	273.98099999999999	274.29500000000002	274.29500000000002	274.608	274.92200000000003	275.23500000000001	275.54899999999998	275.54899999999998	275.86200000000002	276.17599999999999	276.48899999999998	276.803	276.803	277.11599999999999	277.43	277.74299999999999	278.05599999999998	278.05599999999998	278.37	278.68299999999999	278.99700000000001	279.31	279.62400000000002	279.62400000000002	279.93700000000001	280.25099999999998	280.56400000000002	280.87799999999999	280.87799999999999	281.19099999999997	281.505	281.81799999999998	281.81799999999998	282.13200000000001	282.44499999999999	282.44499999999999	282.44499999999999	282.75900000000001	282.75900000000001	282.75900000000001	283.072	283.072	283.072	283.072	283.072	283.072	283.072	283.072	283.072	283.072	282.75900000000001	282.75900000000001	282.44499999999999	282.44499999999999	282.13200000000001	282.13200000000001	281.81799999999998	281.81799999999998	281.505	281.19099999999997	280.87799999999999	280.87799999999999	280.56400000000002	280.25099999999998	280.25099999999998	279.93700000000001	279.62400000000002	279.62400000000002	279.31	279.31	278.99700000000001	278.99700000000001	278.68299999999999	278.68299999999999	278.37	278.05599999999998	278.05599999999998	277.74299999999999	277.74299999999999	277.43	277.43	277.43	277.11599999999999	277.11599999999999	276.803	276.803	276.803	276.48899999999998	276.48899999999998	276.48899999999998	276.48899999999998	276.17599999999999	276.17599999999999	276.17599999999999	275.86200000000002	275.86200000000002	275.86200000000002	275.54899999999998	275.54899999999998	275.54899999999998	275.54899999999998	275.23500000000001	275.23500000000001	275.23500000000001	275.23500000000001	274.92200000000003	274.92200000000003	274.92200000000003	274.92200000000003	274.608	274.608	274.608	274.608	274.29500000000002	274.29500000000002	274.29500000000002	274.29500000000002	274.29500000000002	273.98099999999999	273.98099999999999	273.98099999999999	273.98099999999999	273.98099999999999	273.66800000000001	273.66800000000001	273.66800000000001	273.66800000000001	273.66800000000001	273.35399999999998	273.35399999999998	273.35399999999998	273.35399999999998	273.35399999999998	273.041	273.041	273.041	273.041	273.041	272.72699999999998	272.72699999999998	272.72699999999998	272.72699999999998	272.72699999999998	272.41399999999999	272.41399999999999	272.41399999999999	272.41399999999999	272.41399999999999	272.41399999999999	272.10000000000002	272.10000000000002	272.10000000000002	272.10000000000002	272.10000000000002	272.10000000000002	271.78699999999998	271.78699999999998	271.78699999999998	271.78699999999998	271.78699999999998	271.78699999999998	271.47300000000001	271.47300000000001	271.47300000000001	271.47300000000001	271.47300000000001	271.47300000000001	271.16000000000003	271.16000000000003	271.16000000000003	271.16000000000003	271.16000000000003	271.16000000000003	271.16000000000003	270.846	270.846	270.846	270.846	270.846	270.846	270.846	270.53300000000002	270.53300000000002	270.53300000000002	270.53300000000002	270.53300000000002	270.53300000000002	270.21899999999999	270.21899999999999	270.21899999999999	270.21899999999999	270.21899999999999	270.21899999999999	270.21899999999999	269.90600000000001	269.90600000000001	269.90600000000001	269.90600000000001	269.90600000000001	269.90600000000001	269.90600000000001	269.59199999999998	269.59199999999998	269.59199999999998	269.59199999999998	269.59199999999998	269.59199999999998	269.59199999999998	269.279	269.279	269.279	269.279	269.279	269.279	269.279	269.279	268.96600000000001	268.96600000000001	268.96600000000001	268.96600000000001	268.96600000000001	268.96600000000001	268.96600000000001	268.96600000000001	268.65199999999999	268.65199999999999	268.65199999999999	268.65199999999999	268.65199999999999	268.65199999999999	268.65199999999999	268.65199999999999	268.339	268.339	268.339	268.339	268.339	268.339	268.339	268.339	268.339	268.02499999999998	268.02499999999998	268.02499999999998	268.02499999999998	268.02499999999998	268.02499999999998	268.02499999999998	268.02499999999998	267.71199999999999	267.71199999999999	267.71199999999999	267.71199999999999	267.71199999999999	267.71199999999999	267.71199999999999	267.71199999999999	267.71199999999999	267.39800000000002	267.39800000000002	267.39800000000002	267.39800000000002	267.39800000000002	267.39800000000002	267.39800000000002	267.39800000000002	267.39800000000002	267.08499999999998	267.08499999999998	267.08499999999998	267.08499999999998	267.08499999999998	267.08499999999998	267.08499999999998	267.08499999999998	267.08499999999998	267.08499999999998	266.77100000000002	266.77100000000002	266.77100000000002	266.77100000000002	266.77100000000002	266.77100000000002	266.77100000000002	266.77100000000002	266.77100000000002	266.77100000000002	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.45800000000003	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	266.14400000000001	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.83100000000002	265.517	265.517	265.517	265.517	265.517	265.517	265.517	265.517	265.517	265.517	265.517	265.517	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	265.20400000000001	264.89	264.89	264.89	264.89	264.89	264.89	264.89	264.89	264.89	264.89	264.89	264.89	264.89	264.577	264.577	264.577	264.577	264.577	264.577	264.577	264.577	264.577	264.577	264.577	264.577	264.577	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	264.26299999999998	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.95	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.63600000000002	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.32299999999998	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	263.00900000000001	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.69600000000003	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.38200000000001	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	262.06900000000002	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.755	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.44200000000001	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	261.12900000000002	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.815	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.50200000000001	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	260.18799999999999	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.875	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.56099999999998	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	259.24799999999999	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.93400000000003	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.30700000000002	258.62099999999998	258.62099999999998	258.62099999999998	258.62099999999998	258.93400000000003	258.93400000000003	259.24799999999999	259.24799999999999	259.56099999999998	259.56099999999998	259.875	259.875	260.18799999999999	260.50200000000001	260.815	261.12900000000002	261.44200000000001	261.755	262.06900000000002	262.69600000000003	263.32299999999998	263.95	264.577	265.517	266.45800000000003	267.39800000000002	268.65199999999999	269.59199999999998	270.846	272.10000000000002	273.35399999999998	274.29500000000002	275.54899999999998	276.803	278.05599999999998	279.62400000000002	280.87799999999999	282.13200000000001	283.072	284.63900000000001	286.20699999999999	287.14699999999999	289.02800000000002	289.96899999999999	291.536	292.79000000000002	293.73	295.61099999999999	297.17899999999997	298.43299999999999	299.68700000000001	301.25400000000002	302.50799999999998	304.38900000000001	305.64299999999997	306.89699999999999	308.77699999999999	310.03100000000001	311.59899999999999	312.85300000000001	315.04700000000003	316.61399999999998	317.86799999999999	320.06299999999999	321.63	322.88400000000001	324.45100000000002	326.01900000000001	328.21300000000002	329.78100000000001	331.03500000000003	332.60199999999998	334.16899999999998	336.36399999999998	337.93099999999998	339.49799999999999	341.06599999999997	342.32	343.887	345.45499999999998	347.649	349.21600000000001	350.78399999999999	352.351	353.60500000000002	355.17200000000003	356.74	357.99400000000003	359.56099999999998	361.12900000000002	363.00900000000001	364.577	365.83100000000002	367.08499999999998	368.339	369.59199999999998	370.846	372.1	373.35399999999998	374.608	375.86200000000002	377.11599999999999	378.05599999999998	379.31	380.56400000000002	381.505	382.75900000000001	384.01299999999998	384.95299999999997	385.89299999999997	386.834	Sample 2	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	2E-3	2E-3	1E-3	1E-3	1E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.9E-2	0.02	0.02	2.1999999999999999E-2	2.1999999999999999E-2	2.3E-2	2.4E-2	2.5999999999999999E-2	2.7E-2	2.8000000000000001E-2	2.9000000000000001E-2	0.03	3.2000000000000001E-2	3.3000000000000002E-2	3.5000000000000003E-2	3.5999999999999997E-2	3.7999999999999999E-2	3.9E-2	0.04	4.2000000000000003E-2	4.3999999999999997E-2	4.4999999999999998E-2	4.7E-2	4.8000000000000001E-2	0.05	5.1999999999999998E-2	5.2999999999999999E-2	5.5E-2	5.6000000000000001E-2	5.8000000000000003E-2	0.06	6.0999999999999999E-2	6.3E-2	6.4000000000000001E-2	6.6000000000000003E-2	6.8000000000000005E-2	6.9000000000000006E-2	7.0000000000000007E-2	7.1999999999999995E-2	7.2999999999999995E-2	7.3999999999999996E-2	7.5999999999999998E-2	7.6999999999999999E-2	7.8E-2	7.9000000000000001E-2	0.08	8.2000000000000003E-2	8.3000000000000004E-2	8.4000000000000005E-2	8.5999999999999993E-2	8.6999999999999994E-2	8.7999999999999995E-2	8.8999999999999996E-2	0.09	9.1999999999999998E-2	9.2999999999999999E-2	9.4E-2	9.6000000000000002E-2	9.7000000000000003E-2	9.8000000000000004E-2	9.9000000000000005E-2	0.1	0.10199999999999999	0.10299999999999999	0.104	0.106	0.107	0.108	0.109	0.11	0.112	0.113	0.114	0.11600000000000001	0.11700000000000001	0.11799999999999999	0.11899999999999999	0.12	0.122	0.123	0.123	0.122	0.122	0.123	0.125	0.126	0.127	0.129	0.13	0.13100000000000001	0.13200000000000001	0.13400000000000001	0.13500000000000001	0.13600000000000001	0.13700000000000001	0.13800000000000001	0.14000000000000001	0.14000000000000001	0.14199999999999999	0.14299999999999999	0.14399999999999999	0.14499999999999999	0.14599999999999999	0.14699999999999999	0.14799999999999999	0.14899999999999999	0.15	0.151	0.152	0.153	0.154	0.154	0.155	0.156	0.157	0.158	0.158	0.159	0.16	0.16	0.161	0.16200000000000001	0.16200000000000001	0.16300000000000001	0.16400000000000001	0.16400000000000001	0.16400000000000001	0.16500000000000001	0.16600000000000001	0.16600000000000001	0.16600000000000001	0.16700000000000001	0.16700000000000001	0.16800000000000001	0.16800000000000001	0.16800000000000001	0.16900000000000001	0.16900000000000001	0.17	0.17	0.17	0.17100000000000001	0.17100000000000001	0.17100000000000001	0.17199999999999999	0.17199999999999999	0.17199999999999999	0.17199999999999999	0.17299999999999999	0.17299999999999999	0.17299999999999999	0.17399999999999999	0.17399999999999999	0.17399999999999999	0.17399999999999999	0.17399999999999999	0.17399999999999999	0.17499999999999999	0.17499999999999999	0.17499999999999999	0.17499999999999999	0.17599999999999999	0.17599999999999999	0.17599999999999999	0.17599999999999999	0.17599999999999999	0.17699999999999999	0.17699999999999999	0.17699999999999999	0.17799999999999999	0.17799999999999999	0.17799999999999999	0.17799999999999999	0.17899999999999999	0.17899999999999999	0.18	0.18	0.18	0.18	0.18099999999999999	0.18099999999999999	0.18099999999999999	0.182	0.182	0.182	0.183	0.183	0.184	0.184	0.184	0.184	0.185	0.185	0.186	0.186	0.186	0.187	0.187	0.188	0.188	0.188	0.189	0.189	0.19	0.19	0.19	0.191	0.191	0.192	0.192	0.193	0.193	0.19400000000000001	0.19400000000000001	0.19400000000000001	0.19500000000000001	0.19500000000000001	0.19600000000000001	0.19600000000000001	0.19600000000000001	0.19700000000000001	0.19800000000000001	0.19800000000000001	0.19800000000000001	0.19900000000000001	0.19900000000000001	0.2	0.2	0.20100000000000001	0.20100000000000001	0.20200000000000001	0.20200000000000001	0.20200000000000001	0.20300000000000001	0.20300000000000001	0.20399999999999999	0.20399999999999999	0.20499999999999999	0.20499999999999999	0.20599999999999999	0.20599999999999999	0.20599999999999999	0.20699999999999999	0.20799999999999999	0.20799999999999999	0.20799999999999999	0.20899999999999999	0.20899999999999999	0.21	0.21	0.21099999999999999	0.21099999999999999	0.21199999999999999	0.21199999999999999	0.21299999999999999	0.21299999999999999	0.214	0.214	0.215	0.215	0.216	0.216	0.216	0.217	0.218	0.218	0.218	0.219	0.22	0.22	0.22	0.221	0.221	0.222	0.222	0.223	0.223	0.224	0.224	0.22500000000000001	0.22500000000000001	0.22600000000000001	0.22600000000000001	0.22700000000000001	0.22700000000000001	0.22700000000000001	0.22800000000000001	0.22900000000000001	0.22900000000000001	0.23	0.23	0.23100000000000001	0.23100000000000001	0.23200000000000001	0.23200000000000001	0.23300000000000001	0.23300000000000001	0.23400000000000001	0.23400000000000001	0.23400000000000001	0.23499999999999999	0.23599999999999999	0.23599999999999999	0.23599999999999999	0.23699999999999999	0.23699999999999999	0.23799999999999999	0.23799999999999999	0.23899999999999999	0.23899999999999999	0.24	0.24	0.24099999999999999	0.24099999999999999	0.24199999999999999	0.24199999999999999	0.24299999999999999	0.24299999999999999	0.24399999999999999	0.24399999999999999	0.245	0.246	0.246	0.246	0.247	0.248	0.248	0.248	0.249	0.25	0.25	0.25	0.251	0.252	0.252	0.252	0.253	0.254	0.254	0.254	0.255	0.25600000000000001	0.25600000000000001	0.25600000000000001	0.25700000000000001	0.25800000000000001	0.25800000000000001	0.25900000000000001	0.25900000000000001	0.26	0.26	0.26	0.26100000000000001	0.26200000000000001	0.26200000000000001	0.26200000000000001	0.26300000000000001	0.26400000000000001	0.26400000000000001	0.26400000000000001	0.26500000000000001	0.26600000000000001	0.26600000000000001	0.26600000000000001	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26800000000000002	0.26900000000000002	0.27	0.27	0.27	0.27100000000000002	0.27100000000000002	0.27200000000000002	0.27200000000000002	0.27300000000000002	0.27400000000000002	0.27400000000000002	0.27400000000000002	0.27500000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27800000000000002	0.27800000000000002	0.27900000000000003	0.27900000000000003	0.28000000000000003	0.28000000000000003	0.28100000000000003	0.28100000000000003	0.28199999999999997	0.28199999999999997	0.28299999999999997	0.28299999999999997	0.28399999999999997	0.28399999999999997	0.28499999999999998	0.28499999999999998	0.28599999999999998	0.28599999999999998	0.28699999999999998	0.28699999999999998	0.28799999999999998	0.28799999999999998	0.28899999999999998	0.28899999999999998	0.28999999999999998	0.28999999999999998	0.29099999999999998	0.29099999999999998	0.29199999999999998	0.29199999999999998	0.29299999999999998	0.29299999999999998	0.29399999999999998	0.29399999999999998	0.29499999999999998	0.29499999999999998	0.29599999999999999	0.29599999999999999	0.29699999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.29899999999999999	0.3	0.3	0.30099999999999999	0.30099999999999999	0.30199999999999999	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30499999999999999	0.30499999999999999	0.30599999999999999	0.30599999999999999	0.307	0.307	0.308	0.308	0.309	0.31	0.31	0.31	0.311	0.312	0.312	0.312	0.313	0.314	0.314	0.314	0.315	0.316	0.316	0.316	0.317	0.318	0.318	0.318	0.31900000000000001	0.32	0.32	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32500000000000001	0.32500000000000001	0.32600000000000001	0.32600000000000001	0.32700000000000001	0.32700000000000001	0.32800000000000001	0.32800000000000001	0.32900000000000001	0.32900000000000001	0.33	0.33	0.33100000000000002	0.33100000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33300000000000002	0.33400000000000002	0.33400000000000002	0.33400000000000002	0.33500000000000002	0.33600000000000002	0.33600000000000002	0.33600000000000002	0.33700000000000002	0.33800000000000002	0.33800000000000002	0.33800000000000002	0.33900000000000002	0.34	0.34	0.34	0.34100000000000003	0.34100000000000003	0.34200000000000003	0.34200000000000003	0.34300000000000003	0.34300000000000003	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34699999999999998	0.34799999999999998	0.34799999999999998	0.34899999999999998	0.34899999999999998	0.35	0.35	0.35	0.35099999999999998	0.35099999999999998	0.35199999999999998	0.35199999999999998	0.35299999999999998	0.35299999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35599999999999998	0.35599999999999998	0.35599999999999998	0.35699999999999998	0.35799999999999998	0.35799999999999998	0.35799999999999998	0.35899999999999999	0.36	0.36	0.36	0.36099999999999999	0.36199999999999999	0.36199999999999999	0.36199999999999999	0.36299999999999999	0.36299999999999999	0.36399999999999999	0.36399999999999999	0.36499999999999999	0.36499999999999999	0.36599999999999999	0.36599999999999999	0.36699999999999999	0.36699999999999999	0.36799999999999999	0.36799999999999999	0.36899999999999999	0.36899999999999999	0.37	0.37	0.371	0.371	0.372	0.372	0.373	0.373	0.374	0.374	0.375	0.375	0.376	0.376	0.377	0.377	0.378	0.378	0.379	0.379	0.38	0.38	0.38100000000000001	0.38100000000000001	0.38200000000000001	0.38200000000000001	0.38300000000000001	0.38300000000000001	0.38400000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38600000000000001	0.38600000000000001	0.38600000000000001	0.38700000000000001	0.38800000000000001	0.38800000000000001	0.38800000000000001	0.38900000000000001	0.38900000000000001	0.39	0.39	0.39100000000000001	0.39100000000000001	0.39200000000000002	0.39200000000000002	0.39300000000000002	0.39300000000000002	0.39300000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39600000000000002	0.39600000000000002	0.39700000000000002	0.39700000000000002	0.39800000000000002	0.39800000000000002	0.39800000000000002	0.39900000000000002	0.4	0.4	0.4	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40300000000000002	0.40300000000000002	0.40400000000000003	0.40500000000000003	0.40500000000000003	0.40600000000000003	0.40600000000000003	0.40699999999999997	0.40699999999999997	0.40799999999999997	0.40799999999999997	0.40899999999999997	0.40899999999999997	0.41	0.41	0.41099999999999998	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41199999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41399999999999998	0.41499999999999998	0.41499999999999998	0.41599999999999998	0.41599999999999998	0.41699999999999998	0.41699999999999998	0.41799999999999998	0.41799999999999998	0.41899999999999998	0.41899999999999998	0.42	0.42	0.42099999999999999	0.42099999999999999	0.42199999999999999	0.42199999999999999	0.42199999999999999	0.42299999999999999	0.42299999999999999	0.42399999999999999	0.42399999999999999	0.42499999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42799999999999999	0.42799999999999999	0.42799999999999999	0.42899999999999999	0.43	0.43	0.43	0.43099999999999999	0.43099999999999999	0.432	0.432	0.433	0.433	0.434	0.434	0.434	0.435	0.436	0.436	0.436	0.437	0.437	0.438	0.438	0.438	0.439	0.44	0.44	0.44	0.441	0.441	0.442	0.442	0.443	0.443	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44500000000000001	0.44500000000000001	0.44600000000000001	0.44600000000000001	0.44700000000000001	0.44700000000000001	0.44800000000000001	0.44800000000000001	0.44800000000000001	0.44900000000000001	0.45	0.45	0.45	0.45100000000000001	0.45100000000000001	0.45200000000000001	0.45200000000000001	0.45300000000000001	0.45300000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45700000000000002	0.45800000000000002	0.45800000000000002	0.45800000000000002	0.45900000000000002	0.46	0.46	0.46	0.46100000000000002	0.46100000000000002	0.46200000000000002	0.46200000000000002	0.46300000000000002	0.46300000000000002	0.46400000000000002	0.46400000000000002	0.46500000000000002	0.46500000000000002	0.46600000000000003	0.46600000000000003	0.46600000000000003	0.46700000000000003	0.46800000000000003	0.46800000000000003	0.46800000000000003	0.46899999999999997	0.46899999999999997	0.47	0.47	0.47099999999999997	0.47099999999999997	0.47199999999999998	0.47199999999999998	0.47199999999999998	0.47299999999999998	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47499999999999998	0.47499999999999998	0.47599999999999998	0.47599999999999998	0.47599999999999998	0.47699999999999998	0.47799999999999998	0.47799999999999998	0.47799999999999998	0.47899999999999998	0.47899999999999998	0.48	0.48	0.48099999999999998	0.48099999999999998	0.48199999999999998	0.48199999999999998	0.48199999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48399999999999999	0.48499999999999999	0.48499999999999999	0.48599999999999999	0.48599999999999999	0.48599999999999999	0.48699999999999999	0.48799999999999999	0.48799999999999999	0.48799999999999999	0.48899999999999999	0.48899999999999999	0.49	0.49	0.49099999999999999	0.49099999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49299999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.495	0.495	0.496	0.496	0.497	0.497	0.498	0.498	0.498	0.499	0.5	0.5	0.5	0.501	0.502	0.502	0.503	0.503	0.504	0.504	0.505	0.505	0.50600000000000001	0.50600000000000001	0.50600000000000001	0.50700000000000001	0.50800000000000001	0.50800000000000001	0.50900000000000001	0.50900000000000001	0.51	0.51	0.51100000000000001	0.51100000000000001	0.51200000000000001	0.51200000000000001	0.51300000000000001	0.51300000000000001	0.51400000000000001	0.51400000000000001	0.51500000000000001	0.51500000000000001	0.51600000000000001	0.51600000000000001	0.51700000000000002	0.51700000000000002	0.51800000000000002	0.51800000000000002	0.51900000000000002	0.51900000000000002	0.52	0.52	0.52100000000000002	0.52100000000000002	0.52200000000000002	0.52200000000000002	0.52300000000000002	0.52300000000000002	0.52400000000000002	0.52400000000000002	0.52400000000000002	0.52500000000000002	0.52600000000000002	0.52600000000000002	0.52600000000000002	0.52700000000000002	0.52800000000000002	0.52800000000000002	0.52900000000000003	0.52900000000000003	0.53	0.53	0.53100000000000003	0.53100000000000003	0.53200000000000003	0.53200000000000003	0.53300000000000003	0.53300000000000003	0.53400000000000003	0.53400000000000003	0.53500000000000003	0.53500000000000003	0.53600000000000003	0.53600000000000003	0.53700000000000003	0.53700000000000003	0.53800000000000003	0.53800000000000003	0.53900000000000003	0.54	0.54	0.54	0.54100000000000004	0.54100000000000004	0.54200000000000004	0.54200000000000004	0.54300000000000004	0.54300000000000004	0.54400000000000004	0.54400000000000004	0.54500000000000004	0.54500000000000004	0.54600000000000004	0.54600000000000004	0.54700000000000004	0.48399999999999999	0.49	0.49399999999999999	0.5	0.502	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.502	0.502	0.502	0.502	0.502	0.502	0.502	0.502	0.5	0.5	0.5	0.5	0.5	0.5	0.5	0.5	0.5	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.5	0.5	0.502	0.504	0.504	0.50600000000000001	0.51	0.51200000000000001	0.51400000000000001	0.52	0.52200000000000002	0.52400000000000002	0.53	0.53200000000000003	0.53600000000000003	0.54200000000000004	0.54400000000000004	0.55000000000000004	0.55400000000000005	0.56000000000000005	0.56399999999999995	0.56999999999999995	0.57599999999999996	0.58199999999999996	0.58599999999999997	0.59399999999999997	0.6	0.60599999999999998	0.61399999999999999	0.622	0.63	0.63400000000000001	0.64400000000000002	0.65200000000000002	0.66	0.66600000000000004	0.67600000000000005	0.68400000000000005	0.69399999999999995	0.70199999999999996	0.71199999999999997	0.72199999999999998	0.73199999999999998	0.74199999999999999	0.752	0.76200000000000001	0.77200000000000002	0.78200000000000003	0.79400000000000004	0.80400000000000005	0.81599999999999995	0.82599999999999996	0.84	0.85199999999999998	0.86399999999999999	0.876	0.89	0.90200000000000002	0.91400000000000003	0.92600000000000005	0.94	0.95399999999999996	0.96599999999999997	0.98199999999999998	0.996	1.012	1.024	1.04	1.054	1.07	1.0840000000000001	1.0960000000000001	1.1060000000000001	1.1220000000000001	1.1399999999999999	1.1559999999999999	1.1719999999999999	1.19	1.206	1.222	1.242	1.26	1.276	1.294	1.3120000000000001	1.33	1.35	1.3660000000000001	1.3859999999999999	1.4059999999999999	1.4239999999999999	1.444	1.464	1.484	1.504	1.524	1.544	1.5640000000000001	1.5860000000000001	1.6060000000000001	1.6259999999999999	1.6459999999999999	1.6659999999999999	1.6859999999999999	1.706	1.726	1.746	1.766	1.786	1.81	1.83	1.85	1.87	1.89	1.91	1.93	1.948	1.968	1.988	2.008	2.028	2.048	2.0680000000000001	2.0920000000000001	2.1120000000000001	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.73599999999999999	0.73599999999999999	0.73599999999999999	0.73599999999999999	0.73599999999999999	0.73599999999999999	0.73599999999999999	0.73599999999999999	0.73599999999999999	1.105	1.105	1.105	1.105	1.105	1.105	1.105	1.4730000000000001	1.4730000000000001	1.4730000000000001	1.4730000000000001	1.4730000000000001	1.841	1.841	1.841	1.841	1.841	1.841	2.2090000000000001	2.2090000000000001	2.2090000000000001	2.2090000000000001	2.2090000000000001	2.577	2.577	2.577	2.577	2.9460000000000002	2.9460000000000002	2.9460000000000002	2.9460000000000002	3.3140000000000001	3.3140000000000001	3.3140000000000001	3.3140000000000001	3.3140000000000001	3.6819999999999999	3.6819999999999999	3.6819999999999999	4.05	4.05	4.05	4.05	4.4180000000000001	4.4180000000000001	4.4180000000000001	4.4180000000000001	4.7859999999999996	4.7859999999999996	4.7859999999999996	5.1550000000000002	5.1550000000000002	5.1550000000000002	5.1550000000000002	5.5229999999999997	5.5229999999999997	5.5229999999999997	5.5229999999999997	5.891	5.891	5.891	5.891	6.2590000000000003	6.2590000000000003	6.2590000000000003	6.2590000000000003	6.6269999999999998	6.6269999999999998	6.6269999999999998	6.6269999999999998	6.6269999999999998	6.9960000000000004	6.9960000000000004	6.9960000000000004	6.9960000000000004	6.9960000000000004	7.3639999999999999	7.3639999999999999	7.3639999999999999	7.3639999999999999	7.3639999999999999	7.3639999999999999	7.3639999999999999	7.7320000000000002	7.7320000000000002	7.7320000000000002	7.7320000000000002	7.7320000000000002	7.7320000000000002	7.7320000000000002	7.7320000000000002	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.1	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.468	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	8.8369999999999997	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.2050000000000001	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.5730000000000004	9.9410000000000007	9.9410000000000007	9.9410000000000007	9.9410000000000007	9.9410000000000007	9.9410000000000007	9.9410000000000007	9.9410000000000007	10.308999999999999	10.308999999999999	10.308999999999999	10.308999999999999	10.308999999999999	10.308999999999999	10.308999999999999	10.677	10.677	10.677	10.677	10.677	11.045999999999999	11.045999999999999	11.045999999999999	11.045999999999999	11.414	11.414	11.414	11.782	11.782	12.15	12.15	12.15	12.518000000000001	12.518000000000001	12.887	13.255000000000001	13.255000000000001	13.622999999999999	13.622999999999999	13.991	14.359	14.728	15.096	15.464	15.832000000000001	16.568000000000001	17.305	18.041	18.777999999999999	19.513999999999999	20.619	21.355	22.459	23.564	24.669	25.405000000000001	26.878	28.350999999999999	29.087	30.56	31.664000000000001	33.137	34.61	35.713999999999999	37.186999999999998	38.292000000000002	39.764000000000003	40.869	42.341999999999999	43.445999999999998	44.918999999999997	46.024000000000001	47.496000000000002	48.600999999999999	49.337000000000003	50.442	51.914999999999999	53.018999999999998	53.756	55.228000000000002	56.332999999999998	57.069000000000003	57.805999999999997	59.277999999999999	60.383000000000003	61.119	61.856000000000002	63.328000000000003	64.064999999999998	65.168999999999997	65.906000000000006	67.010000000000005	68.114999999999995	68.850999999999999	69.956000000000003	70.691999999999993	71.796999999999997	72.533000000000001	73.27	74.742000000000004	75.478999999999999	76.215000000000003	77.319999999999993	78.055999999999997	78.792000000000002	79.528999999999996	81.001000000000005	81.738	82.474000000000004	82.841999999999999	83.578999999999994	83.947000000000003	84.683000000000007	85.052000000000007	85.787999999999997	86.156000000000006	86.891999999999996	87.629000000000005	88.364999999999995	89.102000000000004	89.837999999999994	90.573999999999998	91.311000000000007	92.046999999999997	93.152000000000001	93.888000000000005	94.623999999999995	95.361000000000004	96.096999999999994	96.834000000000003	97.57	98.305999999999997	99.043000000000006	99.778999999999996	100.14700000000001	100.884	101.62	101.988	102.72499999999999	103.461	103.82899999999999	104.197	104.934	105.30200000000001	106.038	106.40600000000001	106.77500000000001	107.143	107.511	107.879	108.616	108.98399999999999	109.352	109.72	110.08799999999999	110.45699999999999	110.45699999999999	110.825	111.193	111.56100000000001	111.56100000000001	111.929	112.298	112.666	112.666	113.03400000000001	113.402	113.402	113.77	113.77	114.13800000000001	114.50700000000001	114.50700000000001	114.875	114.875	115.24299999999999	115.24299999999999	115.611	115.611	115.979	115.979	116.348	116.348	116.348	116.71599999999999	116.71599999999999	116.71599999999999	117.084	117.084	117.452	117.452	117.452	117.82	117.82	117.82	118.18899999999999	118.18899999999999	118.18899999999999	118.557	118.557	118.557	118.925	118.925	119.29300000000001	119.29300000000001	119.29300000000001	119.661	119.661	120.029	120.029	120.398	120.398	120.76600000000001	120.76600000000001	121.134	121.134	121.502	121.502	121.87	121.87	122.239	122.239	122.607	122.607	122.97499999999999	122.97499999999999	123.343	123.711	123.711	124.08	124.08	124.44799999999999	124.44799999999999	124.816	124.816	125.184	125.55200000000001	125.55200000000001	125.92	125.92	126.289	126.657	126.657	127.02500000000001	127.393	127.393	127.761	128.13	128.13	128.49799999999999	128.49799999999999	128.86600000000001	129.23400000000001	129.23400000000001	129.602	129.971	129.971	130.339	130.339	130.70699999999999	131.07499999999999	131.44300000000001	131.44300000000001	131.81100000000001	132.18	132.18	132.548	132.916	132.916	133.28399999999999	133.65199999999999	133.65199999999999	134.02099999999999	134.38900000000001	134.38900000000001	134.75700000000001	135.125	135.49299999999999	135.49299999999999	135.86199999999999	136.22999999999999	136.22999999999999	136.59800000000001	136.59800000000001	136.96600000000001	137.334	137.703	138.071	138.071	138.43899999999999	138.80699999999999	138.80699999999999	139.17500000000001	139.17500000000001	139.54300000000001	139.91200000000001	140.28	140.648	140.648	141.01599999999999	141.38399999999999	141.38399999999999	141.75299999999999	142.12100000000001	142.489	142.857	142.857	143.22499999999999	143.59399999999999	143.96199999999999	144.33000000000001	144.69800000000001	144.69800000000001	145.066	145.434	145.803	146.17099999999999	146.53899999999999	146.90700000000001	146.90700000000001	147.27500000000001	147.64400000000001	148.012	148.38	148.38	148.74799999999999	149.11600000000001	149.48500000000001	149.85300000000001	150.221	150.221	150.589	150.95699999999999	151.32499999999999	151.69399999999999	152.06200000000001	152.43	152.43	152.798	153.166	153.535	153.90299999999999	153.90299999999999	154.27099999999999	154.63900000000001	155.00700000000001	155.376	155.376	155.744	156.11199999999999	156.47999999999999	156.84800000000001	156.84800000000001	157.21600000000001	157.58500000000001	157.953	158.321	158.68899999999999	158.68899999999999	159.05699999999999	159.42599999999999	159.79400000000001	160.16200000000001	160.16200000000001	160.898	161.267	161.267	161.63499999999999	162.00299999999999	162.37100000000001	162.739	163.107	163.107	163.476	163.84399999999999	164.21199999999999	164.58	164.94800000000001	164.94800000000001	165.31700000000001	165.685	166.053	166.42099999999999	166.42099999999999	166.78899999999999	167.15799999999999	167.52600000000001	167.89400000000001	168.262	168.262	168.63	168.999	169.36699999999999	169.73500000000001	170.10300000000001	170.10300000000001	170.471	170.839	171.208	171.57599999999999	171.94399999999999	171.94399999999999	172.31200000000001	172.68	173.04900000000001	173.417	173.417	173.785	174.15299999999999	174.52099999999999	174.89	175.25800000000001	175.25800000000001	175.626	175.994	176.36199999999999	176.73	177.09899999999999	177.09899999999999	177.46700000000001	177.83500000000001	178.203	178.571	178.94	178.94	179.30799999999999	179.67599999999999	180.04400000000001	180.41200000000001	180.41200000000001	180.78100000000001	181.149	181.517	181.88499999999999	182.25299999999999	182.25299999999999	182.62200000000001	182.99	183.358	183.726	184.09399999999999	184.09399999999999	184.46199999999999	184.83099999999999	185.19900000000001	185.56700000000001	185.935	185.935	186.303	186.672	187.04	187.40799999999999	187.77600000000001	187.77600000000001	188.14400000000001	188.51300000000001	188.881	189.249	189.249	189.61699999999999	189.98500000000001	190.35300000000001	190.72200000000001	191.09	191.09	191.458	191.82599999999999	192.19399999999999	192.56299999999999	192.93100000000001	193.29900000000001	193.29900000000001	193.667	194.035	194.404	194.77199999999999	195.14	195.14	195.50800000000001	195.876	196.244	196.613	196.98099999999999	196.98099999999999	197.34899999999999	197.71700000000001	198.08500000000001	198.45400000000001	198.822	199.19	199.55799999999999	199.92599999999999	199.92599999999999	200.29499999999999	200.66300000000001	201.03100000000001	201.399	201.767	202.13499999999999	202.13499999999999	202.50399999999999	202.87200000000001	203.24	203.608	203.976	203.976	204.345	204.71299999999999	205.08099999999999	205.44900000000001	205.81700000000001	205.81700000000001	206.18600000000001	206.554	206.922	207.29	207.29	207.65799999999999	208.02699999999999	208.39500000000001	208.76300000000001	209.131	209.131	209.499	209.86699999999999	210.23599999999999	210.60400000000001	210.60400000000001	210.97200000000001	211.34	211.708	212.077	212.44499999999999	212.44499999999999	212.81299999999999	213.18100000000001	213.54900000000001	213.91800000000001	214.286	214.286	214.654	215.02199999999999	215.39	215.75800000000001	215.75800000000001	216.12700000000001	216.495	216.863	217.23099999999999	217.59899999999999	217.59899999999999	217.96799999999999	218.33600000000001	218.70400000000001	219.072	219.072	219.44	219.809	220.17699999999999	220.54499999999999	220.54499999999999	220.91300000000001	221.28100000000001	221.649	222.018	222.386	222.386	222.75399999999999	223.12200000000001	223.49	223.85900000000001	223.85900000000001	224.227	224.595	224.595	224.96299999999999	225.33099999999999	225.7	226.06800000000001	226.43600000000001	226.43600000000001	226.804	227.172	227.54	227.90899999999999	228.27699999999999	228.27699999999999	228.64500000000001	229.01300000000001	229.381	229.75	230.11799999999999	230.11799999999999	230.48599999999999	230.85400000000001	231.22200000000001	231.59100000000001	231.959	231.959	232.327	232.69499999999999	233.06299999999999	233.43199999999999	233.8	233.8	234.16800000000001	234.536	234.904	235.27199999999999	235.27199999999999	235.64099999999999	236.00899999999999	236.37700000000001	236.745	237.113	237.113	237.482	237.85	238.21799999999999	238.58600000000001	238.95400000000001	238.95400000000001	239.32300000000001	239.691	240.059	240.42699999999999	240.79499999999999	241.16300000000001	241.16300000000001	241.53200000000001	241.9	242.268	242.636	243.00399999999999	243.00399999999999	243.37299999999999	243.74100000000001	244.10900000000001	244.477	244.845	244.845	245.214	245.58199999999999	245.95	246.31800000000001	246.68600000000001	246.68600000000001	247.054	247.423	247.791	248.15899999999999	248.52699999999999	248.89500000000001	249.26400000000001	249.26400000000001	249.63200000000001	250	250.36799999999999	250.73599999999999	251.10499999999999	251.10499999999999	251.47300000000001	251.84100000000001	252.209	252.577	252.946	252.946	253.31399999999999	253.68199999999999	254.05	254.41800000000001	254.786	254.786	255.155	255.523	255.89099999999999	256.25900000000001	256.62700000000001	256.62700000000001	256.99599999999998	257.36399999999998	257.73200000000003	257.73200000000003	258.10000000000002	258.46800000000002	258.83699999999999	259.20499999999998	259.20499999999998	259.57299999999998	259.94099999999997	260.30900000000003	260.67700000000002	261.04599999999999	261.41399999999999	261.78199999999998	261.78199999999998	262.14999999999998	262.51799999999997	262.887	263.255	263.62299999999999	263.62299999999999	263.99099999999999	264.35899999999998	264.72800000000001	265.096	265.464	265.464	265.83199999999999	266.2	266.56799999999998	266.93700000000001	266.93700000000001	267.30500000000001	267.673	267.673	268.041	268.40899999999999	268.77800000000002	269.14600000000002	269.14600000000002	269.51400000000001	269.88200000000001	270.25	270.61900000000003	270.61900000000003	270.98700000000002	271.35500000000002	271.72300000000001	272.09100000000001	272.09100000000001	272.45999999999998	272.82799999999997	273.19600000000003	273.56400000000002	273.56400000000002	273.93200000000002	274.3	274.66899999999998	275.03699999999998	275.40499999999997	275.77300000000002	275.77300000000002	276.14100000000002	276.51	276.51	276.87799999999999	277.24599999999998	277.61399999999998	277.61399999999998	277.98200000000003	278.35000000000002	278.71899999999999	279.08699999999999	279.08699999999999	279.45499999999998	279.82299999999998	280.19099999999997	280.56	280.56	280.928	281.29599999999999	281.66399999999999	282.03199999999998	282.03199999999998	282.40100000000001	282.76900000000001	283.137	283.505	283.87299999999999	283.87299999999999	284.24200000000002	284.61	284.97800000000001	285.346	285.346	285.714	286.08199999999999	286.45100000000002	286.81900000000002	286.81900000000002	287.18700000000001	287.55500000000001	287.923	288.29199999999997	288.29199999999997	288.66000000000003	289.02800000000002	289.02800000000002	289.39600000000002	289.76400000000001	290.13299999999998	290.50099999999998	290.86900000000003	290.86900000000003	291.23700000000002	291.60500000000002	291.97300000000001	292.34199999999998	292.34199999999998	292.70999999999998	293.07799999999997	293.44600000000003	293.81400000000002	293.81400000000002	294.18299999999999	294.55099999999999	294.91899999999998	295.28699999999998	295.65499999999997	295.65499999999997	296.392	296.392	296.76	297.12799999999999	297.49599999999998	297.86500000000001	298.233	298.233	298.601	298.96899999999999	299.33699999999999	299.70499999999998	299.70499999999998	300.07400000000001	300.44200000000001	300.81	301.178	301.178	301.54599999999999	301.91500000000002	302.28300000000002	302.65100000000001	303.01900000000001	303.01900000000001	303.387	303.75599999999997	304.12400000000002	304.49200000000002	304.49200000000002	304.86	305.22800000000001	305.596	305.96499999999997	306.33300000000003	306.33300000000003	306.70100000000002	307.06900000000002	307.43700000000001	307.80599999999998	308.17399999999998	308.17399999999998	308.54199999999997	308.91000000000003	309.27800000000002	309.64699999999999	310.01499999999999	310.01499999999999	310.38299999999998	310.75099999999998	311.11900000000003	311.48700000000002	311.85599999999999	311.85599999999999	312.22399999999999	312.59199999999998	312.95999999999998	313.32799999999997	313.32799999999997	313.697	314.065	314.43299999999999	314.80099999999999	315.16899999999998	315.16899999999998	315.53800000000001	315.90600000000001	316.274	316.642	317.01	317.37799999999999	317.37799999999999	317.74700000000001	318.11500000000001	318.483	318.851	319.21899999999999	319.21899999999999	319.58800000000002	319.95600000000002	320.32400000000001	320.69200000000001	321.06	321.42899999999997	321.79700000000003	322.16500000000002	322.53300000000002	322.90100000000001	322.90100000000001	323.27	323.63799999999998	324.00599999999997	324.37400000000002	324.74200000000002	325.11	325.47899999999998	325.47899999999998	325.84699999999998	326.21499999999997	326.58300000000003	326.95100000000002	327.32	327.68799999999999	328.05599999999998	328.05599999999998	328.42399999999998	328.79199999999997	329.161	329.529	329.89699999999999	330.26499999999999	330.63299999999998	330.63299999999998	331.00099999999998	331.37	331.738	332.10599999999999	332.47399999999999	332.84199999999998	332.84199999999998	333.21100000000001	333.57900000000001	333.947	334.315	334.68299999999999	335.05200000000002	335.05200000000002	335.42	335.78800000000001	336.15600000000001	336.524	336.892	337.26100000000002	337.62900000000002	337.62900000000002	337.99700000000001	338.733	338.733	339.10199999999998	339.47	339.83800000000002	340.20600000000002	340.57400000000001	340.94299999999998	341.31099999999998	341.31099999999998	341.67899999999997	342.04700000000003	342.41500000000002	342.78399999999999	343.15199999999999	343.52	343.88799999999998	343.88799999999998	344.25599999999997	344.62400000000002	344.99299999999999	345.36099999999999	345.72899999999998	346.09699999999998	346.09699999999998	346.46499999999997	346.834	347.202	347.57	347.93799999999999	347.93799999999999	348.30599999999998	348.67500000000001	348.67500000000001	349.04300000000001	349.04300000000001	349.04300000000001	349.04300000000001	349.411	349.411	349.411	349.411	349.04300000000001	349.04300000000001	349.04300000000001	349.04300000000001	348.67500000000001	348.67500000000001	348.30599999999998	348.30599999999998	347.93799999999999	347.57	347.57	347.202	346.834	346.46499999999997	346.09699999999998	345.72899999999998	345.36099999999999	344.99299999999999	344.62400000000002	344.62400000000002	344.25599999999997	343.88799999999998	343.52	343.15199999999999	342.78399999999999	342.78399999999999	342.41500000000002	342.04700000000003	342.04700000000003	341.67899999999997	341.31099999999998	341.31099999999998	340.94299999999998	340.57400000000001	340.57400000000001	340.20600000000002	340.20600000000002	339.83800000000002	339.83800000000002	339.47	339.47	339.47	339.10199999999998	339.10199999999998	338.733	338.733	338.36500000000001	338.36500000000001	338.36500000000001	337.99700000000001	337.99700000000001	337.99700000000001	337.62900000000002	337.62900000000002	337.62900000000002	337.26100000000002	337.26100000000002	337.26100000000002	336.892	336.892	336.892	336.524	336.524	336.524	336.15600000000001	336.15600000000001	336.15600000000001	336.15600000000001	335.78800000000001	335.78800000000001	335.78800000000001	335.78800000000001	335.42	335.42	335.42	335.05200000000002	335.05200000000002	335.05200000000002	335.05200000000002	334.68299999999999	334.68299999999999	334.68299999999999	334.68299999999999	334.315	334.315	333.947	333.947	333.947	333.57900000000001	333.57900000000001	333.57900000000001	333.57900000000001	333.21100000000001	333.21100000000001	333.21100000000001	333.21100000000001	332.84199999999998	332.84199999999998	332.84199999999998	332.84199999999998	332.84199999999998	332.47399999999999	332.47399999999999	332.47399999999999	332.47399999999999	332.47399999999999	332.10599999999999	332.10599999999999	332.10599999999999	332.10599999999999	332.10599999999999	331.738	331.738	331.738	331.738	331.738	331.37	331.37	331.37	331.37	331.37	331.00099999999998	331.00099999999998	331.00099999999998	331.00099999999998	331.00099999999998	331.00099999999998	330.63299999999998	330.63299999999998	330.63299999999998	330.63299999999998	330.63299999999998	330.63299999999998	330.26499999999999	330.26499999999999	330.26499999999999	330.26499999999999	330.26499999999999	330.26499999999999	329.89699999999999	329.89699999999999	329.89699999999999	329.89699999999999	329.89699999999999	329.89699999999999	329.529	329.529	329.529	329.529	329.529	329.529	329.529	329.161	329.161	329.161	329.161	329.161	329.161	329.161	328.79199999999997	328.79199999999997	328.79199999999997	328.79199999999997	328.79199999999997	328.79199999999997	328.42399999999998	328.42399999999998	328.42399999999998	328.42399999999998	328.42399999999998	328.42399999999998	328.42399999999998	328.05599999999998	328.05599999999998	328.05599999999998	328.05599999999998	328.05599999999998	328.05599999999998	328.05599999999998	327.68799999999999	327.68799999999999	327.68799999999999	327.68799999999999	327.68799999999999	327.68799999999999	327.68799999999999	327.32	327.32	327.32	327.32	327.32	327.32	327.32	326.95100000000002	326.95100000000002	326.95100000000002	326.95100000000002	326.95100000000002	326.95100000000002	326.95100000000002	326.58300000000003	326.58300000000003	326.58300000000003	326.58300000000003	326.58300000000003	326.58300000000003	326.58300000000003	326.21499999999997	326.21499999999997	326.21499999999997	326.21499999999997	326.21499999999997	326.21499999999997	326.21499999999997	326.21499999999997	325.84699999999998	325.84699999999998	325.84699999999998	325.84699999999998	325.84699999999998	325.84699999999998	325.84699999999998	325.84699999999998	325.47899999999998	325.47899999999998	325.47899999999998	325.47899999999998	325.47899999999998	325.47899999999998	325.47899999999998	325.47899999999998	325.11	325.11	325.11	325.11	325.11	325.11	325.11	325.11	325.11	324.74200000000002	324.74200000000002	324.74200000000002	324.74200000000002	324.74200000000002	324.74200000000002	324.74200000000002	324.74200000000002	324.74200000000002	324.37400000000002	324.37400000000002	324.37400000000002	324.37400000000002	324.37400000000002	324.37400000000002	324.37400000000002	324.37400000000002	324.37400000000002	324.00599999999997	324.00599999999997	324.00599999999997	324.00599999999997	324.00599999999997	324.00599999999997	324.00599999999997	324.00599999999997	324.00599999999997	323.63799999999998	323.63799999999998	323.63799999999998	323.63799999999998	323.63799999999998	323.63799999999998	323.63799999999998	323.63799999999998	323.63799999999998	323.27	323.27	323.27	323.27	323.27	323.27	323.27	323.27	323.27	323.27	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.90100000000001	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.53300000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	322.16500000000002	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.79700000000003	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.42899999999997	321.06	321.06	321.06	321.06	321.06	321.06	321.06	321.06	321.06	321.06	321.06	321.06	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.69200000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	320.32400000000001	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.95600000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.58800000000002	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	319.21899999999999	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.851	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.483	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	318.11500000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.74700000000001	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.37799999999999	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	317.01	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.642	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	316.274	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.90600000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.53800000000001	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	315.16899999999998	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.80099999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.43299999999999	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	314.065	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.697	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.32799999999997	313.697	313.697	313.697	313.697	314.065	314.065	314.065	314.43299999999999	314.43299999999999	314.80099999999999	314.80099999999999	315.16899999999998	315.16899999999998	315.53800000000001	315.90600000000001	315.90600000000001	316.274	316.642	317.01	317.37799999999999	318.11500000000001	318.851	319.58800000000002	320.32400000000001	321.42899999999997	322.53300000000002	324.00599999999997	325.47899999999998	326.58300000000003	327.68799999999999	329.161	330.63299999999998	332.10599999999999	333.57900000000001	334.68299999999999	336.15600000000001	337.62900000000002	339.10199999999998	340.94299999999998	342.41500000000002	343.52	345.36099999999999	347.202	348.30599999999998	350.14699999999999	351.988	353.09300000000002	355.30200000000002	356.77499999999998	358.61599999999999	360.08800000000002	361.56099999999998	363.77	365.24299999999999	367.452	368.92500000000001	370.76600000000002	372.97500000000002	374.44799999999998	375.92	377.76100000000002	379.971	381.81099999999998	383.28399999999999	384.75700000000001	386.23	388.43900000000002	390.28	391.75299999999999	393.22500000000002	395.43400000000003	397.27499999999998	398.74799999999999	400.221	402.06200000000001	403.90300000000002	406.48	407.95299999999997	409.79399999999998	411.267	413.108	414.58	416.42099999999999	418.63	420.10300000000001	421.94400000000002	423.41699999999997	424.89	426.73	428.20299999999997	429.67599999999999	431.149	432.62200000000001	434.09399999999999	435.19900000000001	437.40800000000002	438.51299999999998	439.98500000000001	440.72199999999998	441.45800000000003	442.56299999999999	443.29899999999998	444.03500000000003	444.77199999999999	445.50799999999998	446.24400000000003	446.98099999999999	447.71699999999998	448.45400000000001	449.19	449.92599999999999	450.66300000000001	451.399	452.50400000000002	453.24	454.34500000000003	455.08100000000002	Sample 3	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7999999999999999E-2	0.02	2.1000000000000001E-2	2.1999999999999999E-2	2.3E-2	2.4E-2	2.5999999999999999E-2	2.7E-2	2.8000000000000001E-2	0.03	3.2000000000000001E-2	3.3000000000000002E-2	3.5000000000000003E-2	3.6999999999999998E-2	3.7999999999999999E-2	0.04	4.2000000000000003E-2	4.3999999999999997E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.7E-2	0.05	5.1999999999999998E-2	5.3999999999999999E-2	5.6000000000000001E-2	5.6000000000000001E-2	6.0999999999999999E-2	6.3E-2	6.6000000000000003E-2	6.8000000000000005E-2	7.0000000000000007E-2	7.1999999999999995E-2	7.3999999999999996E-2	7.5999999999999998E-2	7.8E-2	8.1000000000000003E-2	8.3000000000000004E-2	8.5000000000000006E-2	8.5999999999999993E-2	8.7999999999999995E-2	0.09	9.1999999999999998E-2	9.4E-2	9.6000000000000002E-2	9.8000000000000004E-2	9.9000000000000005E-2	0.10100000000000001	0.10299999999999999	0.105	0.107	0.108	0.11	0.112	0.114	0.11600000000000001	0.11799999999999999	0.12	0.121	0.123	0.125	0.127	0.128	0.13	0.13200000000000001	0.13400000000000001	0.13600000000000001	0.13800000000000001	0.13900000000000001	0.14099999999999999	0.14299999999999999	0.14399999999999999	0.14599999999999999	0.14799999999999999	0.15	0.152	0.154	0.155	0.157	0.159	0.16	0.16200000000000001	0.16400000000000001	0.16600000000000001	0.16800000000000001	0.16900000000000001	0.17100000000000001	0.17299999999999999	0.17399999999999999	0.17599999999999999	0.17799999999999999	0.18	0.18099999999999999	0.183	0.185	0.186	0.188	0.19	0.191	0.193	0.19400000000000001	0.19600000000000001	0.19800000000000001	0.19900000000000001	0.20100000000000001	0.20200000000000001	0.20399999999999999	0.20499999999999999	0.20599999999999999	0.20799999999999999	0.20899999999999999	0.21	0.21199999999999999	0.21299999999999999	0.214	0.215	0.216	0.218	0.218	0.22	0.221	0.222	0.223	0.224	0.224	0.22600000000000001	0.22600000000000001	0.22700000000000001	0.22800000000000001	0.22900000000000001	0.23	0.23	0.23100000000000001	0.23200000000000001	0.23200000000000001	0.23300000000000001	0.23400000000000001	0.23400000000000001	0.23499999999999999	0.23599999999999999	0.23599999999999999	0.23599999999999999	0.23699999999999999	0.23699999999999999	0.23799999999999999	0.23799999999999999	0.23799999999999999	0.23899999999999999	0.23899999999999999	0.24	0.24	0.24	0.24	0.24099999999999999	0.24099999999999999	0.24199999999999999	0.24199999999999999	0.24199999999999999	0.24299999999999999	0.24299999999999999	0.24399999999999999	0.24399999999999999	0.24399999999999999	0.245	0.245	0.246	0.246	0.246	0.246	0.247	0.247	0.248	0.248	0.248	0.249	0.249	0.25	0.25	0.25	0.251	0.251	0.252	0.252	0.252	0.253	0.254	0.254	0.254	0.255	0.255	0.25600000000000001	0.25600000000000001	0.25600000000000001	0.25700000000000001	0.25700000000000001	0.25800000000000001	0.25800000000000001	0.25800000000000001	0.25900000000000001	0.25900000000000001	0.26	0.26	0.26	0.26100000000000001	0.26100000000000001	0.26200000000000001	0.26200000000000001	0.26300000000000001	0.26300000000000001	0.26400000000000001	0.26400000000000001	0.26400000000000001	0.26500000000000001	0.26500000000000001	0.26600000000000001	0.26600000000000001	0.26600000000000001	0.26700000000000002	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26900000000000002	0.26900000000000002	0.27	0.27	0.27	0.27100000000000002	0.27100000000000002	0.27200000000000002	0.27200000000000002	0.27200000000000002	0.27300000000000002	0.27400000000000002	0.27400000000000002	0.27400000000000002	0.27500000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27800000000000002	0.27800000000000002	0.27800000000000002	0.27900000000000003	0.27900000000000003	0.28000000000000003	0.28000000000000003	0.28100000000000003	0.28100000000000003	0.28199999999999997	0.28199999999999997	0.28199999999999997	0.28299999999999997	0.28299999999999997	0.28399999999999997	0.28399999999999997	0.28499999999999998	0.28499999999999998	0.28599999999999998	0.28599999999999998	0.28599999999999998	0.28699999999999998	0.28699999999999998	0.28799999999999998	0.28799999999999998	0.28899999999999998	0.28899999999999998	0.28999999999999998	0.28999999999999998	0.28999999999999998	0.29099999999999998	0.29199999999999998	0.29199999999999998	0.29199999999999998	0.29299999999999998	0.29299999999999998	0.29399999999999998	0.29399999999999998	0.29499999999999998	0.29499999999999998	0.29599999999999999	0.29599999999999999	0.29599999999999999	0.29699999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.29899999999999999	0.3	0.3	0.3	0.30099999999999999	0.30199999999999999	0.30199999999999999	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30399999999999999	0.30499999999999999	0.30599999999999999	0.30599999999999999	0.30599999999999999	0.307	0.307	0.308	0.308	0.309	0.309	0.31	0.31	0.31	0.311	0.311	0.312	0.312	0.313	0.313	0.314	0.314	0.314	0.315	0.316	0.316	0.316	0.317	0.317	0.318	0.318	0.318	0.31900000000000001	0.32	0.32	0.32	0.32100000000000001	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32400000000000001	0.32500000000000001	0.32500000000000001	0.32600000000000001	0.32600000000000001	0.32700000000000001	0.32700000000000001	0.32800000000000001	0.32800000000000001	0.32800000000000001	0.32800000000000001	0.33	0.33	0.33	0.33100000000000002	0.33100000000000002	0.33200000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33400000000000002	0.33400000000000002	0.33400000000000002	0.33500000000000002	0.33500000000000002	0.33600000000000002	0.33600000000000002	0.33700000000000002	0.33700000000000002	0.33800000000000002	0.33800000000000002	0.33800000000000002	0.33800000000000002	0.33900000000000002	0.34	0.34	0.34100000000000003	0.34100000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34300000000000003	0.34399999999999997	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34699999999999998	0.34799999999999998	0.34799999999999998	0.34799999999999998	0.34899999999999998	0.34899999999999998	0.35	0.35	0.35099999999999998	0.35099999999999998	0.35199999999999998	0.35199999999999998	0.35199999999999998	0.35299999999999998	0.35399999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35499999999999998	0.35599999999999998	0.35599999999999998	0.35699999999999998	0.35699999999999998	0.35799999999999998	0.35799999999999998	0.35799999999999998	0.35899999999999999	0.36	0.36	0.36	0.36099999999999999	0.36099999999999999	0.36199999999999999	0.36199999999999999	0.36199999999999999	0.36199999999999999	0.36399999999999999	0.36399999999999999	0.36399999999999999	0.36499999999999999	0.36499999999999999	0.36599999999999999	0.36599999999999999	0.36699999999999999	0.36699999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36899999999999999	0.37	0.37	0.37	0.371	0.371	0.372	0.372	0.373	0.373	0.374	0.374	0.375	0.375	0.376	0.376	0.376	0.377	0.378	0.378	0.378	0.379	0.379	0.38	0.38	0.38100000000000001	0.38100000000000001	0.38200000000000001	0.38200000000000001	0.38300000000000001	0.38300000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38500000000000001	0.38600000000000001	0.38600000000000001	0.38600000000000001	0.38700000000000001	0.38800000000000001	0.38800000000000001	0.38800000000000001	0.38900000000000001	0.39	0.39	0.39	0.39100000000000001	0.39200000000000002	0.39200000000000002	0.39200000000000002	0.39300000000000002	0.39300000000000002	0.39400000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39600000000000002	0.39600000000000002	0.39700000000000002	0.39700000000000002	0.39800000000000002	0.39800000000000002	0.39900000000000002	0.39900000000000002	0.4	0.4	0.40100000000000002	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40300000000000002	0.40400000000000003	0.40400000000000003	0.40400000000000003	0.40500000000000003	0.40600000000000003	0.40600000000000003	0.40600000000000003	0.40699999999999997	0.40799999999999997	0.40799999999999997	0.40799999999999997	0.40899999999999997	0.40899999999999997	0.41	0.41	0.41099999999999998	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41299999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41399999999999998	0.41499999999999998	0.41599999999999998	0.41599999999999998	0.41599999999999998	0.41699999999999998	0.41799999999999998	0.41799999999999998	0.41799999999999998	0.41899999999999998	0.42	0.42	0.42	0.42099999999999999	0.42099999999999999	0.42199999999999999	0.42199999999999999	0.42299999999999999	0.42299999999999999	0.42399999999999999	0.42399999999999999	0.42399999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42699999999999999	0.42699999999999999	0.42799999999999999	0.42899999999999999	0.42899999999999999	0.43	0.43	0.43099999999999999	0.43099999999999999	0.432	0.432	0.432	0.433	0.434	0.434	0.434	0.435	0.435	0.436	0.436	0.437	0.437	0.438	0.438	0.439	0.439	0.44	0.44	0.441	0.441	0.442	0.442	0.442	0.443	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44500000000000001	0.44500000000000001	0.44600000000000001	0.44600000000000001	0.44700000000000001	0.44700000000000001	0.44800000000000001	0.44800000000000001	0.44900000000000001	0.44900000000000001	0.45	0.45	0.45	0.45100000000000001	0.45100000000000001	0.45100000000000001	0.45200000000000001	0.45300000000000001	0.45300000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45700000000000002	0.45800000000000002	0.45800000000000002	0.45900000000000002	0.45900000000000002	0.46	0.46	0.46100000000000002	0.46100000000000002	0.46200000000000002	0.46200000000000002	0.46200000000000002	0.46300000000000002	0.46300000000000002	0.46400000000000002	0.46400000000000002	0.46500000000000002	0.46500000000000002	0.46600000000000003	0.46600000000000003	0.46700000000000003	0.46700000000000003	0.46800000000000003	0.46800000000000003	0.46800000000000003	0.46899999999999997	0.46899999999999997	0.47	0.47	0.47099999999999997	0.47099999999999997	0.47199999999999998	0.47199999999999998	0.47299999999999998	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47499999999999998	0.47499999999999998	0.47599999999999998	0.47599999999999998	0.47599999999999998	0.47699999999999998	0.47699999999999998	0.47799999999999998	0.47799999999999998	0.47899999999999998	0.47899999999999998	0.48	0.48	0.48099999999999998	0.48099999999999998	0.48199999999999998	0.48199999999999998	0.48199999999999998	0.48299999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48499999999999999	0.48499999999999999	0.48599999999999999	0.48599999999999999	0.48699999999999999	0.48699999999999999	0.48799999999999999	0.48799999999999999	0.48799999999999999	0.48899999999999999	0.49	0.49	0.49	0.49099999999999999	0.49099999999999999	0.49199999999999999	0.49199999999999999	0.49299999999999999	0.49299999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.495	0.496	0.496	0.496	0.497	0.497	0.498	0.498	0.499	0.499	0.5	0.5	0.501	0.501	0.502	0.502	0.502	0.503	0.504	0.504	0.504	0.505	0.505	0.50600000000000001	0.50600000000000001	0.50700000000000001	0.50700000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50900000000000001	0.50900000000000001	0.51	0.51	0.51100000000000001	0.51100000000000001	0.51200000000000001	0.51200000000000001	0.51200000000000001	0.51300000000000001	0.51300000000000001	0.51400000000000001	0.51400000000000001	0.51500000000000001	0.51500000000000001	0.51600000000000001	0.51600000000000001	0.51600000000000001	0.51700000000000002	0.51800000000000002	0.51800000000000002	0.51800000000000002	0.51900000000000002	0.52	0.52	0.52	0.52100000000000002	0.52100000000000002	0.52200000000000002	0.52200000000000002	0.52300000000000002	0.52300000000000002	0.52400000000000002	0.52400000000000002	0.52500000000000002	0.52500000000000002	0.52600000000000002	0.52600000000000002	0.52600000000000002	0.52700000000000002	0.52800000000000002	0.52800000000000002	0.52800000000000002	0.52900000000000003	0.53	0.53	0.53	0.53100000000000003	0.53200000000000003	0.53200000000000003	0.53200000000000003	0.53300000000000003	0.53400000000000003	0.53400000000000003	0.53400000000000003	0.53500000000000003	0.53600000000000003	0.53600000000000003	0.53600000000000003	0.53700000000000003	0.53800000000000003	0.53800000000000003	0.53800000000000003	0.53900000000000003	0.54	0.54	0.54	0.54100000000000004	0.54100000000000004	0.54200000000000004	0.54200000000000004	0.54300000000000004	0.54300000000000004	0.54400000000000004	0.54400000000000004	0.54400000000000004	0.54500000000000004	0.54600000000000004	0.54600000000000004	0.54600000000000004	0.54700000000000004	0.54800000000000004	0.54800000000000004	0.54900000000000004	0.54900000000000004	0.55000000000000004	0.55000000000000004	0.55000000000000004	0.55100000000000005	0.55100000000000005	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.5	0.5	0.5	0.5	0.5	0.5	0.5	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.496	0.496	0.498	0.5	0.504	0.50600000000000001	0.50600000000000001	0.50800000000000001	0.51400000000000001	0.51600000000000001	0.51800000000000002	0.52	0.52600000000000002	0.52800000000000002	0.53400000000000003	0.53800000000000003	0.54	0.54600000000000004	0.55000000000000004	0.55600000000000005	0.56000000000000005	0.56599999999999995	0.57399999999999995	0.57799999999999996	0.58399999999999996	0.59	0.59599999999999997	0.60399999999999998	0.61	0.61599999999999999	0.624	0.63	0.63800000000000001	0.64800000000000002	0.65600000000000003	0.66400000000000003	0.67	0.68	0.68799999999999994	0.69799999999999995	0.70599999999999996	0.71599999999999997	0.72599999999999998	0.73599999999999999	0.746	0.75600000000000001	0.76600000000000001	0.77800000000000002	0.78800000000000003	0.79800000000000004	0.81	0.82399999999999995	0.83399999999999996	0.84599999999999997	0.85599999999999998	0.86799999999999999	0.88	0.89400000000000002	0.90600000000000003	0.92	0.93200000000000005	0.94599999999999995	0.96	0.97199999999999998	0.98799999999999999	1.002	1.016	1.03	1.046	1.0580000000000001	1.0680000000000001	1.0820000000000001	1.0980000000000001	1.1120000000000001	1.1299999999999999	1.1459999999999999	1.1619999999999999	1.18	1.196	1.212	1.23	1.248	1.266	1.282	1.302	1.32	1.3380000000000001	1.3580000000000001	1.3759999999999999	1.3959999999999999	1.4159999999999999	1.4319999999999999	1.452	1.472	1.492	1.516	1.532	1.556	1.5720000000000001	1.5960000000000001	1.6160000000000001	1.6359999999999999	1.6559999999999999	1.6759999999999999	1.696	1.716	1.736	1.756	1.776	1.798	1.8180000000000001	1.8380000000000001	1.8580000000000001	1.8779999999999999	1.8979999999999999	1.9179999999999999	1.9379999999999999	1.958	1.978	2	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	1.276	1.276	1.276	1.276	1.276	1.276	1.276	1.276	1.276	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.913	1.913	1.913	1.913	1.913	2.2320000000000002	2.2320000000000002	2.2320000000000002	2.2320000000000002	2.2320000000000002	2.5510000000000002	2.5510000000000002	2.5510000000000002	2.5510000000000002	2.5510000000000002	2.87	2.87	2.87	2.87	3.1890000000000001	3.1890000000000001	3.1890000000000001	3.508	3.508	3.508	3.508	3.827	3.827	3.827	4.1449999999999996	4.1449999999999996	4.1449999999999996	4.4640000000000004	4.4640000000000004	4.4640000000000004	4.7830000000000004	4.7830000000000004	4.7830000000000004	5.1020000000000003	5.1020000000000003	5.1020000000000003	5.4210000000000003	5.4210000000000003	5.4210000000000003	5.74	5.74	6.0590000000000002	6.0590000000000002	6.0590000000000002	6.3780000000000001	6.3780000000000001	6.3780000000000001	6.6959999999999997	6.6959999999999997	6.6959999999999997	7.0149999999999997	7.0149999999999997	7.0149999999999997	7.0149999999999997	7.3339999999999996	7.3339999999999996	7.3339999999999996	7.3339999999999996	7.6529999999999996	7.6529999999999996	7.6529999999999996	7.6529999999999996	7.9720000000000004	7.9720000000000004	7.9720000000000004	7.9720000000000004	7.9720000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.8849999999999998	9.8849999999999998	9.8849999999999998	9.8849999999999998	10.204000000000001	10.204000000000001	10.204000000000001	10.523	10.523	10.842000000000001	10.842000000000001	11.161	11.161	11.48	11.798	12.117000000000001	12.117000000000001	12.436	12.755000000000001	13.393000000000001	13.712	14.349	14.987	15.944000000000001	16.582000000000001	17.219000000000001	18.175999999999998	19.132999999999999	20.408000000000001	21.684000000000001	22.959	23.916	25.190999999999999	26.786000000000001	28.38	29.655999999999999	30.611999999999998	31.888000000000002	33.481999999999999	35.076999999999998	36.033000000000001	37.628	38.584000000000003	40.179000000000002	41.454000000000001	43.048000000000002	44.323999999999998	45.917999999999999	47.194000000000003	48.151000000000003	50.064	51.02	51.976999999999997	53.570999999999998	54.527999999999999	55.804000000000002	56.76	58.036000000000001	59.311	60.268000000000001	61.223999999999997	62.819000000000003	63.776000000000003	64.731999999999999	65.688999999999993	66.644999999999996	68.239999999999995	69.195999999999998	70.153000000000006	71.11	72.385000000000005	73.341999999999999	74.617000000000004	75.893000000000001	76.849000000000004	77.805999999999997	78.763000000000005	79.718999999999994	80.676000000000002	82.27	83.227000000000004	84.183999999999997	85.14	86.096999999999994	87.054000000000002	88.01	89.286000000000001	90.242000000000004	91.518000000000001	92.474000000000004	93.430999999999997	94.388000000000005	95.343999999999994	96.62	97.576999999999998	98.533000000000001	99.49	100.446	101.40300000000001	102.36	103.316	104.273	105.23	106.505	107.462	108.41800000000001	109.375	110.33199999999999	111.288	111.926	112.883	113.839	114.477	115.434	116.071	117.02800000000001	117.666	118.622	119.26	119.898	120.536	121.492	122.13	122.768	123.40600000000001	124.04300000000001	124.681	125.319	125.95699999999999	126.276	126.913	127.551	128.18899999999999	128.50800000000001	129.14500000000001	129.464	130.102	130.42099999999999	131.059	131.37799999999999	131.696	132.334	132.65299999999999	132.97200000000001	133.291	133.61000000000001	133.929	134.24700000000001	134.566	134.88499999999999	135.20400000000001	135.523	135.523	135.84200000000001	136.161	136.161	136.47999999999999	136.798	136.798	137.11699999999999	137.11699999999999	137.43600000000001	137.755	137.755	138.07400000000001	138.07400000000001	138.393	138.71199999999999	138.71199999999999	139.03100000000001	139.34899999999999	139.34899999999999	139.66800000000001	139.98699999999999	139.98699999999999	140.30600000000001	140.625	140.625	140.94399999999999	141.26300000000001	141.58199999999999	141.58199999999999	141.9	141.9	142.21899999999999	142.53800000000001	142.857	142.857	143.17599999999999	143.17599999999999	143.495	143.81399999999999	143.81399999999999	144.13300000000001	144.452	144.452	144.77000000000001	145.089	145.089	145.40799999999999	145.727	145.727	146.04599999999999	146.36500000000001	146.36500000000001	146.684	147.00299999999999	147.00299999999999	147.321	147.63999999999999	147.63999999999999	147.959	148.27799999999999	148.27799999999999	148.59700000000001	148.59700000000001	148.916	149.23500000000001	149.554	149.87200000000001	149.87200000000001	150.191	150.191	150.51	150.82900000000001	150.82900000000001	151.148	151.46700000000001	151.786	151.786	152.10499999999999	152.423	152.423	152.74199999999999	153.06100000000001	153.06100000000001	153.38	153.69900000000001	154.018	154.018	154.33699999999999	154.65600000000001	154.65600000000001	154.97399999999999	155.29300000000001	155.29300000000001	155.61199999999999	155.93100000000001	156.25	156.25	156.56899999999999	156.88800000000001	156.88800000000001	157.20699999999999	157.52600000000001	157.52600000000001	157.84399999999999	158.16300000000001	158.482	158.482	158.80099999999999	159.12	159.12	159.43899999999999	159.75800000000001	159.75800000000001	160.077	160.39500000000001	160.714	160.714	161.03299999999999	161.352	161.352	161.67099999999999	161.99	161.99	162.309	162.62799999999999	162.946	163.26499999999999	163.26499999999999	163.584	163.90299999999999	163.90299999999999	164.22200000000001	164.541	164.541	164.86	165.179	165.49700000000001	165.49700000000001	165.816	166.13499999999999	166.45400000000001	166.45400000000001	166.773	167.09200000000001	167.411	167.73	168.048	168.048	168.36699999999999	168.68600000000001	169.005	169.32400000000001	169.32400000000001	169.643	169.96199999999999	170.28100000000001	170.59899999999999	170.59899999999999	170.91800000000001	171.23699999999999	171.55600000000001	171.875	171.875	172.19399999999999	172.51300000000001	172.83199999999999	173.15	173.15	173.46899999999999	173.78800000000001	174.107	174.42599999999999	174.42599999999999	174.745	175.06399999999999	175.38300000000001	175.702	175.702	176.02	176.339	176.65799999999999	176.65799999999999	176.977	177.29599999999999	177.61500000000001	177.934	177.934	178.25299999999999	178.571	178.89	179.209	179.209	179.52799999999999	179.84700000000001	180.166	180.48500000000001	180.48500000000001	180.804	181.12200000000001	181.441	181.76	181.76	182.07900000000001	182.398	182.71700000000001	183.036	183.036	183.35499999999999	183.673	183.99199999999999	184.31100000000001	184.31100000000001	184.63	184.94900000000001	185.268	185.58699999999999	185.90600000000001	186.22399999999999	186.22399999999999	186.54300000000001	186.86199999999999	187.18100000000001	187.5	187.5	187.81899999999999	188.13800000000001	188.45699999999999	188.45699999999999	188.77600000000001	189.09399999999999	189.41300000000001	189.732	189.732	190.05099999999999	190.37	190.68899999999999	191.00800000000001	191.00800000000001	191.327	191.64500000000001	191.964	192.28299999999999	192.28299999999999	192.602	192.92099999999999	193.24	193.559	193.559	193.87799999999999	194.196	194.51499999999999	194.834	195.15299999999999	195.15299999999999	195.47200000000001	195.791	196.11	196.429	196.74700000000001	197.066	197.066	197.38499999999999	197.70400000000001	198.023	198.34200000000001	198.34200000000001	198.661	198.98	199.298	199.61699999999999	199.93600000000001	199.93600000000001	200.255	200.57400000000001	200.893	201.21199999999999	201.21199999999999	201.53100000000001	201.84899999999999	202.16800000000001	202.48699999999999	202.48699999999999	202.80600000000001	203.125	203.44399999999999	203.76300000000001	203.76300000000001	204.08199999999999	204.4	204.71899999999999	205.03800000000001	205.03800000000001	205.357	205.67599999999999	205.995	206.31399999999999	206.31399999999999	206.63300000000001	206.952	207.27	207.589	207.589	207.90799999999999	208.227	208.54599999999999	208.86500000000001	209.184	209.184	209.50299999999999	209.821	210.14	210.459	210.77799999999999	210.77799999999999	211.09700000000001	211.416	211.73500000000001	212.054	212.37200000000001	212.37200000000001	212.691	213.01	213.32900000000001	213.648	213.96700000000001	214.286	214.286	214.60499999999999	214.923	215.24199999999999	215.56100000000001	215.88	215.88	216.19900000000001	216.518	216.83699999999999	217.15600000000001	217.47399999999999	217.79300000000001	217.79300000000001	218.11199999999999	218.43100000000001	218.75	219.06899999999999	219.38800000000001	219.70699999999999	219.70699999999999	220.02600000000001	220.66300000000001	220.66300000000001	220.982	221.30099999999999	221.62	221.93899999999999	222.25800000000001	222.577	222.89500000000001	222.89500000000001	223.214	223.53299999999999	223.852	224.17099999999999	224.49	224.809	224.809	225.12799999999999	225.446	225.76499999999999	226.084	226.40299999999999	226.72200000000001	227.041	227.041	227.36	227.679	227.99700000000001	228.316	228.63499999999999	228.95400000000001	228.95400000000001	229.273	229.59200000000001	229.911	230.23	230.548	230.86699999999999	230.86699999999999	231.18600000000001	231.505	231.82400000000001	232.143	232.46199999999999	232.78100000000001	232.78100000000001	233.09899999999999	233.41800000000001	233.73699999999999	234.05600000000001	234.375	234.69399999999999	235.01300000000001	235.33199999999999	235.33199999999999	235.65	235.96899999999999	236.28800000000001	236.607	236.607	237.245	237.56399999999999	237.56399999999999	237.88300000000001	238.202	238.52	238.839	239.15799999999999	239.477	239.477	239.79599999999999	240.11500000000001	240.434	240.75299999999999	241.071	241.39	241.39	241.709	242.02799999999999	242.34700000000001	242.666	242.98500000000001	242.98500000000001	243.304	243.62200000000001	243.941	244.26	244.57900000000001	244.57900000000001	244.898	245.21700000000001	245.536	245.85499999999999	246.173	246.173	246.49199999999999	246.81100000000001	247.13	247.44900000000001	247.768	248.08699999999999	248.08699999999999	248.40600000000001	248.72399999999999	249.04300000000001	249.04300000000001	249.36199999999999	249.68100000000001	250	250.31899999999999	250.63800000000001	250.63800000000001	250.95699999999999	251.27600000000001	251.59399999999999	251.91300000000001	252.232	252.232	252.55099999999999	252.87	253.18899999999999	253.50800000000001	253.827	253.827	254.14500000000001	254.464	254.78299999999999	255.102	255.42099999999999	255.42099999999999	255.74	256.05900000000003	256.37799999999999	256.69600000000003	257.01499999999999	257.01499999999999	257.334	257.65300000000002	257.97199999999998	258.291	258.61	258.61	258.92899999999997	259.24700000000001	259.56599999999997	259.88499999999999	260.20400000000001	260.20400000000001	260.52300000000002	260.84199999999998	261.161	261.48	261.798	261.798	262.11700000000002	262.43599999999998	262.755	263.07400000000001	263.39299999999997	263.39299999999997	263.71199999999999	264.03100000000001	264.34899999999999	264.66800000000001	264.98700000000002	264.98700000000002	265.30599999999998	265.625	265.94400000000002	266.26299999999998	266.58199999999999	266.58199999999999	266.90100000000001	267.21899999999999	267.53800000000001	267.85700000000003	268.17599999999999	268.17599999999999	268.495	268.81400000000002	269.13299999999998	269.452	269.77	269.77	270.089	270.40800000000002	270.72699999999998	271.04599999999999	271.36500000000001	271.36500000000001	271.68400000000003	272.00299999999999	272.32100000000003	272.64	272.959	272.959	273.27800000000002	273.59699999999998	273.916	274.23500000000001	274.55399999999997	274.55399999999997	274.87200000000001	275.19099999999997	275.51	275.82900000000001	276.14800000000002	276.14800000000002	276.46699999999998	276.786	277.10500000000002	277.423	277.74200000000002	277.74200000000002	278.06099999999998	278.38	278.69900000000001	279.01799999999997	279.33699999999999	279.65600000000001	279.65600000000001	279.97399999999999	280.29300000000001	280.61200000000002	280.93099999999998	281.25	281.25	281.56900000000002	281.88799999999998	282.20699999999999	282.52499999999998	282.84399999999999	282.84399999999999	283.16300000000001	283.48200000000003	283.80099999999999	284.12	284.43900000000002	284.75799999999998	284.75799999999998	285.077	285.39499999999998	285.714	286.03300000000002	286.35199999999998	286.35199999999998	286.67099999999999	286.99	287.30900000000003	287.62799999999999	287.94600000000003	287.94600000000003	288.26499999999999	288.584	288.90300000000002	289.22199999999998	289.22199999999998	289.541	289.86	290.17899999999997	290.49700000000001	290.81599999999997	290.81599999999997	291.13499999999999	291.45400000000001	291.77300000000002	292.09199999999998	292.09199999999998	292.411	292.73	293.048	293.36700000000002	293.68599999999998	293.68599999999998	294.005	294.32400000000001	294.64299999999997	294.96199999999999	295.28100000000001	295.28100000000001	295.59899999999999	295.91800000000001	296.23700000000002	296.55599999999998	296.875	297.19400000000002	297.19400000000002	297.51299999999998	297.83199999999999	298.15100000000001	298.46899999999999	298.78800000000001	299.10700000000003	299.42599999999999	299.42599999999999	299.745	300.06400000000002	300.38299999999998	300.702	301.02	301.339	301.65800000000002	301.97699999999998	301.97699999999998	302.29599999999999	302.61500000000001	302.93400000000003	303.25299999999999	303.57100000000003	303.89	304.209	304.52800000000002	304.52800000000002	304.84699999999998	305.166	305.48500000000001	305.80399999999997	306.12200000000001	306.44099999999997	306.76	307.07900000000001	307.07900000000001	307.39800000000002	307.71699999999998	308.036	308.35500000000002	308.673	308.99200000000002	309.31099999999998	309.31099999999998	309.63	309.94900000000001	310.26799999999997	310.58699999999999	310.90600000000001	310.90600000000001	311.22399999999999	311.54300000000001	311.86200000000002	311.86200000000002	311.86200000000002	311.86200000000002	312.18099999999998	312.18099999999998	312.18099999999998	312.18099999999998	312.18099999999998	312.18099999999998	311.86200000000002	311.86200000000002	311.86200000000002	311.54300000000001	311.54300000000001	311.22399999999999	311.22399999999999	310.90600000000001	310.58699999999999	310.58699999999999	310.26799999999997	309.94900000000001	309.63	309.31099999999998	308.99200000000002	308.673	308.673	308.35500000000002	308.036	307.71699999999998	307.39800000000002	307.39800000000002	307.07900000000001	306.76	306.44099999999997	306.44099999999997	306.12200000000001	305.80399999999997	305.80399999999997	305.48500000000001	305.48500000000001	305.166	304.84699999999998	304.84699999999998	304.52800000000002	304.52800000000002	304.209	304.209	303.89	303.89	303.89	303.57100000000003	303.57100000000003	303.25299999999999	303.25299999999999	303.25299999999999	302.93400000000003	302.93400000000003	302.61500000000001	302.61500000000001	302.61500000000001	302.29599999999999	302.29599999999999	302.29599999999999	302.29599999999999	301.97699999999998	301.97699999999998	301.97699999999998	301.65800000000002	301.65800000000002	301.65800000000002	301.65800000000002	301.339	301.339	301.339	301.339	301.02	301.02	301.02	301.02	300.702	300.702	300.702	300.38299999999998	300.38299999999998	300.38299999999998	300.38299999999998	300.06400000000002	300.06400000000002	300.06400000000002	300.06400000000002	299.745	299.745	299.745	299.42599999999999	299.42599999999999	299.42599999999999	299.42599999999999	299.10700000000003	299.10700000000003	299.10700000000003	299.10700000000003	299.10700000000003	298.78800000000001	298.78800000000001	298.78800000000001	298.78800000000001	298.78800000000001	298.46899999999999	298.46899999999999	298.46899999999999	298.46899999999999	298.46899999999999	298.15100000000001	298.15100000000001	298.15100000000001	298.15100000000001	298.15100000000001	297.83199999999999	297.83199999999999	297.83199999999999	297.83199999999999	297.83199999999999	297.83199999999999	297.51299999999998	297.51299999999998	297.51299999999998	297.51299999999998	297.51299999999998	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	296.875	296.875	296.875	296.875	296.875	296.875	296.55599999999998	296.55599999999998	296.55599999999998	296.55599999999998	296.55599999999998	296.55599999999998	296.23700000000002	296.23700000000002	296.23700000000002	296.23700000000002	296.23700000000002	296.23700000000002	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.005	294.005	294.005	294.005	294.005	294.005	294.005	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.048	293.048	293.048	293.048	293.048	293.048	293.048	293.048	292.73	292.73	292.73	292.73	292.73	292.73	292.73	292.73	292.73	292.411	292.411	292.411	292.411	292.411	292.411	292.411	292.411	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.84399999999999	282.84399999999999	282.84399999999999	283.16300000000001	283.16300000000001	283.48200000000003	283.48200000000003	283.80099999999999	284.12	284.43900000000002	284.43900000000002	284.75799999999998	285.077	285.39499999999998	285.714	286.35199999999998	286.99	287.62799999999999	288.26499999999999	289.22199999999998	290.17899999999997	291.45400000000001	292.411	293.68599999999998	294.64299999999997	295.59899999999999	296.875	298.15100000000001	299.10700000000003	301.02	302.29599999999999	303.57100000000003	304.52800000000002	306.12200000000001	307.39800000000002	308.99200000000002	310.26799999999997	311.54300000000001	313.13799999999998	314.09399999999999	316.00799999999998	317.60199999999998	318.87799999999999	320.15300000000002	322.06599999999997	323.34199999999998	325.255	326.53100000000001	328.125	330.03800000000001	331.31400000000002	333.22699999999998	334.82100000000003	336.09699999999998	337.37200000000001	339.60500000000002	340.88	342.47399999999999	343.75	345.02499999999998	346.93900000000002	348.53300000000002	349.80900000000003	351.084	353.31599999999997	354.59199999999998	356.18599999999998	357.78100000000001	359.05599999999998	360.65100000000001	362.88299999999998	364.47699999999998	366.07100000000003	367.666	368.94099999999997	370.536	372.13	374.36200000000002	375.63799999999998	377.23200000000003	378.827	380.10199999999998	381.69600000000003	382.97199999999998	384.56599999999997	385.84199999999998	388.07400000000001	389.34899999999999	390.625	391.90100000000001	393.17599999999999	394.452	395.72699999999998	397.00299999999999	398.27800000000002	399.55399999999997	400.51	401.786	402.74200000000002	404.01799999999997	404.97399999999999	405.93099999999998	406.88799999999998	407.84399999999999	408.80099999999999	409.75799999999998	410.714	Percentage Strain (%)


Stress (MPa)




Woven Fibre Comparison - Carbon vs Flax vs Kevlar
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Stress (MPa)




Weave Comparison - Carbon Woven vs Non Woven Bioresin
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Resin Comparison - Carbon Twill Epoxy vs Carbon Twill Bioresin

Carbon Twill Epoxy	0	0	0	0	0	0	0	0	0	0	0	0	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	0	-1E-3	-1E-3	-1E-3	-1E-3	0	0	0	0	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.7000000000000001E-2	1.7999999999999999E-2	1.7999999999999999E-2	1.9E-2	0.02	0.02	2.1999999999999999E-2	2.1999999999999999E-2	2.4E-2	2.4E-2	2.5000000000000001E-2	2.5999999999999999E-2	2.8000000000000001E-2	2.9000000000000001E-2	0.03	3.1E-2	3.2000000000000001E-2	3.4000000000000002E-2	3.5000000000000003E-2	3.5999999999999997E-2	3.7999999999999999E-2	0.04	4.2000000000000003E-2	4.2999999999999997E-2	4.4999999999999998E-2	4.5999999999999999E-2	4.8000000000000001E-2	0.05	5.1999999999999998E-2	5.3999999999999999E-2	5.6000000000000001E-2	5.8000000000000003E-2	0.06	6.2E-2	6.4000000000000001E-2	6.5000000000000002E-2	6.5000000000000002E-2	6.6000000000000003E-2	6.7000000000000004E-2	7.0000000000000007E-2	7.1999999999999995E-2	7.3999999999999996E-2	7.5999999999999998E-2	7.8E-2	0.08	8.2000000000000003E-2	8.4000000000000005E-2	8.5999999999999993E-2	8.7999999999999995E-2	8.8999999999999996E-2	9.0999999999999998E-2	9.2999999999999999E-2	9.2999999999999999E-2	9.7000000000000003E-2	9.9000000000000005E-2	0.1	0.10199999999999999	0.104	0.106	0.108	0.11	0.112	0.114	0.115	0.11700000000000001	0.11899999999999999	0.121	0.122	0.124	0.126	0.128	0.13	0.13100000000000001	0.13300000000000001	0.13500000000000001	0.13700000000000001	0.13800000000000001	0.14000000000000001	0.14199999999999999	0.14399999999999999	0.14599999999999999	0.14699999999999999	0.14899999999999999	0.151	0.153	0.154	0.156	0.158	0.16	0.161	0.16300000000000001	0.16500000000000001	0.16600000000000001	0.16800000000000001	0.17	0.17199999999999999	0.17299999999999999	0.17499999999999999	0.17599999999999999	0.17799999999999999	0.18	0.182	0.183	0.185	0.186	0.188	0.19	0.191	0.193	0.19400000000000001	0.19600000000000001	0.19700000000000001	0.19800000000000001	0.2	0.20100000000000001	0.20200000000000001	0.20399999999999999	0.20499999999999999	0.20599999999999999	0.20799999999999999	0.20899999999999999	0.21	0.21099999999999999	0.21199999999999999	0.21299999999999999	0.214	0.215	0.216	0.217	0.218	0.219	0.22	0.22	0.221	0.222	0.223	0.224	0.224	0.22500000000000001	0.22600000000000001	0.22600000000000001	0.22700000000000001	0.22700000000000001	0.22800000000000001	0.22800000000000001	0.22900000000000001	0.22900000000000001	0.23	0.23	0.23100000000000001	0.23100000000000001	0.23200000000000001	0.23200000000000001	0.23200000000000001	0.23200000000000001	0.23300000000000001	0.23300000000000001	0.23400000000000001	0.23400000000000001	0.23400000000000001	0.23400000000000001	0.23499999999999999	0.23499999999999999	0.23499999999999999	0.23599999999999999	0.23599999999999999	0.23599999999999999	0.23699999999999999	0.23699999999999999	0.23699999999999999	0.23799999999999999	0.23799999999999999	0.23799999999999999	0.23899999999999999	0.23899999999999999	0.24	0.24	0.24	0.24	0.24099999999999999	0.24099999999999999	0.24199999999999999	0.24199999999999999	0.24199999999999999	0.24299999999999999	0.24299999999999999	0.24299999999999999	0.24399999999999999	0.24399999999999999	0.24399999999999999	0.245	0.245	0.246	0.246	0.246	0.247	0.247	0.248	0.248	0.248	0.249	0.249	0.25	0.25	0.25	0.25	0.251	0.251	0.252	0.252	0.252	0.253	0.253	0.254	0.254	0.254	0.255	0.255	0.25600000000000001	0.25600000000000001	0.25600000000000001	0.25700000000000001	0.25700000000000001	0.25800000000000001	0.25800000000000001	0.25800000000000001	0.25900000000000001	0.26	0.26	0.26	0.26100000000000001	0.26100000000000001	0.26200000000000001	0.26200000000000001	0.26200000000000001	0.26300000000000001	0.26300000000000001	0.26400000000000001	0.26400000000000001	0.26400000000000001	0.26500000000000001	0.26500000000000001	0.26600000000000001	0.26600000000000001	0.26700000000000002	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26800000000000002	0.26900000000000002	0.26900000000000002	0.27	0.27	0.27	0.27100000000000002	0.27100000000000002	0.27200000000000002	0.27200000000000002	0.27300000000000002	0.27300000000000002	0.27400000000000002	0.27400000000000002	0.27400000000000002	0.27500000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27800000000000002	0.27800000000000002	0.27900000000000003	0.27900000000000003	0.28000000000000003	0.28000000000000003	0.28000000000000003	0.28100000000000003	0.28100000000000003	0.28199999999999997	0.28199999999999997	0.28199999999999997	0.28299999999999997	0.28399999999999997	0.28399999999999997	0.28399999999999997	0.28499999999999998	0.28499999999999998	0.28599999999999998	0.28599999999999998	0.28599999999999998	0.28699999999999998	0.28699999999999998	0.28799999999999998	0.28799999999999998	0.28899999999999998	0.28899999999999998	0.28999999999999998	0.28999999999999998	0.28999999999999998	0.29099999999999998	0.29099999999999998	0.29199999999999998	0.29199999999999998	0.29199999999999998	0.29299999999999998	0.29399999999999998	0.29399999999999998	0.29399999999999998	0.29499999999999998	0.29499999999999998	0.29599999999999999	0.29599999999999999	0.29599999999999999	0.29699999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.29899999999999999	0.3	0.3	0.30099999999999999	0.30099999999999999	0.30199999999999999	0.30199999999999999	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30499999999999999	0.30499999999999999	0.30599999999999999	0.30599999999999999	0.30599999999999999	0.307	0.307	0.308	0.308	0.309	0.309	0.31	0.31	0.311	0.311	0.312	0.312	0.312	0.313	0.314	0.314	0.314	0.315	0.315	0.316	0.316	0.317	0.317	0.318	0.318	0.31900000000000001	0.31900000000000001	0.32	0.32	0.32	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32400000000000001	0.32500000000000001	0.32500000000000001	0.32600000000000001	0.32600000000000001	0.32700000000000001	0.32700000000000001	0.32800000000000001	0.32800000000000001	0.32900000000000001	0.32900000000000001	0.33	0.33	0.33	0.33100000000000002	0.33200000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33400000000000002	0.33400000000000002	0.33400000000000002	0.33500000000000002	0.33600000000000002	0.33600000000000002	0.33600000000000002	0.33700000000000002	0.33700000000000002	0.33800000000000002	0.33800000000000002	0.33900000000000002	0.33900000000000002	0.34	0.34	0.34	0.34100000000000003	0.34200000000000003	0.34200000000000003	0.34300000000000003	0.34300000000000003	0.34399999999999997	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34799999999999998	0.34799999999999998	0.34799999999999998	0.34899999999999998	0.35	0.35	0.35	0.35099999999999998	0.35099999999999998	0.35199999999999998	0.35199999999999998	0.35299999999999998	0.35299999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35499999999999998	0.35599999999999998	0.35599999999999998	0.35699999999999998	0.35699999999999998	0.35799999999999998	0.35799999999999998	0.35799999999999998	0.35899999999999999	0.36	0.36	0.36	0.36099999999999999	0.36099999999999999	0.36199999999999999	0.36199999999999999	0.36299999999999999	0.36299999999999999	0.36399999999999999	0.36399999999999999	0.36499999999999999	0.36499999999999999	0.36599999999999999	0.36599999999999999	0.36699999999999999	0.36699999999999999	0.36799999999999999	0.36799999999999999	0.36899999999999999	0.36899999999999999	0.37	0.37	0.37	0.371	0.372	0.372	0.372	0.373	0.374	0.374	0.374	0.375	0.376	0.376	0.376	0.377	0.377	0.378	0.378	0.379	0.379	0.38	0.38	0.38	0.38100000000000001	0.38200000000000001	0.38200000000000001	0.38200000000000001	0.38300000000000001	0.38400000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38500000000000001	0.38600000000000001	0.38600000000000001	0.38700000000000001	0.38700000000000001	0.38800000000000001	0.38800000000000001	0.38900000000000001	0.38900000000000001	0.39	0.39	0.39100000000000001	0.39100000000000001	0.39200000000000002	0.39200000000000002	0.39300000000000002	0.39300000000000002	0.39400000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39600000000000002	0.39600000000000002	0.39600000000000002	0.39700000000000002	0.39800000000000002	0.39800000000000002	0.39800000000000002	0.39900000000000002	0.4	0.4	0.4	0.40100000000000002	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40300000000000002	0.40400000000000003	0.40400000000000003	0.40400000000000003	0.40500000000000003	0.40600000000000003	0.40600000000000003	0.40600000000000003	0.40699999999999997	0.40699999999999997	0.40799999999999997	0.40799999999999997	0.40899999999999997	0.40899999999999997	0.41	0.41	0.41099999999999998	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41199999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41399999999999998	0.41499999999999998	0.41599999999999998	0.41599999999999998	0.41599999999999998	0.41699999999999998	0.41699999999999998	0.41799999999999998	0.41799999999999998	0.41899999999999998	0.41899999999999998	0.42	0.42	0.42	0.42099999999999999	0.42199999999999999	0.42199999999999999	0.42199999999999999	0.42299999999999999	0.42299999999999999	0.42399999999999999	0.42399999999999999	0.42499999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42799999999999999	0.42799999999999999	0.42799999999999999	0.42899999999999999	0.43	0.43	0.43	0.43099999999999999	0.43099999999999999	0.432	0.432	0.432	0.433	0.434	0.434	0.434	0.435	0.435	0.436	0.436	0.437	0.437	0.438	0.438	0.439	0.439	0.44	0.44	0.44	0.441	0.441	0.442	0.442	0.443	0.443	0.44400000000000001	0.44400000000000001	0.44500000000000001	0.44500000000000001	0.44600000000000001	0.44600000000000001	0.44600000000000001	0.44700000000000001	0.44800000000000001	0.44800000000000001	0.44800000000000001	0.44900000000000001	0.44900000000000001	0.45	0.45	0.45100000000000001	0.45100000000000001	0.45200000000000001	0.45200000000000001	0.45200000000000001	0.45300000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45800000000000002	0.45800000000000002	0.45800000000000002	0.45900000000000002	0.45900000000000002	0.46	0.46	0.46100000000000002	0.46100000000000002	0.46200000000000002	0.46200000000000002	0.46200000000000002	0.46300000000000002	0.46400000000000002	0.46400000000000002	0.46400000000000002	0.46500000000000002	0.46500000000000002	0.46600000000000003	0.46600000000000003	0.46600000000000003	0.46700000000000003	0.46800000000000003	0.46800000000000003	0.46800000000000003	0.46899999999999997	0.46899999999999997	0.47	0.47	0.47	0.47099999999999997	0.47099999999999997	0.47199999999999998	0.47199999999999998	0.47299999999999998	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47399999999999998	0.47499999999999998	0.47599999999999998	0.47599999999999998	0.47599999999999998	0.47699999999999998	0.47699999999999998	0.47799999999999998	0.47799999999999998	0.47799999999999998	0.47899999999999998	0.47899999999999998	0.48	0.48	0.48099999999999998	0.48099999999999998	0.48199999999999998	0.48199999999999998	0.48199999999999998	0.48299999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48499999999999999	0.48499999999999999	0.48599999999999999	0.48599999999999999	0.48599999999999999	0.48699999999999999	0.48699999999999999	0.48799999999999999	0.48799999999999999	0.48899999999999999	0.48899999999999999	0.49	0.49	0.49	0.49099999999999999	0.49099999999999999	0.49199999999999999	0.49199999999999999	0.49299999999999999	0.49299999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.495	0.495	0.496	0.496	0.496	0.497	0.498	0.498	0.498	0.499	0.499	0.5	0.5	0.5	0.501	0.501	0.502	0.502	0.503	0.503	0.504	0.504	0.504	0.505	0.505	0.50600000000000001	0.50600000000000001	0.50700000000000001	0.50700000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50900000000000001	0.50900000000000001	0.51	0.51	0.51	0.51100000000000001	0.51200000000000001	0.51200000000000001	0.51200000000000001	0.51300000000000001	0.51300000000000001	0.51400000000000001	0.51400000000000001	0.51400000000000001	0.51500000000000001	0.51600000000000001	0.51600000000000001	0.51600000000000001	0.51700000000000002	0.51700000000000002	0.51800000000000002	0.51800000000000002	0.51800000000000002	0.51900000000000002	0.52	0.52	0.52	0.52100000000000002	0.52100000000000002	0.52200000000000002	0.52200000000000002	0.52300000000000002	0.52300000000000002	0.52400000000000002	0.52400000000000002	0.52400000000000002	0.52500000000000002	0.52500000000000002	0.52600000000000002	0.52600000000000002	0.52700000000000002	0.52700000000000002	0.52800000000000002	0.52800000000000002	0.52800000000000002	0.52900000000000003	0.52900000000000003	0.53	0.53	0.53	0.53100000000000003	0.53200000000000003	0.53200000000000003	0.53200000000000003	0.53300000000000003	0.53300000000000003	0.53400000000000003	0.53400000000000003	0.53500000000000003	0.53500000000000003	0.53600000000000003	0.53600000000000003	0.53600000000000003	0.53700000000000003	0.53700000000000003	0.53800000000000003	0.53800000000000003	0.53900000000000003	0.53900000000000003	0.54	0.54	0.54	0.54100000000000004	0.54100000000000004	0.54200000000000004	0.54200000000000004	0.54300000000000004	0.54300000000000004	0.54400000000000004	0.54400000000000004	0.54400000000000004	0.54500000000000004	0.54500000000000004	0.54600000000000004	0.48799999999999999	0.49199999999999999	0.5	0.502	0.502	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.502	0.502	0.502	0.502	0.502	0.502	0.502	0.502	0.502	0.5	0.5	0.5	0.5	0.5	0.5	0.5	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49199999999999999	0.49399999999999999	0.49399999999999999	0.498	0.5	0.5	0.502	0.504	0.50800000000000001	0.51	0.51200000000000001	0.51800000000000002	0.52	0.52200000000000002	0.52800000000000002	0.53200000000000003	0.53400000000000003	0.54	0.54400000000000004	0.55000000000000004	0.55400000000000005	0.56000000000000005	0.56399999999999995	0.57199999999999995	0.57799999999999996	0.58199999999999996	0.59	0.59399999999999997	0.60199999999999998	0.61	0.61399999999999999	0.622	0.63	0.63800000000000001	0.64400000000000002	0.65400000000000003	0.66200000000000003	0.67	0.68	0.68799999999999994	0.69799999999999995	0.70799999999999996	0.71399999999999997	0.72399999999999998	0.73399999999999999	0.74399999999999999	0.754	0.76800000000000002	0.77800000000000002	0.78800000000000003	0.8	0.81	0.82199999999999995	0.83199999999999996	0.84399999999999997	0.85799999999999998	0.87	0.88200000000000001	0.89400000000000002	0.90800000000000003	0.92	0.93200000000000005	0.94799999999999995	0.96	0.97399999999999998	0.99	1.002	1.018	1.032	1.048	1.0620000000000001	1.0780000000000001	1.0920000000000001	1.1080000000000001	1.1180000000000001	1.1299999999999999	1.1479999999999999	1.1619999999999999	1.18	1.198	1.214	1.23	1.248	1.264	1.284	1.302	1.32	1.3380000000000001	1.3580000000000001	1.3779999999999999	1.3939999999999999	1.4139999999999999	1.4319999999999999	1.452	1.472	1.492	1.512	1.532	1.552	1.5740000000000001	1.5920000000000001	1.6140000000000001	1.6339999999999999	1.6539999999999999	1.6739999999999999	1.694	1.714	1.734	1.756	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.68400000000000005	0.68400000000000005	0.68400000000000005	0.68400000000000005	0.68400000000000005	0.68400000000000005	0.68400000000000005	0.68400000000000005	0.68400000000000005	1.026	1.026	1.026	1.026	1.026	1.026	1.026	1.3680000000000001	1.3680000000000001	1.3680000000000001	1.3680000000000001	1.3680000000000001	1.71	1.71	1.71	1.71	1.71	2.052	2.052	2.052	2.052	2.052	2.3940000000000001	2.3940000000000001	2.3940000000000001	2.3940000000000001	2.3940000000000001	2.7360000000000002	2.7360000000000002	2.7360000000000002	2.7360000000000002	3.0779999999999998	3.0779999999999998	3.0779999999999998	3.0779999999999998	3.0779999999999998	3.42	3.42	3.42	3.42	3.762	3.762	3.762	3.762	3.762	4.1040000000000001	4.1040000000000001	4.1040000000000001	4.1040000000000001	4.4459999999999997	4.4459999999999997	4.4459999999999997	4.4459999999999997	4.4459999999999997	4.7880000000000003	4.7880000000000003	4.7880000000000003	4.7880000000000003	5.13	5.13	5.13	5.13	5.13	5.4720000000000004	5.4720000000000004	5.4720000000000004	5.4720000000000004	5.4720000000000004	5.8140000000000001	5.8140000000000001	5.8140000000000001	5.8140000000000001	5.8140000000000001	5.8140000000000001	6.1559999999999997	6.1559999999999997	6.1559999999999997	6.1559999999999997	6.1559999999999997	6.1559999999999997	6.1559999999999997	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.4980000000000002	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	6.84	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.1820000000000004	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.524	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	7.8659999999999997	8.2080000000000002	8.2080000000000002	8.2080000000000002	8.2080000000000002	8.2080000000000002	8.2080000000000002	8.2080000000000002	8.2080000000000002	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.5500000000000007	8.8919999999999995	8.8919999999999995	8.8919999999999995	8.8919999999999995	8.8919999999999995	8.8919999999999995	9.234	9.234	9.234	9.234	9.5760000000000005	9.5760000000000005	9.5760000000000005	9.5760000000000005	9.9179999999999993	9.9179999999999993	9.9179999999999993	10.26	10.26	10.26	10.602	10.602	10.944000000000001	10.944000000000001	11.286	11.286	11.628	11.628	11.97	12.311999999999999	12.311999999999999	12.654	12.996	13.337999999999999	13.337999999999999	14.022	14.364000000000001	15.048	15.39	16.074000000000002	17.100000000000001	17.783999999999999	18.468	19.152000000000001	20.178000000000001	21.204000000000001	22.23	22.914000000000001	23.94	24.966000000000001	26.334	27.36	28.728000000000002	29.754000000000001	30.78	31.463999999999999	32.832000000000001	33.515999999999998	34.884	35.909999999999997	37.277999999999999	38.646000000000001	39.33	40.698	41.723999999999997	43.091999999999999	44.118000000000002	45.143999999999998	46.512	47.195999999999998	48.564	49.59	50.616	51.984000000000002	53.351999999999997	54.378	55.404000000000003	56.771999999999998	57.798000000000002	58.823999999999998	59.85	60.875999999999998	62.244	63.268999999999998	64.295000000000002	65.320999999999998	66.688999999999993	67.715000000000003	68.741	69.766999999999996	70.450999999999993	71.477000000000004	72.503	73.870999999999995	74.897000000000006	75.923000000000002	76.606999999999999	77.632999999999996	78.659000000000006	79.685000000000002	81.052999999999997	82.078999999999994	82.763000000000005	83.789000000000001	84.814999999999998	85.498999999999995	86.525000000000006	87.551000000000002	88.576999999999998	89.260999999999996	90.629000000000005	91.655000000000001	92.680999999999997	93.364999999999995	94.391000000000005	95.417000000000002	96.100999999999999	97.126999999999995	97.811000000000007	98.837000000000003	99.863	100.547	101.57299999999999	102.25700000000001	103.283	103.967	104.99299999999999	106.361	107.045	108.071	108.755	109.43899999999999	110.465	111.149	111.833	112.517	113.20099999999999	113.88500000000001	114.569	115.253	115.937	116.621	117.30500000000001	117.64700000000001	118.331	119.015	119.357	120.041	120.383	121.06699999999999	121.40900000000001	122.093	122.435	123.119	123.461	123.803	124.145	124.48699999999999	125.17100000000001	125.51300000000001	125.855	126.197	126.539	126.881	127.223	127.223	127.565	127.907	128.249	128.59100000000001	128.59100000000001	128.93299999999999	129.27500000000001	129.27500000000001	129.61699999999999	129.61699999999999	129.959	129.959	130.30099999999999	130.30099999999999	130.643	130.643	130.643	130.98500000000001	130.98500000000001	131.327	131.327	131.66900000000001	131.66900000000001	132.011	132.011	132.35300000000001	132.35300000000001	132.69499999999999	132.69499999999999	133.03700000000001	133.03700000000001	133.37899999999999	133.37899999999999	133.721	133.721	134.06299999999999	134.06299999999999	134.405	134.405	134.74700000000001	134.74700000000001	135.089	135.089	135.43100000000001	135.43100000000001	135.773	135.773	136.11500000000001	136.11500000000001	136.45699999999999	136.45699999999999	136.79900000000001	136.79900000000001	137.14099999999999	137.14099999999999	137.483	137.483	137.82499999999999	138.167	138.167	138.167	138.50899999999999	138.851	138.851	139.19300000000001	139.19300000000001	139.535	139.535	139.87700000000001	139.87700000000001	140.21899999999999	140.21899999999999	140.56100000000001	140.90299999999999	140.90299999999999	141.245	141.245	141.58699999999999	141.58699999999999	141.929	141.929	142.27099999999999	142.613	142.613	142.95500000000001	142.95500000000001	143.297	143.63900000000001	143.63900000000001	143.63900000000001	143.98099999999999	144.32300000000001	144.32300000000001	144.66499999999999	144.66499999999999	145.00700000000001	145.34899999999999	145.34899999999999	145.691	145.691	146.03299999999999	146.375	146.375	146.71700000000001	146.71700000000001	147.059	147.40100000000001	147.40100000000001	147.74299999999999	147.74299999999999	148.08500000000001	148.42699999999999	148.42699999999999	148.76900000000001	148.76900000000001	149.11099999999999	149.453	149.453	149.79499999999999	149.79499999999999	150.137	150.47900000000001	150.47900000000001	150.821	150.821	151.16300000000001	151.505	151.505	151.84700000000001	151.84700000000001	152.18899999999999	152.53100000000001	152.53100000000001	152.87299999999999	152.87299999999999	153.215	153.55699999999999	153.55699999999999	153.899	153.899	154.24100000000001	154.583	154.583	154.92500000000001	154.92500000000001	155.267	155.60900000000001	155.95099999999999	155.95099999999999	156.29300000000001	156.29300000000001	156.63499999999999	156.977	156.977	157.31899999999999	157.31899999999999	157.661	158.00299999999999	158.00299999999999	158.345	158.345	158.68700000000001	159.029	159.029	159.37100000000001	159.37100000000001	159.71299999999999	160.05500000000001	160.05500000000001	160.39699999999999	160.739	161.08099999999999	161.08099999999999	161.423	161.76499999999999	162.107	162.107	162.44900000000001	162.791	162.791	163.13300000000001	163.47499999999999	163.47499999999999	163.81700000000001	164.15899999999999	164.15899999999999	164.501	164.84299999999999	164.84299999999999	165.185	165.52699999999999	165.52699999999999	165.869	166.21100000000001	166.21100000000001	166.553	166.89500000000001	167.23699999999999	167.23699999999999	167.57900000000001	167.92099999999999	167.92099999999999	168.26300000000001	168.60499999999999	168.60499999999999	168.947	169.28899999999999	169.631	169.97300000000001	169.97300000000001	170.315	170.65700000000001	170.999	170.999	171.34100000000001	171.68299999999999	172.02500000000001	172.02500000000001	172.36699999999999	172.709	173.05099999999999	173.05099999999999	173.393	173.73500000000001	173.73500000000001	174.077	174.41900000000001	174.761	174.761	175.10300000000001	175.44499999999999	175.78700000000001	176.12899999999999	176.471	176.471	176.81299999999999	177.155	177.49700000000001	177.49700000000001	177.839	178.18100000000001	178.523	178.523	178.86500000000001	179.20699999999999	179.54900000000001	179.54900000000001	179.89099999999999	180.233	180.57499999999999	180.917	180.917	181.25899999999999	181.601	181.94300000000001	181.94300000000001	182.285	182.62700000000001	182.96899999999999	183.31100000000001	183.65299999999999	183.65299999999999	183.995	184.33699999999999	184.679	184.679	185.02099999999999	185.363	185.70500000000001	185.70500000000001	186.047	186.38900000000001	186.73	187.072	187.072	187.41399999999999	187.75700000000001	188.09800000000001	188.09800000000001	188.441	188.78200000000001	189.124	189.46600000000001	189.80799999999999	189.80799999999999	190.15	190.49199999999999	190.834	190.834	191.17599999999999	191.518	191.86	192.202	192.202	192.54400000000001	192.886	193.22800000000001	193.22800000000001	193.57	193.91200000000001	194.25399999999999	194.596	194.596	194.93799999999999	195.28	195.62200000000001	195.62200000000001	195.964	196.30600000000001	196.648	196.648	196.99	197.33199999999999	197.67400000000001	198.01599999999999	198.01599999999999	198.358	198.7	199.042	199.042	199.38399999999999	199.726	200.06800000000001	200.06800000000001	200.41	200.75200000000001	201.09399999999999	201.43600000000001	201.43600000000001	201.77799999999999	202.12	202.46199999999999	202.46199999999999	202.804	203.14599999999999	203.488	203.488	203.83	204.172	204.51400000000001	204.85599999999999	204.85599999999999	205.19800000000001	205.54	205.88200000000001	205.88200000000001	206.22399999999999	206.566	206.90799999999999	207.25	207.25	207.59200000000001	207.934	208.27600000000001	208.27600000000001	208.61799999999999	208.96	209.30199999999999	209.30199999999999	209.64400000000001	209.98599999999999	210.328	210.67	210.67	211.012	211.35400000000001	211.696	211.696	212.03800000000001	212.38	212.72200000000001	213.06399999999999	213.06399999999999	213.40600000000001	213.74799999999999	214.09	214.09	214.43199999999999	214.774	215.11600000000001	215.458	215.458	215.8	216.142	216.48400000000001	216.48400000000001	216.82599999999999	217.16800000000001	217.51	217.852	217.852	218.19399999999999	218.536	218.87799999999999	219.22	219.22	219.56200000000001	219.904	220.24600000000001	220.24600000000001	220.58799999999999	220.93	221.27199999999999	221.27199999999999	221.614	221.95599999999999	222.298	222.64	222.982	222.982	223.32400000000001	223.666	224.00800000000001	224.00800000000001	224.35	224.69200000000001	225.03399999999999	225.376	225.376	225.71799999999999	226.06	226.40199999999999	226.40199999999999	226.744	227.08600000000001	227.428	227.428	227.77	228.11199999999999	228.45400000000001	228.45400000000001	228.79599999999999	229.13800000000001	229.13800000000001	229.48	229.822	230.16399999999999	230.16399999999999	230.506	230.84800000000001	231.19	231.53200000000001	231.53200000000001	231.874	232.21600000000001	232.55799999999999	232.55799999999999	232.9	233.24199999999999	233.584	233.584	233.92599999999999	234.268	234.61	234.61	234.952	235.29400000000001	235.636	235.97800000000001	235.97800000000001	236.32	236.66200000000001	237.00399999999999	237.00399999999999	237.346	237.68799999999999	238.03	238.03	238.37200000000001	238.714	239.05600000000001	239.398	239.398	239.74	240.08199999999999	240.42400000000001	240.42400000000001	240.76599999999999	241.108	241.45	241.45	241.792	242.13399999999999	242.476	242.81800000000001	242.81800000000001	243.16	243.50200000000001	243.84399999999999	243.84399999999999	244.18600000000001	244.52799999999999	244.87	244.87	245.21199999999999	245.554	245.89599999999999	246.238	246.238	246.58	246.922	247.26400000000001	247.26400000000001	247.60599999999999	247.94800000000001	248.29	248.29	248.63200000000001	248.97399999999999	249.316	249.316	249.65799999999999	250	250.34200000000001	250.684	250.684	251.02600000000001	251.36799999999999	251.71	251.71	252.05199999999999	252.39400000000001	252.73599999999999	252.73599999999999	253.078	253.42	253.762	253.762	254.10400000000001	254.446	254.78800000000001	254.78800000000001	255.13	255.47200000000001	255.81399999999999	256.15600000000001	256.15600000000001	256.49799999999999	256.83999999999997	257.18200000000002	257.18200000000002	257.524	257.86599999999999	258.20800000000003	258.20800000000003	258.55	258.892	259.23399999999998	259.23399999999998	259.57600000000002	259.91800000000001	260.26	260.26	260.60199999999998	260.94400000000002	261.286	261.286	261.62799999999999	261.97000000000003	262.31200000000001	262.31200000000001	262.654	262.99599999999998	263.33800000000002	263.33800000000002	263.68	264.02199999999999	264.36399999999998	264.36399999999998	264.70600000000002	265.048	265.39	265.39	265.73200000000003	266.07400000000001	266.416	266.416	266.75799999999998	267.10000000000002	267.44200000000001	267.44200000000001	267.78399999999999	268.12599999999998	268.46800000000002	268.46800000000002	268.81	269.15199999999999	269.49400000000003	269.49400000000003	269.83600000000001	270.178	270.52	270.52	270.86200000000002	271.20400000000001	271.54599999999999	271.54599999999999	271.88799999999998	272.23	272.572	272.572	272.91399999999999	273.25599999999997	273.59800000000001	273.59800000000001	273.94	274.28199999999998	274.62400000000002	274.62400000000002	274.96600000000001	275.30799999999999	275.64999999999998	275.64999999999998	275.99200000000002	276.334	276.67599999999999	276.67599999999999	277.01799999999997	277.01799999999997	277.36	277.702	278.04399999999998	278.04399999999998	278.38600000000002	278.72800000000001	279.07	279.07	279.41199999999998	279.75400000000002	280.096	280.096	280.43799999999999	280.77999999999997	281.12200000000001	281.12200000000001	281.464	281.80599999999998	282.14800000000002	282.14800000000002	282.83199999999999	282.83199999999999	283.17399999999998	283.51600000000002	283.858	283.858	284.2	284.54199999999997	284.88400000000001	284.88400000000001	285.226	285.56799999999998	285.91000000000003	286.25200000000001	286.25200000000001	286.59399999999999	286.93599999999998	287.27800000000002	287.27800000000002	287.62	287.96199999999999	288.30399999999997	288.30399999999997	288.64600000000002	288.988	289.33	289.67200000000003	289.67200000000003	290.01400000000001	290.35599999999999	290.69799999999998	290.69799999999998	291.04000000000002	291.38200000000001	291.72399999999999	292.06599999999997	292.06599999999997	292.40800000000002	292.75	293.09199999999998	293.09199999999998	293.43400000000003	293.77600000000001	294.11799999999999	294.45999999999998	294.45999999999998	294.80200000000002	295.14400000000001	295.48599999999999	295.48599999999999	295.82799999999997	296.17	296.512	296.512	296.85399999999998	297.19600000000003	297.53800000000001	297.88	297.88	298.22199999999998	298.56400000000002	298.90600000000001	298.90600000000001	299.24799999999999	299.58999999999997	299.93200000000002	299.93200000000002	300.274	300.61599999999999	300.95800000000003	301.3	301.3	301.642	301.98399999999998	302.32600000000002	302.32600000000002	302.66800000000001	302.66800000000001	302.66800000000001	303.01	303.01	303.01	303.01	303.01	303.01	303.01	303.01	303.01	303.01	303.01	302.66800000000001	302.66800000000001	302.32600000000002	302.32600000000002	301.98399999999998	301.98399999999998	301.642	301.3	301.3	300.95800000000003	300.61599999999999	300.274	299.93200000000002	299.58999999999997	299.24799999999999	298.90600000000001	298.56400000000002	298.22199999999998	297.88	297.53800000000001	297.19600000000003	297.19600000000003	296.85399999999998	296.512	296.17	295.82799999999997	295.48599999999999	295.48599999999999	295.14400000000001	294.80200000000002	294.45999999999998	294.45999999999998	294.11799999999999	293.77600000000001	293.43400000000003	293.43400000000003	293.43400000000003	293.09199999999998	292.75	292.75	292.40800000000002	292.40800000000002	292.06599999999997	292.06599999999997	291.72399999999999	291.38200000000001	291.38200000000001	291.38200000000001	291.04000000000002	291.04000000000002	290.69799999999998	290.69799999999998	290.35599999999999	290.35599999999999	290.01400000000001	290.01400000000001	290.01400000000001	289.67200000000003	289.67200000000003	289.33	289.33	289.33	288.988	288.988	288.988	288.64600000000002	288.64600000000002	288.64600000000002	288.30399999999997	288.30399999999997	288.30399999999997	288.30399999999997	287.96199999999999	287.62	287.62	287.27800000000002	287.27800000000002	286.93599999999998	286.93599999999998	286.59399999999999	286.59399999999999	286.25200000000001	286.25200000000001	286.25200000000001	285.91000000000003	285.91000000000003	285.91000000000003	285.91000000000003	285.56799999999998	285.56799999999998	285.56799999999998	285.56799999999998	285.56799999999998	285.226	285.226	285.226	284.88400000000001	284.88400000000001	284.88400000000001	284.88400000000001	284.88400000000001	284.54199999999997	284.54199999999997	284.54199999999997	284.54199999999997	284.2	284.2	284.2	284.2	284.2	283.858	283.858	283.858	283.858	283.858	283.51600000000002	283.51600000000002	283.51600000000002	283.51600000000002	283.51600000000002	283.17399999999998	283.17399999999998	283.17399999999998	283.17399999999998	283.17399999999998	282.83199999999999	282.83199999999999	282.83199999999999	282.83199999999999	282.83199999999999	282.49	282.49	282.49	282.49	282.49	282.14800000000002	282.14800000000002	282.14800000000002	282.14800000000002	282.14800000000002	282.14800000000002	281.80599999999998	281.80599999999998	281.80599999999998	281.80599999999998	281.80599999999998	281.80599999999998	281.464	281.464	281.464	281.464	281.464	281.464	281.12200000000001	281.12200000000001	281.12200000000001	281.12200000000001	281.12200000000001	281.12200000000001	280.77999999999997	280.77999999999997	280.77999999999997	280.77999999999997	280.77999999999997	280.77999999999997	280.43799999999999	280.43799999999999	280.43799999999999	280.43799999999999	280.43799999999999	280.43799999999999	280.096	280.096	280.096	280.096	280.096	280.096	280.096	279.75400000000002	279.75400000000002	279.75400000000002	279.75400000000002	279.75400000000002	279.75400000000002	279.75400000000002	279.41199999999998	279.41199999999998	279.41199999999998	279.41199999999998	279.41199999999998	279.41199999999998	279.41199999999998	279.07	279.07	279.07	279.07	279.07	279.07	279.07	278.72800000000001	278.72800000000001	278.72800000000001	278.72800000000001	278.72800000000001	278.72800000000001	278.72800000000001	278.38600000000002	278.38600000000002	278.38600000000002	278.38600000000002	278.38600000000002	278.38600000000002	278.38600000000002	278.04399999999998	278.04399999999998	278.04399999999998	278.04399999999998	278.04399999999998	278.04399999999998	278.04399999999998	277.702	277.702	277.702	277.702	277.702	277.702	277.702	277.702	277.36	277.36	277.36	277.36	277.36	277.36	277.36	277.01799999999997	277.01799999999997	277.01799999999997	277.01799999999997	277.01799999999997	277.01799999999997	277.01799999999997	277.01799999999997	276.67599999999999	276.67599999999999	276.67599999999999	276.67599999999999	276.67599999999999	276.67599999999999	276.67599999999999	276.67599999999999	276.67599999999999	276.334	276.334	276.334	276.334	276.334	276.334	276.334	276.334	275.99200000000002	275.99200000000002	275.99200000000002	275.99200000000002	275.99200000000002	275.99200000000002	275.99200000000002	275.99200000000002	275.99200000000002	275.64999999999998	275.64999999999998	275.64999999999998	275.64999999999998	275.64999999999998	275.64999999999998	275.64999999999998	275.64999999999998	275.64999999999998	275.30799999999999	275.30799999999999	275.30799999999999	275.30799999999999	275.30799999999999	275.30799999999999	275.30799999999999	275.30799999999999	275.30799999999999	274.96600000000001	274.96600000000001	274.96600000000001	274.96600000000001	274.96600000000001	274.96600000000001	274.96600000000001	274.96600000000001	274.96600000000001	274.96600000000001	274.62400000000002	274.62400000000002	274.62400000000002	274.62400000000002	274.62400000000002	274.62400000000002	274.62400000000002	274.62400000000002	274.62400000000002	274.62400000000002	274.28199999999998	274.28199999999998	274.28199999999998	274.28199999999998	274.28199999999998	274.28199999999998	274.28199999999998	274.28199999999998	274.28199999999998	274.28199999999998	273.94	273.94	273.94	273.94	273.94	273.94	273.94	273.94	273.94	273.94	273.94	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.59800000000001	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	273.25599999999997	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.91399999999999	272.572	272.572	272.572	272.572	272.572	272.572	272.572	272.572	272.572	272.572	272.572	272.572	272.23	272.23	272.23	272.23	272.23	272.23	272.23	272.23	272.23	272.23	272.23	272.23	272.23	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.88799999999998	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.54599999999999	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	271.20400000000001	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.86200000000002	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.52	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	270.178	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.83600000000001	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.49400000000003	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	269.15199999999999	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.81	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.46800000000002	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	268.12599999999998	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.78399999999999	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.44200000000001	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	267.10000000000002	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.75799999999998	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.416	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	266.07400000000001	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.73200000000003	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.39	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.048	265.39	265.39	265.39	265.39	265.39	265.73200000000003	265.73200000000003	265.73200000000003	266.07400000000001	266.07400000000001	266.416	266.416	266.75799999999998	267.10000000000002	267.10000000000002	267.44200000000001	267.78399999999999	268.12599999999998	268.12599999999998	268.46800000000002	269.15199999999999	269.49400000000003	270.178	270.86200000000002	271.88799999999998	272.572	273.59800000000001	274.96600000000001	276.334	277.702	278.72800000000001	280.096	281.464	282.14800000000002	283.51600000000002	284.88400000000001	286.25200000000001	287.62	289.33	290.69799999999998	292.06599999999997	293.09199999999998	294.80200000000002	296.512	297.53800000000001	299.24799999999999	300.95800000000003	301.98399999999998	304.036	305.06200000000001	307.11399999999998	308.48200000000003	309.85000000000002	311.90199999999999	313.27	315.32100000000003	316.68900000000002	318.05700000000002	320.45100000000002	321.81900000000002	323.18700000000001	324.55500000000001	326.94900000000001	328.31700000000001	329.685	331.39499999999998	333.447	334.815	336.18299999999999	337.55099999999999	339.26100000000002	341.31299999999999	342.68099999999998	344.04899999999998	345.41699999999997	347.12700000000001	348.83699999999999	350.20499999999998	352.25700000000001	353.625	354.99299999999999	356.36099999999999	357.72899999999998	358.755	359.78100000000001	360.80700000000002	361.83300000000003	362.85899999999998	364.22699999999998	365.25299999999999	365.93700000000001	366.96300000000002	368.33100000000002	369.35700000000003	370.38299999999998	371.40899999999999	372.435	373.46100000000001	373.46100000000001	329.00099999999998	Carbon Twill Bioresin	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-2E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	-1E-3	0	0	0	0	0	0	0	0	0	1E-3	1E-3	1E-3	1E-3	1E-3	1E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	2E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	3.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	4.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	5.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	6.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	7.0000000000000001E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.0000000000000002E-3	8.0000000000000002E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	8.9999999999999993E-3	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	0.01	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.0999999999999999E-2	1.2E-2	1.2E-2	1.2999999999999999E-2	1.2999999999999999E-2	1.4E-2	1.4999999999999999E-2	1.6E-2	1.6E-2	1.7000000000000001E-2	1.7999999999999999E-2	0.02	2.1000000000000001E-2	2.1999999999999999E-2	2.3E-2	2.4E-2	2.5999999999999999E-2	2.7E-2	2.8000000000000001E-2	0.03	3.2000000000000001E-2	3.3000000000000002E-2	3.5000000000000003E-2	3.6999999999999998E-2	3.7999999999999999E-2	0.04	4.2000000000000003E-2	4.3999999999999997E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.5999999999999999E-2	4.7E-2	0.05	5.1999999999999998E-2	5.3999999999999999E-2	5.6000000000000001E-2	5.6000000000000001E-2	6.0999999999999999E-2	6.3E-2	6.6000000000000003E-2	6.8000000000000005E-2	7.0000000000000007E-2	7.1999999999999995E-2	7.3999999999999996E-2	7.5999999999999998E-2	7.8E-2	8.1000000000000003E-2	8.3000000000000004E-2	8.5000000000000006E-2	8.5999999999999993E-2	8.7999999999999995E-2	0.09	9.1999999999999998E-2	9.4E-2	9.6000000000000002E-2	9.8000000000000004E-2	9.9000000000000005E-2	0.10100000000000001	0.10299999999999999	0.105	0.107	0.108	0.11	0.112	0.114	0.11600000000000001	0.11799999999999999	0.12	0.121	0.123	0.125	0.127	0.128	0.13	0.13200000000000001	0.13400000000000001	0.13600000000000001	0.13800000000000001	0.13900000000000001	0.14099999999999999	0.14299999999999999	0.14399999999999999	0.14599999999999999	0.14799999999999999	0.15	0.152	0.154	0.155	0.157	0.159	0.16	0.16200000000000001	0.16400000000000001	0.16600000000000001	0.16800000000000001	0.16900000000000001	0.17100000000000001	0.17299999999999999	0.17399999999999999	0.17599999999999999	0.17799999999999999	0.18	0.18099999999999999	0.183	0.185	0.186	0.188	0.19	0.191	0.193	0.19400000000000001	0.19600000000000001	0.19800000000000001	0.19900000000000001	0.20100000000000001	0.20200000000000001	0.20399999999999999	0.20499999999999999	0.20599999999999999	0.20799999999999999	0.20899999999999999	0.21	0.21199999999999999	0.21299999999999999	0.214	0.215	0.216	0.218	0.218	0.22	0.221	0.222	0.223	0.224	0.224	0.22600000000000001	0.22600000000000001	0.22700000000000001	0.22800000000000001	0.22900000000000001	0.23	0.23	0.23100000000000001	0.23200000000000001	0.23200000000000001	0.23300000000000001	0.23400000000000001	0.23400000000000001	0.23499999999999999	0.23599999999999999	0.23599999999999999	0.23599999999999999	0.23699999999999999	0.23699999999999999	0.23799999999999999	0.23799999999999999	0.23799999999999999	0.23899999999999999	0.23899999999999999	0.24	0.24	0.24	0.24	0.24099999999999999	0.24099999999999999	0.24199999999999999	0.24199999999999999	0.24199999999999999	0.24299999999999999	0.24299999999999999	0.24399999999999999	0.24399999999999999	0.24399999999999999	0.245	0.245	0.246	0.246	0.246	0.246	0.247	0.247	0.248	0.248	0.248	0.249	0.249	0.25	0.25	0.25	0.251	0.251	0.252	0.252	0.252	0.253	0.254	0.254	0.254	0.255	0.255	0.25600000000000001	0.25600000000000001	0.25600000000000001	0.25700000000000001	0.25700000000000001	0.25800000000000001	0.25800000000000001	0.25800000000000001	0.25900000000000001	0.25900000000000001	0.26	0.26	0.26	0.26100000000000001	0.26100000000000001	0.26200000000000001	0.26200000000000001	0.26300000000000001	0.26300000000000001	0.26400000000000001	0.26400000000000001	0.26400000000000001	0.26500000000000001	0.26500000000000001	0.26600000000000001	0.26600000000000001	0.26600000000000001	0.26700000000000002	0.26700000000000002	0.26800000000000002	0.26800000000000002	0.26900000000000002	0.26900000000000002	0.27	0.27	0.27	0.27100000000000002	0.27100000000000002	0.27200000000000002	0.27200000000000002	0.27200000000000002	0.27300000000000002	0.27400000000000002	0.27400000000000002	0.27400000000000002	0.27500000000000002	0.27500000000000002	0.27600000000000002	0.27600000000000002	0.27700000000000002	0.27700000000000002	0.27800000000000002	0.27800000000000002	0.27800000000000002	0.27900000000000003	0.27900000000000003	0.28000000000000003	0.28000000000000003	0.28100000000000003	0.28100000000000003	0.28199999999999997	0.28199999999999997	0.28199999999999997	0.28299999999999997	0.28299999999999997	0.28399999999999997	0.28399999999999997	0.28499999999999998	0.28499999999999998	0.28599999999999998	0.28599999999999998	0.28599999999999998	0.28699999999999998	0.28699999999999998	0.28799999999999998	0.28799999999999998	0.28899999999999998	0.28899999999999998	0.28999999999999998	0.28999999999999998	0.28999999999999998	0.29099999999999998	0.29199999999999998	0.29199999999999998	0.29199999999999998	0.29299999999999998	0.29299999999999998	0.29399999999999998	0.29399999999999998	0.29499999999999998	0.29499999999999998	0.29599999999999999	0.29599999999999999	0.29599999999999999	0.29699999999999999	0.29699999999999999	0.29799999999999999	0.29799999999999999	0.29899999999999999	0.29899999999999999	0.3	0.3	0.3	0.30099999999999999	0.30199999999999999	0.30199999999999999	0.30199999999999999	0.30299999999999999	0.30299999999999999	0.30399999999999999	0.30399999999999999	0.30399999999999999	0.30499999999999999	0.30599999999999999	0.30599999999999999	0.30599999999999999	0.307	0.307	0.308	0.308	0.309	0.309	0.31	0.31	0.31	0.311	0.311	0.312	0.312	0.313	0.313	0.314	0.314	0.314	0.315	0.316	0.316	0.316	0.317	0.317	0.318	0.318	0.318	0.31900000000000001	0.32	0.32	0.32	0.32100000000000001	0.32100000000000001	0.32200000000000001	0.32200000000000001	0.32200000000000001	0.32300000000000001	0.32400000000000001	0.32400000000000001	0.32400000000000001	0.32500000000000001	0.32500000000000001	0.32600000000000001	0.32600000000000001	0.32700000000000001	0.32700000000000001	0.32800000000000001	0.32800000000000001	0.32800000000000001	0.32800000000000001	0.33	0.33	0.33	0.33100000000000002	0.33100000000000002	0.33200000000000002	0.33200000000000002	0.33200000000000002	0.33300000000000002	0.33400000000000002	0.33400000000000002	0.33400000000000002	0.33500000000000002	0.33500000000000002	0.33600000000000002	0.33600000000000002	0.33700000000000002	0.33700000000000002	0.33800000000000002	0.33800000000000002	0.33800000000000002	0.33800000000000002	0.33900000000000002	0.34	0.34	0.34100000000000003	0.34100000000000003	0.34200000000000003	0.34200000000000003	0.34200000000000003	0.34300000000000003	0.34399999999999997	0.34399999999999997	0.34399999999999997	0.34499999999999997	0.34499999999999997	0.34599999999999997	0.34599999999999997	0.34699999999999998	0.34699999999999998	0.34799999999999998	0.34799999999999998	0.34799999999999998	0.34899999999999998	0.34899999999999998	0.35	0.35	0.35099999999999998	0.35099999999999998	0.35199999999999998	0.35199999999999998	0.35199999999999998	0.35299999999999998	0.35399999999999998	0.35399999999999998	0.35399999999999998	0.35499999999999998	0.35499999999999998	0.35599999999999998	0.35599999999999998	0.35699999999999998	0.35699999999999998	0.35799999999999998	0.35799999999999998	0.35799999999999998	0.35899999999999999	0.36	0.36	0.36	0.36099999999999999	0.36099999999999999	0.36199999999999999	0.36199999999999999	0.36199999999999999	0.36199999999999999	0.36399999999999999	0.36399999999999999	0.36399999999999999	0.36499999999999999	0.36499999999999999	0.36599999999999999	0.36599999999999999	0.36699999999999999	0.36699999999999999	0.36799999999999999	0.36799999999999999	0.36799999999999999	0.36899999999999999	0.37	0.37	0.37	0.371	0.371	0.372	0.372	0.373	0.373	0.374	0.374	0.375	0.375	0.376	0.376	0.376	0.377	0.378	0.378	0.378	0.379	0.379	0.38	0.38	0.38100000000000001	0.38100000000000001	0.38200000000000001	0.38200000000000001	0.38300000000000001	0.38300000000000001	0.38400000000000001	0.38400000000000001	0.38500000000000001	0.38500000000000001	0.38600000000000001	0.38600000000000001	0.38600000000000001	0.38700000000000001	0.38800000000000001	0.38800000000000001	0.38800000000000001	0.38900000000000001	0.39	0.39	0.39	0.39100000000000001	0.39200000000000002	0.39200000000000002	0.39200000000000002	0.39300000000000002	0.39300000000000002	0.39400000000000002	0.39400000000000002	0.39500000000000002	0.39500000000000002	0.39600000000000002	0.39600000000000002	0.39700000000000002	0.39700000000000002	0.39800000000000002	0.39800000000000002	0.39900000000000002	0.39900000000000002	0.4	0.4	0.40100000000000002	0.40100000000000002	0.40200000000000002	0.40200000000000002	0.40300000000000002	0.40300000000000002	0.40400000000000003	0.40400000000000003	0.40400000000000003	0.40500000000000003	0.40600000000000003	0.40600000000000003	0.40600000000000003	0.40699999999999997	0.40799999999999997	0.40799999999999997	0.40799999999999997	0.40899999999999997	0.40899999999999997	0.41	0.41	0.41099999999999998	0.41099999999999998	0.41199999999999998	0.41199999999999998	0.41299999999999998	0.41299999999999998	0.41399999999999998	0.41399999999999998	0.41399999999999998	0.41499999999999998	0.41599999999999998	0.41599999999999998	0.41599999999999998	0.41699999999999998	0.41799999999999998	0.41799999999999998	0.41799999999999998	0.41899999999999998	0.42	0.42	0.42	0.42099999999999999	0.42099999999999999	0.42199999999999999	0.42199999999999999	0.42299999999999999	0.42299999999999999	0.42399999999999999	0.42399999999999999	0.42399999999999999	0.42499999999999999	0.42599999999999999	0.42599999999999999	0.42599999999999999	0.42699999999999999	0.42699999999999999	0.42699999999999999	0.42799999999999999	0.42899999999999999	0.42899999999999999	0.43	0.43	0.43099999999999999	0.43099999999999999	0.432	0.432	0.432	0.433	0.434	0.434	0.434	0.435	0.435	0.436	0.436	0.437	0.437	0.438	0.438	0.439	0.439	0.44	0.44	0.441	0.441	0.442	0.442	0.442	0.443	0.44400000000000001	0.44400000000000001	0.44400000000000001	0.44500000000000001	0.44500000000000001	0.44600000000000001	0.44600000000000001	0.44700000000000001	0.44700000000000001	0.44800000000000001	0.44800000000000001	0.44900000000000001	0.44900000000000001	0.45	0.45	0.45	0.45100000000000001	0.45100000000000001	0.45100000000000001	0.45200000000000001	0.45300000000000001	0.45300000000000001	0.45400000000000001	0.45400000000000001	0.45400000000000001	0.45500000000000002	0.45600000000000002	0.45600000000000002	0.45600000000000002	0.45700000000000002	0.45700000000000002	0.45800000000000002	0.45800000000000002	0.45900000000000002	0.45900000000000002	0.46	0.46	0.46100000000000002	0.46100000000000002	0.46200000000000002	0.46200000000000002	0.46200000000000002	0.46300000000000002	0.46300000000000002	0.46400000000000002	0.46400000000000002	0.46500000000000002	0.46500000000000002	0.46600000000000003	0.46600000000000003	0.46700000000000003	0.46700000000000003	0.46800000000000003	0.46800000000000003	0.46800000000000003	0.46899999999999997	0.46899999999999997	0.47	0.47	0.47099999999999997	0.47099999999999997	0.47199999999999998	0.47199999999999998	0.47299999999999998	0.47299999999999998	0.47399999999999998	0.47399999999999998	0.47499999999999998	0.47499999999999998	0.47599999999999998	0.47599999999999998	0.47599999999999998	0.47699999999999998	0.47699999999999998	0.47799999999999998	0.47799999999999998	0.47899999999999998	0.47899999999999998	0.48	0.48	0.48099999999999998	0.48099999999999998	0.48199999999999998	0.48199999999999998	0.48199999999999998	0.48299999999999998	0.48299999999999998	0.48399999999999999	0.48399999999999999	0.48499999999999999	0.48499999999999999	0.48599999999999999	0.48599999999999999	0.48699999999999999	0.48699999999999999	0.48799999999999999	0.48799999999999999	0.48799999999999999	0.48899999999999999	0.49	0.49	0.49	0.49099999999999999	0.49099999999999999	0.49199999999999999	0.49199999999999999	0.49299999999999999	0.49299999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.495	0.496	0.496	0.496	0.497	0.497	0.498	0.498	0.499	0.499	0.5	0.5	0.501	0.501	0.502	0.502	0.502	0.503	0.504	0.504	0.504	0.505	0.505	0.50600000000000001	0.50600000000000001	0.50700000000000001	0.50700000000000001	0.50800000000000001	0.50800000000000001	0.50800000000000001	0.50900000000000001	0.50900000000000001	0.51	0.51	0.51100000000000001	0.51100000000000001	0.51200000000000001	0.51200000000000001	0.51200000000000001	0.51300000000000001	0.51300000000000001	0.51400000000000001	0.51400000000000001	0.51500000000000001	0.51500000000000001	0.51600000000000001	0.51600000000000001	0.51600000000000001	0.51700000000000002	0.51800000000000002	0.51800000000000002	0.51800000000000002	0.51900000000000002	0.52	0.52	0.52	0.52100000000000002	0.52100000000000002	0.52200000000000002	0.52200000000000002	0.52300000000000002	0.52300000000000002	0.52400000000000002	0.52400000000000002	0.52500000000000002	0.52500000000000002	0.52600000000000002	0.52600000000000002	0.52600000000000002	0.52700000000000002	0.52800000000000002	0.52800000000000002	0.52800000000000002	0.52900000000000003	0.53	0.53	0.53	0.53100000000000003	0.53200000000000003	0.53200000000000003	0.53200000000000003	0.53300000000000003	0.53400000000000003	0.53400000000000003	0.53400000000000003	0.53500000000000003	0.53600000000000003	0.53600000000000003	0.53600000000000003	0.53700000000000003	0.53800000000000003	0.53800000000000003	0.53800000000000003	0.53900000000000003	0.54	0.54	0.54	0.54100000000000004	0.54100000000000004	0.54200000000000004	0.54200000000000004	0.54300000000000004	0.54300000000000004	0.54400000000000004	0.54400000000000004	0.54400000000000004	0.54500000000000004	0.54600000000000004	0.54600000000000004	0.54600000000000004	0.54700000000000004	0.54800000000000004	0.54800000000000004	0.54900000000000004	0.54900000000000004	0.55000000000000004	0.55000000000000004	0.55000000000000004	0.55100000000000005	0.55100000000000005	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.504	0.5	0.5	0.5	0.5	0.5	0.5	0.5	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.498	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.496	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.49399999999999999	0.496	0.496	0.498	0.5	0.504	0.50600000000000001	0.50600000000000001	0.50800000000000001	0.51400000000000001	0.51600000000000001	0.51800000000000002	0.52	0.52600000000000002	0.52800000000000002	0.53400000000000003	0.53800000000000003	0.54	0.54600000000000004	0.55000000000000004	0.55600000000000005	0.56000000000000005	0.56599999999999995	0.57399999999999995	0.57799999999999996	0.58399999999999996	0.59	0.59599999999999997	0.60399999999999998	0.61	0.61599999999999999	0.624	0.63	0.63800000000000001	0.64800000000000002	0.65600000000000003	0.66400000000000003	0.67	0.68	0.68799999999999994	0.69799999999999995	0.70599999999999996	0.71599999999999997	0.72599999999999998	0.73599999999999999	0.746	0.75600000000000001	0.76600000000000001	0.77800000000000002	0.78800000000000003	0.79800000000000004	0.81	0.82399999999999995	0.83399999999999996	0.84599999999999997	0.85599999999999998	0.86799999999999999	0.88	0.89400000000000002	0.90600000000000003	0.92	0.93200000000000005	0.94599999999999995	0.96	0.97199999999999998	0.98799999999999999	1.002	1.016	1.03	1.046	1.0580000000000001	1.0680000000000001	1.0820000000000001	1.0980000000000001	1.1120000000000001	1.1299999999999999	1.1459999999999999	1.1619999999999999	1.18	1.196	1.212	1.23	1.248	1.266	1.282	1.302	1.32	1.3380000000000001	1.3580000000000001	1.3759999999999999	1.3959999999999999	1.4159999999999999	1.4319999999999999	1.452	1.472	1.492	1.516	1.532	1.556	1.5720000000000001	1.5960000000000001	1.6160000000000001	1.6359999999999999	1.6559999999999999	1.6759999999999999	1.696	1.716	1.736	1.756	1.776	1.798	1.8180000000000001	1.8380000000000001	1.8580000000000001	1.8779999999999999	1.8979999999999999	1.9179999999999999	1.9379999999999999	1.958	1.978	2	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.31900000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.63800000000000001	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	0.95699999999999996	1.276	1.276	1.276	1.276	1.276	1.276	1.276	1.276	1.276	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.5940000000000001	1.913	1.913	1.913	1.913	1.913	2.2320000000000002	2.2320000000000002	2.2320000000000002	2.2320000000000002	2.2320000000000002	2.5510000000000002	2.5510000000000002	2.5510000000000002	2.5510000000000002	2.5510000000000002	2.87	2.87	2.87	2.87	3.1890000000000001	3.1890000000000001	3.1890000000000001	3.508	3.508	3.508	3.508	3.827	3.827	3.827	4.1449999999999996	4.1449999999999996	4.1449999999999996	4.4640000000000004	4.4640000000000004	4.4640000000000004	4.7830000000000004	4.7830000000000004	4.7830000000000004	5.1020000000000003	5.1020000000000003	5.1020000000000003	5.4210000000000003	5.4210000000000003	5.4210000000000003	5.74	5.74	6.0590000000000002	6.0590000000000002	6.0590000000000002	6.3780000000000001	6.3780000000000001	6.3780000000000001	6.6959999999999997	6.6959999999999997	6.6959999999999997	7.0149999999999997	7.0149999999999997	7.0149999999999997	7.0149999999999997	7.3339999999999996	7.3339999999999996	7.3339999999999996	7.3339999999999996	7.6529999999999996	7.6529999999999996	7.6529999999999996	7.6529999999999996	7.9720000000000004	7.9720000000000004	7.9720000000000004	7.9720000000000004	7.9720000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.2910000000000004	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.61	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	8.9290000000000003	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.2469999999999999	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.5660000000000007	9.8849999999999998	9.8849999999999998	9.8849999999999998	9.8849999999999998	10.204000000000001	10.204000000000001	10.204000000000001	10.523	10.523	10.842000000000001	10.842000000000001	11.161	11.161	11.48	11.798	12.117000000000001	12.117000000000001	12.436	12.755000000000001	13.393000000000001	13.712	14.349	14.987	15.944000000000001	16.582000000000001	17.219000000000001	18.175999999999998	19.132999999999999	20.408000000000001	21.684000000000001	22.959	23.916	25.190999999999999	26.786000000000001	28.38	29.655999999999999	30.611999999999998	31.888000000000002	33.481999999999999	35.076999999999998	36.033000000000001	37.628	38.584000000000003	40.179000000000002	41.454000000000001	43.048000000000002	44.323999999999998	45.917999999999999	47.194000000000003	48.151000000000003	50.064	51.02	51.976999999999997	53.570999999999998	54.527999999999999	55.804000000000002	56.76	58.036000000000001	59.311	60.268000000000001	61.223999999999997	62.819000000000003	63.776000000000003	64.731999999999999	65.688999999999993	66.644999999999996	68.239999999999995	69.195999999999998	70.153000000000006	71.11	72.385000000000005	73.341999999999999	74.617000000000004	75.893000000000001	76.849000000000004	77.805999999999997	78.763000000000005	79.718999999999994	80.676000000000002	82.27	83.227000000000004	84.183999999999997	85.14	86.096999999999994	87.054000000000002	88.01	89.286000000000001	90.242000000000004	91.518000000000001	92.474000000000004	93.430999999999997	94.388000000000005	95.343999999999994	96.62	97.576999999999998	98.533000000000001	99.49	100.446	101.40300000000001	102.36	103.316	104.273	105.23	106.505	107.462	108.41800000000001	109.375	110.33199999999999	111.288	111.926	112.883	113.839	114.477	115.434	116.071	117.02800000000001	117.666	118.622	119.26	119.898	120.536	121.492	122.13	122.768	123.40600000000001	124.04300000000001	124.681	125.319	125.95699999999999	126.276	126.913	127.551	128.18899999999999	128.50800000000001	129.14500000000001	129.464	130.102	130.42099999999999	131.059	131.37799999999999	131.696	132.334	132.65299999999999	132.97200000000001	133.291	133.61000000000001	133.929	134.24700000000001	134.566	134.88499999999999	135.20400000000001	135.523	135.523	135.84200000000001	136.161	136.161	136.47999999999999	136.798	136.798	137.11699999999999	137.11699999999999	137.43600000000001	137.755	137.755	138.07400000000001	138.07400000000001	138.393	138.71199999999999	138.71199999999999	139.03100000000001	139.34899999999999	139.34899999999999	139.66800000000001	139.98699999999999	139.98699999999999	140.30600000000001	140.625	140.625	140.94399999999999	141.26300000000001	141.58199999999999	141.58199999999999	141.9	141.9	142.21899999999999	142.53800000000001	142.857	142.857	143.17599999999999	143.17599999999999	143.495	143.81399999999999	143.81399999999999	144.13300000000001	144.452	144.452	144.77000000000001	145.089	145.089	145.40799999999999	145.727	145.727	146.04599999999999	146.36500000000001	146.36500000000001	146.684	147.00299999999999	147.00299999999999	147.321	147.63999999999999	147.63999999999999	147.959	148.27799999999999	148.27799999999999	148.59700000000001	148.59700000000001	148.916	149.23500000000001	149.554	149.87200000000001	149.87200000000001	150.191	150.191	150.51	150.82900000000001	150.82900000000001	151.148	151.46700000000001	151.786	151.786	152.10499999999999	152.423	152.423	152.74199999999999	153.06100000000001	153.06100000000001	153.38	153.69900000000001	154.018	154.018	154.33699999999999	154.65600000000001	154.65600000000001	154.97399999999999	155.29300000000001	155.29300000000001	155.61199999999999	155.93100000000001	156.25	156.25	156.56899999999999	156.88800000000001	156.88800000000001	157.20699999999999	157.52600000000001	157.52600000000001	157.84399999999999	158.16300000000001	158.482	158.482	158.80099999999999	159.12	159.12	159.43899999999999	159.75800000000001	159.75800000000001	160.077	160.39500000000001	160.714	160.714	161.03299999999999	161.352	161.352	161.67099999999999	161.99	161.99	162.309	162.62799999999999	162.946	163.26499999999999	163.26499999999999	163.584	163.90299999999999	163.90299999999999	164.22200000000001	164.541	164.541	164.86	165.179	165.49700000000001	165.49700000000001	165.816	166.13499999999999	166.45400000000001	166.45400000000001	166.773	167.09200000000001	167.411	167.73	168.048	168.048	168.36699999999999	168.68600000000001	169.005	169.32400000000001	169.32400000000001	169.643	169.96199999999999	170.28100000000001	170.59899999999999	170.59899999999999	170.91800000000001	171.23699999999999	171.55600000000001	171.875	171.875	172.19399999999999	172.51300000000001	172.83199999999999	173.15	173.15	173.46899999999999	173.78800000000001	174.107	174.42599999999999	174.42599999999999	174.745	175.06399999999999	175.38300000000001	175.702	175.702	176.02	176.339	176.65799999999999	176.65799999999999	176.977	177.29599999999999	177.61500000000001	177.934	177.934	178.25299999999999	178.571	178.89	179.209	179.209	179.52799999999999	179.84700000000001	180.166	180.48500000000001	180.48500000000001	180.804	181.12200000000001	181.441	181.76	181.76	182.07900000000001	182.398	182.71700000000001	183.036	183.036	183.35499999999999	183.673	183.99199999999999	184.31100000000001	184.31100000000001	184.63	184.94900000000001	185.268	185.58699999999999	185.90600000000001	186.22399999999999	186.22399999999999	186.54300000000001	186.86199999999999	187.18100000000001	187.5	187.5	187.81899999999999	188.13800000000001	188.45699999999999	188.45699999999999	188.77600000000001	189.09399999999999	189.41300000000001	189.732	189.732	190.05099999999999	190.37	190.68899999999999	191.00800000000001	191.00800000000001	191.327	191.64500000000001	191.964	192.28299999999999	192.28299999999999	192.602	192.92099999999999	193.24	193.559	193.559	193.87799999999999	194.196	194.51499999999999	194.834	195.15299999999999	195.15299999999999	195.47200000000001	195.791	196.11	196.429	196.74700000000001	197.066	197.066	197.38499999999999	197.70400000000001	198.023	198.34200000000001	198.34200000000001	198.661	198.98	199.298	199.61699999999999	199.93600000000001	199.93600000000001	200.255	200.57400000000001	200.893	201.21199999999999	201.21199999999999	201.53100000000001	201.84899999999999	202.16800000000001	202.48699999999999	202.48699999999999	202.80600000000001	203.125	203.44399999999999	203.76300000000001	203.76300000000001	204.08199999999999	204.4	204.71899999999999	205.03800000000001	205.03800000000001	205.357	205.67599999999999	205.995	206.31399999999999	206.31399999999999	206.63300000000001	206.952	207.27	207.589	207.589	207.90799999999999	208.227	208.54599999999999	208.86500000000001	209.184	209.184	209.50299999999999	209.821	210.14	210.459	210.77799999999999	210.77799999999999	211.09700000000001	211.416	211.73500000000001	212.054	212.37200000000001	212.37200000000001	212.691	213.01	213.32900000000001	213.648	213.96700000000001	214.286	214.286	214.60499999999999	214.923	215.24199999999999	215.56100000000001	215.88	215.88	216.19900000000001	216.518	216.83699999999999	217.15600000000001	217.47399999999999	217.79300000000001	217.79300000000001	218.11199999999999	218.43100000000001	218.75	219.06899999999999	219.38800000000001	219.70699999999999	219.70699999999999	220.02600000000001	220.66300000000001	220.66300000000001	220.982	221.30099999999999	221.62	221.93899999999999	222.25800000000001	222.577	222.89500000000001	222.89500000000001	223.214	223.53299999999999	223.852	224.17099999999999	224.49	224.809	224.809	225.12799999999999	225.446	225.76499999999999	226.084	226.40299999999999	226.72200000000001	227.041	227.041	227.36	227.679	227.99700000000001	228.316	228.63499999999999	228.95400000000001	228.95400000000001	229.273	229.59200000000001	229.911	230.23	230.548	230.86699999999999	230.86699999999999	231.18600000000001	231.505	231.82400000000001	232.143	232.46199999999999	232.78100000000001	232.78100000000001	233.09899999999999	233.41800000000001	233.73699999999999	234.05600000000001	234.375	234.69399999999999	235.01300000000001	235.33199999999999	235.33199999999999	235.65	235.96899999999999	236.28800000000001	236.607	236.607	237.245	237.56399999999999	237.56399999999999	237.88300000000001	238.202	238.52	238.839	239.15799999999999	239.477	239.477	239.79599999999999	240.11500000000001	240.434	240.75299999999999	241.071	241.39	241.39	241.709	242.02799999999999	242.34700000000001	242.666	242.98500000000001	242.98500000000001	243.304	243.62200000000001	243.941	244.26	244.57900000000001	244.57900000000001	244.898	245.21700000000001	245.536	245.85499999999999	246.173	246.173	246.49199999999999	246.81100000000001	247.13	247.44900000000001	247.768	248.08699999999999	248.08699999999999	248.40600000000001	248.72399999999999	249.04300000000001	249.04300000000001	249.36199999999999	249.68100000000001	250	250.31899999999999	250.63800000000001	250.63800000000001	250.95699999999999	251.27600000000001	251.59399999999999	251.91300000000001	252.232	252.232	252.55099999999999	252.87	253.18899999999999	253.50800000000001	253.827	253.827	254.14500000000001	254.464	254.78299999999999	255.102	255.42099999999999	255.42099999999999	255.74	256.05900000000003	256.37799999999999	256.69600000000003	257.01499999999999	257.01499999999999	257.334	257.65300000000002	257.97199999999998	258.291	258.61	258.61	258.92899999999997	259.24700000000001	259.56599999999997	259.88499999999999	260.20400000000001	260.20400000000001	260.52300000000002	260.84199999999998	261.161	261.48	261.798	261.798	262.11700000000002	262.43599999999998	262.755	263.07400000000001	263.39299999999997	263.39299999999997	263.71199999999999	264.03100000000001	264.34899999999999	264.66800000000001	264.98700000000002	264.98700000000002	265.30599999999998	265.625	265.94400000000002	266.26299999999998	266.58199999999999	266.58199999999999	266.90100000000001	267.21899999999999	267.53800000000001	267.85700000000003	268.17599999999999	268.17599999999999	268.495	268.81400000000002	269.13299999999998	269.452	269.77	269.77	270.089	270.40800000000002	270.72699999999998	271.04599999999999	271.36500000000001	271.36500000000001	271.68400000000003	272.00299999999999	272.32100000000003	272.64	272.959	272.959	273.27800000000002	273.59699999999998	273.916	274.23500000000001	274.55399999999997	274.55399999999997	274.87200000000001	275.19099999999997	275.51	275.82900000000001	276.14800000000002	276.14800000000002	276.46699999999998	276.786	277.10500000000002	277.423	277.74200000000002	277.74200000000002	278.06099999999998	278.38	278.69900000000001	279.01799999999997	279.33699999999999	279.65600000000001	279.65600000000001	279.97399999999999	280.29300000000001	280.61200000000002	280.93099999999998	281.25	281.25	281.56900000000002	281.88799999999998	282.20699999999999	282.52499999999998	282.84399999999999	282.84399999999999	283.16300000000001	283.48200000000003	283.80099999999999	284.12	284.43900000000002	284.75799999999998	284.75799999999998	285.077	285.39499999999998	285.714	286.03300000000002	286.35199999999998	286.35199999999998	286.67099999999999	286.99	287.30900000000003	287.62799999999999	287.94600000000003	287.94600000000003	288.26499999999999	288.584	288.90300000000002	289.22199999999998	289.22199999999998	289.541	289.86	290.17899999999997	290.49700000000001	290.81599999999997	290.81599999999997	291.13499999999999	291.45400000000001	291.77300000000002	292.09199999999998	292.09199999999998	292.411	292.73	293.048	293.36700000000002	293.68599999999998	293.68599999999998	294.005	294.32400000000001	294.64299999999997	294.96199999999999	295.28100000000001	295.28100000000001	295.59899999999999	295.91800000000001	296.23700000000002	296.55599999999998	296.875	297.19400000000002	297.19400000000002	297.51299999999998	297.83199999999999	298.15100000000001	298.46899999999999	298.78800000000001	299.10700000000003	299.42599999999999	299.42599999999999	299.745	300.06400000000002	300.38299999999998	300.702	301.02	301.339	301.65800000000002	301.97699999999998	301.97699999999998	302.29599999999999	302.61500000000001	302.93400000000003	303.25299999999999	303.57100000000003	303.89	304.209	304.52800000000002	304.52800000000002	304.84699999999998	305.166	305.48500000000001	305.80399999999997	306.12200000000001	306.44099999999997	306.76	307.07900000000001	307.07900000000001	307.39800000000002	307.71699999999998	308.036	308.35500000000002	308.673	308.99200000000002	309.31099999999998	309.31099999999998	309.63	309.94900000000001	310.26799999999997	310.58699999999999	310.90600000000001	310.90600000000001	311.22399999999999	311.54300000000001	311.86200000000002	311.86200000000002	311.86200000000002	311.86200000000002	312.18099999999998	312.18099999999998	312.18099999999998	312.18099999999998	312.18099999999998	312.18099999999998	311.86200000000002	311.86200000000002	311.86200000000002	311.54300000000001	311.54300000000001	311.22399999999999	311.22399999999999	310.90600000000001	310.58699999999999	310.58699999999999	310.26799999999997	309.94900000000001	309.63	309.31099999999998	308.99200000000002	308.673	308.673	308.35500000000002	308.036	307.71699999999998	307.39800000000002	307.39800000000002	307.07900000000001	306.76	306.44099999999997	306.44099999999997	306.12200000000001	305.80399999999997	305.80399999999997	305.48500000000001	305.48500000000001	305.166	304.84699999999998	304.84699999999998	304.52800000000002	304.52800000000002	304.209	304.209	303.89	303.89	303.89	303.57100000000003	303.57100000000003	303.25299999999999	303.25299999999999	303.25299999999999	302.93400000000003	302.93400000000003	302.61500000000001	302.61500000000001	302.61500000000001	302.29599999999999	302.29599999999999	302.29599999999999	302.29599999999999	301.97699999999998	301.97699999999998	301.97699999999998	301.65800000000002	301.65800000000002	301.65800000000002	301.65800000000002	301.339	301.339	301.339	301.339	301.02	301.02	301.02	301.02	300.702	300.702	300.702	300.38299999999998	300.38299999999998	300.38299999999998	300.38299999999998	300.06400000000002	300.06400000000002	300.06400000000002	300.06400000000002	299.745	299.745	299.745	299.42599999999999	299.42599999999999	299.42599999999999	299.42599999999999	299.10700000000003	299.10700000000003	299.10700000000003	299.10700000000003	299.10700000000003	298.78800000000001	298.78800000000001	298.78800000000001	298.78800000000001	298.78800000000001	298.46899999999999	298.46899999999999	298.46899999999999	298.46899999999999	298.46899999999999	298.15100000000001	298.15100000000001	298.15100000000001	298.15100000000001	298.15100000000001	297.83199999999999	297.83199999999999	297.83199999999999	297.83199999999999	297.83199999999999	297.83199999999999	297.51299999999998	297.51299999999998	297.51299999999998	297.51299999999998	297.51299999999998	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	297.19400000000002	296.875	296.875	296.875	296.875	296.875	296.875	296.55599999999998	296.55599999999998	296.55599999999998	296.55599999999998	296.55599999999998	296.55599999999998	296.23700000000002	296.23700000000002	296.23700000000002	296.23700000000002	296.23700000000002	296.23700000000002	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.91800000000001	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.59899999999999	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	295.28100000000001	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.96199999999999	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.64299999999997	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.32400000000001	294.005	294.005	294.005	294.005	294.005	294.005	294.005	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.68599999999998	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.36700000000002	293.048	293.048	293.048	293.048	293.048	293.048	293.048	293.048	292.73	292.73	292.73	292.73	292.73	292.73	292.73	292.73	292.73	292.411	292.411	292.411	292.411	292.411	292.411	292.411	292.411	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	292.09199999999998	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.77300000000002	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.45400000000001	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	291.13499999999999	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.81599999999997	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.49700000000001	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	290.17899999999997	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.86	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.541	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	289.22199999999998	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.90300000000002	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.584	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	288.26499999999999	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.94600000000003	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.62799999999999	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	287.30900000000003	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.99	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.67099999999999	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.35199999999998	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	286.03300000000002	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.714	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.39499999999998	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	285.077	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.75799999999998	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.43900000000002	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	284.12	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.80099999999999	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.48200000000003	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	283.16300000000001	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.84399999999999	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.20699999999999	282.52499999999998	282.52499999999998	282.52499999999998	282.52499999999998	282.84399999999999	282.84399999999999	282.84399999999999	283.16300000000001	283.16300000000001	283.48200000000003	283.48200000000003	283.80099999999999	284.12	284.43900000000002	284.43900000000002	284.75799999999998	285.077	285.39499999999998	285.714	286.35199999999998	286.99	287.62799999999999	288.26499999999999	289.22199999999998	290.17899999999997	291.45400000000001	292.411	293.68599999999998	294.64299999999997	295.59899999999999	296.875	298.15100000000001	299.10700000000003	301.02	302.29599999999999	303.57100000000003	304.52800000000002	306.12200000000001	307.39800000000002	308.99200000000002	310.26799999999997	311.54300000000001	313.13799999999998	314.09399999999999	316.00799999999998	317.60199999999998	318.87799999999999	320.15300000000002	322.06599999999997	323.34199999999998	325.255	326.53100000000001	328.125	330.03800000000001	331.31400000000002	333.22699999999998	334.82100000000003	336.09699999999998	337.37200000000001	339.60500000000002	340.88	342.47399999999999	343.75	345.02499999999998	346.93900000000002	348.53300000000002	349.80900000000003	351.084	353.31599999999997	354.59199999999998	356.18599999999998	357.78100000000001	359.05599999999998	360.65100000000001	362.88299999999998	364.47699999999998	366.07100000000003	367.666	368.94099999999997	370.536	372.13	374.36200000000002	375.63799999999998	377.23200000000003	378.827	380.10199999999998	381.69600000000003	382.97199999999998	384.56599999999997	385.84199999999998	388.07400000000001	389.34899999999999	390.625	391.90100000000001	393.17599999999999	394.452	395.72699999999998	397.00299999999999	398.27800000000002	399.55399999999997	400.51	401.786	402.74200000000002	404.01799999999997	404.97399999999999	405.93099999999998	406.88799999999998	407.84399999999999	408.80099999999999	409.75799999999998	410.714	Percentage Strain (%)


Stress (MPa)




Weave Comparison - Flax Woven vs Non Woven Bioresin
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Carbon Epoxy Stress vs Strain
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Carbon Non-Woven Bioresin Stress vs Strain
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Flax Woven Bioresin Stress vs Strain
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Flax Non Woven Bioresin Stress vs Strain
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Fig. 3. Environmental analysis of carbon fibers composites and biocomposites.
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Material Cross-Sectional Area (mm*2)
Aluminium 22.50
Carbon Twill Epoxy 10.88
Carbon Twill Bioresin 10.22
Carbon Non-Woven Bioresin 19.84
Flax Twill Bioresin 25.50
Flax Non-woven Bioresin 23.76
Kevlar 15.68
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Experimental

EZ Composites / Literature

UTS (MPa) | Failure Strain% | YM(GPa) UTS (MPa) YM (GPa)

A 114.89 20.40 46.98 | 100.00 - 135.00 69.00
Carbon Epoxy 373.46 173 55.09 N/A 6.12-118.55
Carbon Woven Bio 410.71 2.00 57.49 N/A 6.00-118.52
Carbon Non WovenBio | 136.54 2.27 11.77 | 290.00-330.00 | 25.00 - 35.00

FlaxWoven Bio 90.78 3.78 5.81 58.00-61.00 | 6.00-7.00

Flax Non Woven Bio 88.56 4.46 6.58 37.00 - 44.00 5.00

Kevlar 286.6 4.24 12.96 N/A 13.93 - 16.00
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AVG MIN MAX STD DEV CofV AVG MIN MAX STD DEV CofV

Carbon Epoxy 332.32 123.08 487.31 89.71 26.99 55.11 37.08 70.00 7.86 14.26

Carbon Woven Bio 341.77 78.89 751.16 169.07 49.47 55.33 26.40 96.53 15.67 28.33

Carbon Non Woven Bio 168.70 42.54 261.78 54.77 32.46 15.40 3.76 41.90 10.69 69.40

Flax Woven Bio 69.77 19.81 100.33 27.45 39.34 1.79 1.37 2.14 0.24 13.51

Flax Non Woven Bio 31.91 10.83 67.06 16.08 50.38 5.33 0.19 11.61 3.35 62.75

Kevlar 266.17 112.78 373.72 89.26 33.53 22.85 7.27 55.05 12.58 55.06

Youngs Modulus (GPa) UTS (MPa)
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Composite Type  UTS Youngs Modulus Sustainability Implementation ease

Carbon Epoxy 5 5 1 5

Carbon Woven Bio 5 5 3 4

Carbon Non Woven Bio 2 2 3 4

Flax Woven Bio 2 1 4 2

Flax Non Woven Bio 1 1 5 2

Kevlar 3 2 2 3

Material Property vs Sustainability Ranking /5
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1050A (S1B) _SMITIIS

Chemical Composition (weight %)

Al Si Fe Cu Mn Mg Zn Ti Others (ea)
Min 99.50
Max 0.25 0.40 0.05 0.05 0.05 0.07 0.05 0.03

Typical Mechanical Properties

Tensile strength N/mm? 100-135

Yield strength N/mm? Min 75 (approx. only)
Shear strength N/mm? 70

Elongation % (AS0) 4-8

Brinell Hardness HB 35

Thermal conductivity W/m.K 229

Melting range SC 645-657

Electrical conductivity % IACS 58.4

Coefficient of thermal expansion 1/K 23.5x106

Elastic modulus MPa 69000

The mechanical properties of (unalloyed) 1050A are low. The corollary of this is the good forming properties of this grade.
If both forming and higher mechanical properties are required then we recommend the potential selection of grades
3103 (NS3) or 5251 (NS4). In general, the better mechanical properties the lower the formability.




