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Tensile testing is a method of testing a specimen’s mechanical properties. Tensile test is a form of destructive testing which shows how a material will react to stresses given upon it until point of failure [1].  Tensile testing is one of the most popular ways to determine the structure of a material.  A massive benefit of tensile testing is the high productivity rate, this is highly important in the steel industry due to the large number of volumes produced which requires quick and accurate testing. Another large benefit is the vast amount of information that can be created from on single tensile test [2]. Again, this is important in the steel industry as automotive customer are particular with mechanical properties. For example, an interstitial free steel that is going to be pressed will need a high elongation value so it doesn’t crack under the load it will be placed under [3]. Another example is on a dual phase steel, the ultimate tensile strength needs to be high as this steel will go into a pillar of a car which is integral to the structural support of the vehicle [4]. The tensile test derives this information by pulling a specimen at a set load for a constant rate until it fractures. From the data provided, stress and strain graphs are generated using calculations which can be worked out by simple equations. A materials UTS and YPE can be displayed [2]. 

A Denison tensile testing machine will be used in this report to analyse various specimens.  The type of Denison tensile testing machine being used is a top fixed machine. This implies that the top of the machine is fixed and the lower body will move on a slider towards the floor. This will in effect create the tensile tension while the sample remains clamped in the jaws. The tests that will be completed in this experiment will have a 40mm gap between the jaws. The main body runs on a slider to cause tensile tension in the sample held in the jaws. All tests are used with a 40mm gap between the jaws. The software that is used is the Max test software programme. The setting used is the “stop and destroy” which tells the machine to stop pulling after there is no tension left in the machine. 

In this experiment the materials that are being used are Specimen A (0.1% carbon steel), Specimen C (0.29% carbon steel), Specimen W (Copper), Specimen X (Brass) and specimen R (Aluminium). In this experiment only metals are being examined, composites and plastics can also undergo a tensile test to show their mechanical properties. However, of the materials that are being examined two of which are ferrous and three are nonferrous.  Ferrous material is made with iron and nonferrous is material made without iron.
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[bookmark: _Toc73694754]Figure 1 - 0.1% vs 0.29% carbon steels load vs extension
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[bookmark: _Toc73694755]Figure 2 - Elastic region of 0.1% and 0.29% carbon steels


[bookmark: _Toc73694756]Figure 3 - Stress-strain graph for 0.1% and 0.29% carbon steels

[bookmark: _Toc73694757]Figure 4 Calculating the slope of the elastic region

[bookmark: _Toc73694758]Figure 5 0.2% offset proof stress

[bookmark: _Toc73694759]Figure 6 - Stress-strain graph for all materials tested



	
	Diameter
	12.72

	Area
	127.076166

	Gauge length
	54

	Fracture area of A
	43.5915616

	Fracture area of C
	43.5915616
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Youngs Modulus of A 
Youngs modulus	 = Stess/Strain = 59.18 MPa/0.027
			= 2.19 GPa
			
		
Youngs Modulus of C 
Youngs modulus 	= Stress/Strain = 59.18 MPa/0.027
			= 2.19 GPa

UTS of A = Maximium stress = 130.5MPa
UTS of C = Maximium stress = 133.19MPa

Sample A – Upper yeild point = 125.20MPa
Sample A – Lower yeild point = 124.14MPa

Sample C – No upper or lower yeild point on this curve.

Used the 0.2% offset rule to calculate the proof stress.

The slope of the elastic region was calculated which gave a result of 2068.38. This was then multiplied by the original stress results to give 0.2% stress readings. The 0.2% strain readings were calculated by adding 0.002 to the original strain calcultions. This data was then plotted on a scatter diagram. Where the 0.2% trend line crosses the stress strain curve is the proof stress. I enturpreted that is will be 88 MPa by reffering to figure 5.

% Reduction of area 	= (oringal area-area of fracture point)/original area *100
			=(127.08 – 43.59) / 127.08 *100
			= 65.7%

% elongation of sample A 	= (length at fracture – oringinal length) / Original length * 100
				= ( (7.884 + 54) – 54) / 54 *100
				= (61.884 – 54) / 54 * 100
				= 14.6%
% elongation of sample C	=(length at fracture – oringinal length) / Original length * 100				= ( (11.753 + 54) – 54) / 54 *100								=(65.753 – 54) / 54 * 100
				= 21.77%

Nominal stress of sample A at fracture 	= Load / Area before deformation has occurred						= 11.64 KN / 127.08mm2
						= 91.6 MPa
	
Nominal stress of sample C at fracture 	= Load / Area before deformation has occurred						= 13.28 KN / 127.08mm2
						= 104.5 MPa


Actual stress of sample A at fracture 		= Load / Area at fracture									= 11.64 KN / 43.59mm2
						= 267.03 MPa

Actual stress of sample C at fracture 		= Load / Area at fracture
						= 13.28 KN / 43.59mm2
						= 304.66 MPa


[bookmark: _Toc73694761]Figure 8 - Load/extension for all material tested
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The ultimate tensile strength is the maximum stress that can be exhibited on a material on a stress- strain curve. It is the maximum stress that can be introduced in the cross-sectional area when a constant load is applied. For very brittle materials, the UTS point states the separation area on a stress-strain graph.  Formable materials that are ductile, the UTS point shows the area that necking will occur and will then result in fracture as the cross-sectional area decreases [5]. The UTS of the 0.1% carbon steel tested is very high when compared to the other non-ferrous materials tested. Another factor which can affect this is the interstitial bonding of the carbon atoms in the materials lattice. The smaller carbon atoms fit in between the gaps of the iron atoms; these are called interstices [6].

[bookmark: _Toc73694778]Yield strength  

The yield point is the limit of elastic behaviour when referring to the stress-strain diagram. It is usually shown on a stress-strain curve as a sharp bend at the end of the elastic region. After a material passes its yield point it will never return to its original shape as it has now entered the plastic deformation region. A material that has a high yield strength can withstand a high stress without being affected by plastic deformation which is present in strong and brittle materials. If a material has a low yield strength it will display characteristics of a ductile and soft material [7]. 

For materials that do not show a clear end point to the linear trend, a method called an offset calculation can be used to calculate the yield strength. This will be calculated by using the stress-strain curve. A line is offset along the strain axis at 0.2%. The offset yield point is determined as the point of intersection between this line and the original stress-strain curve [8].

[bookmark: _Toc73694779]Youngs modulus

Youngs modulus is the constant that correlates the proportion of stress vs strain when being placed under elastic deformation. This factor can be seen at the beginning of the stress vs strain curve where the trend follows a linear correlation. Youngs modulus can be calculated by dividing stress over strain. Youngs modulus is a critical component when analysing the stiffness of a material. If the young’s modulus of a material is low or has a relatively flat elastic trend, the material displays ductile and low strength characteristics. If the Young’s modulus of a material is high and has a steep elastic trend, the specimen that is being tested will show characteristics of a brittle and high strength material [9].
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Poisson’s ratio is a term used to identify a materials ductility. This is done via a tensile test where the material in question will experience expansion by tensile forces. To calculate the Poisson’s ratio, you have to divide the transverse strain by the axial strain. Transverse strain is the strain in the direction perpendicular to the force being placed on it and the axial strain is calculated by the direction the force is being applied to it.  If a material exhibits a low Poisson’s ratio this implies that the material is brittle and easy to fracture. However, if a material exhibits a high Poisson’s ratio this implies that it is very ductile and difficult to fracture [10].

[bookmark: _Toc73694781]Plastic deformation

Once a material has reached its elastic limit, further straining will result in permanent deformation. Plastic deformation implies that deformation present after yielding will be permanent and non-recoverable.  The plastic region of the stress-strain curve differs to elastic region as it does not have a linear relationship with stress [11].

[bookmark: _Toc73694782]Hardness

 Hardness of a material is reflected on how much resistance to penetration it exhibits. You are unable to calculate hardness using a stress-strain curve as it must be calculated by using an indenter with a standard load applied. However, hardness has a very close relationship with ultimate tensile strength implying that if a material has a high strength, it will also be very hard [12].

[bookmark: _Toc73694783]Ductility

Ductility is the ability of a material to be plastically deformed without fracture. Ductility is a clear indication of how soft or malleable a material is. Percentage elongation and percentage reduction in area are two ways of showing a materials ductility via a tensile test. If a material exhibits a low ductility, it suggests that it is brittle and will fracture after very little deformation. A high ductility suggests that a material has a high resistance to fracture [13].

[bookmark: _Toc73694784]0.1% carbon steel stress-strain curve analysis

[bookmark: _Toc73694785]Characteristics

· High UTS
· High Yield point
· Brittle 
· Small % elongation


0.1% carbon steel will consist of predominantly of a phase called ferrite. Ferrite is a solid solution phase of carbon dissolved in iron and has a BCC structure. From the stress strain curves it is clear that the 0.1 % carbon steel has a lower ultimate tensile strength than 0.29 % carbon steel. This is down to the lower amount of carbon present which has an impact on the amount of pearlite that can be produced in solution.  Pearlite is overlapping layers of ferrite and cementite which is also known as iron carbide.  When comparing the UTS against the nonferrous metals it is much higher and this is due to the interstitial alloying of carbon and iron. When comparing 0.1% vs 0.29% carbon samples, they both have very similar young’s moduli. This implies that they both behave very similarly while obeying hooke’s law. Hooke’s law explains that the force needed to extend a specimen is proportional to the distance gained [14].  Youngs modulus is an effective way of determining a materials mechanical property in the elastic region. 


[bookmark: _Toc73694786]0.29 % carbon steel stress-strain analysis
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· High UTS strength
· High hardness
· Very ductile
· A high % of elongation

0.29 % carbon steel is a medium carbon steel, this type of steel will have a lower amount of ferrite and more pearlite than a 0.1% carbon steel. Depending on how it was processed it may even contain a small percentage of martensite if it was quenched at a high rate. Studies would usually confirm that an increase in carbon content would show a decrease in ductility. When referring to the stress-strain graph produced this is not the case.  The likely reason of this is due to the alloying elements within the microstructure that have been added which will enhance the ductility and also give a high strength. The 0.29 % carbon steel shows a gradual deviation from linear behaviour as yielding begins.


[bookmark: _Toc73694788]Aluminium stress-strain analysis

[bookmark: _Toc73694789]Characteristics

· The highest young’s modulus
· The highest of the nonferrous UTS
· The most brittle material
· The lowest % elongation
· Brittle fracture

When reflecting on the aluminium tensile result it is clear that it is the strongest of the nonferrous metals tested. It has to be strong due to large use in the construction industry where its only surpassed by steel as the most common structural material. The aluminium specimen doesn’t have a clear yield point so this will need to be calculated using the offset method at 2% strain. Aluminium’s advantage when compared against steel is its weight. An aluminium sheet will weigh a lot lighter than a steel counterpart. Another benefit of aluminium is its corrosion properties.

[bookmark: _Toc73694790]Copper stress-strain analysis

[bookmark: _Toc73694791]Characteristics

· Low UTS
· High region of plastic deformation
· Malleable
· No clear yield point
· Soft material

Copper has the lowest strength of all materials tested.  Similar to aluminium, copper doesn’t have no clear yield point. Referring to the load extension graph, copper has the flattest trend which implies the material exhibits ductile properties. Copper also has one of the largest % elongation of the material tested in this experiment. It is important for copper to be highly malleable due to in the construction industry for plumbing and roofing etc.


[bookmark: _Toc73694792]Brass stress-strain analysis

[bookmark: _Toc73694793]Characteristics

· The second highest strain result produced.
· Ductile
· Brittle fracture 
· Fairly strong material
· Can undertake a large plastic deformation

Brass the second lowest UTS from the material tested in this experiment. From examining the stress-strain curve it is clear that this brass specimen can withstand a large amount of plastic deformation. However, the majority of this plastic deformation is within the strain hardening region. Once the material gets to the ultimate tensile stress limit it fractures implying that a brittle fracture has occurred with no necking.
[bookmark: _Toc73694794]Conclusion

It is clear that the tensile test is imperative to understanding mechanical properties for varying materials. It’s clear through the report that understanding a materials mechanical property is important for the industrial uses of various parts. Understanding that for example, a car door panel needs to be strong enough to keep its passengers safe but at the same time needs a level of ductility to be pressed and formed into the required shape. This report also highlights the importance of understanding materials down to the atomic structure. For example, understanding that steel gets its high strength from the interstitial bonding between the iron and carbon atoms. Also, the effect of how alloying elements can make typically brittle materials more ductile. This is seen with the 0.29 % carbon steel as it has a greater percentage elongation that the 0.1 % carbon steel.
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0.29% carbon steel Proof stress

Elastic	
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Stress MPa




Stress vs stran graph for all materials

0.1% carbon steel	0.0	0.0	3.7037037037037E-5	0.00012962962962963	0.000259259259259259	0.00037037037037037	0.000481481481481481	0.00062962962962963	0.00074074074074074	0.000851851851851852	0.000962962962962963	0.00111111111111111	0.00122222222222222	0.00137037037037037	0.00148148148148148	0.00159259259259259	0.00174074074074074	0.00185185185185185	0.00198148148148148	0.00211111111111111	0.00222222222222222	0.00233333333333333	0.00248148148148148	0.00259259259259259	0.0027037037037037	0.00285185185185185	0.00296296296296296	0.00309259259259259	0.00322222222222222	0.00333333333333333	0.00346296296296296	0.00359259259259259	0.0037037037037037	0.00383333333333333	0.00396296296296296	0.00409259259259259	0.0042037037037037	0.00433333333333333	0.00446296296296296	0.00457407407407407	0.00472222222222222	0.00483333333333333	0.00494444444444444	0.00509259259259259	0.0052037037037037	0.00531481481481481	0.00546296296296296	0.00557407407407407	0.00572222222222222	0.00583333333333333	0.00594444444444444	0.00609259259259259	0.0062037037037037	0.00631481481481481	0.00646296296296296	0.00657407407407407	0.0067037037037037	0.00683333333333333	0.00694444444444444	0.00707407407407407	0.0072037037037037	0.00731481481481481	0.00744444444444444	0.00757407407407407	0.0077037037037037	0.00781481481481481	0.00796296296296296	0.00807407407407407	0.00818518518518518	0.00833333333333333	0.00844444444444444	0.00855555555555555	0.0087037037037037	0.00881481481481481	0.00892592592592592	0.00907407407407407	0.00918518518518518	0.00929629629629629	0.00944444444444444	0.00955555555555555	0.00966666666666666	0.00979629629629629	0.00992592592592592	0.010037037037037	0.0101666666666667	0.0102962962962963	0.0104074074074074	0.010537037037037	0.0106666666666667	0.0107777777777778	0.0109074074074074	0.011037037037037	0.0111481481481481	0.0112962962962963	0.0114074074074074	0.0115185185185185	0.0116481481481481	0.0117777777777778	0.0118888888888889	0.012037037037037	0.0121481481481481	0.0122592592592593	0.0124074074074074	0.0125185185185185	0.0126666666666667	0.0127777777777778	0.0128888888888889	0.013	0.0131481481481481	0.0132592592592593	0.0133703703703704	0.0135185185185185	0.0136296296296296	0.0137407407407407	0.0138888888888889	0.014	0.0141481481481481	0.0142592592592593	0.0143703703703704	0.0145185185185185	0.0146296296296296	0.0147592592592593	0.0148888888888889	0.015	0.0151296296296296	0.0152592592592593	0.0153703703703704	0.0155	0.0156296296296296	0.0157592592592593	0.0158703703703704	0.016	0.0161296296296296	0.0162407407407407	0.0163703703703704	0.0165	0.0166111111111111	0.0167592592592593	0.0168703703703704	0.0169814814814815	0.0171296296296296	0.0172407407407407	0.0173518518518519	0.0175	0.0176111111111111	0.0177592592592593	0.0178703703703704	0.0179814814814815	0.0181296296296296	0.0182407407407407	0.0183703703703704	0.0185	0.0186296296296296	0.0187407407407407	0.0188518518518518	0.019	0.0191111111111111	0.0192592592592593	0.0193703703703704	0.0194814814814815	0.0196296296296296	0.0197407407407407	0.0198703703703704	0.02	0.0201111111111111	0.0202407407407407	0.0203703703703704	0.0205	0.0206111111111111	0.0207592592592593	0.0208703703703704	0.0210185185185185	0.0211296296296296	0.0212407407407407	0.0213888888888889	0.0215	0.0216296296296296	0.0217592592592593	0.0218703703703704	0.022	0.0221296296296296	0.0222592592592593	0.0223703703703704	0.0225185185185185	0.0226296296296296	0.0227407407407407	0.0228703703703704	0.023	0.0231111111111111	0.0232592592592593	0.0233703703703704	0.0235185185185185	0.0236296296296296	0.0237407407407407	0.0238888888888889	0.024	0.0241296296296296	0.0242592592592593	0.0243703703703704	0.0245	0.0246296296296296	0.0247592592592593	0.0248703703703704	0.025	0.0251296296296296	0.0252407407407407	0.0253888888888889	0.0255	0.0256481481481481	0.0257592592592593	0.0258703703703704	0.0259814814814815	0.0261296296296296	0.0262407407407407	0.0263888888888889	0.0265	0.0266296296296296	0.0267592592592593	0.0268703703703704	0.027	0.0271296296296296	0.0272592592592593	0.0273703703703704	0.0275	0.0276296296296296	0.0277407407407407	0.0278703703703704	0.028	0.0281481481481481	0.0282592592592593	0.0283703703703704	0.0285185185185185	0.0286296296296296	0.0287592592592593	0.0288888888888889	0.029	0.0291296296296296	0.0292592592592593	0.0293888888888889	0.0295	0.0296296296296296	0.0297592592592593	0.0298703703703704	0.0300185185185185	0.0301296296296296	0.0302407407407407	0.0303888888888889	0.0305	0.0306481481481481	0.0307592592592593	0.0308703703703704	0.0310185185185185	0.0311296296296296	0.0312592592592593	0.0313888888888889	0.0315	0.0316296296296296	0.0317592592592593	0.0318888888888889	0.032	0.0321296296296296	0.0322592592592593	0.0323703703703704	0.0325	0.0326296296296296	0.0327407407407407	0.0328888888888889	0.033	0.0331481481481481	0.0332592592592593	0.0333888888888889	0.0335185185185185	0.0336296296296296	0.0337592592592593	0.0338888888888889	0.034	0.0341296296296296	0.0342592592592593	0.0343888888888889	0.0345	0.0346296296296296	0.0347592592592593	0.0348703703703704	0.0350185185185185	0.0351296296296296	0.0352407407407407	0.0353888888888889	0.0355	0.0356111111111111	0.0357592592592593	0.0358703703703704	0.0360185185185185	0.0361296296296296	0.0362407407407407	0.0363888888888889	0.0365	0.0366111111111111	0.0367592592592593	0.0368703703703704	0.0369814814814815	0.0371111111111111	0.0372407407407407	0.0373518518518518	0.0374814814814815	0.0376111111111111	0.0377407407407407	0.0378518518518518	0.0379814814814815	0.0381111111111111	0.0382222222222222	0.0383703703703704	0.0384814814814815	0.0385925925925926	0.0387407407407407	0.0388518518518518	0.038962962962963	0.0391111111111111	0.0392222222222222	0.0393333333333333	0.0394814814814815	0.0395925925925926	0.0397407407407407	0.0398518518518518	0.039962962962963	0.0401111111111111	0.0402222222222222	0.0403518518518518	0.0404814814814815	0.0405925925925926	0.0407222222222222	0.0408518518518518	0.040962962962963	0.0410925925925926	0.0412222222222222	0.0413333333333333	0.041462962962963	0.0415925925925926	0.0417222222222222	0.0418333333333333	0.041962962962963	0.0420740740740741	0.0422037037037037	0.0423333333333333	0.042462962962963	0.0425740740740741	0.0427222222222222	0.0428333333333333	0.0429814814814815	0.0430925925925926	0.0432037037037037	0.0433518518518518	0.043462962962963	0.0435740740740741	0.0437222222222222	0.0438333333333333	0.043962962962963	0.0440925925925926	0.0442222222222222	0.0443333333333333	0.044462962962963	0.0445925925925926	0.0447037037037037	0.0448333333333333	0.044962962962963	0.0450740740740741	0.0452222222222222	0.0453333333333333	0.0454444444444444	0.0455925925925926	0.0457037037037037	0.0458518518518518	0.045962962962963	0.0460740740740741	0.0462222222222222	0.0463333333333333	0.046462962962963	0.0465925925925926	0.0467037037037037	0.0468333333333333	0.046962962962963	0.0470925925925926	0.0472037037037037	0.0473333333333333	0.047462962962963	0.0475740740740741	0.0477222222222222	0.0478333333333333	0.0479444444444444	0.0480925925925926	0.0482222222222222	0.0483518518518518	0.048462962962963	0.0485740740740741	0.0487222222222222	0.0488333333333333	0.048962962962963	0.0490925925925926	0.0492037037037037	0.0493333333333333	0.0494629629629629	0.0495740740740741	0.0497037037037037	0.0498333333333333	0.0499629629629629	0.0500740740740741	0.0502037037037037	0.0503333333333333	0.0504444444444444	0.0505740740740741	0.0507037037037037	0.0508518518518518	0.0509629629629629	0.0510740740740741	0.0512222222222222	0.0513333333333333	0.0514444444444444	0.0515925925925926	0.0517037037037037	0.0518333333333333	0.051962962962963	0.0520740740740741	0.0522037037037037	0.0523333333333333	0.0524444444444444	0.0525740740740741	0.0527037037037037	0.0528333333333333	0.0529444444444444	0.0530925925925926	0.0532037037037037	0.0533518518518518	0.053462962962963	0.0535740740740741	0.0537222222222222	0.0538333333333333	0.0539444444444444	0.0540925925925926	0.0542037037037037	0.0543148148148148	0.054462962962963	0.0545740740740741	0.0547037037037037	0.0548333333333333	0.0549444444444444	0.0550740740740741	0.0552037037037037	0.0553333333333333	0.0554444444444444	0.0555555555555555	0.0557037037037037	0.0558148148148148	0.0559629629629629	0.0560740740740741	0.0561851851851852	0.0563333333333333	0.0564444444444444	0.0565740740740741	0.0567037037037037	0.0568148148148148	0.0569444444444444	0.0570740740740741	0.0572037037037037	0.0573148148148148	0.057462962962963	0.0575740740740741	0.0576851851851852	0.0578333333333333	0.0579444444444444	0.0580925925925926	0.0582037037037037	0.0583333333333333	0.058462962962963	0.0585740740740741	0.0587037037037037	0.0588333333333333	0.0589444444444444	0.0590740740740741	0.0592037037037037	0.0593148148148148	0.0594444444444444	0.0595740740740741	0.0597037037037037	0.0598148148148148	0.0599444444444444	0.0600740740740741	0.0601851851851852	0.0603333333333333	0.0604444444444444	0.0605925925925926	0.0607037037037037	0.0608148148148148	0.0609629629629629	0.0610740740740741	0.0611851851851852	0.0613333333333333	0.0614444444444444	0.0615740740740741	0.0617037037037037	0.0618148148148148	0.0619444444444444	0.0620740740740741	0.0622037037037037	0.0623148148148148	0.0624444444444444	0.0625740740740741	0.0626851851851852	0.0628148148148148	0.0629444444444444	0.0630555555555555	0.0632037037037037	0.0633148148148148	0.0634259259259259	0.0635555555555555	0.0636851851851852	0.0637962962962963	0.0639259259259259	0.0640555555555555	0.0641666666666667	0.0642962962962963	0.0644259259259259	0.064537037037037	0.0646851851851852	0.0647962962962963	0.0649074074074074	0.0650555555555555	0.0651666666666667	0.0652777777777778	0.0654259259259259	0.065537037037037	0.0656481481481481	0.0657962962962963	0.0659074074074074	0.0660185185185185	0.0661666666666667	0.0662777777777778	0.0664259259259259	0.066537037037037	0.0666481481481481	0.0667962962962963	0.0669074074074074	0.0670185185185185	0.0671666666666667	0.0672777777777778	0.0673888888888889	0.067537037037037	0.0676481481481481	0.0677777777777778	0.0679074074074074	0.0680185185185185	0.0681481481481481	0.0682777777777778	0.0684074074074074	0.0685185185185185	0.0686481481481481	0.0687777777777778	0.0688888888888889	0.0690185185185185	0.0691481481481481	0.0692592592592592	0.0693888888888889	0.0695185185185185	0.0696296296296296	0.0697777777777778	0.0698888888888889	0.07	0.0701481481481481	0.0702592592592593	0.0703703703703704	0.0705185185185185	0.0706296296296296	0.0707777777777778	0.0708888888888889	0.071	0.0711481481481481	0.0712592592592593	0.0713703703703704	0.0715185185185185	0.0716296296296296	0.0717407407407407	0.0718888888888889	0.072	0.0721296296296296	0.0722592592592593	0.0723703703703704	0.0725	0.0726296296296296	0.0727592592592593	0.0728703703703704	0.073	0.0731296296296296	0.0732407407407407	0.0733888888888889	0.0735	0.0736111111111111	0.0737407407407407	0.0738703703703704	0.0739814814814815	0.0741296296296296	0.0742407407407407	0.0743518518518518	0.0745	0.0746111111111111	0.0747222222222222	0.0748703703703704	0.0749814814814815	0.0751111111111111	0.0752407407407407	0.0753518518518518	0.075462962962963	0.0756111111111111	0.0757222222222222	0.0758333333333333	0.0759814814814815	0.0760925925925926	0.0762037037037037	0.0763518518518518	0.0764629629629629	0.0765925925925926	0.0767222222222222	0.0768333333333333	0.0769629629629629	0.0770925925925926	0.0772222222222222	0.0773333333333333	0.0774629629629629	0.0775925925925926	0.0777037037037037	0.0778518518518518	0.0779629629629629	0.0780740740740741	0.0782222222222222	0.0783333333333333	0.0784444444444444	0.0785925925925926	0.0787037037037037	0.0788148148148148	0.078962962962963	0.0790740740740741	0.0791851851851852	0.0793333333333333	0.0794444444444444	0.0795925925925926	0.0797037037037037	0.0798333333333333	0.0799629629629629	0.0800740740740741	0.0802037037037037	0.0803333333333333	0.0804444444444444	0.0805740740740741	0.0807037037037037	0.0808333333333333	0.0809444444444444	0.0810740740740741	0.0812037037037037	0.0813148148148148	0.0814629629629629	0.0815740740740741	0.0816851851851852	0.0818333333333333	0.0819444444444444	0.0820925925925926	0.0822037037037037	0.0823333333333333	0.082462962962963	0.0825925925925926	0.0827037037037037	0.0828333333333333	0.082962962962963	0.083074074074074	0.0832037037037037	0.0833333333333333	0.0834444444444444	0.0835925925925926	0.0837037037037037	0.0838518518518518	0.0839629629629629	0.0840925925925926	0.0842222222222222	0.0843333333333333	0.0844629629629629	0.0845925925925926	0.0847222222222222	0.0848333333333333	0.0849629629629629	0.0850925925925926	0.0852037037037037	0.0853518518518518	0.0854629629629629	0.0855740740740741	0.0857222222222222	0.0858333333333333	0.0859814814814815	0.0860925925925926	0.0862222222222222	0.0863518518518518	0.0864629629629629	0.0865925925925926	0.0867222222222222	0.0868518518518518	0.0869629629629629	0.0871111111111111	0.0872222222222222	0.0873333333333333	0.0874629629629629	0.0875925925925926	0.0877037037037037	0.0878518518518518	0.0879629629629629	0.0880740740740741	0.0882222222222222	0.0883333333333333	0.0884444444444444	0.0885925925925926	0.0887037037037037	0.0888148148148148	0.0889629629629629	0.0890740740740741	0.0891851851851852	0.0893333333333333	0.0894444444444444	0.0895925925925926	0.0897037037037037	0.0898148148148148	0.0899629629629629	0.090074074074074	0.0901851851851852	0.0903333333333333	0.0904444444444444	0.090574074074074	0.0907037037037037	0.0908148148148148	0.0909444444444444	0.091074074074074	0.0912037037037037	0.0913148148148148	0.0914444444444444	0.0915740740740741	0.0916851851851852	0.0918148148148148	0.0919444444444444	0.0920555555555555	0.0922037037037037	0.0923148148148148	0.0924259259259259	0.092574074074074	0.0926851851851852	0.0928148148148148	0.0929444444444444	0.0930555555555555	0.0931851851851852	0.0933148148148148	0.0934259259259259	0.0935555555555555	0.0936851851851852	0.0937962962962963	0.0939259259259259	0.0940555555555555	0.0941851851851852	0.0942962962962963	0.0944259259259259	0.0945555555555555	0.0946666666666666	0.0947962962962963	0.0949259259259259	0.095037037037037	0.0951851851851852	0.0952962962962963	0.0954074074074074	0.0955555555555555	0.0956666666666667	0.0958148148148148	0.0959259259259259	0.096037037037037	0.0961851851851852	0.0962962962962963	0.0964074074074074	0.0965555555555555	0.0966666666666666	0.0967777777777778	0.0969259259259259	0.097037037037037	0.0971666666666666	0.0972962962962963	0.0974074074074074	0.097537037037037	0.0976666666666666	0.0977777777777778	0.0979074074074074	0.098037037037037	0.0981666666666666	0.0982777777777778	0.0984259259259259	0.098537037037037	0.0986481481481481	0.0987962962962963	0.0989074074074074	0.0990555555555555	0.0991666666666667	0.0992777777777777	0.0993888888888889	0.099537037037037	0.0996481481481481	0.0997592592592592	0.0999074074074074	0.100018518518519	0.100166666666667	0.100277777777778	0.100388888888889	0.1005	0.100648148148148	0.100759259259259	0.10087037037037	0.101018518518519	0.10112962962963	0.101277777777778	0.101388888888889	0.1015	0.101648148148148	0.101759259259259	0.10187037037037	0.102018518518519	0.10212962962963	0.102240740740741	0.102388888888889	0.1025	0.102611111111111	0.102759259259259	0.10287037037037	0.103	0.10312962962963	0.103240740740741	0.103351851851852	0.1035	0.103611111111111	0.103722222222222	0.10387037037037	0.103981481481481	0.104092592592593	0.104240740740741	0.104351851851852	0.104481481481481	0.104611111111111	0.104722222222222	0.104851851851852	0.104981481481481	0.105092592592593	0.105222222222222	0.105351851851852	0.105462962962963	0.105592592592593	0.105722222222222	0.105851851851852	0.105962962962963	0.106092592592593	0.106222222222222	0.106333333333333	0.106462962962963	0.106592592592593	0.106703703703704	0.106851851851852	0.106962962962963	0.107074074074074	0.107222222222222	0.107333333333333	0.107481481481481	0.107592592592593	0.107703703703704	0.107851851851852	0.107962962962963	0.108074074074074	0.108222222222222	0.108333333333333	0.108462962962963	0.108592592592593	0.108703703703704	0.108833333333333	0.108962962962963	0.109092592592593	0.109203703703704	0.109351851851852	0.109462962962963	0.109574074074074	0.109722222222222	0.109833333333333	0.109944444444444	0.110092592592593	0.110203703703704	0.110351851851852	0.110462962962963	0.110592592592593	0.110722222222222	0.110833333333333	0.110962962962963	0.111092592592593	0.111222222222222	0.111333333333333	0.111481481481481	0.111592592592593	0.111703703703704	0.111851851851852	0.111962962962963	0.112092592592593	0.112222222222222	0.112333333333333	0.112462962962963	0.112592592592593	0.112703703703704	0.112833333333333	0.112962962962963	0.113092592592593	0.113203703703704	0.113351851851852	0.113462962962963	0.113574074074074	0.113722222222222	0.113833333333333	0.113944444444444	0.114092592592593	0.114203703703704	0.114314814814815	0.114462962962963	0.114574074074074	0.114722222222222	0.114833333333333	0.114944444444444	0.115092592592593	0.115203703703704	0.115314814814815	0.115462962962963	0.115574074074074	0.115703703703704	0.115833333333333	0.115944444444444	0.116074074074074	0.116203703703704	0.116314814814815	0.116444444444444	0.116574074074074	0.116703703703704	0.116814814814815	0.116944444444444	0.117074074074074	0.117185185185185	0.117314814814815	0.117444444444444	0.117555555555556	0.117703703703704	0.117814814814815	0.117925925925926	0.118074074074074	0.118185185185185	0.118333333333333	0.118444444444444	0.118555555555556	0.118703703703704	0.118814814814815	0.118925925925926	0.119074074074074	0.119185185185185	0.119314814814815	0.119444444444444	0.119555555555556	0.119685185185185	0.119814814814815	0.119925925925926	0.120055555555556	0.120185185185185	0.120314814814815	0.120425925925926	0.120574074074074	0.120685185185185	0.120796296296296	0.120944444444444	0.121055555555556	0.121203703703704	0.121314814814815	0.121425925925926	0.121574074074074	0.121685185185185	0.121814814814815	0.121944444444444	0.122055555555556	0.122185185185185	0.122314814814815	0.122425925925926	0.122555555555556	0.122685185185185	0.122796296296296	0.122925925925926	0.123055555555556	0.123185185185185	0.123296296296296	0.123425925925926	0.123555555555556	0.123666666666667	0.123796296296296	0.123925925925926	0.124037037037037	0.124185185185185	0.124296296296296	0.124444444444444	0.124555555555556	0.124666666666667	0.124814814814815	0.124925925925926	0.125037037037037	0.125185185185185	0.125296296296296	0.125425925925926	0.125555555555556	0.125666666666667	0.125796296296296	0.125925925925926	0.126037037037037	0.126166666666667	0.126296296296296	0.126407407407407	0.126537037037037	0.126666666666667	0.126777777777778	0.126888888888889	0.127037037037037	0.127148148148148	0.127277777777778	0.127407407407407	0.127518518518519	0.127648148148148	0.127777777777778	0.127888888888889	0.128018518518519	0.128148148148148	0.128259259259259	0.128388888888889	0.128518518518519	0.12862962962963	0.128759259259259	0.128888888888889	0.129	0.12912962962963	0.129259259259259	0.129388888888889	0.1295	0.12962962962963	0.129759259259259	0.12987037037037	0.129981481481481	0.13012962962963	0.130240740740741	0.130388888888889	0.1305	0.130611111111111	0.130759259259259	0.13087037037037	0.131	0.13112962962963	0.131240740740741	0.13137037037037	0.1315	0.13162962962963	0.131740740740741	0.13187037037037	0.132	0.132111111111111	0.132259259259259	0.13237037037037	0.132481481481481	0.13262962962963	0.132740740740741	0.132851851851852	0.133	0.133111111111111	0.133259259259259	0.13337037037037	0.133481481481481	0.13362962962963	0.133740740740741	0.13387037037037	0.134	0.13412962962963	0.134240740740741	0.134388888888889	0.1345	0.134611111111111	0.134759259259259	0.13487037037037	0.135018518518519	0.13512962962963	0.135240740740741	0.135388888888889	0.1355	0.13562962962963	0.135759259259259	0.135888888888889	0.136	0.136148148148148	0.136259259259259	0.13637037037037	0.136518518518518	0.13662962962963	0.136777777777778	0.136888888888889	0.137	0.137148148148148	0.137259259259259	0.137388888888889	0.137518518518518	0.137648148148148	0.137759259259259	0.137888888888889	0.138018518518518	0.13812962962963	0.138277777777778	0.138388888888889	0.1385	0.138648148148148	0.138759259259259	0.13887037037037	0.139018518518518	0.13912962962963	0.139240740740741	0.139388888888889	0.1395	0.139648148148148	0.139759259259259	0.13987037037037	0.140018518518519	0.14012962962963	0.140259259259259	0.140388888888889	0.140518518518519	0.14062962962963	0.140759259259259	0.140888888888889	0.141	0.141148148148148	0.141259259259259	0.14137037037037	0.141518518518519	0.14162962962963	0.141740740740741	0.141888888888889	0.142	0.142148148148148	0.142259259259259	0.14237037037037	0.142518518518519	0.14262962962963	0.142740740740741	0.142888888888889	0.143	0.14312962962963	0.143259259259259	0.143388888888889	0.1435	0.14362962962963	0.143759259259259	0.14387037037037	0.144	0.14412962962963	0.144240740740741	0.144388888888889	0.1445	0.144611111111111	0.144759259259259	0.14487037037037	0.145018518518519	0.14512962962963	0.145240740740741	0.145388888888889	0.1455	0.14562962962963	0.145759259259259	0.145888888888889	0.146	0.146240740740741	0.146351851851852	0.146462962962963	0.146592592592593	0.146703703703704	0.146833333333333	0.146962962962963	0.147092592592593	0.147203703703704	0.147333333333333	0.147462962962963	0.147574074074074	0.147722222222222	0.147833333333333	0.147944444444444	0.148092592592593	0.148203703703704	0.148333333333333	0.148462962962963	0.148592592592593	0.148703703703704	0.148833333333333	0.148962962962963	0.149074074074074	0.149222222222222	0.149333333333333	0.149444444444444	0.149592592592593	0.149703703703704	0.149851851851852	0.149962962962963	0.150074074074074	0.150222222222222	0.150333333333333	0.150462962962963	0.150592592592593	0.150703703703704	0.150833333333333	0.150962962962963	0.151074074074074	0.151203703703704	0.151333333333333	0.151444444444444	0.151574074074074	0.151703703703704	0.151833333333333	0.151944444444444	0.152074074074074	0.152185185185185	0.152314814814815	0.152444444444444	0.152574074074074	0.152685185185185	0.152833333333333	0.152944444444444	0.153055555555556	0.153185185185185	0.153314814814815	0.153425925925926	0.153555555555556	0.153685185185185	0.153777777777778	0.153888888888889	0.154037037037037	0.154166666666667	0.154296296296296	0.154407407407407	0.154537037037037	0.154666666666667	0.154777777777778	0.0	-0.0786929626458088	-0.0786929626458088	-0.0786929626458088	-0.0786929626458088	-0.0786929626458088	-0.0393464813229044	-0.0393464813229044	-0.0393464813229044	0.0	0.0	0.0393464813229044	0.0393464813229044	0.0786929626458088	0.118039443968713	0.118039443968713	0.157385925291618	0.236078887937426	0.275425369260331	0.354118331906139	0.432811294551948	0.511504257197757	0.62954370116647	0.786929626458088	0.904969070426801	1.101701477041323	1.298433883655845	1.534512771593271	1.809938140853602	2.164056472759742	2.518174804665881	2.911639617894925	3.305104431123969	3.737915725675916	4.05268757625915	4.288766464196577	4.682231277425621	5.075696090654667	5.351121459914997	5.74458627314404	6.216744049018892	6.531515899602128	7.003673675476981	7.35779200738312	7.90864274590378	8.302107559132826	8.69557237236187	9.285769592205436	9.67923440543448	10.11204569998643	10.7415894011529	11.13505421438194	11.56786550893389	11.96133032216293	12.5908740233294	12.98433883655845	13.4171501311104	13.84996142566234	14.28277272021429	14.91231642138076	15.34512771593271	15.77793901048466	16.21075030503661	16.64356159958855	17.11571937546341	17.54853067001535	18.21742085250473	18.68957862837959	19.12238992293153	19.59454769880638	20.06670547468124	20.49951676923319	20.97167454510804	21.40448583965999	21.87664361553484	22.3094549100868	23.01769157389907	23.45050286845101	23.92266064432586	24.35547193887782	24.82762971475267	25.26044100930462	25.69325230385656	26.12606359840851	26.55887489296046	26.95233970618951	27.38515100074146	27.8179622952934	28.29012007116824	28.7229313657202	29.11639617894925	29.54920747350118	29.98201876805314	30.4148300626051	30.80829487583414	31.4378385770006	31.83130339022965	32.2247682034587	32.61823301668774	33.01169782991677	33.40516264314582	33.79862745637487	34.19209226960391	34.58555708283296	34.979021896062	35.37248670929104	35.7659515225201	36.15941633574914	36.51353466765526	36.90699948088432	37.26111781279045	37.6152361446966	38.00870095792564	38.36281928983177	38.67759114041501	39.03170947232115	39.38582780422728	39.73994613613343	40.05471798671666	40.4088363186228	40.72360816920605	41.03838001978928	41.3531518703725	41.66792372095575	41.98269557153898	42.29746742212222	42.61223927270545	42.88766464196577	43.16309001122612	43.47786186180934	43.75328723106967	44.02871260033	44.30413796959034	44.57956333885067	44.8156422267881	45.09106759604842	45.36649296530876	45.60257185324618	45.87799722250652	46.15342259176684	46.38950147970426	46.6255803676417	46.86165925557913	47.09773814351655	47.33381703145398	47.56989591939141	47.80597480732883	48.04205369526625	48.23878610188077	48.47486498981819	48.67159739643273	48.90767628437015	49.10440869098468	49.30114109759919	49.53721998553662	49.73395239215115	49.93068479876566	50.1274172053802	50.36349609331759	50.56022849993214	50.75696090654665	50.95369331316117	51.18977220109861	51.38650460771311	51.58323701432764	51.77996942094217	51.9767018275567	52.17343423417121	52.33082015946283	52.33082015946283	52.13408775284831	52.09474127152541	52.37016664078574	52.68493849136897	52.9997103419522	53.23578922988964	53.47186811782705	53.70794700576448	53.904679412379	54.10141181899353	54.29814422560805	54.49487663222257	54.6916090388371	54.88834144545162	55.04572737074324	55.24245977735776	55.43919218397228	55.6359245905868	55.83265699720133	55.99004292249294	56.18677532910747	56.383507735722	56.54089366101359	56.73762606762812	56.89501199291975	57.09174439953427	57.2491303248259	57.4458627314404	57.64259513805493	57.83932754466944	57.91802050731525	58.1147529139298	58.3114853205443	58.50821772715882	58.70495013377334	58.90168254038787	59.0984149470024	59.2951473536169	59.49187976023142	59.68861216684595	59.88534457346046	60.082076980075	60.27880938668952	60.43619531198113	60.63292771859566	60.82966012521017	61.06573901314761	61.26247141976214	61.45920382637664	61.65593623299118	61.8526686396057	62.04940104622022	62.16744049018893	62.36417289680345	62.56090530341797	62.75763771003249	62.95437011664701	63.15110252326154	63.34783492987606	63.58391381781349	63.78064622442801	63.97737863104253	64.13476455633415	64.33149696294867	64.44953640691738	64.56757585088609	64.6856152948548	64.84300122014643	65.03973362676095	65.27581251469836	65.4725449213129	65.70862380925032	65.94470269718776	66.14143510380228	66.3775139917397	66.57424639835421	66.77097880496873	66.96771121158325	67.20379009952067	67.40052250613521	67.59725491274973	67.79398731936425	67.9907197259788	68.18745213259328	68.3448380578849	68.50222398317654	68.65960990846815	68.81699583375976	68.93503527772847	69.09242120302011	69.28915360963462	69.48588601624914	69.72196490418657	69.91869731080108	70.11542971741561	70.35150860535304	70.54824101196756	70.7449734185821	71.05974526916531	71.25647767577985	71.49255656371728	71.68928897033179	71.8860213769463	72.08275378356082	72.27948619017535	72.47621859678986	72.67295100340438	72.86968341001892	73.10576229795633	73.30249470457088	73.4992271111854	73.69595951779989	73.89269192441444	74.08942433102897	74.28615673764348	74.48288914425801	74.67962155087253	74.87635395748704	75.07308636410156	75.2698187707161	75.46655117733061	75.66328358394515	75.86001599055965	76.05674839717416	76.25348080378868	76.45021321040321	76.68629209834065	76.88302450495517	77.07975691156967	77.27648931818419	77.47322172479873	77.66995413141325	77.82734005670486	78.0240724633194	78.26015135125681	78.45688375787135	78.65361616448585	78.85034857110038	79.04708097771491	79.24381338432945	79.44054579094397	79.63727819755846	79.834010604173	80.03074301078752	80.22747541740205	80.42420782401657	80.62094023063106	80.8176726372456	81.01440504386013	81.21113745047465	81.40786985708918	81.64394874502661	81.84068115164111	82.03741355825566	82.23414596487018	82.43087837148467	82.62761077809921	82.82434318471374	83.02107559132825	83.2178079979428	83.4145404045573	83.61127281117182	83.80800521778632	84.00473762440086	84.20147003101538	84.39820243762989	84.59493484424443	84.79166725085894	84.98839965747348	85.22447854541089	85.42121095202543	85.61794335863995	85.81467576525447	86.01140817186898	86.20814057848349	86.40487298509803	86.60160539171256	86.79833779832708	86.9950702049416	87.19180261155611	87.38853501817063	87.58526742478517	87.78199983139968	87.97873223801419	88.17546464462872	88.37219705124325	88.60827593918067	88.80500834579519	89.0017407524097	89.2378196403472	89.43455204696167	89.6312844535762	89.8280168601907	90.02474926680524	90.26082815474267	90.4575605613572	90.65429296797171	90.85102537458621	91.00841129987784	91.16579722516946	91.36252963178398	91.5199155570756	91.67730148236723	91.83468740765885	91.99207333295044	92.18880573956496	92.3461916648566	92.54292407147111	92.70030999676274	92.89704240337727	93.09377480999177	93.29050721660629	93.48723962322084	93.68397202983535	93.88070443644986	94.07743684306436	94.2741692496789	94.47090165629344	94.66763406290796	94.86436646952247	95.061098876137	95.2578312827515	95.454563689366	95.61194961465766	95.8086820212722	96.00541442788671	96.20214683450122	96.39887924111576	96.59561164773027	96.7923440543448	96.98907646095931	97.14646238625092	97.34319479286546	97.53992719947998	97.7760060874174	97.9727384940319	98.16947090064643	98.32685682593807	98.52358923255258	98.7203216391671	98.91705404578162	99.11378645239614	99.31051885901067	99.4679047843023	99.66463719091681	99.86136959753134	100.0581020041459	100.2941808920833	100.4909132986978	100.6876457053123	100.9237245932498	101.1204569998643	101.3171894064788	101.5139218130933	101.7106542197078	101.9467331076453	102.1434655142598	102.3795444021972	102.5762768088117	102.8123556967492	103.0090881033637	103.2451669913011	103.4418993979156	103.6386318045302	103.8747106924676	104.0714430990821	104.2681755056966	104.5042543936341	104.7009868002486	104.8977192068631	105.0944516134776	105.330530501415	105.5272629080296	105.7239953146441	105.9207277212586	106.1174601278731	106.3141925344877	106.5109249411022	106.7076573477167	106.9043897543312	107.0617756796228	107.2585080862374	107.4552404928519	107.6519728994664	107.8487053060809	108.0454377126954	108.2028236379871	108.3995560446016	108.5962884512161	108.7930208578306	108.9504067831222	109.1471391897368	109.3045251150284	109.501257521643	109.6586434469345	109.855375853549	110.0127617788407	110.2094941854552	110.3668801107468	110.5636125173613	110.760344923976	110.9570773305904	111.1538097372049	111.3505421438194	111.5472745504339	111.7046604757256	111.940739363663	112.1374717702775	112.334204176892	112.5309365835065	112.7276689901211	112.9244013967356	113.1211338033501	113.3178662099646	113.5145986165792	113.6719845418708	113.8687169484853	114.0261028737769	114.1834887990685	114.3015282430373	114.3015282430373	114.1834887990685	114.0261028737769	113.8687169484853	113.7900239858395	113.9080634298082	114.1047958364227	114.3408747243601	114.5376071309747	114.7343395375892	114.9704184255266	115.1671508321411	115.3245367574328	115.5212691640473	115.678655089339	115.8360410146305	115.9540804585992	116.1114663838909	116.2295058278596	116.3868917531512	116.5442776784428	116.7016636037344	116.859049529026	117.0164354543176	117.1738213796093	117.331207304901	117.4885932301925	117.6459791554841	117.8033650807757	117.9607510060674	118.118136931359	118.2755228566506	118.4329087819422	118.550948225911	118.7083341512025	118.8657200764942	118.9837595204629	119.1411454457545	119.2591848897232	119.3772243336919	119.5346102589835	119.6526497029522	119.770689146921	119.9280750722126	120.0461145161813	120.16415396015	120.2821934041187	120.4002328480874	120.5182722920561	120.6756582173478	120.7150046986707	120.8330441426394	120.990430067931	121.1084695118997	121.1871624745455	121.3052019185142	121.4232413624829	121.5412808064517	121.6593202504204	121.7773596943891	121.8953991383578	121.9740921010036	122.0921315449723	122.210170988941	122.249517470264	122.3675569142327	122.4462498768785	122.5642893208472	122.642982283493	122.7610217274617	122.8397146901075	122.9577541340762	123.036447096722	123.1544865406907	123.2331795033365	123.3118724659823	123.4299119099511	123.5086048725969	123.6266443165656	123.7053372792114	123.7840302418572	123.902069685826	123.9807626484717	124.0594556111175	124.1381485737633	124.2561880177321	124.334880980378	124.4135739430237	124.4922669056695	124.5709598683153	124.6496528309611	124.7283457936069	124.7676922749298	124.8463852375756	124.9250782002214	125.0037711628672	125.0824641255131	125.121810606836	125.161157088159	125.2005035694818	125.161157088159	125.0824641255131	124.9644246815443	124.8463852375756	124.7676922749298	124.688999312284	124.6496528309611	124.688999312284	124.7283457936069	124.8070387562527	124.8463852375756	124.8857317188985	124.9250782002214	124.9644246815443	125.0037711628672	125.0431176441901	125.0824641255131	125.121810606836	125.2005035694818	125.2398500508047	125.2791965321276	125.3578894947734	125.3972359760963	125.4365824574192	125.515275420065	125.554621901388	125.6333148640337	125.6726613453566	125.7513543080024	125.7513543080024	125.8300472706482	125.8693937519711	125.9480867146169	125.98743319594	126.0661261585857	126.1054726399086	126.1448191212315	126.2235120838773	126.2628585652002	126.341551527846	126.341551527846	126.4202444904918	126.4595909718147	126.4989374531376	126.5382839344605	126.6169768971063	126.6563233784292	126.6956698597521	126.7743628223979	126.8137093037208	126.8530557850438	126.8924022663667	126.9710952290125	127.0104417103354	127.0497881916583	127.0891346729812	127.1284811543041	127.167827635627	127.2465205982728	127.2858670795957	127.2858670795957	127.3252135609186	127.4039065235644	127.4432530048873	127.4825994862102	127.4825994862102	127.5219459675331	127.6006389301789	127.6399854115018	127.6793318928246	127.6793318928246	127.7580248554706	127.7973713367934	127.8367178181164	127.8760642994393	127.8760642994393	127.9154107807622	127.9547572620851	127.994103743408	128.0727967060538	128.0727967060538	128.1121431873767	128.1514896686996	128.1908361500225	128.2301826313453	128.2695291126683	128.2695291126683	128.3088755939912	128.3482220753141	128.387568556637	128.42691503796	128.4662615192828	128.4662615192828	128.5056080006057	128.5449544819286	128.5843009632515	128.6236474445744	128.6236474445744	128.6629939258974	128.7023404072202	128.7416868885432	128.781033369866	128.820379851189	128.859726332512	128.859726332512	128.8990728138347	128.9384192951577	128.9777657764806	128.9777657764806	129.0171122578035	129.0564587391264	129.0958052204493	129.0958052204493	129.1351517017721	129.1744981830951	129.1744981830951	129.2138446644179	129.2531911457409	129.2531911457409	129.2925376270638	129.3318841083867	129.3318841083867	129.3712305897096	129.3712305897096	129.4105770710325	129.4105770710325	129.4499235523554	129.4892700336783	129.4892700336783	129.5286165150012	129.5679629963242	129.5679629963242	129.5679629963242	129.607309477647	129.64665595897	129.64665595897	129.686002440293	129.686002440293	129.7253489216158	129.7253489216158	129.7646954029387	129.7646954029387	129.7646954029387	129.8040418842616	129.8433883655845	129.8433883655845	129.8827348469074	129.8827348469074	129.8827348469074	129.9220813282303	129.9220813282303	129.9614278095532	129.9614278095532	129.9614278095532	130.0007742908761	130.0007742908761	130.040120772199	130.040120772199	130.040120772199	130.0794672535219	130.0794672535219	130.1188137348447	130.1188137348447	130.1188137348447	130.1188137348447	130.1581602161677	130.1581602161677	130.1975066974906	130.1975066974906	130.1975066974906	130.2368531788135	130.2368531788135	130.2368531788135	130.2368531788135	130.2761996601364	130.2761996601364	130.2761996601364	130.3155461414593	130.3155461414593	130.3155461414593	130.3155461414593	130.3155461414593	130.3548926227822	130.3548926227822	130.3548926227822	130.3548926227822	130.3942391041051	130.3942391041051	130.3942391041051	130.3942391041051	130.3942391041051	130.3942391041051	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.3942391041051	130.3942391041051	130.3942391041051	130.3942391041051	130.3942391041051	130.3548926227822	130.3548926227822	130.3548926227822	130.3548926227822	130.3548926227822	130.3155461414593	130.3155461414593	130.3155461414593	130.2761996601364	130.2761996601364	130.2761996601364	130.2761996601364	130.2368531788135	130.2368531788135	130.2368531788135	130.1975066974906	130.1975066974906	130.1975066974906	130.1581602161677	130.1581602161677	130.1581602161677	130.1188137348447	130.1188137348447	130.0794672535219	130.0794672535219	130.0794672535219	130.040120772199	130.040120772199	130.0007742908761	130.0007742908761	130.0007742908761	129.9614278095532	129.9614278095532	129.9220813282303	129.9220813282303	129.8827348469074	129.8827348469074	129.8433883655845	129.8433883655845	129.8040418842616	129.7646954029387	129.7646954029387	129.7253489216158	129.7253489216158	129.686002440293	129.64665595897	129.64665595897	129.607309477647	129.5679629963242	129.5679629963242	129.5286165150012	129.4892700336783	129.4499235523554	129.4499235523554	129.4105770710325	129.3712305897096	129.2925376270638	129.2531911457409	129.2138446644179	129.1744981830951	129.1351517017721	129.0958052204493	129.0564587391264	128.9777657764806	128.9384192951577	128.8990728138347	128.859726332512	128.781033369866	128.7416868885432	128.7023404072202	128.6629939258974	128.5843009632515	128.5449544819286	128.5056080006057	128.42691503796	128.387568556637	128.3088755939912	128.2695291126683	128.2301826313453	128.1514896686996	128.1121431873767	128.0334502247309	127.994103743408	127.9547572620851	127.8760642994393	127.8367178181164	127.7580248554706	127.7186783741476	127.6399854115018	127.561292448856	127.5219459675331	127.4825994862102	127.4039065235644	127.3645600422415	127.2858670795957	127.2071741169499	127.167827635627	127.1284811543041	127.0497881916583	126.9710952290125	126.9317487476895	126.8530557850438	126.7743628223979	126.735016341075	126.6563233784292	126.6169768971063	126.5382839344605	126.4595909718147	126.4202444904918	126.341551527846	126.3022050465231	126.1841656025544	126.1448191212315	126.0661261585857	126.0267796772628	125.908740233294	125.8693937519711	125.7907007893253	125.7513543080024	125.6726613453566	125.5939683827108	125.515275420065	125.4365824574192	125.3578894947734	125.3185430134505	125.2398500508047	125.121810606836	125.0824641255131	125.0037711628672	124.9250782002214	124.8463852375756	124.8070387562527	124.688999312284	124.6103063496382	124.5316133869924	124.4529204243466	124.3742274617008	124.295534499055	124.2168415364091	124.1381485737633	124.0594556111175	123.9807626484717	123.902069685826	123.8233767231801	123.7053372792114	123.5872978352427	123.5086048725969	123.4299119099511	123.3512189473053	123.2725259846595	123.1544865406907	123.0757935780449	122.9971006153991	122.8397146901075	122.7610217274617	122.6823287648159	122.5642893208472	122.4855963582014	122.4069033955555	122.2888639515868	122.1708245076181	122.0527850636494	121.9740921010036	121.8560526570349	121.7773596943891	121.6593202504204	121.5806272877746	121.4625878438058	121.38389488116	121.2265089558684	121.1084695118997	120.990430067931	120.9117371052852	120.7936976613165	120.6756582173478	120.596965254702	120.4789258107332	120.3608863667645	120.2428469227958	120.0854609975042	119.9674215535355	119.8493821095668	119.770689146921	119.6526497029522	119.5346102589835	119.4165708150148	119.2985313710461	119.1804919270774	119.0624524831087	118.94441303914	118.7476806325254	118.6296411885567	118.511601744588	118.3542158192964	118.2361763753277	118.118136931359	118.0000974873903	117.8820580434216	117.7246721181299	117.6066326741612	117.4885932301925	117.331207304901	117.1738213796093	117.0164354543176	116.8983960103489	116.7803565663802	116.6229706410886	116.5049311971199	116.3475452718283	116.2295058278596	116.1114663838909	115.9540804585992	115.8360410146305	115.678655089339	115.5606156453702	115.4032297200786	115.2064973134641	115.0491113881724	114.8917254628808	114.7736860189121	114.6163000936205	114.4982606496518	114.3408747243601	114.1834887990685	114.0654493550998	113.9080634298082	113.7506775045166	113.593291579225	113.4752521352563	113.3178662099646	113.160480284673	113.0030943593814	112.8850549154127	112.7276689901211	112.4915901021837	112.334204176892	112.1768182516004	112.0587788076317	111.9013928823401	111.7440069570485	111.5866210317568	111.4292351064652	111.2718491811736	111.114463255882	110.9570773305904	110.7996914052988	110.6423054800071	110.4849195547155	110.3275336294239	110.1701477041323	109.9734152975178	109.8160293722262	109.6586434469345	109.501257521643	109.3438715963513	109.1864856710597	108.9897532644452	108.8323673391535	108.5962884512161	108.4389025259245	108.24217011931	108.0847841940184	107.9273982687267	107.7306658621122	107.5732799368206	107.3765475302061	107.2191616049145	107.0617756796228	106.8650432730083	106.7076573477167	106.5109249411022	106.3535390158106	106.156806609196	105.9994206839044	105.8026882772899	105.6453023519983	105.4485699453838	105.2518375387692	105.0944516134776	104.8977192068631	104.7009868002486	104.543600874957	104.3468684683424	104.1501360617279	103.9927501364363	103.7960177298218	103.5992853232073	103.4025529165927	103.2058205099782	103.0090881033637	102.8517021780721	102.5369303274888	102.3401979208743	102.1434655142598	101.9467331076453	101.7500007010307	101.5532682944162	101.3565358878017	101.1598034811872	100.9630710745727	100.7269921866352	100.5302597800207	100.3335273734062	100.1367949667917	99.90071607885423	99.70398367223971	99.5072512656252	99.27117237768776	99.07443997107324	98.8777075644587	98.64162867652131	98.4448962699068	98.20881738196935	97.9727384940319	97.7760060874174	97.53992719947998	97.30384831154254	97.06776942360512	96.87103701699057	96.63495812905316	96.39887924111576	96.16280035317831	95.9267214652409	95.69064257730348	95.454563689366	95.2184848014286	94.9430594321683	94.70698054423085	94.47090165629344	94.07743684306436	93.80201147380404	93.56593258586662	93.29050721660629	93.01508184734597	92.70030999676274	92.4248846275024	92.11011277691917	91.5986085197214	77.2371428368613	8.34145404045573	-3.265757949801064	-3.265757949801064	-3.187064987155256	-3.14771850583235	-3.305104431123969	-3.265757949801064	-3.22641146847816	-3.305104431123969	-3.265757949801064	-3.265757949801064	-3.305104431123969	-3.305104431123969	-3.305104431123969	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.305104431123969	-3.305104431123969	-3.305104431123969	-3.265757949801064	-3.305104431123969	-3.305104431123969	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.305104431123969	-3.305104431123969	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.305104431123969	-3.305104431123969	-3.305104431123969	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.305104431123969	-3.305104431123969	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	-3.265757949801064	0.29% carbon steel	0.000111111111111111	0.0	0.0	1.85185185185185E-5	0.000111111111111111	0.000222222222222222	0.000351851851851852	0.000462962962962963	0.000574074074074074	0.000685185185185185	0.000833333333333333	0.000944444444444444	0.00105555555555556	0.0012037037037037	0.00131481481481481	0.00142592592592593	0.00157407407407407	0.00168518518518518	0.0017962962962963	0.00194444444444444	0.00205555555555556	0.00216666666666667	0.0022962962962963	0.00242592592592593	0.00253703703703704	0.00266666666666667	0.0027962962962963	0.00290740740740741	0.00303703703703704	0.00316666666666667	0.00327777777777778	0.00340740740740741	0.00353703703703704	0.00364814814814815	0.00377777777777778	0.00390740740740741	0.00401851851851852	0.00416666666666667	0.00427777777777778	0.00438888888888889	0.00453703703703704	0.00464814814814815	0.00475925925925926	0.00490740740740741	0.00501851851851852	0.00512962962962963	0.00527777777777778	0.00538888888888889	0.00553703703703704	0.00564814814814815	0.00575925925925926	0.00590740740740741	0.00601851851851852	0.00612962962962963	0.00627777777777778	0.00638888888888889	0.0065	0.00664814814814815	0.00675925925925926	0.00687037037037037	0.00701851851851852	0.00712962962962963	0.00725925925925926	0.00738888888888889	0.0075	0.00762962962962963	0.00775925925925926	0.00787037037037037	0.0079074074074074	0.00798148148148148	0.00809259259259259	0.00822222222222222	0.00835185185185185	0.00846296296296296	0.00861111111111111	0.00872222222222222	0.00887037037037037	0.00898148148148148	0.00909259259259259	0.00924074074074074	0.00935185185185185	0.00948148148148148	0.00961111111111111	0.00972222222222222	0.00985185185185185	0.00998148148148148	0.0100925925925926	0.0102222222222222	0.0103518518518519	0.0104814814814815	0.0105925925925926	0.0107407407407407	0.0108518518518518	0.010962962962963	0.0111111111111111	0.0112222222222222	0.0113703703703704	0.0114814814814815	0.0115925925925926	0.0116111111111111	0.0117592592592593	0.0118703703703704	0.0119814814814815	0.0121296296296296	0.0122407407407407	0.0123518518518518	0.0125	0.0126111111111111	0.0127592592592593	0.0128703703703704	0.0129814814814815	0.0131296296296296	0.0132407407407407	0.0133703703703704	0.0135	0.0136111111111111	0.0137407407407407	0.0138703703703704	0.0139814814814815	0.0141111111111111	0.0142407407407407	0.0143703703703704	0.0144814814814815	0.0146111111111111	0.0147407407407407	0.0148518518518518	0.0149814814814815	0.0151111111111111	0.0152222222222222	0.0153518518518518	0.0154814814814815	0.0155925925925926	0.0157222222222222	0.0158518518518518	0.015962962962963	0.0161111111111111	0.0162222222222222	0.0163333333333333	0.0164814814814815	0.0165925925925926	0.0167037037037037	0.0168518518518518	0.016962962962963	0.0170740740740741	0.0172222222222222	0.0173333333333333	0.0174814814814815	0.0175925925925926	0.0177037037037037	0.0178518518518518	0.017962962962963	0.0180740740740741	0.0182222222222222	0.0183333333333333	0.018462962962963	0.0185740740740741	0.0187037037037037	0.0188333333333333	0.0189444444444444	0.0190740740740741	0.0192037037037037	0.0193148148148148	0.0194444444444444	0.0195740740740741	0.0196851851851852	0.0198333333333333	0.0199444444444444	0.0200925925925926	0.0202037037037037	0.0203148148148148	0.020462962962963	0.0205740740740741	0.0207037037037037	0.0208333333333333	0.0209444444444444	0.0210740740740741	0.0212037037037037	0.0213148148148148	0.0214444444444444	0.0215740740740741	0.0216851851851852	0.0218148148148148	0.0219444444444444	0.0220740740740741	0.0221851851851852	0.0223148148148148	0.0224444444444444	0.0225555555555555	0.0226851851851852	0.0228148148148148	0.0229259259259259	0.0230555555555556	0.0231851851851852	0.0232962962962963	0.0234444444444444	0.0235555555555556	0.0236666666666667	0.0238148148148148	0.0239259259259259	0.024037037037037	0.0241851851851852	0.0242962962962963	0.0244444444444444	0.0245555555555556	0.0246851851851852	0.0248148148148148	0.0249259259259259	0.0250555555555556	0.0251851851851852	0.0252962962962963	0.0254259259259259	0.0255555555555555	0.0256666666666667	0.0257962962962963	0.0259259259259259	0.026037037037037	0.0261666666666667	0.0262962962962963	0.0264259259259259	0.026537037037037	0.0266666666666667	0.0267962962962963	0.0269074074074074	0.027037037037037	0.0271481481481481	0.0272777777777778	0.0274074074074074	0.0275185185185185	0.0276481481481481	0.0277777777777778	0.0278888888888889	0.0280185185185185	0.0281481481481481	0.0282592592592593	0.0283888888888889	0.0285185185185185	0.0286481481481481	0.0287592592592593	0.0288888888888889	0.0290185185185185	0.0291296296296296	0.0292592592592593	0.0293888888888889	0.0295	0.0296296296296296	0.0297592592592593	0.0298703703703704	0.03	0.0301296296296296	0.0302407407407407	0.0303888888888889	0.0305	0.0306111111111111	0.0307592592592593	0.0308703703703704	0.0309814814814815	0.0311296296296296	0.0312407407407407	0.0313518518518518	0.0315	0.0316111111111111	0.0317592592592593	0.0318703703703704	0.0319814814814815	0.0321296296296296	0.0322407407407407	0.0323518518518518	0.0325	0.0326111111111111	0.0327407407407407	0.0328703703703704	0.0329814814814815	0.0331111111111111	0.0332407407407407	0.0333703703703704	0.0334814814814815	0.0336111111111111	0.0337407407407407	0.0338518518518518	0.034	0.0341111111111111	0.0342222222222222	0.0343703703703704	0.0344814814814815	0.0346296296296296	0.0347407407407407	0.0348703703703704	0.035	0.0351111111111111	0.0352407407407407	0.0353703703703704	0.0354814814814815	0.0356111111111111	0.0357407407407407	0.0358703703703704	0.0359814814814815	0.0361296296296296	0.0362407407407407	0.0363518518518518	0.0365	0.0366111111111111	0.0367592592592593	0.0368703703703704	0.037	0.0371111111111111	0.0372407407407407	0.0373703703703704	0.0374814814814815	0.0376111111111111	0.0377407407407407	0.0378518518518518	0.038	0.0381111111111111	0.0382592592592592	0.0383703703703704	0.0385	0.0386296296296296	0.0387592592592592	0.0388703703703704	0.039	0.0391296296296296	0.0392407407407407	0.0393703703703704	0.0395	0.0396111111111111	0.0397592592592592	0.0398703703703704	0.0399814814814815	0.0401296296296296	0.0402407407407407	0.0403888888888889	0.0405	0.0406111111111111	0.0407592592592593	0.0408703703703704	0.041	0.0411296296296296	0.0412407407407407	0.0413518518518518	0.0415	0.0416111111111111	0.0417407407407407	0.0418703703703704	0.042	0.0421111111111111	0.0422407407407407	0.0423703703703704	0.0424814814814815	0.0426111111111111	0.0427407407407407	0.0428518518518518	0.0429814814814815	0.0431111111111111	0.0432222222222222	0.0433703703703704	0.0434814814814815	0.0436296296296296	0.0437407407407407	0.0438518518518518	0.044	0.0441111111111111	0.0442222222222222	0.0443703703703704	0.0444814814814815	0.0446111111111111	0.0447407407407407	0.0448703703703704	0.0449814814814815	0.0451111111111111	0.0452407407407407	0.0453518518518518	0.0455	0.0456111111111111	0.0457222222222222	0.0458703703703704	0.0459814814814815	0.0460925925925926	0.0462407407407407	0.0463518518518518	0.0465	0.0466111111111111	0.0467222222222222	0.0468703703703704	0.0469814814814815	0.0471111111111111	0.0472407407407407	0.0473518518518518	0.0474814814814815	0.0476111111111111	0.0477222222222222	0.0478518518518518	0.0479814814814815	0.0481111111111111	0.0482222222222222	0.0483703703703704	0.0484814814814815	0.0486296296296296	0.0487407407407407	0.0488518518518518	0.048962962962963	0.0491111111111111	0.0492222222222222	0.0493703703703704	0.0494814814814815	0.0495925925925926	0.0497407407407407	0.0498518518518518	0.0499629629629629	0.0501111111111111	0.0502222222222222	0.0503518518518518	0.0504814814814815	0.0506111111111111	0.0507222222222222	0.0508518518518518	0.0509814814814815	0.0510925925925926	0.0512407407407407	0.0513518518518518	0.051462962962963	0.0516111111111111	0.0517222222222222	0.0518333333333333	0.0519814814814815	0.0520925925925926	0.0522037037037037	0.0523518518518518	0.052462962962963	0.0526111111111111	0.0527222222222222	0.0528333333333333	0.0529814814814815	0.0530925925925926	0.0532037037037037	0.0533518518518518	0.053462962962963	0.0535740740740741	0.0537222222222222	0.0538333333333333	0.0539444444444444	0.0540925925925926	0.0542037037037037	0.0543333333333333	0.054462962962963	0.0545740740740741	0.0546851851851852	0.0548333333333333	0.0549444444444444	0.0550740740740741	0.0552037037037037	0.0553148148148148	0.0554444444444444	0.0555555555555555	0.0556851851851852	0.0558148148148148	0.0559259259259259	0.0560555555555555	0.0561851851851852	0.0562962962962963	0.0564444444444444	0.0565555555555555	0.0566666666666667	0.0568148148148148	0.0569259259259259	0.057037037037037	0.0571851851851852	0.0572962962962963	0.0574074074074074	0.0575555555555555	0.0576666666666667	0.0577777777777778	0.0579259259259259	0.058037037037037	0.0581481481481481	0.0582962962962963	0.0584074074074074	0.0585555555555555	0.0586666666666667	0.0587962962962963	0.0589259259259259	0.059037037037037	0.0591666666666667	0.0592962962962963	0.0594074074074074	0.059537037037037	0.0596666666666667	0.0597777777777778	0.0599074074074074	0.060037037037037	0.0601666666666667	0.0602777777777778	0.0604259259259259	0.060537037037037	0.0606481481481481	0.0607962962962963	0.0609074074074074	0.0610185185185185	0.0611666666666667	0.0612777777777778	0.0614259259259259	0.061537037037037	0.0616666666666667	0.0617962962962963	0.0619074074074074	0.062037037037037	0.0621666666666667	0.0622962962962963	0.0624074074074074	0.062537037037037	0.0626666666666666	0.0627777777777778	0.0629259259259259	0.063037037037037	0.0631851851851852	0.0632962962962963	0.0634259259259259	0.0635555555555555	0.0636666666666667	0.0637962962962963	0.0639259259259259	0.0640555555555555	0.0641666666666667	0.0642962962962963	0.0644259259259259	0.064537037037037	0.0646851851851852	0.0647962962962963	0.0649444444444444	0.0650555555555555	0.0651666666666667	0.0653148148148148	0.0654259259259259	0.065537037037037	0.0656851851851852	0.0657962962962963	0.0659074074074074	0.0660555555555555	0.0661666666666667	0.0662777777777778	0.0664259259259259	0.066537037037037	0.0666666666666667	0.0667962962962963	0.0669259259259259	0.067037037037037	0.0671851851851852	0.0672962962962963	0.0674074074074074	0.0675555555555555	0.0676666666666667	0.0677777777777778	0.0679259259259259	0.068037037037037	0.0681851851851852	0.0682962962962963	0.0684074074074074	0.0685555555555555	0.0686666666666667	0.0687962962962963	0.0689259259259259	0.069037037037037	0.0691666666666667	0.0692962962962963	0.0694074074074074	0.069537037037037	0.0696666666666667	0.0697962962962963	0.0699074074074074	0.0700555555555555	0.0701666666666667	0.0702777777777778	0.0704259259259259	0.070537037037037	0.0706481481481481	0.0707962962962963	0.0709074074074074	0.0710555555555555	0.0711666666666667	0.0712962962962963	0.0714259259259259	0.071537037037037	0.0716666666666667	0.0717962962962963	0.0719259259259259	0.072037037037037	0.0721666666666666	0.0722962962962963	0.0724074074074074	0.0725555555555555	0.0726666666666667	0.0727777777777778	0.0729259259259259	0.073037037037037	0.0731851851851852	0.0732962962962963	0.0734074074074074	0.0735555555555555	0.0736666666666667	0.0737777777777778	0.0739259259259259	0.074037037037037	0.0741666666666667	0.0742777777777778	0.0744074074074074	0.074537037037037	0.0746481481481481	0.0747962962962963	0.0749074074074074	0.0750555555555555	0.0751666666666667	0.0752777777777778	0.0754259259259259	0.075537037037037	0.0756481481481481	0.0757962962962963	0.0759074074074074	0.0760185185185185	0.0761666666666667	0.0762777777777778	0.0764074074074074	0.076537037037037	0.0766666666666667	0.0767777777777778	0.0769074074074074	0.0770185185185185	0.0771481481481482	0.0772962962962963	0.0774074074074074	0.0775185185185185	0.0776481481481481	0.0777777777777778	0.0778888888888889	0.078037037037037	0.0781481481481481	0.0782592592592593	0.0783888888888889	0.0785185185185185	0.0786296296296296	0.0787592592592593	0.0788888888888889	0.079	0.0791481481481481	0.0792592592592593	0.0794074074074074	0.0795185185185185	0.0796296296296296	0.0797407407407407	0.0798888888888889	0.08	0.0801481481481481	0.0802592592592592	0.0803703703703704	0.0805185185185185	0.0806296296296296	0.0807407407407407	0.0808888888888889	0.081	0.0811111111111111	0.0812592592592592	0.0813703703703704	0.0814814814814815	0.0816296296296296	0.0817407407407407	0.0818703703703704	0.082	0.0821296296296296	0.0822407407407407	0.0823703703703704	0.0825	0.0826111111111111	0.0827407407407407	0.0828703703703703	0.0829814814814815	0.0831111111111111	0.0832407407407407	0.0833518518518518	0.0835	0.0836111111111111	0.0837222222222222	0.0838703703703704	0.0839814814814815	0.0841296296296296	0.0842407407407407	0.0843518518518518	0.0845	0.0846111111111111	0.0847407407407407	0.0848703703703704	0.0849814814814815	0.0851111111111111	0.0852407407407407	0.0853703703703704	0.0854814814814815	0.0856111111111111	0.0857407407407407	0.0858518518518518	0.086	0.0861111111111111	0.0862592592592593	0.0863703703703703	0.0864814814814815	0.0866296296296296	0.0867407407407407	0.0868703703703703	0.087	0.0871111111111111	0.0872407407407407	0.0873703703703704	0.0875	0.0876111111111111	0.0877592592592592	0.0878703703703704	0.0879814814814815	0.0881296296296296	0.0882407407407407	0.0883888888888889	0.0885	0.0886111111111111	0.0887592592592592	0.0888703703703704	0.089	0.0891296296296296	0.0892592592592592	0.0893703703703703	0.0895185185185185	0.0896296296296296	0.0897777777777778	0.0898888888888889	0.09	0.0901481481481481	0.0902592592592592	0.0903703703703703	0.0905185185185185	0.0906296296296296	0.0907592592592592	0.0908888888888889	0.0910185185185185	0.0911296296296296	0.0912592592592592	0.0913888888888889	0.0915	0.0916481481481481	0.0917592592592592	0.0919074074074074	0.0920185185185185	0.0921296296296296	0.0922777777777778	0.0923888888888889	0.0925185185185185	0.0926296296296296	0.0927592592592592	0.0928888888888889	0.093	0.0931481481481481	0.0932592592592592	0.0933703703703703	0.0935185185185185	0.0936296296296296	0.0937777777777778	0.0938888888888889	0.0940185185185185	0.0941481481481481	0.0942592592592592	0.0943888888888889	0.0945185185185185	0.0946296296296296	0.0947592592592592	0.0949074074074074	0.0950185185185185	0.0951296296296296	0.0952777777777777	0.0953888888888889	0.095537037037037	0.0956481481481481	0.0957592592592592	0.0959074074074074	0.0960185185185185	0.0961481481481481	0.0962777777777778	0.0963888888888889	0.0965185185185185	0.0966481481481481	0.0967777777777778	0.0968888888888889	0.097037037037037	0.0971481481481481	0.0972592592592592	0.0974074074074074	0.0975185185185185	0.0976666666666666	0.0977777777777778	0.0978888888888889	0.098037037037037	0.0981481481481481	0.0982592592592592	0.0984074074074074	0.0985185185185185	0.0986481481481481	0.0987777777777777	0.0988888888888889	0.0990185185185185	0.0991481481481481	0.0992777777777777	0.0993888888888889	0.099537037037037	0.0996481481481481	0.0997592592592592	0.0999074074074074	0.100018518518519	0.100166666666667	0.100277777777778	0.100407407407407	0.100537037037037	0.100648148148148	0.100777777777778	0.100907407407407	0.101037037037037	0.101148148148148	0.101277777777778	0.101407407407407	0.101518518518519	0.101666666666667	0.101777777777778	0.101925925925926	0.102037037037037	0.102148148148148	0.102296296296296	0.102407407407407	0.102518518518519	0.102666666666667	0.102777777777778	0.102907407407407	0.103037037037037	0.103148148148148	0.103277777777778	0.103407407407407	0.103537037037037	0.103648148148148	0.103796296296296	0.103907407407407	0.104018518518519	0.104148148148148	0.104277777777778	0.104388888888889	0.104518518518519	0.104648148148148	0.104759259259259	0.104907407407407	0.105018518518519	0.105166666666667	0.105277777777778	0.105388888888889	0.1055	0.105648148148148	0.105759259259259	0.105907407407407	0.106018518518519	0.106148148148148	0.106277777777778	0.106388888888889	0.106518518518519	0.106648148148148	0.106759259259259	0.106888888888889	0.107018518518519	0.10712962962963	0.107259259259259	0.107388888888889	0.1075	0.10762962962963	0.107759259259259	0.10787037037037	0.108	0.10812962962963	0.108259259259259	0.10837037037037	0.108518518518519	0.10862962962963	0.108740740740741	0.108888888888889	0.109	0.109148148148148	0.109259259259259	0.10937037037037	0.109518518518519	0.10962962962963	0.109759259259259	0.109888888888889	0.11	0.110111111111111	0.110259259259259	0.11037037037037	0.1105	0.11062962962963	0.110740740740741	0.11087037037037	0.111	0.11112962962963	0.111240740740741	0.111351851851852	0.1115	0.111611111111111	0.111759259259259	0.11187037037037	0.112	0.11212962962963	0.112240740740741	0.112351851851852	0.1125	0.11262962962963	0.112740740740741	0.11287037037037	0.113	0.113111111111111	0.113240740740741	0.11337037037037	0.113481481481481	0.11362962962963	0.113740740740741	0.113851851851852	0.114	0.114111111111111	0.114259259259259	0.11437037037037	0.114481481481481	0.11462962962963	0.114759259259259	0.11487037037037	0.115	0.11512962962963	0.115240740740741	0.11537037037037	0.1155	0.115611111111111	0.115759259259259	0.11587037037037	0.115981481481481	0.11612962962963	0.116240740740741	0.116388888888889	0.1165	0.116611111111111	0.116759259259259	0.11687037037037	0.117	0.11712962962963	0.117240740740741	0.11737037037037	0.1175	0.11762962962963	0.117740740740741	0.11787037037037	0.117981481481481	0.118111111111111	0.118240740740741	0.11837037037037	0.118481481481481	0.11862962962963	0.118740740740741	0.118851851851852	0.119	0.119111111111111	0.119259259259259	0.11937037037037	0.1195	0.11962962962963	0.119740740740741	0.11987037037037	0.12	0.120111111111111	0.120240740740741	0.12037037037037	0.1205	0.120611111111111	0.120740740740741	0.12087037037037	0.120981481481481	0.12112962962963	0.121240740740741	0.121351851851852	0.1215	0.121611111111111	0.121759259259259	0.12187037037037	0.122	0.12212962962963	0.122240740740741	0.12237037037037	0.1225	0.12262962962963	0.122740740740741	0.12287037037037	0.123	0.123111111111111	0.123259259259259	0.12337037037037	0.123481481481481	0.12362962962963	0.123740740740741	0.123888888888889	0.124	0.124111111111111	0.124259259259259	0.12437037037037	0.1245	0.12462962962963	0.124740740740741	0.12487037037037	0.125	0.12512962962963	0.125240740740741	0.12537037037037	0.1255	0.125611111111111	0.125759259259259	0.12587037037037	0.126018518518518	0.12612962962963	0.126240740740741	0.126388888888889	0.1265	0.12662962962963	0.126759259259259	0.12687037037037	0.127	0.12712962962963	0.127259259259259	0.12737037037037	0.1275	0.12762962962963	0.127740740740741	0.12787037037037	0.128	0.128111111111111	0.128240740740741	0.12837037037037	0.128481481481481	0.12862962962963	0.128740740740741	0.128888888888889	0.129	0.129111111111111	0.129259259259259	0.12937037037037	0.1295	0.12962962962963	0.129740740740741	0.12987037037037	0.129981481481481	0.130111111111111	0.130240740740741	0.130351851851852	0.1305	0.130611111111111	0.130722222222222	0.13087037037037	0.130981481481481	0.13112962962963	0.131240740740741	0.131351851851852	0.1315	0.131611111111111	0.131722222222222	0.13187037037037	0.131981481481481	0.132092592592593	0.132240740740741	0.132351851851852	0.132481481481481	0.132611111111111	0.132722222222222	0.132833333333333	0.132981481481481	0.133092592592593	0.133203703703704	0.133351851851852	0.133462962962963	0.133592592592593	0.133722222222222	0.133833333333333	0.133962962962963	0.134092592592593	0.134203703703704	0.134333333333333	0.134462962962963	0.134574074074074	0.134703703703704	0.134833333333333	0.134962962962963	0.135074074074074	0.135203703703704	0.135333333333333	0.135444444444444	0.135574074074074	0.135703703703704	0.135814814814815	0.135962962962963	0.136074074074074	0.136185185185185	0.136333333333333	0.136444444444444	0.136555555555556	0.136703703703704	0.136814814814815	0.136962962962963	0.137074074074074	0.137185185185185	0.137333333333333	0.137444444444444	0.137555555555556	0.137703703703704	0.137814814814815	0.137944444444444	0.138074074074074	0.138185185185185	0.138314814814815	0.138444444444444	0.138555555555556	0.138685185185185	0.138814814814815	0.138944444444444	0.139055555555556	0.139185185185185	0.139314814814815	0.139425925925926	0.139574074074074	0.139685185185185	0.139796296296296	0.139944444444444	0.140055555555556	0.140166666666667	0.140314814814815	0.140425925925926	0.140574074074074	0.140685185185185	0.140796296296296	0.140944444444444	0.141055555555556	0.141166666666667	0.141314814814815	0.141425925925926	0.141555555555556	0.141685185185185	0.141796296296296	0.141925925925926	0.142055555555556	0.142166666666667	0.142296296296296	0.142425925925926	0.142555555555556	0.142666666666667	0.142796296296296	0.142907407407407	0.143037037037037	0.143166666666667	0.143296296296296	0.143407407407407	0.143537037037037	0.143666666666667	0.143777777777778	0.143925925925926	0.144037037037037	0.144148148148148	0.144277777777778	0.144407407407407	0.144518518518519	0.144666666666667	0.144777777777778	0.144888888888889	0.145037037037037	0.145148148148148	0.145259259259259	0.145407407407407	0.145518518518519	0.145666666666667	0.145777777777778	0.145888888888889	0.146037037037037	0.146148148148148	0.146277777777778	0.146407407407407	0.146518518518519	0.146648148148148	0.146777777777778	0.146888888888889	0.147018518518519	0.147148148148148	0.147277777777778	0.147388888888889	0.147518518518519	0.147648148148148	0.147759259259259	0.147907407407407	0.148018518518519	0.14812962962963	0.148277777777778	0.148388888888889	0.1485	0.148648148148148	0.148759259259259	0.148888888888889	0.149018518518519	0.14912962962963	0.149259259259259	0.149388888888889	0.1495	0.14962962962963	0.149759259259259	0.149888888888889	0.15	0.150148148148148	0.150259259259259	0.150407407407407	0.150518518518519	0.15062962962963	0.150777777777778	0.150888888888889	0.151	0.151148148148148	0.151259259259259	0.151388888888889	0.151518518518519	0.151648148148148	0.151759259259259	0.151888888888889	0.152018518518519	0.15212962962963	0.152277777777778	0.152388888888889	0.152537037037037	0.152648148148148	0.152759259259259	0.152907407407407	0.153018518518519	0.15312962962963	0.153277777777778	0.153407407407407	0.153518518518518	0.153666666666667	0.153777777777778	0.153888888888889	0.154037037037037	0.154148148148148	0.154259259259259	0.154407407407407	0.154518518518518	0.154666666666667	0.154777777777778	0.154888888888889	0.155037037037037	0.155148148148148	0.155259259259259	0.155407407407407	0.155518518518518	0.155648148148148	0.155777777777778	0.155888888888889	0.156018518518519	0.156148148148148	0.156259259259259	0.156388888888889	0.156518518518519	0.15662962962963	0.156759259259259	0.156888888888889	0.157018518518518	0.15712962962963	0.157259259259259	0.157388888888889	0.1575	0.15762962962963	0.157759259259259	0.15787037037037	0.158018518518518	0.15812962962963	0.158277777777778	0.158388888888889	0.1585	0.158611111111111	0.158759259259259	0.15887037037037	0.159018518518518	0.15912962962963	0.159240740740741	0.159388888888889	0.1595	0.159611111111111	0.159759259259259	0.15987037037037	0.16	0.16012962962963	0.160240740740741	0.16037037037037	0.1605	0.16062962962963	0.160740740740741	0.16087037037037	0.161	0.161111111111111	0.161240740740741	0.16137037037037	0.161481481481481	0.16162962962963	0.161740740740741	0.161851851851852	0.162	0.162111111111111	0.162222222222222	0.16237037037037	0.162481481481481	0.162592592592593	0.162740740740741	0.162851851851852	0.163	0.163111111111111	0.163222222222222	0.16337037037037	0.163481481481481	0.163592592592593	0.163740740740741	0.163851851851852	0.163962962962963	0.164111111111111	0.164222222222222	0.164351851851852	0.164481481481481	0.164611111111111	0.164722222222222	0.164851851851852	0.164981481481481	0.165092592592593	0.165222222222222	0.165351851851852	0.165462962962963	0.165611111111111	0.165722222222222	0.165833333333333	0.165981481481481	0.166092592592593	0.166203703703704	0.166351851851852	0.166462962962963	0.166574074074074	0.166722222222222	0.166833333333333	0.166962962962963	0.167092592592593	0.167203703703704	0.167333333333333	0.167462962962963	0.167592592592593	0.167703703703704	0.167833333333333	0.167962962962963	0.168074074074074	0.168203703703704	0.168333333333333	0.168444444444444	0.168574074074074	0.168703703703704	0.168814814814815	0.168944444444444	0.169055555555556	0.169185185185185	0.169314814814815	0.169425925925926	0.169555555555556	0.169685185185185	0.169814814814815	0.169925925925926	0.170055555555556	0.170185185185185	0.170296296296296	0.170425925925926	0.170555555555556	0.170666666666667	0.170796296296296	0.170925925925926	0.171037037037037	0.171166666666667	0.171296296296296	0.171407407407407	0.171537037037037	0.171666666666667	0.171777777777778	0.171907407407407	0.172037037037037	0.172148148148148	0.172277777777778	0.172407407407407	0.172518518518519	0.172648148148148	0.172777777777778	0.172888888888889	0.173018518518519	0.173148148148148	0.173259259259259	0.173388888888889	0.173518518518519	0.17362962962963	0.173777777777778	0.173888888888889	0.174037037037037	0.174148148148148	0.174259259259259	0.174407407407407	0.174518518518519	0.17462962962963	0.174777777777778	0.174888888888889	0.175018518518519	0.175148148148148	0.175259259259259	0.175388888888889	0.175518518518519	0.17562962962963	0.175759259259259	0.175888888888889	0.176	0.17612962962963	0.176259259259259	0.176388888888889	0.1765	0.17662962962963	0.176759259259259	0.17687037037037	0.177018518518518	0.17712962962963	0.177240740740741	0.177388888888889	0.1775	0.177648148148148	0.177759259259259	0.17787037037037	0.178018518518519	0.17812962962963	0.178259259259259	0.178388888888889	0.1785	0.17862962962963	0.178759259259259	0.178888888888889	0.179	0.17912962962963	0.179259259259259	0.17937037037037	0.179518518518519	0.17962962962963	0.179777777777778	0.179888888888889	0.18	0.180148148148148	0.180259259259259	0.180388888888889	0.180518518518518	0.18062962962963	0.180759259259259	0.180888888888889	0.181018518518519	0.18112962962963	0.181259259259259	0.181388888888889	0.1815	0.181648148148148	0.181759259259259	0.18187037037037	0.182018518518519	0.18212962962963	0.182240740740741	0.182388888888889	0.1825	0.182611111111111	0.182759259259259	0.18287037037037	0.183018518518518	0.18312962962963	0.183240740740741	0.183388888888889	0.1835	0.18362962962963	0.183759259259259	0.18387037037037	0.184	0.18412962962963	0.184240740740741	0.18437037037037	0.1845	0.184611111111111	0.184740740740741	0.18487037037037	0.185	0.185111111111111	0.185222222222222	0.18537037037037	0.185481481481481	0.185592592592593	0.185740740740741	0.185851851851852	0.185962962962963	0.186111111111111	0.186222222222222	0.18637037037037	0.186481481481481	0.186592592592593	0.186740740740741	0.186851851851852	0.186962962962963	0.187111111111111	0.187222222222222	0.187351851851852	0.187481481481481	0.187611111111111	0.187722222222222	0.187851851851852	0.187981481481481	0.188092592592593	0.188240740740741	0.188351851851852	0.188462962962963	0.188611111111111	0.188722222222222	0.188833333333333	0.188981481481481	0.189092592592593	0.189203703703704	0.189351851851852	0.189462962962963	0.189611111111111	0.189722222222222	0.189833333333333	0.189981481481481	0.190092592592593	0.190222222222222	0.190351851851852	0.190462962962963	0.190592592592593	0.190722222222222	0.190833333333333	0.190962962962963	0.191092592592593	0.191222222222222	0.191333333333333	0.191462962962963	0.191592592592593	0.191703703703704	0.191851851851852	0.191962962962963	0.192074074074074	0.192222222222222	0.192333333333333	0.192444444444444	0.192592592592593	0.192703703703704	0.192814814814815	0.192962962962963	0.193074074074074	0.193222222222222	0.193333333333333	0.193444444444444	0.193592592592593	0.193703703703704	0.193833333333333	0.193962962962963	0.194074074074074	0.194185185185185	0.194333333333333	0.194444444444444	0.194555555555556	0.194703703703704	0.194814814814815	0.194944444444444	0.195074074074074	0.195185185185185	0.195296296296296	0.195444444444444	0.195555555555556	0.195685185185185	0.195814814814815	0.195925925925926	0.196037037037037	0.196185185185185	0.196296296296296	0.196425925925926	0.196555555555556	0.196666666666667	0.196796296296296	0.196925925925926	0.197055555555556	0.197166666666667	0.197296296296296	0.197407407407407	0.197537037037037	0.197666666666667	0.197796296296296	0.197907407407407	0.198037037037037	0.198166666666667	0.198277777777778	0.198407407407407	0.198537037037037	0.198648148148148	0.198796296296296	0.198907407407407	0.199018518518518	0.199166666666667	0.199277777777778	0.199388888888889	0.199537037037037	0.199648148148148	0.199796296296296	0.199907407407407	0.200018518518519	0.200166666666667	0.200277777777778	0.200388888888889	0.200537037037037	0.200648148148148	0.200777777777778	0.200907407407407	0.201037037037037	0.201148148148148	0.201277777777778	0.201407407407407	0.201518518518519	0.201666666666667	0.201777777777778	0.201888888888889	0.202037037037037	0.202148148148148	0.202296296296296	0.202407407407407	0.202537037037037	0.202666666666667	0.202777777777778	0.202907407407407	0.203037037037037	0.203166666666667	0.203277777777778	0.203407407407407	0.203537037037037	0.203648148148148	0.203796296296296	0.203907407407407	0.204037037037037	0.204166666666667	0.204296296296296	0.204407407407407	0.204555555555556	0.204666666666667	0.204777777777778	0.204925925925926	0.205037037037037	0.205148148148148	0.205296296296296	0.205407407407407	0.205555555555556	0.205666666666667	0.205796296296296	0.205925925925926	0.206037037037037	0.206166666666667	0.206296296296296	0.206425925925926	0.206537037037037	0.206685185185185	0.206796296296296	0.206907407407407	0.207055555555556	0.207166666666667	0.207277777777778	0.207425925925926	0.207537037037037	0.207648148148148	0.207796296296296	0.207907407407407	0.208018518518519	0.208166666666667	0.208277777777778	0.208425925925926	0.208537037037037	0.208666666666667	0.208796296296296	0.208907407407407	0.209037037037037	0.209166666666667	0.209296296296296	0.209407407407407	0.209537037037037	0.209666666666667	0.209777777777778	0.209925925925926	0.210037037037037	0.210148148148148	0.210296296296296	0.210407407407407	0.210555555555556	0.210666666666667	0.210777777777778	0.210925925925926	0.211037037037037	0.211148148148148	0.211296296296296	0.211407407407407	0.211537037037037	0.211666666666667	0.211777777777778	0.211907407407407	0.212037037037037	0.212148148148148	0.212277777777778	0.212407407407407	0.212537037037037	0.212648148148148	0.212777777777778	0.212907407407407	0.213018518518519	0.213166666666667	0.213277777777778	0.213388888888889	0.213537037037037	0.213648148148148	0.213796296296296	0.213907407407407	0.214018518518519	0.214166666666667	0.214277777777778	0.214407407407407	0.214537037037037	0.214666666666667	0.214777777777778	0.214907407407407	0.215018518518519	0.215148148148148	0.215277777777778	0.215407407407407	0.215518518518519	0.215648148148148	0.215777777777778	0.215888888888889	0.216037037037037	0.216148148148148	0.216259259259259	0.216407407407407	0.216518518518519	0.216666666666667	0.216777777777778	0.216907407407407	0.217037037037037	0.217148148148148	0.217277777777778	0.217407407407407	0.217537037037037	0.217648148148148	0.217814814814815	0.218018518518518	0.218111111111111	0.218240740740741	0.218351851851852	0.218481481481481	0.218611111111111	0.218722222222222	0.218851851851852	0.218981481481481	0.219092592592593	0.219222222222222	0.219351851851852	0.219481481481481	0.219592592592593	0.219722222222222	0.219851851851852	0.219962962962963	0.220092592592593	0.220222222222222	0.220333333333333	0.220481481481481	0.220592592592593	0.220703703703704	0.220851851851852	0.220962962962963	0.221074074074074	0.221222222222222	0.221333333333333	0.221444444444444	0.221592592592593	0.221703703703704	0.221814814814815	0.221962962962963	0.222074074074074	0.222222222222222	0.222333333333333	0.222444444444444	0.222574074074074	0.222703703703704	0.222814814814815	0.222944444444444	0.223074074074074	0.223185185185185	0.223314814814815	0.223444444444444	0.223574074074074	0.223685185185185	0.223833333333333	0.223944444444444	0.224055555555556	0.224203703703704	0.224314814814815	0.224425925925926	0.224574074074074	0.224685185185185	0.224833333333333	0.224944444444444	0.225055555555556	0.225203703703704	0.225314814814815	0.225425925925926	0.225574074074074	0.225685185185185	0.225796296296296	0.225944444444444	0.226055555555556	0.226185185185185	0.226314814814815	0.226444444444444	0.226555555555556	0.226685185185185	0.226814814814815	0.226925925925926	0.227074074074074	0.227185185185185	0.227296296296296	0.227444444444444	0.227555555555556	0.227703703703704	0.227814814814815	0.227925925925926	0.228074074074074	0.228185185185185	0.228314814814815	0.228444444444444	0.228574074074074	0.228685185185185	0.228814814814815	0.228944444444444	0.229055555555556	0.229203703703704	0.229314814814815	0.229425925925926	0.229574074074074	0.229685185185185	0.229833333333333	0.229944444444444	0.230055555555556	0.230203703703704	0.230314814814815	0.230425925925926	0.230574074074074	0.230685185185185	0.230814814814815	0.230944444444444	0.231074074074074	0.231185185185185	0.231333333333333	0.231444444444444	0.231592592592593	0.231703703703704	0.231814814814815	0.231925925925926	0.232074074074074	0.232185185185185	0.232333333333333	0.232444444444444	0.232555555555556	0.232703703703704	0.232814814814815	0.232944444444444	0.233074074074074	0.233203703703704	0.233314814814815	0.233444444444444	0.233574074074074	0.233685185185185	0.233814814814815	0.233944444444444	0.234055555555556	0.234203703703704	0.234314814814815	0.234425925925926	0.234574074074074	0.234685185185185	0.0	0.0	0.0	0.0	0.0393464813229044	0.0393464813229044	0.0393464813229044	0.0393464813229044	0.0393464813229044	0.0393464813229044	0.0786929626458088	0.0786929626458088	0.0786929626458088	0.118039443968713	0.118039443968713	0.118039443968713	0.157385925291618	0.157385925291618	0.196732406614522	0.196732406614522	0.236078887937426	0.236078887937426	0.275425369260331	0.275425369260331	0.314771850583235	0.354118331906139	0.393464813229044	0.393464813229044	0.472157775874853	0.550850738520661	0.668890182489374	0.786929626458088	0.944315551749705	1.062354995718418	1.25908740233294	1.455819808947462	1.652552215561984	1.927977584822315	2.203402954082646	2.518174804665881	2.911639617894925	3.383797393769777	3.934648132290438	4.524845352134005	5.154389053300474	5.74458627314404	6.138051086373084	6.767594787539553	7.436484970028928	7.947989227226685	8.69557237236187	9.24642311088253	10.03335273734062	10.62354995718418	11.21374717702775	12.11871624745455	12.74825994862102	13.3778036497875	14.3614656828601	14.99100938402657	15.69924604783885	16.36813623032822	17.0370264128176	18.09938140853602	18.76827159102538	19.43716177351477	20.06670547468124	20.69624917584771	21.24709991436837	21.64056472759741	21.95533657818064	22.23076194744098	22.54553379802421	23.17507749919068	23.64723527506554	24.04070008829458	24.43416490152363	24.78828323342976	25.18174804665881	25.57521285988784	25.92933119179398	26.28344952370012	26.67691433692918	27.03103266883532	27.38515100074146	27.73926933264759	28.09338766455373	28.44750599645987	28.80162432836601	29.15574266027215	29.50986099217829	29.82463284276152	30.17875117466767	30.4935230252509	30.84764135715704	31.31979913303189	31.63457098361512	31.94934283419835	32.2641146847816	32.50019357271903	32.61823301668774	32.77561894197936	33.16908375520839	33.56254856843744	33.87732041902067	34.15274578828101	34.46751763886424	34.74294300812457	35.0183683773849	35.29379374664523	35.56921911590557	35.84464448516589	36.12006985442623	36.39549522368655	36.6709205929469	36.90699948088432	37.18242485014464	37.41850373808207	37.6939291073424	37.93000799527983	38.16608688321724	38.4021657711547	38.63824465909209	38.87432354702953	39.11040243496696	39.34648132290439	39.58256021084181	39.81863909877924	40.01537150539377	40.25145039333119	40.56622224391442	40.80230113185184	40.99903353846637	41.1957659450809	41.39249835169542	41.58923075830994	41.78596316492446	41.98269557153898	42.17942797815351	42.33681390344512	42.53354631005964	42.73027871667416	42.92701112328869	43.12374352990321	43.32047593651773	43.51720834313225	43.71394074974678	43.87132667503838	43.9893661190071	44.14675204429872	44.34348445091322	44.54021685752777	44.73694926414229	44.9336816707568	45.13041407737133	45.28780000266294	45.48453240927746	45.68126481589199	45.87799722250652	46.07472962912104	46.27146203573555	46.46819444235008	46.6649268489646	46.86165925557913	47.05839166219364	47.25512406880817	47.4912029567456	47.64858888203722	47.84532128865174	48.04205369526625	48.2781325832037	48.47486498981819	48.67159739643273	48.86832980304725	48.94702276569304	49.14375517230758	49.34048757892209	49.53721998553662	49.73395239215115	49.93068479876566	50.1274172053802	50.32414961199471	50.52088201860924	50.71761442522375	50.91434683183827	51.1110792384528	51.30781164506731	51.50454405168184	51.70127645829636	51.89800886491088	52.13408775284831	52.33082015946283	52.52755256607736	52.72428497269188	52.96036386062931	53.15709626724382	53.35382867385834	53.55056108047287	53.74729348708739	53.8653329310561	54.06206533767063	54.29814422560805	54.53422311354547	54.77030200148291	54.96703440809742	55.20311329603486	55.39984570264937	55.6359245905868	55.83265699720133	56.06873588513876	56.26546829175327	56.50154717969069	56.69827958630522	56.93435847424264	57.13109088085717	57.32782328747169	57.56390217540912	57.79998106334653	57.99671346996107	58.2327923578985	58.46887124583592	58.70495013377334	58.94102902171077	59.17710790964819	59.37384031626272	59.60991920420014	59.84599809213758	60.0427304987521	60.27880938668952	60.51488827462694	60.75096716256437	60.9870460505018	61.26247141976214	61.49855030769956	61.73462919563697	61.97070808357442	62.20678697151184	62.40351937812636	62.63959826606378	62.83633067267831	63.03306307929282	63.26914196723025	63.46587437384477	63.6626067804593	63.89868566839672	64.13476455633415	64.33149696294867	64.56757585088609	64.80365473882351	65.00038714543804	65.23646603337547	65.43319843998998	65.6692773279274	65.86600973454195	66.06274214115643	66.2988210290939	66.4955534357084	66.73163232364584	66.92836473026037	67.12509713687484	67.3611760248123	67.51856195010393	67.71529435671845	67.91202676333298	68.0694126886246	68.2661450952391	68.46287750185363	68.62026342714526	68.81699583375976	69.0137282403743	69.21046064698882	69.40719305360333	69.60392546021787	69.80065786683238	69.99739027344691	70.1547761987385	70.35150860535304	70.54824101196756	70.7449734185821	70.9417058251966	71.13843823181112	71.33517063842564	71.5319030450402	71.72863545165468	71.92536785826921	72.08275378356082	72.27948619017535	72.47621859678986	72.67295100340438	72.86968341001892	73.06641581663344	73.26314822324796	73.4992271111854	73.69595951779989	73.93203840573734	74.12877081235182	74.3648497002893	74.5615821069038	74.75831451351833	74.95504692013285	75.15177932674737	75.34851173336189	75.54524413997643	75.70263006526803	75.86001599055965	76.05674839717416	76.2141343224658	76.41086672908032	76.60759913569483	76.76498506098646	76.96171746760097	77.15844987421551	77.35518228083001	77.55191468744456	77.74864709405907	77.9453795006736	78.10276542596521	78.2994978325797	78.49623023919426	78.69296264580877	78.85034857110038	79.04708097771491	79.20446690300653	79.40119930962104	79.55858523491267	79.7553176415272	79.95205004814171	80.10943597343332	80.30616838004786	80.46355430533948	80.66028671195399	80.8176726372456	80.97505856253721	81.17179096915174	81.32917689444334	81.52590930105788	81.68329522634951	81.88002763296402	82.03741355825566	82.23414596487018	82.39153189016177	82.54891781545339	82.74565022206792	82.90303614735953	83.06042207265114	83.2571544792657	83.4145404045573	83.57192632984892	83.72931225514054	83.88669818043215	84.08343058704668	84.2408165123383	84.39820243762989	84.5555883629215	84.71297428821316	84.90970669482767	85.0670926201193	85.22447854541089	85.38186447070252	85.53925039599414	85.69663632128575	85.85402224657737	86.05075465319189	86.20814057848349	86.36552650377513	86.52291242906675	86.68029835435836	86.83768427965	86.9950702049416	87.15245613023319	87.30984205552481	87.46722798081648	87.62461390610806	87.78199983139968	87.93938575669129	88.09677168198293	88.25415760727454	88.41154353256615	88.60827593918067	88.7656618644723	88.92304778976391	89.04108723373263	89.11978019637843	89.27716612167006	89.43455204696167	89.59193797225328	89.74932389754491	89.90670982283652	90.06409574812813	90.26082815474267	90.4182140800343	90.5756000053259	90.73298593061751	90.89037185590912	91.04775778120077	91.20514370649238	91.36252963178398	91.5199155570756	91.67730148236723	91.83468740765885	91.99207333295044	92.14945925824208	92.30684518353368	92.46423110882531	92.62161703411691	92.73965647808564	92.89704240337727	93.05442832866888	93.2118142539605	93.36920017925211	93.5265861045437	93.68397202983535	93.84135795512697	93.95939739909568	94.1167833243873	94.2741692496789	94.43155517497052	94.58894110026215	94.74632702555377	94.86436646952247	95.02175239481409	95.17913832010569	95.29717776407443	95.454563689366	95.61194961465766	95.72998905862636	95.887374983918	96.0447609092096	96.16280035317831	96.32018627846993	96.47757220376154	96.59561164773027	96.75299757302186	96.87103701699057	97.02842294228221	97.18580886757381	97.34319479286546	97.46123423683417	97.61862016212578	97.7366596060945	97.89404553138611	98.01208497535481	98.16947090064643	98.32685682593807	98.4448962699068	98.60228219519838	98.7203216391671	98.8777075644587	98.99574700842743	99.15313293371904	99.27117237768776	99.42855830297937	99.5465977469481	99.70398367223971	99.82202311620841	99.94006256017715	100.0974484854688	100.2154879294375	100.3335273734062	100.412220336052	100.5302597800207	100.6482992239894	100.805685149281	100.9237245932498	101.0417640372185	101.1598034811872	101.3171894064788	101.4352288504475	101.5532682944162	101.6713077383849	101.8286936636766	101.9467331076453	102.064772551614	102.1828119955827	102.3008514395514	102.4188908835201	102.5762768088117	102.6943162527805	102.8123556967492	102.930395140718	103.0484345846866	103.1664740286553	103.284513472624	103.4025529165927	103.5205923605615	103.6386318045302	103.7566712484989	103.8747106924676	103.9927501364363	104.110789580405	104.2288290243737	104.3075219870195	104.4255614309883	104.543600874957	104.6616403189257	104.7796797628944	104.8977192068631	105.0157586508318	105.1337980948005	105.2124910574463	105.330530501415	105.4485699453838	105.5666093893525	105.6453023519983	105.763341795967	105.8813812399357	105.9994206839044	106.0781136465502	106.196153090519	106.3141925344877	106.4322319784564	106.5109249411022	106.628964385071	106.7470038290396	106.8256967916854	106.9437362356541	107.0617756796228	107.1404686422686	107.2585080862374	107.3372010488832	107.4552404928519	107.5339334554977	107.6519728994664	107.7700123434351	107.809358824758	107.8880517874038	108.0060912313726	108.0847841940184	108.2028236379871	108.281516600633	108.3995560446016	108.4782490072474	108.5962884512161	108.6749814138619	108.7536743765077	108.8717138204764	108.9504067831222	109.068446227091	109.1471391897368	109.2651786337055	109.3438715963513	109.46191104032	109.5406040029658	109.6192969656116	109.7373364095803	109.8160293722262	109.9340688161949	110.0127617788407	110.0914547414865	110.2094941854552	110.288187148101	110.3668801107468	110.4849195547155	110.5636125173613	110.6423054800071	110.760344923976	110.8390378866217	110.8783843679446	110.9570773305904	111.0357702932362	111.114463255882	111.2325026998507	111.3111956624965	111.3898886251423	111.4685815877881	111.5472745504339	111.6259675130797	111.7440069570485	111.8226999196943	111.9013928823401	111.9800858449859	112.0587788076317	112.1374717702775	112.2161647329233	112.334204176892	112.4128971395378	112.4915901021837	112.5702830648295	112.6489760274753	112.7276689901211	112.8063619527669	112.8850549154127	112.9637478780585	113.0424408407043	113.1211338033501	113.199826765996	113.2391732473188	113.3178662099646	113.3965591726105	113.4752521352563	113.5539450979021	113.6326380605479	113.6719845418708	113.7506775045166	113.8293704671624	113.9080634298082	113.986756392454	114.0654493550998	114.1441423177456	114.2228352803914	114.3015282430373	114.3802212056831	114.458914168329	114.5376071309747	114.6163000936205	114.6949930562663	114.7736860189121	114.8523789815579	114.9310719442037	115.0097649068495	115.0884578694953	115.1671508321411	115.2064973134641	115.2458437947869	115.3245367574328	115.4032297200786	115.4819226827244	115.5606156453702	115.5999621266931	115.678655089339	115.7573480519847	115.7966945333076	115.8753874959534	115.9540804585992	115.9934269399221	116.0721199025679	116.1508128652138	116.1901593465367	116.2688523091825	116.3475452718283	116.3868917531512	116.465584715797	116.5049311971199	116.5836241597657	116.6623171224115	116.7016636037344	116.7803565663802	116.8197030477031	116.859049529026	116.9377424916718	116.9770889729947	117.0557819356406	117.0951284169635	117.1738213796093	117.2131678609322	117.291860823578	117.331207304901	117.4099002675467	117.4492467488696	117.5279397115154	117.5672861928383	117.6066326741612	117.685325636807	117.7246721181299	117.8033650807757	117.8427115620986	117.9214045247444	117.9607510060674	118.0394439687132	118.0787904500361	118.1574834126819	118.1968298940048	118.2361763753277	118.2755228566506	118.3542158192964	118.3935623006193	118.4329087819422	118.511601744588	118.550948225911	118.6296411885567	118.6689876698796	118.7083341512025	118.7870271138484	118.8263735951712	118.9050665578171	118.94441303914	118.9837595204629	119.0624524831087	119.1017989644316	119.1804919270774	119.2198384084003	119.2591848897232	119.2985313710461	119.337877852369	119.4165708150148	119.4559172963377	119.5346102589835	119.5739567403064	119.6133032216293	119.6919961842752	119.731342665598	119.770689146921	119.8493821095668	119.8887285908897	119.9280750722126	119.9674215535355	120.0067680348584	120.0461145161813	120.1248074788271	120.16415396015	120.203500441473	120.2821934041187	120.3215398854416	120.3608863667645	120.4002328480874	120.4789258107332	120.5182722920561	120.557618773379	120.596965254702	120.6363117360249	120.6756582173478	120.7150046986707	120.7936976613165	120.8330441426394	120.8723906239623	120.9117371052852	120.9510835866081	121.0297765492539	121.0691230305768	121.1084695118997	121.1084695118997	121.1478159932226	121.2265089558684	121.2658554371913	121.3052019185142	121.3445483998371	121.38389488116	121.4232413624829	121.4625878438058	121.5019343251288	121.5412808064517	121.6199737690975	121.6593202504204	121.6986667317433	121.7380132130662	121.7773596943891	121.816706175712	121.8560526570349	121.8953991383578	121.9347456196807	121.9740921010036	122.0134385823265	122.0527850636494	122.0921315449723	122.1314780262952	122.1708245076181	122.210170988941	122.249517470264	122.2888639515868	122.3282104329097	122.3675569142327	122.4069033955555	122.4462498768785	122.4462498768785	122.4855963582014	122.5249428395243	122.5642893208472	122.6036358021701	122.642982283493	122.6823287648159	122.7216752461388	122.7610217274617	122.8003682087846	122.8003682087846	122.8397146901075	122.8790611714304	122.9184076527533	122.9577541340762	122.9971006153991	123.036447096722	123.0757935780449	123.1151400593678	123.1544865406907	123.1938330220136	123.1938330220136	123.2331795033365	123.2725259846595	123.3118724659823	123.3512189473053	123.3905654286282	123.4299119099511	123.4299119099511	123.469258391274	123.5086048725969	123.5479513539198	123.5872978352427	123.6266443165656	123.6659907978885	123.7053372792114	123.7446837605343	123.7446837605343	123.7840302418572	123.8233767231801	123.862723204503	123.902069685826	123.902069685826	123.9414161671488	123.9807626484717	124.0201091297946	124.0201091297946	124.0594556111175	124.0988020924404	124.1381485737633	124.1774950550863	124.2168415364091	124.2561880177321	124.2561880177321	124.295534499055	124.334880980378	124.3742274617008	124.4135739430237	124.4529204243466	124.4529204243466	124.4922669056695	124.5316133869924	124.5709598683153	124.6103063496382	124.6496528309611	124.6496528309611	124.688999312284	124.7283457936069	124.7676922749298	124.8070387562527	124.8463852375756	124.8857317188985	124.9250782002214	124.9644246815443	125.0037711628672	125.0431176441901	125.0431176441901	125.0824641255131	125.121810606836	125.161157088159	125.2005035694818	125.2005035694818	125.2398500508047	125.2791965321276	125.3185430134505	125.3578894947734	125.3972359760963	125.3972359760963	125.4365824574192	125.4365824574192	125.4759289387421	125.515275420065	125.515275420065	125.554621901388	125.5939683827108	125.5939683827108	125.6333148640337	125.6726613453566	125.6726613453566	125.7120078266795	125.7120078266795	125.7513543080024	125.7513543080024	125.7907007893253	125.7907007893253	125.8300472706482	125.8300472706482	125.8693937519711	125.8693937519711	125.908740233294	125.908740233294	125.9480867146169	125.9480867146169	125.98743319594	125.98743319594	126.0267796772628	126.0267796772628	126.0661261585857	126.0661261585857	126.0661261585857	126.1054726399086	126.1054726399086	126.1448191212315	126.1448191212315	126.1448191212315	126.1841656025544	126.1841656025544	126.1841656025544	126.2235120838773	126.2235120838773	126.2628585652002	126.2628585652002	126.3022050465231	126.3022050465231	126.3022050465231	126.341551527846	126.341551527846	126.341551527846	126.3808980091689	126.3808980091689	126.4202444904918	126.4202444904918	126.4202444904918	126.4595909718147	126.4595909718147	126.4989374531376	126.4989374531376	126.4989374531376	126.5382839344605	126.5382839344605	126.5776304157834	126.5776304157834	126.5776304157834	126.6169768971063	126.6169768971063	126.6563233784292	126.6563233784292	126.6563233784292	126.6956698597521	126.6956698597521	126.735016341075	126.735016341075	126.735016341075	126.7743628223979	126.7743628223979	126.8137093037208	126.8137093037208	126.8137093037208	126.8530557850438	126.8530557850438	126.8924022663667	126.8924022663667	126.8924022663667	126.9317487476895	126.9317487476895	126.9710952290125	126.9710952290125	126.9710952290125	127.0104417103354	127.0104417103354	127.0104417103354	127.0497881916583	127.0497881916583	127.0891346729812	127.0891346729812	127.0891346729812	127.1284811543041	127.1284811543041	127.1284811543041	127.167827635627	127.167827635627	127.167827635627	127.2071741169499	127.2071741169499	127.2465205982728	127.2465205982728	127.2465205982728	127.2858670795957	127.2858670795957	127.2858670795957	127.3252135609186	127.3252135609186	127.3252135609186	127.3645600422415	127.3645600422415	127.4039065235644	127.4039065235644	127.4039065235644	127.4432530048873	127.4432530048873	127.4432530048873	127.4825994862102	127.4825994862102	127.4825994862102	127.5219459675331	127.5219459675331	127.5219459675331	127.561292448856	127.561292448856	127.6006389301789	127.6006389301789	127.6006389301789	127.6399854115018	127.6399854115018	127.6399854115018	127.6793318928246	127.6793318928246	127.6793318928246	127.7186783741476	127.7186783741476	127.7186783741476	127.7580248554706	127.7580248554706	127.7580248554706	127.7973713367934	127.7973713367934	127.7973713367934	127.8367178181164	127.8367178181164	127.8367178181164	127.8760642994393	127.8760642994393	127.8760642994393	127.9154107807622	127.9154107807622	127.9547572620851	127.9547572620851	127.9547572620851	127.9547572620851	127.994103743408	127.994103743408	128.0334502247309	128.0334502247309	128.0334502247309	128.0727967060538	128.0727967060538	128.0727967060538	128.1121431873767	128.1121431873767	128.1121431873767	128.1514896686996	128.1514896686996	128.1514896686996	128.1908361500225	128.1908361500225	128.1908361500225	128.2301826313453	128.2301826313453	128.2301826313453	128.2695291126683	128.2695291126683	128.2695291126683	128.3088755939912	128.3088755939912	128.3088755939912	128.3482220753141	128.3482220753141	128.3482220753141	128.387568556637	128.387568556637	128.387568556637	128.42691503796	128.42691503796	128.42691503796	128.4662615192828	128.4662615192828	128.4662615192828	128.5056080006057	128.5056080006057	128.5056080006057	128.5449544819286	128.5449544819286	128.5449544819286	128.5843009632515	128.5843009632515	128.5843009632515	128.5843009632515	128.6236474445744	128.6236474445744	128.6236474445744	128.6629939258974	128.6629939258974	128.6629939258974	128.7023404072202	128.7023404072202	128.7023404072202	128.7416868885432	128.7416868885432	128.7416868885432	128.781033369866	128.781033369866	128.781033369866	128.820379851189	128.820379851189	128.820379851189	128.820379851189	128.859726332512	128.859726332512	128.859726332512	128.8990728138347	128.8990728138347	128.8990728138347	128.9384192951577	128.9384192951577	128.9384192951577	128.9777657764806	128.9777657764806	128.9777657764806	129.0171122578035	129.0171122578035	129.0171122578035	129.0564587391264	129.0564587391264	129.0564587391264	129.0958052204493	129.0958052204493	129.0958052204493	129.1351517017721	129.1351517017721	129.1351517017721	129.1351517017721	129.1744981830951	129.1744981830951	129.2138446644179	129.2138446644179	129.2138446644179	129.2531911457409	129.2531911457409	129.2531911457409	129.2925376270638	129.2925376270638	129.2925376270638	129.3318841083867	129.3318841083867	129.3318841083867	129.3712305897096	129.3712305897096	129.3712305897096	129.4105770710325	129.4105770710325	129.4105770710325	129.4499235523554	129.4499235523554	129.4499235523554	129.4892700336783	129.4892700336783	129.4892700336783	129.5286165150012	129.5286165150012	129.5286165150012	129.5679629963242	129.5679629963242	129.5679629963242	129.607309477647	129.607309477647	129.607309477647	129.64665595897	129.64665595897	129.64665595897	129.686002440293	129.686002440293	129.686002440293	129.7253489216158	129.7253489216158	129.7253489216158	129.7646954029387	129.7646954029387	129.7646954029387	129.8040418842616	129.8040418842616	129.8040418842616	129.8433883655845	129.8433883655845	129.8433883655845	129.8827348469074	129.8827348469074	129.8827348469074	129.9220813282303	129.9220813282303	129.9220813282303	129.9614278095532	129.9614278095532	129.9614278095532	129.9614278095532	130.0007742908761	130.0007742908761	130.0007742908761	130.040120772199	130.040120772199	130.040120772199	130.0794672535219	130.0794672535219	130.0794672535219	130.1188137348447	130.1188137348447	130.1188137348447	130.1188137348447	130.1581602161677	130.1581602161677	130.1581602161677	130.1975066974906	130.1975066974906	130.1975066974906	130.2368531788135	130.2368531788135	130.2368531788135	130.2368531788135	130.2761996601364	130.2761996601364	130.2761996601364	130.2761996601364	130.3155461414593	130.3155461414593	130.3155461414593	130.3548926227822	130.3548926227822	130.3548926227822	130.3548926227822	130.3942391041051	130.3942391041051	130.3942391041051	130.3942391041051	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.433585585428	130.472932066751	130.472932066751	130.472932066751	130.472932066751	130.512278548074	130.512278548074	130.512278548074	130.512278548074	130.5516250293968	130.5516250293968	130.5516250293968	130.5516250293968	130.5516250293968	130.5909715107197	130.5909715107197	130.5909715107197	130.5909715107197	130.5909715107197	130.6303179920426	130.6303179920426	130.6303179920426	130.6303179920426	130.6303179920426	130.6696644733655	130.6696644733655	130.6696644733655	130.6696644733655	130.6696644733655	130.7090109546884	130.7090109546884	130.7090109546884	130.7090109546884	130.7090109546884	130.7483574360113	130.7483574360113	130.7483574360113	130.7483574360113	130.7483574360113	130.7877039173342	130.7877039173342	130.7877039173342	130.7877039173342	130.7877039173342	130.8270503986571	130.8270503986571	130.8270503986571	130.8270503986571	130.8270503986571	130.86639687998	130.86639687998	130.86639687998	130.86639687998	130.9057433613029	130.9057433613029	130.9057433613029	130.9057433613029	130.9057433613029	130.9450898426258	130.9450898426258	130.9450898426258	130.9450898426258	130.9844363239487	130.9844363239487	130.9844363239487	130.9844363239487	131.0237828052716	131.0237828052716	131.0237828052716	131.0237828052716	131.0631292865945	131.0631292865945	131.0631292865945	131.0631292865945	131.0631292865945	131.1024757679174	131.1024757679174	131.1024757679174	131.1024757679174	131.1418222492403	131.1418222492403	131.1418222492403	131.1418222492403	131.1811687305632	131.1811687305632	131.1811687305632	131.1811687305632	131.2205152118861	131.2205152118861	131.2205152118861	131.2205152118861	131.259861693209	131.259861693209	131.259861693209	131.259861693209	131.259861693209	131.2992081745319	131.2992081745319	131.2992081745319	131.2992081745319	131.3385546558548	131.3385546558548	131.3385546558548	131.3385546558548	131.3779011371778	131.3779011371778	131.3779011371778	131.3779011371778	131.4172476185007	131.4172476185007	131.4172476185007	131.4172476185007	131.4565940998235	131.4565940998235	131.4565940998235	131.4565940998235	131.4959405811465	131.4959405811465	131.4959405811465	131.4959405811465	131.5352870624694	131.5352870624694	131.5352870624694	131.5352870624694	131.5746335437923	131.5746335437923	131.5746335437923	131.5746335437923	131.6139800251152	131.6139800251152	131.6139800251152	131.6139800251152	131.6533265064381	131.6533265064381	131.6533265064381	131.6533265064381	131.692672987761	131.692672987761	131.692672987761	131.692672987761	131.732019469084	131.732019469084	131.732019469084	131.732019469084	131.732019469084	131.7713659504068	131.7713659504068	131.7713659504068	131.7713659504068	131.7713659504068	131.8107124317297	131.8107124317297	131.8107124317297	131.8107124317297	131.8107124317297	131.8500589130526	131.8500589130526	131.8500589130526	131.8500589130526	131.8500589130526	131.8500589130526	131.8894053943755	131.8894053943755	131.8894053943755	131.8894053943755	131.8894053943755	131.8894053943755	131.8894053943755	131.8894053943755	131.9287518756984	131.9287518756984	131.9287518756984	131.9287518756984	131.9287518756984	131.9287518756984	131.9287518756984	131.9287518756984	131.9287518756984	131.9287518756984	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	131.9680983570213	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0074448383442	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.0467913196671	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.08613780099	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1254842823129	132.1648307636358	132.1648307636358	132.1648307636358	132.1648307636358	132.1648307636358	132.1648307636358	132.2041772449587	132.2041772449587	132.2041772449587	132.2041772449587	132.2435237262815	132.2435237262815	132.2435237262815	132.2828702076046	132.2828702076046	132.2828702076046	132.3222166889274	132.3222166889274	132.3222166889274	132.3615631702503	132.3615631702503	132.3615631702503	132.4009096515733	132.4009096515733	132.4402561328962	132.4402561328962	132.4796026142191	132.4796026142191	132.4796026142191	132.518949095542	132.518949095542	132.558295576865	132.558295576865	132.5976420581878	132.5976420581878	132.6369885395107	132.6369885395107	132.6763350208336	132.6763350208336	132.7156815021565	132.7550279834794	132.7550279834794	132.7943744648022	132.7943744648022	132.8337209461252	132.8337209461252	132.8730674274481	132.8730674274481	132.912413908771	132.912413908771	132.912413908771	132.951760390094	132.951760390094	132.9911068714168	132.9911068714168	133.0304533527397	133.0304533527397	133.0304533527397	133.0697998340626	133.0697998340626	133.0697998340626	133.0697998340626	133.1091463153855	133.1091463153855	133.1091463153855	133.1091463153855	133.1484927967084	133.1484927967084	133.1484927967084	133.1484927967084	133.1484927967084	133.1484927967084	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1878392780314	133.1484927967084	133.1484927967084	133.1484927967084	133.1484927967084	133.1091463153855	133.1091463153855	133.1091463153855	133.0697998340626	133.0697998340626	133.0697998340626	133.0304533527397	133.0304533527397	132.9911068714168	132.9911068714168	132.951760390094	132.951760390094	132.912413908771	132.912413908771	132.8730674274481	132.8337209461252	132.8337209461252	132.7943744648022	132.7550279834794	132.7156815021565	132.7156815021565	132.6763350208336	132.6369885395107	132.5976420581878	132.558295576865	132.518949095542	132.518949095542	132.4402561328962	132.4009096515733	132.3615631702503	132.2828702076046	132.2041772449587	132.1254842823129	132.0074448383442	131.9287518756984	131.8107124317297	131.732019469084	131.6139800251152	131.4959405811465	131.4172476185007	131.259861693209	131.1811687305632	131.0631292865945	130.9450898426258	130.86639687998	130.7483574360113	130.6303179920426	130.512278548074	130.3942391041051	130.3155461414593	130.1975066974906	130.0794672535219	129.9614278095532	129.8040418842616	129.7253489216158	129.607309477647	129.4892700336783	129.3318841083867	129.2531911457409	129.0958052204493	129.0171122578035	128.8990728138347	128.7416868885432	128.6629939258974	128.5449544819286	128.387568556637	128.3088755939912	128.1908361500225	128.0334502247309	127.9154107807622	127.7973713367934	127.6399854115018	127.5219459675331	127.4432530048873	127.3252135609186	127.167827635627	127.0497881916583	126.9317487476895	126.8137093037208	126.6956698597521	126.4989374531376	126.3808980091689	126.2628585652002	126.1448191212315	126.0267796772628	125.8693937519711	125.7513543080024	125.5939683827108	125.4759289387421	125.3578894947734	125.2398500508047	125.121810606836	124.9250782002214	124.8070387562527	124.688999312284	124.5316133869924	124.4135739430237	124.295534499055	124.1774950550863	124.0594556111175	123.902069685826	123.7840302418572	123.5872978352427	123.469258391274	123.3118724659823	123.1938330220136	123.036447096722	122.9184076527533	122.7610217274617	122.642982283493	122.4855963582014	122.3675569142327	122.210170988941	122.0134385823265	121.8953991383578	121.7380132130662	121.5806272877746	121.4625878438058	121.3052019185142	121.1478159932226	121.0297765492539	120.8723906239623	120.7150046986707	120.557618773379	120.4395793294103	120.2821934041187	120.1248074788271	119.9674215535355	119.810035628244	119.6133032216293	119.4559172963377	119.2985313710461	119.1411454457545	118.9837595204629	118.8263735951712	118.6689876698796	118.511601744588	118.3542158192964	118.1968298940048	118.0394439687132	117.8427115620986	117.685325636807	117.5279397115154	117.3705537862238	117.1738213796093	117.0164354543176	116.8197030477031	116.6623171224115	116.465584715797	116.1901593465367	115.9934269399221	115.7966945333076	115.5999621266931	115.4032297200786	115.2064973134641	115.0097649068495	114.813032500235	114.6163000936205	114.3802212056831	114.1834887990685	113.986756392454	113.7506775045166	113.5539450979021	113.3178662099646	113.0817873220272	112.8850549154127	112.6489760274753	112.4128971395378	112.1768182516004	111.8226999196943	111.5866210317568	111.3111956624965	111.0751167745591	110.7996914052988	110.5242660360384	110.2488406667781	109.9734152975178	109.6586434469345	109.3438715963513	109.0290997457681	108.7143278951848	108.3602095632787	108.0060912313726	107.6126264181435	107.2191616049145	106.589617903748	106.1174601278731	105.4879164267067	104.5042543936341	97.5792736808029	37.10373188749884	0.118039443968713	-1.298433883655845	-1.377126846301653	-1.298433883655845	-1.33778036497875	-1.416473327624558	-1.33778036497875	-1.33778036497875	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.416473327624558	-1.416473327624558	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.416473327624558	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	-1.377126846301653	Aluminium	0.00012962962962963	0.0	0.0	3.7037037037037E-5	0.00012962962962963	0.000259259259259259	0.00037037037037037	0.000481481481481481	0.000592592592592592	0.000722222222222222	0.000851851851851852	0.000962962962962963	0.00109259259259259	0.00122222222222222	0.00133333333333333	0.00148148148148148	0.00159259259259259	0.0017037037037037	0.00185185185185185	0.00196296296296296	0.00207407407407407	0.00222222222222222	0.00233333333333333	0.00244444444444444	0.00259259259259259	0.0027037037037037	0.00285185185185185	0.00296296296296296	0.00307407407407407	0.00322222222222222	0.00333333333333333	0.00344444444444444	0.00359259259259259	0.0037037037037037	0.00383333333333333	0.00396296296296296	0.00407407407407407	0.0042037037037037	0.00433333333333333	0.00444444444444444	0.00457407407407407	0.0047037037037037	0.00483333333333333	0.00494444444444444	0.00507407407407407	0.0052037037037037	0.00531481481481481	0.00546296296296296	0.00557407407407407	0.00568518518518518	0.00583333333333333	0.00594444444444444	0.00609259259259259	0.0062037037037037	0.00631481481481481	0.00646296296296296	0.00657407407407407	0.00668518518518518	0.00683333333333333	0.00694444444444444	0.00707407407407407	0.0072037037037037	0.00731481481481481	0.00744444444444444	0.00757407407407407	0.00768518518518518	0.00781481481481481	0.00794444444444444	0.00807407407407407	0.00818518518518518	0.00833333333333333	0.00844444444444444	0.00855555555555555	0.0087037037037037	0.00881481481481481	0.00892592592592592	0.00907407407407407	0.00918518518518518	0.00933333333333333	0.00944444444444444	0.00957407407407407	0.0097037037037037	0.00981481481481481	0.00992592592592592	0.0100740740740741	0.0102037037037037	0.0103148148148148	0.0104444444444444	0.0105740740740741	0.0106851851851852	0.0108148148148148	0.0109444444444444	0.0110555555555556	0.0112037037037037	0.0113148148148148	0.0114259259259259	0.0115555555555556	0.0116851851851852	0.0117962962962963	0.0119444444444444	0.0120555555555556	0.0121666666666667	0.0123148148148148	0.0124259259259259	0.0125740740740741	0.0126851851851852	0.0127962962962963	0.0129444444444444	0.0130555555555556	0.0131851851851852	0.0133148148148148	0.0134259259259259	0.0135555555555556	0.0136851851851852	0.0138148148148148	0.0139259259259259	0.0140555555555556	0.0141851851851852	0.0142962962962963	0.0144444444444444	0.0145555555555556	0.0146666666666667	0.0148148148148148	0.0149259259259259	0.015037037037037	0.0151851851851852	0.0152962962962963	0.0154444444444444	0.0155555555555556	0.0156666666666667	0.0158148148148148	0.0159259259259259	0.016037037037037	0.0161851851851852	0.0162962962962963	0.0164259259259259	0.0165555555555556	0.0166666666666667	0.0167962962962963	0.0169259259259259	0.0170555555555556	0.0171666666666667	0.0173148148148148	0.0174259259259259	0.017537037037037	0.0176851851851852	0.0177962962962963	0.0179444444444444	0.0180555555555555	0.0181666666666667	0.0183148148148148	0.0184259259259259	0.018537037037037	0.0186666666666667	0.0187962962962963	0.0189259259259259	0.019037037037037	0.0191851851851852	0.0192962962962963	0.0194444444444444	0.0195555555555556	0.0196666666666667	0.0198148148148148	0.0199259259259259	0.020037037037037	0.0201851851851852	0.0202962962962963	0.0204259259259259	0.0205555555555556	0.0206666666666667	0.0207962962962963	0.0209259259259259	0.0210555555555556	0.0211666666666667	0.0212962962962963	0.0214259259259259	0.021537037037037	0.0216851851851852	0.0217962962962963	0.0219074074074074	0.0220555555555556	0.0221666666666667	0.0223148148148148	0.0224259259259259	0.022537037037037	0.0226851851851852	0.0227962962962963	0.0229074074074074	0.0230555555555556	0.0231666666666667	0.0232962962962963	0.0234259259259259	0.023537037037037	0.0236481481481481	0.0237962962962963	0.0239074074074074	0.0240185185185185	0.0241666666666667	0.0242777777777778	0.0244074074074074	0.024537037037037	0.0246481481481481	0.0247777777777778	0.0249074074074074	0.0250185185185185	0.0251481481481481	0.0252777777777778	0.0254074074074074	0.0255185185185185	0.0256481481481481	0.0257592592592593	0.0258888888888889	0.0260185185185185	0.0261481481481481	0.0262592592592593	0.0263888888888889	0.0265185185185185	0.0266296296296296	0.0267592592592593	0.0268888888888889	0.027	0.0271481481481481	0.0272592592592593	0.0273703703703704	0.0275	0.0276296296296296	0.0277407407407407	0.0278888888888889	0.028	0.0281111111111111	0.0282592592592593	0.0283703703703704	0.0285185185185185	0.0286296296296296	0.0287407407407407	0.0288888888888889	0.029	0.0291111111111111	0.0292592592592593	0.0293703703703704	0.0294814814814815	0.0296296296296296	0.0297407407407407	0.0298703703703704	0.03	0.0301111111111111	0.0302407407407407	0.0303703703703704	0.0305	0.0306111111111111	0.0307407407407407	0.0308518518518518	0.0309814814814815	0.0311296296296296	0.0312407407407407	0.0313518518518518	0.0315	0.0316111111111111	0.0317592592592593	0.0318703703703704	0.0319814814814815	0.0321296296296296	0.0322407407407407	0.0323518518518518	0.0325	0.0326111111111111	0.0327407407407407	0.0328703703703704	0.0329814814814815	0.0331111111111111	0.0332407407407407	0.0333703703703704	0.0334814814814815	0.0336296296296296	0.0337407407407407	0.0338518518518518	0.034	0.0341111111111111	0.0342222222222222	0.0343703703703704	0.0344814814814815	0.0346296296296296	0.0347407407407407	0.0348518518518518	0.035	0.0351111111111111	0.0352222222222222	0.0353703703703704	0.0354814814814815	0.0356111111111111	0.0357407407407407	0.0358518518518518	0.0359814814814815	0.0361111111111111	0.0362222222222222	0.0363518518518518	0.0364814814814815	0.0366111111111111	0.0367222222222222	0.0368518518518518	0.036962962962963	0.0370925925925926	0.0372037037037037	0.0373518518518518	0.037462962962963	0.0375740740740741	0.0377222222222222	0.0378333333333333	0.0379814814814815	0.0380925925925926	0.0382037037037037	0.0383518518518518	0.038462962962963	0.0385740740740741	0.0387222222222222	0.0388333333333333	0.038962962962963	0.0390925925925926	0.0392037037037037	0.0393148148148148	0.0394629629629629	0.0395740740740741	0.0397037037037037	0.0398333333333333	0.0399444444444444	0.0400740740740741	0.0402037037037037	0.0403148148148148	0.0404444444444444	0.0405740740740741	0.0407037037037037	0.0408148148148148	0.0409444444444444	0.0410740740740741	0.0412222222222222	0.0413333333333333	0.0414444444444444	0.0415555555555556	0.0417037037037037	0.0418148148148148	0.041962962962963	0.0420740740740741	0.0421851851851852	0.0423333333333333	0.0424444444444444	0.0425740740740741	0.0427037037037037	0.0428148148148148	0.0429444444444444	0.0430740740740741	0.0432037037037037	0.0433148148148148	0.0434444444444444	0.0435740740740741	0.0436851851851852	0.0438333333333333	0.0439444444444444	0.0440555555555555	0.0442037037037037	0.0443148148148148	0.044462962962963	0.0445740740740741	0.0446851851851852	0.0448333333333333	0.0449444444444444	0.0450740740740741	0.0452037037037037	0.0453148148148148	0.0454444444444444	0.0455740740740741	0.0457037037037037	0.0458148148148148	0.0459444444444444	0.0460740740740741	0.0461851851851852	0.0463333333333333	0.0464444444444444	0.0465555555555555	0.0467037037037037	0.0468148148148148	0.046962962962963	0.0470740740740741	0.0472037037037037	0.0473333333333333	0.0474444444444444	0.0475740740740741	0.0477037037037037	0.0478333333333333	0.0479444444444444	0.0480740740740741	0.0482037037037037	0.0483148148148148	0.048462962962963	0.0485740740740741	0.0486851851851852	0.0488333333333333	0.0489444444444444	0.0490925925925926	0.0492037037037037	0.0493148148148148	0.0494629629629629	0.0495740740740741	0.0496851851851852	0.0498333333333333	0.0499444444444444	0.0500740740740741	0.0502037037037037	0.0503148148148148	0.0504444444444444	0.0505740740740741	0.0506851851851852	0.0508148148148148	0.0509444444444444	0.0510740740740741	0.0511851851851852	0.0513333333333333	0.0514444444444444	0.0515925925925926	0.0517037037037037	0.0518148148148148	0.0519259259259259	0.0520740740740741	0.0521851851851852	0.0523333333333333	0.0524444444444444	0.0525740740740741	0.0527037037037037	0.0528148148148148	0.0529444444444444	0.0530740740740741	0.0532037037037037	0.0533148148148148	0.053462962962963	0.0535740740740741	0.0537222222222222	0.0538333333333333	0.0539444444444444	0.0540555555555555	0.0542037037037037	0.0543148148148148	0.054462962962963	0.0545740740740741	0.0546851851851852	0.0548333333333333	0.0549444444444444	0.0550740740740741	0.0552037037037037	0.0553333333333333	0.0554444444444444	0.0555555555555555	0.0557037037037037	0.0558148148148148	0.0559259259259259	0.0560740740740741	0.0561851851851852	0.0563333333333333	0.0564444444444444	0.0565555555555555	0.0567037037037037	0.0568148148148148	0.0569444444444444	0.0570740740740741	0.0572037037037037	0.0573148148148148	0.0574444444444444	0.0575740740740741	0.0576851851851852	0.0578333333333333	0.0579444444444444	0.0580555555555555	0.0582037037037037	0.0583148148148148	0.0584259259259259	0.0585740740740741	0.0586851851851852	0.0588333333333333	0.0589444444444444	0.0590555555555555	0.0592037037037037	0.0593148148148148	0.0594259259259259	0.0595740740740741	0.0596851851851852	0.0598148148148148	0.0599444444444444	0.0600555555555555	0.0601851851851852	0.0603148148148148	0.0604444444444444	0.0605555555555555	0.0606851851851852	0.0608148148148148	0.0609259259259259	0.0610555555555555	0.0611851851851852	0.0612962962962963	0.0614259259259259	0.0615555555555555	0.0616666666666667	0.0618148148148148	0.0619259259259259	0.062037037037037	0.0621851851851852	0.0622962962962963	0.0624074074074074	0.062537037037037	0.0626666666666666	0.0627777777777778	0.0629259259259259	0.063037037037037	0.0631481481481481	0.0632962962962963	0.0634074074074074	0.0635185185185185	0.0636666666666667	0.0637777777777778	0.0638888888888889	0.064037037037037	0.0641481481481481	0.0642592592592593	0.0644074074074074	0.0645185185185185	0.0646296296296296	0.0647777777777778	0.0648888888888889	0.065	0.0651481481481481	0.0652592592592592	0.0653703703703704	0.0655185185185185	0.0656296296296296	0.0657777777777778	0.0658888888888889	0.066	0.0661111111111111	0.0662592592592592	0.0663703703703704	0.0665185185185185	0.0666296296296296	0.0667407407407407	0.0668888888888889	0.067	0.0671296296296296	0.0672592592592592	0.0673703703703704	0.0674814814814815	0.0676296296296296	0.0677407407407407	0.0678703703703704	0.068	0.0681111111111111	0.0682407407407407	0.0683703703703704	0.0684814814814815	0.0686111111111111	0.0687407407407407	0.0688518518518518	0.0689629629629629	0.0691111111111111	0.0692222222222222	0.0693518518518518	0.0694814814814815	0.0695925925925926	0.0697222222222222	0.0698518518518518	0.0699814814814815	0.0700925925925926	0.0702222222222222	0.0703518518518518	0.070462962962963	0.0706111111111111	0.0707222222222222	0.0708703703703704	0.0709814814814815	0.0710925925925926	0.0712407407407407	0.0713518518518519	0.071462962962963	0.0716111111111111	0.0717222222222222	0.0718333333333333	0.0719814814814815	0.0720925925925926	0.0722222222222222	0.0723518518518518	0.072462962962963	0.0725925925925926	0.0727222222222222	0.0728518518518518	0.072962962962963	0.0730925925925926	0.0732222222222222	0.0733333333333333	0.0734814814814815	0.0735925925925926	0.0737037037037037	0.0738518518518518	0.073962962962963	0.0740740740740741	0.0742222222222222	0.0743333333333333	0.074462962962963	0.0745925925925926	0.0747037037037037	0.0748333333333333	0.074962962962963	0.0750740740740741	0.0752037037037037	0.0753333333333333	0.075462962962963	0.0755740740740741	0.0757037037037037	0.0758333333333333	0.0759444444444444	0.0760740740740741	0.0762037037037037	0.0763148148148148	0.0764629629629629	0.0765740740740741	0.0766851851851852	0.0768333333333333	0.0769444444444444	0.0770925925925926	0.0772037037037037	0.0773148148148148	0.0774629629629629	0.0775740740740741	0.0777037037037037	0.0778333333333333	0.0779444444444444	0.0780740740740741	0.0782037037037037	0.0783333333333333	0.0784444444444444	0.0785740740740741	0.0787037037037037	0.0788148148148148	0.078962962962963	0.0790740740740741	0.0791851851851852	0.0793333333333333	0.0794444444444444	0.0795555555555556	0.0797037037037037	0.0798148148148148	0.0799629629629629	0.0800740740740741	0.0802037037037037	0.0803333333333333	0.0804444444444444	0.0805740740740741	0.0807037037037037	0.0808333333333333	0.0809444444444444	0.0810740740740741	0.0812037037037037	0.0813148148148148	0.0814629629629629	0.0815740740740741	0.0816851851851852	0.0818333333333333	0.0819444444444444	0.0820925925925926	0.0822037037037037	0.0823148148148148	0.082462962962963	0.082574074074074	0.0827037037037037	0.0828333333333333	0.0829444444444444	0.083074074074074	0.0832037037037037	0.0833333333333333	0.0834444444444444	0.0835740740740741	0.0837037037037037	0.0838148148148148	0.0839629629629629	0.0840740740740741	0.0841851851851852	0.0843333333333333	0.0844444444444444	0.0845555555555555	0.0847037037037037	0.0848148148148148	0.0849629629629629	0.0850740740740741	0.0851851851851852	0.0853333333333333	0.0854444444444444	0.0855740740740741	0.0857037037037037	0.0858148148148148	0.0859444444444444	0.086074074074074	0.0862037037037037	0.0863148148148148	0.0864444444444444	0.086574074074074	0.0866851851851852	0.0868148148148148	0.0869444444444444	0.0870555555555555	0.0872037037037037	0.0873148148148148	0.0874259259259259	0.0875740740740741	0.0876851851851852	0.0878333333333333	0.0879444444444444	0.0880555555555555	0.0881666666666667	0.0883148148148148	0.0884259259259259	0.088537037037037	0.0886851851851852	0.0887962962962963	0.0889074074074074	0.0890555555555555	0.0891666666666667	0.0893148148148148	0.0894259259259259	0.089537037037037	0.0896851851851852	0.0897962962962963	0.0899074074074074	0.0900555555555555	0.0901666666666666	0.0902962962962963	0.0904259259259259	0.090537037037037	0.0906481481481481	0.0907962962962963	0.0909074074074074	0.091037037037037	0.0911666666666666	0.0912962962962963	0.0914074074074074	0.091537037037037	0.0916481481481481	0.0917777777777778	0.0919074074074074	0.0920185185185185	0.0921481481481481	0.0922777777777778	0.0924074074074074	0.0925185185185185	0.0926296296296296	0.0927777777777778	0.0928888888888889	0.093	0.0931481481481481	0.0932592592592592	0.0934074074074074	0.0935185185185185	0.0936296296296296	0.0937777777777778	0.0938888888888889	0.094	0.0941111111111111	0.0942592592592592	0.0943703703703703	0.0945185185185185	0.0946296296296296	0.0947592592592592	0.0948888888888889	0.095	0.0951296296296296	0.0952592592592592	0.0953703703703704	0.0955	0.0956296296296296	0.0957407407407407	0.0958703703703703	0.096	0.0961296296296296	0.0962407407407407	0.0963703703703703	0.0965	0.0966111111111111	0.0967407407407407	0.0968703703703703	0.0969814814814815	0.0971296296296296	0.0972407407407407	0.0973518518518518	0.0975	0.0976111111111111	0.0977222222222222	0.0978703703703703	0.0979814814814815	0.0980925925925926	0.0982407407407407	0.0983518518518518	0.0984629629629629	0.0986111111111111	0.0987222222222222	0.0988703703703703	0.0989814814814814	0.0990925925925926	0.0992407407407407	0.0993518518518518	0.0994629629629629	0.0996111111111111	0.0997222222222222	0.0998333333333333	0.0999814814814814	0.100092592592593	0.100222222222222	0.100351851851852	0.100462962962963	0.100592592592593	0.100722222222222	0.100833333333333	0.100962962962963	0.101092592592593	0.101222222222222	0.101333333333333	0.101462962962963	0.101592592592593	0.101703703703704	0.101833333333333	0.101962962962963	0.102074074074074	0.102203703703704	0.102333333333333	0.102444444444444	0.102592592592593	0.102703703703704	0.102814814814815	0.102962962962963	0.103074074074074	0.103185185185185	0.103333333333333	0.103444444444444	0.103592592592593	0.103703703703704	0.103814814814815	0.103962962962963	0.104074074074074	0.104185185185185	0.104333333333333	0.104444444444444	0.104574074074074	0.104703703703704	0.104814814814815	0.104944444444444	0.105074074074074	0.105185185185185	0.105314814814815	0.105444444444444	0.105555555555556	0.105685185185185	0.105814814814815	0.105944444444444	0.106055555555556	0.106203703703704	0.106314814814815	0.106425925925926	0.106574074074074	0.106685185185185	0.106833333333333	0.106944444444444	0.107055555555556	0.107203703703704	0.107314814814815	0.107425925925926	0.107574074074074	0.107685185185185	0.107814814814815	0.107944444444444	0.108055555555556	0.108185185185185	0.108314814814815	0.108444444444444	0.108555555555556	0.108703703703704	0.108814814814815	0.108925925925926	0.109074074074074	0.109185185185185	0.109333333333333	0.109444444444444	0.109574074074074	0.109703703703704	0.109833333333333	0.109944444444444	0.110074074074074	0.110203703703704	0.110314814814815	0.110444444444444	0.110574074074074	0.110685185185185	0.110833333333333	0.110944444444444	0.111092592592593	0.111203703703704	0.111314814814815	0.111444444444444	0.111592592592593	0.111703703703704	0.111814814814815	0.111962962962963	0.112074074074074	0.112185185185185	0.112444444444444	0.11262962962963	0.112703703703704	0.112796296296296	0.112907407407407	0.113055555555556	0.113166666666667	0.113277777777778	0.113425925925926	0.113537037037037	0.113666666666667	0.113796296296296	0.113907407407407	0.114037037037037	0.114166666666667	0.114296296296296	0.114407407407407	0.114555555555556	0.114666666666667	0.114777777777778	0.114925925925926	0.115037037037037	0.115148148148148	0.115296296296296	0.115407407407407	0.115518518518519	0.115666666666667	0.115796296296296	0.115925925925926	0.116037037037037	0.116166666666667	0.116296296296296	0.116407407407407	0.116537037037037	0.116666666666667	0.116777777777778	0.116907407407407	0.117037037037037	0.117148148148148	0.117277777777778	0.117407407407407	0.117518518518519	0.117648148148148	0.117777777777778	0.117907407407407	0.118018518518519	0.118148148148148	0.118277777777778	0.118388888888889	0.118537037037037	0.118648148148148	0.118759259259259	0.118907407407407	0.119018518518518	0.119166666666667	0.119277777777778	0.119407407407407	0.119537037037037	0.119648148148148	0.119777777777778	0.119907407407407	0.120018518518519	0.120148148148148	0.120277777777778	0.120407407407407	0.120518518518519	0.120666666666667	0.120777777777778	0.120888888888889	0.121037037037037	0.121148148148148	0.121296296296296	0.121407407407407	0.121518518518519	0.121666666666667	0.121777777777778	0.121888888888889	0.122037037037037	0.122148148148148	0.122277777777778	0.122407407407407	0.122518518518519	0.122648148148148	0.122777777777778	0.122907407407407	0.123018518518519	0.123148148148148	0.123277777777778	0.123388888888889	0.123537037037037	0.123648148148148	0.123759259259259	0.123907407407407	0.124018518518519	0.124166666666667	0.124277777777778	0.124388888888889	0.124537037037037	0.124648148148148	0.124777777777778	0.124907407407407	0.125018518518519	0.125148148148148	0.125277777777778	0.125388888888889	0.125518518518518	0.125648148148148	0.125759259259259	0.125888888888889	0.126018518518518	0.126148148148148	0.126259259259259	0.126388888888889	0.1265	0.12662962962963	0.126759259259259	0.126888888888889	0.127	0.12712962962963	0.127259259259259	0.12737037037037	0.1275	0.12762962962963	0.127740740740741	0.12787037037037	0.128	0.128111111111111	0.128240740740741	0.12837037037037	0.128481481481481	0.128611111111111	0.128740740740741	0.128851851851852	0.128981481481481	0.129111111111111	0.129222222222222	0.12937037037037	0.129481481481481	0.129592592592593	0.129740740740741	0.129851851851852	0.129981481481481	0.130111111111111	0.130222222222222	0.130351851851852	0.130481481481481	0.130592592592593	0.130722222222222	0.130851851851852	0.130981481481481	-0.0393464813229044	-0.0393464813229044	-0.0393464813229044	-0.0393464813229044	-0.0393464813229044	-0.0393464813229044	0.0	0.0786929626458088	0.157385925291618	0.275425369260331	3.5805298003843	4.328112945519481	5.115042571977569	5.862625717112754	6.610208862247936	7.003673675476981	7.751256820612165	8.498839965747348	9.24642311088253	9.95465977469481	10.26943162527805	10.97766828909032	11.6465584715797	12.31544865406907	13.02368531788135	13.69257550037073	14.71558401476624	15.38447419725562	16.09271086106789	16.76160104355727	17.78460955795278	18.45349974044216	19.12238992293153	19.79128010542091	20.49951676923319	21.16840695172256	21.83729713421194	22.46684083537841	23.48984934977391	24.11939305094039	24.78828323342976	25.41782693459623	26.08671711708561	26.71626081825208	27.38515100074146	28.01469470190792	28.68358488439729	29.31312858556377	29.94267228673023	30.57221598789671	31.51653153964642	32.10672875948998	32.73627246065644	33.32646968050002	33.91666690034358	34.50686412018715	35.09706134003071	35.68725855987427	36.23810929839493	36.7889600369156	37.37915725675917	37.93000799527983	38.4415122524776	38.99236299099825	39.503867248196	40.01537150539377	40.52687576259152	41.03838001978928	41.51053779566412	42.02204205286188	42.49419982873674	42.96635760461159	43.43851538048645	43.91067315636129	44.38283093223615	44.85498870811099	45.28780000266294	45.7599577785378	46.19276907308974	46.6255803676417	47.29447055013107	47.72728184468302	48.16009313923497	48.59290443378692	49.02571572833887	49.45852702289081	49.89133831744277	50.32414961199471	50.71761442522375	51.1504257197757	51.58323701432764	51.9767018275567	52.40951312210864	52.80297793533769	53.23578922988964	53.62925404311868	54.06206533767063	54.45553015089968	54.88834144545162	55.28180625868066	55.71461755323259	56.10808236646166	56.50154717969069	56.89501199291975	57.28847680614878	57.68194161937782	58.07540643260688	58.42952476451302	58.82298957774204	59.17710790964819	59.57057272287725	59.92469105478337	60.31815586801243	60.67227419991857	61.06573901314761	61.45920382637664	61.81332215828279	62.20678697151184	62.60025178474088	62.95437011664701	63.34783492987606	63.7019532617822	64.05607159368833	64.44953640691738	64.80365473882351	65.15777307072963	65.55123788395871	65.90535621586484	66.25947454777098	66.57424639835421	66.92836473026037	67.2431365808436	67.55790843142682	67.87268028201007	68.18745213259328	68.46287750185363	68.73830287111396	69.0137282403743	69.28915360963462	69.56457897889494	69.87935082947818	70.1547761987385	70.46954804932175	70.784319899905	71.09909175048821	71.45321008239436	71.80732841430051	72.12210026488373	72.43687211546695	72.7909904473731	73.10576229795633	73.42053414853957	73.69595951779989	74.01073136838315	74.16811729367475	74.4435426629351	74.71896803219542	74.95504692013285	75.1911258080703	75.4272046960077	75.62393710262221	75.86001599055965	76.05674839717416	76.2928272851116	76.52890617304902	76.76498506098646	77.0010639489239	77.2371428368613	77.51256820612163	77.74864709405907	78.0240724633194	78.26015135125681	78.53557672051715	78.77165560845458	79.00773449639201	79.24381338432945	79.47989227226685	79.67662467888138	79.9127035668188	80.10943597343332	80.34551486137077	80.54224726798528	80.7783261559227	80.97505856253721	81.21113745047465	81.40786985708918	81.64394874502661	81.84068115164111	82.07676003957855	82.27349244619306	82.4702248528076	82.70630374074502	82.90303614735953	83.09976855397406	83.29650096058858	83.4932333672031	83.68996577381763	83.88669818043215	84.04408410572377	84.2408165123383	84.43754891895281	84.59493484424443	84.75232076953605	84.94905317615057	85.10643910144218	85.26382502673381	85.42121095202543	85.61794335863995	85.77532928393157	85.93271520922318	86.09010113451478	86.28683354112933	86.44421946642096	86.60160539171256	86.75899131700415	86.87703076097288	86.9557237236187	87.1131096489103	87.27049557420192	87.42788149949355	87.54592094346226	87.70330686875387	87.82134631272257	87.97873223801419	88.09677168198293	88.21481112595164	88.37219705124325	88.49023649521198	88.6476224205036	88.7656618644723	88.92304778976391	89.04108723373263	89.19847315902423	89.35585908431586	89.47389852828456	89.6312844535762	89.78867037886781	89.90670982283652	90.06409574812813	90.18213519209682	90.30017463606558	90.4182140800343	90.536253524003	90.65429296797171	90.77233241194041	90.89037185590912	91.00841129987784	91.12645074384655	91.24449018781528	91.40187611310687	91.4412225944298	91.55926203839851	91.67730148236723	91.79534092633594	91.91338037030465	92.03141981427336	92.11011277691917	92.22815222088788	92.30684518353368	92.4248846275024	92.50357759014821	92.62161703411691	92.70030999676274	92.81834944073145	92.89704240337727	93.01508184734597	93.09377480999177	93.2118142539605	93.29050721660629	93.36920017925211	93.48723962322084	93.56593258586662	93.68397202983535	93.76266499248115	93.80201147380404	93.88070443644986	93.95939739909568	94.07743684306436	94.1561298057102	94.234822768356	94.31351573100181	94.39220869364763	94.47090165629344	94.54959461893923	94.62828758158504	94.70698054423085	94.78567350687668	94.82501998819957	94.90371295084538	94.98240591349116	95.061098876137	95.10044535745986	95.13979183878278	95.2184848014286	95.29717776407443	95.37587072672021	95.454563689366	95.53325665201185	95.61194961465766	95.69064257730348	95.76933553994928	95.84802850259507	95.9267214652409	95.9660679465638	96.0447609092096	96.1234538718554	96.20214683450122	96.28083979714703	96.35953275979283	96.35953275979283	96.43822572243865	96.51691868508446	96.59561164773027	96.63495812905316	96.713651091699	96.75299757302186	96.8316905356677	96.9103834983135	96.9497299796364	97.02842294228221	97.06776942360512	97.14646238625092	97.18580886757381	97.22515534889675	97.30384831154254	97.34319479286546	97.38254127418834	97.46123423683417	97.50058071815707	97.53992719947998	97.5792736808029	97.38254127418834	97.06776942360512	96.8316905356677	96.63495812905316	96.63495812905316	96.55626516640737	96.51691868508446	96.47757220376154	96.47757220376154	96.67430461037608	96.98907646095931	97.22515534889675	97.30384831154254	97.50058071815707	97.65796664344868	97.81535256874031	97.93339201270899	98.05143145667772	98.16947090064643	98.28751034461517	98.40554978858387	98.52358923255258	98.64162867652131	98.7203216391671	98.7990146018129	98.91705404578162	98.99574700842743	99.03509348975036	99.11378645239614	99.19247941504194	99.23182589636487	99.27117237768776	99.31051885901067	99.31051885901067	99.34986534033357	99.38921182165647	99.42855830297937	99.4679047843023	99.4679047843023	99.5072512656252	99.5465977469481	99.585944228271	99.6252907095939	99.66463719091681	99.70398367223971	99.7433301535626	99.78267663488552	99.82202311620841	99.86136959753134	99.94006256017715	99.94006256017715	100.018755522823	100.0581020041459	100.1367949667917	100.1761414481146	100.2154879294375	100.2548344107604	100.2941808920833	100.3728738547291	100.412220336052	100.4909132986978	100.5302597800207	100.5696062613436	100.6482992239894	100.6876457053123	100.7663386679581	100.805685149281	100.8450316306039	100.9237245932498	100.9630710745727	101.0417640372185	101.0811105185414	101.1204569998643	101.1598034811872	101.1991499625101	101.2778429251559	101.3171894064788	101.3958823691246	101.4352288504475	101.4745753317704	101.5532682944162	101.5532682944162	101.631961257062	101.6713077383849	101.5926147757391	100.2941808920833	98.99574700842743	97.93339201270899	97.46123423683417	97.93339201270899	98.20881738196935	98.7990146018129	99.27117237768776	99.70398367223971	100.018755522823	100.0974484854688	100.2941808920833	100.4909132986978	100.6089527426665	100.7663386679581	100.8450316306039	100.9630710745727	101.1204569998643	101.238496443833	101.3958823691246	101.4352288504475	101.5532682944162	101.6713077383849	101.7893471823537	101.9073866263224	101.9467331076453	102.064772551614	102.1828119955827	102.2615049582285	102.3795444021972	102.4188908835201	102.5369303274888	102.6156232901346	102.6943162527805	102.8123556967492	102.8517021780721	102.930395140718	103.0090881033637	103.1271275473324	103.2058205099782	103.2451669913011	103.3238599539469	103.4025529165927	103.4812458792385	103.5599388418843	103.5992853232073	103.6386318045302	103.717324767176	103.7566712484989	103.8353642111447	103.8353642111447	103.8747106924676	103.9140571737905	103.9534036551134	103.9534036551134	103.9534036551134	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	104.0320966177592	104.0320966177592	104.0320966177592	104.0714430990821	104.0714430990821	104.0714430990821	104.110789580405	104.110789580405	104.1501360617279	104.1501360617279	104.1894825430508	104.2288290243737	104.2288290243737	104.2681755056966	104.3075219870195	104.3468684683424	104.3862149496653	104.4255614309883	104.4649079123111	104.4649079123111	104.5042543936341	104.543600874957	104.5829473562799	104.6222938376028	104.6616403189257	104.7009868002486	104.7403332815715	104.7796797628944	104.8190262442173	104.8583727255402	104.8977192068631	104.937065688186	104.9764121695089	105.0551051321547	105.0551051321547	105.0944516134776	105.1337980948005	105.2911840200921	105.409223464061	105.4879164267067	105.5666093893525	105.6453023519983	105.6846488333212	105.6846488333212	105.4485699453838	105.0551051321547	104.6616403189257	104.5042543936341	104.3075219870195	104.110789580405	103.9927501364363	103.8747106924676	103.9534036551134	103.8353642111447	103.7960177298218	103.9534036551134	104.2288290243737	104.3075219870195	104.543600874957	104.7403332815715	104.8583727255402	104.9764121695089	105.0157586508318	105.0944516134776	105.1731445761234	105.2124910574463	105.2518375387692	105.2911840200921	105.330530501415	105.409223464061	105.4485699453838	105.4879164267067	105.4879164267067	105.5666093893525	105.6059558706754	105.6453023519983	105.7239953146441	105.7239953146441	105.8026882772899	105.8813812399357	105.9600742025815	105.9994206839044	105.9994206839044	106.0387671652273	106.0781136465502	106.1174601278731	106.156806609196	106.156806609196	106.196153090519	106.2354995718418	106.2748460531648	106.2748460531648	106.2748460531648	106.3141925344877	106.3141925344877	106.3535390158106	106.3535390158106	106.3535390158106	106.3535390158106	106.3141925344877	106.3141925344877	106.3141925344877	106.3141925344877	106.3141925344877	106.3535390158106	106.3535390158106	106.3535390158106	106.3535390158106	106.3928854971335	106.3928854971335	106.3928854971335	106.3928854971335	106.3928854971335	106.3928854971335	106.3928854971335	106.3928854971335	106.3928854971335	106.4322319784564	106.4322319784564	106.4322319784564	106.4322319784564	106.4715784597793	106.4715784597793	106.5109249411022	106.5109249411022	106.5502714224251	106.5502714224251	106.589617903748	106.589617903748	106.628964385071	106.6683108663938	106.6683108663938	106.7076573477167	106.7470038290396	106.7470038290396	106.7863503103625	106.8256967916854	106.8650432730083	106.9043897543312	106.9437362356541	106.983082716977	107.0224291982999	107.0617756796228	107.2191616049145	107.3765475302061	107.4945869741748	107.6126264181435	107.7306658621122	107.809358824758	107.8880517874038	107.9667447500496	108.0060912313726	108.0454377126954	108.0847841940184	108.1634771566642	108.2028236379871	108.24217011931	108.24217011931	108.281516600633	108.3208630819558	108.3602095632787	108.3602095632787	108.3995560446016	108.3995560446016	108.3995560446016	108.4389025259245	108.4389025259245	108.4389025259245	108.4389025259245	108.3995560446016	108.3995560446016	108.3995560446016	108.3995560446016	108.3602095632787	108.3602095632787	108.3602095632787	108.3602095632787	108.3602095632787	108.3602095632787	108.3208630819558	108.3208630819558	108.3208630819558	108.3208630819558	108.3208630819558	108.3208630819558	108.281516600633	108.281516600633	108.281516600633	108.281516600633	108.281516600633	108.281516600633	108.281516600633	108.281516600633	108.281516600633	108.281516600633	108.3208630819558	108.3208630819558	108.3602095632787	108.3602095632787	108.3602095632787	108.3995560446016	108.3995560446016	108.3995560446016	108.4389025259245	108.4389025259245	108.4782490072474	108.4782490072474	108.5175954885703	108.5175954885703	108.5569419698932	108.5569419698932	108.5962884512161	108.5962884512161	108.635634932539	108.635634932539	108.6749814138619	108.6749814138619	108.6749814138619	108.7143278951848	108.7143278951848	108.7536743765077	108.7536743765077	108.7930208578306	108.7930208578306	108.8323673391535	108.8717138204764	108.9110603017994	108.9110603017994	108.9504067831222	108.9897532644452	108.9897532644452	109.0290997457681	109.068446227091	109.068446227091	109.1077927084139	109.1471391897368	109.1471391897368	109.1864856710597	109.1864856710597	109.2258321523826	109.2651786337055	109.2651786337055	109.3045251150284	109.3045251150284	109.3438715963513	109.3438715963513	109.3832180776742	109.3832180776742	109.3832180776742	109.4225645589971	109.4225645589971	109.46191104032	109.46191104032	109.46191104032	109.46191104032	109.501257521643	109.501257521643	109.501257521643	109.501257521643	109.5406040029658	109.5406040029658	109.5406040029658	109.5799504842887	109.5799504842887	109.5799504842887	109.5799504842887	109.6192969656116	109.6192969656116	109.6192969656116	109.6192969656116	109.6586434469345	109.6586434469345	109.6586434469345	109.6586434469345	109.6586434469345	109.6979899282574	109.6979899282574	109.6979899282574	109.6979899282574	109.7373364095803	109.7373364095803	109.7373364095803	109.7373364095803	109.7373364095803	109.7373364095803	109.7766828909032	109.7766828909032	109.7766828909032	109.7766828909032	109.7766828909032	109.7766828909032	109.7373364095803	109.7373364095803	109.6979899282574	109.6586434469345	109.6192969656116	109.5799504842887	109.5406040029658	109.46191104032	109.4225645589971	109.3438715963513	109.3045251150284	109.2651786337055	109.1864856710597	109.1077927084139	109.068446227091	108.9897532644452	108.9504067831222	108.9110603017994	108.8323673391535	108.7930208578306	108.7143278951848	108.6749814138619	108.635634932539	108.5569419698932	108.5175954885703	108.4389025259245	108.3995560446016	108.3602095632787	108.3208630819558	108.24217011931	108.2028236379871	108.0454377126954	107.9273982687267	107.8487053060809	107.7700123434351	107.6126264181435	107.5339334554977	107.4945869741748	107.4945869741748	107.4552404928519	107.4945869741748	107.4945869741748	107.5339334554977	107.5339334554977	107.5732799368206	107.6126264181435	107.6913193807893	107.7306658621122	107.7700123434351	107.8487053060809	107.9273982687267	107.9667447500496	108.0060912313726	108.0847841940184	108.1634771566642	108.24217011931	108.3602095632787	108.4389025259245	108.5569419698932	108.5962884512161	108.7143278951848	108.7536743765077	108.8717138204764	108.9110603017994	108.9897532644452	109.0290997457681	109.1077927084139	109.1864856710597	109.2258321523826	109.2651786337055	109.3438715963513	109.3832180776742	109.3832180776742	109.4225645589971	109.4225645589971	109.4225645589971	109.4225645589971	109.4225645589971	109.4225645589971	109.46191104032	109.46191104032	109.46191104032	109.501257521643	109.501257521643	109.501257521643	109.501257521643	109.5406040029658	109.5406040029658	109.5406040029658	109.5799504842887	109.5799504842887	109.5799504842887	109.5799504842887	109.6192969656116	109.6192969656116	109.6192969656116	109.6192969656116	109.6586434469345	109.6586434469345	109.6586434469345	109.6979899282574	109.6979899282574	109.7373364095803	109.7373364095803	109.7373364095803	109.7766828909032	109.7766828909032	109.8160293722262	109.8160293722262	109.855375853549	109.894722334872	109.894722334872	109.9340688161949	109.9340688161949	109.9340688161949	109.9340688161949	109.9340688161949	109.894722334872	109.894722334872	109.894722334872	109.855375853549	109.855375853549	109.8160293722262	109.8160293722262	109.8160293722262	109.7766828909032	109.7373364095803	109.7373364095803	109.6979899282574	109.6979899282574	109.6586434469345	109.6192969656116	109.5799504842887	109.501257521643	109.46191104032	109.4225645589971	109.3832180776742	104.3468684683424	55.6359245905868	-9.95465977469481	-10.62354995718418	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.54485699453838	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.58420347586128	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	-10.54485699453838	Copper	1.85185185185185E-5	0.0	0.0	1.85185185185185E-5	0.000111111111111111	0.000222222222222222	0.000351851851851852	0.000481481481481481	0.000592592592592592	0.000722222222222222	0.000833333333333333	0.000944444444444444	0.00109259259259259	0.0012037037037037	0.00133333333333333	0.00146296296296296	0.00157407407407407	0.0017037037037037	0.00183333333333333	0.00196296296296296	0.00207407407407407	0.0022037037037037	0.00233333333333333	0.00244444444444444	0.00259259259259259	0.0027037037037037	0.00281481481481481	0.00296296296296296	0.00307407407407407	0.00318518518518518	0.00333333333333333	0.00344444444444444	0.00355555555555555	0.0037037037037037	0.00381481481481481	0.00396296296296296	0.00407407407407407	0.00418518518518518	0.00433333333333333	0.00444444444444444	0.00455555555555555	0.0047037037037037	0.00481481481481481	0.00494444444444444	0.00507407407407407	0.00518518518518518	0.00529629629629629	0.00544444444444444	0.00555555555555555	0.00566666666666667	0.00581481481481481	0.00592592592592592	0.00603703703703704	0.00618518518518518	0.00629629629629629	0.00642592592592592	0.00655555555555555	0.00666666666666666	0.00679629629629629	0.00692592592592592	0.00703703703703704	0.00716666666666666	0.00729629629629629	0.00740740740740741	0.00753703703703703	0.00766666666666666	0.00779629629629629	0.0079074074074074	0.00803703703703704	0.00814814814814815	0.00827777777777778	0.0084074074074074	0.00851851851851852	0.00864814814814815	0.00877777777777777	0.00888888888888889	0.00901851851851851	0.00914814814814815	0.00925925925925926	0.00938888888888889	0.00951851851851852	0.00964814814814815	0.00975925925925926	0.00988888888888889	0.0100185185185185	0.0101296296296296	0.0102592592592593	0.0103888888888889	0.0105	0.0106296296296296	0.0107592592592593	0.0108703703703704	0.011	0.0111296296296296	0.0112407407407407	0.0113703703703704	0.0115	0.0116111111111111	0.0117592592592593	0.0118703703703704	0.0119814814814815	0.0121296296296296	0.0122407407407407	0.0123518518518518	0.0125	0.0126111111111111	0.0127222222222222	0.0128703703703704	0.0129814814814815	0.0130925925925926	0.0132407407407407	0.0133518518518518	0.013462962962963	0.0136111111111111	0.0137222222222222	0.0138333333333333	0.0139814814814815	0.0140925925925926	0.0142407407407407	0.0143518518518518	0.014462962962963	0.0146111111111111	0.0147222222222222	0.0148333333333333	0.0149814814814815	0.0150925925925926	0.0152037037037037	0.0153518518518518	0.015462962962963	0.0155925925925926	0.0157222222222222	0.0158333333333333	0.015962962962963	0.0160925925925926	0.0162037037037037	0.0163333333333333	0.016462962962963	0.0165740740740741	0.0167037037037037	0.0168333333333333	0.016962962962963	0.0170740740740741	0.0172037037037037	0.0173333333333333	0.0174444444444444	0.0175740740740741	0.0177037037037037	0.0178148148148148	0.0179444444444444	0.0180740740740741	0.0181851851851852	0.0183333333333333	0.0184444444444444	0.0185555555555556	0.0187037037037037	0.0188148148148148	0.0189259259259259	0.019037037037037	0.0191296296296296	0.0192592592592593	0.0193888888888889	0.0195	0.0196296296296296	0.0197592592592593	0.0198703703703704	0.0200185185185185	0.0201296296296296	0.0202407407407407	0.0203888888888889	0.0205	0.0206111111111111	0.0207592592592593	0.0208703703703704	0.0209814814814815	0.0211296296296296	0.0212407407407407	0.0213518518518518	0.0215	0.0216111111111111	0.0217222222222222	0.0218703703703704	0.0219814814814815	0.0220925925925926	0.0222407407407407	0.0223518518518518	0.022462962962963	0.0226111111111111	0.0227222222222222	0.0228333333333333	0.0229814814814815	0.0230925925925926	0.0232037037037037	0.0233518518518518	0.023462962962963	0.0236111111111111	0.0237222222222222	0.0238333333333333	0.0239814814814815	0.0240925925925926	0.0242037037037037	0.0243518518518518	0.024462962962963	0.0245740740740741	0.0247222222222222	0.0248333333333333	0.024962962962963	0.0250925925925926	0.0252037037037037	0.0253333333333333	0.025462962962963	0.0255740740740741	0.0257037037037037	0.0258333333333333	0.025962962962963	0.0260740740740741	0.0262037037037037	0.0263148148148148	0.0264444444444444	0.0265740740740741	0.0267037037037037	0.0268148148148148	0.026962962962963	0.0270740740740741	0.0271851851851852	0.0273333333333333	0.0274444444444444	0.0275555555555555	0.0277037037037037	0.0278148148148148	0.0279259259259259	0.0280740740740741	0.0281851851851852	0.0283333333333333	0.0284444444444444	0.0285740740740741	0.0287037037037037	0.0288148148148148	0.0289444444444444	0.0290740740740741	0.0292037037037037	0.0293148148148148	0.029462962962963	0.0295740740740741	0.0296851851851852	0.0298333333333333	0.0299444444444444	0.0300925925925926	0.0302037037037037	0.0303148148148148	0.030462962962963	0.0305740740740741	0.0306851851851852	0.0308333333333333	0.0309444444444444	0.0310740740740741	0.0312037037037037	0.0313148148148148	0.0314444444444444	0.0315740740740741	0.0317037037037037	0.0318148148148148	0.031962962962963	0.0320740740740741	0.0321851851851852	0.0323333333333333	0.0324444444444444	0.0325555555555555	0.0327037037037037	0.0328148148148148	0.032962962962963	0.0330740740740741	0.0331851851851852	0.0333333333333333	0.0334444444444444	0.0335740740740741	0.0337037037037037	0.0338148148148148	0.0339444444444444	0.0340740740740741	0.0341851851851852	0.0343148148148148	0.0344444444444444	0.0345740740740741	0.0346851851851852	0.0348148148148148	0.0349444444444444	0.0350555555555555	0.0352037037037037	0.0353148148148148	0.0354259259259259	0.0355740740740741	0.0356851851851852	0.0358333333333333	0.0359444444444444	0.0360555555555555	0.0361666666666667	0.0363148148148148	0.0364259259259259	0.0365740740740741	0.0366851851851852	0.0367962962962963	0.0369444444444444	0.0370555555555555	0.0371666666666667	0.0372962962962963	0.0374259259259259	0.037537037037037	0.0376666666666667	0.0377962962962963	0.0379074074074074	0.038037037037037	0.0381666666666667	0.0382962962962963	0.0384074074074074	0.038537037037037	0.0386666666666667	0.0387777777777778	0.0389259259259259	0.039037037037037	0.0391481481481481	0.0392777777777778	0.0394074074074074	0.0395555555555556	0.0396666666666667	0.0397777777777778	0.0399259259259259	0.040037037037037	0.0401481481481481	0.0402962962962963	0.0404074074074074	0.0405185185185185	0.0406666666666667	0.0407777777777778	0.0409074074074074	0.041037037037037	0.0411666666666667	0.0412777777777778	0.0414074074074074	0.041537037037037	0.0416481481481481	0.0417777777777778	0.0419074074074074	0.0420185185185185	0.0421481481481481	0.0422777777777778	0.0423888888888889	0.042537037037037	0.0426481481481481	0.0427592592592593	0.0429074074074074	0.0430185185185185	0.0431666666666667	0.0432777777777778	0.0434074074074074	0.043537037037037	0.0436481481481481	0.0437592592592593	0.0439074074074074	0.0440185185185185	0.0441481481481481	0.0442777777777778	0.0443888888888889	0.0445185185185185	0.0446481481481481	0.0447777777777778	0.0448888888888889	0.0450185185185185	0.0451481481481481	0.0452592592592592	0.0453888888888889	0.0455185185185185	0.0456296296296296	0.0457592592592593	0.0458888888888889	0.046	0.0461296296296296	0.0462592592592593	0.0463703703703704	0.0465	0.0466296296296296	0.0467407407407407	0.0468703703703704	0.047	0.0471111111111111	0.0472592592592592	0.0473703703703704	0.0474814814814815	0.0476111111111111	0.0477407407407407	0.0478518518518518	0.0479814814814815	0.0481111111111111	0.0482222222222222	0.0483703703703704	0.0484814814814815	0.0485925925925926	0.0487407407407407	0.0488518518518518	0.048962962962963	0.0491111111111111	0.0492222222222222	0.0493333333333333	0.0494814814814815	0.0495925925925926	0.0497407407407407	0.0498518518518518	0.0499629629629629	0.0500740740740741	0.0502222222222222	0.0503333333333333	0.0504444444444444	0.0505925925925926	0.0507037037037037	0.0508518518518518	0.0509629629629629	0.0510740740740741	0.0512222222222222	0.0513333333333333	0.051462962962963	0.0515925925925926	0.0517037037037037	0.0518333333333333	0.051962962962963	0.0520740740740741	0.0522037037037037	0.0523333333333333	0.0524444444444444	0.0525740740740741	0.0527037037037037	0.0528333333333333	0.0529444444444444	0.0530740740740741	0.0532037037037037	0.0533148148148148	0.053462962962963	0.0535740740740741	0.0536851851851852	0.0538333333333333	0.0539444444444444	0.0540925925925926	0.0542037037037037	0.0543148148148148	0.054462962962963	0.0545740740740741	0.0546851851851852	0.0548333333333333	0.0549444444444444	0.0550740740740741	0.0552037037037037	0.0553333333333333	0.0554444444444444	0.0555555555555555	0.0557037037037037	0.0558148148148148	0.0559629629629629	0.0560740740740741	0.0561851851851852	0.0563333333333333	0.0564444444444444	0.0565740740740741	0.0567037037037037	0.0568333333333333	0.0569444444444444	0.0570740740740741	0.0572037037037037	0.0573148148148148	0.0574444444444444	0.0575740740740741	0.0576851851851852	0.0578333333333333	0.0579444444444444	0.0580925925925926	0.0582037037037037	0.0583148148148148	0.0584259259259259	0.0585740740740741	0.0586851851851852	0.0588333333333333	0.0589444444444444	0.0590740740740741	0.0592037037037037	0.0593148148148148	0.0594444444444444	0.0595740740740741	0.0596851851851852	0.0598148148148148	0.0599444444444444	0.0600555555555555	0.0601851851851852	0.0603148148148148	0.0604444444444444	0.0605555555555555	0.0606851851851852	0.0607962962962963	0.0609259259259259	0.0610555555555555	0.0611851851851852	0.0612962962962963	0.0614444444444444	0.0615555555555555	0.0616666666666667	0.0618148148148148	0.0619259259259259	0.0620740740740741	0.0621851851851852	0.0622962962962963	0.0624074074074074	0.0625555555555555	0.0626666666666666	0.0628148148148148	0.0629259259259259	0.063037037037037	0.0631851851851852	0.0632962962962963	0.0634259259259259	0.0635555555555555	0.0636666666666667	0.0637962962962963	0.0639259259259259	0.0640555555555555	0.0641666666666667	0.0642962962962963	0.0644259259259259	0.064537037037037	0.0646851851851852	0.0647962962962963	0.0649444444444444	0.0650555555555555	0.0651666666666667	0.0653148148148148	0.0654259259259259	0.0655555555555555	0.0656851851851852	0.0657962962962963	0.0659259259259259	0.0660555555555555	0.0661851851851852	0.0662962962962963	0.0664444444444444	0.0665555555555555	0.0666666666666667	0.0668148148148148	0.0669259259259259	0.067037037037037	0.0671851851851852	0.0672962962962963	0.0674444444444444	0.0675555555555555	0.0676851851851852	0.0678148148148148	0.0679444444444444	0.0680555555555555	0.0682037037037037	0.0683148148148148	0.0684259259259259	0.0685740740740741	0.0686851851851852	0.0687962962962963	0.0689444444444444	0.0690555555555555	0.0692037037037037	0.0693148148148148	0.0694444444444444	0.0695740740740741	0.0696851851851852	0.0698148148148148	0.0699444444444444	0.0700740740740741	0.0701851851851852	0.0703148148148148	0.0704444444444444	0.0705555555555555	0.0707037037037037	0.0708148148148148	0.0709259259259259	0.0710740740740741	0.0711851851851852	0.0713333333333333	0.0714444444444444	0.0715555555555555	0.0717037037037037	0.0718148148148148	0.0719444444444444	0.0720740740740741	0.0721851851851852	0.0722962962962963	0.0724444444444444	0.0725555555555555	0.0726851851851852	0.0728148148148148	0.0729259259259259	0.0730555555555555	0.0731851851851852	0.0733148148148148	0.0734259259259259	0.0735740740740741	0.0736851851851852	0.0737962962962963	0.0739259259259259	0.0740555555555555	0.0741666666666667	0.0743148148148148	0.0744259259259259	0.074537037037037	0.0746851851851852	0.0747962962962963	0.0749259259259259	0.0750555555555555	0.0751666666666667	0.0752962962962963	0.0754259259259259	0.075537037037037	0.0756481481481481	0.0757962962962963	0.0759074074074074	0.076037037037037	0.0761666666666667	0.0762777777777778	0.0764074074074074	0.076537037037037	0.0766481481481481	0.0767777777777778	0.0769074074074074	0.077037037037037	0.0771481481481482	0.0772777777777778	0.0774074074074074	0.0775185185185185	0.0776666666666667	0.0777777777777778	0.0778888888888889	0.078037037037037	0.0781481481481481	0.0782592592592593	0.0784074074074074	0.0785185185185185	0.0786666666666667	0.0787777777777778	0.0789074074074074	0.079037037037037	0.0791481481481481	0.0792592592592593	0.0794074074074074	0.0795185185185185	0.0796481481481481	0.0797777777777778	0.0798888888888889	0.0800185185185185	0.0801481481481481	0.0802777777777778	0.0803888888888889	0.0805185185185185	0.0806481481481481	0.0807592592592592	0.0809074074074074	0.0810185185185185	0.0811666666666666	0.0812777777777778	0.0813888888888889	0.081537037037037	0.0816481481481481	0.0817592592592592	0.0819074074074074	0.0820185185185185	0.0821296296296296	0.0822777777777778	0.0823888888888889	0.0825185185185185	0.0826481481481481	0.0827592592592593	0.0828888888888889	0.0830185185185185	0.0831481481481481	0.0832592592592593	0.0833888888888889	0.0835185185185185	0.0836296296296296	0.0837777777777778	0.0838888888888889	0.084	0.0841296296296296	0.0842592592592592	0.0843703703703704	0.0845185185185185	0.0846296296296296	0.0847777777777778	0.0848888888888889	0.085	0.0851111111111111	0.0852592592592592	0.0853703703703704	0.0855185185185185	0.0856296296296296	0.0857407407407407	0.0858888888888889	0.086	0.0861111111111111	0.0862592592592593	0.0863703703703703	0.0864814814814815	0.0866296296296296	0.0867407407407407	0.0868518518518518	0.087	0.0871111111111111	0.0872222222222222	0.0873703703703704	0.0874814814814815	0.0876111111111111	0.0877407407407407	0.0878703703703704	0.0879814814814815	0.0881111111111111	0.0882407407407407	0.0883518518518518	0.0884814814814815	0.0886111111111111	0.0887222222222222	0.0888518518518518	0.0889814814814815	0.0890925925925926	0.0892222222222222	0.0893518518518518	0.0894629629629629	0.0896111111111111	0.0897222222222222	0.0898703703703703	0.0899814814814815	0.0900925925925926	0.0902407407407407	0.0903518518518518	0.0904629629629629	0.0906111111111111	0.0907222222222222	0.0908518518518518	0.0909814814814815	0.0910925925925926	0.0912222222222222	0.0913518518518518	0.0914814814814815	0.0915925925925926	0.0917222222222222	0.0918518518518518	0.0919629629629629	0.0921111111111111	0.0922222222222222	0.0923703703703704	0.0924814814814815	0.0925925925925926	0.0927222222222222	0.0928518518518518	0.0929814814814815	0.0930925925925926	0.0932222222222222	0.0933518518518518	0.0934629629629629	0.0936111111111111	0.0937222222222222	0.0938333333333333	0.0939814814814815	0.0940925925925926	0.0942407407407407	0.0943518518518518	0.0944814814814815	0.0946111111111111	0.0947222222222222	0.0948518518518518	0.0949814814814814	0.0951111111111111	0.0952222222222222	0.0953703703703704	0.0954814814814814	0.0955925925925926	0.0957407407407407	0.0958518518518518	0.096	0.0961111111111111	0.0962222222222222	0.0963703703703703	0.0964814814814815	0.0966111111111111	0.0967407407407407	0.0968518518518518	0.0969814814814815	0.0971111111111111	0.0972407407407407	0.0973518518518518	0.0975	0.0976111111111111	0.0977222222222222	0.0978703703703703	0.0979814814814815	0.0980925925925926	0.0982407407407407	0.0983518518518518	0.0985	0.0986111111111111	0.0987222222222222	0.0988703703703703	0.0989814814814814	0.0990925925925926	0.0992407407407407	0.0993518518518518	0.0994814814814814	0.0996111111111111	0.0997407407407407	0.0998518518518518	0.0999814814814814	0.100111111111111	0.100222222222222	0.100351851851852	0.100481481481481	0.100592592592593	0.100740740740741	0.100851851851852	0.100962962962963	0.101111111111111	0.101222222222222	0.101333333333333	0.101481481481481	0.101592592592593	0.101740740740741	0.101851851851852	0.101962962962963	0.102111111111111	0.102222222222222	0.102351851851852	0.102481481481481	0.102592592592593	0.102722222222222	0.102851851851852	0.102962962962963	0.103092592592593	0.103222222222222	0.103333333333333	0.103462962962963	0.103592592592593	0.103722222222222	0.103833333333333	0.103981481481481	0.104092592592593	0.104203703703704	0.104351851851852	0.104462962962963	0.104611111111111	0.104722222222222	0.104833333333333	0.104981481481481	0.105092592592593	0.105222222222222	0.105351851851852	0.105462962962963	0.105592592592593	0.105722222222222	0.105833333333333	0.105962962962963	0.106092592592593	0.106222222222222	0.106333333333333	0.106481481481481	0.106592592592593	0.106703703703704	0.106851851851852	0.106962962962963	0.107111111111111	0.107222222222222	0.107351851851852	0.107481481481481	0.107592592592593	0.107722222222222	0.107851851851852	0.107962962962963	0.108092592592593	0.108222222222222	0.108351851851852	0.108462962962963	0.108592592592593	0.108722222222222	0.108833333333333	0.108981481481481	0.109092592592593	0.109203703703704	0.109351851851852	0.109462962962963	0.109611111111111	0.109722222222222	0.109851851851852	0.109981481481481	0.110092592592593	0.110222222222222	0.110351851851852	0.110462962962963	0.110592592592593	0.110722222222222	0.110833333333333	0.110962962962963	0.111092592592593	0.111222222222222	0.111333333333333	0.111444444444444	0.111592592592593	0.111703703703704	0.111814814814815	0.111962962962963	0.112074074074074	0.112222222222222	0.112333333333333	0.112444444444444	0.112592592592593	0.112703703703704	0.112833333333333	0.112962962962963	0.113074074074074	0.113185185185185	0.113333333333333	0.113444444444444	0.113574074074074	0.113703703703704	0.113814814814815	0.113944444444444	0.114074074074074	0.114203703703704	0.114314814814815	0.114444444444444	0.114574074074074	0.114685185185185	0.114814814814815	0.114944444444444	0.115055555555556	0.115203703703704	0.115314814814815	0.115425925925926	0.115574074074074	0.115685185185185	0.115796296296296	0.115944444444444	0.116055555555556	0.116166666666667	0.116314814814815	0.116425925925926	0.116574074074074	0.116685185185185	0.116814814814815	0.116944444444444	0.117055555555556	0.117166666666667	0.117314814814815	0.117425925925926	0.117555555555556	0.117685185185185	0.117814814814815	0.117925925925926	0.118055555555556	0.118185185185185	0.118296296296296	0.118425925925926	0.118555555555556	0.118666666666667	0.118796296296296	0.118925925925926	0.119074074074074	0.119185185185185	0.119296296296296	0.119444444444444	0.119555555555556	0.119685185185185	0.119814814814815	0.119925925925926	0.120055555555556	0.120185185185185	0.120296296296296	0.120425925925926	0.120555555555556	0.120685185185185	0.120796296296296	0.120925925925926	0.121055555555556	0.121166666666667	0.121314814814815	0.121425925925926	0.121574074074074	0.121685185185185	0.121796296296296	0.121944444444444	0.122055555555556	0.122185185185185	0.122314814814815	0.122444444444444	0.122555555555556	0.122685185185185	0.122814814814815	0.122925925925926	0.123074074074074	0.123185185185185	0.123333333333333	0.123444444444444	0.123555555555556	0.123703703703704	0.123814814814815	0.123925925925926	0.124074074074074	0.124185185185185	0.124314814814815	0.124444444444444	0.124574074074074	0.124685185185185	0.124814814814815	0.124944444444444	0.125055555555556	0.125185185185185	0.125314814814815	0.125425925925926	0.125574074074074	0.125685185185185	0.125796296296296	0.125944444444444	0.126055555555556	0.126203703703704	0.126314814814815	0.126444444444444	0.126574074074074	0.126685185185185	0.126814814814815	0.126944444444444	0.127074074074074	0.127185185185185	0.127333333333333	0.127444444444444	0.127555555555556	0.127703703703704	0.127814814814815	0.127925925925926	0.128074074074074	0.128185185185185	0.128333333333333	0.128444444444444	0.128574074074074	0.128703703703704	0.128833333333333	0.128944444444444	0.129074074074074	0.129203703703704	0.129314814814815	0.129462962962963	0.129574074074074	0.129703703703704	0.129833333333333	0.129944444444444	0.130074074074074	0.130203703703704	0.130333333333333	0.130444444444444	0.130574074074074	0.130703703703704	0.130814814814815	0.130962962962963	0.131074074074074	0.131222222222222	0.131333333333333	0.131444444444444	0.131592592592593	0.131703703703704	0.131833333333333	0.131962962962963	0.132092592592593	0.132203703703704	0.132351851851852	0.132462962962963	0.132574074074074	0.132722222222222	0.132833333333333	0.132981481481481	0.133092592592593	0.133222222222222	0.133351851851852	0.133462962962963	0.133592592592593	0.133722222222222	0.133851851851852	0.133962962962963	0.134092592592593	0.134222222222222	0.134333333333333	0.134481481481481	0.134592592592593	0.134703703703704	0.134851851851852	0.134962962962963	0.135111111111111	0.135222222222222	0.135333333333333	0.135481481481481	0.135592592592593	0.135722222222222	0.135851851851852	0.135981481481481	0.136092592592593	0.136222222222222	0.136351851851852	0.136462962962963	0.136611111111111	0.136722222222222	0.136833333333333	0.136981481481481	0.137092592592593	0.137203703703704	0.137351851851852	0.137462962962963	0.137611111111111	0.137722222222222	0.137833333333333	0.137981481481481	0.138092592592593	0.138203703703704	0.138351851851852	0.138462962962963	0.138592592592593	0.138722222222222	0.138833333333333	0.138944444444444	0.139092592592593	0.139222222222222	0.139333333333333	0.139462962962963	0.139574074074074	0.139703703703704	0.139833333333333	0.139962962962963	0.140074074074074	0.140222222222222	0.140333333333333	0.140444444444444	0.140592592592593	0.140703703703704	0.140814814814815	0.140962962962963	0.141074074074074	0.141222222222222	0.141333333333333	0.141444444444444	0.141592592592593	0.141703703703704	0.141833333333333	0.141962962962963	0.142074074074074	0.142203703703704	0.142333333333333	0.142444444444444	0.142574074074074	0.142703703703704	0.142833333333333	0.142944444444444	0.143074074074074	0.143203703703704	0.143314814814815	0.143444444444444	0.143574074074074	0.143685185185185	0.143833333333333	0.143944444444444	0.144055555555556	0.144203703703704	0.144314814814815	0.144425925925926	0.144574074074074	0.144685185185185	0.144833333333333	0.144944444444444	0.145055555555556	0.145203703703704	0.145314814814815	0.145444444444444	0.145574074074074	0.145703703703704	0.145814814814815	0.145944444444444	0.146074074074074	0.146185185185185	0.146314814814815	0.146444444444444	0.146555555555556	0.146703703703704	0.146814814814815	0.146925925925926	0.147074074074074	0.147185185185185	0.147296296296296	0.147444444444444	0.147555555555556	0.147666666666667	0.147814814814815	0.147925925925926	0.148074074074074	0.148185185185185	0.148314814814815	0.148425925925926	0.148555555555556	0.148685185185185	0.148796296296296	0.148944444444444	0.149055555555556	0.149203703703704	0.149314814814815	0.149425925925926	0.149537037037037	0.149685185185185	0.149796296296296	0.149944444444444	0.150055555555556	0.150166666666667	0.150314814814815	0.150425925925926	0.150555555555556	0.150685185185185	0.150796296296296	0.150925925925926	0.151055555555556	0.151166666666667	0.151296296296296	0.151425925925926	0.151555555555556	0.151666666666667	0.151814814814815	0.151925925925926	0.152037037037037	0.152185185185185	0.152296296296296	0.152407407407407	0.152555555555556	0.152666666666667	0.152777777777778	0.152925925925926	0.153037037037037	0.153185185185185	0.153296296296296	0.153407407407407	0.153555555555556	0.153666666666667	0.153796296296296	0.153925925925926	0.154037037037037	0.154166666666667	0.154296296296296	0.154407407407407	0.154537037037037	0.154666666666667	0.154796296296296	0.154907407407407	0.155037037037037	0.155166666666667	0.155277777777778	0.155425925925926	0.155537037037037	0.155648148148148	0.155796296296296	0.155907407407407	0.156055555555556	0.156166666666667	0.156277777777778	0.156425925925926	0.156537037037037	0.156666666666667	0.156796296296296	0.156907407407407	0.157037037037037	0.157166666666667	0.157277777777778	0.157407407407407	0.157555555555556	0.157666666666667	0.157777777777778	0.157925925925926	0.158037037037037	0.158185185185185	0.158296296296296	0.158425925925926	0.158555555555556	0.158666666666667	0.158777777777778	0.158925925925926	0.159037037037037	0.159166666666667	0.159296296296296	0.159425925925926	0.159537037037037	0.159685185185185	0.159796296296296	0.159907407407407	0.160055555555556	0.160166666666667	0.160314814814815	0.160425925925926	0.160537037037037	0.160685185185185	0.160796296296296	0.160907407407407	0.161055555555556	0.161166666666667	0.161296296296296	0.161425925925926	0.161555555555556	0.161666666666667	0.161796296296296	0.161925925925926	0.162037037037037	0.162185185185185	0.162296296296296	0.162407407407407	0.162555555555556	0.162666666666667	0.162814814814815	0.162925925925926	0.163055555555556	0.163185185185185	0.163296296296296	0.163407407407407	0.163555555555556	0.163666666666667	0.163796296296296	0.163925925925926	0.164037037037037	0.164166666666667	0.164296296296296	0.164425925925926	0.164537037037037	0.164685185185185	0.164796296296296	0.164907407407407	0.165055555555556	0.165166666666667	0.165277777777778	0.165425925925926	0.165537037037037	0.165685185185185	0.165796296296296	0.165925925925926	0.166055555555556	0.166166666666667	0.166296296296296	0.166425925925926	0.166555555555556	0.166666666666667	0.166777777777778	0.166925925925926	0.167037037037037	0.167148148148148	0.167296296296296	0.167407407407407	0.167555555555556	0.167666666666667	0.167796296296296	0.167925925925926	0.168037037037037	0.168166666666667	0.168296296296296	0.168425925925926	0.168537037037037	0.168666666666667	0.168796296296296	0.168907407407407	0.169055555555556	0.169166666666667	0.169277777777778	0.169462962962963	0.169592592592593	0.169703703703704	0.169833333333333	0.169962962962963	0.170074074074074	0.170203703703704	0.170351851851852	0.170462962962963	0.170574074074074	0.170722222222222	0.170833333333333	0.170981481481481	0.171092592592593	0.171203703703704	0.171351851851852	0.171462962962963	0.171574074074074	0.171722222222222	0.171833333333333	0.171962962962963	0.172092592592593	0.172222222222222	0.172333333333333	0.172462962962963	0.172592592592593	0.172703703703704	0.172851851851852	0.172962962962963	0.173111111111111	0.173222222222222	0.173333333333333	0.173481481481481	0.173592592592593	0.173722222222222	0.173851851851852	0.173962962962963	0.174092592592593	0.174222222222222	0.174333333333333	0.174462962962963	0.174592592592593	0.174703703703704	0.174833333333333	0.174962962962963	0.175092592592593	0.175203703703704	0.175351851851852	0.175462962962963	0.175574074074074	0.175722222222222	0.175833333333333	0.175944444444444	0.176092592592593	0.176203703703704	0.176314814814815	0.176462962962963	0.176574074074074	0.176722222222222	0.176833333333333	0.176944444444444	0.177092592592593	0.177203703703704	0.177314814814815	0.177462962962963	0.177574074074074	0.177685185185185	0.177833333333333	0.177944444444444	0.178055555555556	0.178203703703704	0.178314814814815	0.178444444444444	0.178574074074074	0.178685185185185	0.178814814814815	0.178944444444444	0.179055555555556	0.179185185185185	0.179314814814815	0.179425925925926	0.179537037037037	0.179685185185185	0.179796296296296	0.179925925925926	0.180055555555556	0.180166666666667	0.180296296296296	0.180425925925926	0.180555555555556	0.180666666666667	0.180796296296296	0.180925925925926	0.181037037037037	0.181166666666667	0.181296296296296	0.181407407407407	0.181537037037037	0.181666666666667	0.181777777777778	0.181907407407407	0.182037037037037	0.182148148148148	0.182277777777778	0.182407407407407	0.182518518518519	0.182666666666667	0.182777777777778	0.182925925925926	0.183037037037037	0.183148148148148	0.183296296296296	0.183407407407407	0.183518518518519	0.183666666666667	0.183777777777778	0.183907407407407	0.184037037037037	0.184148148148148	0.184277777777778	0.184407407407407	0.184518518518519	0.184648148148148	0.184777777777778	0.184907407407407	0.185018518518518	0.185148148148148	0.185277777777778	0.185388888888889	0.1855	0.185648148148148	0.185759259259259	0.185907407407407	0.186018518518519	0.18612962962963	0.186277777777778	0.186388888888889	0.1865	0.186648148148148	0.186759259259259	0.18687037037037	0.187018518518519	0.18712962962963	0.187259259259259	0.187388888888889	0.1875	0.18762962962963	0.187759259259259	0.187888888888889	0.188	0.18812962962963	0.188259259259259	0.18837037037037	0.1885	0.18862962962963	0.188740740740741	0.18887037037037	0.189	0.189111111111111	0.189240740740741	0.18937037037037	0.189481481481481	0.189611111111111	0.189740740740741	0.189851851851852	0.19	0.190111111111111	0.190222222222222	0.19037037037037	0.190481481481481	0.19062962962963	0.190740740740741	0.190851851851852	0.191	0.0	0.0	0.0	0.0	0.0	0.0	0.0	0.0393464813229044	0.0393464813229044	0.0393464813229044	0.0393464813229044	0.0786929626458088	0.0786929626458088	0.118039443968713	0.157385925291618	0.157385925291618	0.196732406614522	0.275425369260331	0.354118331906139	0.432811294551948	0.590197219843566	0.786929626458088	1.062354995718418	4.131380538904961	4.682231277425621	5.233082015946284	5.82327923578985	6.413476455633415	6.72824830621665	7.318445526060215	7.947989227226685	8.577532928393155	9.207076629559625	9.521848480142861	10.15139218130933	10.7809358824758	11.44982606496518	12.04002328480874	12.66956698597521	13.29911068714168	13.92865438830815	14.83362345873496	15.46316715990142	16.05336437974499	16.68290808091146	17.27310530075503	18.17807437118183	18.76827159102538	19.35846881086896	19.94866603071252	20.5388632505561	21.12906047039966	21.67991120892032	22.27010842876388	23.13573101786778	23.68658175638844	24.27677897623201	24.82762971475267	25.41782693459623	25.96867767311689	26.55887489296046	27.10972563148112	27.66057637000178	28.21142710852245	28.76227784704311	29.31312858556377	29.82463284276152	30.37548358128219	31.16241320774028	31.71326394626094	32.2247682034587	32.73627246065644	33.28712319917711	33.79862745637487	34.31013171357262	34.82163597077038	35.29379374664523	35.80529800384299	36.31680226104074	36.7889600369156	37.30046429411335	37.77262206998822	38.24477984586306	38.71693762173792	39.18909539761277	39.62190669216472	40.05471798671666	40.44818279994571	40.88099409449764	41.3138053890496	41.74661668360155	42.14008149683059	42.57289279138254	43.0057040859345	43.39916889916354	43.83198019371548	44.22544500694453	44.61890982017357	45.01237463340262	45.40583944663167	45.95669018515232	46.31080851705845	46.5862338863188	46.86165925557913	47.13708462483945	47.37316351277688	47.6092424007143	47.88466776997463	48.12074665791205	48.3961720271724	48.63225091510983	48.90767628437015	49.14375517230758	49.4191805415679	49.69460591082825	49.97003128008857	50.206110168026	50.48153553728632	50.71761442522375	50.9930397944841	51.2291186824215	51.46519757035894	51.74062293961927	51.9767018275567	52.25212719681703	52.48820608475445	52.76363145401478	52.9997103419522	53.23578922988964	53.47186811782705	53.70794700576448	53.94402589370192	54.21945126296225	54.45553015089968	54.6916090388371	54.92768792677452	55.16376681471195	55.39984570264937	55.6359245905868	55.87200347852423	56.10808236646166	56.30481477307617	56.54089366101359	56.77697254895103	56.97370495556554	57.20978384350298	57.4458627314404	57.64259513805493	57.87867402599234	58.07540643260688	58.3114853205443	58.50821772715882	58.70495013377334	58.94102902171077	59.1377614283253	59.33449383493982	59.45253327890853	59.64926568552305	59.80665161081466	59.92469105478337	60.082076980075	60.35750234933533	60.55423475594985	60.79031364388728	60.9870460505018	61.14443197579341	61.34116438240794	61.53789678902245	61.69528271431408	61.8526686396057	62.04940104622022	62.20678697151184	62.40351937812636	62.56090530341797	62.7182912287096	62.8756771540012	63.03306307929282	63.19044900458444	63.34783492987606	63.50522085516769	63.6626067804593	63.78064622442801	63.93803214971963	64.05607159368833	64.17411103765704	64.25280400030285	64.37084344427158	64.4888828882403	64.606922332209	64.72496177617772	64.84300122014643	65.00038714543804	65.11842658940677	65.23646603337547	65.3545054773442	65.4725449213129	65.55123788395871	65.6692773279274	65.78731677189614	65.86600973454195	65.98404917851065	66.10208862247934	66.18078158512516	66.2988210290939	66.3775139917397	66.4562069543855	66.53489991703131	66.65293936100004	66.73163232364584	66.81032528629165	66.84967176761455	66.92836473026037	67.00705769290617	67.08575065555196	67.1644436181978	67.2431365808436	67.3218295434894	67.40052250613521	67.47921546878102	67.51856195010393	67.59725491274973	67.67594787539554	67.75464083804135	67.79398731936425	67.87268028201007	67.91202676333298	67.9907197259788	68.0694126886246	68.10875916994748	68.1481056512704	68.2267986139162	68.2661450952391	68.3448380578849	68.38418453920782	68.42353102053072	68.50222398317654	68.54157046449944	68.58091694582236	68.62026342714526	68.65960990846815	68.69895638979105	68.77764935243685	68.81699583375976	68.85634231508266	68.89568879640557	68.93503527772847	68.97438175905138	69.0137282403743	69.0530747216972	69.09242120302011	69.131767684343	69.17111416566591	69.21046064698882	69.24980712831173	69.28915360963462	69.32850009095752	69.36784657228043	69.40719305360333	69.44653953492624	69.48588601624914	69.52523249757205	69.56457897889494	69.60392546021787	69.60392546021787	69.64327194154076	69.68261842286365	69.72196490418657	69.72196490418657	69.76131138550948	69.80065786683238	69.80065786683238	69.84000434815528	69.87935082947818	69.87935082947818	69.91869731080108	69.95804379212399	69.95804379212399	69.99739027344691	70.03673675476979	70.03673675476979	70.0760832360927	70.0760832360927	70.11542971741561	70.11542971741561	70.1547761987385	70.19412268006142	70.19412268006142	70.19412268006142	70.23346916138433	70.27281564270724	70.27281564270724	70.31216212403014	70.31216212403014	70.35150860535304	70.35150860535304	70.39085508667595	70.39085508667595	70.43020156799884	70.43020156799884	70.46954804932175	70.46954804932175	70.50889453064465	70.50889453064465	70.50889453064465	70.54824101196756	70.54824101196756	70.58758749329047	70.58758749329047	70.58758749329047	70.62693397461338	70.62693397461338	70.66628045593628	70.66628045593628	70.66628045593628	70.70562693725918	70.70562693725918	70.7449734185821	70.7449734185821	70.7449734185821	70.784319899905	70.784319899905	70.784319899905	70.8236663812279	70.8236663812279	70.8236663812279	70.86301286255078	70.86301286255078	70.86301286255078	70.90235934387371	70.90235934387371	70.90235934387371	70.9417058251966	70.9417058251966	70.9417058251966	70.9417058251966	70.9810523065195	70.9810523065195	70.9810523065195	71.02039878784241	71.02039878784241	71.02039878784241	71.02039878784241	71.05974526916531	71.05974526916531	71.05974526916531	71.05974526916531	71.09909175048821	71.09909175048821	71.09909175048821	71.09909175048821	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.25647767577985	71.25647767577985	71.25647767577985	71.25647767577985	71.25647767577985	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.72863545165468	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.68928897033179	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.6499424890089	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.61059600768597	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.57124952636307	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.5319030450402	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.49255656371728	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.45321008239436	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.41386360107148	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.37451711974855	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.33517063842564	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.29582415710275	71.25647767577985	71.25647767577985	71.25647767577985	71.25647767577985	71.25647767577985	71.25647767577985	71.25647767577985	71.25647767577985	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.21713119445693	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.17778471313403	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.09909175048821	71.09909175048821	71.09909175048821	71.09909175048821	71.09909175048821	71.09909175048821	71.09909175048821	71.05974526916531	71.05974526916531	71.05974526916531	71.05974526916531	71.05974526916531	71.05974526916531	71.05974526916531	71.02039878784241	71.02039878784241	71.02039878784241	71.02039878784241	71.02039878784241	71.02039878784241	71.02039878784241	70.9810523065195	70.9810523065195	70.9810523065195	70.9810523065195	70.9810523065195	70.9417058251966	70.9417058251966	70.9417058251966	70.9417058251966	70.9417058251966	70.9417058251966	70.90235934387371	70.90235934387371	70.90235934387371	70.90235934387371	70.90235934387371	70.90235934387371	70.90235934387371	70.86301286255078	70.86301286255078	70.86301286255078	70.86301286255078	70.86301286255078	70.86301286255078	70.86301286255078	70.8236663812279	70.8236663812279	70.8236663812279	70.8236663812279	70.8236663812279	70.8236663812279	70.784319899905	70.784319899905	70.784319899905	70.784319899905	70.784319899905	70.784319899905	70.784319899905	70.7449734185821	70.7449734185821	70.7449734185821	70.7449734185821	70.7449734185821	70.7449734185821	70.7449734185821	70.7449734185821	70.7449734185821	70.7449734185821	70.784319899905	70.784319899905	70.784319899905	70.784319899905	70.784319899905	70.8236663812279	70.8236663812279	70.8236663812279	70.86301286255078	70.86301286255078	70.86301286255078	70.90235934387371	70.90235934387371	70.90235934387371	70.90235934387371	70.9417058251966	70.9417058251966	70.9417058251966	70.9810523065195	70.9810523065195	70.9810523065195	71.02039878784241	71.02039878784241	71.02039878784241	71.02039878784241	71.05974526916531	71.05974526916531	71.05974526916531	71.09909175048821	71.09909175048821	71.09909175048821	71.09909175048821	71.09909175048821	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.13843823181112	71.09909175048821	71.09909175048821	71.09909175048821	71.05974526916531	71.05974526916531	71.02039878784241	71.02039878784241	70.9810523065195	70.9417058251966	70.9417058251966	70.90235934387371	70.86301286255078	70.86301286255078	70.8236663812279	70.784319899905	70.7449734185821	70.70562693725918	70.66628045593628	70.62693397461338	70.58758749329047	70.54824101196756	70.54824101196756	70.50889453064465	70.43020156799884	70.39085508667595	70.35150860535304	70.31216212403014	70.27281564270724	70.23346916138433	70.19412268006142	70.1547761987385	70.11542971741561	70.0760832360927	70.03673675476979	69.99739027344691	69.95804379212399	69.91869731080108	69.87935082947818	69.84000434815528	69.80065786683238	69.76131138550948	69.72196490418657	69.68261842286365	69.64327194154076	69.60392546021787	69.52523249757205	69.44653953492624	69.36784657228043	69.28915360963462	69.24980712831173	69.17111416566591	69.131767684343	69.09242120302011	69.0530747216972	69.0137282403743	68.97438175905138	68.97438175905138	68.93503527772847	68.93503527772847	68.89568879640557	68.89568879640557	68.89568879640557	68.89568879640557	68.85634231508266	68.85634231508266	68.85634231508266	68.85634231508266	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.81699583375976	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.77764935243685	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.73830287111396	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.69895638979105	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.65960990846815	68.62026342714526	68.62026342714526	68.62026342714526	68.62026342714526	68.62026342714526	68.62026342714526	68.62026342714526	68.62026342714526	68.58091694582236	68.58091694582236	68.58091694582236	68.58091694582236	68.58091694582236	68.58091694582236	68.58091694582236	68.58091694582236	68.54157046449944	68.54157046449944	68.54157046449944	68.54157046449944	68.54157046449944	68.54157046449944	68.50222398317654	68.50222398317654	68.50222398317654	68.50222398317654	68.50222398317654	68.46287750185363	68.46287750185363	68.46287750185363	68.46287750185363	68.46287750185363	68.42353102053072	68.42353102053072	68.42353102053072	68.42353102053072	68.42353102053072	68.38418453920782	68.38418453920782	68.38418453920782	68.38418453920782	68.3448380578849	68.3448380578849	68.3448380578849	68.3448380578849	68.30549157656199	68.30549157656199	68.30549157656199	68.30549157656199	68.2661450952391	68.2661450952391	68.2661450952391	68.2661450952391	68.2267986139162	68.2267986139162	68.2267986139162	68.2267986139162	68.18745213259328	68.18745213259328	68.18745213259328	68.18745213259328	68.1481056512704	68.1481056512704	68.1481056512704	68.10875916994748	68.10875916994748	68.10875916994748	68.10875916994748	68.0694126886246	68.0694126886246	68.0694126886246	68.03006620730168	68.03006620730168	68.03006620730168	68.03006620730168	67.9907197259788	67.9907197259788	67.9907197259788	67.95137324465588	67.95137324465588	67.95137324465588	67.91202676333298	67.91202676333298	67.91202676333298	67.87268028201007	67.87268028201007	67.87268028201007	67.83333380068716	67.83333380068716	67.83333380068716	67.79398731936425	67.79398731936425	67.79398731936425	67.75464083804135	67.75464083804135	67.71529435671845	67.71529435671845	67.71529435671845	67.67594787539554	67.67594787539554	67.63660139407264	67.63660139407264	67.63660139407264	67.59725491274973	67.59725491274973	67.55790843142682	67.55790843142682	67.51856195010393	67.51856195010393	67.47921546878102	67.47921546878102	67.43986898745813	67.43986898745813	67.40052250613521	67.40052250613521	67.3611760248123	67.3611760248123	67.3218295434894	67.3218295434894	67.28248306216651	67.2431365808436	67.2431365808436	67.20379009952067	67.20379009952067	67.1644436181978	67.1644436181978	67.12509713687484	67.08575065555196	67.08575065555196	67.04640417422908	67.00705769290617	66.96771121158325	66.92836473026037	66.88901824893746	66.84967176761455	66.84967176761455	66.81032528629165	66.73163232364584	66.73163232364584	66.69228584232292	66.65293936100004	66.61359287967713	66.53489991703131	66.53489991703131	66.4562069543855	66.4168604730626	66.3775139917397	66.33816751041678	66.2988210290939	66.25947454777098	66.22012806644808	66.18078158512516	66.10208862247934	66.06274214115643	66.02339565983357	65.98404917851065	65.90535621586484	65.86600973454195	65.82666325321903	65.78731677189614	65.70862380925032	65.6692773279274	65.62993084660448	65.55123788395871	65.51189140263581	65.4725449213129	65.3938519586671	65.3545054773442	65.31515899602127	65.23646603337547	65.19711955205257	65.11842658940677	65.07908010808383	65.03973362676095	64.96104066411517	64.92169418279223	64.88234770146931	64.80365473882351	64.7643082575006	64.6856152948548	64.64626881353188	64.56757585088609	64.5282293695632	64.44953640691738	64.4101899255945	64.33149696294867	64.29215048162576	64.21345751897995	64.17411103765704	64.09541807501125	64.01672511236544	63.97737863104253	63.89868566839672	63.81999270575091	63.78064622442801	63.7019532617822	63.6626067804593	63.58391381781349	63.50522085516769	63.46587437384477	63.38718141119896	63.30848844855316	63.26914196723025	63.19044900458444	63.11175604193864	63.03306307929282	62.99371659796993	62.91502363532412	62.83633067267831	62.75763771003249	62.7182912287096	62.63959826606378	62.56090530341797	62.52155882209508	62.40351937812636	62.32482641548054	62.28547993415764	62.20678697151184	62.12809400886603	62.08874752754312	62.01005456489731	61.8920151209286	61.81332215828279	61.7739756769599	61.69528271431408	61.61658975166826	61.53789678902245	61.45920382637664	61.41985734505375	61.30181790108504	61.22312493843923	61.14443197579341	61.06573901314761	60.9870460505018	60.908353087856	60.82966012521017	60.79031364388728	60.67227419991857	60.59358123727276	60.51488827462694	60.43619531198113	60.35750234933533	60.27880938668952	60.20011642404371	60.12142346139789	60.0427304987521	59.92469105478337	59.80665161081466	59.72795864816886	59.64926568552305	59.57057272287725	59.49187976023142	59.41318679758562	59.33449383493982	59.255800872294	59.1377614283253	59.05906846567948	58.98037550303367	58.86233605906497	58.74429661509624	58.66560365245044	58.58691068980463	58.46887124583592	58.39017828319011	58.3114853205443	58.19344587657558	58.1147529139298	58.03605995128397	57.91802050731525	57.76063458202364	57.68194161937782	57.56390217540912	57.4852092127633	57.36716976879459	57.28847680614878	57.17043736218007	57.05239791821135	56.93435847424264	56.85566551159683	56.65893310498232	56.54089366101359	56.4228542170449	56.30481477307617	56.18677532910747	56.02938940381585	55.6359245905868	49.45852702289081	17.54853067001535	-1.927977584822315	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.88863110349941	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	-1.849284622176506	Brass	0.0	0.0	0.0	0.0	1.85185185185185E-5	3.7037037037037E-5	9.25925925925927E-5	0.000111111111111111	0.00012962962962963	0.000185185185185185	0.000203703703703704	0.000222222222222222	0.000277777777777778	0.000296296296296296	0.000314814814814815	0.00037037037037037	0.000388888888888889	0.000407407407407407	0.000462962962962963	0.000481481481481481	0.0005	0.000555555555555555	0.000574074074074074	0.000592592592592592	0.000648148148148148	0.000666666666666666	0.000685185185185185	0.00074074074074074	0.000759259259259259	0.000777777777777778	0.000833333333333333	0.000851851851851852	0.00087037037037037	0.000925925925925926	0.000944444444444444	0.001	0.00101851851851852	0.00103703703703704	0.00109259259259259	0.00111111111111111	0.00112962962962963	0.00114814814814815	0.0012037037037037	0.00122222222222222	0.00127777777777778	0.0012962962962963	0.00131481481481481	0.00133333333333333	0.00138888888888889	0.00140740740740741	0.00146296296296296	0.00148148148148148	0.0015	0.00155555555555556	0.00157407407407407	0.00159259259259259	0.00164814814814815	0.00166666666666667	0.00168518518518518	0.00174074074074074	0.00175925925925926	0.00177777777777778	0.00183333333333333	0.00185185185185185	0.00187037037037037	0.00192592592592593	0.00194444444444444	0.00196296296296296	0.00201851851851852	0.00203703703703704	0.00205555555555556	0.00211111111111111	0.00212962962962963	0.00214814814814815	0.0022037037037037	0.00222222222222222	0.00225925925925926	0.0022962962962963	0.00231481481481481	0.00235185185185185	0.00238888888888889	0.00240740740740741	0.00244444444444444	0.00248148148148148	0.0025	0.00253703703703704	0.00257407407407407	0.00259259259259259	0.00262962962962963	0.00266666666666667	0.00268518518518518	0.00272222222222222	0.00275925925925926	0.00277777777777778	0.00281481481481481	0.00285185185185185	0.00287037037037037	0.00290740740740741	0.00294444444444444	0.00296296296296296	0.003	0.00303703703703704	0.00307407407407407	0.00309259259259259	0.00312962962962963	0.00314814814814815	0.00318518518518518	0.00322222222222222	0.00325925925925926	0.00327777777777778	0.00331481481481481	0.00335185185185185	0.00337037037037037	0.00340740740740741	0.00344444444444444	0.00346296296296296	0.0035	0.00353703703703704	0.00355555555555555	0.00359259259259259	0.00362962962962963	0.00364814814814815	0.00368518518518518	0.00372222222222222	0.00374074074074074	0.00377777777777778	0.00381481481481481	0.00383333333333333	0.00387037037037037	0.00390740740740741	0.00392592592592592	0.00396296296296296	0.004	0.00401851851851852	0.00405555555555555	0.00409259259259259	0.00411111111111111	0.00414814814814815	0.00418518518518518	0.0042037037037037	0.00424074074074074	0.00427777777777778	0.0042962962962963	0.00435185185185185	0.00437037037037037	0.00438888888888889	0.00442592592592592	0.00446296296296296	0.00448148148148148	0.00453703703703704	0.00455555555555555	0.00457407407407407	0.00462962962962963	0.00464814814814815	0.00466666666666667	0.00472222222222222	0.00474074074074074	0.00475925925925926	0.00481481481481481	0.00483333333333333	0.00485185185185185	0.00490740740740741	0.00492592592592593	0.00494444444444444	0.005	0.00501851851851852	0.00503703703703704	0.00509259259259259	0.00511111111111111	0.00512962962962963	0.00518518518518518	0.0052037037037037	0.00522222222222222	0.00527777777777778	0.00529629629629629	0.00531481481481481	0.00537037037037037	0.00538888888888889	0.00540740740740741	0.00546296296296296	0.00548148148148148	0.0055	0.00555555555555555	0.00557407407407407	0.00562962962962963	0.00564814814814815	0.00566666666666667	0.00568518518518518	0.00574074074074074	0.00575925925925926	0.00581481481481481	0.00583333333333333	0.00585185185185185	0.00590740740740741	0.00592592592592592	0.00594444444444444	0.006	0.00601851851851852	0.00603703703703704	0.00609259259259259	0.00611111111111111	0.00612962962962963	0.00618518518518518	0.0062037037037037	0.00622222222222222	0.00627777777777778	0.00629629629629629	0.00631481481481481	0.00637037037037037	0.00638888888888889	0.0064074074074074	0.00646296296296296	0.00648148148148148	0.0065	0.00655555555555555	0.00657407407407407	0.00659259259259259	0.00664814814814815	0.00666666666666666	0.00668518518518518	0.00674074074074074	0.00675925925925926	0.00677777777777778	0.00683333333333333	0.00685185185185185	0.00687037037037037	0.00692592592592592	0.00694444444444444	0.00696296296296296	0.00701851851851852	0.00703703703703704	0.00707407407407407	0.00711111111111111	0.00712962962962963	0.00714814814814815	0.0072037037037037	0.00722222222222222	0.00725925925925926	0.00729629629629629	0.00731481481481481	0.00735185185185185	0.00738888888888889	0.00740740740740741	0.00744444444444444	0.00748148148148148	0.0075	0.00753703703703703	0.00757407407407407	0.00759259259259259	0.00762962962962963	0.00766666666666666	0.00768518518518518	0.00772222222222222	0.00775925925925926	0.00777777777777778	0.00781481481481481	0.00785185185185185	0.00787037037037037	0.0079074074074074	0.00794444444444444	0.00796296296296296	0.008	0.00803703703703704	0.00807407407407407	0.00809259259259259	0.00812962962962963	0.00814814814814815	0.00818518518518518	0.00822222222222222	0.00824074074074074	0.00827777777777778	0.00831481481481481	0.00835185185185185	0.00837037037037037	0.0084074074074074	0.00844444444444444	0.00846296296296296	0.0085	0.00853703703703704	0.00855555555555555	0.00859259259259259	0.00862962962962963	0.00864814814814815	0.00868518518518518	0.00872222222222222	0.00874074074074074	0.00877777777777777	0.00881481481481481	0.00883333333333333	0.00887037037037037	0.00890740740740741	0.00892592592592592	0.00896296296296296	0.009	0.00901851851851851	0.00905555555555555	0.00909259259259259	0.00911111111111111	0.00914814814814815	0.00918518518518518	0.0092037037037037	0.00924074074074074	0.00927777777777777	0.00929629629629629	0.00933333333333333	0.00937037037037037	0.00938888888888889	0.00942592592592592	0.00946296296296296	0.00948148148148148	0.00951851851851852	0.00955555555555555	0.00957407407407407	0.00962962962962963	0.00964814814814815	0.00966666666666666	0.00972222222222222	0.00974074074074074	0.00975925925925926	0.00981481481481481	0.00983333333333333	0.00985185185185185	0.00990740740740741	0.00992592592592592	0.00994444444444444	0.01	0.0100185185185185	0.010037037037037	0.0100925925925926	0.0101111111111111	0.0101296296296296	0.0101851851851852	0.0102037037037037	0.0102222222222222	0.0102777777777778	0.0102962962962963	0.0103148148148148	0.0103703703703704	0.0103888888888889	0.0104444444444444	0.010462962962963	0.0104814814814815	0.0105	0.0105555555555556	0.0105740740740741	0.0106296296296296	0.0106481481481481	0.0106666666666667	0.0107222222222222	0.0107407407407407	0.0107592592592593	0.0108148148148148	0.0108333333333333	0.0108518518518518	0.0109074074074074	0.0109259259259259	0.0109444444444444	0.011	0.0110185185185185	0.011037037037037	0.0110925925925926	0.0111111111111111	0.0111296296296296	0.0111851851851852	0.0112037037037037	0.0112222222222222	0.0112777777777778	0.0112962962962963	0.0113148148148148	0.0113703703703704	0.0113888888888889	0.0114074074074074	0.011462962962963	0.0114814814814815	0.0115	0.0115555555555556	0.0115740740740741	0.0116111111111111	0.0116481481481481	0.0116666666666667	0.0117037037037037	0.0117407407407407	0.0117592592592593	0.0117962962962963	0.0118333333333333	0.0118518518518518	0.0118888888888889	0.0119259259259259	0.0119444444444444	0.0119814814814815	0.0120185185185185	0.012037037037037	0.0120740740740741	0.0121111111111111	0.0121296296296296	0.0121666666666667	0.0122037037037037	0.0122407407407407	0.0122592592592593	0.0122962962962963	0.0123333333333333	0.0123518518518518	0.0123888888888889	0.0124259259259259	0.0124444444444444	0.0124814814814815	0.0125185185185185	0.012537037037037	0.0125740740740741	0.0126111111111111	0.0126296296296296	0.0126666666666667	0.0127037037037037	0.0127222222222222	0.0127592592592593	0.0127962962962963	0.0128148148148148	0.0128518518518518	0.0128888888888889	0.0129074074074074	0.0129444444444444	0.0129814814814815	0.013	0.0130555555555556	0.0130740740740741	0.0130925925925926	0.0131296296296296	0.0131666666666667	0.0131851851851852	0.0132222222222222	0.0132592592592593	0.0132777777777778	0.0133333333333333	0.0133518518518518	0.0133703703703704	0.0134259259259259	0.0134444444444444	0.013462962962963	0.0135185185185185	0.013537037037037	0.0135555555555556	0.0136111111111111	0.0136296296296296	0.0136481481481481	0.0137037037037037	0.0137222222222222	0.0137407407407407	0.0137962962962963	0.0138148148148148	0.0138333333333333	0.0138888888888889	0.0139074074074074	0.0139259259259259	0.0139814814814815	0.014	0.0140185185185185	0.0140740740740741	0.0140925925925926	0.0141481481481481	0.0141666666666667	0.0141851851851852	0.0142037037037037	0.0142592592592593	0.0142777777777778	0.0143333333333333	0.0143518518518518	0.0143703703703704	0.0144259259259259	0.0144444444444444	0.014462962962963	0.0145185185185185	0.014537037037037	0.0145555555555556	0.0146111111111111	0.0146296296296296	0.0146481481481481	0.0147037037037037	0.0147222222222222	0.0147407407407407	0.0147962962962963	0.0148148148148148	0.0148333333333333	0.0148888888888889	0.0149074074074074	0.0149259259259259	0.0149814814814815	0.015	0.0150185185185185	0.0150740740740741	0.0150925925925926	0.0151296296296296	0.0151666666666667	0.0151851851851852	0.0152037037037037	0.0152592592592593	0.0152777777777778	0.0153148148148148	0.0153518518518518	0.0153703703703704	0.0154074074074074	0.0154444444444444	0.015462962962963	0.0155	0.015537037037037	0.0155555555555556	0.0155925925925926	0.0156296296296296	0.0156481481481481	0.0156851851851852	0.0157222222222222	0.0157407407407407	0.0157777777777778	0.0158148148148148	0.0158333333333333	0.0158703703703704	0.0159074074074074	0.0159259259259259	0.015962962962963	0.016	0.0160185185185185	0.0160555555555556	0.0160925925925926	0.0161111111111111	0.0161481481481481	0.0161851851851852	0.0162037037037037	0.0162407407407407	0.0162777777777778	0.0162962962962963	0.0163333333333333	0.0163703703703704	0.0163888888888889	0.0164259259259259	0.016462962962963	0.0164814814814815	0.0165185185185185	0.0165555555555556	0.0165740740740741	0.0166111111111111	0.0166481481481481	0.0166666666666667	0.0167037037037037	0.0167407407407407	0.0167592592592593	0.0167962962962963	0.0168333333333333	0.0168703703703704	0.0168888888888889	0.0169259259259259	0.016962962962963	0.0169814814814815	0.0170185185185185	0.0170555555555556	0.0170740740740741	0.0171111111111111	0.0171481481481481	0.0171666666666667	0.0172037037037037	0.0172407407407407	0.0172592592592593	0.0172962962962963	0.0173333333333333	0.0173518518518519	0.0173888888888889	0.0174259259259259	0.0174444444444444	0.0174814814814815	0.0175185185185185	0.017537037037037	0.0175740740740741	0.0176111111111111	0.0176296296296296	0.0176666666666667	0.0177037037037037	0.0177222222222222	0.0177592592592593	0.0177962962962963	0.0178148148148148	0.0178518518518518	0.0178888888888889	0.0179074074074074	0.0179444444444444	0.0179814814814815	0.018	0.018037037037037	0.0180740740740741	0.0180925925925926	0.0181296296296296	0.0181666666666667	0.0181851851851852	0.0182222222222222	0.0182592592592593	0.0182777777777778	0.0183148148148148	0.0183518518518518	0.0183703703703704	0.0184074074074074	0.0184444444444444	0.018462962962963	0.0185	0.018537037037037	0.0185555555555556	0.0185740740740741	0.0186296296296296	0.0186481481481481	0.0186666666666667	0.0187222222222222	0.0187407407407407	0.0187592592592593	0.0188148148148148	0.0188333333333333	0.0188518518518518	0.0189074074074074	0.0189259259259259	0.0189444444444444	0.019	0.0190185185185185	0.019037037037037	0.0190925925925926	0.0191111111111111	0.0191296296296296	0.0191851851851852	0.0192037037037037	0.0192592592592593	0.0192777777777778	0.0192962962962963	0.0193148148148148	0.0193703703703704	0.0193888888888889	0.0194444444444444	0.019462962962963	0.0194814814814815	0.019537037037037	0.0195555555555556	0.0195740740740741	0.0196296296296296	0.0196481481481481	0.0196666666666667	0.0197222222222222	0.0197407407407407	0.0197592592592593	0.0198148148148148	0.0198333333333333	0.0198518518518518	0.0199074074074074	0.0199259259259259	0.0199444444444444	0.02	0.0200185185185185	0.020037037037037	0.0200925925925926	0.0201111111111111	0.0201296296296296	0.0201851851851852	0.0202037037037037	0.0202222222222222	0.0202777777777778	0.0202962962962963	0.0203148148148148	0.0203703703703704	0.0203888888888889	0.0204074074074074	0.020462962962963	0.0204814814814815	0.0205	0.0205555555555556	0.0205740740740741	0.0205925925925926	0.0206481481481481	0.0206666666666667	0.0206851851851852	0.0207407407407407	0.0207592592592593	0.0207777777777778	0.0208333333333333	0.0208518518518518	0.0208888888888889	0.0209259259259259	0.0209444444444444	0.0209814814814815	0.0210185185185185	0.021037037037037	0.0210740740740741	0.0211111111111111	0.0211296296296296	0.0211666666666667	0.0212037037037037	0.0212222222222222	0.0212592592592593	0.0212962962962963	0.0213148148148148	0.0213518518518518	0.0213888888888889	0.0214074074074074	0.0214444444444444	0.0214814814814815	0.0215185185185185	0.021537037037037	0.0215740740740741	0.0216111111111111	0.0216296296296296	0.0216666666666667	0.0217037037037037	0.0217222222222222	0.0217592592592593	0.0217962962962963	0.0218148148148148	0.0218518518518518	0.0218888888888889	0.0219074074074074	0.0219444444444444	0.0219814814814815	0.022	0.022037037037037	0.0220740740740741	0.0220925925925926	0.0221296296296296	0.0221666666666667	0.0221851851851852	0.0222222222222222	0.0222592592592593	0.0222777777777778	0.0223333333333333	0.0223518518518518	0.0223703703703704	0.0224259259259259	0.0224444444444444	0.022462962962963	0.0225185185185185	0.022537037037037	0.0225555555555555	0.0226111111111111	0.0226296296296296	0.0226481481481481	0.0227037037037037	0.0227222222222222	0.0227407407407407	0.0227962962962963	0.0228148148148148	0.0228333333333333	0.0228888888888889	0.0229074074074074	0.0229259259259259	0.0229814814814815	0.023	0.0230185185185185	0.0230740740740741	0.0230925925925926	0.0231111111111111	0.0231666666666667	0.0231851851851852	0.0232037037037037	0.0232592592592593	0.0232777777777778	0.0232962962962963	0.0233518518518518	0.0233703703703704	0.0233888888888889	0.0234444444444444	0.023462962962963	0.0234814814814815	0.023537037037037	0.0235555555555556	0.0235740740740741	0.0236296296296296	0.0236481481481481	0.0236666666666667	0.0237222222222222	0.0237407407407407	0.0237962962962963	0.0238148148148148	0.0238333333333333	0.0238518518518518	0.0239074074074074	0.0239259259259259	0.0239814814814815	0.024	0.0240185185185185	0.0240740740740741	0.0240925925925926	0.0241111111111111	0.0241666666666667	0.0241851851851852	0.0242037037037037	0.0242592592592593	0.0242777777777778	0.0242962962962963	0.0243518518518518	0.0243703703703704	0.0243888888888889	0.0244444444444444	0.024462962962963	0.0244814814814815	0.024537037037037	0.0245555555555556	0.0245925925925926	0.0246296296296296	0.0246481481481481	0.0246666666666667	0.0247222222222222	0.0247407407407407	0.0247777777777778	0.0248148148148148	0.0248333333333333	0.0248703703703704	0.0249074074074074	0.0249259259259259	0.024962962962963	0.025	0.0250185185185185	0.0250555555555556	0.0250925925925926	0.0251111111111111	0.0251481481481481	0.0251851851851852	0.0252037037037037	0.0252407407407407	0.0252777777777778	0.0252962962962963	0.0253333333333333	0.0253703703703704	0.0253888888888889	0.0254259259259259	0.025462962962963	0.0254814814814815	0.0255185185185185	0.0255555555555555	0.0255740740740741	0.0256111111111111	0.0256481481481481	0.0256666666666667	0.0257037037037037	0.0257407407407407	0.0257777777777778	0.0257962962962963	0.0258333333333333	0.0258703703703704	0.0258888888888889	0.0259259259259259	0.025962962962963	0.0259814814814815	0.0260185185185185	0.0260555555555556	0.0260740740740741	0.0261111111111111	0.0261481481481481	0.0261666666666667	0.0262037037037037	0.0262407407407407	0.0262592592592593	0.0262962962962963	0.0263333333333333	0.0263518518518518	0.0263888888888889	0.0264259259259259	0.0264444444444444	0.0264814814814815	0.0265185185185185	0.026537037037037	0.0265740740740741	0.0266111111111111	0.0266296296296296	0.0266851851851852	0.0267037037037037	0.0267222222222222	0.0267592592592593	0.0267962962962963	0.0268148148148148	0.0268703703703704	0.0268888888888889	0.0269074074074074	0.026962962962963	0.0269814814814815	0.027	0.0270555555555556	0.0270740740740741	0.0270925925925926	0.0271481481481481	0.0271666666666667	0.0271851851851852	0.0272407407407407	0.0272592592592593	0.0272777777777778	0.0273333333333333	0.0273518518518518	0.0273703703703704	0.0274259259259259	0.0274444444444444	0.027462962962963	0.0275185185185185	0.027537037037037	0.0275555555555555	0.0276111111111111	0.0276296296296296	0.0276851851851852	0.0277037037037037	0.0277222222222222	0.0277777777777778	0.0277962962962963	0.0278148148148148	0.0278333333333333	0.0278888888888889	0.0279074074074074	0.027962962962963	0.0279814814814815	0.028	0.0280555555555555	0.0280740740740741	0.0280925925925926	0.0281481481481481	0.0281666666666667	0.0281851851851852	0.0282407407407407	0.0282592592592593	0.0282777777777778	0.0283333333333333	0.0283518518518518	0.0283703703703704	0.0284259259259259	0.0284444444444444	0.028462962962963	0.0285185185185185	0.028537037037037	0.0285740740740741	0.0286111111111111	0.0286296296296296	0.0286666666666667	0.0287037037037037	0.0287222222222222	0.0287592592592593	0.0287962962962963	0.0288148148148148	0.0288518518518518	0.0288888888888889	0.0289074074074074	0.0289444444444444	0.0289814814814815	0.029	0.029037037037037	0.0290740740740741	0.0290925925925926	0.0291296296296296	0.0291666666666667	0.0291851851851852	0.0292222222222222	0.0292592592592593	0.0292777777777778	0.0293148148148148	0.0293518518518518	0.0293888888888889	0.0294074074074074	0.0294444444444444	0.029462962962963	0.0295	0.029537037037037	0.0295740740740741	0.0295925925925926	0.0296296296296296	0.0296481481481481	0.0296851851851852	0.0297222222222222	0.0297592592592593	0.0297777777777778	0.0298148148148148	0.0298333333333333	0.0298703703703704	0.0299074074074074	0.0299444444444444	0.029962962962963	0.03	0.030037037037037	0.0300555555555555	0.0300925925925926	0.0301296296296296	0.0301481481481481	0.0301851851851852	0.0302222222222222	0.0302407407407407	0.0302777777777778	0.0302962962962963	0.0303333333333333	0.0303703703703704	0.0304074074074074	0.0304259259259259	0.030462962962963	0.0305	0.0305185185185185	0.0305555555555555	0.0305925925925926	0.0306111111111111	0.0306481481481481	0.0306851851851852	0.0307037037037037	0.0307407407407407	0.0307777777777778	0.0307962962962963	0.0308333333333333	0.0308703703703704	0.0308888888888889	0.0309259259259259	0.030962962962963	0.0309814814814815	0.0310185185185185	0.0310555555555555	0.0310740740740741	0.0311111111111111	0.0311481481481481	0.0311666666666667	0.0312037037037037	0.0312407407407407	0.0312592592592593	0.0312962962962963	0.0313333333333333	0.0313518518518518	0.0313888888888889	0.0314259259259259	0.0314444444444444	0.0314814814814815	0.0315185185185185	0.031537037037037	0.0315740740740741	0.0316111111111111	0.0316296296296296	0.0316666666666667	0.0317037037037037	0.0317222222222222	0.0317592592592593	0.0317962962962963	0.0318148148148148	0.0318518518518518	0.0318888888888889	0.0319074074074074	0.031962962962963	0.0319814814814815	0.032	0.032037037037037	0.0320740740740741	0.0320925925925926	0.0321481481481481	0.0321666666666667	0.0321851851851852	0.0322222222222222	0.0322592592592593	0.0322777777777778	0.0323333333333333	0.0323518518518518	0.0323703703703704	0.0324074074074074	0.0324444444444444	0.032462962962963	0.0325185185185185	0.032537037037037	0.0325555555555555	0.0326111111111111	0.0326296296296296	0.0326481481481481	0.0327037037037037	0.0327222222222222	0.0327407407407407	0.0327962962962963	0.0328148148148148	0.0328333333333333	0.0328888888888889	0.0329074074074074	0.0329259259259259	0.0329814814814815	0.033	0.0330185185185185	0.0330740740740741	0.0330925925925926	0.0331111111111111	0.0331666666666667	0.0331851851851852	0.0332037037037037	0.0332592592592593	0.0332777777777778	0.0332962962962963	0.0333518518518518	0.0333703703703704	0.0333888888888889	0.0334444444444444	0.033462962962963	0.0334814814814815	0.033537037037037	0.0335555555555555	0.0335740740740741	0.0336296296296296	0.0336481481481481	0.0336666666666667	0.0337222222222222	0.0337407407407407	0.0337592592592593	0.0338148148148148	0.0338333333333333	0.0338518518518518	0.0339074074074074	0.0339259259259259	0.0339444444444444	0.034	0.0340185185185185	0.034037037037037	0.0340925925925926	0.0341111111111111	0.0341296296296296	0.0341851851851852	0.0342037037037037	0.0342592592592593	0.0342777777777778	0.0342962962962963	0.0343148148148148	0.0343703703703704	0.0343888888888889	0.0344444444444444	0.034462962962963	0.0344814814814815	0.034537037037037	0.0345555555555555	0.0345740740740741	0.0346296296296296	0.0346481481481481	0.0346666666666667	0.0347222222222222	0.0347407407407407	0.0347592592592593	0.0348148148148148	0.0348333333333333	0.0348518518518518	0.0349074074074074	0.0349259259259259	0.0349444444444444	0.035	0.0350185185185185	0.035037037037037	0.0350925925925926	0.0351111111111111	0.0351296296296296	0.0351851851851852	0.0352037037037037	0.0352222222222222	0.0352777777777778	0.0352962962962963	0.0353148148148148	0.0353703703703704	0.0353888888888889	0.0354074074074074	0.035462962962963	0.0354814814814815	0.0355	0.0355555555555555	0.0355740740740741	0.0355925925925926	0.0356481481481481	0.0356666666666667	0.0356851851851852	0.0357407407407407	0.0357592592592593	0.0357962962962963	0.0358333333333333	0.0358518518518518	0.0358703703703704	0.0359259259259259	0.0359444444444444	0.0359814814814815	0.0360185185185185	0.036037037037037	0.0360740740740741	0.0361111111111111	0.0361296296296296	0.0361666666666667	0.0362037037037037	0.0362222222222222	0.0362592592592593	0.0362962962962963	0.0363148148148148	0.0363518518518518	0.0363888888888889	0.0364074074074074	0.0364444444444444	0.0364814814814815	0.0365	0.036537037037037	0.0365740740740741	0.0365925925925926	0.0366296296296296	0.0366666666666667	0.0366851851851852	0.0367222222222222	0.0367592592592593	0.0367777777777778	0.0368148148148148	0.0368518518518518	0.0368703703703704	0.0369074074074074	0.0369444444444444	0.0369814814814815	0.037	0.037037037037037	0.0370555555555555	0.0370925925925926	0.0371111111111111	0.0371666666666667	0.0371851851851852	0.0372037037037037	0.0372592592592593	0.0372777777777778	0.0372962962962963	0.0373518518518518	0.0373703703703704	0.0373888888888889	0.0374444444444444	0.037462962962963	0.0374814814814815	0.037537037037037	0.0375555555555555	0.0375740740740741	0.0376296296296296	0.0376481481481481	0.0376666666666667	0.0377222222222222	0.0377407407407407	0.0377592592592593	0.0378148148148148	0.0378333333333333	0.0378518518518518	0.0379074074074074	0.0379259259259259	0.0379444444444444	0.038	0.0380185185185185	0.038037037037037	0.0380925925925926	0.0381111111111111	0.0381296296296296	0.0381851851851852	0.0382037037037037	0.0382592592592592	0.0382777777777778	0.0382962962962963	0.0383148148148148	0.0383703703703704	0.0383888888888889	0.0384444444444444	0.038462962962963	0.0384814814814815	0.038537037037037	0.0385555555555555	0.0385740740740741	0.0386296296296296	0.0386481481481481	0.0386666666666667	0.0387222222222222	0.0387407407407407	0.0387592592592592	0.0388148148148148	0.0388333333333333	0.0388518518518518	0.0389074074074074	0.0389259259259259	0.0389444444444444	0.039	0.0390185185185185	0.039037037037037	0.0390925925925926	0.0391111111111111	0.0391296296296296	0.0391851851851852	0.0392037037037037	0.0392222222222222	0.0392777777777778	0.0392962962962963	0.0393148148148148	0.0393703703703704	0.0393888888888889	0.0394074074074074	0.0394629629629629	0.0394814814814815	0.0395185185185185	0.0395555555555556	0.0395740740740741	0.0395925925925926	0.0396481481481481	0.0396666666666667	0.0397037037037037	0.0397407407407407	0.0397592592592592	0.0397777777777778	0.0398333333333333	0.0398518518518518	0.0398888888888889	0.0399259259259259	0.0399444444444444	0.0399814814814815	0.0400185185185185	0.040037037037037	0.0400740740740741	0.0401111111111111	0.0401296296296296	0.0401666666666667	0.0402037037037037	0.0402222222222222	0.0402592592592593	0.0402962962962963	0.0403148148148148	0.0403518518518518	0.0403888888888889	0.0404074074074074	0.0404444444444444	0.0404814814814815	0.0405	0.040537037037037	0.0405740740740741	0.0405925925925926	0.0406296296296296	0.0406666666666667	0.0406851851851852	0.0407222222222222	0.0407592592592593	0.0407777777777778	0.0408148148148148	0.0408518518518518	0.0408703703703704	0.0409074074074074	0.0409444444444444	0.0409814814814815	0.041	0.041037037037037	0.0410740740740741	0.0410925925925926	0.0411296296296296	0.0411666666666667	0.0411851851851852	0.0412222222222222	0.0412592592592593	0.0412777777777778	0.0413148148148148	0.0413518518518518	0.0413703703703704	0.0414074074074074	0.0414444444444444	0.041462962962963	0.0415	0.041537037037037	0.0415555555555556	0.0415925925925926	0.0416296296296296	0.0416481481481481	0.0416851851851852	0.0417222222222222	0.0417407407407407	0.0417962962962963	0.0418148148148148	0.0418333333333333	0.0418703703703704	0.0419074074074074	0.0419259259259259	0.0419814814814815	0.042	0.0420185185185185	0.0420740740740741	0.0420925925925926	0.0421111111111111	0.0421481481481481	0.0421851851851852	0.0422037037037037	0.0422592592592593	0.0422777777777778	0.0422962962962963	0.0423518518518518	0.0423703703703704	0.0423888888888889	0.0424444444444444	0.042462962962963	0.0424814814814815	0.042537037037037	0.0425555555555555	0.0425740740740741	0.0426296296296296	0.0426481481481481	0.0426666666666667	0.0427222222222222	0.0427407407407407	0.0427592592592593	0.0428148148148148	0.0428333333333333	0.0428518518518518	0.0429074074074074	0.0429259259259259	0.0429444444444444	0.043	0.0430185185185185	0.043037037037037	0.0430925925925926	0.0431111111111111	0.0431296296296296	0.0431851851851852	0.0432037037037037	0.0432222222222222	0.0432777777777778	0.0432962962962963	0.0433148148148148	0.0433703703703704	0.0433888888888889	0.0434074074074074	0.043462962962963	0.0434814814814815	0.0435	0.0435555555555555	0.0435740740740741	0.0435925925925926	0.0436481481481481	0.0436666666666667	0.0436851851851852	0.0437407407407407	0.0437592592592593	0.0437777777777778	0.0438333333333333	0.0438518518518518	0.0438703703703704	0.0439259259259259	0.0439444444444444	0.043962962962963	0.0440185185185185	0.044037037037037	0.0440555555555555	0.0441111111111111	0.0441296296296296	0.0441481481481481	0.0442037037037037	0.0442222222222222	0.0442407407407407	0.0442962962962963	0.0443148148148148	0.0443333333333333	0.0443888888888889	0.0444074074074074	0.0444259259259259	0.0444814814814815	0.0445	0.0445185185185185	0.0445740740740741	0.0445925925925926	0.0446111111111111	0.0446666666666667	0.0446851851851852	0.0447037037037037	0.0447592592592592	0.0447777777777778	0.0447962962962963	0.0448518518518518	0.0448703703703704	0.0448888888888889	0.0449444444444444	0.044962962962963	0.0449814814814815	0.045037037037037	0.0450555555555555	0.0450740740740741	0.0451296296296296	0.0451481481481481	0.0451666666666667	0.0452222222222222	0.0452407407407407	0.0452592592592592	0.0453148148148148	0.0453333333333333	0.0453518518518518	0.0454074074074074	0.0454259259259259	0.0454814814814815	0.0455	0.0455185185185185	0.0455740740740741	0.0455925925925926	0.0456111111111111	0.0456296296296296	0.0456851851851852	0.0457037037037037	0.0457592592592593	0.0457777777777778	0.0457962962962963	0.0458518518518518	0.0458703703703704	0.0458888888888889	0.0459444444444444	0.045962962962963	0.0459814814814815	0.046037037037037	0.0460555555555555	0.0460740740740741	0.0461296296296296	0.0461481481481481	0.0461666666666667	0.0462222222222222	0.0462407407407407	0.0462592592592593	0.0463148148148148	0.0463333333333333	0.0463518518518518	0.0464074074074074	0.0464259259259259	0.0464444444444444	0.0465	0.0465185185185185	0.0465555555555555	0.0465925925925926	0.0466111111111111	0.0466296296296296	0.0466851851851852	0.0467037037037037	0.0467407407407407	0.0467777777777778	0.0467962962962963	0.0468333333333333	0.0468703703703704	0.0468888888888889	0.0469259259259259	0.046962962962963	0.0469814814814815	0.0470185185185185	0.0470555555555555	0.0470740740740741	0.0471111111111111	0.0471481481481481	0.0471666666666667	0.0472037037037037	0.0472407407407407	0.0472592592592592	0.0472962962962963	0.0473333333333333	0.0473518518518518	0.0473888888888889	0.0474259259259259	0.0474444444444444	0.0474814814814815	0.0475185185185185	0.047537037037037	0.0475740740740741	0.0476111111111111	0.0476296296296296	0.0476666666666667	0.0477037037037037	0.0477222222222222	0.0477592592592593	0.0477962962962963	0.0478333333333333	0.0478518518518518	0.0478888888888889	0.0479074074074074	0.0479444444444444	0.0479814814814815	0.0480185185185185	0.048037037037037	0.0480740740740741	0.0481111111111111	0.0481296296296296	0.0481666666666667	0.0482037037037037	0.0482222222222222	0.0482592592592592	0.0482962962962963	0.0483148148148148	0.0483518518518518	0.0483888888888889	0.0484074074074074	0.0484444444444444	0.0484814814814815	0.0485	0.048537037037037	0.0485740740740741	0.0485925925925926	0.0486481481481481	0.0486666666666667	0.0486851851851852	0.0487407407407407	0.0487592592592592	0.0487777777777778	0.0488333333333333	0.0488518518518518	0.0488703703703704	0.0489259259259259	0.0489444444444444	0.048962962962963	0.0490185185185185	0.049037037037037	0.0490555555555555	0.0491111111111111	0.0491296296296296	0.0491481481481481	0.0492037037037037	0.0492222222222222	0.0492407407407407	0.0492962962962963	0.0493148148148148	0.0493333333333333	0.0493888888888889	0.0494074074074074	0.0494259259259259	0.0494814814814815	0.0495	0.0495185185185185	0.0495740740740741	0.0495925925925926	0.0496111111111111	0.0496666666666667	0.0496851851851852	0.0497037037037037	0.0497592592592592	0.0497777777777778	0.0497962962962963	0.0498518518518518	0.0498703703703704	0.0498888888888889	0.0499444444444444	0.0499629629629629	0.0500185185185185	0.050037037037037	0.0500555555555555	0.0501111111111111	0.0501296296296296	0.0501481481481481	0.0502037037037037	0.0502222222222222	0.0502407407407407	0.0502962962962963	0.0503148148148148	0.0503333333333333	0.0503888888888889	0.0504074074074074	0.0504259259259259	0.0504814814814815	0.0505	0.0505185185185185	0.0505740740740741	0.0505925925925926	0.0506111111111111	0.0506666666666667	0.0506851851851852	0.0507222222222222	0.0507592592592593	0.0507777777777778	0.0508148148148148	0.0508518518518518	0.0508703703703704	0.0509074074074074	0.0509444444444444	0.0509629629629629	0.051	0.051037037037037	0.0510740740740741	0.0510925925925926	0.0511296296296296	0.0511666666666667	0.0511851851851852	0.0512222222222222	0.0512592592592592	0.0512777777777778	0.0513148148148148	0.0513518518518518	0.0513703703703704	0.0514259259259259	0.0514444444444444	0.051462962962963	0.0515185185185185	0.051537037037037	0.0515555555555555	0.0516111111111111	0.0516296296296296	0.0516481481481481	0.0517037037037037	0.0517222222222222	0.0517407407407407	0.0517962962962963	0.0518148148148148	0.0518333333333333	0.0518888888888889	0.0519074074074074	0.0519259259259259	0.0519814814814815	0.052	0.0520185185185185	0.0520740740740741	0.0520925925925926	0.0521111111111111	0.0521666666666667	0.0521851851851852	0.0522407407407407	0.0522592592592593	0.0522777777777778	0.0522962962962963	0.0523518518518518	0.0523703703703704	0.0524259259259259	0.0524444444444444	0.052462962962963	0.0525185185185185	0.052537037037037	0.0525555555555555	0.0526111111111111	0.0526296296296296	0.0526481481481481	0.0527037037037037	0.0527222222222222	0.0527407407407407	0.0527962962962963	0.0528148148148148	0.0528333333333333	0.0528888888888889	0.0529074074074074	0.0529259259259259	0.0529814814814815	0.053	0.0530185185185185	0.0530740740740741	0.0530925925925926	0.0531296296296296	0.0531666666666667	0.0531851851851852	0.0532222222222222	0.0532592592592592	0.0532777777777778	0.0533148148148148	0.0533518518518518	0.0533703703703704	0.0534074074074074	0.0534444444444444	0.053462962962963	0.0535	0.053537037037037	0.0535555555555555	0.0535925925925926	0.0536296296296296	0.0536666666666667	0.0536851851851852	0.0537222222222222	0.0537592592592592	0.0537777777777778	0.0538148148148148	0.0538518518518518	0.0538703703703704	0.0539074074074074	0.0539444444444444	0.053962962962963	0.054	0.054037037037037	0.0540555555555555	0.0540925925925926	0.0541296296296296	0.0541481481481481	0.0541851851851852	0.0542222222222222	0.0542407407407407	0.0542962962962963	0.0543148148148148	0.0543333333333333	0.0543888888888889	0.0544074074074074	0.0544259259259259	0.0544814814814815	0.0545	0.0545185185185185	0.0545740740740741	0.0545925925925926	0.0546111111111111	0.0546666666666667	0.0546851851851852	0.0547037037037037	0.0547592592592592	0.0547777777777778	0.0547962962962963	0.0548518518518518	0.0548703703703704	0.0548888888888889	0.0549444444444444	0.054962962962963	0.0550185185185185	0.055037037037037	0.0550555555555555	0.0551111111111111	0.0551296296296296	0.0551481481481481	0.0552037037037037	0.0552222222222222	0.0552407407407407	0.0552962962962963	0.0553148148148148	0.0553333333333333	0.0553888888888889	0.0554074074074074	0.0554259259259259	0.0554814814814815	0.0555	0.0555185185185185	0.0555555555555555	0.0555925925925926	0.0556111111111111	0.0556481481481481	0.0556851851851852	0.0557037037037037	0.0557407407407407	0.0557777777777778	0.0558148148148148	0.0558333333333333	0.0558703703703704	0.0559074074074074	0.0559259259259259	0.0559629629629629	0.056	0.0560185185185185	0.0560555555555555	0.0560925925925926	0.0561111111111111	0.0561481481481481	0.0561851851851852	0.0562037037037037	0.0562407407407407	0.0562777777777778	0.0562962962962963	0.0563333333333333	0.0563703703703704	0.0563888888888889	0.0564444444444444	0.056462962962963	0.0564814814814815	0.056537037037037	0.0565555555555555	0.0565740740740741	0.0566296296296296	0.0566481481481481	0.0566666666666667	0.0567222222222222	0.0567407407407407	0.0567592592592592	0.0568148148148148	0.0568333333333333	0.0568518518518518	0.0569074074074074	0.0569259259259259	0.0569444444444444	0.057	0.0570185185185185	0.057037037037037	0.0570925925925926	0.0571111111111111	0.0571296296296296	0.0571851851851852	0.0572037037037037	0.0572222222222222	0.0572777777777778	0.0572962962962963	0.0573518518518518	0.0573703703703704	0.0573888888888889	0.0574074074074074	0.057462962962963	0.0574814814814815	0.057537037037037	0.0575555555555555	0.0575740740740741	0.0576296296296296	0.0576481481481481	0.0576666666666667	0.0577222222222222	0.0577407407407407	0.0577592592592592	0.0578148148148148	0.0578333333333333	0.0578518518518518	0.0579074074074074	0.0579259259259259	0.0579444444444444	0.058	0.0580185185185185	0.058037037037037	0.0580925925925926	0.0581111111111111	0.0581296296296296	0.0581851851851852	0.0582037037037037	0.0582222222222222	0.0582777777777778	0.0582962962962963	0.0583333333333333	0.0583703703703704	0.0583888888888889	0.0584074074074074	0.058462962962963	0.0584814814814815	0.0585185185185185	0.0585555555555555	0.0585740740740741	0.0586111111111111	0.0586481481481481	0.0586666666666667	0.0587037037037037	0.0587407407407407	0.0587592592592592	0.0587962962962963	0.0588333333333333	0.0588518518518518	0.0588888888888889	0.0589259259259259	0.0589444444444444	0.0589814814814815	0.0590185185185185	0.059037037037037	0.0590740740740741	0.0591111111111111	0.0591296296296296	0.0591666666666667	0.0592037037037037	0.0592222222222222	0.0592592592592592	0.0592962962962963	0.0593148148148148	0.0593518518518518	0.0593888888888889	0.0594074074074074	0.0594444444444444	0.0594814814814815	0.0595	0.059537037037037	0.0595740740740741	0.0595925925925926	0.0596296296296296	0.0596666666666667	0.0596851851851852	0.0597222222222222	0.0597592592592592	0.0597777777777778	0.0598148148148148	0.0598518518518518	0.0598703703703704	0.0599074074074074	0.0599444444444444	0.0599629629629629	0.06	0.060037037037037	0.0600555555555555	0.0600925925925926	0.0601296296296296	0.0601481481481481	0.0601851851851852	0.0602222222222222	0.0602592592592593	0.0602777777777778	0.0603148148148148	0.0603333333333333	0.0603703703703704	0.0604074074074074	0.0604444444444444	0.060462962962963	0.0605	0.060537037037037	0.0605555555555555	0.0605925925925926	0.0606296296296296	0.0606481481481481	0.0606851851851852	0.0607222222222222	0.0607407407407407	0.0607777777777778	0.0608148148148148	0.0608333333333333	0.0608888888888889	0.0609074074074074	0.0609259259259259	0.0609814814814815	0.061	0.0610185185185185	0.0610740740740741	0.0610925925925926	0.0611111111111111	0.0611666666666667	0.0611851851851852	0.0612037037037037	0.0612592592592592	0.0612777777777778	0.0612962962962963	0.0613518518518518	0.0613703703703704	0.0613888888888889	0.0614444444444444	0.061462962962963	0.0614814814814815	0.061537037037037	0.0615555555555555	0.0615740740740741	0.0616296296296296	0.0616481481481481	0.0616666666666667	0.0617222222222222	0.0617407407407407	0.0617592592592592	0.0618148148148148	0.0618333333333333	0.0618888888888889	0.0619074074074074	0.0619259259259259	0.0619444444444444	0.062	0.0620185185185185	0.0620740740740741	0.0620925925925926	0.0621111111111111	0.0621666666666667	0.0621851851851852	0.0622037037037037	0.0622592592592593	0.0622777777777778	0.0622962962962963	0.0623518518518518	0.0623703703703704	0.0623888888888889	0.0624444444444444	0.062462962962963	0.0624814814814815	0.062537037037037	0.0625555555555555	0.0625740740740741	0.0626296296296296	0.0626481481481481	0.0626666666666666	0.0627222222222222	0.0627407407407407	0.0627592592592592	0.0628148148148148	0.0628333333333333	0.0628703703703704	0.0629074074074074	0.0629259259259259	0.0629444444444444	0.063	0.0630185185185185	0.063037037037037	0.0630925925925926	0.0631111111111111	0.0631481481481481	0.0631851851851852	0.0632037037037037	0.0632407407407407	0.0632777777777778	0.0632962962962963	0.0633333333333333	0.0633703703703704	0.0633888888888889	0.0634259259259259	0.0634629629629629	0.0634814814814815	0.0635185185185185	0.0635555555555555	0.0635740740740741	0.0636111111111111	0.0636481481481481	0.0636666666666667	0.0637037037037037	0.0637407407407407	0.0637592592592593	0.0637962962962963	0.0638333333333333	0.0638518518518518	0.0638888888888889	0.0639259259259259	0.0639444444444444	0.0639814814814815	0.0640185185185185	0.064037037037037	0.0640740740740741	0.0641111111111111	0.0641296296296296	0.0641666666666667	0.0642037037037037	0.0642222222222222	0.0642592592592593	0.0642962962962963	0.0643333333333333	0.0643518518518518	0.0643888888888889	0.0644259259259259	0.0644444444444444	0.0644814814814815	0.0645185185185185	0.064537037037037	0.0645740740740741	0.0646111111111111	0.0646296296296296	0.0646666666666667	0.0647037037037037	0.0647222222222222	0.0647777777777778	0.0647962962962963	0.0648148148148148	0.0648703703703704	0.0648888888888889	0.0649074074074074	0.0649444444444444	0.0649814814814815	0.065	0.065037037037037	0.0650740740740741	0.0650925925925926	0.0651481481481481	0.0651666666666667	0.0651851851851852	0.0652407407407407	0.0652592592592592	0.0652777777777778	0.0653333333333333	0.0653518518518518	0.0653703703703704	0.0654259259259259	0.0654444444444444	0.0654629629629629	0.0655185185185185	0.065537037037037	0.0655555555555555	0.0656111111111111	0.0656296296296296	0.0656481481481481	0.0657037037037037	0.0657222222222222	0.0657777777777778	0.0657962962962963	0.0658148148148148	0.0658703703703704	0.0658888888888889	0.0659074074074074	0.0659629629629629	0.0659814814814815	0.066	0.0660555555555555	0.0660740740740741	0.0660925925925926	0.0661481481481481	0.0661666666666667	0.0661851851851852	0.0662407407407407	0.0662592592592592	0.0662777777777778	0.0663333333333333	0.0663518518518518	0.0663888888888889	0.0664259259259259	0.0664444444444444	0.0664814814814815	0.0665185185185185	0.066537037037037	0.0665740740740741	0.0666111111111111	0.0666296296296296	0.0666666666666667	0.0667037037037037	0.0667222222222222	0.0667592592592592	0.0667962962962963	0.0668148148148148	0.0668518518518518	0.0668888888888889	0.0669074074074074	0.0669444444444444	0.0669814814814815	0.067	0.067037037037037	0.0670740740740741	0.0670925925925926	0.0671296296296296	0.0671666666666667	0.0671851851851852	0.0672222222222222	0.0672592592592592	0.0672777777777778	0.0673148148148148	0.0673518518518518	0.0673703703703704	0.0674074074074074	0.0674444444444444	0.0674629629629629	0.0675	0.067537037037037	0.0675555555555555	0.0675925925925926	0.0676296296296296	0.0676481481481481	0.0676851851851852	0.0677222222222222	0.0677407407407407	0.0677777777777778	0.0678148148148148	0.0678333333333333	0.0678703703703704	0.0679074074074074	0.0679259259259259	0.0679629629629629	0.068	0.0680185185185185	0.0680555555555555	0.0680925925925926	0.0681111111111111	0.0681481481481481	0.0681851851851852	0.0682037037037037	0.0682407407407407	0.0682777777777778	0.0683148148148148	0.0683333333333333	0.0683703703703704	0.0683888888888889	0.0684259259259259	0.0684629629629629	0.0685	0.0685185185185185	0.0685555555555555	0.0685740740740741	0.0686111111111111	0.0686481481481481	0.0686666666666667	0.0687037037037037	0.0687407407407407	0.0687777777777778	0.0687962962962963	0.0688333333333333	0.0688518518518518	0.0688888888888889	0.0689259259259259	0.0689444444444444	0.0689814814814815	0.0690185185185185	0.069037037037037	0.0690740740740741	0.0691111111111111	0.0691296296296296	0.0691666666666667	0.0692037037037037	0.0692222222222222	0.0692592592592592	0.0692962962962963	0.0693148148148148	0.0693518518518518	0.0693888888888889	0.0694074074074074	0.0694444444444444	0.0694814814814815	0.0695	0.069537037037037	0.0695740740740741	0.0695925925925926	0.0696296296296296	0.0696666666666667	0.0696851851851852	0.0697222222222222	0.0697592592592592	0.0697777777777778	0.0698148148148148	0.0698518518518518	0.0698703703703704	0.0699074074074074	0.0699444444444444	0.0699629629629629	0.07	0.070037037037037	0.0700740740740741	0.0700925925925926	0.0701296296296296	0.0701666666666667	0.0701851851851852	0.0702222222222222	0.0702592592592593	0.0702777777777778	0.0703148148148148	0.0703518518518518	0.0703703703703704	0.0704074074074074	0.0704444444444444	0.070462962962963	0.0705	0.070537037037037	0.0705555555555555	0.0705925925925926	0.0706296296296296	0.0706481481481481	0.0706851851851852	0.0707222222222222	0.0707407407407407	0.0707777777777778	0.0708148148148148	0.0708333333333333	0.0708703703703704	0.0709074074074074	0.0709259259259259	0.070962962962963	0.071	0.0710185185185185	0.0710555555555555	0.0710925925925926	0.0711111111111111	0.0711481481481481	0.0711851851851852	0.0712037037037037	0.0712407407407407	0.0712777777777778	0.0712962962962963	0.0713333333333333	0.0713703703703704	0.0713888888888889	0.0714259259259259	0.071462962962963	0.0714814814814815	0.0715185185185185	0.0715555555555555	0.0715740740740741	0.0716111111111111	0.0716481481481481	0.0716666666666667	0.0717037037037037	0.0717407407407407	0.0717592592592593	0.0717962962962963	0.0718333333333333	0.0718518518518518	0.0718888888888889	0.0719259259259259	0.0719444444444444	0.0719814814814815	0.0720185185185185	0.072037037037037	0.0720925925925926	0.0721111111111111	0.0721296296296296	0.0721851851851852	0.0722037037037037	0.0722222222222222	0.0722777777777778	0.0722962962962963	0.0723148148148148	0.0723703703703704	0.0723888888888889	0.0724074074074074	0.072462962962963	0.0724814814814815	0.0725	0.0725555555555555	0.0725740740740741	0.0725925925925926	0.0726481481481481	0.0726666666666667	0.0726851851851852	0.0727407407407407	0.0727592592592593	0.0727777777777778	0.0728333333333333	0.0728518518518518	0.0728703703703704	0.0729259259259259	0.0729444444444444	0.073	0.0730185185185185	0.073037037037037	0.0730555555555555	0.0731111111111111	0.0731296296296296	0.0731851851851852	0.0732037037037037	0.0732222222222222	0.0732777777777778	0.0732962962962963	0.0733148148148148	0.0733703703703704	0.0733888888888889	0.0734074074074074	0.073462962962963	0.0734814814814815	0.0735	0.0735555555555555	0.0735740740740741	0.0735925925925926	0.0736481481481481	0.0736666666666667	0.0736851851851852	0.0737407407407407	0.0737592592592593	0.0737777777777778	0.0738333333333333	0.0738518518518518	0.0738703703703704	0.0739259259259259	0.0739444444444444	0.073962962962963	0.0740185185185185	0.074037037037037	0.0740740740740741	0.0740925925925926	0.0741296296296296	0.0741481481481481	0.0741851851851852	0.0742222222222222	0.0742592592592593	0.0742777777777778	0.0743148148148148	0.0743518518518518	0.0743703703703704	0.0744074074074074	0.0744444444444444	0.074462962962963	0.0745	0.074537037037037	0.0745555555555555	0.0745925925925926	0.0746296296296296	0.0746481481481481	0.0746851851851852	0.0747222222222222	0.0747407407407407	0.0747777777777778	0.0748148148148148	0.0748333333333333	0.0748703703703704	0.0749074074074074	0.0749259259259259	0.074962962962963	0.075	0.0750185185185185	0.0750740740740741	0.0750925925925926	0.0751111111111111	0.0751666666666667	0.0751851851851852	0.0752037037037037	0.0752592592592593	0.0752777777777778	0.0752962962962963	0.0753518518518518	0.0753703703703704	0.0753888888888889	0.0754444444444444	0.075462962962963	0.0754814814814815	0.075537037037037	0.0755555555555555	0.0755740740740741	0.0756296296296296	0.0756481481481481	0.0757037037037037	0.0757222222222222	0.0757407407407407	0.0757962962962963	0.0758148148148148	0.0758333333333333	0.0758888888888889	0.0759074074074074	0.0759259259259259	0.0759814814814815	0.076	0.0760185185185185	0.0760740740740741	0.0760925925925926	0.0761111111111111	0.0761666666666667	0.0761851851851852	0.0762037037037037	0.0762592592592593	0.0762777777777778	0.0763148148148148	0.0763518518518518	0.0763703703703704	0.0763888888888889	0.0764444444444444	0.0764629629629629	0.0765	0.076537037037037	0.0765555555555555	0.0765925925925926	0.0766296296296296	0.0766481481481481	0.0766851851851852	0.0767222222222222	0.0767407407407407	0.0767777777777778	0.0768148148148148	0.0768333333333333	0.0768703703703704	0.0769074074074074	0.0769444444444444	0.0769629629629629	0.077	0.077037037037037	0.0770555555555555	0.0770925925925926	0.0771296296296296	0.0771481481481482	0.0771851851851852	0.0772222222222222	0.0772407407407407	0.0772777777777778	0.0773148148148148	0.0773333333333333	0.0773703703703704	0.0774074074074074	0.0774259259259259	0.0774814814814815	0.0775	0.0775185185185185	0.0775740740740741	0.0775925925925926	0.0776111111111111	0.0776666666666667	0.0776851851851852	0.0777037037037037	0.0777592592592592	0.0777777777777778	0.0777962962962963	0.0778518518518518	0.0778703703703704	0.0778888888888889	0.0779444444444444	0.0779629629629629	0.0779814814814815	0.078037037037037	0.0780555555555555	0.0781111111111111	0.0781296296296296	0.0781481481481481	0.0782037037037037	0.0782222222222222	0.0782407407407407	0.0782962962962963	0.0783148148148148	0.0783333333333333	0.0783888888888889	0.0784074074074074	0.0784259259259259	0.0784814814814815	0.0785	0.0785185185185185	0.0785740740740741	0.0785925925925926	0.0786296296296296	0.0786666666666667	0.0786851851851852	0.0787222222222222	0.0787592592592593	0.0787777777777778	0.0788148148148148	0.0788518518518518	0.0788703703703704	0.0789074074074074	0.0789444444444444	0.078962962962963	0.079	0.079037037037037	0.0790555555555555	0.0790925925925926	0.0791296296296296	0.0791481481481481	0.0791851851851852	0.0792222222222222	0.0792592592592593	0.0792777777777778	0.0793148148148148	0.0793333333333333	0.0793703703703704	0.0794074074074074	0.0794444444444444	0.079462962962963	0.0795	0.079537037037037	0.0795555555555556	0.0795925925925926	0.0796296296296296	0.0796481481481481	0.0796851851851852	0.0797222222222222	0.0797407407407407	0.0797777777777778	0.0798148148148148	0.0798333333333333	0.0798888888888889	0.0799074074074074	0.0799259259259259	0.0799629629629629	0.08	0.0800185185185185	0.0800740740740741	0.0800925925925926	0.0801111111111111	0.0801666666666666	0.0801851851851852	0.0802037037037037	0.0802592592592592	0.0802777777777778	0.0802962962962963	0.0803518518518518	0.0803703703703704	0.0804259259259259	0.0804444444444444	0.0804629629629629	0.0805185185185185	0.080537037037037	0.0805555555555555	0.0806111111111111	0.0806296296296296	0.0806481481481481	0.0807037037037037	0.0807222222222222	0.0807407407407407	0.0807962962962963	0.0808148148148148	0.0808333333333333	0.0808888888888889	0.0809074074074074	0.0809259259259259	0.0809814814814815	0.081	0.0810185185185185	0.0810740740740741	0.0810925925925926	0.0811111111111111	0.0811666666666666	0.0811851851851852	0.0812037037037037	0.0812592592592592	0.0812777777777778	0.0812962962962963	0.0813518518518518	0.0813703703703704	0.0813888888888889	0.0814444444444444	0.0814629629629629	0.0814814814814815	0.081537037037037	0.0815555555555555	0.0815740740740741	0.0816296296296296	0.0816481481481481	0.0816851851851852	0.0817222222222222	0.0817407407407407	0.0817592592592592	0.0818148148148148	0.0818333333333333	0.0818703703703704	0.0819074074074074	0.0819259259259259	0.0819629629629629	0.082	0.0820185185185185	0.0820555555555555	0.0820925925925926	0.0821111111111111	0.0821481481481481	0.0821851851851852	0.0822037037037037	0.0822407407407407	0.0822777777777778	0.0822962962962963	0.0823333333333333	0.0823703703703704	0.0823888888888889	0.0824259259259259	0.082462962962963	0.0824814814814815	0.0825185185185185	0.0825555555555555	0.082574074074074	0.0826111111111111	0.0826481481481481	0.0826851851851852	0.0827037037037037	0.0827407407407407	0.0827777777777778	0.0827962962962963	0.0828333333333333	0.0828703703703703	0.0828888888888889	0.0829259259259259	0.082962962962963	0.0829814814814815	0.0830185185185185	0.0830555555555555	0.083074074074074	0.0831111111111111	0.0831481481481481	0.0831666666666666	0.0832037037037037	0.0832407407407407	0.0832592592592593	0.0832962962962963	0.0833333333333333	0.0833518518518518	0.0833888888888889	0.0834259259259259	0.0834444444444444	0.0834814814814815	0.0835185185185185	0.083537037037037	0.0835740740740741	0.0836111111111111	0.0836296296296296	0.0836666666666667	0.0837037037037037	0.0837222222222222	0.0837592592592592	0.0837962962962963	0.0838148148148148	0.0838518518518518	0.0838888888888889	0.0839074074074074	0.0839444444444444	0.0839814814814815	0.084	0.0840555555555555	0.0840740740740741	0.0840925925925926	0.0841296296296296	0.0841666666666667	0.0841851851851852	0.0842407407407407	0.0842592592592592	0.0842777777777778	0.0843333333333333	0.0843518518518518	0.0843703703703704	0.0844259259259259	0.0844444444444444	0.0844629629629629	0.0845185185185185	0.084537037037037	0.0845555555555555	0.0846111111111111	0.0846296296296296	0.0846481481481481	0.0847037037037037	0.0847222222222222	0.0847407407407407	0.0847962962962963	0.0848148148148148	0.0848703703703704	0.0848888888888889	0.0849074074074074	0.0849629629629629	0.0849814814814815	0.085	0.0850555555555555	0.0850740740740741	0.0850925925925926	0.0851481481481481	0.0851666666666667	0.0851851851851852	0.0852407407407407	0.0852592592592592	0.0852777777777778	0.0853333333333333	0.0853518518518518	0.0853703703703704	0.0854259259259259	0.0854444444444444	0.0854629629629629	0.0855185185185185	0.085537037037037	0.0855555555555555	0.0856111111111111	0.0856296296296296	0.0856666666666667	0.0857037037037037	0.0857222222222222	0.0857592592592592	0.0857962962962963	0.0858148148148148	0.0858518518518518	0.0858888888888889	0.0859074074074074	0.0859444444444444	0.0859814814814815	0.086	0.086037037037037	0.086074074074074	0.0860925925925926	0.0861296296296296	0.0861666666666666	0.0862037037037037	0.0862222222222222	0.0862592592592593	0.0862962962962963	0.0863148148148148	0.0863518518518518	0.0863888888888889	0.0864074074074074	0.0864444444444444	0.0864814814814815	0.0865	0.086537037037037	0.086574074074074	0.0865925925925926	0.0866296296296296	0.0866666666666666	0.0866851851851852	0.0867222222222222	0.0867592592592592	0.0867777777777778	0.0868333333333333	0.0868518518518518	0.0868703703703703	0.0869259259259259	0.0869444444444444	0.0869629629629629	0.0870185185185185	0.087037037037037	0.0870555555555555	0.0871111111111111	0.0871296296296296	0.0871481481481481	0.0872037037037037	0.0872222222222222	0.0872407407407407	0.0872962962962963	0.0873148148148148	0.0873703703703704	0.0873888888888889	0.0874074074074074	0.0874629629629629	0.0874814814814815	0.0875	0.0875555555555555	0.0875740740740741	0.0875925925925926	0.0876481481481481	0.0876666666666667	0.0876851851851852	0.0877407407407407	0.0877592592592592	0.0877962962962963	0.0878333333333333	0.0878518518518518	0.0878703703703704	0.0879259259259259	0.0879444444444444	0.0879814814814815	0.0880185185185185	0.088037037037037	0.0880740740740741	0.0881111111111111	0.0881296296296296	0.0881666666666667	0.0882037037037037	0.0882222222222222	0.0882592592592592	0.0882962962962963	0.0883148148148148	0.0883518518518518	0.0883888888888889	0.0884074074074074	0.0884444444444444	0.0884814814814815	0.0885185185185185	0.088537037037037	0.0885740740740741	0.0886111111111111	0.0886296296296296	0.0886666666666667	0.0887037037037037	0.0887222222222222	0.0887592592592592	0.0887962962962963	0.0888148148148148	0.0888518518518518	0.0888888888888889	0.0889074074074074	0.0889444444444444	0.0889814814814815	0.089	0.089037037037037	0.0890740740740741	0.0890925925925926	0.0891481481481481	0.0891666666666667	0.0891851851851852	0.0892407407407407	0.0892592592592592	0.0892777777777778	0.0893333333333333	0.0893518518518518	0.0893703703703703	0.0894259259259259	0.0894444444444444	0.0894629629629629	0.0895185185185185	0.089537037037037	0.0895925925925926	0.0896111111111111	0.0896296296296296	0.0896851851851852	0.0897037037037037	0.0897222222222222	0.0897777777777778	0.0897962962962963	0.0898148148148148	0.0898703703703703	0.0898888888888889	0.0899259259259259	0.0899629629629629	0.0899814814814815	0.0900185185185185	0.0900555555555555	0.090074074074074	0.0901111111111111	0.0901481481481481	0.0901666666666666	0.0902037037037037	0.0902407407407407	0.0902777777777778	0.0902962962962963	0.0903333333333333	0.0903703703703703	0.0903888888888889	0.0904259259259259	0.0904629629629629	0.0904814814814815	0.0905185185185185	0.0905555555555555	0.090574074074074	0.0906111111111111	0.0906481481481481	0.0906666666666666	0.0907037037037037	0.0907407407407407	0.0907592592592592	0.0907962962962963	0.0908333333333333	0.0908518518518518	0.0909074074074074	0.0909259259259259	0.0909444444444444	0.0909814814814815	0.0910185185185185	0.091037037037037	0.091074074074074	0.0911111111111111	0.0911296296296296	0.0911851851851852	0.0912037037037037	0.0912222222222222	0.0912777777777778	0.0912962962962963	0.0913148148148148	0.0913703703703704	0.0913888888888889	0.0914074074074074	0.0914629629629629	0.0914814814814815	0.091537037037037	0.0915555555555555	0.0915740740740741	0.0915925925925926	0.0916481481481481	0.0916666666666666	0.0917222222222222	0.0917407407407407	0.0917592592592592	0.0918148148148148	0.0918333333333333	0.0918518518518518	0.0919074074074074	0.0919259259259259	0.0919444444444444	0.092	0.0920185185185185	0.0920555555555555	0.0920925925925926	0.0921111111111111	0.0921481481481481	0.0921851851851852	0.0922037037037037	0.0922407407407407	0.0922777777777778	0.0922962962962963	0.0923333333333333	0.0923703703703704	0.0923888888888889	0.0924259259259259	0.0924629629629629	0.0925	0.0925185185185185	0.0925555555555555	0.0925925925925926	0.0926111111111111	0.0926296296296296	0.0926851851851852	0.0927037037037037	0.0927222222222222	0.0927777777777778	0.0927962962962963	0.0928148148148148	0.0928703703703703	0.0928888888888889	0.0929074074074074	0.0929629629629629	0.0929814814814815	0.093	0.0930555555555555	0.093074074074074	0.0930925925925926	0.0931481481481481	0.0931666666666666	0.0931851851851852	0.0932407407407407	0.0932592592592592	0.0933148148148148	0.0933333333333333	0.0933518518518518	0.0934074074074074	0.0934259259259259	0.0934444444444444	0.0935	0.0935185185185185	0.093537037037037	0.0935925925925926	0.0936111111111111	0.0936296296296296	0.0936851851851852	0.0937037037037037	0.0937222222222222	0.0937777777777778	0.0937962962962963	0.0938148148148148	0.0938703703703703	0.0938888888888889	0.0939074074074074	0.0939629629629629	0.0939814814814815	0.094	0.0940555555555555	0.094074074074074	0.0941111111111111	0.0941481481481481	0.0941666666666666	0.0941851851851852	0.0942407407407407	0.0942592592592592	0.0942777777777778	0.0943333333333333	0.0943518518518518	0.0943888888888889	0.0944259259259259	0.0944444444444444	0.0944814814814815	0.0945185185185185	0.094537037037037	0.094574074074074	0.0946111111111111	0.0946296296296296	0.0946666666666666	0.0947037037037037	0.0947222222222222	0.0947592592592592	0.0947962962962963	0.0948148148148148	0.0948518518518518	0.0948888888888889	0.0949074074074074	0.0949444444444444	0.0949814814814814	0.095	0.095037037037037	0.095074074074074	0.0950925925925926	0.0951296296296296	0.0951666666666667	0.0951851851851852	0.0952222222222222	0.0952592592592592	0.0952777777777777	0.0953148148148148	0.0953518518518518	0.0953703703703704	0.0954074074074074	0.0954444444444444	0.0954629629629629	0.0955	0.095537037037037	0.095574074074074	0.0955925925925926	0.0956296296296296	0.0956481481481481	0.0956851851851852	0.0957222222222222	0.0957407407407407	0.0957777777777777	0.0958148148148148	0.0958518518518518	0.0958703703703703	0.0959074074074074	0.0959259259259259	0.0959629629629629	0.096	0.096037037037037	0.0960555555555555	0.0960925925925926	0.0961296296296296	0.0961481481481481	0.0961851851851852	0.0962222222222222	0.0962407407407407	0.0962777777777778	0.0963148148148148	0.0963333333333333	0.0963703703703703	0.0964074074074074	0.0964259259259259	0.0964629629629629	0.0965	0.0965185185185185	0.0965555555555555	0.0965925925925926	0.0966111111111111	0.0966481481481481	0.0966851851851852	0.0967037037037037	0.0967407407407407	0.0967777777777778	0.0967962962962963	0.0968333333333333	0.0968703703703703	0.0968888888888889	0.0969259259259259	0.0969629629629629	0.0969814814814815	0.097037037037037	0.0970555555555555	0.0970740740740741	0.0971111111111111	0.0971481481481481	0.0971666666666666	0.0972037037037037	0.0972407407407407	0.0972592592592592	0.0973148148148148	0.0973333333333333	0.0973518518518518	0.0973888888888889	0.0974259259259259	0.0974444444444444	0.0975	0.0975185185185185	0.097537037037037	0.0975925925925926	0.0976111111111111	0.0976296296296296	0.0976851851851852	0.0977037037037037	0.0977222222222222	0.0977777777777778	0.0977962962962963	0.0978148148148148	0.0978703703703703	0.0978888888888889	0.0979074074074074	0.0979629629629629	0.0979814814814815	0.098	0.0980555555555555	0.0980740740740741	0.0980925925925926	0.0981481481481481	0.0981666666666666	0.0981851851851852	0.0982407407407407	0.0982592592592592	0.0982777777777778	0.0983333333333333	0.0983518518518518	0.0983703703703703	0.0984259259259259	0.0984444444444444	0.0984629629629629	0.0985185185185185	0.098537037037037	0.0985555555555555	0.0986111111111111	0.0986296296296296	0.0986481481481481	0.0987037037037037	0.0987222222222222	0.0987407407407407	0.0987962962962963	0.0988148148148148	0.0988333333333333	0.0988888888888889	0.0989074074074074	0.0989629629629629	0.0989814814814814	0.099	0.0990555555555555	0.099074074074074	0.0990925925925926	0.0991481481481481	0.0991666666666667	0.0991851851851852	0.0992407407407407	0.0992592592592592	0.0992777777777777	0.0993333333333333	0.0993518518518518	0.0993703703703703	0.0994259259259259	0.0994444444444444	0.0994629629629629	0.0995185185185185	0.099537037037037	0.0995555555555555	0.0996111111111111	0.0996296296296296	0.0996481481481481	0.0997037037037037	0.0997222222222222	0.0997592592592592	0.0997962962962963	0.0998148148148148	0.0998518518518518	0.0998888888888889	0.0999074074074074	0.0999444444444444	0.0999814814814814	0.1	0.100037037037037	0.100074074074074	0.100092592592593	0.10012962962963	0.100166666666667	0.100185185185185	0.100222222222222	0.100259259259259	0.100277777777778	0.100314814814815	0.100351851851852	0.10037037037037	0.100407407407407	0.100444444444444	0.100462962962963	0.1005	0.100537037037037	0.100574074074074	0.100592592592593	0.10062962962963	0.100666666666667	0.100685185185185	0.100722222222222	0.100759259259259	0.100777777777778	0.100814814814815	0.100851851851852	0.10087037037037	0.100907407407407	0.100944444444444	0.100962962962963	0.101	0.101037037037037	0.101055555555556	0.101092592592593	0.10112962962963	0.101148148148148	0.101185185185185	0.101222222222222	0.101240740740741	0.101277777777778	0.101314814814815	0.101333333333333	0.101388888888889	0.101407407407407	0.101425925925926	0.101481481481481	0.1015	0.101518518518519	0.101555555555556	0.101592592592593	0.101611111111111	0.101666666666667	0.101685185185185	0.101703703703704	0.101759259259259	0.101777777777778	0.101796296296296	0.101851851851852	0.10187037037037	0.101888888888889	0.101944444444444	0.101962962962963	0.101981481481481	0.102037037037037	0.102055555555556	0.102074074074074	0.10212962962963	0.102148148148148	0.102166666666667	0.102222222222222	0.102240740740741	0.102296296296296	0.102314814814815	0.102333333333333	0.102351851851852	0.102407407407407	0.102425925925926	0.102481481481481	0.1025	0.102518518518519	0.102574074074074	0.102592592592593	0.102611111111111	0.102666666666667	0.102685185185185	0.102703703703704	0.102759259259259	0.102777777777778	0.102796296296296	0.102851851851852	0.10287037037037	0.102888888888889	0.102944444444444	0.102962962962963	0.102981481481481	0.103037037037037	0.103055555555556	0.103092592592593	0.10312962962963	0.103148148148148	0.103185185185185	0.103222222222222	0.103240740740741	0.103277777777778	0.103314814814815	0.103333333333333	0.10337037037037	0.103407407407407	0.103425925925926	0.103462962962963	0.1035	0.103518518518519	0.103555555555556	0.103592592592593	0.103611111111111	0.103648148148148	0.103685185185185	0.103703703703704	0.103740740740741	0.103777777777778	0.103796296296296	0.103833333333333	0.10387037037037	0.103888888888889	0.103925925925926	0.103962962962963	0.103981481481481	0.104018518518519	0.104055555555556	0.104092592592593	0.104111111111111	0.104148148148148	0.104185185185185	0.104203703703704	0.104240740740741	0.104277777777778	0.104296296296296	0.104333333333333	0.10437037037037	0.104388888888889	0.104425925925926	0.104462962962963	0.104481481481481	0.104518518518519	0.104555555555556	0.104574074074074	0.10462962962963	0.104648148148148	0.104666666666667	0.104722222222222	0.104740740740741	0.104759259259259	0.104814814814815	0.104833333333333	0.104851851851852	0.104907407407407	0.104925925925926	0.104944444444444	0.105	0.105018518518519	0.105037037037037	0.105092592592593	0.105111111111111	0.10512962962963	0.105185185185185	0.105203703703704	0.105222222222222	0.105277777777778	0.105296296296296	0.105314814814815	0.10537037037037	0.105388888888889	0.105407407407407	0.105462962962963	0.105481481481481	0.1055	0.105555555555556	0.105574074074074	0.105592592592593	0.105648148148148	0.105666666666667	0.105685185185185	0.105740740740741	0.105759259259259	0.105814814814815	0.105833333333333	0.105851851851852	0.105907407407407	0.105925925925926	0.105944444444444	0.106	0.106018518518519	0.106037037037037	0.106092592592593	0.106111111111111	0.10612962962963	0.106185185185185	0.106203703703704	0.106222222222222	0.106277777777778	0.106296296296296	0.106314814814815	0.10637037037037	0.106388888888889	0.106407407407407	0.106462962962963	0.106481481481481	0.1065	0.106555555555556	0.106574074074074	0.106611111111111	0.106648148148148	0.106666666666667	0.106703703703704	0.106740740740741	0.106759259259259	0.106796296296296	0.106833333333333	0.106851851851852	0.106888888888889	0.106925925925926	0.106944444444444	0.106981481481481	0.107018518518519	0.107037037037037	0.107074074074074	0.107111111111111	0.10712962962963	0.107166666666667	0.107203703703704	0.107222222222222	0.107259259259259	0.107296296296296	0.107314814814815	0.107351851851852	0.107388888888889	0.107407407407407	0.107444444444444	0.107481481481481	0.1075	0.107537037037037	0.107574074074074	0.107592592592593	0.10762962962963	0.107666666666667	0.107685185185185	0.107722222222222	0.107759259259259	0.107777777777778	0.107814814814815	0.107851851851852	0.10787037037037	0.107907407407407	0.107944444444444	0.107962962962963	0.108	0.108037037037037	0.108055555555556	0.108092592592593	0.10812962962963	0.108148148148148	0.108185185185185	0.108222222222222	0.108240740740741	0.108277777777778	0.108314814814815	0.108333333333333	0.10837037037037	0.108407407407407	0.108425925925926	0.108462962962963	0.1085	0.108518518518519	0.108555555555556	0.108592592592593	0.108611111111111	0.108648148148148	0.108685185185185	0.108722222222222	0.108740740740741	0.108777777777778	0.108814814814815	0.108833333333333	0.10887037037037	0.108907407407407	0.108925925925926	0.108962962962963	0.109	0.109018518518519	0.109055555555556	0.109092592592593	0.109111111111111	0.109148148148148	0.109185185185185	0.109203703703704	0.109240740740741	0.109277777777778	0.109296296296296	0.109351851851852	0.10937037037037	0.109388888888889	0.109425925925926	0.109462962962963	0.109481481481481	0.109537037037037	0.109555555555556	0.109574074074074	0.109611111111111	0.109648148148148	0.109666666666667	0.109722222222222	0.109740740740741	0.109759259259259	0.109814814814815	0.109833333333333	0.109851851851852	0.109907407407407	0.109925925925926	0.109944444444444	0.11	0.110018518518519	0.110037037037037	0.110092592592593	0.110111111111111	0.11012962962963	0.110185185185185	0.110203703703704	0.110222222222222	0.110277777777778	0.110296296296296	0.110314814814815	0.11037037037037	0.110388888888889	0.110407407407407	0.110462962962963	0.110481481481481	0.1105	0.110555555555556	0.110574074074074	0.110592592592593	0.110648148148148	0.110666666666667	0.110685185185185	0.110740740740741	0.110759259259259	0.110777777777778	0.110833333333333	0.110851851851852	0.11087037037037	0.110925925925926	0.110944444444444	0.110962962962963	0.111018518518519	0.111037037037037	0.111055555555556	0.111111111111111	0.11112962962963	0.111166666666667	0.111203703703704	0.111222222222222	0.111259259259259	0.111296296296296	0.111314814814815	0.111351851851852	0.111388888888889	0.111407407407407	0.111444444444444	0.111481481481481	0.1115	0.111537037037037	0.111574074074074	0.111592592592593	0.11162962962963	0.111666666666667	0.111685185185185	0.111722222222222	0.111759259259259	0.111796296296296	0.111814814814815	0.111851851851852	0.11187037037037	0.111907407407407	0.111944444444444	0.111981481481481	0.112	0.112037037037037	0.112074074074074	0.112092592592593	0.11212962962963	0.112166666666667	0.112185185185185	0.112222222222222	0.112259259259259	0.112277777777778	0.112314814814815	0.112351851851852	0.11237037037037	0.112407407407407	0.112444444444444	0.112462962962963	0.1125	0.112537037037037	0.112555555555556	0.112592592592593	0.11262962962963	0.112648148148148	0.112685185185185	0.112722222222222	0.112740740740741	0.112796296296296	0.112814814814815	0.112833333333333	0.112888888888889	0.112907407407407	0.112925925925926	0.112981481481481	0.113	0.113018518518519	0.113074074074074	0.113092592592593	0.113111111111111	0.113166666666667	0.113185185185185	0.113203703703704	0.113259259259259	0.113277777777778	0.113333333333333	0.113351851851852	0.11337037037037	0.113425925925926	0.113444444444444	0.113462962962963	0.113518518518519	0.113537037037037	0.113555555555556	0.113611111111111	0.11362962962963	0.113648148148148	0.113703703703704	0.113722222222222	0.113740740740741	0.113796296296296	0.113814814814815	0.113833333333333	0.113888888888889	0.113907407407407	0.113944444444444	0.113981481481481	0.114	0.114037037037037	0.114074074074074	0.114092592592593	0.11412962962963	0.114166666666667	0.114185185185185	0.114222222222222	0.114259259259259	0.114277777777778	0.114314814814815	0.114351851851852	0.114388888888889	0.114407407407407	0.114444444444444	0.114481481481481	0.1145	0.114537037037037	0.114574074074074	0.114592592592593	0.11462962962963	0.114666666666667	0.114685185185185	0.114722222222222	0.114759259259259	0.114777777777778	0.114833333333333	0.114851851851852	0.11487037037037	0.114925925925926	0.114944444444444	0.114962962962963	0.115018518518519	0.115037037037037	0.115055555555556	0.115111111111111	0.11512962962963	0.115185185185185	0.115203703703704	0.115222222222222	0.115240740740741	0.115296296296296	0.115314814814815	0.11537037037037	0.115388888888889	0.115407407407407	0.115462962962963	0.115481481481481	0.1155	0.115555555555556	0.115574074074074	0.115592592592593	0.115648148148148	0.115666666666667	0.115685185185185	0.115740740740741	0.115759259259259	0.115796296296296	0.115833333333333	0.115851851851852	0.11587037037037	0.115925925925926	0.115944444444444	0.115981481481481	0.116018518518518	0.116037037037037	0.116074074074074	0.116111111111111	0.11612962962963	0.116166666666667	0.116203703703704	0.116222222222222	0.116259259259259	0.116296296296296	0.116333333333333	0.116351851851852	0.116388888888889	0.116425925925926	0.116444444444444	0.116481481481481	0.116518518518519	0.116537037037037	0.116574074074074	0.116611111111111	0.11662962962963	0.116666666666667	0.116703703703704	0.116722222222222	0.116759259259259	0.116796296296296	0.116814814814815	0.116851851851852	0.116888888888889	0.116907407407407	0.116962962962963	0.116981481481481	0.117	0.117055555555556	0.117074074074074	0.117092592592593	0.117148148148148	0.117166666666667	0.117185185185185	0.117240740740741	0.117259259259259	0.117314814814815	0.117333333333333	0.117351851851852	0.117407407407407	0.117425925925926	0.117444444444444	0.1175	0.117518518518519	0.117537037037037	0.117592592592593	0.117611111111111	0.11762962962963	0.117685185185185	0.117703703703704	0.117722222222222	0.117777777777778	0.117796296296296	0.117814814814815	0.11787037037037	0.117888888888889	0.117907407407407	0.117962962962963	0.117981481481481	0.118	0.118055555555556	0.118074074074074	0.118111111111111	0.118148148148148	0.118166666666667	0.118203703703704	0.118240740740741	0.118259259259259	0.118296296296296	0.118333333333333	0.118351851851852	0.118388888888889	0.118425925925926	0.118444444444444	0.118481481481481	0.118518518518519	0.118555555555556	0.118574074074074	0.118611111111111	0.118648148148148	0.118666666666667	0.118703703703704	0.118740740740741	0.118759259259259	0.118796296296296	0.118833333333333	0.118851851851852	0.118888888888889	0.118925925925926	0.118944444444444	0.118981481481481	0.119018518518518	0.119037037037037	0.119092592592593	0.119111111111111	0.11912962962963	0.119185185185185	0.119203703703704	0.119222222222222	0.119277777777778	0.119296296296296	0.119314814814815	0.11937037037037	0.119388888888889	0.119444444444444	0.119462962962963	0.119481481481481	0.119537037037037	0.119555555555556	0.119574074074074	0.11962962962963	0.119648148148148	0.119666666666667	0.119722222222222	0.119740740740741	0.119759259259259	0.119814814814815	0.119833333333333	0.119851851851852	0.119907407407407	0.119925925925926	0.119944444444444	0.12	0.120018518518519	0.120037037037037	0.120092592592593	0.120111111111111	0.12012962962963	0.120185185185185	0.120203703703704	0.120222222222222	0.120277777777778	0.120296296296296	0.120314814814815	0.12037037037037	0.120388888888889	0.120407407407407	0.120462962962963	0.120481481481481	0.120518518518519	0.120555555555556	0.120574074074074	0.120592592592593	0.120648148148148	0.120666666666667	0.120703703703704	0.120740740740741	0.120759259259259	0.120796296296296	0.120833333333333	0.120851851851852	0.120888888888889	0.120925925925926	0.120944444444444	0.120981481481481	0.121018518518519	0.121037037037037	0.121074074074074	0.121111111111111	0.12112962962963	0.121166666666667	0.121203703703704	0.121222222222222	0.121259259259259	0.121296296296296	0.121333333333333	0.121351851851852	0.121388888888889	0.121425925925926	0.121444444444444	0.121481481481481	0.121518518518519	0.121537037037037	0.121574074074074	0.121611111111111	0.12162962962963	0.121666666666667	0.121703703703704	0.121722222222222	0.121759259259259	0.121796296296296	0.121814814814815	0.121851851851852	0.121888888888889	0.121907407407407	0.121944444444444	0.121981481481481	0.122	0.122037037037037	0.122074074074074	0.122092592592593	0.122148148148148	0.122166666666667	0.122185185185185	0.122240740740741	0.122259259259259	0.122277777777778	0.122333333333333	0.122351851851852	0.12237037037037	0.122425925925926	0.122444444444444	0.122462962962963	0.122518518518519	0.122537037037037	0.122555555555556	0.122611111111111	0.12262962962963	0.122648148148148	0.122703703703704	0.122722222222222	0.122740740740741	0.122796296296296	0.122814814814815	0.122833333333333	0.122888888888889	0.122907407407407	0.122925925925926	0.122981481481481	0.123	0.123018518518519	0.123074074074074	0.123092592592593	0.123148148148148	0.123166666666667	0.123185185185185	0.123240740740741	0.123259259259259	0.123277777777778	0.123296296296296	0.123351851851852	0.12337037037037	0.123425925925926	0.123444444444444	0.123462962962963	0.123518518518519	0.123537037037037	0.123555555555556	0.123611111111111	0.12362962962963	0.123648148148148	0.123703703703704	0.123722222222222	0.123740740740741	0.123796296296296	0.123814814814815	0.123833333333333	0.123888888888889	0.123907407407407	0.123925925925926	0.123981481481481	0.124	0.124037037037037	0.124074074074074	0.124092592592593	0.12412962962963	0.124166666666667	0.124185185185185	0.124222222222222	0.124259259259259	0.124277777777778	0.124314814814815	0.124351851851852	0.12437037037037	0.124407407407407	0.124444444444444	0.124462962962963	0.1245	0.124537037037037	0.124555555555556	0.124592592592593	0.12462962962963	0.124666666666667	0.124685185185185	0.124722222222222	0.124759259259259	0.124777777777778	0.124814814814815	0.124851851851852	0.12487037037037	0.124907407407407	0.124944444444444	0.124962962962963	0.125	0.125037037037037	0.125055555555556	0.125092592592593	0.12512962962963	0.125148148148148	0.125185185185185	0.125222222222222	0.125240740740741	0.125277777777778	0.125314814814815	0.125333333333333	0.12537037037037	0.125407407407407	0.125425925925926	0.125462962962963	0.1255	0.125518518518518	0.125574074074074	0.125592592592593	0.125611111111111	0.125666666666667	0.125685185185185	0.125703703703704	0.125759259259259	0.125777777777778	0.125796296296296	0.125851851851852	0.12587037037037	0.125888888888889	0.125944444444444	0.125962962962963	0.126018518518518	0.126037037037037	0.126055555555556	0.126111111111111	0.12612962962963	0.126148148148148	0.126203703703704	0.126222222222222	0.126240740740741	0.126296296296296	0.126314814814815	0.126333333333333	0.126388888888889	0.126407407407407	0.126425925925926	0.126481481481481	0.1265	0.126518518518518	0.126574074074074	0.126592592592593	0.12662962962963	0.126666666666667	0.126685185185185	0.126703703703704	0.126759259259259	0.126777777777778	0.126814814814815	0.126851851851852	0.12687037037037	0.126907407407407	0.126944444444444	0.126962962962963	0.127	0.127037037037037	0.127055555555556	0.127092592592593	0.12712962962963	0.127148148148148	0.127185185185185	0.127222222222222	0.127240740740741	0.127277777777778	0.127314814814815	0.127333333333333	0.12737037037037	0.127407407407407	0.127444444444444	0.127462962962963	0.1275	0.127537037037037	0.127555555555556	0.127592592592593	0.12762962962963	0.127648148148148	0.127685185185185	0.127722222222222	0.127740740740741	0.127777777777778	0.127814814814815	0.127833333333333	0.12787037037037	0.127907407407407	0.127925925925926	0.127962962962963	0.128	0.128018518518519	0.128055555555556	0.128092592592593	0.128111111111111	0.128166666666667	0.128185185185185	0.128203703703704	0.128259259259259	0.128277777777778	0.128296296296296	0.128351851851852	0.12837037037037	0.128388888888889	0.128444444444444	0.128462962962963	0.128481481481481	0.128537037037037	0.128555555555556	0.128611111111111	0.12862962962963	0.128648148148148	0.128703703703704	0.128722222222222	0.128740740740741	0.128796296296296	0.128814814814815	0.128833333333333	0.128888888888889	0.128907407407407	0.128925925925926	0.128981481481481	0.129	0.129018518518518	0.129074074074074	0.129092592592593	0.129111111111111	0.129166666666667	0.129185185185185	0.129222222222222	0.129259259259259	0.129277777777778	0.129314814814815	0.129351851851852	0.12937037037037	0.129407407407407	0.129444444444444	0.129462962962963	0.1295	0.129537037037037	0.129555555555556	0.129592592592593	0.12962962962963	0.129648148148148	0.129685185185185	0.129703703703704	0.129759259259259	0.129777777777778	0.129796296296296	0.129833333333333	0.12987037037037	0.129888888888889	0.129944444444444	0.129962962962963	0.129981481481481	0.130037037037037	0.130055555555556	0.130074074074074	0.13012962962963	0.130148148148148	0.130166666666667	0.130222222222222	0.130240740740741	0.130259259259259	0.130314814814815	0.130333333333333	0.130351851851852	0.130407407407407	0.130425925925926	0.130444444444444	0.1305	0.130518518518518	0.130574074074074	0.130592592592593	0.130611111111111	0.130666666666667	0.130685185185185	0.130703703703704	0.130759259259259	0.130777777777778	0.130796296296296	0.130851851851852	0.13087037037037	0.130888888888889	0.130944444444444	0.130962962962963	0.131	0.131037037037037	0.131055555555556	0.131092592592593	0.13112962962963	0.131148148148148	0.131185185185185	0.131222222222222	0.131240740740741	0.131277777777778	0.131314814814815	0.131333333333333	0.13137037037037	0.131407407407407	0.131425925925926	0.131462962962963	0.1315	0.131518518518519	0.131555555555556	0.131592592592593	0.13162962962963	0.131648148148148	0.131685185185185	0.131722222222222	0.131740740740741	0.131777777777778	0.131814814814815	0.131833333333333	0.13187037037037	0.131907407407407	0.131925925925926	0.131962962962963	0.132	0.132018518518518	0.132055555555556	0.132092592592593	0.132111111111111	0.132148148148148	0.132185185185185	0.132203703703704	0.132240740740741	0.132277777777778	0.132296296296296	0.132333333333333	0.13237037037037	0.132388888888889	0.132425925925926	0.132462962962963	0.132481481481481	0.132518518518518	0.132555555555556	0.132574074074074	0.132611111111111	0.132648148148148	0.132666666666667	0.132703703703704	0.132740740740741	0.132759259259259	0.132796296296296	0.132833333333333	0.132851851851852	0.132888888888889	0.132925925925926	0.132944444444444	0.133	0.133018518518518	0.133037037037037	0.133092592592593	0.133111111111111	0.13312962962963	0.133185185185185	0.133203703703704	0.133222222222222	0.133277777777778	0.133296296296296	0.133314814814815	0.13337037037037	0.133388888888889	0.133407407407407	0.133462962962963	0.133481481481481	0.1335	0.133555555555556	0.133574074074074	0.133592592592593	0.133648148148148	0.133666666666667	0.133685185185185	0.133740740740741	0.133759259259259	0.133777777777778	0.133833333333333	0.133851851851852	0.133907407407407	0.133925925925926	0.133944444444444	0.134	0.134018518518518	0.134037037037037	0.134092592592593	0.134111111111111	0.13412962962963	0.134185185185185	0.134203703703704	0.134222222222222	0.134277777777778	0.134296296296296	0.134314814814815	0.13437037037037	0.134388888888889	0.134407407407407	0.134462962962963	0.134481481481481	0.1345	0.134555555555556	0.134574074074074	0.134592592592593	0.134648148148148	0.134666666666667	0.134703703703704	0.134740740740741	0.134759259259259	0.134796296296296	0.134833333333333	0.134851851851852	0.134888888888889	0.134925925925926	0.134944444444444	0.134981481481481	0.135018518518519	0.135037037037037	0.135074074074074	0.135111111111111	0.13512962962963	0.135166666666667	0.135203703703704	0.135222222222222	0.135259259259259	0.135296296296296	0.135314814814815	0.135351851851852	0.135388888888889	0.135407407407407	0.135444444444444	0.135481481481481	0.1355	0.135537037037037	0.135574074074074	0.135592592592593	0.13562962962963	0.135666666666667	0.135685185185185	0.135722222222222	0.135759259259259	0.135796296296296	0.135814814814815	0.135851851851852	0.135888888888889	0.135907407407407	0.135944444444444	0.135981481481481	0.136	0.136037037037037	0.136074074074074	0.136092592592593	0.13612962962963	0.136166666666667	0.136185185185185	0.136222222222222	0.136259259259259	0.136277777777778	0.136314814814815	0.136351851851852	0.13637037037037	0.136407407407407	0.136444444444444	0.136462962962963	0.136518518518518	0.136537037037037	0.136555555555556	0.136611111111111	0.13662962962963	0.136648148148148	0.136703703703704	0.136722222222222	0.136740740740741	0.136796296296296	0.136814814814815	0.136833333333333	0.136888888888889	0.136907407407407	0.136925925925926	0.136981481481481	0.137	0.137018518518518	0.137074074074074	0.137092592592593	0.137111111111111	0.137166666666667	0.137185185185185	0.137203703703704	0.137259259259259	0.137277777777778	0.137296296296296	0.137351851851852	0.13737037037037	0.137388888888889	0.137444444444444	0.137462962962963	0.137481481481481	0.137537037037037	0.137555555555556	0.137611111111111	0.13762962962963	0.137648148148148	0.137666666666667	0.137722222222222	0.137740740740741	0.137796296296296	0.137814814814815	0.137833333333333	0.137888888888889	0.137907407407407	0.137925925925926	0.137981481481481	0.138	0.138018518518518	0.138074074074074	0.138092592592593	0.138111111111111	0.138166666666667	0.138185185185185	0.138203703703704	0.138259259259259	0.138277777777778	0.138296296296296	0.138351851851852	0.13837037037037	0.138407407407407	0.138444444444444	0.138462962962963	0.1385	0.138537037037037	0.138555555555556	0.138592592592593	0.13862962962963	0.138648148148148	0.138685185185185	0.138722222222222	0.138740740740741	0.138777777777778	0.138814814814815	0.138833333333333	0.13887037037037	0.138907407407407	0.138925925925926	0.138962962962963	0.139	0.139018518518518	0.139055555555556	0.139092592592593	0.139111111111111	0.139148148148148	0.139185185185185	0.139222222222222	0.139240740740741	0.139277777777778	0.139296296296296	0.139333333333333	0.13937037037037	0.139407407407407	0.139425925925926	0.139462962962963	0.1395	0.139518518518518	0.139555555555556	0.139592592592593	0.139611111111111	0.139648148148148	0.139685185185185	0.139703703703704	0.139740740740741	0.139777777777778	0.139796296296296	0.139833333333333	0.13987037037037	0.139888888888889	0.139925925925926	0.139962962962963	0.139981481481481	0.140018518518519	0.140055555555556	0.140074074074074	0.140111111111111	0.140148148148148	0.140166666666667	0.140222222222222	0.140240740740741	0.140259259259259	0.140314814814815	0.140333333333333	0.140351851851852	0.140407407407407	0.140425925925926	0.140444444444444	0.1405	0.140518518518519	0.140537037037037	0.140592592592593	0.140611111111111	0.14062962962963	0.140685185185185	0.140703703703704	0.140759259259259	0.140777777777778	0.140796296296296	0.140851851851852	0.14087037037037	0.140888888888889	0.140944444444444	0.140962962962963	0.140981481481481	0.141037037037037	0.141055555555556	0.141074074074074	0.14112962962963	0.141148148148148	0.141185185185185	0.141222222222222	0.141240740740741	0.141277777777778	0.141314814814815	0.141333333333333	0.14137037037037	0.141407407407407	0.141425925925926	0.141462962962963	0.1415	0.141518518518519	0.141555555555556	0.141592592592593	0.141611111111111	0.141648148148148	0.141685185185185	0.141703703703704	0.141740740740741	0.141777777777778	0.141796296296296	0.141833333333333	0.14187037037037	0.141888888888889	0.141925925925926	0.141962962962963	0.141981481481481	0.142018518518519	0.142055555555556	0.142092592592593	0.142111111111111	0.142148148148148	0.142166666666667	0.142203703703704	0.142240740740741	0.142277777777778	0.142296296296296	0.142333333333333	0.14237037037037	0.142388888888889	0.142425925925926	0.142462962962963	0.142481481481481	0.142518518518519	0.142555555555556	0.142574074074074	0.14262962962963	0.142648148148148	0.142666666666667	0.142703703703704	0.142740740740741	0.142759259259259	0.142814814814815	0.142833333333333	0.142851851851852	0.142907407407407	0.142925925925926	0.142944444444444	0.143	0.143018518518519	0.143037037037037	0.143092592592593	0.143111111111111	0.14312962962963	0.143185185185185	0.143203703703704	0.143259259259259	0.143277777777778	0.143296296296296	0.143351851851852	0.14337037037037	0.143388888888889	0.143444444444444	0.143462962962963	0.143481481481481	0.143537037037037	0.143555555555556	0.143592592592593	0.14362962962963	0.143648148148148	0.143685185185185	0.143722222222222	0.143740740740741	0.143777777777778	0.143814814814815	0.143833333333333	0.14387037037037	0.143907407407407	0.143925925925926	0.143962962962963	0.144	0.144018518518519	0.144055555555556	0.144092592592593	0.14412962962963	0.144148148148148	0.144185185185185	0.144222222222222	0.144240740740741	0.144277777777778	0.144314814814815	0.144333333333333	0.14437037037037	0.144407407407407	0.144425925925926	0.144462962962963	0.1445	0.144518518518519	0.144574074074074	0.144592592592593	0.144611111111111	0.144648148148148	0.144685185185185	0.144703703703704	0.144759259259259	0.144777777777778	0.144796296296296	0.144851851851852	0.14487037037037	0.144888888888889	0.144944444444444	0.144962962962963	0.144981481481481	0.145037037037037	0.145055555555556	0.145074074074074	0.14512962962963	0.145148148148148	0.145203703703704	0.145222222222222	0.145240740740741	0.145259259259259	0.145314814814815	0.145333333333333	0.145388888888889	0.145407407407407	0.145425925925926	0.145481481481481	0.1455	0.145518518518519	0.145574074074074	0.145592592592593	0.145611111111111	0.145666666666667	0.145685185185185	0.145722222222222	0.145759259259259	0.145777777777778	0.145814814814815	0.145851851851852	0.14587037037037	0.145907407407407	0.145944444444444	0.145962962962963	0.146	0.146037037037037	0.146055555555556	0.146092592592593	0.14612962962963	0.146148148148148	0.146185185185185	0.146222222222222	0.146240740740741	0.146277777777778	0.146314814814815	0.146333333333333	0.14637037037037	0.146407407407407	0.146425925925926	0.146462962962963	0.1465	0.146537037037037	0.146555555555556	0.146592592592593	0.14662962962963	0.146648148148148	0.146685185185185	0.146722222222222	0.146740740740741	0.146777777777778	0.146814814814815	0.146833333333333	0.14687037037037	0.146907407407407	0.146925925925926	0.146962962962963	0.147	0.147018518518519	0.147055555555556	0.147092592592593	0.147111111111111	0.147166666666667	0.147185185185185	0.147203703703704	0.147240740740741	0.147277777777778	0.147296296296296	0.147351851851852	0.14737037037037	0.147388888888889	0.147444444444444	0.147462962962963	0.147481481481481	0.147537037037037	0.147555555555556	0.147574074074074	0.14762962962963	0.147648148148148	0.147666666666667	0.147722222222222	0.147740740740741	0.147796296296296	0.147814814814815	0.147833333333333	0.147888888888889	0.147907407407407	0.147925925925926	0.147981481481481	0.148	0.148018518518519	0.148074074074074	0.148092592592593	0.148111111111111	0.148148148148148	0.148185185185185	0.148203703703704	0.148240740740741	0.148277777777778	0.148314814814815	0.148333333333333	0.14837037037037	0.148407407407407	0.148425925925926	0.148462962962963	0.1485	0.148518518518519	0.148555555555556	0.148592592592593	0.148611111111111	0.148648148148148	0.148685185185185	0.148703703703704	0.148759259259259	0.148777777777778	0.148796296296296	0.148851851851852	0.14887037037037	0.148888888888889	0.148944444444444	0.148962962962963	0.148981481481481	0.149037037037037	0.149055555555556	0.149111111111111	0.14912962962963	0.149148148148148	0.149166666666667	0.149222222222222	0.149240740740741	0.149296296296296	0.149314814814815	0.149333333333333	0.149388888888889	0.149407407407407	0.149425925925926	0.149481481481481	0.1495	0.149518518518519	0.149574074074074	0.149592592592593	0.149611111111111	0.149666666666667	0.149685185185185	0.149703703703704	0.149759259259259	0.149777777777778	0.149796296296296	0.149851851851852	0.14987037037037	0.149907407407407	0.149944444444444	0.149962962962963	0.15	0.150037037037037	0.150055555555556	0.150092592592593	0.15012962962963	0.150148148148148	0.150185185185185	0.150222222222222	0.150259259259259	0.150277777777778	0.150314814814815	0.150351851851852	0.15037037037037	0.150407407407407	0.150444444444444	0.150462962962963	0.1505	0.150537037037037	0.150555555555556	0.150592592592593	0.15062962962963	0.150648148148148	0.150703703703704	0.150722222222222	0.150740740740741	0.150796296296296	0.150814814814815	0.150833333333333	0.150888888888889	0.150907407407407	0.150925925925926	0.150981481481481	0.151	0.151055555555556	0.151074074074074	0.151092592592593	0.151148148148148	0.151166666666667	0.151185185185185	0.151240740740741	0.151259259259259	0.151277777777778	0.151333333333333	0.151351851851852	0.15137037037037	0.151425925925926	0.151444444444444	0.151462962962963	0.151518518518519	0.151537037037037	0.151574074074074	0.151611111111111	0.15162962962963	0.151666666666667	0.151703703703704	0.151722222222222	0.151759259259259	0.151796296296296	0.151814814814815	0.151851851851852	0.151888888888889	0.151907407407407	0.151944444444444	0.151981481481481	0.152018518518519	0.152037037037037	0.152074074074074	0.152111111111111	0.15212962962963	0.152166666666667	0.152203703703704	0.152222222222222	0.152259259259259	0.152296296296296	0.152314814814815	0.152351851851852	0.152388888888889	0.152407407407407	0.152444444444444	0.152481481481481	0.1525	0.152537037037037	0.152574074074074	0.152592592592593	0.152648148148148	0.152666666666667	0.152685185185185	0.152740740740741	0.152759259259259	0.152777777777778	0.152833333333333	0.152851851851852	0.15287037037037	0.152925925925926	0.152944444444444	0.153	0.153018518518519	0.153037037037037	0.153092592592593	0.153111111111111	0.15312962962963	0.153185185185185	0.153203703703704	0.153222222222222	0.153277777777778	0.153296296296296	0.153314814814815	0.15337037037037	0.153388888888889	0.153425925925926	0.153462962962963	0.153481481481481	0.153518518518518	0.153555555555556	0.153574074074074	0.153611111111111	0.153648148148148	0.153666666666667	0.153703703703704	0.153740740740741	0.153777777777778	0.153796296296296	0.153833333333333	0.15387037037037	0.153888888888889	0.153925925925926	0.153962962962963	0.153981481481481	0.154018518518519	0.154055555555556	0.154074074074074	0.154111111111111	0.154148148148148	0.154166666666667	0.154203703703704	0.154240740740741	0.154259259259259	0.154296296296296	0.154333333333333	0.154351851851852	0.154407407407407	0.154425925925926	0.154444444444444	0.1545	0.154518518518518	0.154537037037037	0.154592592592593	0.154611111111111	0.15462962962963	0.154685185185185	0.154703703703704	0.154722222222222	0.154777777777778	0.154796296296296	0.154814814814815	0.15487037037037	0.154888888888889	0.154944444444444	0.154962962962963	0.154981481481481	0.155037037037037	0.155055555555556	0.155074074074074	0.15512962962963	0.155166666666667	0.155222222222222	0.155277777777778	0.155333333333333	0.155407407407407	0.155462962962963	0.155518518518518	0.155592592592593	0.155648148148148	0.155703703703704	0.155777777777778	0.155833333333333	0.155907407407407	0.155962962962963	0.156018518518519	0.156092592592593	0.156148148148148	0.156203703703704	0.156277777777778	0.156333333333333	0.156388888888889	0.156462962962963	0.156537037037037	0.156574074074074	0.156648148148148	0.156722222222222	0.156759259259259	0.156833333333333	0.156907407407407	0.156944444444444	0.157018518518518	0.157092592592593	0.157166666666667	0.157203703703704	0.157277777777778	0.157351851851852	0.157407407407407	0.157462962962963	0.157537037037037	0.157592592592593	0.157648148148148	0.157722222222222	0.157777777777778	0.157833333333333	0.157907407407407	0.157962962962963	0.158037037037037	0.158092592592593	0.158148148148148	0.158222222222222	0.158277777777778	0.158333333333333	0.158407407407407	0.158462962962963	0.158518518518519	0.158592592592593	0.158648148148148	0.158703703703704	0.158777777777778	0.158833333333333	0.158888888888889	0.158962962962963	0.159037037037037	0.159074074074074	0.159148148148148	0.159203703703704	0.159259259259259	0.159333333333333	0.159388888888889	0.159444444444444	0.159518518518519	0.159592592592593	0.15962962962963	0.159703703703704	0.159777777777778	0.159814814814815	0.159888888888889	0.159962962962963	0.16	0.160074074074074	0.160148148148148	0.160185185185185	0.160259259259259	0.160333333333333	0.16037037037037	0.160444444444444	0.160518518518518	0.160592592592593	0.16062962962963	0.160703703703704	0.160777777777778	0.160814814814815	0.160888888888889	0.160962962962963	0.161	0.161074074074074	0.161148148148148	0.161185185185185	0.161259259259259	0.161333333333333	0.161388888888889	0.161444444444444	0.161518518518518	0.161574074074074	0.16162962962963	0.161703703703704	0.161759259259259	0.161814814814815	0.161888888888889	0.161944444444444	0.162	0.162074074074074	0.16212962962963	0.162185185185185	0.162259259259259	0.162314814814815	0.162388888888889	0.162444444444444	0.1625	0.162574074074074	0.16262962962963	0.162685185185185	0.162759259259259	0.162814814814815	0.16287037037037	0.162944444444444	0.163	0.163055555555556	0.16312962962963	0.163203703703704	0.163240740740741	0.163314814814815	0.163388888888889	0.163425925925926	0.1635	0.163574074074074	0.163611111111111	0.163685185185185	0.163759259259259	0.163833333333333	0.16387037037037	0.163944444444444	0.164018518518518	0.164055555555556	0.16412962962963	0.164203703703704	0.164240740740741	0.164314814814815	0.164388888888889	0.164425925925926	0.1645	0.164574074074074	0.16462962962963	0.164685185185185	0.164759259259259	0.164814814814815	0.16487037037037	0.164944444444444	0.165	0.165055555555556	0.16512962962963	0.165185185185185	0.165259259259259	0.165314814814815	0.16537037037037	0.165444444444444	0.1655	0.165555555555556	0.16562962962963	0.165685185185185	0.165740740740741	0.165814814814815	0.16587037037037	0.165925925925926	0.166	0.166055555555556	0.166111111111111	0.166185185185185	0.166240740740741	0.166296296296296	0.16637037037037	0.166444444444444	0.166481481481481	0.166555555555556	0.16662962962963	0.166666666666667	0.166740740740741	0.166814814814815	0.166851851851852	0.166925925925926	0.167	0.167055555555556	0.167111111111111	0.167185185185185	0.167240740740741	0.167296296296296	0.16737037037037	0.167425925925926	0.1675	0.167555555555556	0.167611111111111	0.167685185185185	0.167740740740741	0.167796296296296	0.16787037037037	0.167925925925926	0.167981481481481	0.168055555555556	0.16812962962963	0.168166666666667	0.168240740740741	0.168314814814815	0.168351851851852	0.168425925925926	0.1685	0.168537037037037	0.168611111111111	0.168685185185185	0.168722222222222	0.168796296296296	0.16887037037037	0.168907407407407	0.168981481481481	0.169055555555556	0.169092592592593	0.169166666666667	0.169240740740741	0.169314814814815	0.169351851851852	0.169425925925926	0.1695	0.169537037037037	0.169611111111111	0.169685185185185	0.169722222222222	0.169796296296296	0.16987037037037	0.169925925925926	0.169981481481481	0.170055555555556	0.170111111111111	0.170166666666667	0.170240740740741	0.170296296296296	0.170351851851852	0.170425925925926	0.170481481481481	0.170555555555556	0.170611111111111	0.170666666666667	0.170740740740741	0.170796296296296	0.170851851851852	0.170925925925926	0.170981481481481	0.171037037037037	0.171111111111111	0.171185185185185	0.171222222222222	0.171296296296296	0.17137037037037	0.171481481481481	0.171574074074074	0.17162962962963	0.171666666666667	0.171740740740741	0.171814814814815	0.171851851851852	0.171925925925926	0.172	0.172037037037037	0.172111111111111	0.172185185185185	0.172240740740741	0.172296296296296	0.17237037037037	0.172425925925926	0.172481481481481	0.172555555555556	0.172611111111111	0.172666666666667	0.172740740740741	0.172796296296296	0.17287037037037	0.172925925925926	0.172981481481481	0.173055555555556	0.173111111111111	0.173166666666667	0.173240740740741	0.173314814814815	0.173351851851852	0.173425925925926	0.1735	0.173537037037037	0.173611111111111	0.173685185185185	0.173722222222222	0.173796296296296	0.17387037037037	0.173907407407407	0.173981481481481	0.174055555555556	0.174092592592593	0.174166666666667	0.174240740740741	0.174277777777778	0.174351851851852	0.174425925925926	0.1745	0.174537037037037	0.174611111111111	0.174685185185185	0.174722222222222	0.174796296296296	0.17487037037037	0.174907407407407	0.174981481481481	0.175055555555556	0.175092592592593	0.175166666666667	0.175240740740741	0.175296296296296	0.175351851851852	0.175425925925926	0.175481481481481	0.175537037037037	0.175611111111111	0.175666666666667	0.175740740740741	0.175796296296296	0.175851851851852	0.175925925925926	0.175981481481481	0.176037037037037	0.176111111111111	0.176166666666667	0.176222222222222	0.176296296296296	0.176351851851852	0.176407407407407	0.176481481481481	0.176555555555556	0.176592592592593	0.176666666666667	0.176740740740741	0.176777777777778	0.176851851851852	0.176925925925926	0.176962962962963	0.177037037037037	0.177111111111111	0.177148148148148	0.177222222222222	0.177296296296296	0.177333333333333	0.177407407407407	0.177481481481481	0.177555555555556	0.177592592592593	0.177666666666667	0.177740740740741	0.177796296296296	0.177851851851852	0.177925925925926	0.177981481481481	0.178037037037037	0.178111111111111	0.178166666666667	0.178240740740741	0.178296296296296	0.178351851851852	0.178425925925926	0.1785	0.178537037037037	0.178611111111111	0.178685185185185	0.178722222222222	0.178796296296296	0.17887037037037	0.178907407407407	0.178981481481481	0.179055555555556	0.179092592592593	0.179166666666667	0.179240740740741	0.179277777777778	0.179351851851852	0.179425925925926	0.1795	0.179537037037037	0.179611111111111	0.179685185185185	0.179740740740741	0.179796296296296	0.17987037037037	0.179925925925926	0.179981481481481	0.180055555555556	0.180111111111111	0.180185185185185	0.180240740740741	0.180296296296296	0.18037037037037	0.180444444444444	0.180481481481481	0.180555555555556	0.18062962962963	0.180666666666667	0.180740740740741	0.180814814814815	0.180851851851852	0.180925925925926	0.181	0.181037037037037	0.181111111111111	0.181185185185185	0.181222222222222	0.181296296296296	0.18137037037037	0.181444444444444	0.181481481481481	0.181555555555556	0.18162962962963	0.181666666666667	0.181740740740741	0.181814814814815	0.18187037037037	0.181925925925926	0.182	0.182055555555556	0.182111111111111	0.182185185185185	0.182240740740741	0.182296296296296	0.18237037037037	0.182425925925926	0.1825	0.182555555555556	0.182611111111111	0.182685185185185	0.182759259259259	0.182796296296296	0.18287037037037	0.182944444444444	0.182981481481481	0.183055555555556	0.18312962962963	0.183166666666667	0.183240740740741	0.183314814814815	0.183388888888889	0.183425925925926	0.1835	0.183574074074074	0.183611111111111	0.183685185185185	0.183759259259259	0.183796296296296	0.18387037037037	0.183944444444444	0.184	0.184055555555556	0.18412962962963	0.184185185185185	0.184240740740741	0.184314814814815	0.18437037037037	0.184444444444444	0.1845	0.184555555555556	0.18462962962963	0.184685185185185	0.184740740740741	0.184814814814815	0.18487037037037	0.184925925925926	0.185	0.185074074074074	0.185111111111111	0.185185185185185	0.185259259259259	0.185296296296296	0.18537037037037	0.185444444444444	0.185481481481481	0.185555555555556	0.18562962962963	0.185666666666667	0.185740740740741	0.185814814814815	0.18587037037037	0.185925925925926	0.186	0.186055555555556	0.186111111111111	0.186185185185185	0.186240740740741	0.186296296296296	0.18637037037037	0.186425925925926	0.1865	0.186555555555556	0.186611111111111	0.186685185185185	0.186740740740741	0.186796296296296	0.18687037037037	0.186925925925926	0.186981481481481	0.187055555555556	0.18712962962963	0.187166666666667	0.187240740740741	0.187314814814815	0.187388888888889	0.0	0.0	0.0	0.0	0.0	0.0	0.0	0.0	0.0	0.0	0.0393464813229044	0.0393464813229044	0.0393464813229044	0.0786929626458088	0.0786929626458088	0.118039443968713	0.118039443968713	0.157385925291618	0.157385925291618	0.196732406614522	0.236078887937426	0.236078887937426	0.275425369260331	0.314771850583235	0.354118331906139	0.354118331906139	0.393464813229044	0.432811294551948	0.472157775874853	0.511504257197757	0.590197219843566	0.62954370116647	0.708236663812279	0.786929626458088	0.904969070426801	0.98366203307261	1.062354995718418	1.180394439687132	1.298433883655845	1.377126846301653	1.495166290270367	1.61320573423908	1.731245178207793	1.809938140853602	1.88863110349941	2.006670547468124	2.124709991436837	2.24274943540555	2.282095916728454	2.400135360697168	2.518174804665881	2.59686776731169	2.714907211280402	2.832946655249116	2.911639617894925	3.029679061863638	3.108372024509447	3.22641146847816	3.305104431123969	3.423143875092682	3.501836837738491	3.5805298003843	3.698569244353012	3.777262206998821	3.934648132290438	4.013341094936247	4.092034057582055	4.21007350155077	4.288766464196577	4.406805908165291	4.524845352134005	4.603538314779812	4.682231277425621	4.800270721394336	4.918310165363048	4.997003128008857	5.115042571977569	5.233082015946284	5.311774978592091	5.429814422560805	5.508507385206614	5.665893310498231	5.74458627314404	5.82327923578985	5.941318679758562	6.020011642404372	6.177397567695987	6.256090530341797	6.334783492987606	6.45282293695632	6.531515899602128	6.610208862247936	6.767594787539553	6.885634231508267	6.964327194154077	7.043020156799885	7.161059600768597	7.239752563414407	7.397138488706025	7.475831451351833	7.593870895320547	7.672563857966355	7.790603301935068	7.869296264580877	7.987335708549589	8.066028671195398	8.184068115164113	8.26276107780992	8.380800521778636	8.459493484424445	8.577532928393155	8.656225891038966	8.774265335007678	8.852958297653486	8.9709977416222	9.128383666913816	9.207076629559625	9.32511607352834	9.40380903617415	9.521848480142861	9.639887924111573	9.718580886757383	9.836620330726098	9.915313293371905	10.03335273734062	10.15139218130933	10.23008514395514	10.34812458792385	10.42681755056966	10.54485699453838	10.6628964385071	10.7415894011529	10.85962884512161	10.97766828909032	11.05636125173613	11.17440069570485	11.29244013967356	11.37113310231937	11.48917254628808	11.56786550893389	11.6859049529026	11.84329087819422	11.96133032216293	12.04002328480874	12.15806272877746	12.27610217274617	12.35479513539198	12.4728345793607	12.5908740233294	12.66956698597521	12.78760642994393	12.90564587391264	12.98433883655845	13.10237828052716	13.22041772449587	13.29911068714168	13.4171501311104	13.53518957507911	13.61388253772492	13.73192198169363	13.84996142566234	13.96800086963106	14.04669383227687	14.16473327624558	14.28277272021429	14.3614656828601	14.47950512682882	14.59754457079753	14.71558401476624	14.79427697741205	14.91231642138076	15.03035586534948	15.10904882799528	15.227088271964	15.34512771593271	15.46316715990142	15.54186012254723	15.65989956651595	15.77793901048466	15.89597845445337	15.97467141709918	16.09271086106789	16.21075030503661	16.32878974900532	16.40748271165113	16.52552215561984	16.64356159958855	16.76160104355727	16.87964048752598	16.95833345017178	17.0763728941405	17.19441233810922	17.31245178207793	17.39114474472374	17.50918418869245	17.62722363266117	17.74526307662988	17.86330252059859	17.9419954832444	18.06003492721311	18.21742085250473	18.33546029647345	18.45349974044216	18.57153918441087	18.68957862837959	18.76827159102538	18.88631103499411	19.00435047896282	19.12238992293153	19.24042936690023	19.31912232954605	19.43716177351477	19.55520121748348	19.6732406614522	19.79128010542091	19.86997306806672	19.98801251203542	20.10605195600414	20.22409139997286	20.34213084394156	20.46017028791028	20.578209731879	20.6569026945248	20.77494213849352	20.89298158246223	21.01102102643094	21.12906047039966	21.24709991436837	21.32579287701418	21.44383232098289	21.5618717649516	21.67991120892032	21.79795065288903	21.91599009685774	21.99468305950355	22.11272250347227	22.23076194744098	22.3488013914097	22.46684083537841	22.58488027934712	22.66357324199292	22.78161268596163	22.89965212993035	23.01769157389907	23.13573101786778	23.2537704618365	23.37180990580521	23.45050286845101	23.56854231241972	23.68658175638844	23.80462120035715	23.92266064432586	24.04070008829458	24.15873953226328	24.27677897623201	24.35547193887782	24.47351138284653	24.59155082681524	24.70959027078395	24.82762971475267	24.94566915872137	25.0637086026901	25.18174804665881	25.26044100930462	25.37848045327333	25.49651989724205	25.61455934121076	25.73259878517947	25.85063822914818	25.96867767311689	26.08671711708561	26.16541007973142	26.28344952370012	26.40148896766884	26.51952841163756	26.63756785560627	26.75560729957498	26.87364674354369	26.95233970618951	27.07037915015822	27.18841859412692	27.30645803809564	27.42449748206436	27.54253692603307	27.66057637000178	27.7786158139705	27.89665525793921	27.97534822058502	28.09338766455373	28.21142710852245	28.32946655249116	28.44750599645987	28.56554544042859	28.68358488439729	28.80162432836601	28.91966377233473	28.99835673498053	29.11639617894925	29.23443562291796	29.35247506688667	29.47051451085538	29.5885539548241	29.70659339879281	29.82463284276152	29.94267228673023	30.02136524937605	30.13940469334476	30.25744413731347	30.37548358128219	30.4935230252509	30.61156246921961	30.72960191318833	30.84764135715704	30.96568080112574	31.08372024509447	31.16241320774028	31.28045265170898	31.3984920956777	31.51653153964642	31.63457098361512	31.75261042758384	31.87064987155254	31.98868931552126	32.06738227816707	32.1854217221358	32.30346116610449	32.42150061007322	32.53954005404193	32.65757949801063	32.77561894197936	32.89365838594807	33.01169782991677	33.0903907925626	33.2084302365313	33.32646968050002	33.44450912446873	33.56254856843744	33.68058801240615	33.79862745637487	33.91666690034358	34.0347063443123	34.1133993069581	34.23143875092682	34.34947819489552	34.46751763886424	34.58555708283296	34.70359652680167	34.78228948944746	34.9003289334162	35.0183683773849	35.13640782135361	35.25444726532231	35.37248670929104	35.49052615325976	35.56921911590557	35.68725855987427	35.80529800384299	35.9233374478117	36.04137689178042	36.15941633574914	36.23810929839493	36.35614874236365	36.47418818633236	36.59222763030108	36.71026707426979	36.82830651823851	36.94634596220722	37.06438540617593	37.18242485014464	37.26111781279045	37.37915725675917	37.49719670072788	37.6152361446966	37.73327558866531	37.85131503263402	37.96935447660272	38.04804743924853	38.16608688321724	38.28412632718598	38.4021657711547	38.5202052151234	38.63824465909209	38.75628410306081	38.87432354702953	38.95301650967534	39.07105595364405	39.18909539761277	39.3071348415815	39.4251742855502	39.54321372951891	39.62190669216472	39.73994613613343	39.85798558010214	39.97602502407085	40.09406446803956	40.21210391200828	40.330143355977	40.44818279994571	40.52687576259152	40.64491520656023	40.76295465052895	40.88099409449764	40.99903353846637	41.11707298243508	41.2351124264038	41.3138053890496	41.43184483301831	41.54988427698704	41.66792372095575	41.78596316492446	41.90400260889317	41.98269557153898	42.1007350155077	42.2187744594764	42.33681390344512	42.45485334741384	42.57289279138254	42.69093223535126	42.76962519799707	42.88766464196577	43.0057040859345	43.12374352990321	43.24178297387192	43.35982241784061	43.47786186180934	43.55655482445515	43.67459426842387	43.7926337123926	43.91067315636129	44.02871260033	44.10740556297582	44.22544500694453	44.34348445091322	44.46152389488195	44.57956333885067	44.6976027828194	44.7762957454652	44.89433518943391	45.01237463340262	45.13041407737133	45.24845352134005	45.32714648398586	45.44518592795457	45.56322537192328	45.68126481589199	45.7993042598607	45.87799722250652	45.99603666647522	46.11407611044395	46.23211555441266	46.35015499838137	46.42884796102717	46.54688740499589	46.6649268489646	46.78296629293332	46.90100573690203	46.97969869954784	47.09773814351655	47.21577758748526	47.33381703145398	47.45185647542267	47.5305494380685	47.64858888203722	47.76662832600593	47.88466776997463	47.96336073262045	48.08140017658916	48.19943962055788	48.31747906452658	48.4355185084953	48.5142114711411	48.63225091510983	48.75029035907853	48.86832980304725	48.94702276569304	49.06506220966177	49.18310165363048	49.30114109759919	49.379834060245	49.49787350421371	49.61591294818244	49.73395239215115	49.81264535479695	49.93068479876566	50.04872424273438	50.1667636867031	50.2454566493489	50.36349609331759	50.48153553728632	50.56022849993214	50.67826794390084	50.79630738786957	50.91434683183827	50.9930397944841	51.1110792384528	51.2291186824215	51.30781164506731	51.42585108903604	51.54389053300475	51.62258349565055	51.74062293961927	51.85866238358798	51.9767018275567	52.0553947902025	52.17343423417121	52.29147367813992	52.37016664078574	52.48820608475445	52.60624552872316	52.68493849136897	52.80297793533769	52.9210173793064	52.9997103419522	53.11774978592092	53.23578922988964	53.31448219253544	53.43252163650416	53.55056108047287	53.62925404311868	53.74729348708739	53.8653329310561	53.94402589370192	54.06206533767063	54.18010478163934	54.25879774428515	54.37683718825387	54.49487663222257	54.57356959486839	54.6916090388371	54.80964848280581	54.88834144545162	55.00638088942033	55.12442033338904	55.20311329603486	55.32115274000357	55.39984570264937	55.51788514661808	55.6359245905868	55.71461755323259	55.83265699720133	55.95069644117004	56.02938940381585	56.14742884778455	56.22612181043037	56.34416125439907	56.4622006983678	56.54089366101359	56.65893310498232	56.77697254895103	56.85566551159683	56.97370495556554	57.05239791821135	57.17043736218007	57.28847680614878	57.36716976879459	57.4852092127633	57.56390217540912	57.68194161937782	57.79998106334653	57.87867402599234	57.99671346996107	58.07540643260688	58.19344587657558	58.2721388392214	58.39017828319011	58.50821772715882	58.58691068980463	58.70495013377334	58.78364309641915	58.90168254038787	58.98037550303367	59.0984149470024	59.17710790964819	59.2951473536169	59.37384031626272	59.49187976023142	59.57057272287725	59.68861216684595	59.76730512949176	59.88534457346046	59.96403753610629	60.082076980075	60.12142346139789	60.23946290536662	60.31815586801243	60.43619531198113	60.51488827462694	60.59358123727276	60.71162068124146	60.79031364388728	60.908353087856	60.9870460505018	61.10508549447052	61.18377845711632	61.26247141976214	61.38051086373085	61.45920382637664	61.57724327034536	61.65593623299118	61.73462919563697	61.8526686396057	61.9313616022515	62.04940104622022	62.12809400886603	62.20678697151184	62.32482641548054	62.40351937812636	62.48221234077217	62.60025178474088	62.67894474738669	62.75763771003249	62.8756771540012	62.95437011664701	63.03306307929282	63.11175604193864	63.22979548590735	63.30848844855316	63.38718141119896	63.46587437384477	63.54456733649057	63.6626067804593	63.74129974310511	63.81999270575091	63.89868566839672	63.97737863104253	64.05607159368833	64.17411103765704	64.25280400030285	64.33149696294867	64.4101899255945	64.4888828882403	64.56757585088609	64.64626881353188	64.72496177617772	64.80365473882351	64.88234770146931	64.96104066411517	65.07908010808383	65.15777307072963	65.23646603337547	65.27581251469836	65.3938519586671	65.43319843998998	65.51189140263581	65.59058436528161	65.6692773279274	65.74797029057323	65.82666325321903	65.90535621586484	65.98404917851065	66.06274214115643	66.14143510380228	66.18078158512516	66.25947454777098	66.33816751041678	66.4168604730626	66.4562069543855	66.53489991703131	66.61359287967713	66.65293936100004	66.73163232364584	66.81032528629165	66.84967176761455	66.92836473026037	66.96771121158325	67.00705769290617	67.08575065555196	67.1644436181978	67.20379009952067	67.28248306216651	67.3611760248123	67.43986898745813	67.47921546878102	67.55790843142682	67.63660139407264	67.67594787539554	67.75464083804135	67.79398731936425	67.87268028201007	67.91202676333298	67.9907197259788	68.03006620730168	68.0694126886246	68.10875916994748	68.1481056512704	68.18745213259328	68.18745213259328	68.2267986139162	68.2267986139162	68.2267986139162	68.18745213259328	68.03006620730168	67.67594787539554	67.2431365808436	66.81032528629165	66.57424639835421	66.22012806644808	65.86600973454195	65.55123788395871	65.23646603337547	64.96104066411517	64.72496177617772	64.606922332209	64.6856152948548	64.80365473882351	64.96104066411517	65.11842658940677	65.27581251469836	65.43319843998998	65.59058436528161	65.6692773279274	65.82666325321903	65.94470269718776	66.10208862247934	66.22012806644808	66.3775139917397	66.4955534357084	66.61359287967713	66.73163232364584	66.84967176761455	66.96771121158325	67.08575065555196	67.20379009952067	67.3218295434894	67.43986898745813	67.51856195010393	67.63660139407264	67.71529435671845	67.83333380068716	67.95137324465588	68.0694126886246	68.18745213259328	68.2267986139162	68.3448380578849	68.46287750185363	68.54157046449944	68.65960990846815	68.69895638979105	68.81699583375976	68.93503527772847	69.0137282403743	69.131767684343	69.17111416566591	69.24980712831173	69.36784657228043	69.44653953492624	69.56457897889494	69.60392546021787	69.68261842286365	69.76131138550948	69.87935082947818	69.95804379212399	69.99739027344691	70.0760832360927	70.1547761987385	70.23346916138433	70.31216212403014	70.35150860535304	70.43020156799884	70.50889453064465	70.58758749329047	70.66628045593628	70.70562693725918	70.784319899905	70.86301286255078	70.9417058251966	71.02039878784241	71.05974526916531	71.13843823181112	71.17778471313403	71.25647767577985	71.33517063842564	71.37451711974855	71.45321008239436	71.57124952636307	71.61059600768597	71.68928897033179	71.7679819329776	71.84667489562341	71.92536785826921	71.96471433959212	72.08275378356082	72.16144674620665	72.24013970885246	72.27948619017535	72.39752563414408	72.47621859678986	72.55491155943568	72.63360452208148	72.7516439660502	72.86968341001892	73.02706933531055	73.14510877927925	73.30249470457088	73.42053414853957	73.4992271111854	73.57792007383121	73.61726655515411	73.69595951779989	73.73530599912283	73.77465248044572	73.85334544309153	73.93203840573734	73.97138488706025	74.05007784970604	74.12877081235182	74.16811729367475	74.2074637749977	74.28615673764348	74.32550321896638	74.4041961816122	74.4435426629351	74.52223562558089	74.60092858822671	74.64027506954963	74.67962155087253	74.71896803219542	74.79766099484125	74.83700747616415	74.91570043880995	74.95504692013285	75.03373988277865	75.07308636410156	75.15177932674737	75.15177932674737	75.2304722893932	75.2698187707161	75.34851173336189	75.38785821468478	75.46655117733061	75.5058976586535	75.54524413997643	75.62393710262221	75.62393710262221	75.70263006526803	75.74197654659095	75.78132302791387	75.86001599055965	75.89936247188257	75.93870895320545	75.97805543452836	76.01740191585128	76.05674839717416	76.13544135981996	76.13544135981996	76.17478784114289	76.2141343224658	76.25348080378868	76.2928272851116	76.33217376643449	76.37152024775741	76.37152024775741	76.41086672908032	76.45021321040321	76.48955969172612	76.48955969172612	76.52890617304902	76.52890617304902	76.52890617304902	76.56825265437194	76.56825265437194	76.56825265437194	76.60759913569483	76.60759913569483	76.60759913569483	76.60759913569483	76.64694561701774	76.64694561701774	76.64694561701774	76.60759913569483	76.60759913569483	76.60759913569483	76.60759913569483	76.56825265437194	76.56825265437194	76.56825265437194	76.52890617304902	76.52890617304902	76.52890617304902	76.52890617304902	76.52890617304902	76.52890617304902	76.52890617304902	76.56825265437194	76.56825265437194	76.56825265437194	76.60759913569483	76.64694561701774	76.64694561701774	76.68629209834065	76.68629209834065	76.72563857966354	76.72563857966354	76.76498506098646	76.80433154230936	76.80433154230936	76.80433154230936	76.84367802363225	76.84367802363225	76.88302450495517	76.88302450495517	76.88302450495517	76.88302450495517	76.88302450495517	76.88302450495517	76.88302450495517	76.84367802363225	76.84367802363225	76.80433154230936	76.76498506098646	76.72563857966354	76.64694561701774	76.60759913569483	76.52890617304902	76.45021321040321	76.37152024775741	76.33217376643449	76.25348080378868	76.17478784114289	76.09609487849708	76.01740191585128	75.97805543452836	75.86001599055965	75.78132302791387	75.70263006526803	75.58459062129932	75.58459062129932	75.5058976586535	75.4272046960077	75.34851173336189	75.30916525203898	75.30916525203898	75.2698187707161	75.2304722893932	75.1911258080703	75.1911258080703	75.2304722893932	75.2304722893932	75.2304722893932	75.2304722893932	75.2698187707161	75.30916525203898	75.30916525203898	75.34851173336189	75.38785821468478	75.38785821468478	75.4272046960077	75.46655117733061	75.54524413997643	75.58459062129932	75.66328358394515	75.70263006526803	75.78132302791387	75.86001599055965	75.89936247188257	75.97805543452836	76.01740191585128	76.09609487849708	76.17478784114289	76.25348080378868	76.33217376643449	76.37152024775741	76.45021321040321	76.52890617304902	76.60759913569483	76.68629209834065	76.76498506098646	76.84367802363225	76.88302450495517	76.96171746760097	77.0404104302468	77.1191033928926	77.2371428368613	77.27648931818419	77.35518228083001	77.43387524347584	77.51256820612163	77.55191468744456	77.63060765009035	77.70930061273616	77.74864709405907	77.78799357538197	77.86668653802778	77.90603301935068	77.9847259819965	78.0240724633194	78.0634189446423	78.14211190728811	78.18145838861101	78.26015135125681	78.2994978325797	78.33884431390263	78.37819079522554	78.45688375787135	78.49623023919426	78.57492320184007	78.57492320184007	78.65361616448585	78.69296264580877	78.77165560845458	78.8110020897775	78.85034857110038	78.92904153374619	79.00773449639201	79.12577394036072	79.20446690300653	79.28315986565233	79.36185282829815	79.47989227226685	79.55858523491267	79.63727819755846	79.71597116020428	79.7946641228501	79.834010604173	79.9127035668188	79.99139652946461	80.03074301078752	80.07008949211043	80.14878245475622	80.22747541740205	80.30616838004786	80.38486134269365	80.42420782401657	80.50290078666238	80.54224726798528	80.5815937493082	80.62094023063106	80.66028671195399	80.73897967459979	80.7783261559227	80.8176726372456	80.8570191185685	80.89636559989141	80.93571208121433	80.97505856253721	81.01440504386013	81.05375152518305	81.09309800650593	81.13244448782885	81.17179096915174	81.21113745047465	81.25048393179756	81.28983041312046	81.32917689444334	81.40786985708918	81.4472163384121	81.48656281973497	81.52590930105788	81.5652557823808	81.5652557823808	81.6046022637037	81.64394874502661	81.68329522634951	81.72264170767241	81.76198818899531	81.80133467031822	81.84068115164111	81.88002763296402	81.91937411428692	81.95872059560985	81.99806707693274	82.03741355825566	82.07676003957855	82.07676003957855	82.11610652090145	82.15545300222433	82.19479948354728	82.23414596487018	82.27349244619306	82.31283892751597	82.35218540883888	82.39153189016177	82.43087837148467	82.43087837148467	82.4702248528076	82.50957133413048	82.54891781545339	82.58826429677631	82.62761077809921	82.66695725942211	82.70630374074502	82.74565022206792	82.78499670339083	82.82434318471374	82.82434318471374	82.86368966603664	82.90303614735953	82.94238262868245	82.98172911000536	83.02107559132825	83.06042207265114	83.09976855397406	83.13911503529697	83.13911503529697	83.17846151661985	83.2178079979428	83.2571544792657	83.29650096058858	83.29650096058858	83.3358474419115	83.37519392323441	83.4145404045573	83.45388688588021	83.45388688588021	83.4932333672031	83.532579848526	83.57192632984892	83.61127281117182	83.6506192924947	83.6506192924947	83.68996577381763	83.72931225514054	83.72931225514054	83.76865873646342	83.80800521778632	83.84735169910926	83.88669818043215	83.88669818043215	83.92604466175507	83.96539114307797	83.96539114307797	84.00473762440086	84.04408410572377	84.08343058704668	84.08343058704668	84.12277706836956	84.1621235496925	84.1621235496925	84.20147003101538	84.2408165123383	84.2408165123383	84.28016299366118	84.3195094749841	84.35885595630701	84.35885595630701	84.39820243762989	84.43754891895281	84.43754891895281	84.47689540027572	84.51624188159863	84.51624188159863	84.5555883629215	84.5555883629215	84.59493484424443	84.63428132556734	84.63428132556734	84.67362780689022	84.71297428821316	84.71297428821316	84.75232076953605	84.79166725085894	84.79166725085894	84.83101373218184	84.83101373218184	84.87036021350474	84.90970669482767	84.90970669482767	84.94905317615057	84.94905317615057	84.98839965747348	85.02774613879636	85.02774613879636	85.02774613879636	85.0670926201193	85.10643910144218	85.10643910144218	85.14578558276509	85.14578558276509	85.18513206408797	85.18513206408797	85.22447854541089	85.22447854541089	85.26382502673381	85.26382502673381	85.30317150805669	85.30317150805669	85.3425179893796	85.3425179893796	85.38186447070252	85.38186447070252	85.42121095202543	85.42121095202543	85.42121095202543	85.46055743334832	85.46055743334832	85.49990391467123	85.49990391467123	85.49990391467123	85.53925039599414	85.53925039599414	85.57859687731704	85.57859687731704	85.61794335863995	85.61794335863995	85.61794335863995	85.65728983996285	85.65728983996285	85.69663632128575	85.69663632128575	85.69663632128575	85.73598280260863	85.73598280260863	85.77532928393157	85.77532928393157	85.77532928393157	85.81467576525447	85.81467576525447	85.81467576525447	85.85402224657737	85.85402224657737	85.89336872790028	85.89336872790028	85.89336872790028	85.93271520922318	85.93271520922318	85.93271520922318	85.97206169054608	85.97206169054608	85.97206169054608	86.01140817186898	86.01140817186898	86.01140817186898	86.05075465319189	86.05075465319189	86.05075465319189	86.09010113451478	86.09010113451478	86.09010113451478	86.12944761583771	86.12944761583771	86.12944761583771	86.1687940971606	86.1687940971606	86.1687940971606	86.1687940971606	86.20814057848349	86.20814057848349	86.20814057848349	86.24748705980641	86.24748705980641	86.24748705980641	86.28683354112933	86.28683354112933	86.28683354112933	86.32618002245221	86.32618002245221	86.32618002245221	86.32618002245221	86.36552650377513	86.36552650377513	86.36552650377513	86.40487298509803	86.40487298509803	86.40487298509803	86.44421946642096	86.44421946642096	86.44421946642096	86.44421946642096	86.48356594774385	86.48356594774385	86.48356594774385	86.52291242906675	86.52291242906675	86.52291242906675	86.52291242906675	86.56225891038964	86.56225891038964	86.56225891038964	86.60160539171256	86.60160539171256	86.60160539171256	86.64095187303545	86.64095187303545	86.64095187303545	86.64095187303545	86.68029835435836	86.68029835435836	86.68029835435836	86.71964483568127	86.71964483568127	86.71964483568127	86.75899131700415	86.75899131700415	86.75899131700415	86.75899131700415	86.79833779832708	86.79833779832708	86.79833779832708	86.83768427965	86.83768427965	86.83768427965	86.87703076097288	86.87703076097288	86.87703076097288	86.91637724229578	86.91637724229578	86.91637724229578	86.9557237236187	86.9557237236187	86.9557237236187	86.9557237236187	86.9950702049416	86.9950702049416	86.9950702049416	87.0344166862645	87.0344166862645	87.0344166862645	87.0737631675874	87.0737631675874	87.0737631675874	87.1131096489103	87.1131096489103	87.1131096489103	87.15245613023319	87.15245613023319	87.15245613023319	87.19180261155611	87.19180261155611	87.19180261155611	87.19180261155611	87.23114909287902	87.23114909287902	87.23114909287902	87.27049557420192	87.27049557420192	87.27049557420192	87.30984205552481	87.30984205552481	87.30984205552481	87.34918853684775	87.34918853684775	87.34918853684775	87.38853501817063	87.38853501817063	87.38853501817063	87.38853501817063	87.42788149949355	87.42788149949355	87.42788149949355	87.46722798081648	87.46722798081648	87.46722798081648	87.50657446213935	87.50657446213935	87.50657446213935	87.50657446213935	87.54592094346226	87.54592094346226	87.54592094346226	87.58526742478517	87.58526742478517	87.58526742478517	87.62461390610806	87.62461390610806	87.62461390610806	87.62461390610806	87.66396038743098	87.66396038743098	87.66396038743098	87.70330686875387	87.70330686875387	87.70330686875387	87.70330686875387	87.74265335007677	87.74265335007677	87.74265335007677	87.78199983139968	87.78199983139968	87.78199983139968	87.78199983139968	87.82134631272257	87.82134631272257	87.82134631272257	87.82134631272257	87.8606927940455	87.8606927940455	87.8606927940455	87.9000392753684	87.9000392753684	87.9000392753684	87.9000392753684	87.93938575669129	87.93938575669129	87.93938575669129	87.93938575669129	87.97873223801419	87.97873223801419	87.97873223801419	88.01807871933711	88.01807871933711	88.01807871933711	88.01807871933711	88.05742520066002	88.05742520066002	88.05742520066002	88.05742520066002	88.09677168198293	88.09677168198293	88.09677168198293	88.09677168198293	88.13611816330581	88.13611816330581	88.13611816330581	88.13611816330581	88.17546464462872	88.17546464462872	88.17546464462872	88.17546464462872	88.21481112595164	88.21481112595164	88.21481112595164	88.21481112595164	88.25415760727454	88.25415760727454	88.25415760727454	88.25415760727454	88.29350408859745	88.29350408859745	88.29350408859745	88.29350408859745	88.33285056992035	88.33285056992035	88.33285056992035	88.33285056992035	88.37219705124325	88.37219705124325	88.37219705124325	88.37219705124325	88.41154353256615	88.41154353256615	88.41154353256615	88.41154353256615	88.45089001388905	88.45089001388905	88.45089001388905	88.45089001388905	88.49023649521198	88.49023649521198	88.49023649521198	88.49023649521198	88.52958297653484	88.52958297653484	88.52958297653484	88.52958297653484	88.56892945785777	88.56892945785777	88.56892945785777	88.56892945785777	88.60827593918067	88.60827593918067	88.60827593918067	88.60827593918067	88.60827593918067	88.6476224205036	88.6476224205036	88.6476224205036	88.6476224205036	88.68696890182647	88.68696890182647	88.68696890182647	88.68696890182647	88.7263153831494	88.7263153831494	88.7263153831494	88.7263153831494	88.7656618644723	88.7656618644723	88.7656618644723	88.7656618644723	88.80500834579519	88.80500834579519	88.80500834579519	88.80500834579519	88.80500834579519	88.8443548271181	88.8443548271181	88.8443548271181	88.8443548271181	88.88370130844099	88.88370130844099	88.88370130844099	88.88370130844099	88.92304778976391	88.92304778976391	88.92304778976391	88.92304778976391	88.92304778976391	88.96239427108681	88.96239427108681	88.96239427108681	88.96239427108681	89.0017407524097	89.0017407524097	89.0017407524097	89.0017407524097	89.04108723373263	89.04108723373263	89.04108723373263	89.04108723373263	89.04108723373263	89.08043371505552	89.08043371505552	89.08043371505552	89.08043371505552	89.11978019637843	89.11978019637843	89.11978019637843	89.11978019637843	89.15912667770134	89.15912667770134	89.15912667770134	89.15912667770134	89.15912667770134	89.19847315902423	89.19847315902423	89.19847315902423	89.19847315902423	89.2378196403472	89.2378196403472	89.2378196403472	89.2378196403472	89.2378196403472	89.27716612167006	89.27716612167006	89.27716612167006	89.27716612167006	89.31651260299295	89.31651260299295	89.31651260299295	89.31651260299295	89.35585908431586	89.35585908431586	89.35585908431586	89.35585908431586	89.35585908431586	89.39520556563877	89.39520556563877	89.39520556563877	89.39520556563877	89.43455204696167	89.43455204696167	89.43455204696167	89.43455204696167	89.43455204696167	89.47389852828456	89.47389852828456	89.47389852828456	89.47389852828456	89.5132450096075	89.5132450096075	89.5132450096075	89.5132450096075	89.55259149093038	89.55259149093038	89.55259149093038	89.55259149093038	89.55259149093038	89.59193797225328	89.59193797225328	89.59193797225328	89.59193797225328	89.6312844535762	89.6312844535762	89.6312844535762	89.6312844535762	89.6312844535762	89.67063093489907	89.67063093489907	89.67063093489907	89.67063093489907	89.70997741622199	89.70997741622199	89.70997741622199	89.70997741622199	89.70997741622199	89.74932389754491	89.74932389754491	89.74932389754491	89.74932389754491	89.78867037886781	89.78867037886781	89.78867037886781	89.78867037886781	89.78867037886781	89.8280168601907	89.8280168601907	89.8280168601907	89.8280168601907	89.86736334151362	89.86736334151362	89.86736334151362	89.86736334151362	89.86736334151362	89.90670982283652	89.90670982283652	89.90670982283652	89.90670982283652	89.94605630415943	89.94605630415943	89.94605630415943	89.94605630415943	89.94605630415943	89.98540278548234	89.98540278548234	89.98540278548234	89.98540278548234	90.02474926680524	90.02474926680524	90.02474926680524	90.02474926680524	90.02474926680524	90.06409574812813	90.06409574812813	90.06409574812813	90.06409574812813	90.10344222945103	90.10344222945103	90.10344222945103	90.10344222945103	90.10344222945103	90.14278871077393	90.14278871077393	90.14278871077393	90.14278871077393	90.18213519209682	90.18213519209682	90.18213519209682	90.18213519209682	90.18213519209682	90.22148167341975	90.22148167341975	90.22148167341975	90.22148167341975	90.26082815474267	90.26082815474267	90.26082815474267	90.26082815474267	90.26082815474267	90.30017463606558	90.30017463606558	90.30017463606558	90.30017463606558	90.30017463606558	90.33952111738846	90.33952111738846	90.33952111738846	90.33952111738846	90.37886759871137	90.37886759871137	90.37886759871137	90.37886759871137	90.37886759871137	90.4182140800343	90.4182140800343	90.4182140800343	90.4182140800343	90.4182140800343	90.4575605613572	90.4575605613572	90.4575605613572	90.4575605613572	90.49690704268008	90.49690704268008	90.49690704268008	90.49690704268008	90.49690704268008	90.536253524003	90.536253524003	90.536253524003	90.536253524003	90.536253524003	90.5756000053259	90.5756000053259	90.5756000053259	90.5756000053259	90.5756000053259	90.6149464866488	90.6149464866488	90.6149464866488	90.6149464866488	90.6149464866488	90.65429296797171	90.65429296797171	90.65429296797171	90.65429296797171	90.65429296797171	90.69363944929462	90.69363944929462	90.69363944929462	90.69363944929462	90.69363944929462	90.73298593061751	90.73298593061751	90.73298593061751	90.73298593061751	90.73298593061751	90.77233241194041	90.77233241194041	90.77233241194041	90.77233241194041	90.81167889326332	90.81167889326332	90.81167889326332	90.81167889326332	90.81167889326332	90.85102537458621	90.85102537458621	90.85102537458621	90.85102537458621	90.85102537458621	90.89037185590912	90.89037185590912	90.89037185590912	90.89037185590912	90.89037185590912	90.92971833723205	90.92971833723205	90.92971833723205	90.92971833723205	90.92971833723205	90.96906481855493	90.96906481855493	90.96906481855493	90.96906481855493	90.96906481855493	91.00841129987784	91.00841129987784	91.00841129987784	91.00841129987784	91.00841129987784	91.04775778120077	91.04775778120077	91.04775778120077	91.04775778120077	91.04775778120077	91.08710426252365	91.08710426252365	91.08710426252365	91.08710426252365	91.08710426252365	91.12645074384655	91.12645074384655	91.12645074384655	91.12645074384655	91.12645074384655	91.16579722516946	91.16579722516946	91.16579722516946	91.16579722516946	91.16579722516946	91.20514370649238	91.20514370649238	91.20514370649238	91.20514370649238	91.20514370649238	91.24449018781528	91.24449018781528	91.24449018781528	91.24449018781528	91.24449018781528	91.2838366691382	91.2838366691382	91.2838366691382	91.2838366691382	91.2838366691382	91.2838366691382	91.32318315046106	91.32318315046106	91.32318315046106	91.32318315046106	91.32318315046106	91.36252963178398	91.36252963178398	91.36252963178398	91.36252963178398	91.36252963178398	91.40187611310687	91.40187611310687	91.40187611310687	91.40187611310687	91.40187611310687	91.4412225944298	91.4412225944298	91.4412225944298	91.4412225944298	91.4412225944298	91.4805690757527	91.4805690757527	91.4805690757527	91.4805690757527	91.4805690757527	91.4805690757527	91.5199155570756	91.5199155570756	91.5199155570756	91.5199155570756	91.5199155570756	91.55926203839851	91.55926203839851	91.55926203839851	91.55926203839851	91.55926203839851	91.5986085197214	91.5986085197214	91.5986085197214	91.5986085197214	91.5986085197214	91.63795500104431	91.63795500104431	91.63795500104431	91.63795500104431	91.63795500104431	91.67730148236723	91.67730148236723	91.67730148236723	91.67730148236723	91.67730148236723	91.67730148236723	91.71664796369013	91.71664796369013	91.71664796369013	91.71664796369013	91.71664796369013	91.75599444501304	91.75599444501304	91.75599444501304	91.75599444501304	91.75599444501304	91.79534092633594	91.79534092633594	91.79534092633594	91.79534092633594	91.79534092633594	91.79534092633594	91.83468740765885	91.83468740765885	91.83468740765885	91.83468740765885	91.83468740765885	91.87403388898173	91.87403388898173	91.87403388898173	91.87403388898173	91.87403388898173	91.91338037030465	91.91338037030465	91.91338037030465	91.91338037030465	91.91338037030465	91.91338037030465	91.95272685162755	91.95272685162755	91.95272685162755	91.95272685162755	91.95272685162755	91.99207333295044	91.99207333295044	91.99207333295044	91.99207333295044	91.99207333295044	91.99207333295044	92.03141981427336	92.03141981427336	92.03141981427336	92.03141981427336	92.03141981427336	92.07076629559626	92.07076629559626	92.07076629559626	92.07076629559626	92.07076629559626	92.11011277691917	92.11011277691917	92.11011277691917	92.11011277691917	92.11011277691917	92.11011277691917	92.14945925824208	92.14945925824208	92.14945925824208	92.14945925824208	92.14945925824208	92.18880573956496	92.18880573956496	92.18880573956496	92.18880573956496	92.18880573956496	92.18880573956496	92.22815222088788	92.22815222088788	92.22815222088788	92.22815222088788	92.22815222088788	92.26749870221078	92.26749870221078	92.26749870221078	92.26749870221078	92.26749870221078	92.26749870221078	92.30684518353368	92.30684518353368	92.30684518353368	92.30684518353368	92.30684518353368	92.3461916648566	92.3461916648566	92.3461916648566	92.3461916648566	92.3461916648566	92.3461916648566	92.38553814617947	92.38553814617947	92.38553814617947	92.38553814617947	92.38553814617947	92.38553814617947	92.4248846275024	92.4248846275024	92.4248846275024	92.4248846275024	92.4248846275024	92.46423110882531	92.46423110882531	92.46423110882531	92.46423110882531	92.46423110882531	92.46423110882531	92.50357759014821	92.50357759014821	92.50357759014821	92.50357759014821	92.50357759014821	92.50357759014821	92.54292407147111	92.54292407147111	92.54292407147111	92.54292407147111	92.54292407147111	92.54292407147111	92.582270552794	92.582270552794	92.582270552794	92.582270552794	92.582270552794	92.582270552794	92.62161703411691	92.62161703411691	92.62161703411691	92.62161703411691	92.62161703411691	92.66096351543982	92.66096351543982	92.66096351543982	92.66096351543982	92.66096351543982	92.66096351543982	92.70030999676274	92.70030999676274	92.70030999676274	92.70030999676274	92.70030999676274	92.70030999676274	92.73965647808564	92.73965647808564	92.73965647808564	92.73965647808564	92.73965647808564	92.73965647808564	92.77900295940853	92.77900295940853	92.77900295940853	92.77900295940853	92.77900295940853	92.77900295940853	92.81834944073145	92.81834944073145	92.81834944073145	92.81834944073145	92.81834944073145	92.81834944073145	92.85769592205435	92.85769592205435	92.85769592205435	92.85769592205435	92.85769592205435	92.85769592205435	92.89704240337727	92.89704240337727	92.89704240337727	92.89704240337727	92.89704240337727	92.89704240337727	92.89704240337727	92.93638888470015	92.93638888470015	92.93638888470015	92.93638888470015	92.93638888470015	92.93638888470015	92.97573536602304	92.97573536602304	92.97573536602304	92.97573536602304	92.97573536602304	92.97573536602304	93.01508184734597	93.01508184734597	93.01508184734597	93.01508184734597	93.01508184734597	93.01508184734597	93.05442832866888	93.05442832866888	93.05442832866888	93.05442832866888	93.05442832866888	93.05442832866888	93.05442832866888	93.09377480999177	93.09377480999177	93.09377480999177	93.09377480999177	93.09377480999177	93.09377480999177	93.1331212913147	93.1331212913147	93.1331212913147	93.1331212913147	93.1331212913147	93.1331212913147	93.17246777263756	93.17246777263756	93.17246777263756	93.17246777263756	93.17246777263756	93.17246777263756	93.2118142539605	93.2118142539605	93.2118142539605	93.2118142539605	93.2118142539605	93.2118142539605	93.2511607352834	93.2511607352834	93.2511607352834	93.2511607352834	93.2511607352834	93.2511607352834	93.29050721660629	93.29050721660629	93.29050721660629	93.29050721660629	93.29050721660629	93.29050721660629	93.29050721660629	93.32985369792921	93.32985369792921	93.32985369792921	93.32985369792921	93.32985369792921	93.32985369792921	93.36920017925211	93.36920017925211	93.36920017925211	93.36920017925211	93.36920017925211	93.36920017925211	93.408546660575	93.408546660575	93.408546660575	93.408546660575	93.408546660575	93.408546660575	93.408546660575	93.4478931418979	93.4478931418979	93.4478931418979	93.4478931418979	93.4478931418979	93.4478931418979	93.48723962322084	93.48723962322084	93.48723962322084	93.48723962322084	93.48723962322084	93.48723962322084	93.5265861045437	93.5265861045437	93.5265861045437	93.5265861045437	93.5265861045437	93.5265861045437	93.5265861045437	93.56593258586662	93.56593258586662	93.56593258586662	93.56593258586662	93.56593258586662	93.56593258586662	93.60527906718953	93.60527906718953	93.60527906718953	93.60527906718953	93.60527906718953	93.60527906718953	93.60527906718953	93.64462554851247	93.64462554851247	93.64462554851247	93.64462554851247	93.64462554851247	93.64462554851247	93.68397202983535	93.68397202983535	93.68397202983535	93.68397202983535	93.68397202983535	93.68397202983535	93.72331851115824	93.72331851115824	93.72331851115824	93.72331851115824	93.72331851115824	93.72331851115824	93.72331851115824	93.76266499248115	93.76266499248115	93.76266499248115	93.76266499248115	93.76266499248115	93.76266499248115	93.80201147380404	93.80201147380404	93.80201147380404	93.80201147380404	93.80201147380404	93.80201147380404	93.80201147380404	93.84135795512697	93.84135795512697	93.84135795512697	93.84135795512697	93.84135795512697	93.84135795512697	93.88070443644986	93.88070443644986	93.88070443644986	93.88070443644986	93.88070443644986	93.88070443644986	93.92005091777277	93.92005091777277	93.92005091777277	93.92005091777277	93.92005091777277	93.92005091777277	93.92005091777277	93.95939739909568	93.95939739909568	93.95939739909568	93.95939739909568	93.95939739909568	93.95939739909568	93.99874388041858	93.99874388041858	93.99874388041858	93.99874388041858	93.99874388041858	93.99874388041858	94.03809036174148	94.03809036174148	94.03809036174148	94.03809036174148	94.03809036174148	94.03809036174148	94.07743684306436	94.07743684306436	94.07743684306436	94.07743684306436	94.07743684306436	94.07743684306436	94.1167833243873	94.1167833243873	94.1167833243873	94.1167833243873	94.1167833243873	94.1167833243873	94.1167833243873	94.1561298057102	94.1561298057102	94.1561298057102	94.1561298057102	94.1561298057102	94.1561298057102	94.19547628703309	94.19547628703309	94.19547628703309	94.19547628703309	94.19547628703309	94.19547628703309	94.234822768356	94.234822768356	94.234822768356	94.234822768356	94.234822768356	94.234822768356	94.2741692496789	94.2741692496789	94.2741692496789	94.2741692496789	94.2741692496789	94.2741692496789	94.31351573100181	94.31351573100181	94.31351573100181	94.31351573100181	94.31351573100181	94.31351573100181	94.35286221232468	94.35286221232468	94.35286221232468	94.35286221232468	94.35286221232468	94.35286221232468	94.39220869364763	94.39220869364763	94.39220869364763	94.39220869364763	94.39220869364763	94.39220869364763	94.39220869364763	94.43155517497052	94.43155517497052	94.43155517497052	94.43155517497052	94.43155517497052	94.43155517497052	94.47090165629344	94.47090165629344	94.47090165629344	94.47090165629344	94.47090165629344	94.47090165629344	94.51024813761633	94.51024813761633	94.51024813761633	94.51024813761633	94.51024813761633	94.51024813761633	94.54959461893923	94.54959461893923	94.54959461893923	94.54959461893923	94.54959461893923	94.54959461893923	94.58894110026215	94.58894110026215	94.58894110026215	94.58894110026215	94.58894110026215	94.58894110026215	94.58894110026215	94.62828758158504	94.62828758158504	94.62828758158504	94.62828758158504	94.62828758158504	94.62828758158504	94.66763406290796	94.66763406290796	94.66763406290796	94.66763406290796	94.66763406290796	94.66763406290796	94.66763406290796	94.70698054423085	94.70698054423085	94.70698054423085	94.70698054423085	94.70698054423085	94.70698054423085	94.74632702555377	94.74632702555377	94.74632702555377	94.74632702555377	94.74632702555377	94.74632702555377	94.74632702555377	94.78567350687668	94.78567350687668	94.78567350687668	94.78567350687668	94.78567350687668	94.78567350687668	94.78567350687668	94.82501998819957	94.82501998819957	94.82501998819957	94.82501998819957	94.82501998819957	94.82501998819957	94.82501998819957	94.86436646952247	94.86436646952247	94.86436646952247	94.86436646952247	94.86436646952247	94.86436646952247	94.86436646952247	94.90371295084538	94.90371295084538	94.90371295084538	94.90371295084538	94.90371295084538	94.90371295084538	94.90371295084538	94.90371295084538	94.9430594321683	94.9430594321683	94.9430594321683	94.9430594321683	94.9430594321683	94.9430594321683	94.9430594321683	94.98240591349116	94.98240591349116	94.98240591349116	94.98240591349116	94.98240591349116	94.98240591349116	94.98240591349116	95.02175239481409	95.02175239481409	95.02175239481409	95.02175239481409	95.02175239481409	95.02175239481409	95.02175239481409	95.02175239481409	95.061098876137	95.061098876137	95.061098876137	95.061098876137	95.061098876137	95.061098876137	95.061098876137	95.061098876137	95.10044535745986	95.10044535745986	95.10044535745986	95.10044535745986	95.10044535745986	95.10044535745986	95.10044535745986	95.10044535745986	95.13979183878278	95.13979183878278	95.13979183878278	95.13979183878278	95.13979183878278	95.13979183878278	95.13979183878278	95.13979183878278	95.17913832010569	95.17913832010569	95.17913832010569	95.17913832010569	95.17913832010569	95.17913832010569	95.17913832010569	95.2184848014286	95.2184848014286	95.2184848014286	95.2184848014286	95.2184848014286	95.2184848014286	95.2184848014286	95.2184848014286	95.2578312827515	95.2578312827515	95.2578312827515	95.2578312827515	95.2578312827515	95.2578312827515	95.2578312827515	95.29717776407443	95.29717776407443	95.29717776407443	95.29717776407443	95.29717776407443	95.29717776407443	95.29717776407443	95.3365242453973	95.3365242453973	95.3365242453973	95.3365242453973	95.3365242453973	95.3365242453973	95.3365242453973	95.37587072672021	95.37587072672021	95.37587072672021	95.37587072672021	95.37587072672021	95.37587072672021	95.41521720804315	95.41521720804315	95.41521720804315	95.41521720804315	95.41521720804315	95.41521720804315	95.454563689366	95.454563689366	95.454563689366	95.454563689366	95.454563689366	95.454563689366	95.454563689366	95.49391017068895	95.49391017068895	95.49391017068895	95.49391017068895	95.49391017068895	95.49391017068895	95.53325665201185	95.53325665201185	95.53325665201185	95.53325665201185	95.53325665201185	95.53325665201185	95.53325665201185	95.57260313333474	95.57260313333474	95.57260313333474	95.57260313333474	95.57260313333474	95.57260313333474	95.57260313333474	95.61194961465766	95.61194961465766	95.61194961465766	95.61194961465766	95.61194961465766	95.61194961465766	95.61194961465766	95.65129609598057	95.65129609598057	95.65129609598057	95.65129609598057	95.65129609598057	95.65129609598057	95.65129609598057	95.65129609598057	95.69064257730348	95.69064257730348	95.69064257730348	95.69064257730348	95.69064257730348	95.69064257730348	95.69064257730348	95.69064257730348	95.72998905862636	95.72998905862636	95.72998905862636	95.72998905862636	95.72998905862636	95.72998905862636	95.72998905862636	95.72998905862636	95.72998905862636	95.76933553994928	95.76933553994928	95.76933553994928	95.76933553994928	95.76933553994928	95.76933553994928	95.76933553994928	95.76933553994928	95.76933553994928	95.8086820212722	95.8086820212722	95.8086820212722	95.8086820212722	95.8086820212722	95.8086820212722	95.8086820212722	95.8086820212722	95.84802850259507	95.84802850259507	95.84802850259507	95.84802850259507	95.84802850259507	95.84802850259507	95.84802850259507	95.84802850259507	95.887374983918	95.887374983918	95.887374983918	95.887374983918	95.887374983918	95.887374983918	95.887374983918	95.887374983918	95.9267214652409	95.9267214652409	95.9267214652409	95.9267214652409	95.9267214652409	95.9267214652409	95.9267214652409	95.9267214652409	95.9660679465638	95.9660679465638	95.9660679465638	95.9660679465638	95.9660679465638	95.9660679465638	95.9660679465638	96.00541442788671	96.00541442788671	96.00541442788671	96.00541442788671	96.00541442788671	96.00541442788671	96.0447609092096	96.0447609092096	96.0447609092096	96.0447609092096	96.0447609092096	96.0447609092096	96.0447609092096	96.08410739053251	96.08410739053251	96.08410739053251	96.08410739053251	96.08410739053251	96.08410739053251	96.08410739053251	96.1234538718554	96.1234538718554	96.1234538718554	96.1234538718554	96.1234538718554	96.1234538718554	96.16280035317831	96.16280035317831	96.16280035317831	96.16280035317831	96.16280035317831	96.16280035317831	96.20214683450122	96.20214683450122	96.20214683450122	96.20214683450122	96.20214683450122	96.24149331582413	96.24149331582413	96.24149331582413	96.24149331582413	96.24149331582413	96.24149331582413	96.28083979714703	96.28083979714703	96.28083979714703	96.28083979714703	96.28083979714703	96.32018627846993	96.32018627846993	96.32018627846993	96.32018627846993	96.32018627846993	96.32018627846993	96.35953275979283	96.35953275979283	96.35953275979283	96.35953275979283	96.35953275979283	96.39887924111576	96.39887924111576	96.39887924111576	96.39887924111576	96.39887924111576	96.39887924111576	96.43822572243865	96.43822572243865	96.43822572243865	96.43822572243865	96.43822572243865	96.47757220376154	96.47757220376154	96.47757220376154	96.47757220376154	96.47757220376154	96.47757220376154	96.51691868508446	96.51691868508446	96.51691868508446	96.51691868508446	96.51691868508446	96.55626516640737	96.55626516640737	96.55626516640737	96.55626516640737	96.55626516640737	96.55626516640737	96.59561164773027	96.59561164773027	96.59561164773027	96.59561164773027	96.59561164773027	96.59561164773027	96.63495812905316	96.63495812905316	96.63495812905316	96.63495812905316	96.63495812905316	96.63495812905316	96.63495812905316	96.67430461037608	96.67430461037608	96.67430461037608	96.67430461037608	96.67430461037608	96.67430461037608	96.67430461037608	96.713651091699	96.713651091699	96.713651091699	96.713651091699	96.713651091699	96.713651091699	96.713651091699	96.75299757302186	96.75299757302186	96.75299757302186	96.75299757302186	96.75299757302186	96.75299757302186	96.75299757302186	96.7923440543448	96.7923440543448	96.7923440543448	96.7923440543448	96.7923440543448	96.7923440543448	96.7923440543448	96.7923440543448	96.8316905356677	96.8316905356677	96.8316905356677	96.8316905356677	96.8316905356677	96.8316905356677	96.8316905356677	96.8316905356677	96.87103701699057	96.87103701699057	96.87103701699057	96.87103701699057	96.87103701699057	96.87103701699057	96.87103701699057	96.87103701699057	96.87103701699057	96.9103834983135	96.9103834983135	96.9103834983135	96.9103834983135	96.9103834983135	96.9103834983135	96.9103834983135	96.9103834983135	96.9103834983135	96.9497299796364	96.9497299796364	96.9497299796364	96.9497299796364	96.9497299796364	96.9497299796364	96.9497299796364	96.9497299796364	96.9497299796364	96.98907646095931	96.98907646095931	96.98907646095931	96.98907646095931	96.98907646095931	96.98907646095931	96.98907646095931	96.98907646095931	96.98907646095931	96.98907646095931	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.02842294228221	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.06776942360512	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.10711590492803	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.14646238625092	97.18580886757381	97.18580886757381	97.18580886757381	97.18580886757381	97.18580886757381	97.18580886757381	97.18580886757381	97.18580886757381	97.18580886757381	97.18580886757381	97.22515534889675	97.22515534889675	97.22515534889675	97.22515534889675	97.22515534889675	97.22515534889675	97.22515534889675	97.22515534889675	97.22515534889675	97.26450183021964	97.26450183021964	97.26450183021964	97.26450183021964	97.26450183021964	97.26450183021964	97.26450183021964	97.26450183021964	97.30384831154254	97.30384831154254	97.30384831154254	97.30384831154254	97.30384831154254	97.30384831154254	97.30384831154254	97.34319479286546	97.34319479286546	97.34319479286546	97.34319479286546	97.34319479286546	97.34319479286546	97.34319479286546	97.38254127418834	97.38254127418834	97.38254127418834	97.38254127418834	97.38254127418834	97.38254127418834	97.38254127418834	97.42188775551125	97.42188775551125	97.42188775551125	97.42188775551125	97.42188775551125	97.42188775551125	97.42188775551125	97.46123423683417	97.46123423683417	97.46123423683417	97.46123423683417	97.46123423683417	97.46123423683417	97.46123423683417	97.50058071815707	97.50058071815707	97.50058071815707	97.50058071815707	97.50058071815707	97.50058071815707	97.50058071815707	97.53992719947998	97.53992719947998	97.53992719947998	97.53992719947998	97.53992719947998	97.53992719947998	97.53992719947998	97.5792736808029	97.5792736808029	97.5792736808029	97.5792736808029	97.5792736808029	97.5792736808029	97.5792736808029	97.61862016212578	97.61862016212578	97.61862016212578	97.61862016212578	97.61862016212578	97.61862016212578	97.61862016212578	97.65796664344868	97.65796664344868	97.65796664344868	97.65796664344868	97.65796664344868	97.65796664344868	97.65796664344868	97.6973131247716	97.6973131247716	97.6973131247716	97.6973131247716	97.6973131247716	97.6973131247716	97.7366596060945	97.7366596060945	97.7366596060945	97.7366596060945	97.7366596060945	97.7366596060945	97.7366596060945	97.7760060874174	97.7760060874174	97.7760060874174	97.7760060874174	97.7760060874174	97.7760060874174	97.7760060874174	97.7760060874174	97.81535256874031	97.81535256874031	97.81535256874031	97.81535256874031	97.81535256874031	97.81535256874031	97.81535256874031	97.81535256874031	97.85469905006321	97.85469905006321	97.85469905006321	97.85469905006321	97.85469905006321	97.85469905006321	97.85469905006321	97.85469905006321	97.85469905006321	97.85469905006321	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.89404553138611	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.93339201270899	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	97.9727384940319	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.01208497535481	98.05143145667772	98.05143145667772	98.05143145667772	98.05143145667772	98.05143145667772	98.05143145667772	98.05143145667772	98.05143145667772	98.05143145667772	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.09077793800063	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.13012441932356	98.16947090064643	98.16947090064643	98.16947090064643	98.16947090064643	98.16947090064643	98.20881738196935	98.20881738196935	98.20881738196935	98.20881738196935	98.24816386329227	98.24816386329227	98.24816386329227	98.28751034461517	98.28751034461517	98.28751034461517	98.28751034461517	98.32685682593807	98.32685682593807	98.32685682593807	98.36620330726097	98.36620330726097	98.36620330726097	98.40554978858387	98.40554978858387	98.4448962699068	98.4448962699068	98.4448962699068	98.48424275122968	98.48424275122968	98.48424275122968	98.52358923255258	98.52358923255258	98.52358923255258	98.56293571387548	98.56293571387548	98.56293571387548	98.60228219519838	98.60228219519838	98.60228219519838	98.64162867652131	98.64162867652131	98.64162867652131	98.64162867652131	98.68097515784417	98.68097515784417	98.68097515784417	98.68097515784417	98.7203216391671	98.7203216391671	98.7203216391671	98.7203216391671	98.75966812049001	98.75966812049001	98.75966812049001	98.75966812049001	98.7990146018129	98.7990146018129	98.7990146018129	98.7990146018129	98.7990146018129	98.83836108313581	98.83836108313581	98.83836108313581	98.83836108313581	98.83836108313581	98.83836108313581	98.83836108313581	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.8777075644587	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.91705404578162	98.95640052710452	98.95640052710452	98.95640052710452	98.95640052710452	98.95640052710452	98.95640052710452	98.95640052710452	98.99574700842743	98.99574700842743	98.99574700842743	98.99574700842743	98.99574700842743	98.99574700842743	99.03509348975036	99.03509348975036	99.03509348975036	99.03509348975036	99.03509348975036	99.07443997107324	99.07443997107324	99.07443997107324	99.07443997107324	99.07443997107324	99.11378645239614	99.11378645239614	99.11378645239614	99.11378645239614	99.11378645239614	99.15313293371904	99.15313293371904	99.15313293371904	99.15313293371904	99.15313293371904	99.19247941504194	99.19247941504194	99.19247941504194	99.19247941504194	99.19247941504194	99.19247941504194	99.23182589636487	99.23182589636487	99.23182589636487	99.23182589636487	99.23182589636487	99.23182589636487	99.27117237768776	99.27117237768776	99.27117237768776	99.27117237768776	99.27117237768776	99.27117237768776	99.27117237768776	99.27117237768776	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.31051885901067	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.34986534033357	99.38921182165647	99.38921182165647	99.38921182165647	99.38921182165647	99.38921182165647	99.38921182165647	99.38921182165647	99.38921182165647	99.38921182165647	99.42855830297937	99.42855830297937	99.42855830297937	99.42855830297937	99.42855830297937	99.42855830297937	99.42855830297937	99.42855830297937	99.4679047843023	99.4679047843023	99.4679047843023	99.4679047843023	99.4679047843023	99.4679047843023	99.4679047843023	99.5072512656252	99.5072512656252	99.5072512656252	99.5072512656252	99.5072512656252	99.5072512656252	99.5072512656252	99.5465977469481	99.5465977469481	99.5465977469481	99.5465977469481	99.5465977469481	99.5465977469481	99.5465977469481	99.585944228271	99.585944228271	99.585944228271	99.585944228271	99.585944228271	99.585944228271	99.585944228271	99.585944228271	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.6252907095939	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.66463719091681	99.70398367223971	99.70398367223971	99.70398367223971	99.70398367223971	99.70398367223971	99.7433301535626	99.7433301535626	99.7433301535626	99.7433301535626	99.78267663488552	99.78267663488552	99.78267663488552	99.78267663488552	99.82202311620841	99.82202311620841	99.82202311620841	99.82202311620841	99.86136959753134	99.86136959753134	99.86136959753134	99.90071607885423	99.90071607885423	99.90071607885423	99.94006256017715	99.94006256017715	99.94006256017715	99.97940904150004	99.97940904150004	99.97940904150004	100.018755522823	100.018755522823	100.018755522823	100.0581020041459	100.0581020041459	100.0581020041459	100.0581020041459	100.0974484854688	100.0974484854688	100.0974484854688	100.1367949667917	100.1367949667917	100.1367949667917	100.1367949667917	100.1367949667917	100.1761414481146	100.1761414481146	100.1761414481146	100.1761414481146	100.1761414481146	100.2154879294375	100.2154879294375	100.2154879294375	100.2154879294375	100.2154879294375	100.2154879294375	100.2154879294375	100.2154879294375	100.2548344107604	100.2548344107604	100.2548344107604	100.2548344107604	100.2548344107604	100.2548344107604	100.2548344107604	100.2548344107604	100.2548344107604	100.2548344107604	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.2941808920833	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3335273734062	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.3728738547291	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.412220336052	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4515668173749	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.4909132986978	100.5302597800207	100.5302597800207	100.5302597800207	100.5302597800207	100.5302597800207	100.5302597800207	100.5302597800207	100.5696062613436	100.5696062613436	100.5696062613436	100.5696062613436	100.6089527426665	100.6089527426665	100.6089527426665	100.6089527426665	100.6482992239894	100.6482992239894	100.6482992239894	100.6482992239894	100.6876457053123	100.6876457053123	100.6876457053123	100.7269921866352	100.7269921866352	100.7269921866352	100.7663386679581	100.7663386679581	100.7663386679581	100.805685149281	100.805685149281	100.805685149281	100.8450316306039	100.8450316306039	100.8450316306039	100.8843781119268	100.8843781119268	100.8843781119268	100.9237245932498	100.9237245932498	100.9237245932498	100.9630710745727	100.9630710745727	100.9630710745727	100.9630710745727	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	100.9630710745727	100.9630710745727	100.9630710745727	100.9630710745727	100.9237245932498	100.9237245932498	100.9237245932498	100.9237245932498	100.8843781119268	100.8843781119268	100.8843781119268	100.8843781119268	100.8450316306039	100.8450316306039	100.8450316306039	100.8450316306039	100.805685149281	100.805685149281	100.805685149281	100.805685149281	100.7663386679581	100.7663386679581	100.7663386679581	100.7663386679581	100.7269921866352	100.7269921866352	100.7269921866352	100.7269921866352	100.7269921866352	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6482992239894	100.6482992239894	100.6482992239894	100.6482992239894	100.6482992239894	100.6482992239894	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.6876457053123	100.7269921866352	100.7269921866352	100.7269921866352	100.7269921866352	100.7269921866352	100.7269921866352	100.7269921866352	100.7663386679581	100.7663386679581	100.7663386679581	100.7663386679581	100.7663386679581	100.7663386679581	100.805685149281	100.805685149281	100.805685149281	100.805685149281	100.805685149281	100.805685149281	100.8450316306039	100.8450316306039	100.8450316306039	100.8450316306039	100.8450316306039	100.8450316306039	100.8843781119268	100.8843781119268	100.8843781119268	100.8843781119268	100.8843781119268	100.8843781119268	100.9237245932498	100.9237245932498	100.9237245932498	100.9237245932498	100.9237245932498	100.9237245932498	100.9630710745727	100.9630710745727	100.9630710745727	100.9630710745727	100.9630710745727	100.9630710745727	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0024175558956	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0417640372185	101.0811105185414	101.0811105185414	101.0811105185414	101.0811105185414	101.0811105185414	101.0811105185414	101.0811105185414	101.0811105185414	101.1204569998643	101.1204569998643	101.1204569998643	101.1204569998643	101.1204569998643	101.1204569998643	101.1204569998643	101.1598034811872	101.1598034811872	101.1598034811872	101.1598034811872	101.1598034811872	101.1598034811872	101.1598034811872	101.1598034811872	101.1991499625101	101.1991499625101	101.1991499625101	101.1991499625101	101.1991499625101	101.1991499625101	101.1991499625101	101.1991499625101	101.238496443833	101.238496443833	101.238496443833	101.238496443833	101.238496443833	101.238496443833	101.238496443833	101.238496443833	101.238496443833	101.2778429251559	101.2778429251559	101.2778429251559	101.2778429251559	101.2778429251559	101.2778429251559	101.2778429251559	101.2778429251559	101.2778429251559	101.2778429251559	101.3171894064788	101.3171894064788	101.3171894064788	101.3171894064788	101.3171894064788	101.3171894064788	101.3171894064788	101.3171894064788	101.3171894064788	101.3171894064788	101.3565358878017	101.3565358878017	101.3565358878017	101.3565358878017	101.3565358878017	101.3565358878017	101.3565358878017	101.3565358878017	101.3565358878017	101.3565358878017	101.3958823691246	101.3958823691246	101.3958823691246	101.3958823691246	101.3958823691246	101.3958823691246	101.3958823691246	101.3958823691246	101.3958823691246	101.3958823691246	101.4352288504475	101.4352288504475	101.4352288504475	101.4352288504475	101.4352288504475	101.4352288504475	101.4352288504475	101.4352288504475	101.4352288504475	101.4352288504475	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.4745753317704	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5139218130933	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5532682944162	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.5926147757391	101.631961257062	101.631961257062	101.631961257062	101.631961257062	101.631961257062	101.631961257062	101.631961257062	101.631961257062	101.631961257062	101.6713077383849	101.6713077383849	101.6713077383849	101.6713077383849	101.6713077383849	101.6713077383849	101.6713077383849	101.7106542197078	101.7106542197078	101.7106542197078	101.7106542197078	101.7106542197078	101.7106542197078	101.7106542197078	101.7500007010307	101.7500007010307	101.7500007010307	101.7500007010307	101.7500007010307	101.7893471823537	101.7893471823537	101.7893471823537	101.7893471823537	101.7893471823537	101.7893471823537	101.8286936636766	101.8286936636766	101.8286936636766	101.8286936636766	101.8286936636766	101.8286936636766	101.8680401449995	101.8680401449995	101.8680401449995	101.8680401449995	101.8680401449995	101.8680401449995	101.8680401449995	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9073866263224	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9467331076453	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	101.9860795889682	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.0254260702911	102.064772551614	102.064772551614	102.064772551614	102.064772551614	102.064772551614	102.1041190329369	102.1041190329369	102.1041190329369	102.1041190329369	102.1041190329369	102.1041190329369	102.1434655142598	102.1434655142598	102.1434655142598	102.1434655142598	102.1434655142598	102.1828119955827	102.1828119955827	102.1828119955827	102.1828119955827	102.1828119955827	102.1828119955827	102.2221584769056	102.2221584769056	102.2221584769056	102.2221584769056	102.2221584769056	102.2221584769056	102.2615049582285	102.2615049582285	102.2615049582285	102.2615049582285	102.2615049582285	102.2615049582285	102.2615049582285	102.3008514395514	102.3008514395514	102.3008514395514	102.3008514395514	102.3008514395514	102.3008514395514	102.3008514395514	102.3008514395514	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3401979208743	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.3795444021972	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5762768088117	102.5762768088117	102.5762768088117	102.5762768088117	102.5762768088117	102.5762768088117	102.5762768088117	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6943162527805	102.6943162527805	102.6943162527805	102.6943162527805	102.6943162527805	102.6943162527805	102.6943162527805	102.6943162527805	102.6943162527805	102.7336627341034	102.7336627341034	102.7336627341034	102.7336627341034	102.7336627341034	102.7730092154263	102.7730092154263	102.7730092154263	102.7730092154263	102.7730092154263	102.8123556967492	102.8123556967492	102.8123556967492	102.8123556967492	102.8517021780721	102.8517021780721	102.8517021780721	102.891048659395	102.891048659395	102.891048659395	102.930395140718	102.930395140718	102.930395140718	102.9697416220408	102.9697416220408	102.9697416220408	103.0090881033637	103.0090881033637	103.0090881033637	103.0484345846866	103.0484345846866	103.0484345846866	103.0877810660095	103.0877810660095	103.0877810660095	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1664740286553	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.0877810660095	103.0877810660095	103.0877810660095	103.0484345846866	103.0484345846866	103.0484345846866	103.0090881033637	103.0090881033637	103.0090881033637	102.9697416220408	102.9697416220408	102.930395140718	102.930395140718	102.891048659395	102.891048659395	102.891048659395	102.8517021780721	102.8517021780721	102.8123556967492	102.8123556967492	102.7730092154263	102.7730092154263	102.7336627341034	102.7336627341034	102.6943162527805	102.6943162527805	102.6943162527805	102.6549697714575	102.6549697714575	102.6156232901346	102.6156232901346	102.5762768088117	102.5762768088117	102.5369303274888	102.5369303274888	102.5369303274888	102.497583846166	102.497583846166	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.4188908835201	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.458237364843	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.497583846166	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5369303274888	102.5762768088117	102.5762768088117	102.5762768088117	102.5762768088117	102.5762768088117	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6156232901346	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6549697714575	102.6943162527805	102.6943162527805	102.6943162527805	102.6943162527805	102.7336627341034	102.7336627341034	102.7336627341034	102.7336627341034	102.7336627341034	102.7730092154263	102.7730092154263	102.7730092154263	102.7730092154263	102.8123556967492	102.8123556967492	102.8123556967492	102.8123556967492	102.8123556967492	102.8517021780721	102.8517021780721	102.8517021780721	102.8517021780721	102.8517021780721	102.891048659395	102.891048659395	102.891048659395	102.891048659395	102.930395140718	102.930395140718	102.930395140718	102.930395140718	102.930395140718	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2451669913011	103.2451669913011	103.2451669913011	103.2451669913011	103.2451669913011	103.2451669913011	103.284513472624	103.284513472624	103.284513472624	103.284513472624	103.284513472624	103.284513472624	103.3238599539469	103.3238599539469	103.3238599539469	103.3238599539469	103.3238599539469	103.3238599539469	103.3632064352698	103.3632064352698	103.3632064352698	103.3632064352698	103.3632064352698	103.3632064352698	103.3632064352698	103.3632064352698	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.6779782858531	103.6779782858531	103.6779782858531	103.6386318045302	103.6386318045302	103.6386318045302	103.5992853232073	103.5992853232073	103.5599388418843	103.5599388418843	103.5599388418843	103.5205923605615	103.5205923605615	103.4812458792385	103.4812458792385	103.4418993979156	103.4418993979156	103.4025529165927	103.4025529165927	103.4025529165927	103.3632064352698	103.3632064352698	103.3238599539469	103.3238599539469	103.284513472624	103.284513472624	103.2451669913011	103.2451669913011	103.2451669913011	103.2058205099782	103.2058205099782	103.1664740286553	103.1664740286553	103.1271275473324	103.1271275473324	103.1271275473324	103.0877810660095	103.0877810660095	103.0877810660095	103.0484345846866	103.0484345846866	103.0484345846866	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	102.9697416220408	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0090881033637	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0484345846866	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.0877810660095	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1271275473324	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.1664740286553	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2058205099782	103.2451669913011	103.2451669913011	103.2451669913011	103.2451669913011	103.2451669913011	103.2451669913011	103.284513472624	103.284513472624	103.284513472624	103.284513472624	103.284513472624	103.284513472624	103.3238599539469	103.3238599539469	103.3238599539469	103.3238599539469	103.3238599539469	103.3238599539469	103.3632064352698	103.3632064352698	103.3632064352698	103.3632064352698	103.3632064352698	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4025529165927	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4418993979156	103.4812458792385	103.4812458792385	103.4812458792385	103.4812458792385	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5205923605615	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5599388418843	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.5992853232073	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6386318045302	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.6779782858531	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.717324767176	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7566712484989	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.7960177298218	103.8353642111447	103.8353642111447	103.8353642111447	103.8353642111447	103.8747106924676	103.8747106924676	103.8747106924676	103.8747106924676	103.8747106924676	103.8747106924676	103.8747106924676	103.8747106924676	103.9140571737905	103.9140571737905	103.9140571737905	103.9140571737905	103.9140571737905	103.9140571737905	103.9140571737905	103.9140571737905	103.9140571737905	103.9140571737905	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9534036551134	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	103.9927501364363	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0320966177592	104.0714430990821	104.0714430990821	104.0714430990821	104.0714430990821	104.0714430990821	104.0714430990821	104.0714430990821	104.0714430990821	104.0714430990821	104.110789580405	104.110789580405	104.110789580405	104.110789580405	104.110789580405	104.110789580405	104.1501360617279	104.1501360617279	104.1501360617279	104.1501360617279	104.1501360617279	104.1501360617279	104.1501360617279	104.1894825430508	104.1894825430508	104.1894825430508	104.1894825430508	104.1894825430508	104.2288290243737	104.2288290243737	104.2288290243737	104.2288290243737	104.2288290243737	104.2288290243737	104.2681755056966	104.2681755056966	104.2681755056966	104.2681755056966	104.2681755056966	104.2681755056966	104.2681755056966	104.3075219870195	104.3075219870195	104.3075219870195	104.3075219870195	104.3075219870195	104.3075219870195	104.3468684683424	104.3468684683424	104.3468684683424	104.3468684683424	104.3468684683424	104.3468684683424	104.3468684683424	104.3468684683424	104.3862149496653	104.3862149496653	104.3862149496653	104.3862149496653	104.3862149496653	104.3862149496653	104.3862149496653	104.3862149496653	104.3862149496653	104.3862149496653	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4255614309883	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.4649079123111	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.5042543936341	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.543600874957	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.5829473562799	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6222938376028	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.6616403189257	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.7009868002486	104.6616403189257	104.6616403189257	104.6616403189257	104.6222938376028	104.6222938376028	104.6222938376028	104.5829473562799	104.5829473562799	104.543600874957	104.5042543936341	104.5042543936341	104.4649079123111	104.4255614309883	104.3862149496653	104.3075219870195	104.2288290243737	104.110789580405	103.9140571737905	101.3171894064788	100.5302597800207	99.585944228271	94.74632702555377	42.49419982873674	-0.118039443968713	-2.911639617894925	-2.911639617894925	-2.793600173926212	-2.832946655249116	-2.990332580540734	-2.950986099217828	-2.911639617894925	-2.911639617894925	-2.950986099217828	-2.950986099217828	-2.911639617894925	-2.950986099217828	-2.990332580540734	-2.950986099217828	-2.911639617894925	-2.950986099217828	-2.911639617894925	-2.911639617894925	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.911639617894925	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.911639617894925	-2.950986099217828	-2.950986099217828	-2.950986099217828	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.950986099217828	-2.950986099217828	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	-2.911639617894925	Strain


Stress  (MPa)




Load vs extension of all materials
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Load  (KN)




Load vs extension of 0.1% and 0.29% carbon steel
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Load  (KN)




0.1 vs 0.29 carbon steel stress strain curve
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Stress MPa



0.29% carbon steel Proof stress
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