Structural Integrity and Materials Evaluation

Ultrasonic Testing Review Questions.

Question 1.

- In an immersion tank ultrasonic testing system, as illustrated in the figure below, determine the sound energy distribution at the locations indicated.

- In the same system, determine the incident angle required to generate a 45o compression wave in the aluminium block.

- Explain why refraction of the signal occurs at the first material interface with increasing angles of incidence.

- Determine the first critical angle that results in a pure shear wave being present in the aluminium block.

Question 2.

A 3.5MHz conventional ultrasonic transducer is to be used to gauge thickness in mild steel.

- Determine the thickness required of a PZT crystal to produce a resonant frequency of 3.5MHz, given that the compression wave velocity for PZT is 3000 m/s.

- Assuming for the aforementioned crystal that it has a diameter of 6mm, determine the crystals near field distance when transmitting into Perspex.

- Assuming the crystal is in contact with a mild steel surface.  Calculate the 6dB beam width for the crystal at a thickness in mild steel of 25mm.

- Calculate the wavelength of the signal in mild steel.  What are the implications with regard defect sensitivity?