Tensile Testing

University of Wales Trinity Saint David

School of Engineering

Charlie Gallagher

2416608

BEng (Hons) Manufacturing Systems Engineering

30/06/25

Engineering Science

ACMA4028

1697

# Table of Contents

Table of Contents	i

List of Figures	i

1	Introduction	1

2	Testing Procedure	2

3	Results	4

4	Analysis	5

5	Conclusion	15

5.1	Steel	15

5.2	Aluminium	15

5.3	Duralumin	16

5.4	PVC	16

6	Evaluation	17

8	Further Work	18

6	References	19

# List of Figures

Figure 1: Specimen Measurement Guide	2

Figure 2:TecQuipment ES6 Tensile Tester	2

Figure 3:Tensile Tester Dial to 0	3

Figure 4: Diagram Displaying Strain	6

Figure 5: Diagram Displaying Stress	6

Figure 6: Graph Displaying Stress-Strain for Steel	7

Figure 7: Graph Displaying Steel Stress-Strain for Young's Modulus Calculation	7

Figure 8:Graph Displaying Young's Modulus Calculation	7

Figure 9:Graph Displaying Stress-Strain for Aluminium	9

Figure 10:Graph Displaying Aluminium Stress-Strain for Young's Modulus Calculation	9

Figure 11:Graph Displaying Stress-Strain for Duralumin	11

Figure 12:Graph Displaying Duralumin Stress-Strain for Young's Modulus Calculation	11

Figure 13:Graph Displaying Stress-Strain for PVC	13

Figure 14:Graph Displaying PVC Stress-Strain for Young's Modulus Calculation	13

Table 1:Raw Test Data	4

Table 2:Table Displaying Specimen Measurements	5

Table 3: Steel Analysed Data	6

Table 4: Aluminium Analysed Data	9

Table 5: Duralumin Analysed Data	11

Table 6: PVC Analysed Data	13

Equation 1:Strain Equation	7

Equation 2: Stress Equation	7

# Introduction

This assignment aims to demonstrate the process of conducting a tensile test experiment using four different materials, while logging the data and plotting graphs to display the results in the form of Stress-Strain Diagrams. The equipment used in the experiment was a TecQuipment ES6 Tensile Tester Kit, and the four materials used are Steel, Aluminium, Duralumin, and PVC. A tensile test is the test of a material's capabilities. A piece of material gets placed between 2 grips and pulled in opposite directions to put the part under stress until it eventually fractures and breaks. From this test, you’re able to find the stress, strain, Young's modulus, and elongation. Also, by creating stress-strain diagrams, you can also find its yield point and see how it acts under load over time. (TecQuipment, 2012)

Tensile testing is important to help engineers understand how materials will act when put in certain environments. Some examples of where it’s used are in manufacturing to verify that materials meet standards for certain parts and functions. Quality assurance may use tensile testing to ensure that the current products meet the expected standard of their product. An example of a product that goes through rigorous tensile testing is road tires. Engineers must ensure that they can withstand endless inconsistencies in the road and different weather conditions, constantly applying different forces to the material over a long period of time (Instron, n.d.).

# Testing Procedure

- Take measurements of the specimen. Measure the Width, Thickness and Gauge Length (Figure 1).

- Secure the specimen to the tester using the 2 grips (Figure 2) and set the dial to zero (Figure 3).

- Take measurements following the testing guide. Here it was 0.2mm until 5mm, 1mm until 10mm and finally 10mm until break.

- Once the test has been completed and all test points have been recorded, remove the specimen and record the gauge length after the test.

- Repeat this process with all 4 materials.

Figure 1: Specimen Measurement Guide

Figure 2:TecQuipment ES6 Tensile Tester

Figure 3:Tensile Tester Dial to 0

# Results

Table 1 below presents the raw data from the experiment. Column A detailing the Load Nut Movements starting in increments of 0.2mm, then increasing to 1mm, then by 10mm. Columns B, C, D, and E show the Dial Indicator reading for each material at each Load Nut position.

Table 1:Raw Test Data

|  | Dial Indicator (mm) |  |  |  |
| --- | --- | --- | --- | --- |
| Load Nut (mm) | Steel | Aluminium | Duralumin | PVC |
| 0 | 0 | 0 | 0 | 0 |
| 0.2 | 0.18 | 0.15 | 0.17 | 0.06 |
| 0.4 | 0.36 | 0.33 | 0.36 | 0.11 |
| 0.6 | 0.55 | 0.5 | 0.55 | 0.16 |
| 0.8 | 0.74 | 0.67 | 0.73 | 0.22 |
| 1 | 0.92 | 0.85 | 0.89 | 0.24 |
| 1.2 | 1.1 | 1.02 | 1.05 | 0.25 |
| 1.4 | 1.28 | 1.19 | 1.25 | 0.18 |
| 1.6 | 1.46 | 1.36 | 1.41 | 0.19 |
| 1.8 | 1.64 | 1.54 | 1.61 | 0.16 |
| 2 | 1.83 | 1.7 | 1.77 | 0.15 |
| 2.2 | 2 | 1.85 | 1.95 | 0.15 |
| 2.4 | 2.37 | 1.95 | 2.13 | 0.15 |
| 2.6 | 2.44 | 2.07 | 2.29 | 0.14 |
| 2.8 | 2.53 | 2.18 | 2.47 | 0.13 |
| 3 | 2.69 | 2.24 | 2.66 | 0.12 |
| 3.2 | 2.86 | 2.33 | 2.84 | 0.12 |
| 3.4 | 3 | 2.42 | 3.01 | 0.12 |
| 3.6 | 3.13 | 2.46 | 3.19 | 0.12 |
| 3.8 | 3.25 | 2.55 | 3.36 | 0.12 |
| 4 | 3.38 | 2.59 | 3.54 | 0.12 |
| 4.2 | 3.51 | 2.63 | 3.69 | 0.12 |
| 4.4 | 3.62 | 2.65 | 3.85 | 0.14 |
| 4.6 | 3.74 | 2.68 | 4.04 | 0.12 |
| 4.8 | 3.84 |  | 4.21 | 0.2 |
| 5 | 3.96 |  | 4.39 | 0.17 |
| 6 | 4.39 |  | 4.91 | 0.18 |
| 7 | 4.75 |  | 5.09 | 0.16 |
| 8 | 4.99 |  |  | 0.15 |
| 9 | 5.14 |  |  | 0.15 |
| 10 | 5.2 |  |  | 0.15 |
| 20 |  |  |  | 0.14 |
| 30 |  |  |  | 0.13 |
| 40 |  |  |  | 0.12 |
| 50 |  |  |  |  |
| 60 |  |  |  |  |

# Analysis

Table 2:Table Displaying Specimen Measurements

| Steel |  | Aluminium |  | Duralumin |  | PVC |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Width (mm) | 2 | Width (mm) | 2 | Width (mm) | 2 | Width (mm) | 1.9 |
| Thickness (mm) | 0.94 | Thickness (mm) | 1 | Thickness (mm) | 1 | Thickness (mm) | 1 |
| Area (m²) | 0.00000188 | Area (m^2) | 0.000002 | Area (m^2) | 0.000002 | Area (m^2) | 0.0000019 |
| Length (mm) | 30.7 | Length (mm) | 31 | Length (mm) | 31 | Length (mm) | 31 |
| Final Length (mm) | 35.6 | Final Length (mm) | 33 | Final Length (mm) | 32.1 | Final Length (mm) | 53.4 |
| Elongation (%) | 15.96091205 | Elongation (%) | 6.451612903 | Elongation (%) | 3.548387097 | Elongation (%) | 72.25806452 |

Table 3: Steel Analysed Data

| Steel |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Load Nut (mm) | Dial Indicator (mm) | Force (N) | Extension (mm) | Nominal Strain | Stress (MPa) |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.2 | 0.18 | 18 | 0.02 | 0.000651466 | 9.574468085 |
| 0.4 | 0.36 | 36 | 0.04 | 0.001302932 | 19.14893617 |
| 0.6 | 0.55 | 55 | 0.05 | 0.001628664 | 29.25531915 |
| 0.8 | 0.74 | 74 | 0.06 | 0.001954397 | 39.36170213 |
| 1 | 0.92 | 92 | 0.08 | 0.002605863 | 48.93617021 |
| 1.2 | 1.1 | 110 | 0.1 | 0.003257329 | 58.5106383 |
| 1.4 | 1.28 | 128 | 0.12 | 0.003908795 | 68.08510638 |
| 1.6 | 1.46 | 146 | 0.14 | 0.004560261 | 77.65957447 |
| 1.8 | 1.64 | 164 | 0.16 | 0.005211726 | 87.23404255 |
| 2 | 1.83 | 183 | 0.17 | 0.005537459 | 97.34042553 |
| 2.2 | 2 | 200 | 0.2 | 0.006514658 | 106.3829787 |
| 2.4 | 2.37 | 237 | 0.03 | 0.000977199 | 126.0638298 |
| 2.6 | 2.44 | 244 | 0.16 | 0.005211726 | 129.787234 |
| 2.8 | 2.53 | 253 | 0.27 | 0.008794788 | 134.5744681 |
| 3 | 2.69 | 269 | 0.31 | 0.01009772 | 143.0851064 |
| 3.2 | 2.86 | 286 | 0.34 | 0.011074919 | 152.1276596 |
| 3.4 | 3 | 300 | 0.4 | 0.013029316 | 159.5744681 |
| 3.6 | 3.13 | 313 | 0.47 | 0.015309446 | 166.4893617 |
| 3.8 | 3.25 | 325 | 0.55 | 0.017915309 | 172.8723404 |
| 4 | 3.38 | 338 | 0.62 | 0.02019544 | 179.787234 |
| 4.2 | 3.51 | 351 | 0.69 | 0.02247557 | 186.7021277 |
| 4.4 | 3.62 | 362 | 0.78 | 0.025407166 | 192.5531915 |
| 4.6 | 3.74 | 374 | 0.86 | 0.028013029 | 198.9361702 |
| 4.8 | 3.84 | 384 | 0.96 | 0.031270358 | 204.2553191 |
| 5 | 3.96 | 396 | 1.04 | 0.033876221 | 210.6382979 |
| 6 | 4.39 | 439 | 1.61 | 0.052442997 | 233.5106383 |
| 7 | 4.75 | 475 | 2.25 | 0.073289902 | 252.6595745 |
| 8 | 4.99 | 499 | 3.01 | 0.098045603 | 265.4255319 |
| 9 | 5.14 | 514 | 3.86 | 0.125732899 | 273.4042553 |
| 10 | 5.2 | 520 | 4.8 | 0.156351792 | 276.5957447 |
| 11 | 5.25 | 525 | 5.75 | 0.187296417 | 279.2553191 |
| 12 | 5.28 | 528 | 6.72 | 0.218892508 | 280.8510638 |
| 40 |  | 0 | 40 |  | 0 |
| 50 |  | 0 | 50 |  | 0 |
| 60 |  | 0 | 60 |  | 0 |

Above are the Tables representing the analysed raw data from the experiment. Column D displays the extension, calculated using the original length and the length post completion of the test. Column E displays the Nominal Strain calculated using the extension and the original length using the equation below.

ε=Change in LengthOriginal Length

Equation 1:Strain Equation

Figure 4: Diagram Displaying Strain

Column F displays the Stress calculated using the Force and the cross-sectional area. The equation below demonstrates how that calculation is done.

σ=ForceArea

Equation 2: Stress Equation

Figure 5: Diagram Displaying Stress

From this, the Graphs were plotted, showing a stress-strain graph where you can take readings for the yield point and gather information about how the material acted under load. The same process was repeated for the other materials, with the tables below for aluminium, duralumin and PVC.

Figure 6: Graph Displaying Stress-Strain for Steel

Figure 7: Graph Displaying Steel Stress-Strain for Young's Modulus Calculation

Figure 7 above shows the graph before the yield point for steel. This area of the graph is used to calculate Young's Modulus. The Young's modulus is how much a material can resist the strain of a particular stress. This, in other words, is the ratio between stress and strain. Calculated using the gradient of a stress-strain graph before the yield point, as displayed below in Figure 8.

Figure 8:Graph Displaying Young's Modulus Calculation

All the calculations were repeated for each material during the analysis, and graphs and tables were generated for each one, which are all displayed below.

Table 4: Aluminium Analysed Data

| Aluminium |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Load Nut (mm) | Dial Indicator (mm) | Force (N) | Extension (mm) | Nominal Strain | Stress (MPa) |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.2 | 0.15 | 15 | 0.05 | 0.001612903 | 7.5 |
| 0.4 | 0.33 | 33 | 0.07 | 0.002258065 | 16.5 |
| 0.6 | 0.5 | 50 | 0.1 | 0.003225806 | 25 |
| 0.8 | 0.67 | 67 | 0.13 | 0.004193548 | 33.5 |
| 1 | 0.85 | 85 | 0.15 | 0.00483871 | 42.5 |
| 1.2 | 1.02 | 102 | 0.18 | 0.005806452 | 51 |
| 1.4 | 1.19 | 119 | 0.21 | 0.006774194 | 59.5 |
| 1.6 | 1.36 | 136 | 0.24 | 0.007741935 | 68 |
| 1.8 | 1.54 | 154 | 0.26 | 0.008387097 | 77 |
| 2 | 1.7 | 170 | 0.3 | 0.009677419 | 85 |
| 2.2 | 1.85 | 185 | 0.35 | 0.011290323 | 92.5 |
| 2.4 | 1.95 | 195 | 0.45 | 0.014516129 | 97.5 |
| 2.6 | 2.07 | 207 | 0.53 | 0.017096774 | 103.5 |
| 2.8 | 2.18 | 218 | 0.62 | 0.02 | 109 |
| 3 | 2.24 | 224 | 0.76 | 0.024516129 | 112 |
| 3.2 | 2.33 | 233 | 0.87 | 0.028064516 | 116.5 |
| 3.4 | 2.42 | 242 | 0.98 | 0.031612903 | 121 |
| 3.6 | 2.46 | 246 | 1.14 | 0.036774194 | 123 |
| 3.8 | 2.55 | 255 | 1.25 | 0.040322581 | 127.5 |
| 4 | 2.59 | 259 | 1.41 | 0.045483871 | 129.5 |
| 4.2 | 2.63 | 263 | 1.57 | 0.050645161 | 131.5 |
| 4.4 | 2.65 | 265 | 1.75 | 0.056451613 | 132.5 |
| 4.6 | 2.68 | 268 | 1.92 | 0.061935484 | 134 |
| 4.8 |  | 0 | 4.8 |  | 0 |
| 5 |  | 0 | 5 |  | 0 |
| 6 |  | 0 | 6 |  | 0 |
| 7 |  | 0 | 7 |  | 0 |
| 8 |  | 0 | 8 |  | 0 |
| 9 |  | 0 | 9 |  | 0 |
| 10 |  | 0 | 10 |  | 0 |
| 20 |  | 0 | 20 |  | 0 |
| 30 |  | 0 | 30 |  | 0 |
| 40 |  | 0 | 40 |  | 0 |
| 50 |  | 0 | 50 |  | 0 |
| 60 |  | 0 | 60 |  | 0 |

Figure 9:Graph Displaying Stress-Strain for Aluminium

Figure 10:Graph Displaying Aluminium Stress-Strain for Young's Modulus Calculation

Table 5: Duralumin Analysed Data

| Duralumin |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Load Nut (mm) | Dial Indicator (mm) | Force (N) | Extension (mm) | Nominal Strain | Stress (MPa) |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.2 | 0.17 | 17 | 0.03 | 0.000967742 | 8.5 |
| 0.4 | 0.36 | 36 | 0.04 | 0.001290323 | 18 |
| 0.6 | 0.55 | 55 | 0.05 | 0.001612903 | 27.5 |
| 0.8 | 0.73 | 73 | 0.07 | 0.002258065 | 36.5 |
| 1 | 0.89 | 89 | 0.11 | 0.003548387 | 44.5 |
| 1.2 | 1.05 | 105 | 0.15 | 0.00483871 | 52.5 |
| 1.4 | 1.25 | 125 | 0.15 | 0.00483871 | 62.5 |
| 1.6 | 1.41 | 141 | 0.19 | 0.006129032 | 70.5 |
| 1.8 | 1.61 | 161 | 0.19 | 0.006129032 | 80.5 |
| 2 | 1.77 | 177 | 0.23 | 0.007419355 | 88.5 |
| 2.2 | 1.95 | 195 | 0.25 | 0.008064516 | 97.5 |
| 2.4 | 2.13 | 213 | 0.27 | 0.008709677 | 106.5 |
| 2.6 | 2.29 | 229 | 0.31 | 0.01 | 114.5 |
| 2.8 | 2.47 | 247 | 0.33 | 0.010645161 | 123.5 |
| 3 | 2.66 | 266 | 0.34 | 0.010967742 | 133 |
| 3.2 | 2.84 | 284 | 0.36 | 0.011612903 | 142 |
| 3.4 | 3.01 | 301 | 0.39 | 0.012580645 | 150.5 |
| 3.6 | 3.19 | 319 | 0.41 | 0.013225806 | 159.5 |
| 3.8 | 3.36 | 336 | 0.44 | 0.014193548 | 168 |
| 4 | 3.54 | 354 | 0.46 | 0.01483871 | 177 |
| 4.2 | 3.69 | 369 | 0.51 | 0.016451613 | 184.5 |
| 4.4 | 3.85 | 385 | 0.55 | 0.017741935 | 192.5 |
| 4.6 | 4.04 | 404 | 0.56 | 0.018064516 | 202 |
| 4.8 | 4.21 | 421 | 0.59 | 0.019032258 | 210.5 |
| 5 | 4.39 | 439 | 0.61 | 0.019677419 | 219.5 |
| 6 | 4.91 | 491 | 1.09 | 0.03516129 | 245.5 |
| 7 | 5.09 | 509 | 1.91 | 0.061612903 | 254.5 |
| 8 |  | 0 | 8 |  | 0 |
| 9 |  | 0 | 9 |  | 0 |
| 10 |  | 0 | 10 |  | 0 |
| 20 |  | 0 | 20 |  | 0 |
| 30 |  | 0 | 30 |  | 0 |
| 40 |  | 0 | 40 |  | 0 |
| 50 |  | 0 | 50 |  | 0 |
| 60 |  | 0 | 60 |  | 0 |

Figure 11:Graph Displaying Stress-Strain for Duralumin

Figure 12:Graph Displaying Duralumin Stress-Strain for Young's Modulus Calculation

Table 6: PVC Analysed Data

| PVC |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Load Nut (mm) | Dial Indicator (mm) | Force (N) | Extension (mm) | Nominal Strain | Stress (MPa) |
| 0 | 0 | 0 | 0 | 0 | 0 |
| 0.2 | 0.06 | 6 | 0.14 | 0.004516129 | 3.157894737 |
| 0.4 | 0.11 | 11 | 0.29 | 0.009354839 | 5.789473684 |
| 0.6 | 0.16 | 16 | 0.44 | 0.014193548 | 8.421052632 |
| 0.8 | 0.22 | 22 | 0.58 | 0.018709677 | 11.57894737 |
| 1 | 0.24 | 24 | 0.76 | 0.024516129 | 12.63157895 |
| 1.2 | 0.25 | 25 | 0.95 | 0.030645161 | 13.15789474 |
| 1.4 | 0.18 | 18 | 1.22 | 0.039354839 | 9.473684211 |
| 1.6 | 0.19 | 19 | 1.41 | 0.045483871 | 10 |
| 1.8 | 0.16 | 16 | 1.64 | 0.052903226 | 8.421052632 |
| 2 | 0.15 | 15 | 1.85 | 0.059677419 | 7.894736842 |
| 2.2 | 0.15 | 15 | 2.05 | 0.066129032 | 7.894736842 |
| 2.4 | 0.15 | 15 | 2.25 | 0.072580645 | 7.894736842 |
| 2.6 | 0.14 | 14 | 2.46 | 0.079354839 | 7.368421053 |
| 2.8 | 0.13 | 13 | 2.67 | 0.086129032 | 6.842105263 |
| 3 | 0.12 | 12 | 2.88 | 0.092903226 | 6.315789474 |
| 3.2 | 0.12 | 12 | 3.08 | 0.099354839 | 6.315789474 |
| 3.4 | 0.12 | 12 | 3.28 | 0.105806452 | 6.315789474 |
| 3.6 | 0.12 | 12 | 3.48 | 0.112258065 | 6.315789474 |
| 3.8 | 0.12 | 12 | 3.68 | 0.118709677 | 6.315789474 |
| 4 | 0.12 | 12 | 3.88 | 0.12516129 | 6.315789474 |
| 4.2 | 0.12 | 12 | 4.08 | 0.131612903 | 6.315789474 |
| 4.4 | 0.14 | 14 | 4.26 | 0.137419355 | 7.368421053 |
| 4.6 | 0.12 | 12 | 4.48 | 0.144516129 | 6.315789474 |
| 4.8 | 0.2 | 20 | 4.6 | 0.148387097 | 10.52631579 |
| 5 | 0.17 | 17 | 4.83 | 0.155806452 | 8.947368421 |
| 6 | 0.18 | 18 | 5.82 | 0.187741935 | 9.473684211 |
| 7 | 0.16 | 16 | 6.84 | 0.220645161 | 8.421052632 |
| 8 | 0.15 | 15 | 7.85 | 0.253225806 | 7.894736842 |
| 9 | 0.15 | 15 | 8.85 | 0.285483871 | 7.894736842 |
| 10 | 0.15 | 15 | 9.85 | 0.317741935 | 7.894736842 |
| 20 | 0.14 | 14 | 19.86 | 0.640645161 | 7.368421053 |
| 30 | 0.13 | 13 | 29.87 | 0.963548387 | 6.842105263 |
| 40 | 0.12 | 12 | 39.88 | 1.286451613 | 6.315789474 |
| 50 |  | 0 | 50 |  | 0 |
| 60 |  | 0 | 60 |  | 0 |

Figure 13:Graph Displaying Stress-Strain for PVC

Figure 14:Graph Displaying PVC Stress-Strain for Young's Modulus Calculation

# Conclusion

## Steel

The Tensile Stress for steel found in the experiment is around 280 MPa. Comparing this to other results, it seems to be on the lower end. A report by Tenstand measuring 12 different steels found that they had a tensile strength range between 301.1 MPa and 1167.8 MPa. The metal used in this experiment should have a tensile strength of around 330 MPa according to Tenstand. However, when looking at the experiment results, you can see that the experiment resulted in a tensile strength of 50 MPa lower than Testand. This could be because of the temperature on the day (Loveday, Gray, & Aegerter, 2004). A study by W. Mocko and L. Kruszka found that higher temperatures can cause a metal's tensile stress to decrease and vice versa with lower temperatures (Mocko & Kruszka, 2013). The yield strength in this experiment for steel was around 110 MPa. Comparing this again with the Tenstands results, this reading is around 120 MPa lower than it should be. This is a drastic difference and most likely isn’t the result of just one failure during the experiment, such as environmental temperature (Loveday, Gray, & Aegerter, 2004). The calculated Modulus Young result for steel was around 16779 MPa. According to BES Group, mild steel's Young's modulus should be around 200 GPA. The experiment's result was around 16.779 GPa. This is significantly lower than most steels and heavily implies that an error has occurred (BES, 2025). Again, it's likely that the temperature affected the results; however, multiple factors would’ve caused a reading to be as low as this. It's possible that there were some mistakes made when taking the readings during the experiment, which would’ve resulted in the data being so far behind.

## Aluminium

The tensile stress for aluminium in the experiment was around 134 MPa. Referring again to the report by Tenstand, this seems to be lower than average. They measured 5 different types of aluminium with a range of 212.3 MPa to 491.3 MPa. As it's not detailed which type of aluminium was used in the experiment, you cannot be sure which reading to reference, but overall, the result of the experiment is below all readings made by Tenstand. The yield strength recorded in the experiment was 85 MPa.  When comparing this to Tenstands results, it is still below, however, only by around 20 MPa, which is a lot more accurate than the steel readings. The Young modulus reading for aluminium was recorded at 9335.2 MPa or 9.3352 GPa. This is around 60 GPa lower than the average according to BES Group (BES, 2025). The inconsistencies in the readings could be because of the temperature on the day, as discussed above regarding the report by Mocko and Kruszka (Mocko & Kruszka, 2013). However, the size of the inconsistencies would imply that there were more issues during the experiment to cause these errors.

## Duralumin

The tensile stress for duralumin in the experiment was around 250 MPa. According to AZO Materials, duralumin's tensile strength should be around 450 MPa (AZO, 2013). This is below the reference reading and outside of any tolerance. The Young Modulus reading for duralumin in the experiment was 11703 MPa or 11.703 GPa. According to AZO Materials duralumin’s, Modulus should be around 73 GPa, so the experiment's reading is around 60 GPa lower than its reference (AZO, 2013). Again, this is likely to be due to the temperature on the day and possibly errors when taking readings during the experiment.

## PVC

The tensile strength and the yield strength reading for PVC during the experiment were 13 MPa. According to Shimadzu, PVC's tensile strength should be around 66 MPa. Therefore, the reading was again lower than the reference. The Young's modulus reading for PVC was 448 MPa or 0.448 GPa. A report by Escudier and Atkins recorded PVC's Young's modulus at 1.4 GPa (Escudier & Atkins, 2019). This recording is around 1 GPa lower than the reference and once again implies error during testing.

# Evaluation

During the experiment, errors were eliminated in various ways. Firstly, all materials were brought out into the environment at the same time to ensure they were all at the same temperature. the same test equipment was used for each material, including the vernier and tensile tester. All tests were conducted in the same room at the same time. Both the readings and load nut movement were done by the same people to ensure consistency.

# Further Work

If provided the time, some improvements could’ve been made to make the experiment more robust and accurate. Firstly, more people could’ve been involved to help with counting load nut movements, taking readings, taking measurements, and preparing specimens to ensure everything is consistent between materials. More samples of each material could’ve been used to gather more data and remove anomalies from the data when analysing it to ensure results are reliable. Digital verniers could’ve been used to reduce human error when taking measurements of specimens. A way of monitoring the materials' temperatures would’ve made the data more reliable and ensured everything was consistent and the materials were at the optimum temperature. The use of a Denison Tensile Tester would’ve improved the experiment. Using this would’ve ensured that the load nut movements were consistent, by a person doing the movement, most turns are different to one another, and it's difficult to keep each turn at the same speed. Whereas with a Denison, it would’ve ensured this was kept consistent. Also, having the machine measure the extension throughout the experiment would’ve helped with getting more reliable and accurate data. Making these improvements would’ve helped reduce the errors found in the experiment. Ensuring we had a consistent load nut movement would have meant the data would be more reliable and possibly reduced anomalies throughout the experiment. Monitoring the materials' temperatures would’ve also ensured our data was more reliable, as the readings should be closer to the reference results found.

# References

AZO. (2013, January 21). Duralumin - Chemical Composition, Mechanical Properties and Common Applications. Retrieved from AZO Materials: https://www.azom.com/article.aspx?ArticleID=8073

BES. (2025, March 26). A Guide to Young’s Modulus and Material Stiffness. Retrieved from BES Group: https://besgroup.com/blogs/a-guide-to-youngs-modulus-and-material-stiffness/

Escudier, M., & Atkins, T. (2019). Dictionary of Mechanical Engineering. Oxford University Press.

Instron. (n.d.). Tensile Testing An Introduction . Retrieved from instron: https://www.instron.com/en/resources/test-types/tensile-test/#:~:text=Why%20Perform%20a%20Tensile%20Test,required%20specifications%20for%20tensile%20properties.

Loveday, M. S., Gray, T., & Aegerter, J. (2004). Tensile Testing of Metallic Materials: A Review .

Mocko, W., & Kruszka, L. (2013). Results of Strain Rate and Temperature on Mechanical Properties of Selected Structural Steels.

TecQuipment. (2012). Engineering Science Guideance Notes Tensile test ES6.